SDR-11 Specification:

UPW process piping and fittings shall be manufactured from a specialty low-extractable, Polyvinyl Choloride (HDPE) compound with a Cell Classification of 12343 per ASTM D1784.  All pipe and fittings shall be produced to Schedule 80 dimensions, manufactured in strict compliance to ASTM D1785 (pipe), and ASTM D2467 (fittings).  These products shall carry a Type II pressure rating and consistently meet or exceed the applicable Quality Assurance test requirements of these standards with regard to dimensions, workmanship, burst pressure, flattening resistance and end product quality.  All UPW process valves shall be True Union style diaphragm or True Union style quarter turn ball valves produced from the same low-extractable HDPE compound.  All valve diaphragms and seats shall be PTFE; valve o-rings shall be EPDM or Viton® as applicable.  All valve union nuts shall have buttress style threads.  All valve components shall be replaceable.  System components shall be joined utilizing Harvel LXT® One-Step specialty solvent cement specifically formulated for joining the system.  All system components shall be manufactured in the USA by an ISO certified manufacturer.  All UPW piping shall be bagged and sealed immediately after manufacture to maintain cleanliness, boxed and stored indoors at the manufacturing facility until shipped from the factory.  UPW process pipe, components and cement shall be that as provided by Harvel Plastics, inc., trade name Harvel LXT®

SDR-26 Specification:

HDPE SDR 26 pipe material used for the manufacturing of polyethylene pipe shall be PE 3408 High Density Polyethylene (HDPE), meeting the ASTM D3350 CELL classification 345464C.  Polyethylene pipe shall be manufactured in accordance with AWWA C906, consistently meeting and/or exceeding the Quality Assurance test requirements of this standard with regard to pressure rating, material, workmanship, burst pressure, flattening, impact resistance, and extrusion quality.  The pipe shall be manufactured in the USA, using domestic materials, by a certified manufacturer.  All pipe shall be stored indoors after production at the manufacturing site until shipped from factory.

Tangipahoa Landfill Storm Water Pumping System Material List

Qty

Unit

Item

1250

FT

8” SDR26 HDPE PIPE

1150 

FT

10” SDR26 HDPE PIPE

900

FT

4” SDR26 HDPE PIPE

2

EA

4” SDR11 HDPE 90 º SWEEP

1

EA

4” SDR11 HDPE B.F. VALVE

2

EA

4” SDR11 HDPE FLANGE

1

EA

4” SDR11 HDPE 45 º ELL

1

EA

4” SDR11 HDPE CHECKVALVE

1

EA

10”x 4” SDR11 HDPE 30º WYE

2

EA

6” SDR11 HDPE FLANGE

1

EA

6” SDR11 HDPE CHECKVALVE

1

EA

8”x6” SDR11 HDPE REDUCER

2

EA

8” SDR11 HDPE 90 º SWEEP

1

EA

8” SDR11 HDPE 90 º WYE

2

EA

8” SDR11 HDPE B.F. VALVE

4

EA

8” SDR11 HDPE FLANGE

1

EA

10”x8” SDR11 HDPE REDUCER

3

EA

10” SDR11 HDPE 90 º SWEEP

