ST. TAMMANY FIRE PROTECTION DISTRICT NO. 1

FIRE STATION #14

297 STEELE ROAD

SLIDELL LA  70461


SECTION 06402
INTERIOR ARCHITECTURAL WOODWORK
Copyright 2002, The American Institute of Architects (AIA)

Much of this Section consists of Project-specific data.  Examples in the Evaluations were chosen to illustrate possible Section content.  Use these sample paragraphs as models to develop text for specific Project requirements, or delete them if they do not apply.  See Evaluations.

Verify that Section titles referenced in this Section are correct for this Project's Specification; Section titles may have changed.

Copyright 2002 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

Copyright 2003 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.
1.2 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project and to distinguish interior architectural woodwork from items made from wood but specified as finish carpentry, stock cabinets, etc., in other Sections.  AWI's definition of standing and running trim includes "rails used on corridor walls of hospitals or nursing homes, etc., and guard rails at glass openings."

1. Plastic-laminate cabinets.

2. Solid-surfacing-material countertops.

1.3 DEFINITIONS

A. Interior architectural woodwork includes wood furring, blocking, shims, and hanging strips for installing woodwork items unless concealed within other construction before woodwork installation.

Delete paragraph below if no stairs or if carriages are included in rough carpentry.

B. Rough carriages for stairs are a part of interior architectural woodwork.  Platform framing, headers, partition framing, and other rough framing associated with stairwork are specified in Division 6 Section "Rough Carpentry."

1.4 SUBMITTALS

A. Product Data:  For each type of product indicated, including cabinet hardware and accessories and finishing materials and processes.

Retain paragraph above or first paragraph below and edit to suit Project; delete both if not applicable.

B. Product Data:  For solid-surfacing material cabinet hardware and accessories and finishing materials and processes.

Retain subparagraph below with either paragraph above; delete if fire-retardant-treated wood is not required.

C. Shop Drawings:  Show location of each item, dimensioned plans and elevations, large-scale details, attachment devices, and other components.

Retain first subparagraph below only for ornate, complex, or very high quality work.

1. Show details full size.

2. Show locations and sizes of furring, blocking, and hanging strips, including concealed blocking and reinforcement specified in other Sections.

3. Show locations and sizes of cutouts and holes for plumbing fixtures, faucets, soap dispensersand other items installed in architectural woodwork.

Retain subparagraph below only for blueprint-matched work.

Retain subparagraph below only if retaining other requirements for WI's quality certification program.

4. Apply WI-certified compliance label to first page of Shop Drawings.

D. Samples for Initial Selection:

Revise list below to suit Project.

1. Shop-applied opaque finishes.

2. Solid-surfacing materials.

Delete paragraph and subparagraphs above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph and subparagraphs below with or without above.

E. Samples for Verification:

Delete items in subparagraphs below that are not actually needed for control of grain character, color, and finish or expand to include other items.  Sizes listed first comply with those in AWI standard; revise if other sizes are required.

1. Lumber with or for transparent finish, not less than 50 sq. in. 5 inches wide by 24 inches  long, for each species and cut, finished on 1 side and 1 edge.

2. Lumber and panel products with shop-applied opaque finish, 50 sq. in. for lumber and 8 by 10 inches for panels, for each finish system and color, with 1/2 of exposed surface finished.

3. Solid-surfacing materials, 6 inches square.

4. Corner pieces as follows:

a. Cabinet-front frame joints between stiles and rails, as well as exposed end pieces, 18 inches high by 18 inches wide by 6 inches deep.

b. Miter joints for standing trim.

Delete subparagraph below if Product Data are acceptable.

5. Exposed cabinet hardware and accessories, one unit for each type and finish.

F. Product Certificates:  For each type of product, signed by product manufacturer.

If retaining paragraph below, also retain paragraphs in "Quality Assurance" Article that require compliance with selected quality standard and certification program.

G. Woodwork Quality Standard Compliance Certificates:  AWI Quality Certification Program certificates.

Coordinate paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

H. Qualification Data:  For Installer and fabricator.

1.5 QUALITY ASSURANCE

Consider retaining one of two options in paragraph below if AWI quality certification or WI compliance certification is required.  AWI's quality certification is only available if fabricator is a certified participant.  WI will inspect work and provide certification for work that passes inspection if fabricator is not a licensed shop.

A. Fabricator Qualifications:  Shop that employs skilled workers who custom-fabricate products similar to those required for this Project and whose products have a record of successful in-service performance.

B. Source Limitations:  Engage a qualified woodworking firm to assume undivided responsibility for production of interior architectural woodwork with sequence-matched wood veneers and wood doors with face veneers that are sequence matched with woodwork and transparent-finished wood doors that are required to be of same species as woodwork.

C. Quality Standard:  Unless otherwise indicated, comply with AWI's "Architectural Woodwork Quality Standards" for grades of interior architectural woodwork indicated for construction, finishes, installation, and other requirements.

1. Provide AWI Quality Certification Program labels and certificates indicating that woodwork complies with requirements of grades specified.

Delete paragraph and subparagraph below if not required.  If retaining, indicate location, size, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 1.

D. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination."

1.6 DELIVERY, STORAGE, AND HANDLING

A. Do not deliver woodwork until painting and similar operations that could damage woodwork have been completed in installation areas.  If woodwork must be stored in other than installation areas, store only in areas where environmental conditions comply with requirements specified in "Project Conditions" Article.

1.7 PROJECT CONDITIONS

A. Environmental Limitations:  Do not deliver or install woodwork until building is enclosed, wet work is complete, and HVAC system is operating and maintaining temperature and relative humidity at occupancy levels during the remainder of the construction period.

Generally retain paragraph above; retain first paragraph below if humidity will be controlled during occupancy.  If retaining below, select one of three relative humidity ranges or insert another based on local climatological data.  Three ranges given are for painted or finished woodwork.  First applies to Ontario, Quebec, and most of U.S.  Second applies to damp coastal areas of southern U.S. and the Maritime Provinces.  Third applies to dry southwestern U.S. and to Alberta, Manitoba, and Saskatchewan.  For unfinished woodwork, narrower ranges will be required to maintain optimum moisture content.  See map and discussion about relative humidity and moisture content at end of Section 1700 in AWI's quality standards.

B. Environmental Limitations:  Do not deliver or install woodwork until building is enclosed, wet work is complete, and HVAC system is operating and maintaining temperature between 60 and 90 deg F and relative humidity between 43 and 70 percent during the remainder of the construction period.

C. Field Measurements:  Where woodwork is indicated to fit to other construction, verify dimensions of other construction by field measurements before fabrication, and indicate measurements on Shop Drawings.  Coordinate fabrication schedule with construction progress to avoid delaying the Work.

1. Locate concealed framing, blocking, and reinforcements that support woodwork by field measurements before being enclosed, and indicate measurements on Shop Drawings.

Delete subparagraph below if not allowed.

2. Established Dimensions:  Where field measurements cannot be made without delaying the Work, establish dimensions and proceed with fabricating woodwork without field measurements.  Provide allowance for trimming at site, and coordinate construction to ensure that actual dimensions correspond to established dimensions.

1.8 COORDINATION

A. Coordinate sizes and locations of framing, blocking, furring, reinforcements, and other related units of Work specified in other Sections to ensure that interior architectural woodwork can be supported and installed as indicated.

Retain paragraph below if cabinet locks or other hardware applied to woodwork, such as hinges and locks applied to wood jambs, is specified in a hardware section.  Include a similar paragraph for other specific items requiring coordination, such as light fixtures installed in woodwork.

B. Hardware Coordination:  Distribute copies of approved hardware schedule specified in Division 8 Section "Door Hardware (Scheduled by Describing Products)" to fabricator of architectural woodwork; coordinate Shop Drawings and fabrication with hardware requirements.

PART 2 -  PRODUCTS

2.1 WOODWORK FABRICATORS

Retain this Article if a list of preapproved woodworkers is used as a quality-control procedure.  See Evaluations.

A. Available Fabricators:  Subject to compliance with requirements, fabricators offering interior architectural woodwork that may be incorporated into the Work include, but are not limited to, the following:

Retain paragraph above if additional firms will be considered; retain paragraph below if not.  If retaining above, include procedure for approving other firms in the Instructions to Bidders.

B. Fabricators:  Subject to compliance with requirements, provide interior architectural woodwork by one of the following:

Insert list of preapproved firms.  Refer to AWI's or WI's member list for names of woodworking firms that could potentially be included.

2.2 MATERIALS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

A. General:  Provide materials that comply with requirements of AWI's quality standard for each type of woodwork and quality grade specified, unless otherwise indicated.

If all transparent-finished woodwork is same species and cut, retain paragraph above and delete separate requirements for species and cut in other articles; otherwise, delete above.  Similarly, if all opaque-finished woodwork is same species, retain paragraph below and delete separate requirements for species in other articles; otherwise, delete below.  For opaque-finished woodwork, closed-grain hardwood is a better choice than softwoods, except for Economy grade.

B. Wood Species for Opaque Finish:  Any closed-grain hardwood.

Retain paragraph and subparagraphs below if AWI standard is used or if requirements for wood products selected exceed those in WI standard.  Delete standards for products not used.

C. Wood Products:  Comply with the following:

1. Hardboard:  AHA A135.4.

If retaining subparagraph below and low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4, retain option prohibiting urea formaldehyde.  See Evaluations.  SierraPine's "Medex," "Medex NC," and "Medite II" and Weyerhaeuser's "Premier Plus" fiberboard are made without urea formaldehyde.

2. Medium-Density Fiberboard:  ANSI A208.2, Grade MD, made with binder containing no urea formaldehyde.

Retain first subparagraph below instead of subparagraph above if straw-based particleboard is required for LEED-NC or LEED-CI Credit MR 6.  Particleboard below also complies with low-emitting materials requirement for LEED-NC or LEED-CI Credit EQ 4.4.  See Evaluations.

3. Particleboard:  Straw-based particleboard complying with requirements in ANSI A208.1, Grade M-2, except for density.

4. Softwood Plywood:  DOC PS 1, Medium Density Overlay.

Note that the term "plywood" in subparagraph below refers to a wood-based panel with veneers applied to both faces; core may be made up of veneers (either hardwood or softwood), particleboard, medium-density fiberboard, hardboard, or glued-up lumber.  If retaining below and low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4, retain option prohibiting urea formaldehyde.  See Evaluations.

5. Veneer-Faced Panel Products (Hardwood Plywood):  HPVA HP-1, made with adhesive containing no urea formaldehyde.

Retain first paragraph and subparagraphs below for laboratory tops where high degree of chemical resistance is required.

D. Solid-Surfacing Material:  Homogeneous solid sheets of filled plastic resin complying with ISSFA-2.

1. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Retain subparagraph above for nonproprietary or subparagraph below for semiproprietary specification.  Refer to Division 1 Section "Product Requirements." Retain list of manufacturers with either subparagraph.

2. Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

Companies listed below make a range of products that are not all equal in appearance or in performance characteristics.  Some products offered may not comply with ISSFA-2 requirements for Standard type; some may not comply with ISSFA-2 at all.  Verify acceptability of products before retaining manufacturers.

a. ABA Industries.

b. Avonite, Inc.

c. E. I. du Pont de Nemours and Company.

d. Formica Corporation.

e. LG Chemical, Ltd.

f. Meganite Inc.; a division of the Pyrochem Group.

g. Nevamar Company, LLC; Decorative Products Div.

h. Samsung; Cheil Industries Inc.

i. Swan Corporation (The).

j. Transolid, Inc.

k. Wilsonart International; Div. of Premark International, Inc.

Delete option in first subparagraph below if 1/4-inch- (6.4-mm-) thick material is not used.  Special Purpose type is not subject to all the requirements for Standard type.  Special Purpose type must comply with requirements for fungal and bacterial resistance, consistency of color, stain resistance, visual defects, light resistance, boiling water resistance, and high-temperature resistance.  Standard type must comply with these same requirements and with requirements for radiant heat resistance, linear thermal expansion, flexural strength, flexural modulus, Barcol hardness, flatness, and impact resistance.

3. Type:  Standard type, unless Special Purpose type is indicated.

4. Colors and Patterns: As selected by Architect from manufacturer's full range.

2.3 CABINET HARDWARE AND ACCESSORIES

Where close matching of cabinet hardware and door hardware is required, it may be preferable to specify cabinet hardware in Division 8.

A. General:  Provide cabinet hardware and accessory materials associated with architectural cabinets, except for items specified in Division 8 Section "Door Hardware (Scheduled by Describing Products)."

B. Semiconcealed Hinges for Overlay Doors:  BHMA A156.9, B01521.

C. Wire Pulls:  Back mounted, solid metal, 4 inches long, 5/16 inch in diameter.

D. Catches:  Magnetic catches, BHMA A156.9, B03141.

First option in paragraph below specifies standards and clip-type rests for mounting at ends of shelves; second specifies standards and knife-type brackets for mounting at rear of shelves.

E. Adjustable Shelf Standards and Supports:  BHMA A156.9, B04071; with shelf rests, B04081 or BHMA A156.9, B04102; with shelf brackets, B04112.

Shelf rests in first paragraph below are installed in holes drilled in cabinet sides and partitions.

F. Shelf Rests:  BHMA A156.9, B04013; metal or metal, two-pin type with shelf hold-down clip].

G. Drawer Slides:  BHMA A156.9, B05091.

1. Heavy Duty (Grade 1HD-100 and Grade 1HD-200):  Side mounted; full-extension or full-overtravel-extension type; zinc-plated steel ball-bearing slides.

2. File Drawer Slides: Grade 1HD-200; for drawers more than 6 inches high or 24 inches  wide.

H. Door Locks:  BHMA A156.11, E07121.

Locks specified in paragraph above and below are deadbolt locks, surface mounted on inside of door or drawer with only the cylinder exposed on outside; revise either paragraph if another type of lock is required.

Sizes in first paragraph below are two of the many offered.  Other colors, materials, and styles are also available.  1-1/4-inch (32-mm) grommet is "OG series"; 2-inch (51-mm) grommet is "SG series."

I. Grommets for Cable Passage through Countertops:  1-1/4-inch or 2-inch , molded-plastic grommets and matching plastic caps with slot for wire passage.

1. Product:  Subject to compliance with requirements, provide "OG or SG series" by Doug Mockett & Company, Inc.

J. Exposed Hardware Finishes:  For exposed hardware, provide finish that complies with BHMA A156.18 for BHMA finish number indicated. Finish to be selected by Owner:

Subparagraphs below are examples only.  Revise to suit Project.  If more than one finish is required, indicate location of each here or on Drawings.  See Evaluations.

K. For concealed hardware, provide manufacturer's standard finish that complies with product class requirements in BHMA A156.9.

2.4 MISCELLANEOUS MATERIALS

A. Furring, Blocking, Shims, and Hanging Strips:  Softwood or hardwood lumber, kiln dried to less than 15 percent moisture content.

Delete paragraph above or first paragraph below, or both, if specified in a carpentry section.

B. Furring, Blocking, Shims, and Hanging Strips:  Fire-retardant-treated softwood lumber, kiln dried to less than 15 percent moisture content.

C. Anchors:  Select material, type, size, and finish required for each substrate for secure anchorage.  Provide nonferrous-metal or hot-dip galvanized anchors and inserts on inside face of exterior walls and elsewhere as required for corrosion resistance.  Provide toothed-steel or lead expansion sleeves for drilled-in-place anchors.

Retain paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4.  See Evaluations.

D. Adhesives, General:  Do not use adhesives that contain urea formaldehyde.

Retain paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.

E. VOC Limits for Installation Adhesives and Glues:  Use installation adhesives that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

Edit list below by deleting applications not used.  VOC limits listed are from South Coast Air Quality Management District Rule #1168.

1. Wood Glues:  30 g/L.

2. Contact Adhesive:  250 g/L.

2.5 FABRICATION, GENERAL

If all woodwork is same grade, retain first paragraph below and delete separate grades in other articles; otherwise, delete paragraph or retain as default and indicate exceptions in other articles.

A. Interior Woodwork Grade:  Unless otherwise indicated, provide Premium-grade interior woodwork complying with referenced quality standard.

B. Wood Moisture Content:  Comply with requirements of referenced quality standard for wood moisture content in relation to ambient relative humidity during fabrication and in installation areas.

C. Sand fire-retardant-treated wood lightly to remove raised grain on exposed surfaces before fabrication.

D. Fabricate woodwork to dimensions, profiles, and details indicated.  Ease edges to radius indicated for the following:

1. Corners of Cabinets and Edges of Solid-Wood (Lumber) Members 3/4 Inch Thick or Less:  1/16 inch.

2. Edges of Rails and Similar Members More Than 3/4 Inch Thick:  1/8 inch.

For highest-quality work, delete subparagraphs above and retain subparagraph below; otherwise, delete below.

3. Corners of Cabinets and Edges of Solid-Wood (Lumber) Members and Rails:  1/16 inch.

If applicable, insert subparagraph to describe conditions where eased edges are not required.

E. Complete fabrication, including assembly and/or finishing, and hardware application, to maximum extent possible before shipment to Project site.  Disassemble components only as necessary for shipment and installation.  Where necessary for fitting at site, provide ample allowance for scribing, trimming, and fitting.

Retain subparagraph below if Architect will examine work in woodwork shop before it is shipped to Project site.

1. Notify Architect seven days in advance of the dates and times woodwork fabrication will be complete.

Retain subparagraph below for high-quality and large or complex work.

2. Trial fit assemblies at fabrication shop that cannot be shipped completely assembled.  Install dowels, screws, bolted connectors, and other fastening devices that can be removed after trial fitting.  Verify that various parts fit as intended and check measurements of assemblies against field measurements indicated on Shop Drawings before disassembling for shipment.

F. Shop-cut openings to maximum extent possible to receive hardware, appliances, plumbing fixtures, electrical work, and similar items.  Locate openings accurately and use templates or roughing-in diagrams to produce accurately sized and shaped openings.  Sand edges of cutouts to remove splinters and burrs.

1. Seal edges of openings in countertops with a coat of varnish.

G. Install glass to comply with applicable requirements in Division 8 Section "Glazing" and in GANA's "Glazing Manual." For glass in wood frames, secure glass with removable stops.

2.6 INTERIOR STANDING AND RUNNING TRIM FOR OPAQUE FINISH

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  Custom.

For opaque-finished woodwork, closed-grain hardwood is generally a better choice than softwoods, except for Economy grade.

B. Wood Species:  Any closed-grain hardwood.

See Editing Instruction No. 2 in the Evaluations.

C. Backout or groove backs of flat trim members and kerf backs of other wide, flat members, except for members with ends exposed in finished work.

Retain paragraph below or revise if not applicable to all casings.  Plant assembly of casings applies only to Premium and Custom grades and is not required by AWI standards unless so specified.

D. Assemble casings in plant except where limitations of access to place of installation require field assembly.

Retain paragraph below only if required for monumental work.

E. Assemble moldings in plant to maximum extent possible.  Miter corners in plant and prepare for field assembly with bolted fittings designed to pull connections together.

2.7 SOLID-SURFACING-MATERIAL COUNTERTOPS

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  Premium.

Retain one of two options in first paragraph below.

B. Solid-Surfacing-Material Thickness: 3/4 inch Corian or Equal.

C. Colors, Patterns, and Finishes:  Provide materials and products that result in colors of solid-surfacing material complying with the following requirements:

Retain one of three options in subparagraph below.  If retaining first, indicate colors, patterns, and finishes in a separate schedule.

1.       As selected by Architect from manufacturer's full range.

D. Fabricate tops in one piece, unless otherwise indicated.  Comply with solid-surfacing-material manufacturer's written recommendations for adhesives, sealers, fabrication, and finishing.

Delete first subparagraph below if tops do not have applied edges.

1. Fabricate tops with shop-applied edges of materials and configuration indicated.

2. Fabricate tops with shop-applied backsplashes.

E. Drill holes in countertops for plumbing fittings and soap dispensers in shop.

2.8 SHOP FINISHING

Delete this Article if shop finishing is not required.  See Evaluations.  Shop finishing can be used to help comply with LEED-NC or LEED-CI Credit EQ 4.2, which limits VOC content of paints and coatings used within building.

Retain paragraph below and delete other grade requirements, or delete below and specify grades under finish types.  Finish grade can be different from Construction grade.

A. Grade:  Provide finishes of same grades as items to be finished.

Retain one of three paragraphs below to indicate extent of shop finishing required.  Paragraph below requires all work to be shop finished.

B. General:  Finish architectural woodwork at fabrication shop as specified in this Section.  Defer only final touchup, cleaning, and polishing until after installation.

Retain paragraph below if both painted and transparent finishes are used and only transparent finish is shop applied.

C. General:  Shop finish transparent-finished interior architectural woodwork at fabrication shop as specified in this Section.  Refer to Division 9 painting Sections for finishing opaque-finished architectural woodwork.

Retain paragraph below if both shop-finished and field-finished architectural woodwork is required and Drawings indicate which items are required to be shop finished.

D. General:  Shop finish transparent-finished interior architectural woodwork at fabrication shop as specified in this Section. Refer to Division 9 painting Sections for finishing architectural woodwork not indicated to be shop finished.

Retain first paragraph below if any field-finished woodwork is required to be shop primed.

E. Shop Priming:  Shop apply the prime coat including backpriming, if any, for transparent-finished items specified to be field finished.  Refer to Division 9 painting Sections for material and application requirements.

F. Preparation for Finishing:  Comply with referenced quality standard for sanding, filling countersunk fasteners, sealing concealed surfaces, and similar preparations for finishing architectural woodwork, as applicable to each unit of work.

Generally retain subparagraph below.  WI does not require backpriming; AWI only requires it for certain items and grades.  Backpriming helps moderate alternating shrinking and swelling caused by fluctuations in moisture content resulting from variations in relative humidity.

1. Backpriming:  Apply one coat of sealer or primer, compatible with finish coats, to concealed surfaces of woodwork.  Apply two coats to back of paneling and to end-grain surfaces.  Concealed surfaces of plastic-laminate-clad woodwork do not require backpriming when surfaced with plastic laminate, backing paper, or thermoset decorative panels.

If referencing WI standards and retaining Laboratory grade for casework, insert special finishes required.

PART 3 -  EXECUTION

3.1 PREPARATION

A. Before installation, condition woodwork to average prevailing humidity conditions in installation areas.

B. Before installing architectural woodwork, examine shop-fabricated work for completion and complete work as required, including removal of packing and backpriming.

3.2 INSTALLATION

Revise first paragraph below if installation grade is different from fabrication grade.

A. Grade:  Install woodwork to comply with requirements for the same grade specified in Part 2 for fabrication of type of woodwork involved.

B. Assemble woodwork and complete fabrication at Project site to comply with requirements for fabrication in Part 2, to extent that it was not completed in the shop.

C. Install woodwork level, plumb, true, and straight.  Shim as required with concealed shims.  Install level and plumb (including tops) to a tolerance of 1/8 inch in 96 inches.

D. Scribe and cut woodwork to fit adjoining work, refinish cut surfaces, and repair damaged finish at cuts.

Delete first paragraph below if no fire-retardant-treated wood.

E. Fire-Retardant-Treated Wood:  Handle, store, and install fire-retardant-treated wood to comply with chemical treatment manufacturer's written instructions, including those for adhesives used to install woodwork.

F. Anchor woodwork to anchors or blocking built in or directly attached to substrates.  Secure with countersunk, concealed fasteners and blind nailing as required for complete installation.  Use fine finishing nails or finishing screws for exposed fastening, countersunk and filled flush with woodwork and matching final finish if transparent finish is indicated.

Delete paragraph and subparagraphs below if not applicable or considered necessary.

G. Standing and Running Trim:  Install with minimum number of joints possible, using full-length pieces (from maximum length of lumber available) to greatest extent possible.  Do not use pieces less than 96 inches long, except where shorter single-length pieces are necessary.

1. Fill gaps, if any, between top of base and wall with plastic wood filler, sand smooth, and finish same as wood base if finished.

2. Install wall railings on indicated metal brackets securely fastened to wall framing.

3. Install standing and running trim with no more variation from a straight line than 1/8 inch in 96 inches.

H. Cabinets:  Install without distortion so doors and drawers fit openings properly and are accurately aligned.  Adjust hardware to center doors and drawers in openings and to provide unencumbered operation.  Complete installation of hardware and accessory items as indicated.

1. Install cabinets with no more than 1/8 inch in 96-inch sag, bow, or other variation from a straight line.

2. Maintain veneer sequence matching of cabinets with transparent finish.

Revise requirements in subparagraph below as necessary for seismic restraint of cabinets.  Delete if hanging cleats are used and are detailed on Drawings.

3. Fasten wall cabinets through back, near top and bottom, at ends and not more than 16 inches o.c. with No. 10 wafer-head screws sized for 1-inch penetration into wood framing, blocking, or hanging strips.

Delete paragraph and subparagraphs above if no cabinets; delete first paragraph and subparagraphs below if no tops that are not a part of base cabinets.

I. Countertops:  Anchor securely by screwing through corner blocks of base cabinets or other supports into underside of countertop.

Delete first subparagraph below if no solid-surfacing-material countertops.

1. Align adjacent solid-surfacing-material countertops and form seams to comply with manufacturer's written recommendations using adhesive in color to match countertop.  Carefully dress joints smooth, remove surface scratches, and clean entire surface.

2. Install countertops with no more than 1/8 inch in 96-inch sag, bow, or other variation from a straight line.

3. Calk space between backsplash and wall with sealant specified in Division 7 Section "Joint Sealants."

J. Touch up finishing work specified in this Section after installation of woodwork.  Fill nail holes with matching filler where exposed.

Retain paragraph above or below, or both; coordinate with selections made in Part 2 "Shop Finishing" Article.

K. Refer to Division 9 Sections for final finishing of installed architectural woodwork not indicated to be shop finished.

3.3 ADJUSTING AND CLEANING

A. Repair damaged and defective woodwork, where possible, to eliminate functional and visual defects; where not possible to repair, replace woodwork.  Adjust joinery for uniform appearance.

B. Clean, lubricate, and adjust hardware.

C. Clean woodwork on exposed and semiexposed surfaces.  Touch up shop-applied finishes to restore damaged or soiled areas.

END OF DOCUMENT
INTERIOR ARCHITECTURAL WOODWORK

06402 - 8

