Concrete Curing Compound                                            #3

W.R. Meadows, Inc.

- Compound shall conform to ASTM C 309, Type 1-D or 2, except that only a styrene acrylate or chlorinated rubber compound meeting Class B requirements shall be used for surfaces that are to be painted, or receive waterproofing, or floors that are to receive adhesive applications of resilient flooring, and otherwise be compatible with any subsequent material scheduled.

