
SECTION 07411

METAL ROOF PANELS

PART 1 - GENERAL

1.01 SUMMARY

A. Provide manufactured roof panels.

1.02 SUBMITTALS

A. Product Data:  Submit manufacturer's product data and installation instructions for each material and product used. 

B. Shop Drawings:  Submit shop drawings indicating material characteristics, details of construction, connections, and relationship with adjacent construction.

C. Samples:  Submit two representative samples of each material specified indicating visual characteristics and finish.  Include range samples if variation of finish is anticipated.

D. Warranty:  Submit manufacturer’s standard warranty.  Include labor and materials to repair or replace defective materials.

1. Warranty Period:  10 years.

1.03 QUALITY ASSURANCE

A. Comply with governing codes and regulations.  Provide products of acceptable manufacturers which have been in satisfactory use in similar service for three years.  Use experienced installers.  Deliver, handle, and store materials in accordance with manufacturer's instructions.

B. Wind Uplift:  UL 580 for Class 90 wind uplift resistance.

PART 2 - PRODUCTS

2.01 MATERIALS

A. Manufacturers: Met Tile Inc., or approved equal.

B. System Type:

1. Barrel profile manufactured metal roof tile panels.

2. Color as approved by La Quinta, medium dark red tone.

C. Manufactured Roof Panels:

1. Sheet Materials:  Galvanized steel sheet, ASTM A 653, G90 coating, 26 gauge (.0239 inch).

PART 3 - EXECUTION

3.01 INSTALLATION

A. Install materials and systems in accordance with manufacturer's instructions and approved submittals.  Install materials and systems in proper relation with adjacent construction and with uniform appearance.  Coordinate with work of other sections.

B. Restore damaged components and finishes.  Clean and protect work from damage.

END OF SECTION


METAL ROOF PANELS


07411-1

