SECTION 18

PORTLAND CEMENT CONCRETE PAVING

PART 1: 
GENERAL

18.1.1 Related Documents:  The general provisions of the Contract, including the Conditions of the Contract (General, Special and other Conditions) as appropriate, apply to the Work specified in this Section.
18.1.2 Scope of Work:  Furnish all necessary materials, labor and equipment for the complete installation of all Portland cement concrete paving work, as shown on the drawings and specified herein.  Provide all necessary supplementary items for a complete installation intended by documents.

18.1.3 Provisions:

A. All work shall comply with applicable provisions of the State of Louisiana Department of Transportation and Development latest edition “Louisiana Standard Specifications for Roads and Bridges” (DOTD), except as modified herein.

B. Where DOTD is modified herein, unaltered provisions of standard Specifications shall remain in effect.

C. Where general provisions (General, Supplementary Conditions, etc.) of this specification conflict with DOTD, this specification shall govern. DOTD provisions not affected shall remain as part of contract.

D. Whenever the “Department” is referenced in DOTD, change to read the “Owner” as applicable throughout.

PART 2:
PRODUCTS

18.2.1 Materials:

A. All materials shall comply with the DOTD sections entitled “Portland Cement Concrete Pavement”, “Concrete Walks, Drives, and Incidental Paving”, and “Curbs and Gutters”, and Part “Base Course” as required.

B. The compressive strength of the concrete at 28 days shall be 4,000 psi.  The pavement shall not be opened to traffic until a compressive strength of 3,000 psi is attained and in no case shall the pavement be opened to traffic within a three (3) day period after the concrete has been placed.  The concrete shall also have 7 sacks of cement per cubic yard and a 2” to 4” slump range.  The use of Fly Ash in the mix will not be permissible.

C. Joint sealers shall be a hot poured rubberized asphalt accordance with Section 1005.02 (c) of the DOTD Standard Specification.

PART 3:  EXECUTION

18.3.1 Workmanship:  All workmanship shall comply with the DOTD sections listed above.   The final roadway surface shall be a “Drag Finish” as defined in the DOTD Standard Specifications.

18.3.2 Acceptance of Work:  Work will not be acceptable if it does not meet the requirements for 100 percent payment, as indicated in DOTD.

18.3.3 Cleaning:  After completion of paving operations, clean surfaces of excess of spilled materials in a workmanlike manner.

Technical Specifications 

Section 18, Page 2

