Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications

SECTION 06105 – MISCELLANEOUS CARPENTRY 
PART 1 -  GENERAL

1.1 SUMMARY
A. This Section includes the following:

Adjust list below to suit Project.

1. Wood blocking and nailers.

2. Plywood backing panels.

1.2 SUBMITTALS
A. Product Data:  For each type of process and factory-fabricated product.

1. Include data for wood-preservative and fire-retardant treatment from chemical treatment manufacturer and certification by treating plant that treated materials comply with requirements.

PART 2 -  PRODUCTS
2.1 WOOD PRODUCTS, GENERAL

A. Lumber:  DOC PS 20 and applicable rules of grading agencies indicated.  If no grading agency is indicated, provide lumber that complies with the applicable rules of any rules-writing agency certified by the ALSC Board of Review.  Provide lumber graded by an agency certified by the ALSC Board of Review to inspect and grade lumber under the rules indicated.

1. Factory mark each piece of lumber with grade stamp of grading agency.

Select only first option in subparagraph below if authorities having jurisdiction require grade stamps on all materials.

Revise subparagraph below if rough lumber is acceptable for all work.

2. Provide dressed lumber, S4S, unless otherwise indicated.

2.2 WOOD-PRESERVATIVE-TREATED MATERIALS

Delete this Article if not applicable.  See the Evaluations in Division 06 Section "Rough Carpentry" for discussion of formulations.

A. Preservative Treatment by Pressure Process:  AWPA C2.

1. Preservative Chemicals:  Acceptable to authorities having jurisdiction and containing no arsenic or chromium.

B. Kiln-dry lumber after treatment to a maximum moisture content of 19 percent.  Do not use material that is warped or does not comply with requirements for untreated material.

C. Mark lumber with treatment quality mark of an inspection agency approved by the ALSC Board of Review.

Select first option in paragraph below and delete subparagraphs if total treatment is required; otherwise, select second option and retain appropriate subparagraphs.

D. Application:  Treat all miscellaneous carpentry, unless otherwise indicated. 

Retain subparagraph below if Project includes wood adjacent to roofing or waterproofing.

2.3 FIRE-RETARDANT-TREATED MATERIALS

Delete this Article if not applicable.

A. General:  Comply with performance requirements in AWPA C20 (lumber) and AWPA C27 (plywood).

Exterior type is suitable for both exterior and interior applications.  Interior type is only for interior applications.  See Evaluations.

1. Use Exterior type for exterior locations and where indicated.

Delete first subparagraph below if not applicable.  Revise description of locations to suit Project requirements.

2. Use Interior Type A, unless otherwise indicated.

B. Identify fire-retardant-treated wood with appropriate classification marking of testing and inspecting agency acceptable to authorities having jurisdiction.

Select first option in paragraph below and delete subparagraphs if all wood is required to be fire-retardant treated; otherwise, select second option and retain appropriate subparagraphs.

C. Application:  Treat  items indicated on Drawings, and the following:
Edit list below suit local code and Project requirements.

1. Plywood backing panels.

2.4 MISCELLANEOUS LUMBER
A. General:  Provide miscellaneous lumber indicated and lumber for support or attachment of other construction, including the following:

1. Blocking.

2. Nailers.

Delete subparagraph below if prefabricated metal units are used.  Prefabricated metal units may still require blocking or nailers.

Delete any or all of three items below if not required.

B. For items of dimension lumber size, provide Construction or No. 2  grade lumber with 19 percent maximum moisture content of any species.

Retain paragraph and subparagraphs below for furring, grounds, and nailing strips if required, and for truss bracing specified by reference to this Section.

C. For concealed boards, provide lumber with 15percent maximum moisture content and the following species and grades:

Edit list below.  Species groups below are not necessarily of equal quality even when of same grade.

1. Mixed southern pine, No.  2 grade; SPIB.

2.5 PLYWOOD BACKING PANELS

A. Telephone and Electrical Equipment Backing Panels:  DOC PS 1, Exposure 1, C-D Plugged, fire-retardant treated, in thickness indicated or, if not indicated, not less than 1/2-inch (13-mm) nominal thickness.

2.6 FASTENERS
A. General:  Where carpentry is exposed to weather, in ground contact, pressure-preservative treated, or in area of high relative humidity, provide fasteners with hot-dip zinc coating complying with ASTM A 153/A 153M.

B. Power-Driven Fasteners:  NES NER-272.

C. Screws for Fastening to Cold-Formed Metal Framing:  ASTM C 954, except with wafer heads and reamer wings, length as recommended by screw manufacturer for material being fastened.

PART 3 -  EXECUTION
3.1 INSTALLATION, GENERAL

A. Set carpentry to required levels and lines, with members plumb, true to line, cut, and fitted.  Fit carpentry to other construction; scribe and cope as needed for accurate fit.  Locate nailers, blocking, and similar supports to comply with requirements for attaching other construction.

B. Comply with AWPA M4 for applying field treatment to cut surfaces of preservative-treated lumber.

C. Securely attach carpentry work to substrate by anchoring and fastening as indicated, complying with the following:

If retaining subparagraph below, verify that this is acceptable to authorities having jurisdiction.  Also retain one of the other subparagraphs that references a model code fastener schedule complying with local requirements.  Fasteners covered by NES NER-272 are manufactured by member companies of the International Staple, Nail and Tool Association.

1. NES NER-272 for power-driven fasteners.

Retain one of six subparagraphs below, with or without subparagraph above, as required to comply with requirements of Project and local codes.

2. Table 2304.9.1, "Fastening Schedule," in ICC's International Building Code.

END OF SECTION 06105

MISCELLANEOUS CARPENTRY

06105 - 3

