Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications


Copyright 2003 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 06402 - INTERIOR ARCHITECTURAL WOODWORK
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project.

1. Interior standing and running trim.

2. Flush wood paneling and wainscots.

3. Wood cabinets.

4. Plastic-laminate cabinets.

5. Solid-surfacing-material countertops.

6. Shop finishing of woodwork.

B. Interior architectural woodwork includes wood furring, blocking, shims, and hanging strips unless concealed within other construction before woodwork installation.

1.2 SUBMITTALS

A. Product Data:  For solid-surfacing material, cabinet hardware and accessories  andfinishing materials and processes.

B. Shop Drawings:  Show location of each item, dimensioned plans and elevations, large-scale details, attachment devices, and other components.

First paragraph and subparagraphs below assume manufacturer's standard-size Samples are acceptable.  Revise to suit Project.

C. Samples:

1. Lumber and panel products for transparent finish, for each species and cut, finished on one side and one edge.

2. Plastic-laminates, for each type, color, pattern, and surface finish.

3. Melamine surfacing.

4. Solid-surfacing materials.

D. SPiRiT Submittals:

Retain subparagraph and associated subparagraphs below if low-emitting materials are required for LEED Credit EQ 4.4.

1. Credit IEQ 5.C4:

a. Composite wood manufacturer's product data for each composite wood product used indicating that the bonding agent contains no urea formaldehyde.

b. Adhesive manufacturer's product data for each adhesive used indicating that the adhesive contains no urea formaldehyde.

If retaining paragraph below, also retain paragraph in "Quality Assurance" Article that requires compliance with selected quality standard and certification program.  See Evaluations.

E. Woodwork Quality Standard Compliance Certificates:  AWI Quality Certification Program certificates.

1.3 QUALITY ASSURANCE

Delete first paragraph below if Installer is not required to be woodwork fabricator.

A. Installer Qualifications:  Fabricator of woodwork.

B. Quality Standard:  Unless otherwise indicated, comply with AWI's "Architectural Woodwork Quality Standards." 

Consider retaining applicable subparagraph below.  Consider deleting certification for installation if installation may not be performed by woodworking firm.  See Evaluations.

1. Provide AWI Quality Certification Program labels and certificates for woodwork.

1.4 PROJECT CONDITIONS

A. Environmental Limitations:  Do not deliver or install woodwork until building is enclosed, wet work is complete, and HVAC system is operating and maintaining temperature and relative humidity at occupancy levels during the remainder of the construction period.

PART 2 -  PRODUCTS

2.1 MATERIALS

A. Wood Species and Cut for Transparent Finish:  Red oak, plain sawn or sliced.

B. Wood Products:

1. Hardboard:  AHA A135.4.

If retaining subparagraph below and low-emitting materials are required for LEED Credit EQ 4.4, retain option prohibiting urea formaldehyde.  See Evaluations.  SierraPine's "Medex," "Medex NC," and "Medite II" and Weyerhaeuser's "Premier Plus" fiberboard are made without urea formaldehyde.

2. Medium-Density Fiberboard:  ANSI A208.2, Grade MD, made with binder containing no urea formaldehyde.

Retain second option in subparagraph below if low-emitting materials are required for LEED Credit EQ 4.4.  See Evaluations.  Particleboard with exterior glue is made by Rodman Industries.

3. Particleboard:  ANSI A208.1, Grade  M-2-Exterior Glue.

4. Softwood Plywood:  DOC PS 1, Medium Density Overlay.

If retaining subparagraph below and low-emitting materials are required for LEED Credit EQ 4.4, retain option prohibiting urea formaldehyde.  See Evaluations.

5. Veneer-Faced Panel Products (Hardwood Plywood):  HPVA HP-1, made with adhesive containing no urea formaldehyde.

First paragraph below describes "Permalam," frequently called "melamine." If retaining, also retain "Medium-Density Fiberboard" Subparagraph and applicable "Particleboard" subparagraphs in "Wood Products" Paragraph above.

C. Thermoset Decorative Panels:  Particleboard or medium-density fiberboard finished with thermally fused, melamine-impregnated decorative paper complying with LMA SAT-1.

D. High-Pressure Decorative Laminate:  NEMA LD 3, grades as indicated or, if not indicated, as required by woodwork quality standard.

E. Solid-Surfacing Material:  Homogeneous solid sheets of filled plastic resin complying with ISSFA-2.

F. Tempered Float Glass for Cabinet Doors:  ASTM C 1048, Kind FT, Condition A, Type I, Class 1 (clear), Quality-Q3, 6 mm thick, unless otherwise indicated.

2.2 FIRE-RETARDANT-TREATED MATERIALS

A. Provide fire-retardant-treated lumber, plywood, particleboard and fiberboard where required by code.

B. Fire-Retardant-Treated Lumber and Plywood by Pressure Process:  Comply with performance requirements of AWPA C20 (lumber) and AWPA C27 (plywood).  Use Exterior Type or Interior Type A.  Use fire-retardant-treatment formulations that do not bleed through or otherwise adversely affect finishes.  Kiln-dry material after treatment.

C. Fire-Retardant Particleboard:  Panels made from softwood particles and fire-retardant chemicals mixed together at time of panel manufacture with flame-spread index of 25 or less and smoke-developed index of 25 or less per ASTM E 84.

D. Fire-Retardant Fiberboard:  ANSI A208.2 medium-density fiberboard panels made from softwood fibers, synthetic resins, and fire-retardant chemicals mixed together at time of panel manufacture with flame-spread index of 25 or less and smoke-developed index of 200 or less per ASTM E 84.

2.3 CABINET HARDWARE AND ACCESSORIES

A. General:  Provide cabinet hardware and accessory materials associated with architectural woodwork, except for items specified in Division 08 Section "Door Hardware (Scheduled by Describing Products)."

B. Frameless Concealed Hinges (European Type):  BHMA A156.9, B01602, 135 degrees of opening, self-closing.

C. Wire Pulls:  Back mounted, solid metal. 

D. Drawer Slides:  BHMA A156.9, B05091.

1. Standard Duty (Grade 1, Grade 2, and Grade 3): Side mounted and extending under bottom edge of drawer; full-extension  type; epoxy-coated steel with polymer rollers.

2. Heavy Duty (Grade 1HD-100 and Grade 1HD-200):  Side mounted; full-extension  type; zinc-plated steel ball-bearing slides.

Grades in three subparagraphs below correspond to the following initial load test requirements:  Grade 2:  30 lbf (13.3 kg); Grade 1:  50 lbf (22.2 kg); Grade 1HD-100:  100 lbf (44.5 kg); Grade 1HD-200:  200 lbf (90 kg).

3. Box Drawer Slides:  Grade 1HD-100; for drawers not more than 6 inches (150 mm) high and 24 inches (600 mm) wide.

4. File Drawer Slides:  Grade 1HD-200; for drawers more than 6 inches (150 mm) high or 24 inches (600 mm) wide.

5. Pencil Drawer Slides:  Grade 1; for drawers not more than 3 inches (75 mm) high and 24 inches (600 mm) wide.

E. Door Locks:  BHMA A156.11, E07121.

F. Drawer Locks:  BHMA A156.11, E07041.

2.4 MISCELLANEOUS MATERIALS

Delete first paragraph below if specified in a carpentry section.

A. Furring, Blocking, Shims, and Hanging Strips:  Softwood or hardwood lumber, fire-retardant-treated, kiln-dried to less than 15 percent moisture content.

Retain paragraph below if low-emitting materials are required for LEED Credit EQ 4.4.  See Evaluations.

B. Adhesives, General:  Do not use adhesives that contain urea formaldehyde.

2.5 FABRICATION

A. General:  Complete fabrication to maximum extent possible before shipment to Project site.  Where necessary for fitting at site, provide allowance for scribing, trimming, and fitting.

1. Interior Woodwork Grade: 
a. Paneling, Wainscot and Running Trim to receive transparent finish:  Premium

b. All other interior woodwork:  Custom.

2. Shop cut openings to maximum extent possible.  Sand edges of cutouts to remove splinters and burrs.  Seal edges of openings in countertops with a coat of varnish.

3. Install glass to comply with applicable requirements in Division 08 Section "Glazing" and in GANA's "Glazing Manual." For glass in wood frames, secure glass with removable stops.

B. Interior Standing and Running Trim:

1. For transparent-finished trim items wider than available lumber, use veneered construction.  Do not glue for width.

2. Backout or groove backs of flat trim members and kerf backs of other wide, flat members, except for members with ends exposed in finished work.

C. Flush Wood Paneling and Wainscots:

1. Lumber Trim and Edges:  At fabricator's option, trim and edges indicated as solid wood (except moldings) may be either lumber or veneered construction compatible with grain and color of veneered panels.

2. Matching of Adjacent Veneer Leaves:  Book match.

3. Veneer Matching within Panel Face:  Running match.

Retain subparagraph above for Economy grade; retain subparagraph below for Custom or Premium grade.  Options below are listed in order of increasing cost and last option only applies to Premium grade.

4. Panel-Matching Method:  In each separate area, use sequence-matched, uniform-size sets.

Delete subparagraph below if not applicable.

5. Fire-Retardant-Treated Paneling:  Provide panels consisting of wood veneer.  Panels shall have flame-spread index as required by code or less and smoke-developed index of 450 or less per ASTM E 84.

D. Wood Cabinets for Transparent Finish:

1. AWI Type of Cabinet Construction:  Reveal overlay on face frame.

Delete subparagraph below if reveal overlay construction is not used.

2. Reveal Dimension:  1/2 inch (13 mm) .

Retain subparagraph below for Premium-grade cabinets, or delete if selecting lower-quality grade or if grain matching is not required.

3. Grain Direction:  Vertically for drawer fronts, doors, and fixed panels .

Retain subparagraph below for Premium- or Custom-grade cabinets.

4. Matching of Veneer Leaves:  Book match.

Retain first subparagraph below for Premium-grade cabinets.

5. Veneer Matching within Panel Face:  Running match.

6. Semiexposed Surfaces Other Than Drawer Bodies:  Same species and cut indicated for exposed surfaces.

7. Drawer Sides and Backs:  Solid hardwood lumber.

8. Drawer Bottoms:  Hardwood plywood.

Delete subparagraph below if not desired.  Dust panels are not required by standards.

9. Provide dust panels of 1/4-inch (6.4-mm) plywood or tempered hardboard above compartments and drawers, unless located directly under tops.

E. Plastic-Laminate Cabinets:

1. AWI Type of Cabinet Construction:  Flush overlay.

2. Laminate Cladding for Exposed Surfaces:  High-pressure decorative laminate as follows:

Retain grade designations from options in four subparagraphs below.  Grade HGS is 1.2 mm thick, Grades HGL and HGP are 1.0 mm thick, and Grade VGS is 0.7 mm thick.  AWI and WI standards require minimum thickness of 0.028 inch (0.7 mm) regardless of surface type.

a. Horizontal Surfaces Other Than Tops:  Grade HGS.

b. Vertical Surfaces:  Grade HGS.

c. Edges:  Grade HGS.

3. Colors, Patterns, and Finishes:  As selected by Architect from laminate manufacturer's full range of solid colors and patterns in  matte finish.

Delete subparagraph below if not desired.  Dust panels are not required by standards.

4. Provide dust panels of 1/4-inch (6.4-mm) plywood or tempered hardboard above compartments and drawers, unless located directly under tops.

F. Solid-Surfacing-Material Countertops:

1. Solid-Surfacing-Material Thickness:  3/4 inch (19 mm).

2. Colors, Patterns, and Finishes:  As selected from manufacturer's full range.

3. Fabricate tops in one piece with field-applied backsplashes.  Comply with solid-surfacing-material manufacturer's written recommendations for adhesives, sealers, fabrication, and finishing.

2.6 SHOP FINISHING

A. Finish architectural woodwork at fabrication shop.  Defer only final touchup, cleaning, and polishing until after installation.

Generally retain first paragraph below.  WI does not require backpriming; AWI only requires it for certain items and grades.

B. Backpriming:  Apply one coat of sealer or primer, compatible with finish coats, to concealed surfaces of woodwork.  Apply two coats to back of paneling.

C. Transparent Finish:

Retain first subparagraph below unless retaining subparagraph requiring finish to be same grade as woodwork item being finished.

1. Grade:  Premium.

2. AWI Finish System:  Acrylic lacquer .

3. Staining:  Match approved sample for color.

Treatment in first subparagraph below helps prevent blotchiness with wiping stains; it is optional with AWI.

4. Wash Coat for Stained Finish:  Apply a wash-coat sealer to woodwork made from closed-grain wood before staining and finishing.

Coordinate option retained in subparagraph below with effect and finish system selected.  Numerical values for gloss ratings are those published in AWI standard.

5. Sheen:  Satin, 31-45 gloss units measured on 60-degree gloss meter per ASTM D 523.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Before installation, condition woodwork to average prevailing humidity conditions in installation areas.  Examine shop-fabricated work for completion and complete work as required, including removal of packing and backpriming.

Revise first paragraph below if installation grade is different from fabrication grade.

B. Grade:  Install woodwork to comply with requirements for the same grade specified in Part 2 for fabrication of type of woodwork involved.

C. Install woodwork level, plumb, true, and straight to a tolerance of 1/8 inch in 96 inches (3 mm in 2400 mm).  Shim as required with concealed shims.

D. Scribe and cut woodwork to fit adjoining work, refinish cut surfaces, and repair damaged finish at cuts.

E. Anchor woodwork to anchors or blocking built in or directly attached to substrates.  Secure with countersunk, concealed fasteners and blind nailing as required for complete installation.  Use fine finishing nails or finishing screws for exposed fastening, countersunk and filled flush with woodwork and matching final finish if transparent finish is indicated.

Delete any of five paragraphs and associated subparagraphs below if not applicable.

F. Standing and Running Trim:  Install with minimum number of joints possible, using full-length pieces (from maximum length of lumber available) to greatest extent possible. Scarf running joints and stagger in adjacent and related members. Fill gaps, if any, between top of base and wall with plastic wood filler, sand smooth, and finish same as wood base if finished.

G. Paneling:  Anchor paneling to supporting substrate with concealed panel-hanger clips or splined connection strips.  Do not use face fastening, unless covered by trim.

H. Cabinets:  Install without distortion so doors and drawers fit openings properly and are accurately aligned.  Adjust hardware to center doors and drawers in openings and to provide unencumbered operation.

Revise requirements in subparagraph below as necessary for seismic restraint of cabinets.  Delete if hanging cleats are used and are detailed on Drawings.

1. Fasten wall cabinets through back, near top and bottom, at ends and not more than 16 inches (400 mm) o.c. with  No. 10 wafer-head sheet metal screws through metal backing or metal framing behind wall finish.

I. Countertops:  Anchor securely by screwing through corner blocks of base cabinets or other supports into underside of countertop.  Calk space between backsplash and wall with sealant specified in Division 07 Section "Joint Sealants."

END OF SECTION 06402


INTERIOR ARCHITECTURAL WOODWORK

06402 - 6

