Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications


Copyright 2004 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 07115 - BITUMINOUS DAMPPROOFING
Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project.

1. Cold-applied, emulsified-asphalt dampproofing.

1.2 SUBMITTALS

A. Product Data:  For each type of product indicated.

1.3 PROJECT CONDITIONS

Delete paragraph below if no enclosed or interior applications are included in Project.

A. Ventilation:  Provide adequate ventilation during application of dampproofing in enclosed spaces.  Maintain ventilation until dampproofing has cured.

PART 2 -  PRODUCTS

2.1 COLD-APPLIED, EMULSIFIED-ASPHALT DAMPPROOFING

Select one or more of first three paragraphs below; coordinate with applications selected in Part 3.

A. Trowel Coats:  ASTM D 1227, Type II, Class 1.

B. Fibered Brush and Spray Coats:  ASTM D 1227, Type II, Class 1.

C. Brush and Spray Coats:  ASTM D 1227, Type III, Class 1.

D. VOC Content:  Zero.

2.2 MISCELLANEOUS MATERIALS

Product in paragraph below is water based and generally contains little or no VOCs.  Product can be used with either cut-back or emulsion topcoats and is generally more tolerant of damp substrates than product above.

A. Emulsified-Asphalt Primer:  ASTM D 1227, Type III, Class 1, except diluted with water as recommended by manufacturer.

Retain paragraph below if required for flashings and corner protection stripping at internal and external corners, changes in plane, construction joints, etc.

B. Asphalt-Coated Glass Fabric:  ASTM D 1668, Type I.

PART 3 -  EXECUTION

3.1 PREPARATION

A. Clean substrates of projections and substances detrimental to work; fill voids, seal joints, and apply bond breakers if any, as recommended by prime material manufacturer.

3.2 APPLICATION, GENERAL

A. Comply with manufacturer's written recommendations unless more stringent requirements are indicated or required by Project conditions to ensure satisfactory performance of dampproofing.

B. Apply dampproofing to provide continuous plane of protection on exterior face of inner wythe of exterior masonry cavity walls.

3.3 COLD-APPLIED, EMULSIFIED-ASPHALT DAMPPROOFING

If retaining this Article, coordinate paragraphs below with applications required.

A. On Masonry Backup for Dimension Stone Cladding:  Apply primer and 1 brush or spray coat at not less than 1 gal./100 sq. ft. (0.4 L/sq. m).

B. On Exterior Face of Inner Wythe of Cavity Walls:  Apply primer and 1 brush or spray coat at not less than 1 gal./100 sq. ft. (0.4 L/sq. m).

END OF SECTION 07115

BITUMINOUS DAMPPROOFING

07115 - 1

