Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications


SECTION 07162 - CRYSTALLINE WATERPROOFING
PART 1 -  GENERAL

1.1 SUMMARY

A. This Section includes crystalline waterproofing for elevator pits.

1.2 SUBMITTALS

A. Product Data:  For each type of product indicated.

B. Material test reports.

C. Warranty.

1.3 QUALITY ASSURANCE

A. Installer Qualifications:  An employer of workers trained and approved by manufacturer.

1.4 PROJECT CONDITIONS

A. Weather Limitations:  Proceed with application only when existing and forecasted weather conditions permit crystalline waterproofing to be performed according to manufacturer's written instructions and warranty requirements.

B. Proceed with waterproofing work only after pipe sleeves, vents, curbs, inserts, drains, and other projections through the substrate to be waterproofed have been completed.  Proceed only after concrete and masonry substrate defects, including honeycombs, voids, and cracks, have been repaired to provide a sound substrate free of forming materials, including reveal inserts.

C. Ambient Conditions:  Proceed with waterproofing work only if temperature is maintained at 40 deg F (4.4 deg C) or above during work and cure period, and space is well ventilated and kept free of water.

1.5 WARRANTY

A. Special Warranty:  Manufacturer's standard form in which manufacturer and installer agrees to repair or replace components of crystalline waterproofing that fail in materials or workmanship within specified warranty period.

1. Failures include, but are not limited to, the following:

a. Failure to maintain watertight conditions within specified warranty period.

2. Warranty Period:  Five years from date of Substantial Completion.

PART 2 -  PRODUCTS

2.1 MATERIALS

A. Crystalline Waterproofing:  A prepackaged, gray-colored proprietary blend of portland cement, specially treated sand, and active chemicals that, when mixed with water and applied, penetrates by capillary action into concrete or masonry and reacts chemically with free lime in the presence of water to develop crystalline growth within concrete or masonry capillaries to produce an impervious, dense, waterproof concrete or masonry with properties.

1. Permeability:  0 for water at 33 feet (10 m) when tested according to CE CRD-C 48.

2. Compressive Strength:  Minimum 3000 psi (20.7 MPa) when tested according to ASTM C 109/C 109M.

B. Patching Compound:  Cementitious waterproofing and repair mortar for filling and patching tie holes, honeycombs, reveals, and other imperfections; with properties meeting or exceeding the following criteria:

1. Compressive Strength:  7600 psi (52.44 MPa) at 28 days when tested according to ASTM C 109/C 109M.

2. Flexural Strength:  710 psi (4.8 MPa) at 28 days when tested according to ASTM C 348.

3. Shrinkage:  Minus 0.093 percent at 28 days and plus 0.073 percent at 90 days when tested according to ASTM C 596.

C. Plugging Compound:  Cementitious compound with hydrophobic properties; resistant to water and moisture but vapor permeable for all standard applications (vertical, overhead and horizontal surfaces not exposed to vehicular traffic); with properties meeting or exceeding the following criteria:

1. Permeability:  30 feet (9 m) when tested according to CE CRD-C 48.

2. Compressive Strength:  6000 psi (41.4 MPa) at 28 days when tested according to ASTM C 109/C 109M.

3. Flexural Strength:  1000 psi (6.9 MPa) at 28 days when tested according to ASTM C 348.

4. Bond Strength:  300 psi (2.1 MPa) at 14 days when tested according to ASTM C 321.

D. Water:  Potable.

PART 3 -  EXECUTION

3.1 PREPARATION

A. Protect other work from damage from cleaning, preparation, and application of crystalline waterproofing.  Provide temporary enclosure to confine spraying operation and to ensure adequate ambient temperatures and ventilation conditions for application.

B. Stop active water leaks according to waterproofing manufacturer's written instructions.

C. Repair damaged or unsatisfactory concrete or masonry according to manufacturer's written instructions.

D. Surface Preparation:  Comply with waterproofing manufacturer's written instructions to remove efflorescence, chalk, dust, dirt, mortar spatter, grease, oils, curing compounds, and form-release agents to ensure that waterproofing bonds to concrete or masonry surfaces.

1. Clean concrete surfaces according to ASTM D 4258.

a. Prepare smooth-formed and trowel-finished concrete by mechanical abrading or abrasive-blast cleaning according to ASTM D 4259.

2. Concrete Joints:  Clean reveals according to waterproofing manufacturer's written instructions.

3.2 APPLICATION

A. General:  Comply with waterproofing manufacturer's written instructions for application.

1. Dampen surface with water and maintain damp condition until applying waterproofing.

2. Apply waterproofing to negative-side surfaces.

Revise first subparagraph below for number of coats; delete brush or spray application if Contractor has option.

3. Number of Coats:  Two for brush or spray application.

4. Dampen surface between coats.

B. Final Coat Finish:  Smooth.

C. Moist-cure waterproofing for three days immediately after application has set, followed by two days of air drying as recommended in writing by manufacturer.

D. Waterproofing Treatment Extensions:  Extend waterproofing treatment as follows:

Revise four subparagraphs below to suit Project.

1. Onto every substrate in elevator pit including sumps, and similar offsets and features.

Retain paragraph below for horizontal applications that will not receive other permanent protection.

3.3 PROTECTION

A. Protect applied crystalline waterproofing from rapid drying, severe weather exposure, and water accumulation.  Maintain completed Work in moist condition for not less than three days by procedures recommended in writing by waterproofing manufacturer.  Protect waterproofing from temperatures below 36 deg F (2 deg C).

END OF SECTION 07162

CRYSTALLINE WATERPROOFING

07162 - 3

