Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications

Copyright 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 08211 - FLUSH WOOD DOORS
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Solid-core doors with wood-veneer faces.

Retain one or both subparagraphs below if applicable.  See Evaluations.

2. Factory finishing flush wood doors.

3. Factory fitting flush wood doors to frames and factory machining for hardware.

1.2 SUBMITTALS

A. Product Data:  For each type of door indicated.  Include factory-finishing specifications.
B. SPiRiT Submittals:

Retain first subparagraph below and "Forest Certification" Paragraph in "Quality Assurance" Article if flush wood doors are required to be certified for LEED Credit MR 7

1. Certificates for Credit MR 4.C7:  Chain-of-custody certificates certifying that flush wood doors comply with forest certification requirements.  Include evidence that manufacturer is certified for chain of custody by an FSC-accredited certification body.
Retain subparagraph below if low-emitting materials are required for LEED Credit EQ 4.4.

2. Product Data for Credit IEQ 5.C4:  For adhesives and composite wood products, indicating that product contains no urea formaldehyde.

C. Shop Drawings:  Indicate location, size, and hand of each door; elevation of each kind of door; construction details not covered in Product Data; location and extent of hardware blocking; and other pertinent data.

1. Indicate dimensions and locations of mortises and holes for hardware.

2. Indicate dimensions and locations of cutouts.

3. Indicate requirements for veneer matching.

4. Indicate doors to be factory finished and finish requirements.

5. Indicate fire-protection ratings for fire-rated doors.

D. Samples:  For factory-finished doors.

E. Warranty:  Sample of special warranty.

1.3 QUALITY ASSURANCE

Retain first paragraph below if required for LEED Credit MR 7.

A. Manufacturer Qualifications:  A qualified manufacturer that is certified for chain of custody by an FSC-accredited certification body.

Retain one standard in first paragraph below.  Verify applicability of selected standard for Project's geographic location.  Review selected standard and coordinate its requirements with selected options.  See Evaluations.

B. Quality Standard:  In addition to requirements specified, comply with AWI's "Architectural Woodwork Quality Standards Illustrated." 

Retain first paragraph below if wood products are required to be certified for LEED Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.  Before retaining, verify availability of required door types made from certified wood products.  See Evaluations.

C. Forest Certification:  Provide doors made with wood obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

Retain paragraph below and one of first two options, together with one or more of last five options, if fire-rated doors are required.

D. Fire-Rated Wood Doors:  Doors complying with NFPA 80 that are listed and labeled by a qualified testing agency, for fire-protection ratings required. 
1.4 WARRANTY

See Evaluations for door warranties.

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

A. Special Warranty:  Manufacturer's standard form in which manufacturer agrees to repair or replace doors that fail in materials or workmanship within specified warranty period.

1. Failures include, but are not limited to, the following:

a. Warping (bow, cup, or twist) more than 1/4 inch (6.4 mm) in a 42-by-84-inch (1067-by-2134-mm) section.

b. Telegraphing of core construction in face veneers exceeding 0.01 inch in a 3-inch (0.25 mm in a 76.2-mm) span.

Requirements in first subparagraph below are not standard with many manufacturers and could be an added cost if retained.

2. Warranty shall also include installation and finishing that may be required due to repair or replacement of defective doors.

Warranties for exterior doors vary from no warranty to a warranty for a period of up to five years.  Before retaining first subparagraph below, verify availability of warranty period with manufacturers selected; delete if retaining manufacturers that offer no warranty.  Standard manufacturer's warranty generally goes into effect on date of shipment, not date of Substantial Completion.

First subparagraph below is typical; revise if required.

3. Warranty Period for Solid-Core Interior Doors:  Life of installation.

Warranties for hollow-core doors vary with manufacturer and type of hollow core.  Before retaining subparagraph below, verify availability of warranty period with manufacturers selected.  Standard manufacturer's warranties generally go into effect on date of shipment, not date of Substantial Completion.

PART 2 -  PRODUCTS

2.1 DOOR CONSTRUCTION, GENERAL

Retain first paragraph below if low-emitting materials are required for LEED Credit EQ 4.4.

A. Low-Emitting Materials:  Provide doors made with adhesives and composite wood products that do not contain urea formaldehyde.

B. Fire-Protection-Rated Doors:  Provide mineral core as needed to provide fire-protection rating required.

Edge construction in first subparagraph below is used when positive-pressure fire testing is required; surface-applied intumescent seals can also be used.

1. Edge Construction:  Provide edge construction with intumescent seals concealed by outer stile.  Comply with specified requirements for exposed edges.

Retain subparagraph below if steel edges and astragals are not acceptable.  Coordinate availability and ratings with manufacturers selected.  Retain option if positive-pressure fire testing is required.

2. Pairs:  Provide fire-retardant stiles that are listed and labeled for applications required without formed-steel edges and astragals.  Provide stiles with concealed intumescent seals. Comply with specified requirements for exposed edges.

C. Mineral-Core Doors:

1. Core:  Noncombustible mineral product complying with requirements of referenced quality standard and testing and inspecting agency for fire-protection rating required.

2. Blocking:  Provide composite blocking with improved screw-holding capability approved for use in doors of fire-protection ratings required as needed to eliminate through-bolting hardware.

3. Edge Construction:  At hinge stiles, provide laminated-edge construction with improved screw-holding capability and split resistance.  Comply with specified requirements for exposed edges.

2.2 VENEERED-FACED DOORS FOR TRANSPARENT FINISH

A. Interior Solid-Core Doors:

Grade AA faces are required for AWI and WI Premium grade doors; Grade A faces are required for WDMA I.S.1-A Premium grade doors.  WDMA and WI have no Economy grade for doors.

1. Grade:  Premium, with Grade AA.

Options in first subparagraph below are examples only; revise or insert another species.  Last two options are examples of tropical species available as FSC-certified veneers (available from ForestWorld Group).

2. Species:  Red oak.

Option for rift cut in first subparagraph below applies only to oak.

3. Cut:  Plain sliced (flat sliced).

Balance match in first subparagraph below is required for AWI and WI Premium grade doors.  Running match is standard for Custom grade and WDMA Premium grade doors.  See Evaluations.

4. Assembly of Veneer Leaves on Door Faces:  Running match.

5. Pair and Set Match:  Provide for doors hung in same opening or separated only by mullions.

Retain one of five options in first subparagraph below.

6. Core:  Structural composite lumber.

7. Construction:  Five plies.  Stiles and rails are bonded to core, then entire unit abrasive planed before veneering.

2.3 LOUVERS AND LIGHT FRAMES

A. Metal Louvers:

Retain one of three subparagraphs below.

1. Metal and Finish:  Hot-dip galvanized steel, 0.040 inch (1.0 mm) thick, with baked-enamel- or powder-coated finish.

B. Metal Frames for Light Openings in Fire-Rated Doors:  Manufacturer's standard frame formed of 0.048-inch- (1.2-mm-) thick, cold-rolled steel sheet; with baked-enamel- or powder-coated finish; and approved for use in doors of fire-protection rating required.

2.4 FABRICATION

Delete first paragraph below if no doors are required to be factory fitted.  Plastic-laminate-edged and factory-finished doors must be factory fitted and machined.  Fire-rated and plastic-laminate-faced doors with wood edges should also be factory fitted and machined.  Factory fitting and machining for other doors are optional.  See Evaluations.

A. Factory fit doors to suit frame-opening sizes.  Comply with clearance requirements of referenced quality standard for fitting unless otherwise indicated.

1. Comply with requirements in NFPA 80 for fire-rated doors.

Delete first paragraph below if no doors are required to be factory machined.  Retain paragraph and revise to indicate exceptions if only some doors are required to be factory machined.  See Evaluations.

B. Factory machine doors for hardware that is not surface applied.

C. Openings:  Cut and trim openings through doors in factory.

1. Light Openings:  Trim openings with moldings of material and profile indicated.

First subparagraph below is unnecessary if only metal light frames are used.

2. Glazing:  Factory install glazing in doors.  Comply with applicable requirements in Division 08 Section "Glazing."

3. Louvers:  Factory install louvers in prepared openings.

2.5 FACTORY FINISHING

Retain this article if factory finishing is required.  Factory finishing can be used to help comply with LEED Credit EQ 4.2, which limits VOC content of paints and coatings used within building.

A. General:  Comply with referenced quality standard for factory finishing.  Complete fabrication, including fitting doors for openings and machining for hardware that is not surface applied, before finishing.

1. Finish faces, all four edges, edges of cutouts, and mortises.  Stains and fillers may be omitted on top and bottom edges, edges of cutouts, and mortises.

B. Finish doors at factory.  

Caution:  Finish systems can vary among manufacturers.  Require Samples for verification.

C. Transparent Finish:

Usually retain same grade for finish as specified for doors.

1. Grade:    Premium.

Retain one of three "Finish" subparagraphs below and one or more options in subparagraph retained, or insert another option.  Before specifying, verify availability of finishes with manufacturers selected.

2. Finish:  AWI conversion varnish or catalyzed polyurethane system.

3. Staining:  As selected from manufacturer's full range.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Hardware:  For installation, see Division 08 Section "Door Hardware."

B. Installation Instructions:  Install doors to comply with manufacturer's written instructions and the referenced quality standard, and as indicated.

Retain subparagraph below for fire-rated doors.

1. Install fire-rated doors in corresponding fire-rated frames according to NFPA 80.

Retain first paragraph below if all doors are not factory fitted.  Factory fitting of fire-rated doors is preferred to job fitting because of limitations on trimming narrower stiles and rails.

C. Factory-Fitted Doors:  Align in frames for uniform clearance at each edge.

D. Factory-Finished Doors:  Restore finish before installation if fitting or machining is required at Project site.

END OF SECTION 08211

FLUSH WOOD DOORS

08211 - 4

