Copyright 2003 and 2005 AIA
MASTERSPEC Full Length
08/03 (R 05/05)

Copyright 2003 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 035416 - HYDRAULIC CEMENT UNDERLAYMENT
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes hydraulic-cement-based underlayment for use below interior floor coverings.

B. Related Sections include the following:

List below only products that the reader might expect to find in this Section but are specified elsewhere.

1. Division 09 Sections for patching and leveling compounds applied with floor coverings.

Retain paragraph below if allowances are specified for underlayments.  Unless modified in Supplementary Conditions, allowances do not include installation.  See Evaluations.

C. Allowances:  Furnish hydraulic-cement-based underlayment under the allowances specified in Division 01 Section "Allowances."

Retain paragraph below for unit prices if applicable and insert Project-specific requirements.  See Evaluations.

D. Unit Prices:  Administrative and procedural requirements for unit prices are specified in Division 01 Section "Unit Prices."

1.3 SUBMITTALS

A. Product Data:  For each type of product indicated.

Retain paragraph below if survey of existing conditions is required.

B. Shop Drawings:  Plans indicating substrates, locations, and average depths of underlayment based on survey of substrate conditions.

Retain paragraph below if retaining "Product Compatibility" Paragraph in "Quality Assurance" Article.

C. Manufacturer Certificates:  Signed by manufacturers of both underlayment and floor covering system certifying that products are compatible.

Coordinate paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

D. Qualification Data:  For Installer.

Delete paragraph below if no preinstallation conference.

E. Minutes of preinstallation conference.

1.4 QUALITY ASSURANCE

Some manufacturers approve installers, others do not.  Revise first paragraph below to suit products selected.

A. Installer Qualifications:  Installer who is approved by manufacturer for application of underlayment products required for this Project.

B. Product Compatibility:  Manufacturers of both underlayment and floor covering system certify in writing that products are compatible.

Delete paragraph and subparagraphs below if not required.  If retaining, indicate location, size, and details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

C. Mockups:  Apply hydraulic-cement-based underlayment mockups to demonstrate surface finish, bonding, texture, tolerances, and standard of workmanship.

Revise size of mockups in first subparagraph below if required.

1. Apply mockups approximately 100 sq. ft. (9 sq. m) in area in location indicated or, if not indicated, as directed by Architect.

Retain subparagraph below if mockups are erected as part of building rather than separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

2. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 01.

D. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 01 Section "Project Management and Coordination."

1.5 DELIVERY, STORAGE, AND HANDLING

A. Store materials to comply with manufacturer's written instructions to prevent deterioration from moisture or other detrimental effects.

1.6 PROJECT CONDITIONS

A. Environmental Limitations:  Comply with manufacturer's written instructions for substrate temperature, ambient temperature and humidity, ventilation, and other conditions affecting underlayment performance.

1. Place hydraulic-cement-based underlayments only when ambient temperature and temperature of substrates are between 50 and 80 deg F (10 and 27 deg C).

1.7 COORDINATION

A. Coordinate application of underlayment with requirements of floor covering products, including adhesives, specified in Division 09 Sections, to ensure compatibility of products.

PART 2 -  PRODUCTS

2.1 HYDRAULIC-CEMENT-BASED UNDERLAYMENTS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

A. Underlayment:  Hydraulic-cement-based, polymer-modified, self-leveling product that can be applied in minimum uniform thicknesses of 1/8 inch (3 mm) and that can be feathered at edges to match adjacent floor elevations.

1. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

Retain subparagraph above for nonproprietary or subparagraph below for semiproprietary specification; retain list with either subparagraph.  Refer to Division 01 Section "Product Requirements."

2. Products:  Subject to compliance with requirements, provide one of the following:

a. Ardex; [K-15 Self-Leveling Underlayment Concrete] <Insert product name or designation>.

b. Bonsal, W. R. Company; [Self-Leveling Underlayment] <Insert product name or designation>.

c. ChemRex; [MBT Mastertop 110 Plus Underlayment] [Sonneborn Sonocrete Sonoflow] [Thoro Underlayment, Self-Leveling] <Insert product name or designation>.

d. Conspec, a Dayton Superior Company; [Conflow] <Insert product name or designation>.

e. Dayton Superior Corporation; [LeveLayer I] <Insert product name or designation>.

f. Dependable Chemical Co., Inc.; [Skimflow ES] <Insert product name or designation>.

g. L&M Construction Chemicals, Inc.; [Levelex] <Insert product name or designation>.

h. MAPEI Corporation; [Ultraplan 1] <Insert product name or designation>.

i. Maxxon Corporation; [Level-Right] <Insert product name or designation>.

j. US Mix Products Company; [US SPEC Self - Leveling Underlayment] <Insert product name or designation>.

k. <Insert manufacturer's name; product name or designation.>

Revise two subparagraphs below to suit products selected.

3. Cement Binder:  ASTM C 150, portland cement, or hydraulic or blended hydraulic cement as defined by ASTM C 219.

4. Compressive Strength:  Not less than [4100 psi (28 MPa)] <Insert value> at 28 days when tested according to ASTM C 109/C 109M.

Delete subparagraph below if not required.  Some manufacturers recommend additives for applications over cutback adhesive or wood and metal substrates.

5. Underlayment Additive:  Resilient-emulsion product of underlayment manufacturer formulated for use with underlayment when applied to substrate and conditions indicated.

Delete first paragraph and subparagraph below if addition of aggregate filler is not required by manufacturer to achieve thickness indicated.

B. Aggregate:  Well-graded, washed gravel, 1/8 to 1/4 inch (3 to 6 mm); or coarse sand as recommended by underlayment manufacturer.

1. Provide aggregate when recommended in writing by underlayment manufacturer for underlayment thickness required.

C. Water:  Potable and at a temperature of not more than 70 deg F (21 deg C).

When applied over wood, some manufacturers recommend reinforcing their products; see table in Evaluations.  Delete first paragraph below if not applicable.

D. Reinforcement:  For underlayment applied to wood substrates, provide galvanized metal lath or other corrosion-resistant reinforcement recommended in writing by underlayment manufacturer.

E. Primer:  Product of underlayment manufacturer recommended in writing for substrate, conditions, and application indicated.

Delete paragraph below if no metal substrates.  Some manufacturers do not recommend using their products over metal.

F. Corrosion-Resistant Coating:  Recommended in writing by underlayment manufacturer for metal substrates.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates, with Installer present, for conditions affecting performance.

1. Proceed with application only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. General:  Prepare and clean substrate according to manufacturer's written instructions.

1. Treat nonmoving substrate cracks according to manufacturer's written instructions to prevent cracks from telegraphing (reflecting) through underlayment.

2. Fill substrate voids to prevent underlayment from leaking.

Retain applicable substrates in first four paragraphs and associated subparagraphs below.

If underlayments will be installed over adhesive residues, consult manufacturers for recommendations and revise first paragraph below.

B. Concrete Substrates:  Mechanically remove, according to manufacturer's written instructions, laitance, glaze, efflorescence, curing compounds, form-release agents, dust, dirt, grease, oil, and other contaminants that might impair underlayment bond.

Retain subparagraph below if required by manufacturer for underlayment placed on hardened concrete slabs.

1. Moisture Testing:  Perform anhydrous calcium chloride test, ASTM F 1869.  Proceed with installation only after substrates do not exceed a maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/100 sq. m)] <Insert emission> in 24 hours.

C. Wood Substrates:  Mechanically fasten loose boards and panels to eliminate substrate movement and squeaks.  Sand to remove coatings that might impair underlayment bond and remove sanding dust.

Delete subparagraph below if not applicable.

1. Install underlayment reinforcement recommended in writing by manufacturer.

D. Metal Substrates:  Mechanically remove, according to manufacturer's written instructions, rust, foreign matter, and other contaminants that might impair underlayment bond.  Apply corrosion-resistant coating compatible with underlayment if recommended in writing by underlayment manufacturer.

E. Nonporous Substrates:  For ceramic tile, quarry tile, and terrazzo substrates, remove waxes, sealants, and other contaminants that might impair underlayment bond, and prepare surfaces according to manufacturer's written instructions.

F. Adhesion Tests:  After substrate preparation, test substrate for adhesion with underlayment according to manufacturer's written instructions.

3.3 APPLICATION

Indicate underlayment thicknesses on Drawings or insert requirements in this Article.

A. General:  Mix and apply underlayment components according to manufacturer's written instructions.

1. Close areas to traffic during underlayment application and for time period after application recommended in writing by manufacturer.

2. Coordinate application of components to provide optimum underlayment-to-substrate and intercoat adhesion.

Delete subparagraph below if no moving joints in floor.  Detail joints on Drawings and revise below to suit Project.

3. At substrate expansion, isolation, and other moving joints, allow joint of same width to continue through underlayment.

B. Apply primer over prepared substrate at manufacturer's recommended spreading rate.

C. Apply underlayment to produce uniform, level surface.

Delete first subparagraph below if addition of aggregate is not required for thickness indicated.

1. Apply a final layer without aggregate to produce surface.

2. Feather edges to match adjacent floor elevations.

D. Cure underlayment according to manufacturer's written instructions.  Prevent contamination during application and curing processes.

E. Do not install floor coverings over underlayment until after time period recommended in writing by underlayment manufacturer.

F. Remove and replace underlayment areas that evidence lack of bond with substrate, including areas that emit a "hollow" sound when tapped.

3.4 PROTECTION

A. Protect underlayment from concentrated and rolling loads for remainder of construction period.

END OF SECTION 035416

	HYDRAULIC CEMENT UNDERLAYMENT
	035416 - 1



