Copyright 2000 and 2005 AIA
MASTERSPEC Full Length
08/00 (R 05/06)

Copyright 2000 and 2005The American Institute of Architects (AIA)

SECTION 093000 - TILING
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project.

1. Ceramic mosaic tile.

2. Quarry tile.

3. Paver tile.

4. Glazed wall tile.

5. Special-purpose tile.

6. [Stone] [Solid polymer] thresholds installed as part of tile installations.

7. Waterproof membrane for[ thin-set] tile installations.

8. Crack-suppression membrane for thin-set tile installations.

9. Cementitious backer units installed as part of tile installations.

10. Metal edge strips installed as part of tile installations.

B. Related Sections include the following:

List below only products, construction, and equipment that the reader might expect to find in this Section but are specified elsewhere.

Delete first subparagraph below if no existing finishes are to be removed.

1. Division 02 Section "Selective Structure Demolition" for removing existing finishes.

2. Division 03 Section "Cast-in-Place Concrete" for monolithic slab finishes specified for tile substrates.

Delete subparagraph below if not applicable.

3. Division 07 Section "[Self-Adhering Sheet Waterproofing] [Elastomeric Sheet Waterproofing] [Thermoplastic Sheet Waterproofing] [Cold Fluid-Applied Waterproofing] [Hot Fluid-Applied Rubberized Asphalt Waterproofing]" for waterproofing under thickset mortar beds.

Delete subparagraph below if sealant materials and installation for expansion and control joints are specified in this Section.

4. Division 07 Section "Joint Sealants" for sealing of expansion, contraction, control, and isolation joints in tile surfaces.

Retain subparagraph below if local trade practice requires installation of scratch coat by plasterer.

5. Division 09 Section "Portland Cement Plastering" for portland cement scratch coat over metal lath on wall surfaces.

Delete subparagraph below if cementitious backer units are specified in this Section.  See Evaluations.

6. Division 09 Section "Gypsum Veneer Plastering" for cementitious backer units.

Delete first option in first subparagraph below if cementitious backer units are used and are specified in this Section.  See Evaluations.

7. Division 09 Section "Gypsum Board" for [cementitious backer units] [glass-mat, water-resistant backer board].

8. Division 09 Section "Stone Tiling."

Delete subparagraph below if stone thresholds are specified in this Section.

9. Division 09 Section "Stone Flooring" for stone thresholds.

1.3 DEFINITIONS

Coordinate definitions below for tile sizes with titles used to specify dimensions indicated in Part 2 "Tile Products" Article.  Revise if other definitions are needed.  See Editing Instruction No. 5 in the Evaluations.

A. Module Size:  Actual tile size (minor facial dimension as measured per ASTM C 499) plus joint width indicated.

B. Facial Dimension:  Actual tile size (minor facial dimension as measured per ASTM C 499).

Delete paragraph above or below.  Retain above if actual sizes are specified for tile facial dimensions in Part 2 "Tile Products" Article.  Retain below if nominal sizes are specified.

C. Facial Dimension:  Nominal tile size as defined in ANSI A137.1.

1.4 PERFORMANCE REQUIREMENTS

Paragraph and subparagraphs below are based on appendix to the Americans with Disabilities Act (ADA), "Accessibility Guidelines for Buildings and Facilities (ADAAG)," and are not mandatory.  See Evaluations for further discussion on slip resistance and coefficient of friction values.  If retaining below, verify that tile products selected for flooring comply with requirements.

A. Static Coefficient of Friction:  For tile installed on walkway surfaces, provide products with the following values as determined by testing identical products per ASTM C 1028:

Omit step treads and ramp surfaces below if not used.

1. Level Surfaces:  Minimum 0.6.

2. Step Treads:  Minimum 0.6.

3. Ramp Surfaces:  Minimum 0.8.

1.5 SUBMITTALS

A. Product Data:  For each type of product indicated.

Delete first paragraph below if tile installations are not complex enough to justify Shop Drawings.

B. Shop Drawings:  Show locations of each type of tile and tile pattern.  Show widths, details, and locations of expansion, contraction, control, and isolation joints in tile substrates and finished tile surfaces.

C. Samples for Initial Selection:  For each type of tile and grout indicated.  Include Samples of accessories involving color selection.

Delete paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain paragraph and subparagraphs below with or without above.  Revise list of Samples to correspond with products specified.

D. Samples for Verification:

1. Full-size units of each type and composition of tile and for each color and finish required.

Select subparagraph above or first subparagraph below.

2. Assembled samples with grouted joints for each type and composition of tile and for each color and finish required, at least 12 inches (300 mm) square and mounted on rigid panel.  Use grout of type and in color or colors approved for completed work.

3. Full-size units of each type of trim and accessory[ for each color and finish required].

4. Stone thresholds in 6-inch (150-mm) lengths.

5. Metal edge strips in 6-inch (150-mm) lengths.

Retain paragraph and subparagraph below if low-emitting materials are required for LEED-NC and LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives and sealants.

E. LEED Submittal:

1. Credit EQ 4.1:  Manufacturers' product data for [adhesives] [and] [sealants], including printed statement of VOC content.

Certificates in first paragraph below are issued by manufacturers indicating that tile complies with ANSI A137.1 and indicating type and grade of tile according to this standard.  Delete both paragraphs if not required or not available, as may be the case with imported tile.

F. Master Grade Certificates:  For each shipment, type, and composition of tile, signed by tile manufacturer and Installer.

G. Product Certificates:  For each type of product, signed by product manufacturer.

Coordinate paragraph below with qualification requirements in Division 01 Section "Quality Requirements."

H. Qualification Data:  For Installer.

Delete test reports below if not required.  Retain option if needed to establish compliance of products with characteristics specified.

I. Material Test Reports:  For each tile-setting and -grouting product[ and special-purpose tile].

1.6 QUALITY ASSURANCE

Select one of four options in first paragraph below depending on complexity of Project and degree of restriction desired.

A. Source Limitations for Tile:  Obtain all [tile of same type and color or finish] [tile of same type] [tile of same color or finish] [tile] from one source or producer.

1. Obtain tile from same production run and of consistent quality in appearance and physical properties for each contiguous area.

B. Source Limitations for Setting and Grouting Materials:  Obtain ingredients of a uniform quality for each mortar, adhesive, and grout component from a single manufacturer and each aggregate from one source or producer.

C. Source Limitations for Other Products:  Obtain each of the following products specified in this Section through one source from a single manufacturer for each product:

Delete products below not retained in Part 2 and insert those that are added.

1. Stone thresholds.

2. Waterproofing.

3. Joint sealants.

4. Cementitious backer units.

5. Metal edge strips.

Delete paragraph and subparagraphs below if not required.  If retaining, indicate location, size, extent of products for which mockups are required, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

D. Mockups:  Build mockups to [verify selections made under sample Submittals and to demonstrate aesthetic effects] [and qualities of materials and execution].

Division 01 Section "Quality Requirements" states "build mockups in location and of size indicated or, if not indicated, as directed...." Consider inserting size and location requirements in subparagraphs below or showing on Drawings.

1. Build mockup of[ each type of] floor tile installation.

2. Build mockup of[ each type of] wall tile installation.

Retain subparagraph below if mockups are erected as part of building rather than separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

3. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Delete paragraph below if work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 01.

E. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 01 Section "Project Management and Coordination."

Insert requirements for fire-test-response characteristics if Project has fire-rated partitions with ceramic tile face.

1.7 DELIVERY, STORAGE, AND HANDLING

A. Deliver and store packaged materials in original containers with seals unbroken and labels intact until time of use.  Comply with requirement in ANSI A137.1 for labeling sealed tile packages.

B. Store tile and cementitious materials on elevated platforms, under cover, and in a dry location.

C. Store aggregates where grading and other required characteristics can be maintained and contamination avoided.

D. Store [liquid latexes] [and] [emulsion adhesives] in unopened containers and protected from freezing.

Delete below if no tile with temporary protective coating.

E. Handle tile that has temporary protective coating on exposed surfaces to prevent coated surfaces from contacting backs or edges of other units.  If coating does contact bonding surfaces of tile, remove coating from bonding surfaces before setting tile.

1.8 PROJECT CONDITIONS

A. Environmental Limitations:  Do not install tile until construction in spaces is complete and ambient temperature and humidity conditions are maintained at the levels indicated in referenced standards and manufacturer's written instructions.

1.9 EXTRA MATERIALS

Extra materials may not be allowed for publicly funded projects.

A. Furnish extra materials described below that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Revise subparagraph below to suit Project.

1. Tile and Trim Units:  [Furnish quantity of full-size units equal to 3 percent of amount installed, for each type, composition, color, pattern, and size indicated.]

Select option in subparagraph above and delete below, or delete option and retain below.

a. <Insert, in separate subparagraphs, tile type designation or description and quantity required for each category of tile for which extra material is required.>

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

See Editing Instruction No. 2 in the Evaluations.

Edit this Article with other Part 2 articles in which manufacturers and products, or manufacturers only, are named.  See Division 01 Section "Product Requirements" for an explanation of the terms "Available Products," "Products," "Available Manufacturers," "Manufacturers," and "Basis-of-Design Product" and the effect these terms have on "Comparable Product" and "Product Substitution" requirements.

A. In other Part 2 articles where titles below introduce lists, the following requirements apply for product selection:

1. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the products specified.

2. Products:  Subject to compliance with requirements, provide one of the products specified.

3. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the manufacturers specified.

4. Manufacturers:  Subject to compliance with requirements, provide products by one of the manufacturers specified.

5. Basis-of-Design Product:  The design for each tile type is based on the product named.  Subject to compliance with requirements, provide either the named product or a comparable product by one of the other manufacturers specified.

2.2 PRODUCTS, GENERAL

Revise or delete first paragraph and subparagraphs below if another standard is used to specify tile products.

A. ANSI Ceramic Tile Standard:  Provide tile that complies with ANSI A137.1, "Specifications for Ceramic Tile," for types, compositions, and other characteristics indicated.

Revise subparagraph below if seconds (Second grade tile) are acceptable.

1. Provide tile complying with Standard grade requirements, unless otherwise indicated.

Retain subparagraph below with appropriate definitions in Part 1 "Definitions" Article.

2. For facial dimensions of tile, comply with requirements relating to tile sizes specified in Part 1 "Definitions" Article.

B. ANSI Standards for Tile Installation Materials:  Provide materials complying with ANSI standards referenced in "Setting and Grouting Materials" Article.

Where floor areas are indicated to receive tile with or without slip-resistant wearing surface provided by abrasive content or surface, retain recommended requirement for minimum static coefficient of friction in Part 1 "Performance Requirements" Article.  See Evaluations.

C. Colors, Textures, and Patterns:  Where manufacturer's standard products are indicated for tile, grout, and other products requiring selection of colors, surface textures, patterns, and other appearance characteristics, provide specific products or materials complying with the following requirements:

Retain one requirement from options in subparagraph below.  If retaining first option, indicate colors, textures, and patterns on Drawings or by inserts into Part 2 "Tile Products," "Thresholds," and "Setting and Grouting Materials" articles or Part 3 tile installation schedules.  See Editing Instruction No. 3 in the Evaluations.

1. [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

D. Factory Blending:  For tile exhibiting color variations within ranges selected during Sample submittals, blend tile in factory and package so tile units taken from one package show same range in colors as those taken from other packages and match approved Samples.

E. Mounting:  For factory-mounted tile, provide back- or edge-mounted tile assemblies as standard with manufacturer, unless otherwise indicated.

Retain subparagraph below if tile is used in swimming pools, on exteriors, or in wet areas.  According to ANSI A137.1, manufacturers must specify whether back- or edge-mounted tile assemblies are suitable for these installations.

1. Where tile is indicated for installation [in swimming pools] [on exteriors] [or] [in wet areas], do not use back- or edge-mounted tile assemblies unless tile manufacturer specifies in writing that this type of mounting is suitable for installation indicated and has a record of successful in-service performance.

See Editing Instruction No. 4 in the Evaluations before deleting or retaining below; retaining affects other requirements in this Section.

F. Factory-Applied Temporary Protective Coating:  Where indicated under tile type, protect exposed surfaces of tile against adherence of mortar and grout by precoating with continuous film of petroleum paraffin wax, applied hot.  Do not coat unexposed tile surfaces.

2.3 TILE PRODUCTS

See Editing Instructions No. 5 through No. 7 in the Evaluations before editing this Article.  Facial dimensions indicated are examples only.  Coordinate tile facial dimensions or module sizes with definitions retained in Part 1 "Definitions" Article.  Copy and edit each paragraph as needed for each type of tile required.  Insert number to complete designations below.  Use these designations on Drawings to show where tile is required.

Coordinate first paragraph and subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.  Delete paragraph and subparagraphs if manufacturers and products are named for each tile type.  If retaining, delete those manufacturers that do not offer tile types specified in this Article.  See tables in the Evaluations for a list of manufacturers according to product types.

A. [Available ]Manufacturers:

1. American Marazzi Tile, Inc.

2. American Olean; Div. of Dal-Tile International Corp.

3. Buchtal Corporation USA.

4. Cerim-Floor Gres Ceramiche.

5. Crossville Ceramics Company, L.P.

6. Daltile; Div. of Dal-Tile International Inc.

7. Florida Tile Industries, Inc.

8. GranitiFiandre.

9. Interceramic.

10. KPT, Inc.

11. Laufen USA.

12. Lone Star Ceramics Company.

13. Metropolitan Ceramics.

14. Monarch Tile, Inc.

15. Porcelanite, Inc.

16. Quarry Tile Company.

17. Seneca Tiles, Inc.

18. Summitville Tiles, Inc.

19. United States Ceramic Tile Company.

20. Winburn Tile Manufacturing Company.

21. <Insert manufacturer's name.>

B. Unglazed Ceramic Mosaic Tile [CT-<#>]:  Factory-mounted flat tile as follows:

1. Composition:  [Porcelain] [Impervious natural clay or porcelain] [Vitreous or impervious natural clay or porcelain].

2. Surface:  [Smooth, without] [Slip-resistant, with] abrasive admixture.

3. Module Size:  [1 by 1 inch (25.4 by 25.4 mm)] [1 by 2 inches (25.4 by 50.8 mm)] [2 by 2 inches (50.8 by 50.8 mm)] [1-inch (25.4-mm) hexagon] [2-inch (50.8-mm) hexagon] [blend pattern consisting of tiles 1 by 1 inch (25.4 by 25.4 mm), 1 by 2 inches (25.4 by 50.8 mm), and 2 by 2 inches (50.8 by 50.8 mm)] <Insert size>.

4. Nominal Thickness:  1/4 inch (6.35 mm).

5. Face:  [Plain] [Pattern of design indicated,] with cushion edges.

Retain one of two subparagraphs and associated subparagraph below.  Coordinate with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

6. Basis-of-Design Product:  <Insert manufacturer's name; product name or designation and possibly color or color group> or a comparable product of one of the following:

a. <Insert, in separate subparagraphs, manufacturer's name.>

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

C. Glazed Ceramic Mosaic Tile [CT-<#>]:  Factory-mounted flat tile as follows:

1. Composition:  [Porcelain] [Impervious natural clay or porcelain] [Vitreous or impervious natural clay or porcelain].

2. Module Size:  [1 by 1 inch (25.4 by 25.4 mm)] [1 by 2 inches (25.4 by 50.8 mm)] [2 by 2 inches (50.8 by 50.8 mm)] <Insert size>.

3. Thickness:  1/4 inch (6.35 mm).

4. Face:  [Plain] [Pattern of design indicated,] with cushion edges.

Descriptions of glazes in subparagraph below are defined in ASTM C 242; all may not be available in or suitable for this tile type.  If inserting another description, also include list of products meeting that description.

5. Finish:  [Bright, opaque] [Bright, clear] [Mat, opaque] [Mat, clear] [Semimat, opaque] [Semimat, clear] [Vellum, opaque] [Vellum, clear] [Crystalline] <Insert description> glaze.

Retain one of two subparagraphs and associated subparagraph below unless generic specification is required.  Coordinate with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

6. Basis-of-Design Product:  <Insert manufacturer's name; product name or designation and possibly color or color group> or a comparable product of one of the following:

a. <Insert, in separate subparagraphs, manufacturer's name.>

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

D. Unglazed Quarry Tile [CT-<#>]:  Square-edged flat tile as follows:

1. Wearing Surface:  [Nonabrasive, smooth] [Nonabrasive, textured] [Abrasive aggregate embedded in surface].

2. Facial Dimensions:  [3 by 3 inches (76 by 76 mm)] [4 by 4 inches (102 by 102 mm)] [6 by 3 inches (152 by 76 mm)] [6 by 6 inches (152 by 152 mm)] [8 by 3-7/8 inches (203 by 98 mm)] [7-5/8 by 7-5/8 inches (194 by 194 mm)] [8 by 8 inches (203 by 203 mm)] [160 by 320 mm] [140 by 280 mm] [300 by 300 mm] <Insert dimensions>.

3. Thickness:  [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)] [3/4 inch (19 mm)].

4. Face:  [Plain] [Pattern of design indicated].

Delete subparagraph below if not applicable.  If retaining, coordinate with coating requirements specified elsewhere in this Section.  See Editing Instruction No. 4 in the Evaluations.

5. For furan-grouted quarry tile, precoat with temporary protective coating.

Retain one of two subparagraphs and associated subparagraph below unless generic specification is required.  Coordinate with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

6. Basis-of-Design Product:  <Insert manufacturer's name; product name or designation> or a comparable product of one of the following:

a. <Insert, in separate subparagraphs, manufacturer's name.>

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

E. Glazed Quarry Tile [CT-<#>]:  Square-edged flat tile as follows:

1. Wearing Surface:  [Nonabrasive] [Abrasive aggregate embedded in surface].

2. Facial Dimensions:  [3 by 3 inches (76 by 76 mm)] [4 by 4 inches (102 by 102 mm)] [6 by 3 inches (152 by 76 mm)] [6 by 6 inches (152 by 152 mm)] [8 by 3-7/8 inches (203 by 98 mm)] [8 by 8 inches (203 by 203 mm)] <Insert dimensions>.

3. Thickness:  [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)] [3/4 inch (19 mm)].

4. Face:  [Plain] [Pattern of design indicated] [As indicated].

Descriptions of glazes in subparagraph below are defined in ASTM C 242; all may not be available in or suitable for this tile type.  If inserting another description, also include list of products meeting that description.

5. Finish:  [Bright, opaque] [Bright, clear] [Mat, opaque] [Mat, clear] [Semimat, opaque] [Semimat, clear] [Vellum, opaque] [Vellum, clear] [Crystalline] <Insert description> glaze.

Retain one of two subparagraphs and associated subparagraph below unless generic specification is required.  Coordinate with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

6. Basis-of-Design Product:  <Insert manufacturer's name; product name or designation and possibly color or color group> or a comparable product of one of the following:

a. <Insert, in separate subparagraphs, manufacturer's name.>

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

F. Unglazed Paver Tile [CT-<#>]:  Flat tile as follows:

1. Composition:  [Porcelain] [Impervious natural clay or porcelain] [Vitreous or impervious natural clay or porcelain] [Natural clay or porcelain].

2. Facial Dimensions:  [7-3/4 by 3-7/8 inches (197 by 98 mm)] [7-7/8 by 7-7/8 inches (200 by 200 mm)] [11-13/16 by 11-13/16 inches (300 by 300 mm)] [200 by 200 mm] [300 by 300 mm] <Insert dimensions>.

3. Thickness:  [1/4 inch (6.35 mm)] [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)].

4. Face:  [Plain with square or cushion edges] [Plain with square edges] [Plain with cushion edges] [Pattern of design indicated, with square or cushion edges].

Delete subparagraph below if not applicable.  If retaining, coordinate with coating requirements specified elsewhere in this Section.  See Editing Instruction No. 4 in the Evaluations.

5. For latex-portland cement-mortared and -grouted paver tile, precoat with temporary protective coating.

Retain one of two subparagraphs and associated subparagraph below unless generic specification is required.  Coordinate with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

6. Basis-of-Design Product:  <Insert manufacturer's name; product name or designation and possibly color or color group> or a comparable product of one of the following:

a. <Insert, in separate subparagraphs, manufacturer's name.>

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

G. Glazed Paver Tile [CT-<#>]:  Flat tile as follows:

1. Composition:  [Porcelain] [Impervious natural clay or porcelain] [Vitreous or impervious natural clay or porcelain] [Semivitreous, vitreous, or impervious natural clay or porcelain].

2. Facial Dimensions:  [3 by 3 inches (76 by 76 mm)] [4 by 4 inches (102 by 102 mm)] [6 by 6 inches (152 by 152 mm)] [7-3/4 by 3-7/8 inches (197 by 98 mm)] [7-7/8 by 7-7/8 inches (200 by 200 mm)] [11-13/16 by 11-13/16 inches (300 by 300 mm)] [165 by 333 mm] [200 by 250 mm] [250 by 250 mm] [165 by 333 mm] [333 by 333 mm] [400 by 400 mm] <Insert dimensions>.

3. Thickness:  [1/4 inch (6.35 mm)] [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)].

4. Face:  [Plain with square or cushion edges] [Plain with square edges] [Plain with cushion edges] [Pattern of design indicated, with square or cushion edges] [As indicated].

Descriptions of glazes in subparagraph below are defined in ASTM C 242; all may not be available in or suitable for this tile type.  If inserting another description, also include list of products meeting that description.

5. Finish:  [Bright, opaque] [Bright, clear] [Mat, opaque] [Mat, clear] [Semimat, opaque] [Semimat, clear] [Vellum, opaque] [Vellum, clear] [Crystalline] <Insert description> glaze.

Retain one of two subparagraphs and associated subparagraph below unless generic specification is required.  Coordinate with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

6. Basis-of-Design Product:  <Insert manufacturer's name; product name or designation; and possibly color or color group> or a comparable product of one of the following:

a. <Insert, in separate subparagraphs, manufacturer's name.>

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

H. Glazed Wall Tile [CT-<#>]:  Flat tile as follows:

1. Module Size:  [4-1/4 by 4-1/4 inches (108 by 108 mm)] [6 by 4-1/4 inches (152 by 108 mm)] [6 by 6 inches (152 by 152 mm)] [200 by 200 mm] [250 by 250 mm] [200 by 300 mm] <Insert size>.

2. Thickness:  5/16 inch (8 mm).

3. Face:  [Plain with modified square edges or cushion edges] [Plain with modified square edges] [Plain with cushion edges] [Pattern of design indicated, with manufacturer's standard edges].

Descriptions of glazes in first subparagraph below are defined in ASTM C 242; all may not be available in or suitable for this tile type.  If inserting another description, also include list of products meeting that description.

4. Finish:  [Bright, opaque] [Bright, clear] [Mat, opaque] [Mat, clear] [Semimat, opaque] [Semimat, clear] [Vellum, opaque] [Vellum, clear] [Crystalline] <Insert description> glaze.

5. Mounting:  Factory back-mounted.

Delete subparagraph above if tile selected is available in loose form only.  Delete subparagraph below if pregrouted tile is not desired.

6. Mounting:  Pregrouted sheets of tiles factory assembled and grouted with manufacturer's standard silicone rubber.

Retain one of two subparagraphs and associated subparagraph below unless generic specification is required.  Coordinate with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

7. Basis-of-Design Product:  <Insert manufacturer's name; product name or designation and possibly color or color group> or a comparable product of one of the following:

a. <Insert, in separate subparagraphs, manufacturer's name.>

8. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

Insert special-purpose tile requirements here if required.

If glazed wall tile trim units do not match adjoining flat tile, revise paragraph and subparagraphs below and add descriptive requirements by copying subparagraphs from "Glazed Wall Tile" Paragraph.

I. Glazed Wall Tile Trim Units:  Matching characteristics of adjoining flat tile and coordinated with sizes and coursing of adjoining flat tile where applicable.  Provide shapes as follows, selected from manufacturer's standard shapes:

Select shape requirements from examples below that suit installation methods; delete subparagraphs if not applicable.  Revise or supplement to suit Project.

1. Base for Portland Cement Mortar Installations:  Coved, module size [4-1/4 by 4-1/4 inches (108 by 108 mm)] [6 by 6 inches (152 by 152 mm)] [6 by 3-3/4 inches (152 by 95 mm)] <Insert size>.

2. Base for Thin-Set Mortar Installations:  Straight, module size [4-1/4 by 4-1/4 inches (108 by 108 mm)] [6 by 6 inches (152 by 152 mm)] [6 by 2 inches (152 by 51 mm)] <Insert size>.

3. Wainscot Cap for Portland Cement Mortar Installations:  Bullnose cap, module size [4-1/4 by 4-1/4 inches (108 by 108 mm)] [6 by 6 inches (152 by 152 mm)] [6 by 2 inches (152 by 51 mm)] <Insert size>.

4. Wainscot Cap for Thin-Set Mortar Installations:  Surface bullnose, module size [4-1/4 by 4-1/4 inches (108 by 108 mm)] [6 by 6 inches (152 by 152 mm)] [6 by 2 inches (152 by 51 mm)] <Insert size>.

5. Wainscot Cap for Flush Conditions:  Regular flat tile for conditions where tile wainscot is shown flush with wall surface above.

6. External Corners for Portland Cement Mortar Installations:  Bullnose shape with radius of at least 3/4 inch (19 mm), unless otherwise indicated.

7. External Corners for Thin-Set Mortar Installations:  Surface bullnose.

Revise subparagraph below if coved internal angles are required.

8. Internal Corners:  Field-butted square corners except with coved base and cap angle pieces designed to fit with stretcher shapes.

Insert other shapes as required.

If ceramic mosaic trim units do not match adjoining flat tile, revise paragraph and subparagraphs below and add descriptive requirements by copying subparagraphs from "Unglazed Ceramic Mosaic Tile" or "Glazed Ceramic Mosaic Tile" Paragraph.

J. Ceramic Mosaic Trim Units:  Matching characteristics of adjoining flat tile and coordinated with sizes and coursing of adjoining flat tile where applicable.  Provide shapes as follows, selected from manufacturer's standard shapes:

Select shape requirements from examples below that suit installation methods; delete subparagraphs if not applicable.  Revise or supplement to suit Project.

1. Base Cove:  Cove, module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] <Insert size>.

2. Base Cap for Portland Cement Mortar Installations:  Bead (bullnose), module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] <Insert size>.

3. Base Cap for Thin-Set Mortar Installations:  Surface bullnose, module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] [2 by 2 inches (50.8 by 50.8 mm)] <Insert size>.

4. Wainscot Cap for Portland Cement Mortar Installations:  Bead (bullnose), module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] <Insert size>.

5. Wainscot Cap for Thin-Set Mortar Installations:  Surface bullnose, module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] [2 by 2 inches (50.8 by 50.8 mm)] <Insert size>.

6. Wainscot Cap for Flush Conditions:  Regular flat tile for conditions where tile wainscot is shown flush with wall surface above.

7. External Corners for Portland Cement Mortar Installations:  Bead (bullnose), module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] <Insert size>.

8. External Corners for Thin-Set Mortar Installations:  Surface bullnose, module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] [2 by 2 inches (50.8 by 50.8 mm)] <Insert size>.

Revise subparagraph below if field-butted, square internal angles are required.

9. Internal Corners:  Cove, module size [1 by 1 inch (25.4 by 25.4 mm)] [2 by 1 inch (50.8 by 25.4 mm)] <Insert size>.

Units below are available from some manufacturers.  Before retaining, verify availability of required colors and textures with manufacturers selected.

10. Tapered Transition Tile:  Shape designed to effect transition between thickness of tile floor and adjoining floor finishes of different thickness, tapered to provide reduction in thickness from 1/2 to 1/4 inch (12.7 to 6.35 mm) across nominal 4-inch (100-mm) dimension.

Insert other shapes as required.

K. Quarry Tile Trim Units:  Matching characteristics of adjoining flat tile and coordinated with sizes and coursing of adjoining flat tile where applicable.  Provide shapes as follows, selected from manufacturer's standard shapes:

Select shape requirements from examples below that suit installation methods; delete subparagraphs if not applicable.  Revise or supplement to suit Project.

1. Base:  Coved[ with surface bullnose top edge], facial dimensions [6 by 6 inches (152 by 152 mm)] [8 by 3-7/8 inches (203 by 98 mm)] <Insert size>.

2. Wainscot Cap:  Surface bullnose, facial dimensions [6 by 6 inches (152 by 152 mm)] [8 by 3-7/8 inches (203 by 98 mm)] <Insert size>.

3. Wainscot Cap for Flush Conditions:  Regular flat tile for conditions where tile wainscot is shown flush with wall surface above.

Accessories below are generally used with glazed wall tile.  Delete paragraph and subparagraphs if not applicable.  Verify availability with manufacturers selected.  Revise if colors of accessories are different from adjoining tile.

L. Accessories for Glazed Wall Tile:  Provide vitreous china accessories of type and size indicated, in color and finish to match adjoining wall tile, and intended for installing by same method as adjoining wall tile.

Subparagraphs below are examples only.  Revise to suit Project.

1. One soap holder[ with grab handle] for each shower and tub indicated.

2. One paper holder at each water closet.

2.4 THRESHOLDS

A. General:  Fabricate to sizes and profiles indicated or required to provide transition between adjacent floor finishes.

Revise subparagraph below as necessary or delete if accessibility for people with disabilities is not required.  Where difference in floor levels exceeds 1/2 inch (12.7 mm), a ramp must be used for accessibility for people with disabilities; show ramps on Drawings.

1. Bevel edges at 1:2 slope, aligning lower edge of bevel with adjacent floor finish.  Limit height of bevel to 1/2 inch (12.7 mm) or less, and finish bevel to match face of threshold.

B. Granite Thresholds:  ASTM C 615, with [polished] [honed] finish.

Select one of three subparagraphs and associated subparagraph below.

1. Description:  Uniform, [fine] [medium]-grained, [white] [gray] [black] stone without veining.

2. Description:  Match Architect's sample.

3. Description:  Provide[ one of] the following:

a. <Insert, in separate subparagraphs, name of variety and producer, distributor, or importer.>

C. Marble Thresholds:  ASTM C 503 with a minimum abrasion resistance of [10] [12] per ASTM C 1353 or ASTM C 241 and with honed finish.

Select one of three subparagraphs and associated subparagraph below.

1. Description:  Uniform, fine- to medium-grained white stone with gray veining.

2. Description:  Match Architect's sample.

3. Description:  Provide[ one of] the following:

a. <Insert, in separate subparagraphs, name of variety and producer, distributor, or importer.>

D. Slate Thresholds:  ASTM C 629, Classification [I Exterior] [II Interior], with fine, even grain and honed finish.

Select one of three subparagraphs and associated subparagraph below.

1. Description:  Uniform, [black] [blue-black] [gray] [blue-gray] [green] <Insert color> stone[ and unfading].

2. Description:  Match Architect's sample.

3. Description:  Provide[ one of] the following:

a. <Insert, in separate subparagraphs, name of variety and producer, distributor, or importer.>

E. Solid Polymer Thresholds:  Made from homogeneous solid sheets of filled plastic resin complying with material and performance requirements in ANSI Z124.3, for Type 5 or Type 6, without precoated finish.

Coordinate below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Avonite, Inc.

b. DuPont Polymers.

c. Formica Corporation.

d. Nevamar; International Paper; Decorative Products Division.

e. Swan Corporation (The).

f. Wilsonart International; Div. of Premark International, Inc.

g. <Insert manufacturer's name.>

2.5 [WATERPROOFING] [AND] [CRACK-SUPPRESSION MEMBRANES] FOR THIN-SET TILE INSTALLATIONS

If both waterproofing and crack-suppression membranes are required and different products are used for each, copy and re-edit this Article for each application.  If this Article is used to specify waterproofing for portland cement mortar (thickset) tile installations, revise Article title.

Generally retain paragraph below for waterproofing and possibly for crack-suppression membranes.  ANSI A118.10 includes requirements that are also appropriate for crack-suppression membranes.  See Evaluations.

A. General:  Manufacturer's standard product that complies with ANSI A118.10[, selected from the following].

Products below are available for use as either waterproofing or crack-suppression membranes.  Refer to manufacturers' literature for limitations on use.  Other products are available for use as crack-suppression membranes that do not comply with ANSI A118.10.

B. Chlorinated-Polyethylene-Sheet Product:  Nonplasticized, chlorinated polyethylene faced on both sides with high-strength, nonwoven polyester fabric, for adhering to latex-portland cement mortar; 60 inches (1524 mm) wide by 0.030-inch (0.76-mm) nominal thickness.

Coordinate subparagraph below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Product:  Noble Company (The); Nobleseal TS.

C. PVC-Sheet Product:  Two layers of PVC sheet heat-fused together and to facings of bondable nonwoven polyester, for adhering to latex-portland cement mortar; 60 inches (1524 mm) wide by 0.040-inch (1.01-mm) nominal thickness.

Coordinate subparagraph below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Product:  Compotite Corporation; Composeal Gold.

D. Polyethylene-Sheet Product:  Polyethylene faced on both sides with fleece webbing for adhering to latex-portland cement mortar; 39 inches (1000 mm) wide by 0.008-inch (0.203-mm) nominal thickness.

Coordinate subparagraph below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Product:  Schluter Systems L.P.; KERDI.

E. Corrugated-Polyethylene Product:  Corrugated polyethylene with dovetail-shaped corrugations for adhering to latex-portland cement mortar and with anchoring webbing on the underside; 39 inches (1000 mm) wide by 3/16-inch (4-mm) nominal thickness.

Coordinate subparagraph below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Product:  Schluter Systems L.P.; DITRA.

F. Fabric-Reinforced, Modified-Bituminous-Sheet Product:  Self-adhering SBS-modified-bituminous sheet with woven reinforcement facing for adhering to latex-portland cement mortar; 36 inches (914 mm) wide by 0.040-inch (1.01-mm) nominal thickness.

Coordinate subparagraph below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Product:  National Applied Construction Products, Inc.; Strataflex.

G. Fabric-Reinforced, Fluid-Applied Product:  System consisting of liquid-latex rubber and fabric reinforcement.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Custom Building Products; Trowel & Seal Waterproofing and Anti-Fracture Membrane.

b. LATICRETE International Inc.; Laticrete 9235 Waterproof Membrane.

c. MAPEI Corporation; PRP M19.

d. Summitville Tiles, Inc.; S-9000.

e. <Insert manufacturer's name; product.>

H. Unreinforced, Fluid-Applied Product:  Liquid-latex rubber in a consistency suitable for trowel application and intended for use as waterproofing.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Boiardi Products Corporation; Elastiment [324] [644].

b. Custom Building Products; LevelQuick Waterproofing and Anti-Fracture Membrane.

c. Jamo Inc.; Waterproof.

d. <Insert manufacturer's name; product.>

I. Latex-Portland Cement Product:  Flexible mortar consisting of cement-based mix and acrylic-latex additive.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Boiardi Products Corporation; Elastiment 323.

b. MAPEI Corporation; PRP 315.

c. Southern Grouts & Mortars, Inc.; Southcrete 1100.

d. TEC Specialty Products Inc.; TA-324, Triple Flex.

e. <Insert manufacturer's name; product.>

Retain option in paragraph below if low-emitting materials are required for LEED-NC and LEED-CI Credit EQ 4.1.  VOC limit is that for ceramic tile adhesives.  If retaining option, verify that manufacturers' products selected can comply with VOC limit.

J. Urethane Waterproofing and Tile-Setting Adhesive:  One-part liquid-applied urethane[, with a VOC content of 65 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24),] in a consistency suitable for trowel application and intended for use as both waterproofing and tile-setting adhesive in a two-step process.

Coordinate below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Bostik; Hydroment Ultra-Set.

b. Southern Grouts & Mortars, Inc.; Deck-Seal 1000.

c. <Insert manufacturer's name; product.>

2.6 SETTING AND GROUTING MATERIALS

Coordinate paragraph and subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.  If retaining, delete those manufacturers that do not offer setting materials specified in this Article.  See tables in the Evaluations for a list of manufacturers according to product types.

A. [Available ]Manufacturers:

1. Atlas Minerals & Chemicals, Inc.

2. Boiardi Products Corporation.

3. Bonsal, W. R., Company.

4. Bostik.

5. C-Cure.

6. Custom Building Products.

7. DAP, Inc.

8. Jamo Inc.

9. LATICRETE International Inc.

10. MAPEI Corporation.

11. Southern Grouts & Mortars, Inc.

12. Summitville Tiles, Inc.

13. TEC Specialty Products Inc.

14. <Insert manufacturer's name.>

Retain setting and grouting materials below as required for installation methods selected; delete others.  For proprietary products, coordinate with list of manufacturers.

B. Portland Cement Mortar (Thickset) Installation Materials:  ANSI A108.1A and as specified below:

1. Cleavage Membrane:  Asphalt felt, ASTM D 226, Type I (No. 15); or polyethylene sheeting, ASTM D 4397, 4.0 mils (0.1 mm) thick.

Retain subparagraph below for reinforcing mortar bed.

2. Reinforcing Wire Fabric:  Galvanized, welded wire fabric, 2 by 2 inches (50.8 by 50.8 mm) by 0.062-inch (1.57-mm) diameter; comply with ASTM A 185 and ASTM A 82 except for minimum wire size.

Retain subparagraph and associated subparagraphs below for portland cement plaster scratch coat.  Delete if scratch coat is specified in Division 09 Section "Portland Cement Plastering."

3. Expanded Metal Lath:  Diamond-mesh lath complying with ASTM C 847.

a. Base Metal and Finish for Interior Applications:  Uncoated or zinc-coated (galvanized) steel sheet, with uncoated steel sheet painted after fabrication into lath.

Delete subparagraph above or first subparagraph below if not applicable.

b. Base Metal and Finish for Exterior Applications:  Zinc-coated (galvanized) steel sheet.

c. Configuration over Studs and Furring:  Flat.

Delete subparagraph above or first subparagraph below if not applicable.

d. Configuration over Solid Surfaces:  Self-furring.

e. Weight:  [2.5 lb/sq. yd. (1.4 kg/sq. m)] [3.4 lb/sq. yd. (1.8 kg/sq. m)].

Retain subparagraph below if latex additive is required to improve flexibility and other properties of mortar setting bed.

4. Latex Additive:  [Manufacturer's standard] [acrylic resin] [or] [styrene-butadiene-rubber] water emulsion, serving as replacement for part or all of gaging water, of type specifically recommended by latex-additive manufacturer for use with field-mixed portland cement and aggregate mortar bed.

C. Dry-Set Portland Cement Mortar (Thin Set):  ANSI A118.1.

See Evaluations for difference between normal and nonsagging mortar.

1. For wall applications, provide nonsagging mortar that complies with Paragraph C-4.6.1 in addition to the other requirements in ANSI A118.1.

Some manufacturers produce medium-bed, dry-set mortars.  Insert here if required, with wording similar to that used below for medium-bed, latex-portland cement mortar.

D. Latex-Portland Cement Mortar (Thin Set):  ANSI A118.4, consisting of the following:

Retain either subparagraph below.

1. Prepackaged dry-mortar mix containing dry, redispersible, ethylene vinyl acetate additive to which only water must be added at Project site.

2. Prepackaged dry-mortar mix combined with [acrylic resin] [or] [styrene-butadiene-rubber] liquid-latex additive.

Retain below with either subparagraph above.  See Evaluations for difference between normal and nonsagging mortar.

a. For wall applications, provide nonsagging mortar that complies with Paragraph F-4.6.1 in addition to the other requirements in ANSI A118.4.

ANSI A118.4 does not recognize medium-bed mortars.

E. Medium-Bed, Latex-Portland Cement Mortar:  Provide materials composed as follows, with physical properties equaling or exceeding those required for thin-set mortars based on testing of medium-bed specimens according to ANSI A118.4:

Retain either subparagraph below.

1. Prepackaged dry-mortar mix containing dry, redispersible, ethylene vinyl acetate additive to which only water must be added at Project site.

2. Prepackaged dry-mortar mix combined with [acrylic resin] [or] [styrene-butadiene-rubber] liquid-latex additive.

Retain option in paragraph below if low-emitting materials are required for LEED-NC and LEED-CI Credit EQ 4.1.  VOC limit is that for ceramic tile adhesives.

F. Chemical-Resistant, Water-Cleanable, Tile-Setting and -Grouting Epoxy:  ANSI A118.3[, with a VOC content of 65 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24)].

Subparagraph below is an example only.  Some products claim resistance of up to 350 deg F (176 deg C).  Revise subparagraph to suit products and performance required.  See Evaluations.

1. Provide product capable of withstanding continuous and intermittent exposure to temperatures of up to 140 deg F (60 deg C) and 212 deg F (100 deg C), respectively, and certified by manufacturer for intended use.

Insert chemical-resistant performance criteria for above if required.  See ANSI A118.3 and ASTM C 267.  Latter is test method for determining chemical resistance of mortars and grouts.

Retain option in paragraph below if low-emitting materials are required for LEED-NC and LEED-CI Credit EQ 4.1.  VOC limit is that for ceramic tile adhesives.

G. Water-Cleanable, Tile-Setting Epoxy Adhesive:  ANSI A118.3[, with a VOC content of 65 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24)].

Revise paragraph below if silica or other fillers are required and insert chemical-resistant performance criteria as needed.

H. Chemical-Resistant Furan Mortar:  ANSI A118.5, with carbon filler, unless otherwise indicated.

Type II organic adhesive is also available but is suitable only for interior ceilings and walls subject to dry, light service or limited water exposure.

Retain option in paragraph below if low-emitting materials are required for LEED-NC and LEED-CI Credit EQ 4.1.  VOC limit is that for ceramic tile adhesives.

I. Organic Adhesive:  ANSI A136.1, Type I[, with a VOC content of 65 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24)].

Retain types of grout required from seven paragraphs below.  Retain sanded grout for tile installed with joint widths 1/8 inch (3.2 mm) or wider and unsanded grout for tile installed with joint widths 1/8 inch (3.2 mm) or narrower.  Coordinate with module sizes specified in Part 2 and with grout types specified in Part 3 "Floor Tile Installation" and "Wall Tile Installation" articles.

J. Sand-Portland Cement Grout:  ANSI A108.10, composed of white or gray cement and white or colored aggregate as required to produce color indicated.

Delete paragraph above if only prepackaged products are acceptable.  Grout above is field-mixed portland cement and fine-graded sand that is not included in ANSI A118.6 but whose materials are covered in ANSI A108.10.  Retain one or more of first three paragraphs below if only prepackaged products are allowed or if unsanded grout is required.

K. Standard Sanded Cement Grout:  ANSI A118.6, color as indicated.

L. Standard Unsanded Cement Grout:  ANSI A118.6, color as indicated.

M. Polymer-Modified Tile Grout:  ANSI A118.7, color as indicated.

Retain one of three subparagraphs below with last paragraph above.

1. Polymer Type:  Ethylene vinyl acetate, in dry, redispersible form, prepackaged with other dry ingredients.

2. Polymer Type:  [Acrylic resin] [or] [styrene-butadiene rubber] in liquid-latex form for addition to prepackaged dry-grout mix.

3. Polymer Type:  Either ethylene vinyl acetate, in dry, redispersible form, prepackaged with other dry ingredients, or acrylic resin or styrene-butadiene rubber in liquid-latex form for addition to prepackaged dry-grout mix.

Retain one or both subparagraphs below with any of three subparagraphs above.

a. Unsanded grout mixture for joints 1/8 inch (3.2 mm) and narrower.

b. Sanded grout mixture for joints 1/8 inch (3.2 mm) and wider.

N. Chemical-Resistant Furan Grout:  ANSI A118.5.

Insert chemical-resistant performance criteria for above if required.  If both chemical-resistant mortar and grout are specified, reference mortar requirements.

Delete below if no pregrouted tile.

O. Grout for Pregrouted Tile Sheets:  Same silicone rubber used in factory to pregrout tile sheets.

2.7 ELASTOMERIC SEALANTS

Delete this Article if sealant work is specified in Division 07 Section "Joint Sealants."

A. General:  Provide manufacturer's standard chemically curing, elastomeric sealants of base polymer and characteristics indicated that comply with applicable requirements in Division 07 Section "Joint Sealants."

Retain subparagraph below if low-emitting materials are required for LEED-NC and LEED-CI Credit EQ 4.1.  VOC limit is that for architectural sealants.  If retaining below, verify that manufacturers' products selected can comply with VOC limit before retaining them.

1. Use sealants that have a VOC content of [250] <Insert limit> g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Revise paragraph below if color matching is not possible with sealant products selected, which may be the case with mildew-resistant sealant from some manufacturers.

B. Colors:  Provide colors of exposed sealants to match colors of grout in tile adjoining sealed joints, unless otherwise indicated.

Silicone sealant in paragraph below is suitable for joints in nontraffic surfaces only.

C. One-Part, Mildew-Resistant Silicone Sealant:  ASTM C 920; Type S; Grade NS; Class 25; Uses NT, G, A, and, as applicable to nonporous joint substrates indicated, O; formulated with fungicide, intended for sealing interior ceramic tile joints and other nonporous substrates that are subject to in-service exposures of high humidity and extreme temperatures.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Dow Corning Corporation; Dow Corning 786.

b. GE Silicones; Sanitary 1700.

c. Pecora Corporation; Pecora 898 Sanitary Silicone Sealant.

d. Tremco, Inc.; Tremsil 600 White.

e. <Insert manufacturer's name; product.>

D. Multipart, Pourable Urethane Sealant for Use T:  ASTM C 920; Type M; Grade P; Class 25; Uses T, M, A, and, as applicable to joint substrates indicated, O.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Bostik; Chem-Calk 550.

b. Mameco International, Inc.; Vulkem 245.

c. Pecora Corporation; NR-200 Urexpan.

d. Tremco, Inc.; THC-900.

e. <Insert manufacturer's name; product.>

E. Chemical-Resistant Sealants:  For chemical-resistant floors, provide chemical-resistant elastomeric sealant of type recommended and produced by chemical-resistant mortar and grout manufacturer for type of application indicated, with proven service record and compatibility with tile and other setting materials, and with chemical resistance equivalent to mortar/grout.  Include primer and backer rod recommended by manufacturer.

Insert other sealant products, including chemical-resistant sealants, as required.  See Division 07 Section "Joint Sealants."

2.8 CEMENTITIOUS BACKER UNITS

Delete this Article if no cementitious backer units or if they are specified in Division 09 Section "Gypsum Veneer Plastering" or "Gypsum Board."

A. Provide cementitious backer units complying with ANSI A118.9 in maximum lengths available to minimize end-to-end butt joints.

Coordinate thickness below with products selected.  1/4-inch (6.4-mm) thickness is available from C-Cure and Custom Building Products.  1/2-inch (12.7-mm) thickness is available from all manufacturers listed.  5/8-inch (15.9-mm) thickness is available from USG Corporation.

1. Thickness:  [1/4 inch (6.4 mm)] [1/2 inch (12.7 mm)] [Manufacturer's standard thickness, but not less than 1/4 inch (6.4 mm)] [5/8 inch (15.9 mm)] [As indicated].

Coordinate width in either subparagraph below with products selected or delete width requirement for Contractor's option.

2. Width:  [32 inches (813 mm)] [36 inches (915 mm)] [48 inches (1219 mm)] [Manufacturer's standard width, but not less than 32 inches (813 mm)].

Select subparagraph above for IP products with equivalent metric dimensions or subparagraph below for products manufactured to metric sizes.

3. Width:  [800 mm] [900 mm] [1200 mm] [Manufacturer's standard width, but not less than 800 mm].

Coordinate below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

B. [Available ]Products:

1. C-Cure; C-Cure Board 990.

2. Custom Building Products; Wonderboard.

3. FinPan, Inc.; Util-A-Crete Concrete Backer Board.

4. USG Corporation; DUROCK Cement Board.

5. <Insert manufacturer's name; product.>

2.9 MISCELLANEOUS MATERIALS

Delete this Article if no miscellaneous materials.  Revise paragraph below if plastic or brass strips are required.

Delete below if no concrete substrates.

A. Trowelable Underlayments and Patching Compounds:  Latex-modified, portland cement-based formulation provided or approved by manufacturer of tile-setting materials for installations indicated.

Retain paragraph below if metal edge strips are required at junction with other floor finishes; revise if metal-edge control joints are required.

B. Metal Edge Strips:  Angle or L-shape, height to match tile and setting-bed thickness, metallic or combination of metal and PVC or neoprene base, designed specifically for flooring applications, [half-hard brass] [white zinc alloy] [nickel silver] [stainless steel; ASTM A 666, 300 Series] exposed-edge material.

Delete first paragraph and subparagraphs below if no tile with temporary protective coating.

C. Temporary Protective Coating:  [Either product] [Product] indicated below that is formulated to protect exposed surfaces of tile against adherence of mortar and grout; compatible with tile, mortar, and grout products; and easily removable after grouting is completed without damaging grout or tile.

1. Petroleum paraffin wax, fully refined and odorless, containing at least 0.5 percent oil with a melting point of 120 to 140 deg F (49 to 60 deg C) per ASTM D 87.

Retain subparagraph above for either factory or field application; retain subparagraph below if acceptable for field application in lieu of wax.  See Editing Instruction No. 4 in the Evaluations.

2. Grout release in form of manufacturer's standard proprietary liquid coating that is specially formulated and recommended for use as temporary protective coating for tile.

D. Tile Cleaner:  A neutral cleaner capable of removing soil and residue without harming tile and grout surfaces, specifically approved for materials and installations indicated by tile and grout manufacturers.

E. Grout Sealer:  Manufacturer's standard[ silicone] product for sealing grout joints that does not change color or appearance of grout.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Bonsal, W. R., Company; Grout Sealer.

b. Bostik; CeramaSeal Grout Sealer.

c. C-Cure; Penetrating Sealer 978.

d. Custom Building Products; [Surfaceguard] [Grout and Tile] [Grout] Sealer.

e. Jamo Inc.; [Matte Finish] [Penetrating] Sealer.

f. MAPEI Corporation; KER [003, Silicone Spray Sealer for Cementitious Tile Grout] [004, Keraseal Penetrating Sealer for Unglazed Grout and Tile].

g. Southern Grouts & Mortars, Inc.; Silicone Grout Sealer.

h. Summitville Tiles, Inc.; SL-15, Invisible Seal Penetrating Grout and Tile Sealer.

i. TEC Specialty Products Inc.; [TA-256 Penetrating Silicone] [TA-257 Silicone] Grout Sealer.

2.10 MIXING MORTARS AND GROUT

A. Mix mortars and grouts to comply with referenced standards and mortar and grout manufacturers' written instructions.

B. Add materials, water, and additives in accurate proportions.

C. Obtain and use type of mixing equipment, mixer speeds, mixing containers, mixing time, and other procedures to produce mortars and grouts of uniform quality with optimum performance characteristics for installations indicated.

PART 3 -  EXECUTION

3.1 EXAMINATION

Coordinate substrate tolerances, finish, and curing methods specified in Division 03 Section "Cast-in-Place Concrete" with requirements in ANSI A108 Series of tile installation standards.

A. Examine substrates, areas, and conditions where tile will be installed, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of installed tile.

1. Verify that substrates for setting tile are firm; dry; clean; free of oil, waxy films, and curing compounds; and within flatness tolerances required by referenced ANSI A108 Series of tile installation standards for installations indicated.

2. Verify that installation of grounds, anchors, recessed frames, electrical and mechanical units of work, and similar items located in or behind tile has been completed before installing tile.

3. Verify that joints and cracks in tile substrates are coordinated with tile joint locations; if not coordinated, adjust joint locations in consultation with Architect.

B. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. Remove coatings, including curing compounds and other substances that contain soap, wax, oil, or silicone, that are incompatible with tile-setting materials.

B. Provide concrete substrates for tile floors installed with [adhesives] [or] [thin-set mortar] that comply with flatness tolerances specified in referenced ANSI A108 Series of tile installation standards.

1. Fill cracks, holes, and depressions with trowelable leveling and patching compound according to tile-setting material manufacturer's written instructions.  Use product specifically recommended by tile-setting material manufacturer.

2. Remove protrusions, bumps, and ridges by sanding or grinding.

C. Blending:  For tile exhibiting color variations within ranges selected during Sample submittals, verify that tile has been factory blended and packaged so tile units taken from one package show same range of colors as those taken from other packages and match approved Samples.  If not factory blended, either return to manufacturer or blend tiles at Project site before installing.

Delete below if not required or if factory application is exclusively specified in Part 2.  If required for quarry, paver, or other tile set with furan or other grout, retain paragraph and applicable subparagraph for temporary protective coating in Part 2 "Miscellaneous Materials" Article.  See Editing Instruction No. 4 in the Evaluations.

D. Field-Applied Temporary Protective Coating:  Where indicated under tile type or needed to prevent grout from staining or adhering to exposed tile surfaces, precoat them with continuous film of temporary protective coating, taking care not to coat unexposed tile surfaces.

3.3 INSTALLATION, GENERAL

A. ANSI Tile Installation Standards:  Comply with parts of ANSI A108 Series "Specifications for Installation of Ceramic Tile" that apply to types of setting and grouting materials and to methods indicated in ceramic tile installation schedules.

B. TCA Installation Guidelines:  TCA's "Handbook for Ceramic Tile Installation." Comply with TCA installation methods indicated in ceramic tile installation schedules.

C. Extend tile work into recesses and under or behind equipment and fixtures to form complete covering without interruptions, unless otherwise indicated.  Terminate work neatly at obstructions, edges, and corners without disrupting pattern or joint alignments.

D. Accurately form intersections and returns.  Perform cutting and drilling of tile without marring visible surfaces.  Carefully grind cut edges of tile abutting trim, finish, or built-in items for straight aligned joints.  Fit tile closely to electrical outlets, piping, fixtures, and other penetrations so plates, collars, or covers overlap tile.

E. Jointing Pattern:  Lay tile in grid pattern, unless otherwise indicated.  Align joints when adjoining tiles on floor, base, walls, and trim are same size.  Lay out tile work and center tile fields in both directions in each space or on each wall area.  Adjust to minimize tile cutting.  Provide uniform joint widths, unless otherwise indicated.

Delete subparagraph below if no mounted tile.

1. For tile mounted in sheets, make joints between tile sheets same width as joints within tile sheets so joints between sheets are not apparent in finished work.

Delete paragraph below if no wainscots.  Verify that instruction agrees with detailing.

F. Lay out tile wainscots to next full tile beyond dimensions indicated.

Refer to TCA's "Handbook for Ceramic Tile Installation" and to ANSI A108 Series of tile installation standards for data on expansion joints.  Both require joint locations to be indicated on Drawings.  There is no substitute for showing all joints on Drawings.

G. Expansion Joints:  Locate expansion joints and other sealant-filled joints, including control, contraction, and isolation joints, where indicated during installation of setting materials, mortar beds, and tile.  Do not saw-cut joints after installing tiles.

1. Locate joints in tile surfaces directly above joints in concrete substrates.

Delete subparagraph below if joint sealants are specified in referenced Division 07 Section.

2. Prepare joints and apply sealants to comply with requirements in Division 07 Section "Joint Sealants."

H. Grout tile to comply with requirements of the following tile installation standards:

Delete grout applications below if not referenced under specific installation methods in tile installation schedules.

1. For ceramic tile grouts (sand-portland cement; dry-set, commercial portland cement; and latex-portland cement grouts), comply with ANSI A108.10.

2. For chemical-resistant epoxy grouts, comply with ANSI A108.6.

3. For chemical-resistant furan grouts, comply with ANSI A108.8.

Delete below if not applicable or if cementitious backer units are specified in Division 09 Section "Gypsum Veneer Plastering" or "Gypsum Board."

I. At showers, tubs, and where indicated, install cementitious backer units and treat joints to comply with ANSI A108.11 and manufacturer's written instructions for type of application indicated.

3.4 [WATERPROOFING] [AND] [CRACK-SUPPRESSION MEMBRANE] INSTALLATION

Delete this Article if no waterproofing is required.

A. Install waterproofing to comply with ANSI A108.13 and waterproofing manufacturer's written instructions to produce waterproof membrane of uniform thickness bonded securely to substrate.

B. Install crack-suppression membrane to comply with manufacturer's written instructions to produce membrane of uniform thickness bonded securely to substrate.

C. Do not install tile over waterproofing until waterproofing has cured and been tested to determine that it is watertight.

3.5 FLOOR TILE INSTALLATION

A. General:  Install tile to comply with requirements in the Floor Tile Installation Schedule, including those referencing TCA installation methods and ANSI A108 Series of tile installation standards.

Delete subparagraph and associated subparagraphs below if tile types and sizes and Project conditions do not warrant specifying 95 percent coverage or if mortar installation is not specified.

1. For installations indicated below, follow procedures in ANSI A108 Series tile installation standards for providing 95 percent mortar coverage.

Listed locations below are examples only; edit to suit Project.

a. Exterior tile floors.

b. Tile floors in wet areas.

c. Tile swimming pool decks.

d. Tile floors in laundries.

e. Tile floors composed of tiles 8 by 8 inches (200 by 200 mm) or larger.

f. Tile floors composed of rib-backed tiles.

B. Joint Widths:  Install tile on floors with the following joint widths:

Tile measurements below are examples only and are based on widths recommended by American Olean for its products.  Retain one width for each tile type or revise, but only after verifying widths with tile manufacturers for products selected.  Coordinate widths with grout selections and with module sizes and facial dimensions specified for tile types in Part 2.

1. Ceramic Mosaic Tile:  1/16 inch (1.6 mm).

2. Quarry Tile:  [1/4 inch (6.35 mm)] [3/8 inch (9.5 mm)].

3. Paver Tile:  [1/4 inch (6.35 mm)] [3/8 inch (9.5 mm)].

C. Stone Thresholds:  Install stone thresholds at locations indicated; set in same type of setting bed as abutting field tile, unless otherwise indicated.

Delete subparagraph below if not applicable.

1. Set thresholds in latex-portland cement mortar for locations where mortar bed would otherwise be exposed above adjacent nontile floor finish.

D. Metal Edge Strips:  Install at locations indicated or where exposed edge of tile flooring meets carpet, wood, or other flooring that finishes flush with top of tile.

Delete below if grout sealer is not used.  Delete option if no epoxy or furan grouts are used.

E. Grout Sealer:  Apply grout sealer to[ cementitious] grout joints according to grout-sealer manufacturer's written instructions.  As soon as grout sealer has penetrated grout joints, remove excess sealer and sealer that has gotten on tile faces by wiping with soft cloth.

3.6 WALL TILE INSTALLATION

If ceiling installations are also required, either revise this Article title to read "Wall and Ceiling Tile Installations" or create a separate Article.  If former is done, revise references to wall installations in paragraphs below to also incorporate ceilings.

A. Install types of tile designated for wall installations to comply with requirements in the Wall Tile Installation Schedule, including those referencing TCA installation methods and ANSI setting-bed standards.

Delete first paragraph below if portland cement scratch coat and lath are specified in Division 09 Section "Portland Cement Plastering."

B. Install metal lath and scratch coat for walls to comply with ANSI A108.1A, Section 4.1.

C. Joint Widths:  Install tile on walls with the following joint widths:

Tile measurements below are examples only and are based on widths recommended by American Olean for its products.  Retain one width for each tile type or revise, but only after verifying widths with tile manufacturers for products selected.  Coordinate widths with grout selections and with module sizes for ceramic mosaic tile and glazed wall tile specified in Part 2 "Tile Products" Article.

1. Ceramic Mosaic Tile:  1/16 inch (1.6 mm).

2. Glazed Wall Tile:  1/16 inch (1.6 mm).

3. Quarry Tile:  [1/4 inch (6.35 mm)] [3/8 inch (9.5 mm)].

3.7 CLEANING AND PROTECTING

A. Cleaning:  On completion of placement and grouting, clean all ceramic tile surfaces so they are free of foreign matter.

1. Remove [epoxy] [and] [latex-portland cement] grout residue from tile as soon as possible.

2. Clean grout smears and haze from tile according to tile and grout manufacturer's written instructions, but no sooner than 10 days after installation.  Use only cleaners recommended by tile and grout manufacturers and only after determining that cleaners are safe to use by testing on samples of tile and other surfaces to be cleaned.  Protect metal surfaces and plumbing fixtures from effects of cleaning.  Flush surfaces with clean water before and after cleaning.

Delete subparagraph below if not applicable.

3. Remove temporary protective coating by method recommended by coating manufacturer that is acceptable to tile and grout manufacturer.  Trap and remove coating to prevent it from clogging drains.

B. When recommended by tile manufacturer, apply coat of neutral protective cleaner to completed tile walls and floors.  Protect installed tile work with kraft paper or other heavy covering during construction period to prevent staining, damage, and wear.

C. Prohibit foot and wheel traffic from tiled floors for at least seven days after grouting is completed.

D. Before final inspection, remove protective coverings and rinse neutral cleaner from tile surfaces.

See Editing Instruction No. 8 in the Evaluations for suggested ways of editing tile installation schedules below.  It is advisable to have a copy of TCA's "Handbook for Ceramic Tile Installation" at hand while editing schedules below.

3.8 FLOOR TILE INSTALLATION SCHEDULE

Insert number to complete installation designations below.  Use these designations on Drawings to show where tile is required.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

A. Tile Installation [FTI-<#>]:  Exterior floor installation on concrete; cement mortar bed (thickset) bonded to concrete; TCA F101 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

B. Tile Installation [FTI-<#>]:  Exterior floor installation on concrete; thin-set mortar; TCA F102 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

C. Tile Installation [FTI-<#>]:  Interior floor installation on concrete; cement mortar bed (thickset) with cleavage membrane; TCA F111 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

D. Tile Installation [FTI-<#>]:  Interior floor installation on concrete; cement mortar bed (thickset) bonded to concrete; TCA F112 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

E. Tile Installation [FTI-<#>]:  Interior floor installation on concrete; thin-set mortar; TCA F113 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

F. Tile Installation [FTI-<#>]:  Interior floor installation on concrete; cement mortar bed (thickset) with cleavage membrane, [epoxy] [furan] grout; TCA F114 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  Chemical-resistant[, water-cleanable, tile-setting and -grouting epoxy] [furan grout].

G. Tile Installation [FTI-<#>]:  Interior floor installation on concrete; thin-set mortar, [epoxy] [furan] grout; TCA F115 and ANSI A108.5.

1. Tile Type:  [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  Chemical-resistant[, water-cleanable, tile-setting and -grouting epoxy] [furan grout].

H. Tile Installation [FTI-<#>]:  Interior floor installation on concrete; [organic] [water-cleanable epoxy] adhesive; TCA F116 and ANSI A108.4.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

I. Tile Installation [FTI-<#>]:  Interior floor installation on [waterproof] [crack-suppression] membrane over [concrete] [and] [wood]; cement mortar bed (thickset); TCA F121 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

J. Tile Installation [FTI-<#>]:  Interior floor installation on [waterproof] [crack-suppression] membrane over concrete; thin-set mortar; TCA F122 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Thin-Set Mortar:  Latex-portland cement mortar.

3. Grout:  Polymer-modified [sanded] [unsanded] grout.

K. Tile Installation [FTI-<#>]:  Chemical-resistant interior floor installation on concrete; chemical-resistant, water-cleanable, tile-setting and -grouting epoxy; epoxy grout; TCA F131 and ANSI A108.6.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Grout:  Chemical-resistant, water-cleanable, tile-setting and -grouting epoxy.

L. Tile Installation [FTI-<#>]:  Chemical-resistant interior floor installation on concrete; chemical-resistant, water-cleanable, tile-setting and -grouting epoxy on cured cement mortar bed [bonded to concrete subfloor] [installed over cleavage membrane]; epoxy grout; TCA F132 and ANSI A108.6.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Grout:  Chemical-resistant, water-cleanable, tile-setting and -grouting epoxy.

M. Tile Installation [FTI-<#>]:  Chemical-resistant interior floor installation on concrete; chemical-resistant resin mortar; furan grout.  TCA F133 and ANSI A108.5.

1. Tile Type:  [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Resin Mortar:  Chemical-resistant, water-cleanable, tile-setting and -grouting epoxy.

3. Grout:  Chemical-resistant furan grout.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

N. Tile Installation [FTI-<#>]:  Interior floor installation on wood; cement mortar bed (thickset) with cleavage membrane; TCA F141 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

O. Tile Installation [FTI-<#>]:  Interior floor installation on wood; organic adhesive; TCA F142 and ANSI A108.4.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Grout:  [Polymer-modified sanded grout] [Polymer-modified unsanded grout] [Chemical-resistant, water-cleanable, tile-setting and -grouting epoxy].

P. Tile Installation [FTI-<#>]:  Interior floor installation on wood; chemical-resistant, water-cleanable tile-setting and -grouting epoxy; TCA F143 and ANSI A108.6.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Grout:  Chemical-resistant, water-cleanable, tile-setting and -grouting epoxy.

Q. Tile Installation [FTI-<#>]:  Interior floor installation on cementitious backer units over wood; thin-set mortar; TCA F144 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Unglazed quarry] [Glazed quarry] [Unglazed paver] [Glazed paver] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

3.9 WALL TILE INSTALLATION SCHEDULE

Insert number to complete installation designations below.  Use these designations on Drawings to show where tile is required.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

A. Tile Installation [WTI-<#>]:  [Exterior] [or] [interior] wall installation over masonry or concrete; cement mortar bed (thickset); TCA W201 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A and ANSI A108.1C; if retaining either standard, select one mortar type or delete subparagraph if unmodified portland cement is acceptable.  Also delete if ANSI A108.1B is selected.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

3. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

4. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

B. Tile Installation [WTI-<#>]:  [Exterior] [or] [interior] wall installation over sound, dimensionally stable masonry or concrete; thin-set mortar; TCA W202 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

C. Tile Installation [WTI-<#>]:  Interior wall installation over clean, sound, dimensionally stable masonry or concrete; cement mortar bed (thickset) bonded to substrate; TCA W211 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A and ANSI A108.1C; if retaining either standard, select one mortar type or delete subparagraph if unmodified portland cement is acceptable.  Also delete if ANSI A108.1B is selected.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

3. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

4. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

D. Tile Installation [WTI-<#>]:  Interior wall installation over solid backing and solid anchorage for metal lath; cement mortar bed (thickset); TCA W221 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A and ANSI A108.1C; if retaining either standard, select one mortar type or delete subparagraph if unmodified portland cement is acceptable.  Also delete if ANSI A108.1B is selected.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

3. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

4. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

E. Tile Installation [WTI-<#>]:  Interior wall installation over solid backing and solid anchorage for metal lath; one-coat cement mortar bed (thickset); TCA W222 and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A and ANSI A108.1C; if retaining either standard, select one mortar type or delete subparagraph if unmodified portland cement is acceptable.  Also delete if ANSI A108.1B is selected.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above.  Delete if ANSI A108.1A is selected.

3. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

4. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

F. Tile Installation [WTI-<#>]:  Interior wall installation over solid backing, organic adhesive; TCA W223 and ANSI A108.4.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

G. Tile Installation [WTI-<#>]:  Interior wall installation over wood studs or furring; cement mortar bed (thickset); TCA W231 and ANSI A108.1A.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A; either select one mortar type or delete subparagraph if unmodified portland cement is acceptable.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

H. Tile Installation [WTI-<#>]:  Interior wall installation over metal studs; cement mortar bed (thickset); TCA W241 and ANSI A108.1B.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

I. Tile Installation [WTI-<#>]:  Interior wall installation over gypsum board on metal studs; organic adhesive; TCA W242 and ANSI A108.4.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Grout:  Polymer-modified [sanded] [unsanded] grout.

J. Tile Installation [WTI-<#>]:  Interior wall installation over gypsum board; thin-set mortar; TCA W243 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

K. Tile Installation [WTI-<#>]:  Interior wall installation over cementitious backer units; thin-set mortar; TCA W244 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

L. Tile Installation [WTI-<#>]:  Interior wall installation over glass-mat, water-resistant backer board; [thin-set mortar] [organic adhesive]; TCA W245 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Delete first subparagraph below if organic adhesive is used.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

M. Tile Installation [WTI-<#>]:  Interior bathtub wall installation over wood studs; cement mortar bed (thickset); TCA B411 and ANSI A108.1A.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A; either select one mortar type or delete subparagraph if unmodified portland cement is acceptable.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

N. Tile Installation [WTI-<#>]:  Interior bathtub wall installation over metal studs; cement mortar bed (thickset); TCA B411, TCA W241, and ANSI A108.1B.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

O. Tile Installation [WTI-<#>]:  Interior bathtub wall installation over cementitious backer units; thin-set mortar; TCA B412 and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

P. Tile Installation [WTI-<#>]:  Interior bathtub wall installation over water-resistant gypsum board, thin-set mortar; TCA B413, TCA W243, and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

Q. Tile Installation [WTI-<#>]:  Interior bathtub wall installation over glass-mat, water-resistant backer board; [thin-set mortar] [organic adhesive]; TCA B419, TCA W245, and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Delete first subparagraph below if organic adhesive is used.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

If retaining first paragraph below, select one of three ANSI standards.  ANSI A108.1A is wet-set method, ANSI A108.1B is cured-bed method, and ANSI A108.1C allows Contractor choice of using either method.

R. Tile Installation [WTI-<#>]:  Interior wall and shower-receptor installation over solid backing, cement mortar bed (thickset); TCA B414, TCA W221, and [ANSI A108.1A] [ANSI A108.1B] [ANSI A108.1C].

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A and ANSI A108.1C; if retaining either standard, select one mortar type or delete subparagraph if unmodified portland cement is acceptable.  Also delete if ANSI A108.1B is selected.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

Retain one thin-set mortar below if ANSI A108.1B or ANSI A108.1C is selected in paragraph above; delete if ANSI A108.1A is selected.

3. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

4. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

S. Tile Installation [WTI-<#>]:  Interior wall and shower-receptor installation over wood studs; cement mortar bed (thickset); TCA B414, TCA W231, and ANSI A108.1A.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

Subparagraph below is optional with ANSI A108.1A; either select one mortar type or delete subparagraph if unmodified portland cement is acceptable.

2. Bond Coat Mortar for Wet-Set Method:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

T. Tile Installation [WTI-<#>]:  Interior wall and shower-receptor installation over metal studs; cement mortar bed (thickset); TCA B414, TCA W241, and ANSI A108.1B.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

U. Tile Installation [WTI-<#>]:  Interior wall and shower-receptor installation over cementitious backer units; thin-set mortar; TCA B415, TCA W244, and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

V. Tile Installation [WTI-<#>]:  Interior wall and shower-receptor installation over glass-mat, water-resistant backer board; thin-set mortar; TCA B420, TCA W245, and ANSI A108.5.

1. Tile Type:  [Unglazed ceramic mosaic] [Glazed ceramic mosaic] [Glazed wall] tile <Insert tile type designation>.

2. Thin-Set Mortar:  [Dry-set] [Latex-] portland cement mortar.

3. Grout:  [Sand-portland cement] [Standard sanded cement] [Standard unsanded cement] [Polymer-modified sanded] [Polymer-modified unsanded] grout.

Insert other schedules for countertop, renovation, and sound-rated installations.

END OF SECTION 093000

TILING
093000 - 1

