Copyright 2002 and 2005 AIA
MASTERSPEC Full Length
05/02 (R 05/05)

Copyright 2002 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 321373 - CONCRETE PAVING JOINT SEALANTS
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project.

1. Expansion and contraction joints within cement concrete pavement.

2. Joints between cement concrete and asphalt pavement.

B. Related Sections include the following:

List below only construction that the reader might expect to find in this Section but is specified elsewhere.

1. Division 07 Section "Joint Sealants" for sealing nontraffic and traffic joints in locations not specified in this Section.

2. Division 32 Section "Asphalt Paving" for constructing joints between concrete and asphalt pavement.

3. Division 32 Section "Concrete Paving" for constructing joints in concrete pavement.

1.3 SUBMITTALS

A. Product Data:  For each joint-sealant product indicated.

Delete first paragraph below if a color choice is not available for sealant types specified.

B. Samples for Verification:  For each type and color of joint sealant required.  Install joint-sealant samples in 1/2-inch- (13-mm-) wide joints formed between two 6-inch- (150-mm-) long strips of material matching the appearance of exposed surfaces adjacent to joint sealants.

C. Product Certificates:  For each type of joint sealant and accessory, signed by product manufacturer.

Coordinate paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

D. Qualification Data:  For [Installer] [testing agency].

Delete first paragraph and subparagraphs below if testing described is not required elsewhere in this Section.

E. Compatibility and Adhesion Test Reports:  From sealant manufacturer, indicating the following:

1. Materials forming joint substrates and joint-sealant backings have been tested for compatibility and adhesion with joint sealants.

2. Interpretation of test results and written recommendations for primers and substrate preparation needed for adhesion.

F. Product Test Reports:  Based on evaluation of comprehensive tests performed by a qualified testing agency, for sealants.

1.4 QUALITY ASSURANCE

A. Installer Qualifications:  An employer of workers trained and approved by manufacturer.

B. Source Limitations:  Obtain each type of joint sealant through one source from a single manufacturer.

Delete first paragraph and subparagraphs below if no elastomeric pavement joint sealants are specified in Part 2 "Cold-Applied Joint Sealants" Article or if testing is considered unnecessary.

C. Preconstruction Compatibility and Adhesion Testing:  Submit to joint-sealant manufacturers, for testing indicated below, samples of materials that will contact or affect joint sealants.

1. Use [ASTM C 1087] [manufacturer's standard test methods] to determine whether priming and other specific joint preparation techniques are required to obtain rapid, optimum adhesion of joint sealants to joint substrates.

2. Submit not fewer than [eight] <Insert number> pieces of each type of material, including joint substrates, shims, joint-sealant backings, secondary seals, and miscellaneous materials.

3. Schedule sufficient time for testing and analyzing results to prevent delaying the Work.

4. For materials failing tests, obtain joint-sealant manufacturer's written instructions for corrective measures including use of specially formulated primers.

Retain subparagraph below only if sealant installation is not critical.

5. Testing will not be required if joint-sealant manufacturers submit joint preparation data that are based on previous testing of current sealant products for adhesion to, and compatibility with, joint substrates and other materials matching those submitted.

D. Product Testing:  Obtain test results for "Product Test Reports" Paragraph in "Submittals" Article from a qualified testing agency based on testing of current sealant products within a 36-month period preceding the [Notice to Proceed with] [commencement of] the Work.

Retain subparagraph below if Contractor selects testing agency.

1. Testing Agency Qualifications:  An independent testing agency qualified according to ASTM C 1021 for testing indicated, as documented according to ASTM E 548.

1.5 DELIVERY, STORAGE, AND HANDLING

A. Deliver materials to Project site in original unopened containers or bundles with labels indicating manufacturer, product name and designation, color, expiration date, pot life, curing time, and mixing instructions for multicomponent materials.

B. Store and handle materials to comply with manufacturer's written instructions to prevent their deterioration or damage due to moisture, high or low temperatures, contaminants, or other causes.

1.6 PROJECT CONDITIONS

A. Do not proceed with installation of joint sealants under the following conditions:

1. When ambient and substrate temperature conditions are outside limits permitted by joint-sealant manufacturer.

Delete subparagraph above or first subparagraph below.

2. When ambient and substrate temperature conditions are outside limits permitted by joint-sealant manufacturer or are below 40 deg F (4.4 deg C).

3. When joint substrates are wet or covered with frost.

4. Where joint widths are less than those allowed by joint-sealant manufacturer for applications indicated.

5. Where contaminants capable of interfering with adhesion have not yet been removed from joint substrates.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

A. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, products listed in other Part 2 articles.

Retain above for nonproprietary or below for semiproprietary specification.  Refer to Division 01 Section "Product Requirements."  In other Part 2 articles, retain either "Available Products" or "Products" as the title introducing each list of products.

B. Products:  Subject to compliance with requirements, provide one of the products listed in other Part 2 articles.

2.2 MATERIALS, GENERAL

A. Compatibility:  Provide joint sealants, backing materials, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by joint-sealant manufacturer based on testing and field experience.

Delete paragraph below if sealants specified are not offered in a choice of colors, which is the case with most pavement joint sealants.

B. Colors of Exposed Joint Sealants:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.3 COLD-APPLIED JOINT SEALANTS

If subparagraphs titled "Available Products" or "Products" are retained in this Article, coordinate with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

A. Multicomponent Jet-Fuel-Resistant Sealant for Concrete:  Pourable, chemically curing elastomeric formulation complying with the following requirements for formulation and with ASTM C 920 for type, grade, class, and uses indicated:

1. Urethane Formulation:  Type M; Grade P; Class 12-1/2; Uses T, M, and, as applicable to joint substrates indicated, O.

a. [Available ]Products:

1) Pecora Corporation; Urexpan NR-300.

2) <Insert manufacturer's name; product name or designation.>

2. Coal-Tar-Modified Polymer Formulation:  Type M; Grade P; Class 25; Uses T and, as applicable to joint substrates indicated, O.

a. [Available ]Products:

1) Meadows, W. R., Inc.; Sealtight Gardox.

2) <Insert manufacturer's name; product name or designation.>

3. Bitumen-Modified Urethane Formulation:  Type M; Grade P; Class 25; Uses T, M, and, as applicable to joint substrates indicated, O.

a. [Available ]Products:

1) Tremco Sealant/Waterproofing Division; Vulkem 202.

2) <Insert manufacturer's name; product name or designation.>

B. Single-Component Jet-Fuel-Resistant Urethane Sealant for Concrete:  Single-component, pourable, coal-tar-modified, urethane formulation complying with ASTM C 920 for Type S; Grade P; Class 25; Uses T, M, and, as applicable to joint substrates indicated, O.

1. [Available ]Products:

a. Sonneborn, Div. of ChemRex, Inc.; Sonomeric 1.

b. <Insert manufacturer's name; product name or designation.>

C. Type NS Silicone Sealant for Concrete:  Single-component, low-modulus, neutral-curing, nonsag silicone sealant complying with ASTM D 5893 for Type NS.

1. [Available ]Products:

a. Crafco Inc.; RoadSaver Silicone.

b. Dow Corning Corporation; 888.

c. <Insert manufacturer's name; product name or designation.>

D. Type SL Silicone Sealant for Concrete and Asphalt:  Single-component, low-modulus, neutral-curing, self-leveling silicone sealant complying with ASTM D 5893 for Type SL.

1. [Available ]Products:

a. Crafco Inc.; RoadSaver Silicone SL.

b. Dow Corning Corporation; 890-SL.

c. <Insert manufacturer's name; product name or designation.>

E. Multicomponent Low-Modulus Sealant for Concrete and Asphalt:  Proprietary formulation consisting of reactive petropolymer and activator components producing a pourable, self-leveling sealant.

1. [Available ]Products:

a. Meadows, W. R., Inc.; Sof-Seal.

b. <Insert manufacturer's name; product name or designation.>

2.4 HOT-APPLIED JOINT SEALANTS

If subparagraphs titled "Available Products" or "Products" are retained in this Article, coordinate with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

A. Jet-Fuel-Resistant Elastomeric Sealant for Concrete:  Single-component formulation complying with ASTM D 3569.

1. [Available ]Products:

a. Crafco Inc.; Superseal 444/777.

b. Meadows, W. R., Inc.; Poly-Jet 3569.

c. <Insert manufacturer's name; product name or designation.>

Products complying with paragraph above and first paragraph below are unsuitable for use with asphalt pavement.

B. Jet-Fuel-Resistant Sealant for Concrete and Tar Concrete:  Single-component formulation complying with ASTM D 3581.

1. [Available ]Products:

a. Crafco Inc.; Superseal 1614A.

b. Meadows, W. R., Inc.; Poly-Jet 1614.

c. Meadows, W. R., Inc.; Poly-Jet 3406.

d. Meadows, W. R., Inc.; Poly-Jet 3569.

e. <Insert manufacturer's name; product name or designation.>

C. Elastomeric Sealant for Concrete:  Single-component formulation complying with ASTM D 3406.

1. [Available ]Products:

a. Crafco Inc.; Superseal 444/777.

b. Meadows, W. R., Inc.; Poly-Jet 3406.

c. <Insert manufacturer's name; product name or designation.>

D. Sealant for Concrete and Asphalt:  Single-component formulation complying with ASTM D 3405.

1. [Available ]Products:

a. Koch Materials Company; Product No. 9005.

b. Koch Materials Company; Product No. 9030.

c. Meadows, W. R., Inc.; Sealtight Hi-Spec.

d. <Insert manufacturer's name; product name or designation.>

2.5 JOINT-SEALANT BACKER MATERIALS

A. General:  Provide joint-sealant backer materials that are nonstaining; are compatible with joint substrates, sealants, primers, and other joint fillers; and are approved for applications indicated by joint-sealant manufacturer based on field experience and laboratory testing.

Retain paragraph below for use of cold- and hot-applied sealants in joints, such as contraction joints, where backer materials serve only to limit sealant depth and prevent bottom-side adhesion.

B. Round Backer Rods for Cold- and Hot-Applied Sealants:  ASTM D 5249, Type 1, of diameter and density required to control sealant depth and prevent bottom-side adhesion of sealant.

Retain first paragraph below for use of cold- and hot-applied sealants in joints, such as expansion joints, where it is desirable for backing material to fill remainder of joint opening under sealant and minimize intrusion of water and incompressible foreign objects.

C. Backer Strips for Cold- and Hot-Applied Sealants:  ASTM D 5249; Type 2; of thickness and width required to control sealant depth, prevent bottom-side adhesion of sealant, and fill remainder of joint opening under sealant.

D. Round Backer Rods for Cold-Applied Sealants:  ASTM D 5249, Type 3, of diameter and density required to control sealant depth and prevent bottom-side adhesion of sealant.

2.6 PRIMERS

Generally retain this Article unless it is known that priming of substrates is not required with sealants specified.  Purpose of primers is to improve adhesion of sealant to substrate.

A. Primers:  Product recommended by joint-sealant manufacturer where required for adhesion of sealant to joint substrates indicated, as determined from preconstruction joint-sealant-substrate tests and field tests.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine joints indicated to receive joint sealants, with Installer present, for compliance with requirements for joint configuration, installation tolerances, and other conditions affecting joint-sealant performance.

1. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. Surface Cleaning of Joints:  Clean out joints immediately before installing joint sealants to comply with joint-sealant manufacturer's written instructions.

As previously noted in Part 2 "Primers" Article, purpose of primers is to improve adhesion of sealant to substrate.

B. Joint Priming:  Prime joint substrates where indicated or where recommended in writing by joint-sealant manufacturer, based on preconstruction joint-sealant-substrate tests or prior experience.  Apply primer to comply with joint-sealant manufacturer's written instructions.  Confine primers to areas of joint-sealant bond; do not allow spillage or migration onto adjoining surfaces.

3.3 INSTALLATION OF JOINT SEALANTS

A. General:  Comply with joint-sealant manufacturer's written installation instructions for products and applications indicated, unless more stringent requirements apply.

B. Sealant Installation Standard:  Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions indicated.

C. Install backer materials of type indicated to support sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

1. Do not leave gaps between ends of backer materials.

2. Do not stretch, twist, puncture, or tear backer materials.

3. Remove absorbent backer materials that have become wet before sealant application and replace them with dry materials.

D. Install sealants using proven techniques that comply with the following and at the same time backings are installed:

1. Place sealants so they directly contact and fully wet joint substrates.

2. Completely fill recesses provided for each joint configuration.

3. Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

E. Tooling of Nonsag Sealants:  Immediately after sealant application and before skinning or curing begins, tool sealants according to requirements specified below to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint.

1. Remove excess sealants from surfaces adjacent to joint.

2. Use tooling agents that are approved in writing by joint-sealant manufacturer and that do not discolor sealants or adjacent surfaces.

F. Provide joint configuration to comply with joint-sealant manufacturer's written instructions, unless otherwise indicated.

G. Provide recessed joint configuration for silicone sealants of recess depth and at locations indicated.

3.4 CLEANING

A. Clean off excess sealants or sealant smears adjacent to joints as the Work progresses by methods and with cleaning materials approved by manufacturers of joint sealants and of products in which joints occur.

3.5 PROTECTION

A. Protect joint sealants during and after curing period from contact with contaminating substances and from damage resulting from construction operations or other causes so sealants are without deterioration or damage at time of Substantial Completion.  If, despite such protection, damage or deterioration occurs, cut out and remove damaged or deteriorated joint sealants immediately and replace with joint sealant so installations with repaired areas are indistinguishable from the original work.

END OF SECTION 321373

	CONCRETE PAVING JOINT SEALANTS
	321373 - 1



