Copyright 2011 AIA
MasterSpec Professional
08/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 034500 - PRECAST ARCHITECTURAL CONCRETE
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes architectural precast concrete cladding[ and load-bearing] units.

1.2 DEFINITIONS

Retain terms that remain after this Section has been edited for a project.

Retain "Design Reference Sample" Paragraph below if a design reference sample has been preapproved by Architect.

A. Design Reference Sample: Sample of approved architectural precast concrete color, finish and texture, preapproved by Architect.

1.3 PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

1.4 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools.

2. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

C. Design Mixtures: For each precast concrete mixture. Include compressive strength and water-absorption tests.

D. Shop Drawings:

1. Detail fabrication and installation of architectural precast concrete units.

2. Indicate locations, plans, elevations, dimensions, shapes, and cross sections of each unit.

3. Indicate joints, reveals, drips, chamfers, and extent and location of each surface finish.

4. Indicate details at building corners.

Retain "Samples" Paragraph below if finishes, colors, and textures are preselected, specified, or scheduled. Coordinate with sample panels and range samples in "Quality Assurance" Article.

E. Samples: Design reference samples for initial verification of design intent, for each type of finish indicated on exposed surfaces of architectural precast concrete units, in sets of three, representative of finish, color, and texture variations expected; approximately 12 by 12 by 2 inches (300 by 300 by 50 mm).

Retain "Delegated-Design Submittal" Paragraph below if design services have been delegated to Contractor.

F. Delegated-Design Submittal: For architectural precast concrete indicated to comply with performance requirements and design criteria, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

1.5 INFORMATIONAL SUBMITTALS

Retain "Welding certificates" Paragraph below if retaining "Welding Qualifications" Paragraph in "Quality Assurance" Article.

A. Welding certificates.

B. Material certificates.

C. Material Test Reports: For aggregates.

Retain "Field quality-control( and special inspection) reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting. Retain option if Contractor is responsible for special inspections.

D. Field quality-control[ and special inspection] reports.

1.6 QUALITY ASSURANCE

A. Fabricator Qualifications: A firm that assumes responsibility for engineering architectural precast concrete units to comply with performance requirements. This responsibility includes preparation of Shop Drawings and comprehensive engineering analysis by a qualified professional engineer.

Usually retain first subparagraph below. PCI plant certification was established in 1967 and is a different program than APA's plant certification established in 1993. Consult APA or PCI for further information.

1. Designated as a PCI-certified plant for Group A, Category A1 - Architectural Cladding and Load Bearing Units[ at time of bidding][ or designated as an APA-certified plant for production of architectural precast concrete products].

Retain subparagraph below if required for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5.

2. Fabricator is located within 500 miles (800 km) of Project site.

B. Quality-Control Standard: For manufacturing procedures and testing requirements, quality-control recommendations, and dimensional tolerances for types of units required, comply with PCI MNL 117, "Manual for Quality Control for Plants and Production of Architectural Precast Concrete Products."

Retain "Welding Qualifications" Paragraph below if shop or field welding is required. If retaining, also retain "Welding certificates" Paragraph in "Informational Submittals" Article.

C. Welding Qualifications: Qualify procedures and personnel according to AWS D1.1/D.1.1M, "Structural Welding Code - Steel"; and AWS D1.4/D1.4M, "Structural Welding Code - Reinforcing Steel."

PCI recommends review of preproduction sample panels. Revise number and size of sample panels in "Sample Panels" Paragraph below to suit Project.

D. Sample Panels: After sample approval and before fabricating architectural precast concrete units, produce a minimum of [two] <Insert number> sample panels approximately [16 sq. ft. (1.5 sq. m)] <Insert dimension> in area for review by Architect. Incorporate full-scale details of architectural features, finishes, textures, and transitions in sample panels.

1.7 COORDINATION

A. Furnish loose connection hardware and anchorage items to be embedded in or attached to other construction without delaying the Work. Provide locations, setting diagrams, templates, instructions, and directions, as required, for installation.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Delegated Design" Paragraph below if Contractor is required to assume responsibility for design.

A. Delegated Design: Engage a qualified professional engineer, as defined in Section 014000 "Quality Requirements," to design architectural precast concrete units.

B. Design Standards: Comply with ACI 318 (ACI 318M) and design recommendations of PCI MNL 120, "PCI Design Handbook - Precast and Prestressed Concrete," applicable to types of architectural precast concrete units indicated.

Retain "Calculated Fire-Test-Response Characteristics" Paragraph below if fire-rated units or assemblies are required. Retain either option, or both, if acceptable to authorities having jurisdiction.

C. Calculated Fire-Test-Response Characteristics: Provide architectural precast concrete units with fire-resistance rating indicated as calculated according to [ACI 216.1 (ACI 216.1M)] [PCI MNL 124, "Design for Fire Resistance of Precast Prestressed Concrete,"] and acceptable to authorities having jurisdiction.

D. Structural Performance: Provide architectural precast concrete units and connections capable of withstanding design loads indicated within limits and under conditions indicated.

2.2 REINFORCING MATERIALS

Retain one or more paragraphs in this article to suit steel reinforcement requirements. Distinguish locations of each type of reinforcement here or on Drawings. If retaining Part 2 "Performance Requirements" Article, consider reviewing selections with fabricators.

Retain "Recycled Content of Steel Products" Paragraph below if recycled content is required for LEED Credit MR 4. USGBC allows a default value of 25 percent to be used for steel, without documentation; higher percentages can be claimed if they are supported by appropriate documentation.

A. Recycled Content of Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] [60] <Insert number> percent.

B. Reinforcing Bars: ASTM A 615/A 615M, Grade 60 (Grade 420), deformed.

Retain "Low-Alloy-Steel Reinforcing Bars" Paragraph below for reinforcement that is welded or if added ductility is sought.

C. Low-Alloy-Steel Reinforcing Bars: ASTM A 706/A 706M, deformed.

D. Plain-Steel Welded Wire Reinforcement: ASTM A 185/A 185M, fabricated from [as-drawn ][galvanized-]steel wire into flat sheets.

E. Deformed-Steel Welded Wire Reinforcement: ASTM A 497/A 497M, flat sheet.

F. Supports: Suspend reinforcement from back of mold or use bolsters, chairs, spacers, and other devices for spacing, supporting, and fastening reinforcing bars and welded wire reinforcement in place according to PCI MNL 117.

2.3 PRESTRESSING TENDONS

Retain this article if precast concrete units are prestressed, either pretensioned or post-tensioned.

A. Prestressing Strand: ASTM A 416/A 416M, Grade 270 (Grade 1860), uncoated, seven-wire, low-relaxation strand.

For aggressive climates, revise subparagraph below by adding an anchorage device encapsulation system consisting of caps and sleeves.

1. Coat unbonded post-tensioning strand with post-tensioning coating complying with ACI 423.7 and sheath with polypropylene tendon sheathing complying with ACI 423.7. Include anchorage devices and coupler assemblies.

2.4 CONCRETE MATERIALS

Retain materials in this article that are required; revise to suit Project.

Retain "Regional Materials" Paragraph below if required for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5.

A. Regional Materials: Precast architectural concrete shall be manufactured from aggregates[ and cement] that have been extracted or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

B. Portland Cement: ASTM C 150/C 150M, Type I or Type III, gray, unless otherwise indicated.

Mixing with white cement improves color uniformity. White cement has greater color consistency than gray cement and should be used for pastel colors. For darker colors, variations of gray cement have less effect on final color hue.

1. For surfaces exposed to view in finished structure, use gray or white cement, of same type, brand, and mill source.

C. Supplementary Cementitious Materials:

Retain mineral or cementitious admixtures from first four subparagraphs below. Because fly ash and gray silica fume affect color uniformity, they are not recommended by PCI where appearance is important. White silica fume is available.

1. Fly Ash: ASTM C 618, Class C or F, with maximum loss on ignition of 3 percent.

2. Metakaolin: ASTM C 618, Class N.

3. Silica Fume: ASTM C 1240, with optional chemical and physical requirement.

4. Ground Granulated Blast-Furnace Slag: ASTM C 989, Grade 100 or 120.

Retain "Blended Hydraulic Cement" Subparagraph below if factory-blended hydraulic cement is permitted; verify availability of options before specifying. Fly ash, slag, or pozzolanic materials in the nonportland cement part of blended hydraulic cement may slow rate of concrete strengthening and affect color uniformity.

5. Blended Hydraulic Cement: ASTM C 595, [Type IS, portland blast-furnace slag] [Type IP, portland-pozzolan] [Type I (PM), pozzolan-modified portland] [Type I (SM), slag-modified portland] cement.

ASTM C 33/C 33M limits deleterious substances in coarse aggregate depending on climate severity and in-service location of concrete. Class 5S is the most restrictive designation for architectural concrete exposed to severe weathering. PCI MNL 117 also establishes strict limits on deleterious substances for fine and coarse aggregates.

D. Normal-Weight Aggregates: Except as modified by PCI MNL 117, ASTM C 33/C 33M, with coarse aggregates complying with Class 5S. Stockpile fine and coarse aggregates for each type of exposed finish from a single source (pit or quarry) for Project.

Revise "Face-Mixture-Coarse Aggregates" and "Face-Mixture-Fine Aggregates" subparagraphs below to add descriptions of selected coarse- and fine-face aggregate colors and sources if required.

1. Face-Mixture-Coarse Aggregates: Selected, hard, and durable; free of material that reacts with cement or causes staining; to match selected finish sample.

Retain one option in "Gradation" Subparagraph below or insert gradation and maximum aggregate size if known. Fine and coarse aggregates are not always from same source.

a. Gradation: [Uniformly graded] [Gap graded] [To match design reference sample].

2. Face-Mixture-Fine Aggregates: Selected, natural or manufactured sand compatible with coarse aggregate; to match approved finish sample.

Retain "Coloring Admixture" Paragraph below if required. Add color selection if known.

E. Coloring Admixture: ASTM C 979/C 979M, synthetic or natural mineral-oxide pigments or colored water-reducing admixtures, temperature stable, and nonfading.

F. Water: Potable; free from deleterious material that may affect color stability, setting, or strength of concrete and complying with chemical limits of PCI MNL 117.

G. Air-Entraining Admixture: ASTM C 260, certified by manufacturer to be compatible with other required admixtures.

H. Chemical Admixtures: Certified by manufacturer to be compatible with other admixtures and to not contain calcium chloride, or more than 0.15 percent chloride ions or other salts by weight of admixture.

2.5 STEEL CONNECTION MATERIALS

Revise this article to suit Project. Add other materials as required.

A. Carbon-Steel Shapes and Plates: ASTM A 36/A 36M.

B. Carbon-Steel-Headed Studs: ASTM A 108, AISI 1018 through AISI 1020, cold finished, AWS D1.1/D1.1M, Type A or Type B, with arc shields and with minimum mechanical properties of PCI MNL 117, Table 3.2.3.

C. Carbon-Steel Plate: ASTM A 283/A 283M, Grade C.

D. Malleable Iron Castings: ASTM A 47/A 47M, Grade 32510 or Grade 35028.

E. Carbon-Steel Castings: ASTM A 27/A 27M, Grade 60-30 (Grade 415-205).

F. High-Strength, Low-Alloy Structural Steel: ASTM A 572/A 572M.

G. Carbon-Steel Structural Tubing: ASTM A 500/A 500M, Grade B or Grade C.

H. Wrought Carbon-Steel Bars: ASTM A 675/A 675M, Grade 65 (Grade 450).

I. Deformed-Steel Wire or Bar Anchors: ASTM A 496/A 496M or ASTM A 706/A 706M.

ASTM A 307 defines the term "studs" to include stud stock and threaded rods.

J. Carbon-Steel Bolts and Studs: ASTM A 307, Grade A or ASTM F 1554, Grade 36 (ASTM F 568M, Property Class 4.6); carbon-steel, hex-head bolts and studs; carbon-steel nuts, ASTM A 563 (ASTM A 563M); and flat, unhardened steel washers, ASTM F 844.

High-strength bolts are used for friction-type connections between steel members and are not recommended by PCI between steel and concrete because concrete creep and crushing of concrete during bolt tightening reduce effectiveness.

K. High-Strength Bolts and Nuts: ASTM A 325 (ASTM A 325M), Type 1, heavy hex steel structural bolts; heavy hex carbon-steel nuts, ASTM A 563 (ASTM A 563M); and hardened carbon-steel washers, ASTM F 436 (ASTM F 436M).

Retain "Zinc-Coated Finish" Paragraph if galvanized finish is required. Revise locations of galvanized items if required. Field welding should generally not be permitted on galvanized elements unless galvanizing is removed or acceptable welding procedures are submitted. Hot-dip galvanized finish provides greater corrosion resistance than electrodeposited zinc coating. Electrodeposition is usually limited to threaded fasteners.

L. Zinc-Coated Finish: For exterior steel items[, steel in exterior walls,] and items indicated for galvanizing, apply zinc coating by [hot-dip process according to ASTM A 123/A 123M or ASTM A 153/A 153M] [electrodeposition according to ASTM B 633, SC 3, Types 1 and 2].

1. Galvanizing Repair Paint: High-zinc-dust-content paint with dry film containing not less than 94 percent zinc dust by weight, and complying with DOD-P-21035B or SSPC-Paint 20.

Retain "Shop-Primed Finish" Paragraph below if paint finish is required. Revise locations of priming if required. MPI 79 in first option below provides some corrosion protection, while SSPC-Paint 25, without topcoating, provides minimal corrosion protection.

M. Shop-Primed Finish: Prepare surfaces of nongalvanized steel items, except those surfaces to be embedded in concrete, according to requirements in SSPC-SP 3 and shop-apply [lead- and chromate-free, rust-inhibitive primer, complying with performance requirements in MPI 79] [SSPC-Paint 25] according to SSPC-PA 1.

2.6 GROUT MATERIALS

Add other proprietary grout systems to suit Project. Indicate locations of each type of grout in this article or on Drawings if retaining more than one type.

A. Sand-Cement Grout: Portland cement, ASTM C 150/C 150M, Type I, and clean, natural sand, ASTM C 144 or ASTM C 404. Mix at ratio of 1 part cement to 2-1/2 to 3 parts sand, by volume, with minimum water required for placement and hydration. Water-soluble chloride ion content less than 0.06 percent by weight of cement when tested according to ASTM C 1218/C 1218M.

Retain "Nonmetallic, Nonshrink Grout" Paragraph below if required or if cement-grout shrinkage could cause structural deficiency. For critical installations, require manufacturer to provide field supervision.

B. Nonmetallic, Nonshrink Grout: Packaged, nonmetallic, noncorrosive, nonstaining grout containing selected silica sands, portland cement, shrinkage-compensating agents, plasticizing and water-reducing agents, complying with ASTM C 1107/C 1107M, Grade A for drypack and Grades B and C for flowable grout and of consistency suitable for application within a 30-minute working time. Water-soluble chloride ion content less than 0.06 percent by weight of cement when tested according to ASTM C 1218/C 1218M.

C. Epoxy-Resin Grout: Two-component, mineral-filled epoxy resin; ASTM C 881/C 881M, of type, grade, and class to suit requirements.

2.7 CONCRETE MIXTURES

A. Prepare design mixtures for each type of precast concrete required.

Retain first paragraph below if fly ash, ground granulated blast-furnace slag, or metakaolin and silica fume are permitted. Revise percentages to suit Project. White silica fume is available.

B. Limit use of fly ash and ground granulated blast-furnace slag to 20 percent of portland cement by weight; limit metakaolin and silica fume to 10 percent of portland cement by weight.

C. Design mixtures may be prepared by a qualified independent testing agency or by qualified precast plant personnel at architectural precast concrete fabricator's option.

D. Limit water-soluble chloride ions to maximum percentage by weight of cement permitted by ACI 318 (ACI 318M) or PCI MNL 117 when tested according to ASTM C 1218/C 1218M.

Architectural precast concrete units may be manufactured with a separate architectural face mixture and a structural backup mixture. Face and backup mixtures should have similar shrinkage and expansion coefficients. Similar water-cementitious materials ratios and cement-aggregate ratios are recommended by PCI to limit bowing or warping.

E. Normal-Weight Concrete Mixtures: Proportion mixtures by either laboratory trial batch or field test data methods according to ACI 211.1, with materials to be used on Project, to provide normal-weight concrete with the following properties:

Retain "Compressive Strength (28 Days)" Subparagraph below or revise to suit Project. Higher-strength mixtures may be available; verify availability with fabricators.

1. Compressive Strength (28 Days): 5000 psi (34.5 MPa) minimum.

Water absorption indicates susceptibility to weather staining. PCI states that limits in "Water Absorption" Paragraph below are suitable for average exposures. Different parts of a single panel cannot be produced with different absorptions. Verify that fabricators can produce units with lower water absorption because special consolidation techniques to increase concrete density are required.

F. Water Absorption: 6 percent by weight or 14 percent by volume, tested according to ASTM C 642, except for boiling requirement.

G. Add air-entraining admixture at manufacturer's prescribed rate to result in concrete at point of placement having an air content complying with PCI MNL 117.

H. When included in design mixtures, add other admixtures to concrete mixtures according to manufacturer's written instructions.

2.8 FABRICATION

A. Cast-in Anchors, Inserts, Plates, Angles, and Other Anchorage Hardware: Fabricate anchorage hardware with sufficient anchorage and embedment to comply with design requirements. Accurately position for attachment of loose hardware, and secure in place during precasting operations. Locate anchorage hardware where it does not affect position of main reinforcement or concrete placement.

1. Weld-headed studs and deformed bar anchors used for anchorage according to AWS D1.1/D1.1M and AWS C5.4, "Recommended Practices for Stud Welding."

Coordinate first paragraph below with Section 055000 "Metal Fabrications" for furnishing and installing loose hardware items.

B. Furnish loose hardware items including steel plates, clip angles, seat angles, anchors, dowels, cramps, hangers, and other hardware shapes for securing architectural precast concrete units to supporting and adjacent construction.

C. Cast-in reglets, slots, holes, and other accessories in architectural precast concrete units as indicated on the Contract Drawings.

D. Reinforcement: Comply with recommendations in PCI MNL 117 for fabricating, placing, and supporting reinforcement.

E. Reinforce architectural precast concrete units to resist handling, transportation, and erection stresses and specified in-place loads.

Retain first paragraph below for precast, prestressed architectural concrete units. Option to prestress may be left to fabricator if objective is to aid handling and to control cracking of units during installation.

F. Prestress tendons for architectural precast concrete units by either pretensioning or post-tensioning methods. Comply with PCI MNL 117.

G. Comply with requirements in PCI MNL 117 and requirements in this Section for measuring, mixing, transporting, and placing concrete. After concrete batching, no additional water may be added.

Retain first paragraph below if a separate face mixture is required or is Contractor's option.

H. Place face mixture to a minimum thickness after consolidation of the greater of 1 inch (25 mm) or 1.5 times the maximum aggregate size, but not less than the minimum reinforcing cover specified.

I. Place concrete in a continuous operation to prevent cold joints or planes of weakness from forming in precast concrete units.

1. Place backup concrete mixture to ensure bond with face-mixture concrete.

J. Thoroughly consolidate placed concrete by internal and external vibration without dislocating or damaging reinforcement and built-in items, and minimize pour lines, honeycombing, or entrapped air voids on surfaces. Use equipment and procedures complying with PCI MNL 117.

1. Place self-consolidating concrete without vibration according to PCI TR-6, "Interim Guidelines for the Use of Self-Consolidating Concrete in Precast/Prestressed Concrete Institute Member Plants." Ensure adequate bond between face and backup concrete, if used.

K. Comply with PCI MNL 117 for hot- and cold-weather concrete placement.

L. Identify pickup points of architectural precast concrete units and orientation in structure with permanent markings, complying with markings indicated on Shop Drawings. Imprint or permanently mark casting date on each architectural precast concrete unit on a surface that does not show in finished structure.

M. Cure concrete, according to requirements in PCI MNL 117, by moisture retention without heat or by accelerated heat curing using low-pressure live steam or radiant heat and moisture. Cure units until compressive strength is high enough to ensure that stripping does not have an effect on performance or appearance of final product.

N. Discard and replace architectural precast concrete units that do not comply with requirements, including structural, manufacturing tolerance, and appearance, unless repairs meet requirements in PCI MNL 117 and Architect's approval.

2.9 FABRICATION TOLERANCES

A. Fabricate architectural precast concrete units to shapes, lines, and dimensions indicated so each finished unit complies with PCI MNL 117 product tolerances as well as position tolerances for cast-in items.

2.10 FINISHES

A. Exposed faces shall be free of joint marks, grain, and other obvious defects. Corners, including false joints shall be uniform, straight, and sharp. Finish exposed-face surfaces of architectural precast concrete units to match approved [design reference sample] [sample panels] [mockups] and as follows:

This article presumes Architect has preapproved one or more design reference samples. Include complete description of design reference sample here. If preapproving fabricators, coordinate with "Manufacturers" Article. Revise if multiple samples are approved.

1. Design Reference Sample: <Insert description and identify fabricator and code number of sample>.

Retain first subparagraph below if required. If retaining, revise and add reference number; PCI publishes numbered, color photographs of 428 precast concrete finishes; see PCI's Web site, www.pci.org. Add reference number combinations if more than one finish is required.

2. PCI's "Architectural Precast Concrete - Color and Texture Selection Guide," of plate numbers indicated.

Retain type of finish from nine finish subparagraphs below if needed. If more than one finish is required, add locations to finish descriptions or indicate on Drawings. Add more-detailed descriptions of finishes outlined below if greater definition, such as light, medium, or deep, is required. See PCI MNL 117 for more information on finishes. An as-cast finish generally results in a mottled surface or non-uniform finish.

3. As-Cast Surface Finish: Provide surfaces to match approved sample for acceptable surface, air voids, sand streaks, and honeycomb.

4. Textured-Surface Finish: Impart by form liners or inserts.

5. Bushhammer Finish: Use power or hand tools to remove matrix and fracture coarse aggregates.

6. Exposed-Aggregate Finish: Use chemical retarding agents applied to concrete forms and washing and brushing procedures to expose aggregate and surrounding matrix surfaces after form removal.

7. Abrasive-Blast Finish: Use abrasive grit, equipment, application techniques, and cleaning procedures to expose aggregate and surrounding matrix surfaces.

8. Acid-Etched Finish: Use acid and hot-water solution, equipment, application techniques, and cleaning procedures to expose aggregate and surrounding matrix surfaces. Protect hardware, connections, and insulation from acid attach.

9. Honed Finish: Use continuous mechanical abrasion with fine grit, followed by filling and rubbing procedures.

10. Polished Finish: Use continuous mechanical abrasion with fine grit, followed by filling and rubbing procedures.

11. Sand-Embedment Finish: Use selected stones placed in a sand bed in bottom of mold, with sand removed after curing.

Retain one of first two paragraphs below if applicable. Revise second paragraph to float finish or light-broom finish if smooth, steel-trowel finish is unnecessary.

B. Finish exposed [top] [back] surfaces of architectural precast concrete units to match face-surface finish.

C. Finish exposed [top] [back] surfaces of architectural precast concrete units with smooth, steel-trowel finish.

Revise finish in paragraph below to light-broom stippled, or float finish if necessary. Upgrade to smooth, steel-trowel finish if surface is in contact with materials requiring a smooth finish.

D. Finish unexposed surfaces of architectural precast concrete units with as cast finish.

2.11 SOURCE QUALITY CONTROL

Retain "Quality-Control Testing" Paragraph below if establishing a minimum standard of plant testing and inspecting. PCI MNL 117 mandates source testing requirements and a plant "Quality Systems Manual." PCI certification also ensures periodic auditing of plants for compliance with requirements in PCI MNL 117.

A. Quality-Control Testing: Test and inspect precast concrete according to PCI MNL 117 requirements. If using self-consolidating concrete, also test and inspect according to PCI TR-6, ASTM C 1610/C 1610M, ASTM C 1611/C 1611M, ASTM C 1621/C 1621M, and ASTM C 1712.

Retain paragraph below if required. PCI certification may be acceptable to authorities having jurisdiction without further monitoring of plant quality-control and testing program by Owner.

B. Owner will employ an independent testing agency to evaluate architectural precast concrete fabricator's quality-control and testing methods.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Install clips, hangers, bearing pads, and other accessories required for connecting architectural precast concrete units to supporting members and backup materials.

B. Erect architectural precast concrete level, plumb, and square within specified allowable tolerances. Provide temporary supports and bracing as required to maintain position, stability, and alignment of units until permanent connections are completed.

1. Maintain horizontal and vertical joint alignment and uniform joint width as erection progresses.

2. Unless otherwise indicated, maintain uniform joint widths of 3/4 inch (19 mm).

C. Connect architectural precast concrete units in position by bolting, welding, grouting, or as otherwise indicated on Shop Drawings. Remove temporary shims, wedges, and spacers as soon as practical after connecting and grouting are completed.

D. Welding: Comply with applicable requirements in AWS D1.1/D1.1M and AWS D1.4/D1.4M for welding, welding electrodes, appearance, quality of welds, and methods used in correcting welding work.

E. At bolted connections, use lock washers, tack welding, or other approved means to prevent loosening of nuts after final adjustment.

In "Grouting or Dry-Packing Connections and Joints" Paragraph below, revise locations and extent of grouting if required.

F. Grouting or Dry-Packing Connections and Joints: Grout connections where required or indicated. Retain flowable grout in place until hard enough to support itself. Alternatively, pack spaces with stiff dry-pack grout material, tamping until voids are completely filled. Place grout and finish smooth, level, and plumb with adjacent concrete surfaces. Promptly remove grout material from exposed surfaces before it affects finishes or hardens. Keep grouted joints damp for not less than 24 hours after initial set.

3.2 ERECTION TOLERANCES

A. Erect architectural precast concrete units level, plumb, square, and in alignment without exceeding the noncumulative erection tolerances of PCI MNL 117, Appendix I.

3.3 FIELD QUALITY CONTROL

Retain first option in "Special Inspections" Paragraph below if Owner engages a special inspector. Consider retaining second option if authorities having jurisdiction allow Contractor to engage special inspector. If retaining second option, retain "Field quality-control( and special inspection) reports" Paragraph in "Informational Submittals" Article.

A. Special Inspections: [Owner will engage] [Engage] a qualified special inspector to perform the following special inspections and prepare reports:

1. Erection of loadbearing precast concrete members.

2. <Insert special inspections>.

Retain "Testing Agency" Paragraph below, with or without "Special Inspections" Paragraph above, to identify who shall perform tests and inspections. If retaining second option in "Testing Agency" Paragraph, retain "Field quality-control( and special inspection) reports" Paragraph in "Informational Submittals" Article.

B. Testing Agency: [Owner will engage] [Engage] a qualified testing agency to perform tests and inspections and prepare test reports.

C. Visually inspect field welds and test according to ASTM E 165 or to ASTM E 709 and ASTM E 1444. High-strength bolted connections are subject to inspections.

D. Testing agency will report test results promptly and in writing to Contractor and Architect.

E. Repair or remove and replace work where tests and inspections indicate that it does not comply with specified requirements.

F. Additional testing and inspecting, at Contractor's expense, shall be performed to determine compliance of replaced or additional work with specified requirements.

3.4 REPAIRS

Blemishes occurring after delivery are normally repaired before final joint sealing and cleaning as weather permits.

A. Repair architectural precast concrete units if permitted by Architect. Architect reserves the right to reject repaired units that do not comply with requirements.

Precast concrete manufacturer should develop appropriate repair mixtures and techniques during production sample approval process.

B. Mix patching materials and repair units so cured patches blend with color, texture, and uniformity of adjacent exposed surfaces and show no apparent line of demarcation between original and repaired work, when viewed in typical daylight illumination from a distance of 20 feet (6 m).

C. Prepare and repair damaged galvanized coatings with galvanizing repair paint according to ASTM A 780/A 780M.

Retain last paragraph above if using galvanized anchors, connections, and other items; retain first paragraph below if items are prime painted.

D. Wire brush, clean, and paint damaged prime-painted components with same type of shop primer.

E. Remove and replace damaged architectural precast concrete units when repairs do not comply with requirements.

3.5 CLEANING

A. Clean surfaces of precast concrete units exposed to view.

B. Clean mortar, plaster, fireproofing, weld slag, and other deleterious material from concrete surfaces and adjacent materials immediately.

C. Clean exposed surfaces of precast concrete units after erection and completion of joint treatment to remove weld marks, other markings, dirt, and stains.

1. Perform cleaning procedures, if necessary, according to precast concrete fabricator's recommendations. Protect other work from staining or damage due to cleaning operations.

2. Do not use cleaning materials or processes that could change the appearance of exposed concrete finishes or damage adjacent materials.

END OF SECTION 034500

	PRECAST ARCHITECTURAL CONCRETE
	034500 - 1



