Copyright 2012 AIA
MasterSpec Professional
02/12

Copyright 2012 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 042113 - BRICK MASONRY
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Concrete facing brick.

2. Face brick.

Include separate allowances for special shapes if required.

B. Allowances: Face brick is included under Face Brick Allowances as specified in Section 012100 "Allowances."

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product indicated.

B. LEED Submittals:

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools.

1. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials indicating location and distance from Project of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating cost for each regional material and the fraction by weight that is considered regional.

C. Samples: For each type and color of [brick] [and] [colored mortar].

1.3 INFORMATIONAL SUBMITTALS

Usually retain paragraph below. Material certificates are required for all masonry constructed under MSJC Code.

A. Material Certificates: For each type and size of product indicated.

1.4 QUALITY ASSURANCE

A. Masonry Standard: Comply with ACI 530.1/ASCE 6/TMS 602 unless modified by requirements in the Contract Documents.

B. Sample Panels: Build sample panels to verify selections made under sample submittals and to demonstrate aesthetic effects. Comply with requirements in Section 014000 "Quality Requirements" for mockups.

1. Build sample panels for each type of exposed unit masonry construction in sizes approximately [48 inches (1200 mm)] [60 inches (1500 mm)] <Insert size> long by [36 inches (900 mm)] [48 inches (1200 mm)] <Insert size> high[ by full thickness].

1.5 PROJECT CONDITIONS

A. Cold-Weather Requirements: Do not use frozen materials or materials mixed or coated with ice or frost. Do not build on frozen substrates. Remove and replace unit masonry damaged by frost or by freezing conditions. Comply with cold-weather construction requirements contained in ACI 530.1/ASCE 6/TMS 602.

1. Cold-Weather Cleaning: Use liquid cleaning methods only when air temperature is 40 deg F (4 deg C) and higher and will remain so until masonry has dried, but not less than seven days after completing cleaning.

B. Hot-Weather Requirements: Comply with hot-weather construction requirements contained in ACI 530.1/ASCE 6/TMS 602.

PART 2 -  PRODUCTS

2.1 MASONRY UNITS, GENERAL

A. Defective Units: Referenced masonry unit standards may allow a certain percentage of units to contain chips, cracks, or other defects exceeding limits stated in the standard. Do not use units where such defects will be exposed in the completed Work.

2.2 CONCRETE BRICK

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply.

A. Regional Materials: Concrete brick shall be manufactured within 500 miles (800 km) of Project site from aggregates[ and cement] that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

Retain first paragraph below for increased water resistance of units if required. If retaining, also retain water-repellent mortar admixture.

B. Integral Water Repellent: Provide concrete brick made with liquid polymeric, integral water repellent admixture that does not reduce flexural bond strength.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. ACM Chemistries; RainBloc.

b. BASF Aktiengesellschaft; Rheopel Plus.

c. Grace Construction Products; W.R. Grace & Co. -- Conn; Dry-Block.

d. <Insert manufacturer's name; product name or designation>.

C. Concrete Facing Brick: ASTM C 1634.

Retain one of three weights in first subparagraph below or delete subparagraph for Contractor's option.

1. Density Classification: [Lightweight] [Medium weight] [Normal weight].

2. Size (Actual Dimensions): 3-5/8 inches (92 mm) wide by [2-1/4 inches (57 mm)] [2-3/4 inches (70 mm)] [3-5/8 inches (92 mm)] high by [7-5/8 inches (194 mm)] [11-5/8 inches (295 mm)] [15-5/8 inches (397 mm)] long.

3. Texture: [Split-face finish] [Ground-face finish] <Insert description>.

a. Match Architect's samples.

4. Colors: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

2.3 BRICK

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply.

A. Regional Materials: Brick shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

B. General: Provide shapes indicated and as follows.

1. For ends of sills and caps and for similar applications that would otherwise expose unfinished brick surfaces, provide units without cores or frogs and with exposed surfaces finished.

2. Provide special shapes for applications where shapes produced by sawing would result in sawed surfaces being exposed to view.

C. Face Brick: Facing brick complying with ASTM C 216[ or hollow brick complying with ASTM C 652, Class H40V (void areas between 25 and 40 percent of gross cross-sectional area)].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation for acceptable face brick>.

2. Grade: [SW] [MW or SW].

3. Type: [FBX] [FBS] [FBA] [FBX or HBX] [FBS or HBS] [FBA or HBA]

Consider retaining first subparagraph below; it eliminates the need to wet brick before laying. Before retaining, verify that brick selected complies with requirements. See Evaluations.

4. Initial Rate of Absorption: Less than 30 g/30 sq. in. (30 g/194 sq. cm) per minute when tested per ASTM C 67.

Requirement in first subparagraph below will not by itself prevent efflorescence. See Evaluations.

5. Efflorescence: Provide brick that has been tested according to ASTM C 67 and is rated "not effloresced."

Delete first subparagraph below if surface-coated brick is not used.

6. Surface Coating: Brick with colors or textures produced by application of coatings shall withstand 50 cycles of freezing and thawing per ASTM C 67 with no observable difference in the applied finish when viewed from 10 feet (3 m).

Sizes in remaining subparagraphs are examples only. Verify availability of sizes with local suppliers and revise to suit Project.

Retain one of first two subparagraphs below for three courses in 8 inches (203 mm).

7. Size (Actual Dimensions): [3-1/2 inches (89 mm) wide by 2-1/4 inches (57 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-1/4 inches (57 mm) high by 7-5/8 inches (194 mm) long].

8. Size (Actual Dimensions): [3-1/2 inches (89 mm)] [or] [3-5/8 inches (92 mm)] wide by 2-1/4 inches (57 mm) high by 8 inches (203 mm) long.

Retain first subparagraph below for five courses in 16 inches (406 mm).

Retain one of two subparagraphs below for course height of 4 inches (102 mm).

9. Size (Actual Dimensions): [3-1/2 inches (89 mm) wide by 3-1/2 inches (89 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 3-5/8 inches (92 mm) high by 7-5/8 inches (194 mm) long].

10. Size (Actual Dimensions): [3-1/2 inches (89 mm) wide by 3-1/2 inches (89 mm) high by 11-1/2 inches (292 mm) long] [or] [3-5/8 inches (92 mm) wide by 3-5/8 inches (92 mm) high by 11-5/8 inches (295 mm) long].

2.4 MORTAR MATERIALS

Coordinate requirements in this article with those in "Mortar Mixes" Article.

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply.

A. Regional Materials: Aggregate for mortar[, cement, and lime] shall be extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

Retain one or more of first four paragraphs below. Delete masonry cement if not allowed by "Mortar Mixes" Article. See Evaluations for discussion of masonry cement.

B. Portland Cement: ASTM C 150, Type I or II, except Type III may be used for cold-weather construction. Provide natural color or white cement as required to produce mortar color indicated.

C. Hydrated Lime: ASTM C 207, Type S.

Mix in first paragraph below allows better control of color than job-mixed, portland cement-lime mortar. If retaining paragraph, also retain last two paragraphs above.

D. Portland Cement-Lime Mix: Packaged blend of portland cement and hydrated lime containing no other ingredients.

E. Masonry Cement: ASTM C 91.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Capital Materials Corporation; Flamingo Color Masonry Cement.

b. Cemex S.A.B. de C.V; [Brikset Type N] [Citadel Type S] [Dixie Type S] [Kosmortar Type N] [Richmortar] [Victor Plastic Cement].

c. Essroc; [Brixment] [Velvet].

d. Holcim (US) Inc; [Mortamix Masonry Cement] [Rainbow Mortamix Custom Buff Masonry Cement] [White Mortamix Masonry Cement].

e. Lafarge North America Inc; [Lafarge Masonry Cement] [Magnolia Masonry Cement] [Trinity White Masonry Cement].

f. Lehigh Cement Company; [Lehigh Masonry Cement] [Lehigh White Masonry Cement].

g. National Cement Company, Inc; Coosa Masonry Cement.

h. <Insert manufacturer's name; product name or designation>.

Retain first paragraph below for colored cement or for pigments added at Project site.

F. Mortar Pigments: Natural and synthetic iron oxides and chromium oxides, compounded for use in mortar mixes and complying with ASTM C 979. Use only pigments with a record of satisfactory performance in masonry mortar.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Davis Colors; True Tone Mortar Colors.

b. Lanxess Corporation; Bayferrox Iron Oxide Pigments.

c. Solomon Colors, Inc; SGS Mortar Colors.

d. <Insert manufacturer's name; product name or designation>.

Mixes in first paragraph below allow better control of color than job-mixed colored mortar. If retaining, also retain paragraphs above that specify materials included in the mixes retained below.

G. Colored Cement Product: Packaged blend made from [portland cement and hydrated lime] [or] [masonry cement] and mortar pigments, all complying with specified requirements, and containing no other ingredients.

1. Colored Portland Cement-Lime Mix:

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Capital Materials Corporation; Riverton Portland Cement Lime Custom Color.

2) Holcim (US) Inc; Rainbow Mortamix Custom Color Cement/Lime.

3) Lafarge North America Inc; Eaglebond Portland &amp;amp; Lime.

4) Lehigh Cement Company; Lehigh Custom Color Portland/Lime Cement.

5) <Insert manufacturer's name; product name or designation>.

2. Colored Masonry Cement:

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Capital Materials Corporation; Flamingo Color Masonry Cement.

2) Cemex S.A.B. de C.V; Richcolor Masonry Cement.

3) Essroc; Brixment-in-Color.

4) Holcim (US) Inc; Rainbow Mortamix Custom Color Masonry Cement.

5) Lafarge North America Inc; U.S. Cement Custom Color Masonry Cement..

6) Lehigh Cement Company; Lehigh Custom Color Masonry Cement.

7) National Cement Company, Inc; Coosa Masonry Cement.

8) <Insert manufacturer's name; product name or designation>.

H. Aggregate for Mortar: ASTM C 144.

1. White-Mortar Aggregates: Natural white sand or crushed white stone.

2. Colored-Mortar Aggregates: Natural sand or crushed stone of color necessary to produce required mortar color.

First paragraph below is an example of requirement for a concrete admixture often used in cold weather as an antifreeze. Appendix X1 in ASTM C 270 and BIA generally recommend not using admixtures unless they are known to have no adverse effects. Before approving the use of cold-weather admixtures, verify their acceptability by laboratory testing with mortar mix used.

I. Cold-Weather Admixture: Nonchloride, noncorrosive, accelerating admixture complying with ASTM C 494/C 494M, Type C, and recommended by manufacturer for use in masonry mortar of composition indicated.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Euclid Chemical Company (The); Accelguard 80.

b. Grace Construction Products; W.R. Grace & Co. -- Conn; Morset.

c. Sonneborn Products; Trimix-NCA.

d. <Insert manufacturer's name; product name or designation>.

Retain paragraph below if integral water repellent is used in concrete brick.

J. Water-Repellent Admixture: Liquid water-repellent mortar admixture intended for use with concrete masonry units, containing integral water repellent by same manufacturer.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. ACM Chemistries; RainBloc for Mortar.

b. BASF Aktiengesellschaft; Rheopel Mortar Admixture.

c. Grace Construction Products; W.R. Grace & Co. -- Conn; Dry-Block Mortar Admixture.

d. <Insert manufacturer's name; product name or designation>.

2.5 REINFORCEMENT

Standard in first paragraph below includes requirements for hot-dip galvanized, carbon steel. It is not necessary to specify this material separately.

A. Masonry Joint Reinforcement, General: ASTM A 951/A 951M.

B. Masonry Joint Reinforcement for Veneers Anchored with Seismic Masonry-Veneer Anchors: Single 0.187-inch- (4.76-mm-) diameter, hot-dip galvanized, carbon-steel continuous wire.

2.6 TIES AND ANCHORS

A. Materials: Provide ties and anchors specified in this article that are made from materials that comply with the following unless otherwise indicated:

Retain subparagraphs below only for those materials referenced in subsequent paragraphs.

1. Hot-Dip Galvanized, Carbon-Steel Wire: ASTM A 82/A 82M; with ASTM A 153/A 153M, Class B-2 coating.

2. Steel Sheet, Galvanized after Fabrication: ASTM A 1008/A 1008M, Commercial Steel, with ASTM A 153/A 153M, Class B coating.

B. Wire Ties, General: Unless otherwise indicated, size wire ties to extend at least halfway through veneer but with at least 5/8-inch (16-mm) cover on outside face. Outer ends of wires are bent 90 degrees and extend 2 inches (50 mm) parallel to face of veneer.

C. Adjustable Anchors for Connecting to Structural Steel Framing: Provide anchors that allow vertical or horizontal adjustment but resist tension and compression forces perpendicular to plane of wall.

1. Anchor Section for Welding to Steel Frame: Crimped 1/4-inch- (6.35-mm-) diameter, hot-dip galvanized steel wire.

If retaining last option in subparagraph below, note that the MSJC Code does not allow ties made from mill-galvanized wire for interior use in spaces where humidity exceeds 75 percent.

2. Tie Section: Triangular-shaped wire tie, sized to extend within 1 inch (25 mm) of masonry face, made from [0.187-inch- (4.76-mm-)] [0.25-inch- (6.35-mm-)] diameter, hot-dip galvanized steel wire.

D. Adjustable Anchors for Connecting to Concrete: Provide anchors that allow vertical or horizontal adjustment but resist tension and compression forces perpendicular to plane of wall.

Retain "Connector Section" and "Tie Section" subparagraphs below; otherwise, retain "Corrugated Metal Ties" Subparagraph.

1. Connector Section: Dovetail tabs for inserting into dovetail slots in concrete and attached to tie section; formed from [0.060-inch- (1.52-mm-) thick, steel sheet, galvanized after fabrication] [01.05-inch- (2.66-mm-) thick, steel sheet, galvanized after fabrication].

2. Tie Section: Triangular-shaped wire tie, sized to extend within 1 inch (25 mm) of masonry face, made from [0.187-inch- (4.76-mm-)] [0.25-inch- (6.35-mm-)] diameter, hot-dip galvanized steel wire.

3. Corrugated Metal Ties: Metal strips not less than 7/8 inch (22 mm) wide with corrugations having a wavelength of 0.3 to 0.5 inch (7.6 to 12.7 mm) and an amplitude of 0.06 to 0.10 inch (1.5 to 2.5 mm) made from [0.060-inch- (1.52- mm-) thick, steel sheet, galvanized after fabrication] [0.075-inch- (1.90-mm-) thick, steel sheet, galvanized after fabrication] [01.05-inch- (2.66-mm-) thick, steel sheet, galvanized after fabrication] with dovetail tabs for inserting into dovetail slots in concrete and sized to extend to within 1 inch (25 mm) of masonry face.

E. Adjustable Masonry-Veneer Anchors:

1. General: Provide anchors that allow vertical adjustment but resist tension and compression forces perpendicular to plane of wall, for attachment over sheathing to wood or metal studs, and as follows:

First subparagraph below is from BIA Technical Notes 28B.

a. Structural Performance Characteristics: Capable of withstanding a 100-lbf (445-N) load in both tension and compression without deforming or developing play in excess of 0.05 inch (1.3 mm).

Usually retain first subparagraph below along with acceptable types of anchors.

2. Contractor's Option: Unless otherwise indicated, provide any of the following types of anchors:

3. Screw-Attached, Masonry-Veneer Anchors: Units consisting of a wire tie and a metal anchor section.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Dayton Superior Corporation, Dur-O-Wal Division; [D/A 210 with D/A 700-708] [D/A 213].

2) Heckmann Building Products, Inc; [315-D with 316] [Pos-I-Tie].

3) Hohmann & Barnard, Inc; [DW-10] [DW-10-X] [DW-10HS].

4) Wire-Bond; [1004, Type III] [RJ-711] [SureTie].

5) <Insert manufacturer's name; product name or designation>.

b. Anchor Section: Rib-stiffened, sheet metal plate with screw holes top and bottom, having slotted holes for inserting wire tie.

First subparagraph below describes Heckmann Building Products' "Pos-I-Tie" and Wire-Bond's "SureTie."

c. Anchor Section: Corrosion-resistant, self-drilling, eye-screw designed to receive wire tie. Eye-screw has spacer that seats directly against framing and is same thickness as sheathing and has gasketed, washer head that covers hole in sheathing.

Retain first subparagraph below with either "Anchor Section" Subparagraph above.

d. Fabricate sheet metal anchor sections and other sheet metal parts from [0.075-inch- (1.90-mm-) thick, steel sheet, galvanized after fabrication] [1.05-inch- (2.66-mm-) thick, steel sheet, galvanized after fabrication].

e. Wire Ties: Triangular-, rectangular-, or T-shaped wire ties fabricated from [0.187-inch- (4.76-mm-)] [0.25-inch- (6.35-mm-)] diameter, hot-dip galvanized steel wire.

Anchors in first subparagraph below may be used for other than seismic conditions.

4. Seismic Masonry-Veneer Anchors: Units consisting of a metal anchor section and a connector section designed to engage a continuous wire embedded in the veneer mortar joint.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Dayton Superior Corporation, Dur-O-Wal Division; D/A 213S.

2) Hohmann & Barnard, Inc; DW-10-X-Seismiclip.

3) Wire-Bond; RJ-711 with Wire-Bond clip.

4) <Insert manufacturer's name; product name or designation>.

First two subparagraphs below describe Dayton Superior's "D/A 213S."

b. Anchor Section: Rib-stiffened, sheet metal plate with screw holes top and bottom, having slotted holes for inserting connector section.

c. Connector Section: Rib-stiffened, sheet metal bent plate, sheet metal clip, or wire tie and rigid PVC extrusion designed to engage continuous wire. Size connector to extend at least halfway through veneer but with at least 5/8-inch (16-mm) cover on outside face.

d. Fabricate sheet metal anchor sections and other sheet metal parts from [0.075-inch- (1.90-mm-) thick, steel sheet, galvanized after fabrication] [1.05-inch- (2.66-mm-) thick, steel sheet, galvanized after fabrication].

e. Fabricate wire connector sections from [0.187-inch- (4.76-mm-)] [0.25-inch- (6.35-mm-)] diameter, hot-dip galvanized, carbon-steel wire.

Fasteners in first subparagraph below are for steel studs from 0.033 to 0.112 inch (0.8 to 2.8 mm) thick. "Climaseal" and "Stalgard" finishes by ITW Buildex and Textron comply with coating description.

5. Polymer-Coated, Steel Drill Screws for Steel Studs: ASTM C 954 except manufactured with hex washer head and neoprene or EPDM washer, and with organic polymer coating with salt-spray resistance to red rust of more than 800 hours per ASTM B 117.

6. Stainless-Steel Drill Screws for Steel Studs: ASTM C 954 except manufactured with hex washer head and neoprene or EPDM washer.

2.7 EMBEDDED FLASHING MATERIALS

See Evaluations for discussion of flashing materials before editing this article.

Coordinate first paragraph below with Section 076200 "Sheet Metal Flashing and Trim." Metal through-wall flashing is included in that Section.

A. Metal Flashing: Provide metal flashing complying with [SMACNA's "Architectural Sheet Metal Manual"] [Section 076200 "Sheet Metal Flashing and Trim"] and as follows:

Retain one or both subparagraphs below for use with flexible flashing if required. See Evaluations.

1. Metal Drip Edge: Fabricate from stainless steel. Extend at least 3 inches (76 mm) into wall and 1/2 inch (13 mm) out from wall, with outer edge bent down 30 degrees[ and hemmed].

2. Metal Sealant Stop: Fabricate from stainless steel. Extend at least 3 inches (76 mm) into wall and out to exterior face of wall. At exterior face of wall, bend metal back on itself for 3/4 inch (19 mm) and down into joint 1/4 inch (6 mm) to form a stop for retaining sealant backer rod.

Delete first paragraph below if only metal flashing is allowed. If concealed metal flashing is required at certain locations, indicate those locations on Drawings or revise paragraph.

B. Flexible Flashing: Use[ one of] the following unless otherwise indicated:

First subparagraph below is an example only; revise if other laminated products are required.

1. Copper-Laminated Flashing: [5-oz./sq. ft. (1.5-kg/sq. m)] [7-oz./sq. ft. (2-kg/sq. m)] copper sheet bonded between 2 layers of glass-fiber cloth. Use only where flashing is fully concealed in masonry.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Advanced Building Products Inc; [Copper Fabric Flashing] [Copper Sealtite 2000].

2) Dayton Superior Corporation, Dur-O-Wal Division; Copper Fabric Thru-Wall Flashing.

3) Hohmann & Barnard, Inc; H &amp;amp; B C-Fab Flashing.

4) Phoenix Building Products; Type FCC-Fabric Covered Copper.

5) Sandell Manufacturing Co., Inc; Copper Fabric Flashing.

6) York Manufacturing, Inc; Multi-Flash 500.

7) <Insert manufacturer's name; product name or designation>.

Some rubberized-asphalt flashing products are 0.040 inch (1.0 mm) thick; some are 0.030 inch (0.8 mm) thick; others are 0.025 inch (0.6 mm) thick. BIA recommends 0.030 inch (0.76 mm) as a minimum thickness.

2. Rubberized-Asphalt Flashing: Composite flashing product consisting of a pliable, adhesive rubberized-asphalt compound, bonded to a high-density, cross-laminated polyethylene film to produce an overall thickness of not less than [0.030 inch (0.76 mm)] [0.040 inch (1.02 mm)].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Advanced Building Products Inc; Strip-N-Flash.

2) Carlisle Coatings & Waterproofing Inc; CCW-705-TWF Thru-Wall Flashing.

3) Dayton Superior Corporation, Dur-O-Wal Division; Dur-O-Barrier Thru-Wall Flashing.

4) Fiberweb, Clark Hammerbeam Corp; Aquaflash 500.

5) Grace Construction Products; W.R. Grace & Co. -- Conn; Perm-A-Barrier Wall Flashing.

6) Heckmann Building Products, Inc; No. 82 Rubberized-Asphalt Thru-Wall Flashing..

7) Hohmann & Barnard, Inc; Textroflash.

8) Meadows, W.R.,Inc; Air-Shield Thru-Wall Flashing.

9) Polyguard Products, Inc; [Polyguard 300] [Polyguard 400].

10) Sandell Manufacturing Co., Inc; Sando-Seal.

11) Williams Products, Inc; Everlastic MF-40.

12) <Insert manufacturer's name; product name or designation>.

3. Elastomeric Thermoplastic Flashing: Composite flashing product consisting of a polyester-reinforced ethylene interpolymer alloy.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Du Pont; Thru-Wall Flashing.

2) Hohmann & Barnard, Inc; Flex-Flash.

3) Hyload, Inc; Hyload Cloaked Flashing System.

4) Mortar Net USA, Ltd; Total Flash.

5) <Insert manufacturer's name; product name or designation>.

4. EPDM Flashing: Sheet flashing product made from ethylene-propylene-diene terpolymer, complying with ASTM D 4637, 0.040 inch (1.0 mm) thick.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Carlisle Coatings & Waterproofing Inc; Pre-Kleened EPDM Thru-Wall Flashing.

2) Firestone Specialty Products; FlashGuard.

3) Heckmann Building Products, Inc; No. 81 EPDM Thru-Wall Flashing..

4) Hohmann & Barnard, Inc; Epra-Max EPDM Thru-Wall Flashing.

5) Sandell Manufacturing Co., Inc; EPDM Flashing.

6) <Insert manufacturer's name; product name or designation>.

C. Solder and Sealants for Sheet Metal Flashings:[ As specified in Section 076200 "Sheet Metal Flashing and Trim."]

D. Adhesives, Primers, and Seam Tapes for Flashings: Flashing manufacturer's standard products or products recommended by flashing manufacturer for bonding flashing sheets to each other and to substrates.

2.8 MISCELLANEOUS MASONRY ACCESSORIES

A. Compressible Filler: Premolded filler strips complying with ASTM D 1056, Grade 2A1; compressible up to 35 percent; formulated from [neoprene] [urethane] [or] [PVC].

B. Bond-Breaker Strips: Asphalt-saturated, organic roofing felt complying with ASTM D 226, Type I (No. 15 asphalt felt).

C. Weep/Vent Products: Use[ one of] the following unless otherwise indicated:

Retain one or more of three subparagraphs below; delete all if open-head joints are used for weep holes and vents.

1. Cellular Plastic Weep/Vent: One-piece, flexible extrusion made from UV-resistant polypropylene copolymer, full height and width of head joint and depth 1/8 inch (3 mm) less than depth of outer wythe, in color selected from manufacturer's standard.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Advanced Building Products Inc; Mortar Maze weep vent.

2) BLOK-LOK Limited; Cell-Vent.

3) Dayton Superior Corporation, Dur-O-Wal Division; Cell Vents.

4) Heckmann Building Products, Inc; No. 85 Cell Vent..

5) Hohmann & Barnard, Inc; Quadro-Vent.

6) Wire-Bond; Cell Vent.

7) <Insert manufacturer's name; product name or designation>.

2. Mesh Weep/Vent: Free-draining mesh; made from polyethylene strands, full height and width of head joint and depth 1/8 inch (3 mm) less than depth of outer wythe; in color selected from manufacturer's standard.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Mortar Net USA, Ltd; Mortar Net Weep Vents.

2) <Insert manufacturer's name; product name or designation>.

3. Vinyl Weep Hole/Vent: One-piece, offset, T-shaped units made from flexible PVC, designed to fit into a head joint and consisting of a louvered vertical leg, flexible wings to seal against ends of masonry units, and a top flap to keep mortar out of the head joint; in color selected by Architect.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

a. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1) Hohmann & Barnard, Inc; #343 Louvered Weep Hole.

2) Williams Products, Inc; Williams-Goodco Brick Vent.

3) Wire-Bond; Louvered Weepholes.

4) <Insert manufacturer's name; product name or designation>.

Products described in paragraph below can be used to keep weep holes clear and to keep cavity free draining. See Evaluations.

D. Cavity Drainage Material: Free-draining mesh, made from polymer strands that will not degrade within the wall cavity.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Advanced Building Products Inc; [Mortar Break] [Mortar Break II].

b. CavClear/Archovations, Inc; Stone Mat.

c. Dayton Superior Corporation, Dur-O-Wal Division; Polytite MortarStop.

d. Mortar Net USA, Ltd; Mortar Net.

e. <Insert manufacturer's name; product name or designation>.

Usually retain subparagraph below to ensure competition in bidding. If only one configuration is used, revise subparagraph and combine it with the selected configuration.

2. Provide one of the following configurations:

First subparagraph below describes Mortar Net's "Mortar Net."

a. Strips, full-depth of cavity and 10 inches (250 mm) high, with dovetail shaped notches 7 inches (175 mm) deep.

First subparagraph below describes Advanced Building Products' "Mortar Break" and "Mortar Break II," respectively. Usually retain second option if cavity is 1-1/2 inches (38 mm) or larger.

b. Strips, not less than [3/4 inch (19 mm)] [1-1/2 inches (38 mm)] thick and 10 inches (250 mm) high, with dimpled surface designed to catch mortar droppings and prevent weep holes from clogging with mortar.

c. Sheets or strips full depth of cavity and installed to full height of cavity.

Insert other masonry accessories to suit Project.

2.9 MASONRY CLEANERS

Verify acceptability of cleaner for cleaning masonry with pigmented mortar joints and for kinds of masonry units specified.

A. Proprietary Acidic Cleaner: Manufacturer's standard-strength cleaner designed for removing mortar/grout stains, efflorescence, and other new construction stains from new masonry without discoloring or damaging masonry surfaces. Use product expressly approved for intended use by cleaner manufacturer and manufacturer of masonry units being cleaned.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers. Retain subparagraph and list of manufacturers below. See Section 016000 "Product Requirements."

1. Manufacturers: Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. Diedrich Technologies, Inc.

b. EaCo Chem, Inc.

c. PROSOCO, Inc.

d. <Insert manufacturer's name>.

2.10 MORTAR MIXES

A. General: Do not use admixtures, including pigments, air-entraining agents, accelerators, retarders, water-repellent agents, antifreeze compounds, or other admixtures unless otherwise indicated.

1. Do not use calcium chloride in mortar.

2. Use [portland cement-lime] [masonry cement] [or] [mortar cement] mortar unless otherwise indicated.

3. Add cold-weather admixture (if used) at same rate for all mortar that will be exposed to view, regardless of weather conditions, to ensure that mortar color is consistent.

B. Preblended, Dry Mortar Mix: Furnish dry mortar ingredients in form of a preblended mix. Measure quantities by weight to ensure accurate proportions, and thoroughly blend ingredients before delivering to Project site.

C. Mortar for Unit Masonry: Comply with ASTM C 270, Proportion Specification. Provide Type N unless another type is indicated.

D. Pigmented Mortar: Use colored cement product[ or select and proportion pigments with other ingredients to produce color required. Do not add pigments to colored cement products].

Retain three subparagraphs below if retaining option in last paragraph above. Percentages in first two subparagraphs below are for pigments containing only metallic oxides. If pigments containing carbon black are used, carbon black must be limited to 2 percent of portland cement by weight or 1 percent of masonry cement or mortar cement.

1. Pigments shall not exceed 10 percent of portland cement by weight.

2. Pigments shall not exceed 5 percent of masonry cement by weight.

3. Application: Use pigmented mortar for exposed mortar joints.

E. Colored-Aggregate Mortar: Produce required mortar color by using colored aggregates and natural color or white cement as necessary to produce required mortar color.

Insert materials and proportions used for sample in first subparagraph below if known.

1. Mix to match Architect's sample.

2. Application: Use colored aggregate mortar for exposed mortar joints.

PART 3 -  EXECUTION

3.1 INSTALLATION, GENERAL

A. Use full-size units without cutting if possible. If cutting is required to provide a continuous pattern or to fit adjoining construction, cut units with motor-driven saws; provide clean, sharp, unchipped edges. Allow units to dry before laying unless wetting of units is specified. Install cut units with cut surfaces and, where possible, cut edges concealed.

B. Select and arrange units for exposed unit masonry to produce a uniform blend of colors and textures.

Retain paragraph below for high-suction brick. A simple test to determine if wetting is required consists of drawing a circle the size of a quarter on a brick and placing 20 drops of water in the circle; if water is absorbed within 1-1/2 minutes, the brick requires wetting.

C. Wetting of Brick: Wet brick before laying if initial rate of absorption exceeds 30 g/30 sq. in. (30 g/194 sq. cm) per minute when tested per ASTM C 67. Allow units to absorb water so they are damp but not wet at time of laying.

3.2 TOLERANCES

A. Dimensions and Locations of Elements:

1. For dimensions in cross section or elevation do not vary by more than plus 1/2 inch (12 mm) or minus 1/4 inch (6 mm).

2. For location of elements in plan do not vary from that indicated by more than plus or minus 1/2 inch (12 mm).

3. For location of elements in elevation do not vary from that indicated by more than plus or minus 1/4 inch (6 mm) in a story height or 1/2 inch (12 mm) total.

B. Lines and Levels:

1. For bed joints and top surfaces of bearing walls do not vary from level by more than 1/4 inch in 10 feet (6 mm in 3 m), or 1/2 inch (12 mm) maximum.

2. For conspicuous horizontal lines, such as lintels, sills, parapets, and reveals, do not vary from level by more than 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2 inch (12 mm) maximum.

3. For vertical lines and surfaces do not vary from plumb by more than 1/4 inch in 10 feet (6 mm in 3 m), 3/8 inch in 20 feet (9 mm in 6 m), or 1/2 inch (12 mm) maximum.

4. For conspicuous vertical lines, such as external corners, door jambs, reveals, and expansion and control joints, do not vary from plumb by more than 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2 inch (12 mm) maximum.

5. For lines and surfaces do not vary from straight by more than 1/4 inch in 10 feet (6 mm in 3 m), 3/8 inch in 20 feet (9 mm in 6 m), or 1/2 inch (12 mm) maximum.

C. Joints:

If Type FBS Rough brick or Type FBA brick is used, revise tolerances in two subparagraphs below to allow for variation in brick size. Consider restricting tolerances if Type FBX brick is used.

1. For bed joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm), with a maximum thickness limited to 1/2 inch (12 mm); do not vary from bed-joint thickness of adjacent courses by more than 1/8 inch (3 mm).

2. For exposed head joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm).[ Do not vary from adjacent bed-joint and head-joint thicknesses by more than 1/8 inch (3 mm).]

3.3 LAYING MASONRY WALLS

A. Lay out walls in advance for accurate spacing of surface bond patterns with uniform joint thicknesses and for accurate location of openings, movement-type joints, returns, and offsets. Avoid using less-than-half-size units, particularly at corners, jambs, and, where possible, at other locations.

Pattern is usually running bond. If other bond patterns are required, specify in first paragraph below or indicate on Drawings.

B. Bond Pattern for Exposed Masonry: Unless otherwise indicated, lay exposed masonry in running bond; do not use units with less than nominal 4-inch (100-mm) horizontal face dimensions at corners or jambs.

C. Built-in Work: As construction progresses, build in items specified in this and other Sections. Fill in solidly with masonry around built-in items.

Revise paragraph below if flexible perimeter joint or thermal break is required.

D. Fill space between steel frames and masonry solidly with mortar unless otherwise indicated.

3.4 MORTAR BEDDING AND JOINTING

A. Lay hollow brick as follows:

1. With face shells fully bedded in mortar and with head joints of depth equal to bed joints.

2. With entire units, including areas under cells, fully bedded in mortar at starting course on footings.

B. Lay solid masonry units with completely filled bed and head joints; butter ends with sufficient mortar to fill head joints and shove into place. Do not deeply furrow bed joints or slush head joints.

If another joint profile is used, revise paragraph below or show on Drawings.

C. Tool exposed joints slightly concave when thumbprint hard, using a jointer larger than joint thickness unless otherwise indicated.

3.5 ANCHORING MASONRY TO STRUCTURAL STEEL AND CONCRETE

A. Anchor masonry to structural steel and concrete where masonry abuts or faces structural steel or concrete to comply with the following:

1. Provide an open space not less than [1/2 inch (13 mm)] [1 inch (25 mm)] [2 inches (50 mm)] wide between masonry and structural steel or concrete unless otherwise indicated. Keep open space free of mortar and other rigid materials.

2. Anchor masonry with anchors embedded in masonry joints and attached to structure.

3. Space anchors as indicated, but not more than 24 inches (610 mm) o.c. vertically and 36 inches (915 mm) o.c. horizontally.

3.6 ANCHORING MASONRY VENEERS

A. Anchor masonry veneers to [wall framing] [and] [concrete backup] with[ seismic] masonry-veneer anchors to comply with the following requirements:

1. Fasten [screw-attached] [and] [seismic] anchors [through sheathing to wall framing] [and] [to concrete backup] with metal fasteners of type indicated. Use two fasteners unless anchor design only uses one fastener.

BIA Technical Notes 28B recommends 2 inches (50 mm) of air space. Wider air spaces require closer tie spacing.

2. Embed [tie sections] [connector sections and continuous wire] in masonry joints. Provide not less than 2 inches (50 mm) of air space between back of masonry veneer and face of sheathing.

3. Locate anchor sections to allow maximum vertical differential movement of ties up and down.

Subparagraph below is based on the MSJC Code. Closer spacing is for adjustable 2-piece anchors, wire anchors 0.148 inch (3.8 mm) in diameter, and corrugated sheet metal anchors; wider spacing is for all other anchors.

4. Space anchors as indicated, but not more than 16 inches (406 mm) o.c. vertically and [32 inches (813 mm)] [24 inches (610 mm)] o.c. horizontally with not less than 1 anchor for each [3.5 sq. ft. (0.33 sq. m)] [2.67 sq. ft. (0.25 sq. m)] of wall area. Install additional anchors within 12 inches (305 mm) of openings and at intervals, not exceeding 36 inches (914 mm), around perimeter.

3.7 FLASHING, WEEP HOLES, CAVITY DRAINAGE, AND VENTS

Retain option in first paragraph below if wall is designed on rain-screen principle with vents acting to equalize air-pressure differential between cavity and exterior. Indicate spacing of vents and blocking on Drawings. See Evaluations.

A. General: Install embedded flashing and weep holes in masonry at shelf angles, lintels, ledges, other obstructions to downward flow of water in wall, and where indicated.[ Install vents at shelf angles, ledges, and other obstructions to upward flow of air in cavities, and where indicated.]

B. Install flashing as follows unless otherwise indicated:

1. Prepare masonry surfaces so they are smooth and free from projections that could puncture flashing. Where flashing is within mortar joint, place through-wall flashing on sloping bed of mortar and cover with mortar. Before covering with mortar, seal penetrations in flashing with adhesive, sealant, or tape as recommended by flashing manufacturer.

2. At lintels and shelf angles, extend flashing a minimum of 6 inches (150 mm) into masonry at each end. At heads and sills, extend flashing 6 inches (150 mm) at ends and turn up not less than 2 inches (50 mm) to form end dams.

3. Install metal drip edges beneath flexible flashing at exterior face of wall. Stop flexible flashing 1/2 inch (13 mm) back from outside face of wall and adhere flexible flashing to top of metal drip edge.

4. Install metal flashing termination beneath flexible flashing at exterior face of wall. Stop flexible flashing 1/2 inch (13 mm) back from outside face of wall and adhere flexible flashing to top of metal flashing termination.

C. Install weep holes in head joints in exterior wythes of first course of masonry immediately above embedded flashing and as follows:

1. Use [specified weep/vent products] [or] [open head joints] to form weep holes.

2. Space weep holes 24 inches (600 mm) o.c. unless otherwise indicated.

D. Place cavity drainage material in cavities to comply with configuration requirements for cavity drainage material in "Miscellaneous Masonry Accessories" Article.

Retain paragraph below if wall is designed on rain-screen principle with vents acting to equalize air-pressure differential between cavity and exterior. Indicate spacing of vents and blocking on Drawings. See Evaluations.

E. Install vents in head joints in exterior wythes at spacing indicated. Use [specified weep/vent products] [or] [open head joints] to form vents.

1. Close cavities off vertically and horizontally with blocking in manner indicated. Install through-wall flashing and weep holes above horizontal blocking.

3.8 FIELD QUALITY CONTROL

A. Testing and Inspecting: Owner will engage special inspectors to perform tests and inspections and prepare reports. Allow inspectors access to scaffolding and work areas, as needed to perform tests and inspections. Retesting of materials that fail to meet specified requirements shall be done at Contractor's expense.

B. Inspections: Level 1 special inspections according to the "International Building Code."

Requirement in subparagraph below is based on Level 1 special inspection requirements in IBC and Level B quality assurance requirements in MSJC Code. Revise to suit occupancy category.

1. Begin masonry construction only after inspectors have verified proportions of site-prepared mortar.

MSJC Code requires verification of compliance of proportions for site-prepared mortar. Test in paragraph below verifies ratio of aggregate to cementitious materials but does not indicate what cementitious materials are used. Observation of actual mortar mixing procedures as part of inspection program would provide better quality control.

C. Mortar Aggregate Ratio Test (Proportion Specification): For each mix provided, according to ASTM C 780.

3.9 CLEANING

A. In-Progress Cleaning: Clean unit masonry as work progresses by dry brushing to remove mortar fins and smears before tooling joints.

B. Final Cleaning: After mortar is thoroughly set and cured, clean exposed masonry as follows:

1. Test cleaning methods on sample wall panel; leave one-half of panel uncleaned for comparison purposes

Delete first two subparagraphs below if cleaners are not specified in Part 2 or if cleaners are not allowed.

2. Protect adjacent surfaces from contact with cleaner.

3. Wet wall surfaces with water before applying cleaners; remove cleaners promptly by rinsing surfaces thoroughly with clear water.

4. Clean brick by bucket-and-brush hand-cleaning method described in "BIA Technical Notes 20."

Retain last subparagraph above or first subparagraph below. Coordinate with products retained in Part 2. If high-pressure water cleaning or other methods are acceptable, delete or revise subparagraph below and insert applicable requirements.

5. Clean masonry with a proprietary acidic cleaner applied according to manufacturer's written instructions.

6. Clean concrete masonry by cleaning method indicated in NCMA TEK 8-2A applicable to type of stain on exposed surfaces.

3.10 MASONRY WASTE DISPOSAL

Retain first paragraph below if clean masonry waste can be used as fill in footing trenches, etc. This diverts some material from waste stream, conserving landfill space and energy required to haul waste away.

A. Waste Disposal as Fill Material: Dispose of clean masonry waste, including excess or soil-contaminated sand, waste mortar, and broken masonry units, by crushing and mixing with fill material as fill is placed.

1. Do not dispose of masonry waste as fill within 18 inches (450 mm) of finished grade.

B. Excess Masonry Waste: Remove excess clean masonry waste that cannot be used as fill, as described above, and other masonry waste, and legally dispose of off Owner's property.

END OF SECTION 042113

	BRICK MASONRY
	042113 - 1



