Copyright 2010 AIA
MasterSpec Professional
02/10

Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 047200 - CAST STONE MASONRY
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Cast stone trim.

2. Cast stone steps.

3. Cast stone bollards.

4. Cast stone benches.

5. Cast stone curbing.

1.2 ACTION SUBMITTALS

Usually retain first paragraph below for cast stone items that are manufacturer's stock units.

A. Product Data: For each type of product indicated. Include dimensions and finishes.

B. LEED Submittals:

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools; coordinate with requirements selected in Part 2 for materials.

1. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials indicating location and distance from Project of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating cost for each regional material and the fraction by weight that is considered regional.

Usually retain first paragraph below for custom-made units.

C. Shop Drawings: Show fabrication and installation details for cast stone units. Include dimensions, details of reinforcement and anchorages if any, and indication of finished faces.

D. Samples:

1. For each color and texture of cast stone required.

Delete subparagraph below if installation of cast stone is specified in Section 042000 "Unit Masonry."

2. For colored mortar.

1.3 INFORMATIONAL SUBMITTALS

Usually retain first paragraph below unless manufacturers are limited to those known to produce only acceptable products. Coordinate with qualification requirements in Section 014000 "Quality Requirements" and as supplemented in "Quality Assurance" Article.

A. Qualification Data: For manufacturer.

Consider deleting paragraph below if only a few units are required or if tests are considered unnecessary. Delete option if resistance to freezing and thawing is not required. Some consider testing for freeze-thaw resistance unnecessary because compressive-strength and water-absorption requirements in ASTM C 1364 tend to ensure a durable product. Freeze-thaw testing is expensive, but manufacturers should have previously tested their typical products.

B. Material Test Reports: For each mix required to produce cast stone, based on testing according to ASTM C 1364[, including test for resistance to freezing and thawing].

1.4 QUALITY ASSURANCE

The three certification programs in paragraph below are not all the same.

A. Manufacturer Qualifications: A qualified manufacturer of cast stone units similar to those indicated for this Project, that has sufficient production capacity to manufacture required units, and is a plant certified by [the Cast Stone Institute] [the Architectural Precast Association] [or] [the Precast/Prestressed Concrete Institute for Group A, Category AT].

PART 2 -  PRODUCTS

2.1 CAST STONE UNITS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers. Retain first paragraph and list of manufacturers in this article. See Section 016000 "Product Requirements."

A. Manufacturers: Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

The Cast Stone Institute and the Architectural Precast Association have lists of manufacturers on their Web sites.

1. <Insert, in separate subparagraphs, manufacturers' names>.

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply.

B. Regional Materials: Cast stone units shall be manufactured within 500 miles (800 km) of Project site from aggregates[ and cement] that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

Revise first paragraph below if only one method is considered satisfactory. See Evaluations.

C. Provide cast stone units complying with ASTM C 1364 using either the vibrant dry tamp or wet-cast method.

Delete first subparagraph below if freeze-thaw resistance is not required. Some consider testing for freeze-thaw resistance unnecessary because compressive-strength and water-absorption requirements in ASTM C 1364 tend to ensure a durable product. Freeze-thaw testing is expensive, but manufacturers should have previously tested their typical products.

1. Provide units that are resistant to freezing and thawing as determined by laboratory testing according to ASTM C 666/C 666M, Procedure A, as modified by ASTM C 1364.

2. Slope exposed horizontal surfaces 1:12 to drain unless otherwise indicated.

3. Provide raised fillets at backs of sills and at ends indicated to be built into jambs.

4. Provide drips on projecting elements unless otherwise indicated.

D. Cure units as follows:

Two subparagraphs below are based on recommendations of the Cast Stone Institute.

1. Cure units in enclosed moist curing room at 95 to 100 percent relative humidity and temperature of 100 deg F (38 deg C) for 12 hours or 70 deg F (21 deg C) for 16 hours.

2. Keep units damp and continue curing to comply with one of the following:

a. No fewer than five days at mean daily temperature of 70 deg F (21 deg C) or above.

b. No fewer than six days at mean daily temperature of 60 deg F (16 deg C) or above.

c. No fewer than seven days at mean daily temperature of 50 deg F (10 deg C) or above.

d. No fewer than eight days at mean daily temperature of 45 deg F (7 deg C) or above.

Method in first paragraph below is standard for finishing cast stone units; revise if another method is required.

E. Acid etch units after curing to remove cement film from surfaces to be exposed to view.

Exact matches of existing units may be impossible. Creating an architect's sample with known ingredients that is an acceptable approximate match, rather than simply requiring the manufacturer to match existing units and hoping for the best, may help alleviate disputes.

F. Colors and Textures: [Match Architect's samples] [Match existing units] [As selected by Architect from manufacturer's full range].

2.2 ACCESSORIES

A. Anchors: Type and size indicated, fabricated from [Type 304 stainless steel complying with ASTM A 240/A 240M, ASTM A 276, or ASTM A 666] [steel complying with ASTM A 36/A 36M, and hot-dip galvanized to comply with ASTM A 123/A 123M].

B. Dowels: 1/2-inch- (12-mm-) diameter, round bars, fabricated from [Type 304 stainless steel complying with ASTM A 240/A 240M, ASTM A 276, or ASTM A 666] [steel complying with ASTM A 36/A 36M, and hot-dip galvanized to comply with ASTM A 123/A 123M].

C. Proprietary Acidic Cleaner: Manufacturer's standard-strength cleaner complying with requirements in Section 042000 "Unit Masonry," and expressly approved for intended use by cast stone manufacturer and cleaner manufacturer.

2.3 MORTAR

A. Comply with requirements in Section 042000 "Unit Masonry" for mortar materials and mixes.

Retain one mortar type in each of first two subparagraphs below. The Cast Stone Institute recommends Type N; other types may be required by special circumstances.

1. For setting mortar, use [Type S] [Type N].

2. For pointing mortar, use [Type N] [Type O].

3. Pigmented Mortar: Use colored cement product[ or select and proportion pigments with other ingredients to produce color required. Do not add pigments to colored cement products].

Retain "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5; before retaining, verify availability of materials that comply.

B. Regional Materials: Aggregate for mortar [, cement, and lime] shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

2.4 SOURCE QUALITY CONTROL

Consider deleting this article if only a few units are required or if testing is considered unnecessary. Revise if Owner employs testing agency.

A. Engage a qualified independent testing agency to sample and test cast stone units according to ASTM C 1364.

Delete subparagraph below if freeze-thaw resistance is not required. Some consider testing for freeze-thaw resistance unnecessary because compressive-strength and water-absorption requirements in ASTM C 1364 tend to ensure a durable product. Freeze-thaw testing is expensive.

1. Include one test for resistance to freezing and thawing.

PART 3 -  EXECUTION

3.1 SETTING CAST STONE IN MORTAR

Delete first paragraph below if considered unnecessary or if Section 042000 "Unit Masonry" is not used.

A. Install cast stone units to comply with requirements in Section 042000 "Unit Masonry."

B. Set units in full bed of mortar with full head joints unless otherwise indicated.

Retain applicable subparagraphs below; delete those not applicable.

1. Fill dowel holes and anchor slots with mortar.

2. Fill collar joints solid as units are set.

3. Build concealed flashing into mortar joints as units are set.

4. Keep head joints in coping and other units with exposed horizontal surfaces open to receive sealant.

5. Keep joints at shelf angles open to receive sealant.

Delete first two paragraphs below if cast stone is set in mortar without pointing.

C. Rake out joints for pointing with mortar to depths of not less than 3/4 inch (19 mm). Rake joints to uniform depths with square bottoms and clean sides. Scrub faces of units to remove excess mortar as joints are raked.

D. Point mortar joints by placing and compacting mortar in layers not greater than 3/8 inch (10 mm). Compact each layer thoroughly and allow it to become thumbprint hard before applying next layer.

Revise first paragraph below if another joint profile is required.

E. Tool exposed joints slightly concave when thumbprint hard, using a jointer larger than joint thickness unless otherwise indicated.

F. Provide sealant joints at copings and other horizontal surfaces, at expansion, control, and pressure-relieving joints, and at locations indicated.

1. Keep joints free of mortar and other rigid materials.

2. Prepare and apply sealant of type and at locations indicated to comply with applicable requirements in Section 079200 "Joint Sealants."

3.2 SETTING ANCHORED CAST STONE WITH SEALANT-FILLED JOINTS

A. Set units accurately in locations indicated with edges and faces aligned.

1. Install anchors, supports, fasteners, and other attachments to secure units in place.

2. Shim and adjust anchors, supports, and accessories.

B. Fill anchor holes with sealant.

1. Where dowel holes occur at pressure-relieving joints, provide compressible material at ends of dowels.

C. Set cast stone supported on clip or continuous angles on resilient setting shims. Hold shims back from face of cast stone a distance at least equal to width of joint.

D. Keep joints free of mortar and other rigid materials. Remove temporary shims and spacers from joints after anchors and supports are secured in place and cast stone units are anchored.

E. Prepare and apply sealant of type and at locations indicated to comply with applicable requirements in Section 079200 "Joint Sealants."

3.3 INSTALLATION TOLERANCES

Delete this article if tolerances in Section 042000 "Unit Masonry" govern. Tolerances in paragraphs below are based on those included in Section 042000 "Unit Masonry." If retaining, revise to suit Project.

A. Variation from Plumb: Do not exceed 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2 inch (12 mm) maximum.

B. Variation from Level: Do not exceed 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2 inch (12 mm) maximum.

C. Variation in Joint Width: Do not vary joint thickness more than 1/8 inch in 36 inches (3 mm in 900 mm) or one-fourth of nominal joint width, whichever is less.

D. Variation in Plane between Adjacent Surfaces (Lipping): Do not vary from flush alignment with adjacent units or adjacent surfaces indicated to be flush with units by more than 1/16 inch (1.5 mm), except where variation is due to warpage of units within tolerances specified.

3.4 ADJUSTING AND CLEANING

A. Remove and replace stained and otherwise damaged units and units not matching approved Samples. Cast stone may be repaired if methods and results are approved by Architect.

B. Replace units in a manner that results in cast stone matching approved Samples, complying with other requirements, and showing no evidence of replacement.

C. In-Progress Cleaning: Clean cast stone as work progresses.

1. Remove mortar fins and smears before tooling joints.

2. Remove excess sealant immediately, including spills, smears, and spatter.

D. Final Cleaning: After mortar is thoroughly set and cured, clean exposed cast stone to comply with requirements in Section 042000 "Unit Masonry."

END OF SECTION 047200

	CAST STONE MASONRY
	047200 - 1



