Copyright 2011 AIA
MasterSpec Professional
02/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 053100 - STEEL DECKING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Roof deck.

2. Composite floor deck.

3. Noncomposite form deck.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of deck, accessory, and product indicated.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Laboratory Test Reports for Credit EQ 4" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit EQ 4: For primers, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings:

1. Include layout and types of deck panels, anchorage details, reinforcing channels, pans, cut deck openings, special jointing, accessories, and attachments to other construction.

1.3 INFORMATIONAL SUBMITTALS

Retain "Welding certificates" Paragraph below if retaining "Welding Qualifications" Paragraph in "Quality Assurance" Article.

A. Welding certificates.

B. Product certificates.

C. Evaluation reports.

Retain "Field quality-control reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting.

D. Field quality-control reports.

1.4 QUALITY ASSURANCE

Retain "Testing Agency Qualifications" Paragraph below if Contractor selects testing agency or if Contractor is required to provide services of a qualified testing agency in "Field Quality Control" Article. Qualification requirements are in addition to those specified in Section 014000 "Quality Requirements."

A. Testing Agency Qualifications: Qualified according to ASTM E 329 for testing indicated.

Retain "Welding Qualifications" Paragraph below if shop or field welding is required. If retaining, also retain "Welding certificates" Paragraph in "Informational Submittals" Article. AWS states that welding qualifications remain in effect indefinitely unless welding personnel have not welded for more than six months or there is a specific reason to question their ability.

B. Welding Qualifications: Qualify procedures and personnel according to AWS D1.3, "Structural Welding Code - Sheet Steel."

1.5 DELIVERY, STORAGE, AND HANDLING

A. Protect steel deck from corrosion, deformation, and other damage during delivery, storage, and handling.

B. Stack steel deck on platforms or pallets and slope to provide drainage. Protect with a waterproof covering and ventilate to avoid condensation.

PART 2 -  PRODUCTS

2.1 PERFORMANCE REQUIREMENTS

A. AISI Specifications: Comply with calculated structural characteristics of steel deck according to AISI's "North American Specification for the Design of Cold-Formed Steel Structural Members."

Retain "Recycled Content of Steel Products" Paragraph below to specify recycled content if applying for LEED Credit MR 4. USGBC allows a default value of 25 percent to be used for steel, without documentation; higher percentages can be claimed if they are supported by appropriate documentation. The Steel Recycling Institute indicates that steel sheet typically has 23 percent postconsumer recycled content and 1.5 percent preconsumer recycled content.

B. Recycled Content of Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.

Retain "Low-Emitting Materials" Paragraph below if shop-primed deck is used and if required for LEED for Schools.

C. Low-Emitting Materials: Paints and coatings shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

2.2 ROOF DECK

Retain this article if roof deck is required.

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

1. ASC Profiles, Inc.; a Blue Scope Steel company.

2. Canam United States; Canam Group Inc.

3. CMC Joist & Deck.

4. Consolidated Systems, Inc.; Metal Dek Group.

5. Cordeck.

6. DACS, Inc.

7. Epic Metals Corporation.

8. Marlyn Steel Decks, Inc.

9. New Millennium Building Systems, LLC.

10. Nucor Corp.; Vulcraft Group.

11. Roof Deck, Inc.

12. Valley Joist; Subsidiary of EBSCO Industries, Inc.

13. Verco Manufacturing Co.

14. Wheeling Corrugating Company; Div. of Wheeling-Pittsburgh Steel Corporation.

15. <Insert manufacturer's name>.

B. Roof Deck: Fabricate panels, without top-flange stiffening grooves, to comply with "SDI Specifications and Commentary for Steel Roof Deck," in SDI Publication No. 31, and with the following:

Retain one or more of the steel-sheet subparagraphs below to suit Project.

1. Prime-Painted Steel Sheet: ASTM A 1008/A 1008M, Structural Steel (SS), [Grade 33 (230)] [Grade 40 (275)] [Grade 80 (550)] minimum, shop primed with manufacturer's standard baked-on, rust-inhibitive primer.

a. Color: [Manufacturer's standard] [Gray] [White] [Gray top surface with white underside].

2. Galvanized-Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), [Grade 33 (230)] [Grade 40 (275)] [Grade 80 (550)], [G60 (Z180)] [G90 (Z275)] zinc coating.

3. Galvanized and Shop-Primed Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), [Grade 33 (230)] [Grade 40 (275)] [Grade 80 (550)], G60 (Z180) zinc coating; cleaned, pretreated, and primed with manufacturer's standard baked-on, rust-inhibitive primer.

a. Color: [Manufacturer's standard] [Gray] [White] [Gray top surface with white underside].

4. Deck Profile: [As indicated] [Type NR, narrow rib] [Type IR, intermediate rib] [Type WR, wide rib] [Type 3DR, deep rib] [Long span].

5. Profile Depth: [As indicated] [1-1/2 inches (38 mm)] [2 inches (51 mm)] [3 inches (76 mm)] [4-1/2 inches (114 mm)] [6 inches (152 mm)] [7-1/2 inches (190 mm)].

6. Design Uncoated-Steel Thickness: [As indicated] [0.0295 inch (0.75 mm)] [0.0358 inch (0.91 mm)] [0.0474 inch (1.20 mm)] [0.0598 inch (1.52 mm)] [0.0747 inch (1.90 mm)].

2.3 COMPOSITE FLOOR DECK

Retain this article if composite floor deck is required. Insert minimum section properties here or indicate on Drawings.

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

1. ASC Profiles, Inc.; a Blue Scope Steel company.

2. Canam United States; Canam Group Inc.

3. CMC Joist & Deck.

4. Consolidated Systems, Inc.; Metal Dek Group.

5. Cordeck.

6. DACS, Inc.

7. Epic Metals Corporation.

8. Marlyn Steel Decks, Inc.

9. New Millennium Building Systems, LLC.

10. Nucor Corp.; Vulcraft Group.

11. Roof Deck, Inc.

12. Verco Manufacturing Co.

13. Wheeling Corrugating Company; Div. of Wheeling-Pittsburgh Steel Corporation.

14. <Insert manufacturer's name>.

B. Composite Floor Deck: Fabricate panels, with integrally embossed or raised pattern ribs and interlocking side laps, to comply with "SDI Specifications and Commentary for Composite Steel Floor Deck," in SDI Publication No. 31, with the minimum section properties indicated, and with the following:

Retain one or more of the steel-sheet subparagraphs below to suit Project.

1. Prime-Painted Steel Sheet: ASTM A 1008/A 1008M, Structural Steel (SS), [Grade 33 (230)] [Grade 40 (275)] [Grade 80 (550)] minimum, with top surface phosphatized and unpainted and underside surface shop primed with manufacturers' standard [gray] [or] [white] baked-on, rust-inhibitive primer.

Retain either "Galvanized-Steel Sheet" or "Galvanized and Shop-Primed Steel Sheet" Subparagraph below for galvanized-steel sheet. A lightweight coating, G30 (Z90), is the minimum recommended by SDI for composite deck because it is the positive bending reinforcement for slab and must last the life of the structure.

2. Galvanized-Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), Grade 33 (230), [G30 (Z90)] [G60 (Z180)] [G90 (Z275)] zinc coating.

3. Galvanized and Shop-Primed Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), Grade 33 (230), [G30 (Z90)] [G60 (Z180)] zinc coating; with unpainted top surface and cleaned and pretreated bottom surface primed with manufacturer's standard [gray] [white] baked-on, rust-inhibitive primer.

4. Profile Depth: [1-1/2 inches (38 mm)] [2 inches (51 mm)] [3 inches (76 mm)] [As indicated].

5. Design Uncoated-Steel Thickness: [0.0295 inch (0.75 mm)] [0.0358 inch (0.91 mm)] [0.0474 inch (1.20 mm)] [0.0598 inch (1.52 mm)].

2.4 NONCOMPOSITE FORM DECK

Retain this article if noncomposite form deck is required. Form deck may be used as roof deck, floor deck, or both. Insert minimum section properties here or indicate on Drawings.

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

1. ASC Profiles, Inc.; a Blue Scope Steel company.

2. Canam United States; Canam Group Inc.

3. CMC Joist & Deck.

4. Consolidated Systems, Inc.; Metal Dek Group.

5. Cordeck.

6. DACS, Inc.

7. Marlyn Steel Decks, Inc.

8. New Millennium Building Systems, LLC.

9. Nucor Corp.; Vulcraft Group.

10. Roof Deck, Inc.

11. Valley Joist; Subsidiary of EBSCO Industries, Inc.

12. Verco Manufacturing Co.

13. Wheeling Corrugating Company; Div. of Wheeling-Pittsburgh Steel Corporation.

14. <Insert manufacturer's name>.

B. Noncomposite Form Deck: Fabricate ribbed-steel-sheet noncomposite form-deck panels to comply with "SDI Specifications and Commentary for Noncomposite Steel Form Deck," in SDI Publication No. 31, with the minimum section properties indicated, and with the following:

Retain one or more of the steel-sheet subparagraphs below to suit Project.

1. Uncoated Steel Sheet: ASTM A 1008/A 1008M, Structural Steel (SS), [Grade 33 (230)] [Grade 40 (275)] [Grade 80 (550)] minimum.

2. Prime-Painted Steel Sheet: ASTM A 1008/A 1008M, Structural Steel (SS), [Grade 33 (230)] [Grade 40 (275)] [Grade 80 (550)] minimum, with[ top and] underside surface shop primed with manufacturer's standard baked-on, rust-inhibitive primer.

a. Color: [Manufacturer's standard] [Gray] [White] [Gray top surface with white underside].

Retain either "Galvanized-Steel Sheet" or "Galvanized and Shop-Primed Steel Sheet" Subparagraph below for galvanized-steel sheet. A lightweight coating, G30 (Z90), is the minimum recommended by SDI for noncomposite form deck.

3. Galvanized-Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), [Grade 33 (230)] [Grade 40 (275)] [Grade 80 (550)], [G30 (Z90)] [G60 (Z180)] [G90 (Z275)] zinc coating.

4. Galvanized and Shop-Primed Steel Sheet: ASTM A 653/A 653M, Structural Steel (SS), [Grade 33 (230)] [Grade 80 (550)], G60 (Z180) zinc coating; cleaned, pretreated, and primed with manufacturer's standard baked-on, rust-inhibitive primer.

a. Color: [Manufacturer's standard] [Gray] [White] [Gray top surface with white underside].

5. Profile Depth: [9/16 inch (14 mm)] [15/16 inch (24 mm)] [1-5/16 inches (33 mm)] [1-1/2 inches (38 mm)].

6. Design Uncoated-Steel Thickness: [0.0149 inch (0.38 mm)] [0.0179 inch (0.45 mm)] [0.0239 inch (0.61 mm)] [0.0295 inch (0.75 mm)] [0.0358 inch (0.91 mm)] [0.0474 inch (1.20 mm)] [0.0598 inch (1.52 mm)].

2.5 ACCESSORIES

A. General: Provide manufacturer's standard accessory materials for deck that comply with requirements indicated.

B. Mechanical Fasteners: Corrosion-resistant, low-velocity, power-actuated or pneumatically driven carbon-steel fasteners; or self-drilling, self-threading screws.

C. Side-Lap Fasteners: Corrosion-resistant, hexagonal washer head; self-drilling, carbon-steel screws, No. 10 (4.8-mm) minimum diameter.

D. Flexible Closure Strips: Vulcanized, closed-cell, synthetic rubber.

E. Miscellaneous Sheet Metal Deck Accessories: Steel sheet, minimum yield strength of 33,000 psi (230 MPa), not less than 0.0359-inch (0.91-mm) design uncoated thickness, of same material and finish as deck; of profile indicated or required for application.

F. Flat Sump Plates: Single-piece steel sheet, 0.0747 inch (1.90 mm) thick, of same material and finish as deck. For drains, cut holes in the field.

G. Galvanizing Repair Paint: [ASTM A 780] [SSPC-Paint 20 or MIL-P-21035B, with dry film containing a minimum of 94 percent zinc dust by weight].

H. Repair Paint: Manufacturer's standard rust-inhibitive primer of same color as primer.

PART 3 -  EXECUTION

3.1 INSTALLATION, GENERAL

A. Install deck panels and accessories according to applicable specifications and commentary in SDI Publication No. 31, manufacturer's written instructions, and requirements in this Section.

B. Place deck panels on supporting frame and adjust to final position with ends accurately aligned and bearing on supporting frame before being permanently fastened. Do not stretch or contract side-lap interlocks.

C. Place deck panels flat and square and fasten to supporting frame without warp or deflection.

D. Cut and neatly fit deck panels and accessories around openings and other work projecting through or adjacent to deck.

Coordinate reinforcing requirements of openings in first paragraph below with applicable Sections.

E. Provide additional reinforcement and closure pieces at openings as required for strength, continuity of deck, and support of other work.

F. Comply with AWS requirements and procedures for manual shielded metal arc welding, appearance and quality of welds, and methods used for correcting welding work.

Retain first paragraph below if mechanical fastening is permitted.

G. Mechanical fasteners may be used in lieu of welding to fasten deck. Locate mechanical fasteners and install according to deck manufacturer's written instructions.

H. Roof Sump Pans and Sump Plates: Install over openings provided in roof deck and [weld] [mechanically fasten] flanges to top of deck. Space [welds] [mechanical fasteners] not more than 12 inches (305 mm) apart with at least one [weld] [fastener] at each corner.

1. Install reinforcing channels or zees in ribs to span between supports and [weld] [or] [mechanically fasten].

I. Miscellaneous Roof-Deck Accessories: Install ridge and valley plates, finish strips, end closures, and reinforcing channels according to deck manufacturer's written instructions. [Weld] [or] [mechanically fasten] to substrate to provide a complete deck installation.

1. Weld cover plates at changes in direction of roof-deck panels unless otherwise indicated.

J. Pour Stops and Girder Fillers: Weld steel-sheet pour stops and girder fillers to supporting structure according to SDI recommendations unless otherwise indicated.

K. Floor-Deck Closures: Weld steel-sheet column closures, cell closures, and Z-closures to deck, according to SDI recommendations, to provide tight-fitting closures at open ends of ribs and sides of deck.

3.2 FIELD QUALITY CONTROL

Retain "Testing Agency" Paragraph to identify who shall perform tests and inspections. If retaining second option in "Testing Agency" Paragraph, retain "Field quality-control reports" Paragraph in "Informational Submittals" Article.

A. Testing Agency: [Owner will engage] [Engage] a qualified testing agency to perform tests and inspections.

B. Field welds will be subject to inspection.

C. Testing agency will report inspection results promptly and in writing to Contractor and Architect.

D. Remove and replace work that does not comply with specified requirements.

E. Additional inspecting, at Contractor's expense, will be performed to determine compliance of corrected work with specified requirements.

3.3 PROTECTION

A. Galvanizing Repairs: Prepare and repair damaged galvanized coatings on both surfaces of deck with galvanized repair paint according to ASTM A 780 and manufacturer's written instructions.

B. Repair Painting: Wire brush and clean rust spots, welds, and abraded areas on [both surfaces] [top surface] of prime-painted deck immediately after installation, and apply repair paint.

END OF SECTION 053100

	STEEL DECKING
	053100 - 1



