Copyright 2012 AIA
MasterSpec Professional
05/12

Copyright 2012 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 074633 - PLASTIC SIDING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by inserting or deleting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes vinyl [siding] [and] [soffit].

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product.

Retain subparagraph below for vinyl siding if retaining requirement for certification in "Quality Assurance" Article.

1. For vinyl siding, include VSI's official certification logo printed on Product Data.

B. Samples: For vinyl [siding] [and] [soffit] including related accessories.

1.3 INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

A. Qualification Data: For vinyl siding Installer.

B. Product certificates.

C. Research/evaluation reports.

D. Sample warranty.

1.4 CLOSEOUT SUBMITTALS

A. Maintenance data.

1.5 QUALITY ASSURANCE

Retain "Vinyl Siding Installer Qualifications" Paragraph below if a third-party certification program of vinyl siding installers is required. Verify availability of qualified personnel in vicinity of Project if applicable.

A. Vinyl Siding Installer Qualifications: A qualified installer who employs a VSI-certified Installer on Project.

B. Mockups: Build mockups to verify selections made under Sample submittals and to demonstrate aesthetic effects and to set quality standards for fabrication and installation.

Indicate portion of wall represented by mockup on Drawings or draw mockup as separate element.

1. Build mockup of typical wall area as shown on Drawings.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

2. Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

1.6 WARRANTY

When warranties are required, verify with Owner's counsel that warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

A. Special Warranty: Manufacturer agrees to repair or replace products that fail in materials or workmanship within specified warranty period.

Verify available warranties and warranty periods for vinyl siding and soffit.

1. Warranty Period: [10] [25] [50] <Insert number> years from date of Substantial Completion.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 VINYL SIDING

A. Vinyl Siding: Integrally colored product complying with ASTM D 3679.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's name and model number are indicated on Drawings.

2. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

Manufacturers listed below make and sell VSI-certified products; some also make products that are sold under other brand names and are VSI certified.

a. Alside.

b. CertainTeed Corporation.

c. Exterior Portfolio by Crane.

d. Gentek Building Products, Inc.

e. Heartland Building Products; a ProVia company.

f. Kaycan Ltd.

g. Mastic Home Exteriors.

h. Mitten Inc.

i. Norandex; Building Materials Distribution, Inc.

j. RMC Siding.

k. Royal Building Products.

l. Variform, Inc.

m. <Insert manufacturer's name>.

"Vinyl Siding Certification Program" Paragraph below provides third-party verification that vinyl siding complies with referenced ASTM standard.

B. Vinyl Siding Certification Program: Provide products that are listed in VSI's list of certified products.

Retain one or more of first 11 paragraphs below or revise to suit Project.

C. Horizontal Pattern: 6-1/2- or 7-inch (165- or 178-mm) exposure in beaded-edge, single-board style.

D. Horizontal Pattern: 8-inch (203-mm) exposure in plain, [single-board] [double, 4-inch (102-mm) board] [triple, 2-2/3-inch (68-mm) board] <Insert requirement> style.

E. Horizontal Pattern: 8-inch (203-mm) exposure in Dutch-lap, double, 4-inch (102-mm) board style.

F. Horizontal Pattern: 9-inch (229-mm) exposure in plain, [double, 4-1/2-inch (114-mm)] [triple, 3-inch (76-mm)] <Insert requirement> board style.

G. Horizontal Pattern: 9-inch (229-mm) exposure in Dutch-lap, double, 4-1/2-inch (114-mm) board style.

H. Horizontal Pattern: 10-inch (254-mm) exposure in [plain,] [Dutch-lap,] <Insert requirement,> double, 5-inch (127-mm) board style.

I. Vertical Pattern: 6-inch (152-mm) exposure in V-grooved, single-board style.

J. Vertical Pattern: 8-inch (203-mm) exposure in beaded-edge, double, 4-inch (102-mm) board style.

K. Vertical Pattern: 10-inch (254-mm) exposure in V-grooved, double, 5-inch (127-mm) board style.

L. Vertical Pattern: 12-inch (300-mm) exposure in V-grooved, [double, 6-inch (152-mm)] [triple, 4-inch (102-mm)] <Insert requirement> board style.

M. Shingle Pattern: 48-inch- (1200-mm-) wide, [straight-edge notched] [staggered-edge notched] [half-round edge] [octagon edge] <Insert requirement> sheets with wood-grain texture.

N. Texture: [Smooth] [Wood grain] <Insert requirement>.

Delete "Nominal Thickness" Paragraph below if 0.035-inch (0.9-mm) thickness is acceptable. Most low-priced vinyl siding is at least 0.040 inch (1.0 mm) thick; premium siding is 0.044 to 0.048 inch (1.1 to 1.2 mm) thick. See Evaluations.

O. Nominal Thickness: [0.040 inch (1.0 mm)] [0.044 inch (1.1 mm)] <Insert dimension>.

Retain one of three options in "Minimum Profile Depth (Butt Thickness)" Paragraph below or revise to suit Project. Profile depth, pattern, and thickness determine stiffness. Before retaining, verify that profile depth is available in pattern retained.

P. Minimum Profile Depth (Butt Thickness): [1/2 inch (13 mm)] [5/8 inch (16 mm)] [3/4 inch (19 mm)] <Insert dimension>.

Double-thickness hem in "Nailing Hem" Paragraph below is a feature of most manufacturers' premium siding that increases wind resistance.

Q. Nailing Hem: Double thickness.

Finish in "Finish" Paragraph below is offered by some manufacturers on their top-of-the-line siding.

R. Finish: Wood-grain print with clear protective coating containing not less than 70 percent PVDF.

Retain one of three options in "Colors" Subparagraph below. If retaining first option, indicate colors in a separate schedule.

1. Colors: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range of colors].

2.2 VINYL SOFFIT

A. Vinyl Soffit: Integrally colored product complying with ASTM D 4477.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's name and model number are indicated on Drawings.

2. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

a. Alside.

b. CertainTeed Corporation.

c. Exterior Portfolio by Crane.

d. Gentek Building Products, Inc.

e. Heartland Building Products; a ProVia company.

f. Kaycan Ltd.

g. Mastic Home Exteriors.

h. Mitten Inc.

i. Norandex; Building Materials Distribution, Inc.

j. RMC Siding.

k. Royal Building Products.

l. Variform, Inc.

m. <Insert manufacturer's name>.

"Vinyl Siding Certification Program" Paragraph below provides third-party verification that vinyl soffit complies with referenced ASTM standard.

B. Vinyl Siding Certification Program: Provide products that are listed in VSI's list of certified products.

Retain one of four "Pattern" paragraphs below or revise to suit Project.

C. Pattern: 6-inch (152-mm) exposure in [V-grooved, single-board] [beaded-edge, triple, 2-inch (51-mm) board] <Insert requirement> style.

D. Pattern: 8-inch (203-mm) exposure in V-grooved, double, 4-inch (102-mm) board style.

E. Pattern: 10-inch (254-mm) exposure in V-grooved, double, 5-inch (127-mm) board style.

F. Pattern: 12-inch (300-mm) exposure in V-grooved, [double, 6-inch (152-mm)] [triple, 4-inch (102-mm)] <Insert requirement> board style.

G. Texture: [Smooth] [Wood grain] <Insert requirement>.

H. Ventilation: Provide [perforated] [unperforated] soffit[ unless otherwise indicated].

Delete "Nominal Thickness" Paragraph below if 0.030-inch (0.8-mm) thickness is acceptable. Most low-priced vinyl soffit is at least 0.040 inch (1.0 mm) thick; premium soffit is usually 0.044 inch (1.1 mm) thick. See Evaluations.

I. Nominal Thickness: [0.035 inch (0.9 mm)] [0.040 inch (1.0 mm)] [0.044 inch (1.1 mm)] <Insert dimension>.

Retain one of three options in "Minimum Profile Depth" Paragraph below or revise to suit Project. Profile depth, pattern, and thickness determine stiffness. Before retaining, verify that profile depth is available in pattern retained.

J. Minimum Profile Depth: [1/2 inch (13 mm)] [5/8 inch (16 mm)] [3/4 inch (19 mm)] <Insert dimension>.

Retain one of four options in "Colors" Paragraph below. If retaining first option, indicate colors in a separate schedule.

K. Colors: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range of colors] [Match adjacent siding].

2.3 ACCESSORIES

Retain "Siding Accessories, General" Paragraph below if using aluminum or vinyl siding.

A. Siding Accessories, General: Provide starter strips, edge trim, outside and inside corner caps, and other items as recommended by siding manufacturer for building configuration.

1. Provide accessories [made from same material as] [matching color and texture of] adjacent siding unless otherwise indicated.

B. Vinyl Accessories: Integrally colored vinyl accessories complying with ASTM D 3679 except for wind-load resistance.

1. Texture: [Smooth] [Wood grain] <Insert requirement>.

Retain one of four options in "Colors for Decorative Accessories" Paragraph below. If retaining first option, indicate colors in a separate schedule.

C. Colors for Decorative Accessories: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range of colors] [Match adjacent siding].

D. Flashing: Provide [aluminum] [stainless-steel] <Insert metal> flashing complying with Section 076200 "Sheet Metal Flashing and Trim" at window and door heads and where indicated.

1. Finish for Aluminum Flashing: [Siliconized polyester coating, same color as siding] [High-performance organic finish, same color as siding] [Factory-prime coating] <Insert finish>.

E. Fasteners:

1. For fastening to wood, use [siding nails] [ribbed bugle-head screws] of sufficient length to penetrate a minimum of 1 inch (25 mm) into substrate.

2. For fastening to metal, use ribbed bugle-head screws of sufficient length to penetrate a minimum of 1/4 inch (6 mm), or three screw-threads, into substrate.

3. For fastening vinyl, use [aluminum] [hot-dip galvanized] [stainless-steel] fasteners. Where fasteners are exposed to view, use prefinished aluminum fasteners in color to match item being fastened.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. General: Comply with manufacturer's written installation instructions applicable to products and applications indicated unless more stringent requirements apply.

1. Center nails in elongated nailing slots without binding siding to allow for thermal movement.

B. Install vinyl [siding] [and] [soffit] and related accessories according to ASTM D 4756.

1. Install fasteners for horizontal vinyl siding no more than [16 inches (400 mm)] <Insert dimension> o.c.

2. Install fasteners for vertical vinyl siding no more than [12 inches (300 mm)] <Insert dimension> o.c.

C. Install joint sealants as specified in Section 079200 "Joint Sealants" and to produce a weathertight installation.

3.2 ADJUSTING AND CLEANING

A. Remove damaged, improperly installed, or otherwise defective materials and replace with new materials complying with specified requirements.

B. Clean finished surfaces according to manufacturer's written instructions and maintain in a clean condition during construction.

END OF SECTION 074633

	PLASTIC SIDING
	074633 - 1



