Copyright 2011 AIA
MasterSpec Professional
11/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 081416 - FLUSH WOOD DOORS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Solid-core doors with [wood-veneer] [MDO] [hardboard or MDF] [and] [plastic-laminate] faces.

2. Hollow-core doors with [wood-veneer] [hardboard or MDF] [and] [plastic-laminate] faces.

Retain one or both subparagraphs below if applicable. See Evaluations.

3. [Shop priming] [Factory finishing] flush wood doors.

4. Factory fitting flush wood doors to frames and factory machining for hardware.

B. Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

1. Section 083473.16 "Wood Sound Control Door Assemblies" for acoustic flush wood doors.

2. Section 088000 "Glazing" for glass view panels in flush wood doors.

3. Section 134900 "Radiation Protection" for lead-lined flush wood doors.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of door.[ Include factory-finishing specifications.]

B. LEED Submittals:

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools.

1. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-CI. Retain option for Credit MR 5, Option 2.

2. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regionally manufactured[ and regionally extracted and manufactured] materials. Include statement indicating cost for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 1 and Option 2.

a. Include statement indicating location of manufacturer and distance to Project for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 2.

b. Include statement indicating location of manufacturer and point of extraction, harvest, or recovery for each raw material used in regionally extracted and manufactured materials. Indicate distance to Project and fraction by weight of each regionally manufactured material that is regionally extracted.

First option in "Certificates for (Credit MR 6) (Credit MR 7)" Subparagraph below applies to LEED-CS; second applies to LEED-NC, LEED-CI, and LEED for Schools.

3. Certificates for [Credit MR 6] [Credit MR 7]: Chain-of-custody certificates indicating that flush wood doors comply with forest certification requirements.[ Include documentation that manufacturer is certified for chain of custody by an FSC-accredited certification body.] Include statement indicating cost for each certified wood product.

"Product Data for Credit IEQ 4.4" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS.

4. Product Data for Credit IEQ 4.4: For adhesives and composite wood products, documentation indicating that product contains no urea formaldehyde.

"Laboratory Test Reports for Credit IEQ 4.1" Subparagraph below applies to LEED for Schools.

5. Laboratory Test Reports for Credit IEQ 4.1: For adhesives, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

"Laboratory Test Reports for Credit IEQ 4.2" Subparagraph below applies to LEED for Schools.

6. Laboratory Test Reports for Credit IEQ 4.2: For paints and coatings, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

"Laboratory Test Reports for Credit IEQ 4.4" Subparagraph below applies to LEED for Schools.

7. Laboratory Test Reports for Credit IEQ 4.4: For composite wood products, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings: Indicate location, size, and hand of each door; elevation of each kind of door; construction details not covered in Product Data; and the following:

1. Dimensions and locations of blocking.

2. Dimensions and locations of mortises and holes for hardware.

3. Dimensions and locations of cutouts.

4. Undercuts.

5. Requirements for veneer matching.

6. Doors to be factory finished and finish requirements.

7. Fire-protection ratings for fire-rated doors.

D. Samples: For [plastic-laminate door faces] [and] [factory-finished doors].

1.3 INFORMATIONAL SUBMITTALS

A. Quality Standard Compliance Certificates: [AWI Quality Certification] [WI Certified Compliance] Program certificates.

1.4 QUALITY ASSURANCE

Retain "Manufacturer Qualifications" and "Vendor Qualifications" paragraphs below if required for LEED.

A. Manufacturer Qualifications: A qualified manufacturer that [is certified for chain of custody by an FSC-accredited certification body] [and] [is a certified participant in AWI's Quality Certification Program] [is a licensee of WI's Certified Compliance Program].

Chain-of-custody certification is not required for subcontractors (entities that install products) but is required for vendors unless they are simply acting as an agent of manufacturer and the sale is actually between manufacturer and Contractor or subcontractor.

B. Vendor Qualifications: A vendor that is certified for chain of custody by an FSC-accredited certification body.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 MANUFACTURERS

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Manufacturers listed are representative only; many others make flush wood doors. See WDMA's and AWI's Web sites for listings of door manufacturers. Retain only manufacturers offering doors complying with requirements selected for each type used, and insert other manufacturers offering suitable products. See Evaluations and manufacturers' catalogs.

1. Algoma Hardwoods, Inc.

2. Ampco.

3. Chappell Door Co.

4. Eggers Industries.

5. General Veneer Manufacturing Co.

6. Graham Wood Doors; an Assa Abloy Group company.

7. Haley Brothers, Inc.

8. Ipik Door Company.

9. Lambton Doors.

10. Marlite.

11. Marshfield Door Systems, Inc.

12. Mohawk Doors; a Masonite company.

13. Oshkosh Door Company.

14. Poncraft Door Company.

15. Vancouver Door Company.

16. VT Industries, Inc.

17. <Insert manufacturer's name>.

2.2 FLUSH WOOD DOORS, GENERAL

Retain one standard in "Quality Standard" Paragraph below. Review retained standard and coordinate its requirements with retained options. See Evaluations.

A. Quality Standard: In addition to requirements specified, comply with [AWI's, AWMAC's, and WI's "Architectural Woodwork Standards] [WDMA I.S.1-A, "Architectural Wood Flush Doors]."

If retaining subparagraph below, verify applicability of certification for Project's geographic location. Certification programs of both organizations are available to member and nonmember firms.

1. Provide [AWI Quality Certification] [WI Certified Compliance] Labels indicating that doors comply with requirements of grades specified.

Retain first "Regional Materials" Paragraph below for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5 and LEED-CI Credit MR 5, Option 2; before retaining, verify availability of materials that comply. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," or Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

B. Regional Materials: Flush wood doors shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

Retain "Regional Materials" Paragraph below for LEED-CI Credit MR 5, Option 1; before retaining, verify availability of materials that comply.

C. Regional Materials: Flush wood doors shall be manufactured within 500 miles (800 km) of Project site.

Retain "Certified Wood" Paragraph below if doors are required to be certified for LEED. An alternative method of dealing with this credit requirement is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," or Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development" that gives Contractor the option and responsibility to determine how the credit requirement will be met. Manufacturers certifying products as "FSC Mixed Credit" do not have to use 100 percent certified wood in the products, but in their total production manufacturers must use an amount equal to or greater than the percentage of their production that is labeled "FSC Mixed Credit."

D. Certified Wood: Flush wood doors shall be certified as "FSC Pure"[ or "FSC Mixed Credit"] according to FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship," and to FSC STD-40-004, "FSC Standard for Chain of Custody Certification."

Retain first "Low-Emitting Materials" Paragraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.4. Before retaining, verify availability with manufacturers.

E. Low-Emitting Materials: Fabricate doors with adhesives and composite wood products that do not contain urea formaldehyde.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.1 or Credit IEQ 4.4.

F. Low-Emitting Materials: Fabricate doors with [adhesives] [and] [composite wood products] that comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Retain "WDMA I.S.1-A Performance Grade" Paragraph below to specify performance grade if referencing WDMA I.S.1-A. See Evaluations.

G. WDMA I.S.1-A Performance Grade:

1. Heavy Duty unless otherwise indicated.

2. Extra Heavy Duty: [Classrooms] [public toilets] [janitor's closets] [assembly spaces] [exits] [patient rooms] <Insert locations>[ and where indicated].

3. Standard Duty: [Closets (not including janitor's closets)] [private toilets] <Insert locations>[ and where indicated].

Retain "Fire-Rated Wood Doors" Paragraph below if applicable.

H. Fire-Rated Wood Doors: Doors complying with NFPA 80 that are listed and labeled by a qualified testing agency, for fire-protection ratings indicated, based on testing at positive pressure according to [NFPA 252] [or] [UL 10C].

1. Cores: Provide core specified or mineral core as needed to provide fire-protection rating indicated.

Retain "Edge Construction" Subparagraph below unless using surface-applied intumescent seals.

2. Edge Construction: Provide edge construction with intumescent seals concealed by outer stile. Comply with specified requirements for exposed edges.

Retain "Pairs" Subparagraph below if steel edges and astragals are unacceptable. Coordinate availability and ratings with manufacturers.

3. Pairs: Provide fire-retardant stiles that are listed and labeled for applications indicated without formed-steel edges and astragals. Provide stiles with concealed intumescent seals. Comply with specified requirements for exposed edges.

Retain "Smoke- and Draft-Control Door Assemblies" Paragraph below if required. The IBC requires fire door assemblies to comply with smoke- and draft-control requirements in corridors, smoke barriers, and smoke partitions.

I. Smoke- and Draft-Control Door Assemblies: Listed and labeled for smoke and draft control, based on testing according to UL 1784.

Retain "Particleboard-Core Doors" Paragraph below if doors have particleboard cores.

J. Particleboard-Core Doors:

Retain one or more of four options in "Particleboard" Subparagraph below. Grade LD-2 makes a stronger door, has higher screw-holding capacity, and is standard with some manufacturers and optional with others. Before retaining last option, verify availability with door manufacturers.

1. Particleboard: ANSI A208.1, [Grade LD-1] [or] [Grade LD-2][, made with binder containing no urea-formaldehyde].

2. Blocking: Provide wood blocking in particleboard-core doors as needed to eliminate through-bolting hardware.

3. Provide doors with [glued-wood-stave] [or] [structural-composite-lumber] cores instead of particleboard cores for doors indicated to receive exit devices.

K. Structural-Composite-Lumber-Core Doors:

1. Structural Composite Lumber: WDMA I.S.10.

a. Screw Withdrawal, Face: 700 lbf (3100 N).

b. Screw Withdrawal, Edge: 400 lbf (1780 N).

L. Mineral-Core Doors:

1. Core: Noncombustible mineral product complying with requirements of referenced quality standard and testing and inspecting agency for fire-protection rating indicated.

2. Blocking: Provide composite blocking with improved screw-holding capability approved for use in doors of fire-protection ratings indicated as needed to eliminate through-bolting hardware.

3. Edge Construction: At hinge stiles, provide laminated-edge construction with improved screw-holding capability and split resistance. Comply with specified requirements for exposed edges.

M. Hollow-Core Doors:

1. Construction: [Institutional] [Standard] hollow core.

2.3 VENEER-FACED DOORS FOR TRANSPARENT FINISH

See the tables at the end of the Evaluations for a list of manufacturers' products. Use these tables in combination with manufacturers' catalogs or product data to insert series, type, model, and designations of other characteristics.

Copy appropriate paragraphs below and re-edit for each product.

Insert drawing designation for each product required. Use these designations on Drawings to identify each product.

A. Exterior Solid-Core Doors <Insert drawing designation>:

AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires Grade AA faces for Premium-grade doors; WDMA I.S.1-A requires Grade A faces for Premium-grade doors. Both standards require Grade A faces for Custom-grade doors unless Grade B is specified. See Evaluations.

1. Grade: [Premium, with Grade AA faces] [Premium, with Grade A faces] [Custom (Grade A faces)] [Custom (Grade B faces)].

Options in "Species" Subparagraph below are examples only; revise or insert another species. Last two options are examples of tropical species available as FSC-certified veneers (available from ForestWorld Group).

2. Species: [Anigre] [Select white ash] [Figured select white ash] [Select white birch] [Select red birch] [Cherry] [Select red gum] [Figured select red gum] [Select white maple] [Red oak] [White oak] [Persimmon] [Sapele] [Sycamore] [Walnut] <Insert species>.

"Rift cut" option in "Cut" Subparagraph below applies only to oak.

3. Cut: [Rotary cut] [Plain sliced (flat sliced)] [Quarter sliced] [Rift cut].

"Pleasing" option in "Match between Veneer Leaves" Subparagraph below is available only with Grade B veneers.

4. Match between Veneer Leaves: [Book] [Slip] [Pleasing] match.

"Center-balance" option in "Assembly of Veneer Leaves on Door Faces" Subparagraph below is expensive. AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires center-balance match for Premium-grade doors. "Running" option is standard for Custom-grade and WDMA Premium-grade doors. See Evaluations.

5. Assembly of Veneer Leaves on Door Faces: [Center-balance] [Balance] [Running] match.

6. Pair and Set Match: Provide for doors hung in same opening[ or separated only by mullions].

Particleboard cores in "Core" Subparagraph below are not generally recommended for exterior doors.

7. Core: [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber].

Retain one of four options in "Core" Subparagraph above and one of first two options in "Construction" Subparagraph below. Third option below applies to several five-ply doors.

8. Construction: [Five] [Five or seven] plies. Stiles and rails are bonded to core, then entire unit is abrasive planed before veneering.[ Faces are bonded to core using a hot press.]

9. Adhesives: Type I per WDMA T.M.-6.

B. Interior Solid-Core Doors <Insert drawing designation>:

AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires Grade AA faces for Premium-grade doors; WDMA I.S.1-A requires Grade A faces for Premium-grade doors. Both standards require Grade A faces for Custom-grade doors unless Grade B is specified. See Evaluations.

1. Grade: [Premium, with Grade AA faces] [Premium, with Grade A faces] [Custom (Grade A faces)] [Custom (Grade B faces)].

Options in "Species" Subparagraph below are examples only; revise or insert another species.

2. Species: [Anigre] [Select white ash] [Figured select white ash] [Select white birch] [Select red birch] [Cherry] [Select red gum] [Figured select red gum] [Select white maple] [Red oak] [White oak] [Persimmon] [Sapele] [Sycamore] [Walnut] <Insert species>.

"Rift cut" option in "Cut" Subparagraph below applies only to oak.

3. Cut: [Rotary cut] [Plain sliced (flat sliced)] [Quarter sliced] [Rift cut].

"Pleasing" option in "Match between Veneer Leaves" Subparagraph below is available only with Grade B veneers.

4. Match between Veneer Leaves: [Book] [Slip] [Pleasing] match.

"Center-balance" option in "Assembly of Veneer Leaves on Door Faces" Subparagraph below is expensive. AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires center-balance match for Premium-grade doors. "Running" option is standard for Custom-grade and WDMA Premium-grade doors. See Evaluations.

5. Assembly of Veneer Leaves on Door Faces: [Center-balance] [Balance] [Running] match.

6. Pair and Set Match: Provide for doors hung in same opening[ or separated only by mullions].

Retain one of five options in "Core" Subparagraph below.

7. Core: [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber] [Either glued or nonglued wood stave or structural composite lumber].

8. Construction: [Five] [Five or seven] plies. Stiles and rails are bonded to core, then entire unit is abrasive planed before veneering.[ Faces are bonded to core using a hot press.]

Retain one of first two options in "Construction" Subparagraph above or retain "Construction" Subparagraph below. Third option above applies to some five-ply doors. Glued-wood-stave core is available only with bonded construction and nonglued-wood-stave core is available only with nonbonded construction.

9. Construction: Seven plies, either bonded or nonbonded construction.

C. Interior Hollow-Core Doors <Insert drawing designation>:

AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires Grade AA faces for Premium-grade doors; WDMA I.S.1-A requires Grade A faces for Premium-grade doors. Both standards require Grade A faces for Custom-grade doors unless Grade B is specified. See Evaluations.

1. Grade: [Premium, with Grade AA faces] [Premium, with Grade A faces] [Custom (Grade A faces)] [Custom (Grade B faces)].

Options in "Species" Subparagraph below are examples only; revise or insert another species.

2. Species: [Anigre] [Select white ash] [Figured select white ash] [Select white birch] [Select red birch] [Cherry] [Select red gum] [Figured select red gum] [Select white maple] [Red oak] [White oak] [Persimmon] [Sapele] [Sycamore] [Walnut] <Insert species>.

"Rift cut" option in "Cut" Subparagraph below applies only to oak.

3. Cut: [Rotary cut] [Plain sliced (flat sliced)] [Quarter sliced] [Rift cut].

"Pleasing" option in "Match between Veneer Leaves" Subparagraph below is available only with Grade B veneers.

4. Match between Veneer Leaves: [Book] [Slip] [Pleasing] match.

"Center-balance" option in "Assembly of Veneer Leaves on Door Faces" Subparagraph below is expensive. AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" requires center-balance match for Premium-grade doors. "Running" option is standard for Custom-grade and WDMA Premium-grade doors. See Evaluations.

5. Assembly of Veneer Leaves on Door Faces: [Center-balance] [Balance] [Running] match.

6. Pair and Set Match: Provide for doors hung in same opening[ or separated only by mullions].

7. Construction: Seven plies.

2.4 DOORS FOR OPAQUE FINISH

See the tables at the end of the Evaluations for a list of manufacturers' products. Use these tables in combination with manufacturers' catalogs or product data to insert series, type, model, and designations of other characteristics.

Copy appropriate paragraphs below and re-edit for each product.

Insert drawing designation for each product required. Use these designations on Drawings to identify each product.

A. Exterior Solid-Core Doors <Insert drawing designation>:

1. Grade: [Premium] [Custom].

First option in "Faces" Subparagraph below is highest quality. Coordinate with requirements of door grade selected.

2. Faces: [MDO] [Any closed-grain hardwood of mill option].

Particleboard cores in "Core" Subparagraph below are not generally recommended for exterior doors.

3. Core: [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber].

Retain one of four options in "Core" Subparagraph above and one of first two options in "Construction" Subparagraph below. Third option below applies to several five-ply doors.

4. Construction: [Five] [Five or seven] plies. Stiles and rails are bonded to core, then entire unit is abrasive planed before veneering.[ Faces are bonded to core using a hot press.]

5. Adhesives: Type I per WDMA T.M.-6.

B. Interior Solid-Core Doors <Insert drawing designation>:

1. Grade: [Premium] [Custom].

First option in "Faces" Subparagraph below is highest quality; last is most economical. Coordinate with requirements of door grade selected.

2. Faces: [MDO] [Any closed-grain hardwood of mill option] [Hardboard or MDF].

Retain one of five options in "Core" Subparagraph below.

3. Core: [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber] [Either glued or nonglued wood stave or structural composite lumber].

4. Construction: [Three] [Five] [Five or seven] plies. Stiles and rails are bonded to core, then entire unit is abrasive planed before veneering.[ Faces are bonded to core using a hot press.]

Retain one of first three options in "Construction" Subparagraph above or retain "Construction" Subparagraph below. Fourth option above applies to some five-ply doors. Glued-wood-stave core is available only with bonded construction and nonglued-wood-stave core is available only with nonbonded construction. Retain first option in either subparagraph for hardboard. Three-ply construction applies to doors with hardboard or MDF faces.

5. Construction: [Three] [Seven] plies, either bonded or nonbonded.

C. Interior Hollow-Core Doors <Insert drawing designation>:

1. Grade: [Premium] [Custom].

First option in "Faces" Subparagraph below is higher quality than second option. Coordinate with requirements of door grade selected.

2. Faces: [Any closed-grain hardwood of mill option] [Hardboard or MDF].

2.5 PLASTIC-LAMINATE-FACED DOORS

See the tables at the end of the Evaluations for a list of manufacturers' products. Use these tables in combination with manufacturers' catalogs or product data to insert series, type, model, and designations of other characteristics.

Copy appropriate paragraphs below and re-edit for each product.

Insert drawing designation for each product required. Use these designations on Drawings to identify each product.

A. Interior Solid-Core Doors <Insert drawing designation>:

1. Grade: [Premium] [Custom].

Retain one of two options in "Plastic-Laminate Faces" Subparagraph below, usually the first one. First is typical 0.048-inch- (1.2-mm-) thick material; second is 0.118-inch- (3.0-mm-) thick material made specifically for doors and is expensive. Before specifying second option, verify availability with manufacturers.

2. Plastic-Laminate Faces: High-pressure decorative laminates complying with NEMA LD 3, [Grade HGS] [Grade HSH].

Revise "Colors, Patterns, and Finishes" Subparagraph below to indicate color, pattern, and finish if preselected.

3. Colors, Patterns, and Finishes: [As indicated] [As selected by Architect from laminate manufacturer's full range of products].

4. Exposed Vertical Edges: [Hardwood edges for staining to match faces] [Hardwood edges for painting] [Plastic laminate that matches faces, applied before faces].

5. Core: [Particleboard] [Glued wood stave] [Structural composite lumber] [Either glued wood stave or structural composite lumber].

Retain one of four options in "Core" Subparagraph above and one of two "Construction" subparagraphs below. Glued-wood-stave core is only allowed with five-ply construction. See Evaluations.

6. Construction: Three plies. Stiles and rails are bonded to core, then entire unit is abrasive planed before faces are applied.[ Faces are bonded to core using a hot press.]

7. Construction: Five plies. Stiles and rails are bonded to core, then entire unit is abrasive planed before faces and crossbands are applied.[ Faces are bonded to core using a hot press.]

B. Interior Hollow-Core Doors <Insert drawing designation>:

1. Grade: [Premium] [Custom].

Retain one of two options in "Plastic-Laminate Faces" Subparagraph below, usually the first one. First is typical 0.048-inch- (1.2-mm-) thick material; second is 0.118-inch- (3.0-mm-) thick material made specifically for doors and is expensive. Before specifying second option, verify availability with manufacturers.

2. Plastic-Laminate Faces: High-pressure decorative laminates complying with NEMA LD 3, [Grade HGS] [Grade HSH].

Revise "Colors, Patterns, and Finishes" Subparagraph below to indicate color, pattern, and finish if preselected.

3. Colors, Patterns, and Finishes: [As indicated] [As selected by Architect from laminate manufacturer's full range of products].

4. Exposed Vertical Edges: [Hardwood edges for staining to match faces] [Hardwood edges for painting] [Plastic laminate that matches faces, applied before faces].

2.6 LIGHT FRAMES AND LOUVERS

Retain "Wood-Veneered Beads for Light Openings in Fire-Rated Doors" or "Metal Frames for Light Openings in Fire-Rated Doors" Paragraph below if required for doors with fire-protection rating exceeding 20 minutes.

A. Wood-Veneered Beads for Light Openings in Fire-Rated Doors: Manufacturer's standard wood-veneered noncombustible beads matching veneer species of door faces and approved for use in doors of fire-protection rating indicated. Include concealed metal glazing clips where required for opening size and fire-protection rating indicated.

B. Metal Frames for Light Openings in Fire-Rated Doors: Manufacturer's standard frame formed of 0.048-inch- (1.2-mm-) thick, cold-rolled steel sheet; [factory primed for paint] [with baked-enamel- or powder-coated] finish; and approved for use in doors of fire-protection rating indicated.

C. Metal Louvers:

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. Air Louvers, Inc.

b. Anemostat; a Mestek company.

c. L & L Louvers, Inc.

d. Louvers & Dampers, Inc.; a division of Mestek, Inc.

e. McGill Architectural Products.

f. <Insert manufacturer's name>.

Retain one of three "Metal and Finish" subparagraphs below.

2. Metal and Finish: Hot-dip galvanized steel, 0.040 inch (1.0 mm) thick, [factory primed for paint] [with baked-enamel- or powder-coated] finish.

3. Metal and Finish: Extruded aluminum with Class II, clear anodic finish, AA-M12C22A31.

4. Metal and Finish: Extruded aluminum with [light bronze] [medium bronze] [dark bronze] [black], Class II, color anodic finish, AA-M12C22A32/A34.

2.7 FABRICATION

Delete first paragraph below if no doors are required to be factory fitted. Retain paragraph and revise to indicate exceptions if only some doors are required to be factory fitted. Plastic-laminate-edged and factory-finished doors must be factory fitted and machined. Fire-rated and plastic-laminate-faced doors with wood edges should also be factory fitted and machined. Factory fitting and machining for other doors are optional. See Evaluations.

A. Factory fit doors to suit frame-opening sizes indicated. Comply with clearance requirements of referenced quality standard for fitting unless otherwise indicated.

1. Comply with NFPA 80 requirements for fire-rated doors.

Delete first paragraph below if no doors are required to be factory machined. Retain paragraph and revise to indicate exceptions if only some doors are required to be factory machined. See Evaluations.

B. Factory machine doors for hardware that is not surface applied.

C. Openings: Factory cut and trim openings through doors.

1. Light Openings: Trim openings with moldings of material and profile indicated.

"Glazing" Subparagraph below is unnecessary if using only metal light frames.

2. Glazing: Factory install glazing in doors indicated to be factory finished. Comply with applicable requirements in Section 088000 "Glazing."

3. Louvers: Factory install louvers in prepared openings.

2.8 SHOP PRIMING

Retain this article if field-finished doors are required to be shop primed. Factory fitting is recommended to minimize damage to shop-primed doors.

A. Doors for Opaque Finish: Shop prime faces, all four edges, edges of cutouts, and mortises with one coat of wood primer specified in [Section 099113 "Exterior Painting."] [Section 099123" Interior Painting."]

2.9 FACTORY FINISHING

Retain this article if factory finishing is required. Factory finishing can be used to help comply with LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.2, which limits VOC content of paints and coatings used within buildings. Factory finishing also has other advantages. See Evaluations.

A. General: Comply with referenced quality standard for factory finishing. Complete fabrication, including fitting doors for openings and machining for hardware that is not surface applied, before finishing.

1. Finish faces, all four edges, edges of cutouts, and mortises. Stains and fillers may be omitted on[ top and] bottom edges, edges of cutouts, and mortises.

B. Factory finish doors that are indicated to receive transparent finish.

Retain first paragraph below if required for LEED for Schools Credit IEQ 4.

C. Use only paints and coatings that comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

D. Transparent Finish:

In "Grade" Subparagraph below, usually retain same grade for finish as specified for doors.

1. Grade: [Premium] [Custom].

Retain one of two "Finish" subparagraphs below and one or more options in subparagraph retained, or insert another option. Before specifying, verify availability of finishes with manufacturers. Caution: Finish systems vary among manufacturers. Require Samples for verification.

2. Finish: AWI's, AWMAC's, and WI's "Architectural Woodwork Standards" [System 5, conversion varnish] [System 9, UV curable, acrylated epoxy, polyester, or urethane] [System 10, UV curable, water based] [or] [System 11, catalyzed polyurethane] <Insert finish designation>.

3. Finish: [WDMA TR-4 conversion varnish] [or] [WDMA TR-6 catalyzed polyurethane] <Insert finish designation>.

4. Staining: [Match Architect's sample] [As selected by Architect from manufacturer's full range] [None required].

Retain one of three options in "Staining" Subparagraph above and usually one of three options in "Effect" Subparagraph below. Some door manufacturers will not provide filled finish because filling is best done by hand, which cannot be done on a finishing line; instead, some will offer semifilled finish as described below. Delete subparagraph below if using only closed-grain wood species.

5. Effect: [Open-grain finish] [Filled finish] [Semifilled finish, produced by applying an additional finish coat to partially fill the wood pores].

Retain one of two options in "Sheen" Subparagraph below or revise to suit Project.

6. Sheen: [Satin] [Semigloss].

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Hardware: For installation, see [Section 087100 "Door Hardware."] [Section 087111 "Door Hardware (Descriptive Specification)."]

B. Installation Instructions: Install doors to comply with manufacturer's written instructions and referenced quality standard, and as indicated.

Retain first subparagraph below for fire-rated doors.

1. Install fire-rated doors according to NFPA 80.

Retain subparagraph below for smoke- and draft-control doors. The IBC requires fire door assemblies to comply with smoke- and draft-control requirements in corridors, smoke barriers, and smoke partitions.

2. Install smoke- and draft-control doors according to NFPA 105.

Retain "Job-Fitted Doors" Paragraph below if all doors are not factory fitted. Factory fitting of fire-rated doors is preferred to job fitting because of limitations on trimming narrower stiles and rails.

C. Job-Fitted Doors: Align and fit doors in frames with uniform clearances and bevels as indicated below; do not trim stiles and rails in excess of limits set by manufacturer or permitted for fire-rated doors. Machine doors for hardware. Seal edges of doors, edges of cutouts, and mortises after fitting and machining.

1. Clearances: Provide 1/8 inch (3.2 mm) at heads, jambs, and between pairs of doors. Provide 1/8 inch (3.2 mm) from bottom of door to top of decorative floor finish or covering unless otherwise indicated. Where threshold is shown or scheduled, provide 1/4 inch (6.4 mm) from bottom of door to top of threshold unless otherwise indicated.

Retain subparagraph below for fire-rated doors or if doors are not factory fitted.

a. Comply with NFPA 80 for fire-rated doors.

D. Factory-Fitted Doors: Align in frames for uniform clearance at each edge.

E. Factory-Finished Doors: Restore finish before installation if fitting or machining is required at Project site.

END OF SECTION 081416

	FLUSH WOOD DOORS
	081416 - 1



