Copyright 2011 AIA
MasterSpec Professional
05/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 084413 - GLAZED ALUMINUM CURTAIN WALLS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes glazed aluminum curtain walls.

1.2 PREINSTALLATION MEETINGS

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for sealants.

1. Product Data for Credit IEQ 4.1: For glazing sealants used inside the weatherproofing system, documentation including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4.1" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit IEQ 4.1: For glazing sealants used inside the weatherproofing system, documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

C. Shop Drawings: Include plans, elevations, sections, full-size details, and attachments to other work.

1. Show connection to and continuity with adjacent thermal, weather, air, and vapor barriers.

D. Samples: For each exposed finish required.

Retain "Delegated-Design Submittal" Paragraph below if design services have been delegated to Contractor.

E. Delegated-Design Submittal: For glazed aluminum curtain walls indicated to comply with performance requirements and design criteria, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

1.4 INFORMATIONAL SUBMITTALS

A. Energy Performance Certificates: NFRC-certified energy performance values from manufacturer.

B. Product test reports.

C. Field quality-control reports.

D. Sample warranties.

1.5 CLOSEOUT SUBMITTALS

A. Maintenance data.

1.6 QUALITY ASSURANCE

A. Installer Qualifications: An entity that employs installers and supervisors who are trained and approved by manufacturer.

Retain "Testing Agency Qualifications" Paragraph below if Contractor selects testing agency or if Contractor is required to provide services of a qualified testing agency in "Field Quality Control" Article.

B. Testing Agency Qualifications: Qualified according to ASTM E 699 for testing indicated[ and accredited by IAS or ILAC Mutual Recognition Arrangement as complying with ISO/IEC 17025].

C. Product Options: Information on Drawings and in Specifications establishes requirements for aesthetic effects and performance characteristics of assemblies. Aesthetic effects are indicated by dimensions, arrangements, alignment, and profiles of components and assemblies as they relate to sightlines, to one another, and to adjoining construction.

Retain subparagraph below or revise to suit Project.

1. Do not change intended aesthetic effects, as judged solely by Architect, except with Architect's approval. If changes are proposed, submit comprehensive explanatory data to Architect for review.

1.7 WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

A. Special Assembly Warranty: [Manufacturer] [Installer] agrees to repair or replace components of glazed aluminum curtain wall that do not comply with requirements or that fail in materials or workmanship within specified warranty period.

Verify available warranties and warranty periods for glazed aluminum curtain walls.

1. Warranty Period: [Two] [Five] [10] <Insert number> years from date of Substantial Completion.

B. Special Finish Warranty: Standard form in which manufacturer agrees to repair finishes or replace aluminum that shows evidence of deterioration of factory-applied finishes within specified warranty period.

Coordinate "Warranty Period" Subparagraph below with "Aluminum Finishes" Article. AAMA 2604 is intended to represent five years of performance; AAMA 2605 is intended to represent 10 years of performance. Verify available warranties and warranty periods for finishes.

1. Warranty Period: [Five] [10] [20] <Insert number> years from date of Substantial Completion.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Delegated Design" Paragraph below if Contractor is required to assume responsibility for design.

A. Delegated Design: Engage a qualified professional engineer, as defined in Section 014000 "Quality Requirements," to design glazed aluminum curtain walls.

B. General Performance: Comply with performance requirements specified, as determined by testing of glazed aluminum curtain walls representing those indicated for this Project without failure due to defective manufacture, fabrication, installation, or other defects in construction.

1. Glazed aluminum curtain walls shall withstand movements of supporting structure including, but not limited to, story drift, twist, column shortening, long-term creep, and deflection from uniformly distributed and concentrated live loads.

2. Failure also includes the following:

a. Thermal stresses transferring to building structure.

b. Glass breakage.

c. Noise or vibration created by wind and thermal and structural movements.

d. Loosening or weakening of fasteners, attachments, and other components.

e. Failure of operating units.

C. Structural Loads:

Usually indicate on Drawings design loads determined by Project's structural engineer. Verify requirements of authorities having jurisdiction. See Evaluations for additional information.

1. Wind Loads: As indicated on Drawings.

2. Other Design Loads: [As indicated on Drawings] <Insert loads>.

D. Deflection of Framing Members: At design wind pressure, as follows:

Based on Project conditions, more stringent deflection criteria than specified in subparagraphs below may be required; see "Seismic Performance" Article in the Evaluations. First option in "Deflection Normal to Wall Plane" Subparagraph is based on IBC requirements for framing members supporting glass. Second option is based on AAMA TIR-A11 recommendations.

1. Deflection Normal to Wall Plane: Limited to [edge of glass in a direction perpendicular to glass plane not exceeding 1/175 of the glass edge length for each individual glazing lite] [1/175 of clear span for spans up to 13 feet 6 inches (4.1 m) and to 1/240 of clear span plus 1/4 inch (6.35 mm) for spans greater than 13 feet 6 inches (4.1 m)] <Insert deflection limit> or an amount that restricts edge deflection of individual glazing lites to 3/4 inch (19.1 mm), whichever is less.

First option in "Deflection Parallel to Glazing Plane" Subparagraph below is based on typical deflection criteria for glass. Second option is based on GANA's "Glazing Manual."

2. Deflection Parallel to Glazing Plane: Limited to [1/360 of clear span or 1/8 inch (3.2 mm), whichever is smaller] [amount not exceeding that which reduces glazing bite to less than 75 percent of design dimension and that which reduces edge clearance between framing members and glazing or other fixed components to less than 1/8 inch (3.2 mm)].

a. Operable Units: Provide a minimum 1/16-inch (1.6-mm) clearance between framing members and operable units.

Retain "Cantilever Deflection" Subparagraph below for parapets and similar components.

3. Cantilever Deflection: Where framing members overhang an anchor point, as follows:

a. Perpendicular to Plane of Wall: No greater than 1/240 of clear span plus 1/4-inch (6. 35-mm) for spans greater than 11 feet 8-1/4 inches (3.6 m) or 1/175 times span, for spans less than 11 feet 8-1/4 inches (3.6 m).

ASTM E 330 test method evaluates structural performance of glazed aluminum curtain walls and not structural performance of contiguous construction.

E. Structural: Test according to ASTM E 330 as follows:

1. When tested at positive and negative wind-load design pressures, assemblies do not evidence deflection exceeding specified limits.

2. When tested at [150] <Insert number> percent of positive and negative wind-load design pressures, assemblies, including anchorage, do not evidence material failures, structural distress, or permanent deformation of main framing members exceeding [0.2] <Insert number> percent of span.

Minimum test duration according to ASTM E 330 is 10 seconds, which is historically U.S. practice.

3. Test Durations: As required by design wind velocity, but not less than [10] <Insert number> seconds.

F. Air Infiltration: Test according to ASTM E 283 for infiltration as follows:

1. Fixed Framing and Glass Area:

Retain first option in subparagraph below for maximum air-leakage rate based on ASHRAE 90.1 requirements. Static-air-pressure differential of 1.57 lbf/sq. ft. (75 Pa) in second option, equivalent to a 25-mph (40-km/h) wind, is ASHRAE 90.1 minimum; air-pressure differential in third option is equivalent to a 50-mph (80-km/h) wind.

a. Maximum air leakage of [0.06 cfm/sq. ft. (0.30 L/s per sq. m)] <Insert value> at a static-air-pressure differential of [1.57 lbf/sq. ft. (75 Pa)] [6.24 lbf/sq. ft. (300 Pa)] <Insert value>.

Retain "Water Penetration under Static Pressure" Paragraph below for static-pressure method, which is most frequently specified. For water-penetration tests, AAMA 501 states that a static-air-pressure differential of 20 percent of wind-load design pressure provides satisfactory performance in most parts of the U.S. Locations where high winds and heavy rains occur simultaneously require higher test-pressure differences. Both static and dynamic testing may be required or desired for certain designs, particularly those incorporating special water-drainage features such as rain screen walls.

G. Water Penetration under Static Pressure: Test according to ASTM E 331 as follows:

1. No evidence of water penetration through fixed glazing and framing areas when tested according to a minimum static-air-pressure differential of 20 percent of positive wind-load design pressure, but not less than [6.24 lbf/sq. ft. (300 Pa)] [10 lbf/sq. ft. (480 Pa)] [15 lbf/sq. ft. (720 Pa)] <Insert value>.

The IECC and ASHRAE/IES 90.1 require that all fenestration be certified and labeled by the manufacturer for energy performance, based on ratings established by NFRC. Verify which manufacturers have tested glazed aluminum curtain walls and can demonstrate compliance with NFRC. Verify requirements of authorities having jurisdiction.

H. Energy Performance: Certify and label energy performance according to NFRC as follows:

Primary energy performance requirements usually include thermal transmittance (U-factor), solar heat gain coefficient, and air infiltration. Options in subparagraphs below are examples only; revise values to suit climate zone of building envelope as defined by the IECC. Testing for visible light transmittance (VT) is specified in Section 088000 "Glazing."

1. Thermal Transmittance (U-factor): Fixed glazing and framing areas shall have U-factor of not more than [0.45 Btu/sq. ft. x h x deg F (2.55 W/sq. m x K)] [0.57 Btu/sq. ft. x h x deg F (3.23 W/sq. m x K)] [0.69 Btu/sq. ft. x h x deg F (3.92 W/sq. m x K)] <Insert value> as determined according to NFRC 100.

2. Solar Heat Gain Coefficient: Fixed glazing and framing areas shall have a solar heat gain coefficient of no greater than [0.35] [0.40] [0.45] <Insert value> as determined according to NFRC 200.

3. Condensation Resistance: Fixed glazing and framing areas shall have an NFRC-certified condensation resistance rating of no less than [15] [25] [35] [45] <Insert value> as determined according to NFRC 500.

Retain "Windborne-Debris Impact Resistance" Paragraph below for windborne-debris-impact-resistance performance if required by Project. The IBC establishes criteria for buildings in hurricane-prone locations. Verify requirements of authorities having jurisdiction.

I. Windborne-Debris Impact Resistance: Pass missile-impact and cyclic-pressure tests when tested according to ASTM E 1886 and testing information in ASTM E 1996 for [Wind Zone 1] [Wind Zone 2] [Wind Zone 3] [Wind Zone 4].

1. Large-Missile Test: For glazed openings located within 30 feet (9.1 m) of grade.

2. Small-Missile Test: For glazed openings located more than 30 feet (9.1 m) above grade.

J. Thermal Movements: Allow for thermal movements resulting from ambient and surface temperature changes:

Differential values in "Temperature Change" Subparagraph below (for aluminum in particular) are suitable for most of the U.S.

1. Temperature Change: 120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

2.2 MANUFACTURERS

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Retain "Basis-of-Design Product" Paragraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's name and model number are indicated on Drawings.

B. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

1. Arcadia, Inc.

2. Arch Aluminum & Glass Co., Inc.

3. Bruce Wall Systems Corporation.

4. CMI Architectural.

5. EFCO Corporation.

6. Kawneer North America.

7. Oldcastle, Inc.

8. Pittco Architectural Metals, Inc.

9. Shuco USA LP.

10. Tingwall Inc.

11. TRACO.

12. Tubelite.

13. United States Aluminum.

14. Unitized Systems LLC.

15. Waltek & Company Limited.

16. Wausau Window and Wall Systems.

17. YKK AP America Inc.

18. <Insert manufacturer's name>.

2.3 FRAMING

A. Framing Members: Manufacturer's extruded- or formed-aluminum framing members of thickness required and reinforced as required to support imposed loads.

1. Construction: [Thermally broken] [Thermally improved] [Nonthermal] <Insert description>.

2. Glazing System: Retained mechanically with gaskets on four sides.

3. Glazing Plane: [Front] <Insert location>.

4. Finish: [Clear anodic finish] [Color anodic finish] [Baked-enamel or powder-coat finish] [High-performance organic finish].

Retain first option in "Fabrication Method" Subparagraph below to allow installation type to be determined by Contractor; second option requires field assembly; third and fourth options require factory assembly. See Evaluations.

5. Fabrication Method: [Either factory- or field-fabricated system] [Field-fabricated stick system] [Factory-fabricated unitized system] [Factory-fabricated unit and mullion system].

B. Pressure Caps: Manufacturer's standard aluminum components that mechanically retain glazing.

1. Include snap-on aluminum trim that conceals fasteners.

C. Brackets and Reinforcements: Manufacturer's standard high-strength aluminum with nonstaining, nonferrous shims for aligning system components.

D. Materials:

1. Aluminum: Alloy and temper recommended by manufacturer for type of use and finish indicated.

a. Sheet and Plate: ASTM B 209 (ASTM B 209M).

b. Extruded Bars, Rods, Profiles, and Tubes: ASTM B 221 (ASTM B 221M).

c. Extruded Structural Pipe and Tubes: ASTM B 429/B 429M.

d. Structural Profiles: ASTM B 308/B 308M.

Retain "Steel Reinforcement" Subparagraph below for internal steel reinforcement of aluminum framing members; revise to suit Project.

2. Steel Reinforcement: Manufacturer's standard zinc-rich, corrosion-resistant primer complying with SSPC-PS Guide No. 12.00; applied immediately after surface preparation and pretreatment. Select surface preparation methods according to recommendations in SSPC-SP COM, and prepare surfaces according to applicable SSPC standard.

a. Structural Shapes, Plates, and Bars: ASTM A 36/A 36M.

b. Cold-Rolled Sheet and Strip: ASTM A 1008/A 1008M.

c. Hot-Rolled Sheet and Strip: ASTM A 1011/A 1011M.

2.4 GLAZING

A. Glazing: Comply with Section 088000 "Glazing."

B. Glazing Gaskets: Manufacturer's standard sealed-corner pressure-glazing system of black, resilient elastomeric glazing gaskets, setting blocks, and shims or spacers.

C. Glazing Sealants: As recommended by manufacturer.

Retain first paragraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1. VOC content limit is that for architectural sealants.

D. Sealants used inside the weatherproofing system shall have a VOC content of [250] <Insert value> g/L or less.

Retain paragraph below if required for LEED for Schools Credit IEQ 4.1.

E. Sealants used inside the weatherproofing system shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

2.5 FABRICATION

A. Form or extrude aluminum shapes before finishing.

Retain first paragraph below for welding.

B. Weld in concealed locations to greatest extent possible to minimize distortion or discoloration of finish. Remove weld spatter and welding oxides from exposed surfaces by descaling or grinding.

C. Fabricate components that, when assembled, have the following characteristics:

1. Profiles that are sharp, straight, and free of defects or deformations.

2. Accurately fitted joints with ends coped or mitered.

3. Physical and thermal isolation of glazing from framing members.

4. Accommodations for thermal and mechanical movements of glazing and framing to maintain required glazing edge clearances.

Revise first subparagraph below to suit Project. Most glazed aluminum curtain walls are glazed from the exterior. Verify glazing requirements for aluminum-framed systems with manufacturers listed in Part 2 articles.

5. Provisions for field replacement of glazing from [exterior] [interior] [interior for vision glass and exterior for spandrel glazing panels].

Revise first subparagraph below for safety railings if any.

6. Provisions for safety railings mounted [on interior face of mullions] [between mullions at interior].

7. Fasteners, anchors, and connection devices that are concealed from view to greatest extent possible.

Retain subparagraph below for curved components if any.

8. Components curved to indicated radii.

D. Fabricate components to resist water penetration as follows:

System in first subparagraph below uses internal drainage method to protect against both water leakage and excessive air infiltration.

1. Internal guttering system or other means to drain water passing joints, condensation occurring within framing members, and moisture migrating within glazed aluminum curtain wall to exterior.

System in subparagraph below uses pressure-equalization method to protect against both water leakage and excessive air infiltration.

2. Pressure-equalized system or double barrier design with primary air and vapor barrier at interior side of glazed aluminum curtain wall and secondary seal weeped and vented to exterior.

Retain "Factory-Assembled Frame Units" Paragraph below for unitized system or unit-and-mullion system assembly. Revise to suit Project.

E. Factory-Assembled Frame Units:

1. Rigidly secure nonmovement joints.

2. Prepare surfaces that are in contact structural sealant according to sealant manufacturer's written instructions to ensure compatibility and adhesion.

3. Preparation includes, but is not limited to, cleaning and priming surfaces.

4. Seal joints watertight unless otherwise indicated.

5. Install glazing to comply with requirements in Section 088000 "Glazing."

F. After fabrication, clearly mark components to identify their locations in Project according to Shop Drawings.

Insert integral stabilization requirements for descent-control equipment used for maintenance if any.

2.6 ALUMINUM FINISHES

Retain finishes in paragraphs below to suit Project. If retaining more than one, indicate location of each on Drawings or by inserts.

Retain one of two options in "Clear Anodic Finish" Paragraph below. Verify availability with manufacturers.

A. Clear Anodic Finish: AAMA 611, [AA-M12C22A41, Class I, 0.018 mm] [AA-M12C22A31, Class II, 0.010 mm] or thicker.

Retain one of two options in "Color Anodic Finish" Paragraph below. Verify availability with manufacturers.

B. Color Anodic Finish: AAMA 611, [AA-M12C22A42/A44, Class I, 0.018 mm] [AA-M12C22A32/A34, Class II, 0.010 mm] or thicker.

1. Color: [Light bronze] [Medium bronze] [Dark bronze] [Champagne] [Black] <Insert color>.

Options in "Color" Subparagraph above are examples only and may vary in color range and availability among manufacturers. Retain one or delete all above and retain one of two options in "Color" Subparagraph below.

2. Color: [Match Architect's sample] [As selected by Architect from full range of industry colors and color densities].

"Baked-Enamel or Powder-Coat Finish" Paragraph below references AAMA standard for pigmented organic coating on extrusions and panels.

C. Baked-Enamel or Powder-Coat Finish: AAMA 2603 except with a minimum dry film thickness of 1.5 mils (0.04 mm).

1. Color and Gloss: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color and gloss>.

Retain one of two "High-Performance Organic Finish" paragraphs below; if both are required, indicate location of each system on Drawings, in schedules, or by inserts. Retain AAMA 2604 or AAMA 2605 for high- or superior-performance organic coatings, respectively, on extrusions and panels. If specific products are required, name coating manufacturers and products.

D. High-Performance Organic Finish: Two-coat fluoropolymer finish complying with [AAMA 2604] [AAMA 2605] and containing not less than [50] [70] percent [PVDF] [or] [FEVE] resin by weight in color coat.

1. Color and Gloss: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color and gloss>.

E. High-Performance Organic Finish: [Three] [Four]-coat fluoropolymer finish complying with AAMA 2605 and containing not less than [50] [70] percent [PVDF] [or] [FEVE] resin by weight in both color coat and clear topcoat. Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

1. Color and Gloss: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color and gloss>.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. General:

1. Comply with manufacturer's written instructions.

2. Do not install damaged components.

3. Fit joints to produce hairline joints free of burrs and distortion.

4. Rigidly secure nonmovement joints.

5. Install anchors with separators and isolators to prevent metal corrosion and electrolytic deterioration and to prevent impeding movement of moving joints.

6. Where welding is required, weld components in concealed locations to minimize distortion or discoloration of finish. Protect glazing surfaces from welding.

7. Seal joints watertight unless otherwise indicated.

B. Metal Protection:

1. Where aluminum is in contact with dissimilar metals, protect against galvanic action by painting contact surfaces with primer, applying sealant or tape, or installing nonconductive spacers as recommended by manufacturer for this purpose.

2. Where aluminum is in contact concrete or masonry, protect against corrosion by painting contact surfaces with bituminous paint.

C. Install components to drain water passing joints, condensation occurring within framing members, and moisture migrating within glazed aluminum curtain wall to exterior.

D. Install components plumb and true in alignment with established lines and grades.

Retain paragraph below if glazed aluminum curtain walls are not factory glazed.

E. Install glazing as specified in Section 088000 "Glazing."

3.2 FIELD QUALITY CONTROL

Retain this article for testing of glazed aluminum curtain wall during installation or for testing of field mockups.

A. Testing Agency: [Owner will engage] [Engage] a qualified testing agency to perform tests and inspections.

B. Test Area: Perform tests on [one bay at least 30 feet (9.1 m), by one story] [representative areas of glazed aluminum curtain walls] [mockups] <Insert requirements>.

C. Field Quality-Control Testing: Perform the following test on [representative areas of glazed aluminum curtain walls] [mockups] <Insert requirements>.

Inexpensive test in "Water-Spray Test" Subparagraph below tests for deficiencies in workmanship only and is not representative of a wind-driven rain event.

1. Water-Spray Test: Before installation of interior finishes has begun, areas designated by Architect shall be tested according to AAMA 501.2 and shall not evidence water penetration.

a. Perform a minimum of [two] [three] <Insert number> tests in areas as directed by Architect.

See Section 014000 "Quality Requirements" for retesting and reinspecting requirements and Section 017300 "Execution" for requirements for correcting the Work.

D. Glazed aluminum curtain walls will be considered defective if they do not pass tests and inspections.

E. Prepare test and inspection reports.

END OF SECTION 084413

	GLAZED ALUMINUM CURTAIN WALLS
	084413 - 1



