Copyright 2011 AIA
MasterSpec Professional
11/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 088300 - MIRRORS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes the following types of silvered flat glass mirrors:

1. Annealed monolithic glass mirrors.

2. [Film-backed] [Laminated] [Tempered] glass mirrors qualifying as safety glazing.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product indicated.

B. LEED Submittals:

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements selected in Part 2 for adhesives.

1. Product Data for Credit IEQ 4.1: For adhesives, documentation including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit IEQ 4: For adhesives, documentation indicating that they comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings: Include mirror elevations, edge details, mirror hardware, and attachments to other work.

D. Samples:

1. Mirrors: 12 inches (300 mm) square, including edge treatment on two adjoining edges.

2. Mirror Clips: Full size.

3. Mirror Trim: 12 inches (300 mm) long.

1.3 INFORMATIONAL SUBMITTALS

Retain first paragraph below if mirror mastics are specified for installation of mirrors.

A. Preconstruction test reports.

B. Warranty: Sample of special warranty.

1.4 CLOSEOUT SUBMITTALS

A. Maintenance data.

1.5 QUALITY ASSURANCE

A. Glazing Publications: Comply with GANA's "Glazing Manual" and "Mirrors, Handle with Extreme Care: Tips for the Professional on the Care and Handling of Mirrors."

B. Safety Glazing Products: For [film-backed] [laminated] [tempered] mirrors, provide products complying with testing requirements in 16 CFR 1201 for Category II materials.

Retain paragraph below if adhesive applications of mirrors is required.

C. Preconstruction Mirror Mastic Compatibility Test: Submit mirror mastic products to mirror manufacturer for testing to determine compatibility of mastic with mirror backing and substrates on which mirrors are installed.

1.6 WARRANTY

A. Special Warranty: Manufacturer's standard form in which mirror manufacturer agrees to replace mirrors that deteriorate within specified warranty period. Deterioration of mirrors is defined as defects developed from normal use that are not attributed to mirror breakage or to maintaining and cleaning mirrors contrary to manufacturer's written instructions. Defects include discoloration, black spots, and clouding of the silver film.

Before retaining requirement that warranty begins on date of Substantial Completion, verify available warranties and warranty periods with manufacturers listed in Part 2 articles. Manufacturers offer standard warranties for mirrors that begin on date of manufacture, which is typically stamped on back of mirror.

1. Warranty Period: [Five] <Insert number> years from date of [Substantial Completion] [manufacture].

PART 2 -  PRODUCTS

2.1 SILVERED FLAT GLASS MIRRORS

Retaining option in first paragraph below may limit available products. See Evaluations.

A. Glass Mirrors, General: ASTM C 1503[; manufactured using copper-free, low-lead mirror coating process].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers. Retain subparagraph and list of manufacturers below. See Section 016000 "Product Requirements."

1. Manufacturers: Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Mirror manufacturers listed below are members of GANA Mirror Division. Some of those listed may offer mirrors only in stock sheets for fabrication into cut sizes, while others provide both stock sheets and cut sizes.

a. Arch Aluminum & Glass Co., Inc.

b. Avalon Glass and Mirror Company.

c. Binswanger Mirror; a division of Vitro America, Inc.

d. D & W Incorporated
e. Donisi Mirror Company.

f. Gardner Glass, Inc.

g. Gilded Mirrors, Inc.

h. Guardian Industries.

i. Head West.

j. Independent Mirror Industries, Inc.

k. Lenoir Mirror Company.

l. Maran-Wurzell Glass & Mirror.

m. National Glass Industries.

n. Stroupe Mirror Co., Inc.

o. Sunshine Mirror; Westshore Glass Corp.

p. Virginia Mirror Company, Inc.

q. Walker Glass Co., Ltd.

r. <Insert manufacturer's name>.

See ASTM C 1503 for intended use recommendations based on thickness. Mirror Select Quality may be available only in 6-mm thickness.

B. Clear Glass: Mirror [Select] [Glazing] Quality[; ultraclear (low-iron) float glass with a minimum 91 percent visible light transmission].

1. Nominal Thickness: [3.0 mm] [4.0 mm] [5.0 mm] [6.0 mm] [As indicated] <Insert thickness>.

See Evaluations for discussion on effect of tempering on mirror distortion.

C. Tempered Clear Glass: Mirror Glazing Quality, for blemish requirements; and comply with ASTM C 1048 for Kind FT, Condition A, tempered float glass before silver coating is applied.

1. Nominal Thickness: [3.0 mm] [4.0 mm] [5.0 mm] [6.0 mm] [As indicated] <Insert thickness>.

D. Laminated Mirrors: ASTM C 1172, Kind LM.

Retain one of first two subparagraphs below for outer lite glass. Mirror Select Quality may be available only in 6-mm thickness. Revise both subparagraphs if tempered glass is required to suit Project and verify availability with manufacturers.

1. Clear Glass for Outer Lite: Mirror [Select] [Glazing] Quality[; ultraclear (low-iron) float glass with a minimum 91 percent visible light transmission].

2. Nominal Thickness for Outer Lite: [3.0 mm] [4.0 mm] [5.0 mm] [6.0 mm] [As indicated] <Insert thickness>.

Revise first subparagraph below if another glass description is applicable for inner lite glass.

3. Glass for Inner Lite: Annealed float glass; ASTM C 1036, Type I (transparent flat glass), Quality-Q3; Class 1 (clear).

4. Nominal Thickness: [3.0 mm] [4.0 mm] [5.0 mm] [6.0 mm] [As indicated] <Insert thickness>.

5. Interlayer: Mirror manufacturer's standard 0.030-inch- (0.76-mm-) thick, clear polyvinyl-butyral interlayer with a proven record of showing no tendency to delaminate from, or cause damage to, silver coating.

2.2 MISCELLANEOUS MATERIALS

A. Setting Blocks: Elastomeric material with a Shore, Type A durometer hardness of 85, plus or minus 5.

B. Edge Sealer: Approved by mirror manufacturer.

C. Mirror Mastic: An adhesive setting compound, asbestos-free, produced specifically for setting mirrors.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1. VOC limit is that for multipurpose construction adhesives.

1. Adhesive shall have a VOC content of not more than [70] <Insert number> g/L when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

2. Adhesive shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

D. Film Backing for Safety Mirrors: Film backing and pressure-sensitive adhesive; both compatible with mirror backing paint as certified by mirror manufacturer.

2.3 MIRROR HARDWARE

A. Top and Bottom Aluminum J-Channels: Aluminum extrusions with a return deep enough to produce a glazing channel to accommodate mirrors of thickness indicated and in lengths required to cover bottom and top edges of each mirror in a single piece.

1. Finish: [Clear] [Gold] bright anodized.

B. Mirror Bottom Clips: [As indicated] <Insert description or product designation, finish, and manufacturer's name>.

C. Mirror Top Clips: [As indicated] <Insert description or product designation, finish, and manufacturer's name>.

D. Fasteners: Fabricated of same basic metal and alloy as fastened metal and matching it in finished color and texture where fasteners are exposed.

E. Anchors and Inserts: Provide devices as required for mirror hardware installation.

2.4 FABRICATION

A. Cutouts: Fabricate cutouts[ before tempering] for notches and holes in mirrors without marring visible surfaces. Locate and size cutouts so they fit closely around penetrations in mirrors.

B. Mirror Edge Treatment: [Flat polished] [Rounded polished] [Flat high-polished] [Rounded high-polished] [Beveled polished edge of width shown]. Seal edges of mirrors with edge sealer.

C. Film-Backed Safety Mirrors: Apply film backing with adhesive coating over mirror backing paint as recommended in writing by film-backing manufacturer.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Examine substrates, over which mirrors are to be mounted, with Installer present, for compliance with installation tolerances, substrate preparation, and other conditions affecting performance of the Work.

1. Verify compatibility with and suitability of substrates, including compatibility of mirror mastic with existing finishes or primers.

2. Proceed with installation only after unsatisfactory conditions have been corrected and surfaces are dry.

B. Comply with mastic manufacturer's written installation instructions for preparation of substrates, including coating substrates with mastic manufacturer's special bond coating where applicable.

C. General: Install mirrors to comply with mirror manufacturer's written instructions and with referenced GANA publications. Mount mirrors accurately in place in a manner that avoids distorting reflected images.

D. Wall-Mounted Mirrors: Install mirrors with [mastic and ]mirror hardware. Attach mirror hardware securely to mounting surfaces with mechanical fasteners installed with anchors or inserts as applicable. Install fasteners so heads do not impose point loads on backs of mirrors.[ Apply mastic to comply with mastic manufacturer's written instructions for coverage and to allow air circulation between back of mirrors and face of mounting surface.]

E. Protect mirrors from breakage and contaminating substances resulting from construction operations.

F. Do not permit edges of mirrors to be exposed to standing water.

G. Maintain environmental conditions that will prevent mirrors from being exposed to moisture from condensation or other sources for continuous periods of time.

H. Wash exposed surface of mirrors not more than four days before date scheduled for inspections that establish date of Substantial Completion. Wash mirrors as recommended in writing by mirror manufacturer.

END OF SECTION 088300

	MIRRORS
	088300 - 1



