Copyright 2011 AIA
MasterSpec Professional
02/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 092300 - GYPSUM PLASTERING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Gypsum plasterwork on [expanded-metal lath] [unit masonry] [and] [monolithic concrete].

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product indicated.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements selected in Part 2 for sealants.

2. Product Data for Credit IEQ 4.1: For sealants, documentation including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

3. Laboratory Test Reports for Credit IEQ 4: For [gypsum plaster assemblies] [and] [sealants], documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

Usually delete paragraph below and show locations and details of control and expansion joints on Drawings.

C. Shop Drawings: Show locations and installation of control and expansion joints including plans, elevations, sections, details of components, and attachments to other work.

1.3 QUALITY ASSURANCE

Retain first paragraph below only if products specified in Part 2 are part of a fire-resistance-rated assembly. Indicate rating, testing agency, and testing agency's design designations on Drawings.

A. Fire-Resistance Ratings: Where indicated, provide gypsum plaster assemblies identical to those of assemblies tested for fire resistance per ASTM E 119 by a qualified testing agency. Identify products with appropriate markings of applicable testing agency.

Retain first paragraph below for STC-rated assemblies. Indicate design designations of specific assemblies on Drawings.

B. Sound Transmission Characteristics: Where indicated, provide gypsum plaster assemblies identical to those of assemblies tested for STC ratings per ASTM E 90 and classified according to ASTM E 413 by a qualified testing agency.

C. Mockups: Before plastering, install mockups of at least 100 sq. ft. (9 sq. m) in surface area to demonstrate aesthetic effects and set quality standards for materials and execution.

In-place float, sprayed, and textured finishes vary; requiring a mockup is recommended.

Retain subparagraph below if mockups are installed as part of building rather than erected separately and the intention is to make an exception to the default requirement in SECTION 014000 "Quality Requirements" for demolishing and removing mockups when directed unless otherwise indicated.

1. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

1.4 PROJECT CONDITIONS

A. Comply with ASTM C 842 requirements or gypsum plaster manufacturer's written recommendations, whichever are more stringent.

PART 2 -  PRODUCTS

2.1 GYPSUM PLASTER ASSEMBLIES

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.

A. Low-Emitting Materials: Gypsum plaster assemblies shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

2.2 EXPANDED-METAL LATH

A. Expanded-Metal Lath: ASTM C 847, cold-rolled carbon-steel sheet, ASTM A 653/A 653M, G60 (Z180), hot-dip galvanized zinc coated.

Retain first subparagraph below if recycled content is required for LEED-NC, LEED-CI, or LEED-CS Credit MR 4. The USGBC allows a default value of 25 percent to be used for steel without documentation; higher percentages can be claimed if they are supported by appropriate documentation. The Steel Recycling Institute indicates that steel sheet typically has 23 percent postconsumer recycled content and 1.5 percent preconsumer recycled content.

1. Recycled Content: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.

Retain first subparagraph below if paper backing is required. Kraft-paper-backed lath is used to reduce plaster "push-through" or "blow-through" waste. Asphalt-saturated and -laminated paper backings are also available but are typically used only for exterior applications with portland cement plaster. Verify with manufacturers that paper backing is available for lath configurations retained below.

2. Paper Backing: Kraft paper factory bonded to back of lath.

Coordinate lath selections with framing spacing, requirements detailed on Drawings, and installation requirements in Part 3. See "Expanded-Metal Lath" Article in the Evaluations.

3. Diamond-Mesh Lath: [Flat] [Self-furring], [2.5 lb/sq. yd. (1.4 kg/sq. m)] [3.4 lb/sq. yd. (1.8 kg/sq. m)].

Flat rib lath is more rigid than diamond lath. It is not suitable for contour lathing.

4. Flat Rib Lath: Rib depth of not more than 1/8 inch (3.1 mm), [2.75 lb/sq. yd. (1.5 kg/sq. m)] [3.4 lb/sq. yd. (1.8 kg/sq. m)].

2.3 ACCESSORIES

A. General: Comply with ASTM C 841 and coordinate depth of trim and accessories with thicknesses and number of plaster coats required.

If retaining requirements for trims such as cornerbeads and casing beads that are fabricated from more than one material, indicate locations of each on Drawings.

B. Metal Accessories:

Retain first subparagraph below for reinforcing plaster at internal angles of plaster on solid bases and for restrained construction using expanded-metal lath (that is not otherwise lapped); see "Accessories" Article in the Evaluations.

1. Cornerite: Fabricated from expanded-metal lath with ASTM A 653/A 653M, G60 (Z180), hot-dip galvanized zinc coating.

Retain first subparagraph below for reinforcing plaster over joints in nonmetallic bases and between dissimilar plaster bases. Striplath also can be applied diagonally to reinforce plaster at corners of door and window openings and other areas of concentrated stress. See "Accessories" Article in the Evaluations.

2. Striplath: Fabricated from expanded-metal lath with ASTM A 653/A 653M, G60 (Z180), hot-dip galvanized zinc coating.

Delete five subparagraphs below if only plastic is required.

3. Cornerbeads: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel].

a. [Small-nose] [Bull-nose] style; use unless otherwise indicated.

4. Casing Beads: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; square-edged style; with expanded flanges.

5. Control Joints: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; one-piece-type, folded pair of unperforated screeds in M-shaped configuration; with perforated flanges and removable protective tape on plaster face of control joint.

6. Expansion Joints: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; folded pair of unperforated screeds in M-shaped configuration; with expanded flanges.

7. Two-Piece Expansion Joints: Fabricated from [zinc] [or] [zinc-coated (galvanized) steel]; formed to produce slip-joint and square-edged reveal that is adjustable from 1/4 to 5/8 inch (6 to 16 mm) wide; with perforated flanges.

C. Plastic Accessories: Fabricated from high-impact PVC.

1. Cornerbeads: With perforated flanges.

a. [Small-nose] [Bull-nose] style; use unless otherwise indicated.

2. Casing Beads: With perforated flanges in depth required to suit plaster bases indicated and flange length required to suit applications indicated.

a. [Square-edge] [Bull-nose] style; use unless otherwise indicated.

3. Control Joints: One-piece-type, folded pair of unperforated screeds in M-shaped configuration; with perforated flanges and removable protective tape on plaster face of control joint.

4. Expansion Joints: Two-piece type, formed to produce slip-joint and square-edged [1/2-inch- (13-mm-)] [1-inch- (25.4-mm-)] [1-1/2-inch- (38.1-mm-)] <Insert dimension> wide reveal; with perforated concealed flanges.

2.4 MISCELLANEOUS MATERIALS

Water containing salt, alum, or plaster residue accelerates plaster set and may cause efflorescence. Water containing organic or vegetable matter may retard plaster set, cause staining, and interfere with plaster bond.

A. Water for Mixing and Finishing Plaster: Potable and free of substances capable of affecting plaster set or of damaging plaster, lath, or accessories.

Retain bonding compound in first paragraph below if plaster is adhered to structurally sound interior unit masonry or monolithic concrete.

B. Bonding Compound: ASTM C 631.

C. Steel Drill Screws: For metal-to-metal fastening, ASTM C 1002 or ASTM C 954, as required by thickness of metal being fastened; with pan head that is suitable for application; in lengths required to achieve penetration through joined materials of no fewer than three exposed threads.

D. Fasteners for Attaching Metal Lath to Substrates: Complying with ASTM C 841.

Generally retain first paragraph below. Wire, in various diameters, is used for tying expanded-metal lath to framing and supports.

E. Wire: ASTM A 641/A 641M, Class 1 zinc coating, soft temper, not less than 0.0475-inch (1.21-mm) diameter, unless otherwise indicated.

F. Sound Attenuation Blankets: ASTM C 665, Type I (blankets without membrane facing) produced by combining thermosetting resins with mineral fibers manufactured from glass, slag wool, or rock wool.

1. Fire-Resistance-Rated Assemblies: Comply with mineral-fiber requirements of rated assembly.

Retain "Recycled Content" Subparagraph below to specify recycled content if applying for LEED Credit MR 4. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," Section 018113.23 "Sustainable Design Requirements - LEED for Schools" Section that gives Contractor the option and responsibility to determine how these credit requirements will be met.

2. Recycled Content: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent by weight.

G. Acoustical Sealant: As specified in Section 079200 "Joint Sealants."

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1. VOC content limit is that for architectural sealants.

1. Sealants shall have a VOC content of [250] <Insert value> g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

2. Sealants shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

2.5 BASE-COAT PLASTER MATERIALS

Retain "Recycled Content of Gypsum Plaster" Paragraph below if required for LEED Credit MR 4. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

A. Recycled Content of Gypsum Plaster: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

In Project area, verify availability of products retained in this article.

B. Base-Coat Plasters, General: ASTM C 28/C 28M.

C. Lightweight Gypsum Ready-Mixed Plaster: With mill-mixed perlite aggregate.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. National Gypsum Company; Gold Bond Gypsolite.

b. USG Corporation; Structo-Lite.

c. <Insert manufacturer's name; product name or designation>.

D. Gypsum Neat Plaster: For use with job-mixed aggregates.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. National Gypsum Company; Gold Bond Two-Way Hardwall Plaster.

b. USG Corporation; Red Top Gypsum Plaster.

c. <Insert manufacturer's name; product name or designation>.

E. Gypsum Wood-Fibered Plaster:

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. USG Corporation; Red Top Wood Fiber Plaster.

b. <Insert manufacturer's name; product name or designation>.

F. High-Strength Gypsum Neat Plaster: With a minimum, average, dry compressive strength of 2800 psi (19 MPa) per ASTM C 472 for a mix of 100 lb (45 kg) of plaster and 2 cu. ft. (0.06 cu. m) of sand.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. USG Corporation; Structo-Base.

b. <Insert manufacturer's name; product name or designation>.

G. Aggregates for Base-Coat Plasters: ASTM C 35, [sand] [and] [perlite].

2.6 FINISH-COAT PLASTER MATERIALS

Retain "Recycled Content of Gypsum Plaster" Paragraph below if required for LEED Credit MR 4. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

A. Recycled Content of Gypsum Plaster: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

In Project area, verify availability of products retained in this article.

B. Gypsum Gaging Plaster: ASTM C 28/C 28M.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. National Gypsum Company; Gauging Plaster (Super-White).

b. USG Corporation; [Champion Gauging] [Red Top Gauging Gypsum] [Star Gauging] Plaster.

c. <Insert manufacturer's name; product name or designation>.

C. Gypsum Ready-Mixed Finish Plaster: Manufacturer's standard, mill-mixed, gaged, interior finish.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. National Gypsum Company; Gold Bond [Kal-Kote Smooth] [Kal-Kote Texture] [Uni-Kal] [X-KALibur].

b. USG Corporation; [Diamond Brand Interior Finish Plaster] [Imperial Finish Plaster] [Red Top Finish Plaster].

c. <Insert manufacturer's name; product name or designation>.

D. High-Strength Gypsum Gaging Plaster: ASTM C 28/C 28M, with a minimum, average, dry compressive strength of 5000 psi (34 MPa) per ASTM C 472 for a neat mix.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products. See Section 016000 "Product Requirements."

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. USG Corporation; Structo-Gauge.

b. <Insert manufacturer's name; product name or designation>.

E. Lime: ASTM C 206, Type S, special finishing hydrated lime.

F. Lime: ASTM C 206, Type N, normal finishing hydrated lime.

Retain paragraph below for float finishes. Perlite aggregates in second option is used over base coats containing perlite.

G. Aggregates for Float Finishes: ASTM C 35, [sand] [perlite]; graded per ASTM C 842.

If applicable, insert requirements for plaster colorants here; consult manufacturers for recommendations.

2.7 PLASTER MIXES

A. Mixing: Comply with ASTM C 842 and manufacturer's written instructions for applications indicated.

PART 3 -  EXECUTION

3.1 INSTALLATION, GENERAL

A. Protect adjacent work from soiling, spattering, moisture deterioration, and other harmful effects caused by plastering.

B. Fire-Resistance-Rated Assemblies: Install components according to requirements for design designations from listing organization and publication indicated on Drawings.

C. STC-Rated Assemblies: Install components according to requirements for design designations from listing organization and publication indicated on Drawings.

1. Seal construction at perimeters, behind control and expansion joints, and at openings and penetrations with a continuous bead of acoustical sealant. Install acoustical sealant at both faces of partitions at perimeters and through penetrations.

2. Comply with ASTM C 919 and manufacturer's written recommendations for locating edge trim and closing off sound-flanking paths around or through assemblies, including sealing partitions above acoustical ceilings.

D. Sound Attenuation Blankets: Where required, install blankets before installing lath unless blankets are readily installed after lath has been installed on one side.

Revise paragraph above and paragraph below to suit Project. If sound attenuation blankets and acoustical sealant are required in assemblies other than in STC-rated assemblies, show locations on Drawings.

E. Acoustical Sealant: Where required, seal joints between edges of plasterwork and abutting construction with acoustical sealant.

3.2 INSTALLING EXPANDED-METAL LATH

A. Expanded-Metal Lath: Install according to ASTM C 841.

Retain appropriate lath for each location indicated in four subparagraphs below, or delete this article if only one type of lath is required or if locations of each type of lath are shown on Drawings. See "Expanded-Metal Lath" Article in the Evaluations.

1. Partition Framing and Vertical Furring: Install [flat diamond-mesh] [flat rib] lath.

2. Flat-Ceiling and Horizontal Framing: Install [flat diamond-mesh] [flat rib] lath.

Diamond-mesh lath requires closely spaced supports when used on ceilings.

3. Curved-Ceiling Framing: Install flat diamond-mesh lath.

4. On Solid Surfaces, Not Otherwise Furred: Install self-furring, diamond-mesh lath.

3.3 INSTALLING ACCESSORIES

A. General: Install according to ASTM C 841.

B. Cornerbeads: Install at external corners.

C. Casing Beads: Install at terminations of plasterwork, except where plaster passes behind and is concealed by other work and where metal screeds, bases, or frames act as casing beads.

Usually retain first option in paragraph below and show joints on Drawings.

D. Control Joints: Install control joints [at locations indicated on Drawings.] [with spacing between joints in either direction not exceeding the following and in specific locations approved by Architect for visual effect:]

Retain both subparagraphs below if retaining last option in paragraph above.

1. Partitions: 30 feet (9 m).

Retain second option in subparagraph below if ceilings are not isolated from partition construction at perimeters.

2. Ceilings: [50 feet (15 m)] [30 feet (9 m)].

3.4 PLASTER APPLICATION

A. General: Comply with ASTM C 842.

B. Bonding Compound: Apply on [unit masonry] [and] [concrete] plaster bases.

C. Base Coats:

Retain applicable base coats from four subparagraphs below. Coordinate with requirements retained in "Base-Coat Plaster Materials" Article.

1. Base Coats over Expanded-Metal Lath: [High-strength gypsum] [Gypsum neat] plaster with job-mixed sand for scratch and brown coats.

Retain subparagraph above or first subparagraph below for plaster applied to expanded-metal lath.

2. Base Coats over Expanded-Metal Lath:

a. Scratch Coat: Gypsum wood-fibered plaster; neat or with job-mixed sand.

b. Brown Coat: Gypsum [wood-fibered plaster with job-mixed sand] [neat plaster with job-mixed sand] [lightweight ready-mixed plaster] [neat plaster with job-mixed perlite].

3. Base Coats over Unit Masonry: Gypsum [wood-fibered plaster with job-mixed sand] [neat plaster with job-mixed sand] [lightweight ready-mixed plaster] <Insert mix>.

4. Base-Coat Mix over Monolithic Concrete: [Gypsum neat plaster with job-mixed sand] <Insert mix>.

D. Finish Coats:

Retain applicable finish-coat mixes from four subparagraphs below. Coordinate with requirements in "Finish-Coat Plaster Materials" Article and verify manufacturers' recommendations before revising. If finish coats are integrally colored, insert mix requirements.

Gypsum ready-mixed finish plaster is suitable for use only with sanded base coats. High-strength gypsum gaging plaster is unsuitable for use with lightweight-aggregate base coats. Decreasing the proportion of lime in the mix produces a harder, more durable surface, but reduces coverage and workability.

1. Finish-Coat Mix for Smooth-Troweled Finishes: [Gypsum gaging plaster] [Gypsum ready-mixed finish plaster] [High-strength gypsum gaging plaster] <Insert finish-coat plaster>.

2. Finish-Coat Mix for Float Finishes: [Gypsum gaging plaster] <Insert finish-coat plaster>.

3. Finish-Coat Mix for Sprayed Finishes: [Gypsum ready-mixed finish plaster] <Insert finish-coat plaster>.

4. Finish-Coat Mix for Textured Finishes: [Gypsum ready-mixed finish plaster] <Insert finish-coat plaster>.

E. Plaster Finishes:

Coordinate requirements in subparagraphs below with requirements in "Plaster Mixes" Article. If finish coats are integrally colored, insert their locations here.

1. Provide troweled finish [unless otherwise indicated] [where indicated] <Insert locations>.

2. Provide float finish [unless otherwise indicated] [where indicated] <Insert locations>.

3. Provide sprayed finish [unless otherwise indicated] [where indicated] <Insert locations>.

a. Sprayed Finish: [Match Architect's sample] <Insert requirements>.

4. Provide textured finish [where indicated] <Insert locations>.

a. Textured Finish: [Match Architect's sample] <Insert requirements>.

F. Concealed Plaster:

1. Where plaster application will be concealed behind built-in cabinets, similar furnishings, and equipment, apply finish coat.

2. Where plaster application will be concealed above suspended ceilings and in similar locations, finish coat may be omitted.

3. Where plaster application will be used as a base for adhesive application of tile and similar finishes, finish coat may be omitted.

3.5 PLASTER REPAIRS

A. Repair or replace work to eliminate cracks, dents, blisters, buckles, crazing and check cracking, dry outs, efflorescence, sweat outs, and similar defects and where bond to substrate has failed.

END OF SECTION 092300

	GYPSUM PLASTERING
	092300 - 1



