Copyright 2012 AIA
MasterSpec Professional
05/12

Copyright 2012 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 092900 - GYPSUM BOARD
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Interior gypsum board.

2. Exterior gypsum board for ceilings and soffits.

Tile backing panels in first subparagraph below may be specified in this Section or in Section 093000 "Tiling."

3. Tile backing panels.

4. Texture finishes.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools.

2. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-CI. Retain or delete both options.

3. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regionally manufactured[ and regionally extracted and manufactured] materials. Include statement indicating cost for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 1 and Option 2.

a. Include statement indicating location of manufacturer and distance to Project for each regionally manufactured material.

First subparagraph below applies to LEED-CI Credit MR 5, Option 2.

b. Include statement indicating location of manufacturer and point of extraction, harvest, or recovery for each raw material used in regionally extracted and manufactured materials. Indicate distance to Project and fraction by weight of each regionally manufactured material that is regionally extracted.

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for adhesives.

4. Product Data for Credit IEQ 4.1: For adhesives used to laminate gypsum board panels to substrates, documentation including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

5. Laboratory Test Reports for Credit IEQ 4: For adhesives used to laminate gypsum board panels to substrates, documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Samples:

1. Textured Finishes: [Manufacturer's standard size] <Insert size> for each textured finish indicated and on same backing indicated for Work.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Fire-Resistance-Rated Assemblies" Paragraph below where gypsum board is part of fire-resistance-rated assemblies. Indicate design designations of specific assemblies on Drawings.

A. Fire-Resistance-Rated Assemblies: For fire-resistance-rated assemblies, provide materials and construction identical to those tested in assembly indicated according to ASTM E 119 by an independent testing agency.

Retain "STC-Rated Assemblies" Paragraph below where gypsum board is part of STC-rated assemblies. Indicate design designations of specific assemblies on Drawings.

B. STC-Rated Assemblies: For STC-rated assemblies, provide materials and construction identical to those tested in assembly indicated according to ASTM E 90 and classified according to ASTM E 413 by an independent testing agency.

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

C. Low Emitting Materials: For ceiling and wall assemblies, provide materials and construction identical to those tested in assembly and complying with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

2.2 GYPSUM BOARD, GENERAL

Retain "Recycled Content of Gypsum Panel Products" Paragraph below to specify recycled content if applying for LEED Credit MR 4. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

A. Recycled Content of Gypsum Panel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

Retain first "Regional Materials" Paragraph below for LEED-NC, LEED-CS, and LEED for Schools Credit MR 5 or LEED-CI Credit MR 5, Option 2; before retaining, verify availability of materials that comply.

B. Regional Materials: Gypsum panel products shall be manufactured within 500 miles (800 km) of Project site from materials that have been extracted, harvested, or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

Retain "Regional Materials" Paragraph below for LEED-CI Credit MR 5, Option 1; before retaining, verify availability of materials that comply.

C. Regional Materials: Gypsum panel products shall be manufactured within 500 miles (800 km) of Project site.

2.3 INTERIOR GYPSUM BOARD

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

1. American Gypsum.

2. CertainTeed Corp.

3. Georgia-Pacific Gypsum LLC.

4. Lafarge North America Inc.

5. National Gypsum Company.

6. PABCO Gypsum.

7. Temple-Inland.

8. USG Corporation.

9. <Insert manufacturer's name>.

B. Gypsum Wallboard: ASTM C 1396/C 1396M.

Gypsum wallboard is also available in 1/4- and 3/8-inch (6.4- and 9.5-mm) thicknesses for limited applications.

1. Thickness: 1/2 inch (12.7 mm).

2. Long Edges: [Tapered] [Tapered and featured (rounded or beveled) for prefilling].

C. Gypsum Board, Type X: ASTM C 1396/C 1396M.

1. Thickness: 5/8 inch (15.9 mm).

2. Long Edges: [Tapered] [Tapered and featured (rounded or beveled) for prefilling].

D. Flexible Gypsum Board: ASTM C 1396/C 1396M. Manufactured to bend to fit radii and to be more flexible than standard regular-type gypsum board of same thickness.

1. Thickness: 1/4 inch (6.4 mm).

2. Long Edges: Tapered.

E. Gypsum Ceiling Board: ASTM C 1396/C 1396M.

1. Thickness: 1/2 inch (12.7 mm).

2. Long Edges: Tapered.

The foil backing on gypsum board in "Foil-Backed Gypsum Board" Paragraph below creates a vapor barrier. Verify limitations and proper uses with selected manufacturers.

F. Foil-Backed Gypsum Board: ASTM C 1396/C 1396M.

1. Core: [As indicated on Drawings] [3/8 inch (9.5 mm), regular type] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X] [Type C as required by fire-resistance-rated assembly indicated on Drawings].

2. Long Edges: [Tapered] [Tapered and featured (rounded or beveled) for prefilling].

See "Abuse-Resistant Gypsum Board" Article in the Evaluations for additional information.

G. Abuse-Resistant Gypsum Board: ASTM C 1629/C 1629M, [Level 1] [Level 2] [Level 3].

1. Core: [As indicated on Drawings] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

2. Long Edges: Tapered.

3. Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

H. Moisture- and Mold-Resistant Gypsum Board: ASTM C 1396/C 1396M. With moisture- and mold-resistant core and paper surfaces.

1. Core: [As indicated] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

2. Long Edges: Tapered.

3. Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

2.4 SPECIALTY GYPSUM BOARD

Type C gypsum board from different manufacturers cannot be intermixed because the ratings apply only to assemblies identical in materials and construction to those tested.

A. Gypsum Board, Type C: ASTM C 1396/C 1396M. Manufactured to have increased fire-resistive capability.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Gypsum; Firebloc Type C.

b. CertainTeed Corp.; ProRoc Type C.

c. Georgia-Pacific Gypsum LLC; Fireguard C.

d. Lafarge North America Inc.; Firecheck Type C.

e. National Gypsum Company; Gold Bond Fire-Shield C.

f. PABCO Gypsum; Flame Curb Type Super C.

g. Temple-Inland; Type TG-C.

h. USG Corporation; Firecode C Core.

i. <Insert manufacturer's name; product name or designation>.

Type C gypsum board is available in 1/2- and 5/8-inch (12.7- and 15.9-mm) thicknesses.

2. Thickness: As required by fire-resistance-rated assembly indicated on Drawings.

3. Long Edges: Tapered.

B. Glass-Mat Interior Gypsum Board: ASTM C 1658/C 1658M. With fiberglass mat laminated to both sides. Specifically designed for interior use.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Georgia-Pacific Gypsum LLC; DensArmour Plus.

b. <Insert manufacturer's name; product name or designation>.

2. Core: [As indicated] [1/2 inch (12.7 mm), regular type] [1/2 inch (12.7 mm), Type C] [5/8 inch (15.9 mm), Type X] [5/8 inch (15.9 mm), abuse resistant].

3. Long Edges: Tapered.

4. Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

2.5 EXTERIOR GYPSUM BOARD FOR CEILINGS AND SOFFITS

A. Exterior Gypsum Soffit Board: ASTM C 1396/C 1396M, with manufacturer's standard edges.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Gypsum.

b. CertainTeed Corp.

c. Georgia-Pacific Gypsum LLC.

d. Lafarge North America Inc.

e. National Gypsum Company.

f. PABCO Gypsum.

g. Temple-Inland.

h. USG Corporation.

i. <Insert manufacturer's name>.

2. Core: [As indicated] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

B. Glass-Mat Gypsum Sheathing Board: ASTM C 1177/C 1177M, with fiberglass mat laminated to both sides and with manufacturer's standard edges.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. CertainTeed Corp.; GlasRoc Sheathing.

b. Georgia-Pacific Gypsum LLC; Dens-Glass Gold.

c. National Gypsum Company; Gold Bond, e(2)XP.

d. USG Corporation; Securock Glass Mat Sheathing.

e. <Insert manufacturer's name; product name or designation>.

2. Core: [As indicated] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

2.6 TILE BACKING PANELS

Tile backing panels may be specified in this Section or in Section 093000 "Tiling."

A. Glass-Mat, Water-Resistant Backing Board: ASTM C 1178/C 1178M, with manufacturer's standard edges.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. CertainTeed Corp.; GlasRoc Tile Backer.

b. Georgia-Pacific Gypsum LLC; DensShield Tile Backer.

c. <Insert manufacturer's name; product name or designation>.

2. Core: [As indicated on Drawings] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X].

3. Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

B. Cementitious Backer Units: ANSI A118.9 and ASTM C 1288 or 1325, with manufacturer's standard edges.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. C-Cure; C-Cure Board 990.

b. CertainTeed Corp.; FiberCement [Underlayment] [BackerBoard].

c. Custom Building Products; [Wonderboard] [EasyBoard].

d. FinPan, Inc.; [Util-A-Crete Concrete Backer Board] [EZ Backer] [ProTEC].

e. James Hardie Building Products, Inc.; [Hardiebacker] [Hardiebacker 500].

f. National Gypsum Company, Permabase Cement Board.

g. USG Corporation; DUROCK Cement Board.

h. <Insert manufacturer's name; product name or designation>.

2. Thickness: [1/4 inch (6.4 mm)] [1/2 inch (12.7 mm)] [5/8 inch (15.9 mm)] [As indicated].

3. Mold Resistance: ASTM D 3273, score of 10 as rated according to ASTM D 3274.

According to the 2006 International Building Code, water-resistant gypsum backing board is not permitted for use as a backing board for tile in tub and shower areas or as wall board or ceiling panels in shower areas.

C. Water-Resistant Gypsum Backing Board: ASTM C 1396/C 1396M, with manufacturer's standard edges.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Gypsum.

b. CertainTeed Corp.

c. Georgia-Pacific Gypsum LLC.

d. Lafarge North America Inc.

e. PABCO Gypsum.

f. Temple-Inland.

g. USG Corporation.

h. <Insert manufacturer's name>.

2. Core: [As indicated on Drawings] [1/2 inch (12.7 mm), regular type] [5/8 inch (15.9 mm), Type X] [Type C as required by fire-resistance-rated assembly indicated on Drawings].

2.7 TRIM ACCESSORIES

A. Interior Trim: ASTM C 1047.

1. Material: [Galvanized or aluminum-coated steel sheet, rolled zinc, plastic, or paper-faced galvanized steel sheet] [Galvanized or aluminum-coated steel sheet or rolled zinc] [Plastic] [Paper-faced galvanized steel sheet].

B. Exterior Trim: ASTM C 1047.

1. Material: [Hot-dip galvanized steel sheet, plastic, or rolled zinc] <Insert material>.

C. Aluminum Trim: ASTM B 221 (ASTM B 221M), Alloy 6063-T5.

2.8 JOINT TREATMENT MATERIALS

A. General: Comply with ASTM C 475/C 475M.

B. Joint Tape:

1. Interior Gypsum Board: Paper.

2. Exterior Gypsum Soffit Board: Paper.

3. Glass-Mat Gypsum Sheathing Board: 10-by-10 glass mesh.

4. Tile Backing Panels: As recommended by panel manufacturer.

C. Joint Compound for Interior Gypsum Board: For each coat use formulation that is compatible with other compounds applied on previous or for successive coats.

2.9 AUXILIARY MATERIALS

A. Laminating Adhesive: Adhesive or joint compound recommended for directly adhering gypsum panels to continuous substrate.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1. VOC content limit is that for drywall and panel adhesives.

1. Laminating adhesive shall have a VOC content of [50] <Insert value> g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

2. Laminating adhesive shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

B. Steel Drill Screws: ASTM C 1002, unless otherwise indicated.

C. Sound Attenuation Blankets: ASTM C 665, Type I (blankets without membrane facing).

Retain "Recycled Content of Blankets" Subparagraph below to specify recycled content if applying for LEED Credit MR 4. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

1. Recycled Content of Blankets: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

D. Acoustical Joint Sealant: ASTM C 834. Product effectively reduces airborne sound transmission through perimeter joints and openings as demonstrated by testing according to ASTM E 90.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Accumetric LLC; BOSS 824 Acoustical Sound Sealant.

b. Grabber Construction Products; Acoustical Sealant GSC.

c. Pecora Corporation; [AC-20 FTR] [AIS-919].

d. Specified Technologies, Inc.; Smoke N Sound Acoustical Sealant.

e. USG Corporation; SHEETROCK Acoustical Sealant.

f. <Insert manufacturer's name; product>.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1. VOC content limit is that for architectural sealants.

2. Acoustical joint sealant shall have a VOC content of [250] <Insert value> g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

3. Acoustical joint sealant shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

E. Thermal Insulation: As specified in Section 072100 "Thermal Insulation."

F. Vapor Retarder: As specified in Section 072100 "Thermal Insulation."

2.10 TEXTURE FINISHES

A. Primer: As recommended by textured finish manufacturer.

B. Polystyrene Aggregate Ceiling Finish: Water-based, job-mixed, polystyrene aggregate finish with flame-spread and smoke-developed indexes of not more than 25 when tested according to ASTM E 84.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Georgia-Pacific Gypsum LLC; ToughRock Ceiling Textures/Polystyrene.

b. National Gypsum Company; ProForm Perfect Spray.

c. USG Corporation; SHEETROCK Ceiling Spray Texture, QT.

d. <Insert manufacturer's name; product name or designation>.

2. Texture: [Fine] [Medium] [Coarse].

C. Aggregate Finish: Water-based, job-mixed, aggregated, drying-type texture finish for spray application.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. CertainTeed Corp.; ProRoc Wall and Ceiling Spray Texture.

b. Georgia-Pacific Gypsum LLC; ToughRock Ceiling Textures/Vermiculite.

c. USG Corporation; SHEETROCK Wall and Ceiling Spray Texture (Aggregated).

d. <Insert manufacturer's name; product name or designation>.

2. Texture: [Light spatter] [Spatter knock-down] <Insert texture>.

D. Non-Aggregate Finish: Pre-mixed, vinyl texture finish for spray application.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. CertainTeed Corp.; ProRoc Easi-Tex Spray Texture.

b. National Gypsum Company; Perfect Spray EM Texture.

c. USG Corporation; BEADEX FasTex Wall and Ceiling Spray Texture.

d. <Insert manufacturer's name; product name or designation>.

2. Texture: [Orange Peel] [Spatter] [Spatter knock-down] <Insert texture>.

E. Acoustical Finish: Water-based, chemical-setting or drying-type, job-mixed texture finish for spray application.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. International Cellulose Corp.; SonaSpray "fc."

b. USG Corporation; USG Acoustical Plaster Finish.

c. <Insert manufacturer's name; product name or designation>.

2. Application Thickness: [1/2 inch (12.7 mm)] <Insert thickness>.

3. Surface-Burning Characteristics: ASTM E 84.

a. Flame-Spread Index: [25] <Insert value> or less.

b. Smoke-Developed Index: [50] [450] <Insert value> or less.

4. NRC: [0.55] <Insert NRC> according to ASTM C 423.

PART 3 -  EXECUTION

3.1 APPLYING AND FINISHING PANELS

A. Comply with ASTM C 840.

B. Examine panels before installation. Reject panels that are wet, moisture damaged, and mold damaged.

C. Isolate perimeter of gypsum board applied to non-load-bearing partitions at structural abutments, except floors. Provide 1/4- to 1/2-inch- (6.4- to 12.7-mm-) wide spaces at these locations and trim edges with edge trim where edges of panels are exposed. Seal joints between edges and abutting structural surfaces with acoustical sealant.

D. Install trim with back flanges intended for fasteners, attach to framing with same fasteners used for panels. Otherwise, attach trim according to manufacturer's written instructions.

1. Aluminum Trim: Install in locations [indicated on Drawings] <Insert requirements>.

2. Control Joints: Install control joints [at locations indicated on Drawings] [according to ASTM C 840 and in specific locations approved by Architect for visual effect].

E. Prefill open joints[, rounded or beveled edges,] and damaged surface areas.

F. Apply joint tape over gypsum board joints, except for trim products specifically indicated as not intended to receive tape.

See "Gypsum Board Finish Levels" Article in the Evaluations for a discussion of requirements of various levels.

G. Gypsum Board Finish Levels: Finish panels to levels indicated below and according to ASTM C 840:

1. Level 1: Ceiling plenum areas, concealed areas, and where indicated.

2. Level 2: [Panels that are substrate for tile] [Panels that are substrate for acoustical tile] [Where indicated on Drawings] <Insert locations>.

3. Level 3: [Where indicated on Drawings] <Insert locations>.

4. Level 4: [At panel surfaces that will be exposed to view unless otherwise indicated] <Insert locations>.

a. Primer and its application to surfaces are specified in Section 099123 "Interior Painting."

5. Level 5: [Where indicated on Drawings] <Insert locations>.

a. Primer and its application to surfaces are specified in Section 099123 "Interior Painting."

H. Texture Finish Application: Prepare and apply primer to gypsum panels and other surfaces receiving texture finishes. Mix and apply finish using powered spray equipment, to produce a uniform texture[ matching approved mockup and] free of starved spots or other evidence of thin application or of application patterns.

I. Protect adjacent surfaces from drywall compound and texture finishes and promptly remove from floors and other non-drywall surfaces. Repair surfaces stained, marred, or otherwise damaged during drywall application.

J. Remove and replace panels that are wet, moisture damaged, and mold damaged.

END OF SECTION 092900

	GYPSUM BOARD
	092900 - 1



