Copyright 2011 AIA
MasterSpec Professional
05/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 096516 - RESILIENT SHEET FLOORING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes [vinyl] [and] [rubber] sheet flooring.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for adhesives and chemical-bonding compounds.

1. Product Data for Credit IEQ 4.1: For adhesives[ and chemical-bonding compounds], documentation including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4.1" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit IEQ 4.1: For adhesives, documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

First "Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for adhesives and chemical-bonding compounds.

3. Product Data for Credit IEQ 4.3: For adhesives[ and chemical-bonding compounds], documentation including printed statement of VOC content.

"Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for resilient sheet flooring.

4. Product Data for Credit IEQ 4.3: For resilient sheet flooring, documentation from an independent testing agency indicating compliance with the FloorScore standard.

"Laboratory Test Reports for Credit IEQ 4.3" Subparagraph below applies to LEED for Schools.

5. Laboratory Test Reports for Credit IEQ 4.3: For flooring system[ and chemical bonding compounds], documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain "Shop Drawings" Paragraph below if required.

C. Shop Drawings: For each type of flooring. Include flooring layouts, locations of seams, edges, columns, doorways, enclosing partitions, built-in furniture, cabinets, and cutouts.

1. Show details of special patterns.

D. Samples: For each exposed product and for each color and texture specified in manufacturer's standard size, but not less than [6-by-9-inch (150-by-230-mm)] <Insert dimensions> sections.

1. For heat-welding bead, manufacturer's standard-size Samples, but not less than [9 inches (230 mm)] <Insert dimension> long, of each color required.

1.3 CLOSEOUT SUBMITTALS

A. Maintenance data.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Fire-Test-Response Characteristics" Paragraph below if fire-test-response testing is required by authorities having jurisdiction. In most building codes, resilient flooring is exempt from fire-test-response requirements. See "Fire-Test-Response Characteristics" Article in the Evaluations for additional information.

A. Fire-Test-Response Characteristics: For resilient sheet flooring, as determined by testing identical products according to ASTM E 648 or NFPA 253 by a qualified testing agency.

1. Critical Radiant Flux Classification: Class I, not less than 0.45 W/sq. cm.

Retain "FloorScore Compliance" Paragraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.3; before retaining, verify availability of materials that comply.

B. FloorScore Compliance: Resilient sheet flooring shall comply with requirements of FloorScore certification.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.1 or Credit IEQ 4.3.

C. Low-Emitting Materials: Flooring system shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

2.2 UNBACKED VINYL SHEET FLOORING <Insert drawing designation>

Copy this article and re-edit for each unbacked vinyl sheet flooring product.

Insert drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. Armstrong World Industries, Inc; <Insert product name or designation>.

2. Forbo Industries, Inc; <Insert product name or designation>.

3. Gerflor; <Insert product name or designation>.

4. Johnsonite; A Tarkett Company; <Insert product name or designation>.

5. Mannington Mills, Inc; <Insert product name or designation>.

6. Polyflor, Ltd., Distributed by Gerbert Limited; <Insert product name or designation>.

7. <Insert manufacturer's name; product name or designation>.

B. Product Standard: ASTM F 1913.

C. Thickness: [0.080 inch (2.0 mm)] <Insert dimension>.

D. Wearing Surface: [Smooth] [Embossed].

E. Sheet Width: [As standard with manufacturer] [6 feet (1.8 m)] [6.6 feet (2.0 m)] <Insert width>.

Retain "Seamless-Installation Method" Paragraph below for seamless installation. Generally, manufacturers prefer the appearance and performance of seamless installations produced using heat-welded seams or chemically bonded seams. See "General Comments" Article in the Evaluations for a discussion of seamless installation.

F. Seamless-Installation Method: [Heat welded] [Chemically bonded] <Insert requirements>.

Retain "Colors and Patterns" Paragraph below if colors and patterns are not indicated in a separate schedule.

G. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors] <Insert colors and patterns>.

2.3 VINYL SHEET FLOORING WITH BACKING <Insert drawing designation>

Copy this article and re-edit for each vinyl sheet flooring product with backing.

Insert drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. Altro Group; <Insert product name or designation>.

2. Armstrong World Industries, Inc; <Insert product name or designation>.

3. Congoleum Corporation; <Insert product name or designation>.

4. Forbo Industries, Inc; <Insert product name or designation>.

5. Gerflor; <Insert product name or designation>.

6. Lonseal, Inc; <Insert product name or designation>.

7. Mannington Mills, Inc; <Insert product name or designation>.

8. Polyflor, Ltd., Distributed by Gerbert Limited; <Insert product name or designation>.

9. TOLI International; <Insert product name or designation>.

10. <Insert manufacturer's name; product name or designation>.

B. Product Standard: ASTM F 1303.

1. Type (Binder Content): [Type I, minimum binder content of 90 percent] [Type II, minimum binder content of 34 percent].

2. Wear-Layer Thickness: Grade 1.

3. Overall Thickness: [As standard with manufacturer] <Insert thickness>.

4. Interlayer Material: [Foamed plastic] [None].

5. Backing Class: [Class A (fibrous)] [Class B (nonfoamed plastic)] [Class C (foamed plastic)].

C. Wearing Surface: [Smooth] [Embossed] [Smooth with embedded abrasives] [Embossed with embedded abrasives].

D. Sheet Width: [As standard with manufacturer] [5 feet (1.5 m)] [6 feet (1.8 m)] [6.6 feet (2.0 m)] [12 feet (3.6 m)] <Insert width>.

Retain "Seamless-Installation Method" Paragraph below for seamless installation. Generally, manufacturers prefer the appearance and performance of seamless installations produced using heat-welded seams or chemically bonded seams. See "General Comments" Article in the Evaluations for a discussion of seamless installation.

E. Seamless-Installation Method: [Heat welded] [Chemically bonded] <Insert requirements>.

Retain "Colors and Patterns" Paragraph below if colors and patterns are not indicated in a separate schedule.

F. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors] <Insert colors and patterns>.

2.4 UNBACKED RUBBER SHEET FLOORING <Insert drawing designation>

Copy this article and re-edit for each unbacked rubber sheet flooring product.

Insert drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. AB; American Biltrite; <Insert product name or designation>.

2. Flexco; <Insert product name or designation>.

3. Nora Systems, Inc; <Insert product name or designation>.

4. PRF USA, Inc; <Insert product name or designation>.

5. R.C.A. Rubber Company (The) ; <Insert product name or designation>.

6. VPI, LLC, Floor Products Division; <Insert product name or designation>.

7. <Insert manufacturer's name; product name or designation>.

B. Product Standard: ASTM F 1859.

1. Type: [Type I (homogeneous rubber sheet)] [Type II (layered rubber sheet)].

2. Thickness: [As standard with manufacturer] <Insert thickness>.

See "Rubber Sheet Flooring" Article in the Evaluations for a discussion of hardness values.

3. Hardness: [Not less than required by ASTM F 1859] [Manufacturer's standard hardness, measured using Shore, Type A durometer per ASTM D 2240].

C. Wearing Surface: [Smooth] [Textured] [Molded pattern].

1. Molded-Pattern Figure: [Raised discs] [Raised squares] <Insert pattern>.

D. Sheet Width: [As standard with manufacturer] [3.0 feet (0.9 m)] [3.3 feet (1.0 m)] [4.0 feet (1.2 m)] [5 feet (1.5 m)] [6.3 feet (1.9 m)] <Insert width>.

Retain "Seamless-Installation Method" Paragraph below for seamless installation. Generally, manufacturers prefer the appearance and performance of seamless installations produced using heat-welded seams or chemically bonded seams. See "General Comments" Article in the Evaluations for a discussion of seamless installation.

E. Seamless-Installation Method: [Heat welded] [Chemically bonded] <Insert requirements>.

Retain "Colors and Patterns" Paragraph below if colors and patterns are not indicated in a separate schedule.

F. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors] <Insert colors and patterns>.

2.5 RUBBER SHEET FLOORING WITH BACKING <Insert drawing designation>

Copy this article and re-edit for each rubber sheet flooring product with backing.

Insert drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. Nora Systems, Inc; <Insert product name or designation>.

2. <Insert manufacturer's name; product name or designation>.

B. Product Standard: ASTM F 1860.

1. Type: [Type I, homogeneous rubber sheet with backing] [Type II, layered rubber sheet with backing].

2. Wear-Layer Thickness: [As standard with manufacturer] <Insert thickness>.

For molded-pattern (raised-pattern) rubber sheet, overall thickness is generally measured at the thickest cross-sectional area of flooring product.

3. Overall Thickness: [As standard with manufacturer] <Insert thickness>.

Retain and revise "Interlayer Material" Subparagraph below for Type II, layered rubber sheet with backing.

4. Interlayer Material: [As standard with manufacturer] [None].

5. Backing: [Fibrous] [Foamed rubber].

See "Rubber Sheet Flooring" Article in the Evaluations for a discussion of hardness values.

6. Hardness: [Not less than required by ASTM F 1860] [Manufacturer's standard hardness, measured using Shore, Type A durometer per ASTM D 2240].

C. Wearing Surface: [Smooth] <Insert description>.

D. Sheet Width: [As standard with manufacturer] [3.3 feet (1.0 m)] <Insert width>.

Retain "Seamless-Installation Method" Paragraph below for seamless installation. Generally, manufacturers prefer the appearance and performance of seamless installations produced using heat-welded seams or chemically bonded seams. See "General Comments" Article in the Evaluations for a discussion of seamless installation.

E. Seamless-Installation Method: [Heat welded] [Chemically bonded] <Insert requirements>.

Retain "Colors and Patterns" Paragraph below if colors and patterns are not indicated in a separate schedule.

F. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors] <Insert colors and patterns>.

2.6 INSTALLATION MATERIALS

A. Trowelable Leveling and Patching Compounds: Latex-modified, portland cement based or blended hydraulic-cement-based formulation provided or approved by resilient sheet flooring manufacturer for applications indicated.

B. Adhesives: Water-resistant type recommended by flooring and adhesive manufacturers to suit resilient sheet flooring and substrate conditions indicated.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1 or Credit IEQ 4.3. First option is VOC content limit for vinyl composition tile and asphalt tile adhesives; second is that for rubber floor adhesives.

1. Adhesives shall have a VOC content of [50] [60] <Insert value> g/L or less.

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.1.

2. Adhesives shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

C. Seamless-Installation Accessories:

1. Heat-Welding Bead: Manufacturer's solid-strand product for heat welding seams.

a. Color: [As selected by Architect from manufacturer's full range to contrast with flooring] [Match flooring] <Insert color>.

2. Chemical-Bonding Compound: Manufacturer's product for chemically bonding seams.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1 or Credit IEQ 4.3. VOC content limit is that for PVC welding compounds; LEED does not include a limit for rubber welding compounds.

a. Bonding compound shall have a VOC content of 510 g/L or less.

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.3.

b. Bonding compound shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

D. Integral-Flash-Cove-Base Accessories:

1. Cove Strip: 1-inch (25-mm) radius provided or approved by resilient sheet flooring manufacturer.

2. Cap Strip: [Square metal, vinyl, or rubber cap] [Tapered vinyl cap] <Insert requirements> provided or approved by resilient sheet flooring manufacturer.

Retain "Corners" Subparagraph below if applicable. Not all manufacturers' written installation instructions require metal inside and outside corners.

3. Corners: Metal inside and outside corners and end stops provided or approved by resilient sheet flooring manufacturer.

Retain "Floor Polish" Paragraph below for use with most vinyl sheet flooring. Liquid floor polish is generally used instead of paste wax. See "Maintenance Procedures" Article in the Evaluations for additional information.

E. Floor Polish: Provide protective, liquid floor-polish products recommended by resilient sheet flooring manufacturer.

PART 3 -  EXECUTION

3.1 PREPARATION

Extensive surface preparation is required over substrates from which existing flooring has been removed. Requirements vary among manufacturers. Insert requirements to suit Project.

A. Prepare substrates according to resilient sheet flooring manufacturer's written instructions to ensure adhesion of resilient sheet flooring.

B. Concrete Substrates: Prepare according to ASTM F 710.

1. Verify that substrates are dry and free of curing compounds, sealers, and hardeners.

2. Remove substrate coatings and other substances that are incompatible with adhesives and that contain soap, wax, oil, or silicone, using mechanical methods recommended by resilient sheet flooring manufacturer. Do not use solvents.

3. Alkalinity and Adhesion Testing: Perform tests recommended by resilient sheet flooring manufacturer. Proceed with installation only after substrate alkalinity falls within range on pH scale recommended by manufacturer in writing, but not less than 5 or more than [9] [10] <Insert number> pH.

4. Moisture Testing: Proceed with installation only after substrates pass testing according to resilient sheet flooring manufacturer's written recommendations, but not less stringent than the following:

a. Perform anhydrous calcium chloride test according to ASTM F 1869. Proceed with installation only after substrates have maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m)] <Insert rate> in 24 hours.

b. Perform relative humidity test using in situ probes according to ASTM F 2170. Proceed with installation only after substrates have a maximum [75] <Insert number> percent relative humidity level.

C. Fill cracks, holes, and depressions in substrates with trowelable leveling and patching compound; remove bumps and ridges to produce a uniform and smooth substrate.

D. Do not install resilient sheet flooring until it is the same temperature as the space where it is to be installed.

E. Immediately before installation, sweep and vacuum clean substrates to be covered by resilient sheet flooring.

3.2 RESILIENT SHEET FLOORING INSTALLATION

A. Comply with manufacturer's written instructions for installing resilient sheet flooring.

B. Unroll resilient sheet flooring and allow it to stabilize before cutting and fitting.

C. Lay out resilient sheet flooring as follows:

1. Maintain uniformity of flooring direction.

2. Minimize number of seams; place seams in inconspicuous and low-traffic areas, at least 6 inches (152 mm) away from parallel joints in flooring substrates.

3. Match edges of flooring for color shading at seams.

4. Avoid cross seams.

If required, insert requirements for special patterns here.

If built-in items are required to be set on top of resilient sheet flooring, indicate on Drawings and revise first paragraph below.

D. Scribe and cut resilient sheet flooring to butt neatly and tightly to vertical surfaces, permanent fixtures, and built-in furniture including cabinets, pipes, outlets, and door frames.

E. Extend resilient sheet flooring into toe spaces, door reveals, closets, and similar openings.

F. Maintain reference markers, holes, and openings that are in place or marked for future cutting by repeating on resilient sheet flooring as marked on substrates. Use chalk or other nonpermanent marking device.

Retain first paragraph below for resilient sheet flooring installed on floor covers.

G. Install resilient sheet flooring on covers for telephone and electrical ducts and similar items in installation areas. Maintain overall continuity of color and pattern between pieces of flooring installed on covers and adjoining flooring. Tightly adhere flooring edges to substrates that abut covers and to cover perimeters.

H. Adhere resilient sheet flooring to substrates using a full spread of adhesive applied to substrate to produce a completed installation without open cracks, voids, raising and puckering at joints, telegraphing of adhesive spreader marks, and other surface imperfections.

Retain "Seamless Installation" Paragraph below if required.

I. Seamless Installation:

1. Heat-Welded Seams: Comply with ASTM F 1516. Rout joints and heat weld with welding bead to permanently fuse sections into a seamless flooring. Prepare, weld, and finish seams to produce surfaces flush with adjoining flooring surfaces.

2. Chemically Bonded Seams: Bond seams with chemical-bonding compound to permanently fuse sections into a seamless flooring. Prepare seams and apply compound to produce tightly fitted seams without gaps, overlays, or excess bonding compound on flooring surfaces.

J. Integral-Flash-Cove Base: Cove resilient sheet flooring [6 inches (152 mm)] [to dimension indicated] <Insert dimension> up vertical surfaces. Support flooring at horizontal and vertical junction with cove strip. Butt at top against cap strip.

Retain subparagraph below for metal corners.

1. Install metal corners at inside and outside corners.

3.3 CLEANING AND PROTECTION

A. Comply with manufacturer's written instructions for cleaning and protecting resilient sheet flooring.

Before retaining "Floor Polish" Paragraph below, verify manufacturer's written instructions for floor polish. Floor polish is used with most vinyl sheet flooring.

B. Floor Polish: Remove soil, adhesive, and blemishes from flooring surfaces before applying liquid floor polish.

Revise subparagraph below to suit products.

1. Apply [one] [two] [three] <Insert requirement> coat(s).

C. Cover resilient sheet flooring until Substantial Completion.

END OF SECTION 096516

	RESILIENT SHEET FLOORING
	096516 - 1



