Copyright 2011 AIA
MasterSpec Professional
05/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 096519 - RESILIENT TILE FLOORING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Solid vinyl floor tile.

2. Rubber floor tile.

3. Vinyl composition floor tile.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for adhesives and sealants.

1. Product Data for Credit IEQ 4.1: For adhesives [and] [sealants], documentation including printed statement of VOC content.

"Laboratory Test Reports for Credit IEQ 4.1" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit IEQ 4.1: For adhesives, documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

First "Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for adhesives.

3. Product Data for Credit IEQ 4.3: For adhesives, documentation including printed statement of VOC content.

"Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for resilient tile flooring.

4. Product Data for Credit IEQ 4.3: For resilient tile flooring, documentation from an independent testing agency indicating compliance with the FloorScore standard.

"Laboratory Test Reports for Credit IEQ 4.3" Subparagraph below applies to LEED for Schools.

5. Laboratory Test Reports for Credit IEQ 4.3: For flooring system, documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain "Shop Drawings" Paragraph below if required.

C. Shop Drawings: For each type of floor tile. Include floor tile layouts, edges, columns, doorways, enclosing partitions, built-in furniture, cabinets, and cutouts.

1. Show details of special patterns.

D. Samples: Full-size units of each color and pattern of floor tile required.

1.3 CLOSEOUT SUBMITTALS

A. Maintenance data.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Fire-Test-Response Characteristics" Paragraph below if fire-test-response testing is required by authorities having jurisdiction. In most building codes, resilient flooring is exempt from fire-test-response requirements. See "Fire-Test-Response Characteristics" Article in the Evaluations for additional information.

A. Fire-Test-Response Characteristics: For resilient tile flooring, as determined by testing identical products according to ASTM E 648 or NFPA 253 by a qualified testing agency.

1. Critical Radiant Flux Classification: Class I, not less than 0.45 W/sq. cm.

Retain "FloorScore Compliance" Paragraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.3; before retaining, verify availability of materials that comply.

B. FloorScore Compliance: Resilient tile flooring shall comply with requirements of FloorScore certification.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.1 or Credit IEQ 4.3.

C. Low-Emitting Materials: Flooring system shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

2.2 SOLID VINYL FLOOR TILE <Insert drawing designation>

Copy this article and re-edit for each solid vinyl product.

Insert drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. AB; American Biltrite; <Insert product name or designation>.

2. Altro Group; <Insert product name or designation>.

3. Amtico International Inc; <Insert product name or designation>.

4. Armstrong World Industries, Inc; <Insert product name or designation>.

5. Burke Mercer Flooring Products, Division of Burke Industries Inc; <Insert product name or designation>.

6. Flexco, Inc; <Insert product name or designation>.

7. Gerflor; <Insert product name or designation>.

8. Johnsonite; A Tarkett Company; <Insert product name or designation>.

9. Polyflor, Ltd; <Insert product name or designation>.

10. Roppe Corporation, USA; <Insert product name or designation>.

11. TOLI International; <Insert product name or designation>.

12. <Insert manufacturer's name; product name or designation>.

B. Tile Standard: ASTM F 1700.

1. Class: [As indicated by product designations] [Class I, monolithic vinyl tile] [Class II, surface-decorated vinyl tile] [Class III, printed film vinyl tile].

2. Type: [A, smooth surface] [B, embossed surface].

C. Thickness: [0.080 inch (2.0 mm)] [0.100 inch (2.5 mm)] [0.120 inch (3.0 mm)] [0.125 inch (3.2 mm)] <Insert dimension>.

Tiles do not have to be square shaped. If other shapes are required, insert requirements in "Size" Paragraph below.

D. Size: [12 by 12 inches (305 by 305 mm)] [18 by 18 inches (457 by 457 mm)] [24 by 24 inches (610 by 610 mm)] [36 by 36 inches (914 by 914 mm)] [3 by 36 inches (76 by 914 mm)] <Insert dimensions>.

Retain "Color and Patterns" Paragraph below if colors and patterns are not indicated in a separate schedule.

E. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors] <Insert colors and patterns>.

2.3 RUBBER FLOOR TILE <Insert drawing designation>

Copy this article and re-edit for each rubber product.

Insert drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. AB; American Biltrite; <Insert product name or designation>.

2. Burke Mercer Flooring Products, Division of Burke Industries Inc; <Insert product name or designation>.

3. Flexco; <Insert product name or designation>.

4. Johnsonite; A Tarkett Company; <Insert product name or designation>.

5. Mannington Mills, Inc; <Insert product name or designation>.

6. Mondo Rubber International, Inc; <Insert product name or designation>.

7. Nora Rubber Flooring, Freudenberg Building Systems, Inc; <Insert product name or designation>.

8. PRF USA Inc; <Insert product name or designation>.

9. R.C.A. Rubber Company (The) ; <Insert product name or designation>.

10. Roppe Corporation, USA; <Insert product name or designation>.

11. VPI, LLC, Floor Products Division; <Insert product name or designation>.

12. <Insert manufacturer's name; product name or designation>.

B. Tile Standard: ASTM F 1344, [Class I-A, homogeneous rubber tile, solid color] [Class I-B, homogeneous rubber tile, through mottled] [Class II-A, laminated rubber tile, solid-color wear layer] [Class II-B, laminated rubber tile, mottled wear layer].

See "Rubber Floor Tile" Article in the Evaluations for a discussion of hardness values.

C. Hardness: [Not less than 85 as required by ASTM F 1344] [Manufacturer's standard hardness], measured using Shore, Type A durometer per ASTM D 2240.

D. Wearing Surface: [Smooth] [Textured] [Molded pattern].

1. Molded-Pattern Figure: [Raised discs] [Raised squares] <Insert pattern>.

For molded-pattern (raised-pattern) rubber tile, overall thickness is generally measured at the thickest cross-sectional area of the flooring product. Revise "Thickness" Paragraph below to include overall thickness for molded-pattern rubber tile.

E. Thickness: [0.125 inch (3.2 mm)] <Insert dimension>.

F. Size: [12 by 12 inches (305 by 305 mm)] [24 by 24 inches (610 by 610 mm)] <Insert dimensions>.

Retain "Colors and Patterns" Paragraph below if colors and patterns are not indicated in a separate schedule.

G. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors] <Insert colors and patterns>.

2.4 VINYL COMPOSITION FLOOR TILE <Insert drawing designation>

Copy this article and re-edit for each vinyl composition product.

Insert drawing designation. Use these designations on Drawings to identify each product.

Retain "Products" Paragraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

A. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

1. AB; American Biltrite; <Insert product name or designation>.

2. Armstrong World Industries, Inc; <Insert product name or designation>.

3. Congoleum Corporation; <Insert product name or designation>.

4. Mannington Mills, Inc; <Insert product name or designation>.

5. <Insert manufacturer's name; product name or designation>.

B. Tile Standard: ASTM F 1066, [Class 1, solid-color] [Class 2, through-pattern] [Class 3, surface-pattern] tile.

C. Wearing Surface: [Smooth] [Embossed].

A limited number of products are available in 3/32- and 3/16-inch (2.4- and 4.8-mm) thicknesses; if applicable, insert in "Thickness" Paragraph below.

D. Thickness: [0.125 inch (3.2 mm)] <Insert dimension>.

E. Size: 12 by 12 inches (305 by 305 mm).

Retain "Colors and Patterns" Paragraph below if colors and patterns are not indicated in a separate schedule.

F. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from full range of industry colors] <Insert colors and patterns>.

2.5 INSTALLATION MATERIALS

A. Trowelable Leveling and Patching Compounds: Latex-modified, portland cement based or blended hydraulic-cement-based formulation provided or approved by floor tile manufacturer for applications indicated.

B. Adhesives: Water-resistant type recommended by floor tile and adhesive manufacturers to suit floor tile and substrate conditions indicated.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1 or Credit IEQ 4.3.

1. Adhesives shall comply with the following limits for VOC content:

a. Vinyl Composition Tile Adhesives: 50 g/L or less.

b. Rubber Floor Adhesives: 60 g/L or less.

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.1.

2. Adhesives shall comply with the testing and product requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain "Floor Polish" Paragraph below for use with most vinyl composition floor tile and some solid vinyl floor tile. Liquid floor polish is generally used instead of paste wax. See "Maintenance Procedures" Article in the Evaluations for additional information.

C. Floor Polish: Provide protective, liquid floor-polish products recommended by floor tile manufacturer.

PART 3 -  EXECUTION

3.1 PREPARATION

Extensive surface preparation is required over substrates from which existing flooring has been removed. Requirements vary among manufacturers. Insert requirements to suit Project.

A. Prepare substrates according to floor tile manufacturer's written instructions to ensure adhesion of resilient products.

B. Concrete Substrates: Prepare according to ASTM F 710.

1. Verify that substrates are dry and free of curing compounds, sealers, and hardeners.

2. Remove substrate coatings and other substances that are incompatible with adhesives and that contain soap, wax, oil, or silicone, using mechanical methods recommended by floor tile manufacturer. Do not use solvents.

3. Alkalinity and Adhesion Testing: Perform tests recommended by floor tile manufacturer. Proceed with installation only after substrate alkalinity falls within range on pH scale recommended by manufacturer in writing, but not less than 5 or more than [9] [10] <Insert number> pH.

4. Moisture Testing: Proceed with installation only after substrates pass testing according to floor tile manufacturer's written recommendations, but not less stringent than the following:

a. Perform anhydrous calcium chloride test according to ASTM F 1869. Proceed with installation only after substrates have maximum moisture-vapor-emission rate of [3 lb of water/1000 sq. ft. (1.36 kg of water/92.9 sq. m)] <Insert rate> in 24 hours.

b. Perform relative humidity test using in situ probes according to ASTM F 2170. Proceed with installation only after substrates have a maximum [75] <Insert number> percent relative humidity level.

Retain "Access Flooring Panels" Paragraph below for floor tile installed on access flooring.

C. Access Flooring Panels: Remove protective film of oil or other coating using method recommended by access flooring manufacturer.

D. Fill cracks, holes, and depressions in substrates with trowelable leveling and patching compound; remove bumps and ridges to produce a uniform and smooth substrate.

E. Do not install floor tiles until they are the same temperature as the space where they are to be installed.

F. Immediately before installation, sweep and vacuum clean substrates to be covered by resilient floor tile.

3.2 FLOOR TILE INSTALLATION

A. Comply with manufacturer's written instructions for installing floor tile.

B. Lay out floor tiles from center marks established with principal walls, discounting minor offsets, so tiles at opposite edges of room are of equal width. Adjust as necessary to avoid using cut widths that equal less than one-half tile at perimeter.

1. Lay tiles [square with room axis] [at a 45-degree angle with room axis] [in pattern indicated] <Insert requirements>.

C. Match floor tiles for color and pattern by selecting tiles from cartons in the same sequence as manufactured and packaged, if so numbered. Discard broken, cracked, chipped, or deformed tiles.

1. Lay tiles [with grain running in one direction] [with grain direction alternating in adjacent tiles (basket-weave pattern)] [in pattern of colors and sizes indicated].

If built-in items are required to be set on top of floor tile, indicate on Drawings and revise first paragraph below.

D. Scribe, cut, and fit floor tiles to butt neatly and tightly to vertical surfaces and permanent fixtures including built-in furniture, cabinets, pipes, outlets, and door frames.

E. Extend floor tiles into toe spaces, door reveals, closets, and similar openings. Extend floor tiles to center of door openings.

F. Maintain reference markers, holes, and openings that are in place or marked for future cutting by repeating on floor tiles as marked on substrates. Use chalk or other nonpermanent marking device.

Retain first paragraph below for floor tile installed on floor covers.

G. Install floor tiles on covers for telephone and electrical ducts, building expansion-joint covers, and similar items in finished floor areas. Maintain overall continuity of color and pattern between pieces of tile installed on covers and adjoining tiles. Tightly adhere tile edges to substrates that abut covers and to cover perimeters.

Revise paragraph below if other-than-full-spread adhesive method is recommended by manufacturer for substrate and tile products.

H. Adhere floor tiles to flooring substrates using a full spread of adhesive applied to substrate to produce a completed installation without open cracks, voids, raising and puckering at joints, telegraphing of adhesive spreader marks, and other surface imperfections.

3.3 CLEANING AND PROTECTION

A. Comply with manufacturer's written instructions for cleaning and protecting floor tile.

Before retaining "Floor Polish" Paragraph below, verify manufacturer's written instructions for floor polish. Floor polish is used with most vinyl composition floor tile and some solid vinyl floor tile.

B. Floor Polish: Remove soil, adhesive, and blemishes from floor tile surfaces before applying liquid floor polish.

Revise subparagraph below to suit products.

1. Apply [one] [two] [three] <Insert requirements> coat(s).

C. Cover floor tile until Substantial Completion.

END OF SECTION 096519

	RESILIENT TILE FLOORING
	096519 - 1



