Copyright 2012 AIA
MasterSpec Professional
02/12

Copyright 2012 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 096623 - RESINOUS MATRIX TERRAZZO FLOORING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes thin-set, epoxy-resin terrazzo flooring[ and base].

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Product Data for Credit IEQ 4.1" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for adhesives.

2. Product Data for Credit IEQ 4.1: For adhesives, documentation including printed statement of VOC content.

"Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for sealers.

3. Product Data for Credit IEQ 4.3: For sealers, documentation including printed statement of VOC content.

"Product Data for Credit IEQ 4.3" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS; coordinate with requirements for flooring system.

4. Product Data for Credit IEQ 4.3: For terrazzo flooring, documentation from an independent testing agency indicating compliance with the FloorScore Standard.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

5. Laboratory Test Reports for Credit IEQ 4: For [adhesives] [and] [flooring system], documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings: Include terrazzo installation requirements. Include plans, elevations, sections, component details, and attachments to other work.

D. Samples: For each exposed product and for each color and texture specified.

1.3 CLOSEOUT SUBMITTALS

A. Maintenance data.

1.4 QUALITY ASSURANCE

A. Installer Qualifications: Engage an installer who is a contractor member of NTMA.

B. Mockups: Build mockups to verify selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

1.5 FIELD CONDITIONS

A. Environmental Limitations: Comply with manufacturer's written instructions for substrate temperature, ambient temperature, moisture, ventilation, and other conditions affecting terrazzo installation.

B. Control and collect water and dust produced by grinding operations. Protect adjacent construction from detrimental effects of grinding operations.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations in Section 096600 "Terrazzo Flooring" for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

A. NTMA Standards: Comply with NTMA's "Terrazzo Specifications and Design Guide" and with written recommendations for terrazzo type indicated unless more stringent requirements are specified.

Retain "FloorScore Compliance" Paragraph below if required for LEED-NC, LEED-CS, or LEED-CI Credit IEQ 4.3.

B. FloorScore Compliance: Terrazzo floors shall comply with requirements of FloorScore Standard.

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools Credit IEQ 4.

C. Low-Emitting Materials: Flooring system shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

2.2 EPOXY-RESIN TERRAZZO

Copy and re-edit "Epoxy-Resin Terrazzo" Paragraph below if more than one type is required; insert a unique designation for each type and indicate locations on Drawings. Polyacrylate-modified cement and polyester-resin terrazzo are not included in the Section Text but may be inserted if required.

A. Epoxy-Resin Terrazzo <Insert designation>: Comply with NTMA's "Terrazzo Specifications and Design Guide" and manufacturer's written instructions for matrix and aggregate proportions and mixing.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Crossfield Products Corp., Dex-O-Tex Division; [Cheminert] [Spectrum].

b. General Polymers; Sherwin Williams; Terrazzo 1100.

c. Key Resin Company; Key Epoxy Terrazzo.

d. Master Terrazzo Technologies LLC; Morricite.

e. Quadrant Chemical Corporation; Quadset Epoxy Terrazzo.

f. TEC Specialty; H.B. Fuller Construction Products Inc; Tuff-Lite Epoxy Terrazzo.

g. Terrazzo & Marble Supply Companies; Terroxy Resin Systems.

h. <Insert manufacturer's name; product name or designation>.

2. Thickness: [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)] [As indicated] <Insert dimension> nominal.

Retain "Mix Color and Pattern" Subparagraph below for NTMA-formulated design mixes. Mixes that match NTMA thin-set plates are available but generally require a 3/8-inch (9.5-mm) topping thickness.

3. Mix Color and Pattern: [As selected by Architect from full range of industry colors] [As selected by Architect from NTMA standard-terrazzo plates] [As selected by Architect from NTMA thin-set terrazzo plates] <Insert manufacturer's or NTMA's color plate designation> <Insert custom design-mix attributes>.

B. Materials:

Retain "Flexible Reinforcing Membrane" Subparagraph below if required.

1. Flexible Reinforcing Membrane: Manufacturer's resinous membrane[ with fiberglass scrim] for substrate-crack preparation and reflective-crack reduction.

2. Primer: [Manufacturer's product recommended for substrate and use indicated] <Insert requirements>.

3. Epoxy-Resin Matrix: [Manufacturer's standard recommended for use indicated] <Insert requirements> and in color required for mix indicated.

"Physical Properties without Aggregates" and "Physical Properties with Aggregates" subparagraphs below are based on NTMA's "Terrazzo Specifications and Design Guide." Revise to suit Project. If conductive system is required, insert electrical-resistance requirements.

a. Physical Properties without Aggregates:

1) Hardness: 60 to 85 per ASTM D 2240, Shore D.

2) Minimum Tensile Strength: 3000 psi (20.7 MPa) per ASTM D 638 for a 2-inch (51-mm) specimen made using a "C" die per ASTM D 412.

3) Minimum Compressive Strength: 10,000 psi (6.9 MPa) per ASTM D 695, Specimen B cylinder.

4) Chemical Resistance: No deleterious effects by contaminants listed below after seven-day immersion at room temperature per ASTM D 1308.

a) Distilled water.

b) Mineral water.

c) Isopropanol.

d) Ethanol.

e) 0.025 percent detergent solution.

f) 1.0 percent soap solution.

g) 10 percent sodium hydroxide.

h) 10 percent hydrochloric acid.

i) 30 percent sulfuric acid.

j) 5 percent acetic acid.

b. Physical Properties with Aggregates: For resin blended with Georgia white marble, ground, grouted, and cured per requirements in NTMA's "Terrazzo Specifications and Design Guide"; comply with the following:

1) Flammability: Self-extinguishing, maximum extent of burning 1/4 inch (6.35 mm) per ASTM D 635.

2) Thermal Coefficient of Linear Expansion: 0.0025 inch/inch per deg F (0.0025 mm/mm per 0.5556 deg C) for temperature range of minus 12 to plus 140 deg F (minus 24 to plus 60 deg C) per ASTM D 696.

4. Aggregates: Comply with NTMA gradation standards for mix indicated and contain no deleterious or foreign matter.

a. Abrasion and Impact Resistance: Less than 40 percent loss per ASTM C 131.

b. 24-Hour Absorption Rate: Less than 0.75 percent.

c. Dust Content: Less than 1.0 percent by weight.

Retain "Recycled Content of Epoxy-Resin Terrazzo" Subparagraph below to specify recycled content if applying for LEED Credit MR 4. An alternative method of dealing with these credit requirements is to retain requirement in Section 018113.13 "Sustainable Design Requirements - LEED for New Construction and Major Renovations," Section 018113.16 "Sustainable Design Requirements - LEED for Commercial Interiors," Section 018113.19 "Sustainable Design Requirements - LEED for Core and Shell Development," Section 018113.23 "Sustainable Design Requirements - LEED for Schools" that gives Contractor the option and responsibility to determine how these credit requirements will be met.

d. Recycled Content of Epoxy-Resin Terrazzo: Postconsumer recycled content plus one-half of preconsumer recycled content not less than <Insert number> percent.

5. Finishing Grout: Resin based.

2.3 STRIP MATERIALS

See "Strip Materials" Article in the Evaluations in Section 096600 "Terrazzo Flooring" for discussion of strip-material types, finishes, and placement.

A. Thin-Set Divider Strips: L-type angle, 1/4 inch (6.4 mm) deep.

Brass may react with resinous matrices. Verify that material retained in "Material" Subparagraph below is acceptable to terrazzo manufacturers.

1. Material: [As indicated] [White-zinc alloy] [Brass] [Aluminum] [Plastic, in color selected from full range of industry colors] <Insert requirements>.

2. Top Width: [As indicated] [1/8 inch (3.2 mm)] [1/4 inch (6.4 mm)] <Insert dimension>.

B. Heavy-Top Divider Strips: L-type angle in depth required for topping thickness indicated.

1. Bottom-Section Material: [As indicated] [Galvanized steel] [Matching top-section material] <Insert requirements>.

Brass may react with resinous matrices. Verify that material retained in "Top-Section Material" Subparagraph below is acceptable to terrazzo manufacturers.

2. Top-Section Material: [As indicated] [White-zinc alloy] [Brass] [Aluminum] [Plastic, in color selected from full range of industry colors] <Insert requirements>.

3. Top-Section Width: [As indicated] [1/8 inch (3.2 mm)] [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)] <Insert dimension>.

C. Control-Joint Strips: Separate, double L-type angles, positioned back to back, that match material and color of divider strips and in depth required for topping thickness indicated.

D. Accessory Strips: Match divider-strip width, material, and color unless otherwise indicated. Use the following types of accessory strips as required to provide a complete installation:

1. Base-bead strips for exposed top edge of terrazzo base.

2. Edge-bead strips for exposed edges of terrazzo.

3. Nosings for terrazzo stair treads and landings.

4. <Insert requirements>.

Retain "Abrasive Strips" Paragraph below for terrazzo stair treads and landings.

E. Abrasive Strips: [Three-line] [Two-line] [One-line] [Abrasive nosing strip and two-line] <Insert requirements> abrasive inserts at nosings. Silicon carbide or aluminum oxide, or combination of both, in epoxy-resin binder and set in channel.

1. Width: [1/2 inch (12.7 mm)] <Insert dimension>.

2. Depth: As required by terrazzo thickness.

3. Length: [4 inches (100 mm) less than stair width] [As indicated] <Insert dimension>.

4. Color: [As selected by Architect from full range of industry colors] <Insert requirements>.

2.4 MISCELLANEOUS ACCESSORIES

A. Strip Adhesive: Epoxy-resin adhesive recommended by adhesive manufacturer for this use.

Retain first subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.1. VOC content limit is that for multipurpose construction adhesives.

1. Adhesives shall have a VOC content of 70 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

Retain subparagraph below if required for LEED for Schools Credit IEQ 4.

2. Adhesives shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

B. Strip Anchoring Devices: Provide mechanical anchoring devices or adhesives for strip materials as recommended by manufacturer and required for secure attachment to substrate.

C. Patching and Fill Material: Terrazzo manufacturer's resinous product approved and recommended by manufacturer for application indicated.

D. Joint Compound: Terrazzo manufacturer's resinous product approved and recommended by manufacturer for application indicated.

E. Resinous Matrix Terrazzo Cleaner: Chemically neutral cleaner with pH factor between 7 and 10 that is biodegradable, phosphate free, and recommended by sealer manufacturer for use on terrazzo type indicated.

Revise "Sealer" Paragraph below for sealer type. Consult NTMA and terrazzo manufacturers for recommendations.

F. Sealer: [Slip- and stain-resistant, penetrating-type sealer that is chemically neutral; does not affect terrazzo color or physical properties; is recommended by sealer manufacturer; and complies with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated] [Acrylic] [Urethane] [Chemical-resistant epoxy] <Insert requirements>.

1. Surface Friction: Not less than 0.6 according to ASTM D 2047.

2. Acid-Base Properties: With pH factor between 7 and 10.

Retain subparagraph below if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.3.

3. Sealers shall have a VOC content of 200 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

PART 3 -  EXECUTION

3.1 PREPARATION

A. Clean substrates of substances, including oil, grease, and curing compounds, that might impair terrazzo bond. Provide clean, dry, and neutral substrate for terrazzo application.

Retain "Concrete Slabs" Paragraph below for concrete substrates or insert requirements for other substrates such as wood or quarry tile; consult manufacturers for recommendations.

B. Concrete Slabs:

1. Provide sound concrete surfaces free of laitance, glaze, efflorescence, curing compounds, form-release agents, dust, dirt, grease, oil, and other contaminants incompatible with terrazzo.

a. Shot-blast surfaces with an apparatus that abrades the concrete surface, contains the dispensed shot within the apparatus, and recirculates the shot by vacuum pickup.

b. Repair damaged and deteriorated concrete according to terrazzo manufacturer's written recommendations.[ Install flexible reinforcing membrane at substrate cracks in areas to receive terrazzo.]

c. Use patching and fill material to fill holes and depressions in substrates according to terrazzo manufacturer's written instructions.

C. Verify that concrete substrates are dry and moisture-vapor emissions are within acceptable levels according to manufacturer's written instructions.

1. Moisture Testing: Test for moisture content by [method recommended in writing by terrazzo manufacturer] [calcium chloride test] [in-situ probe test] <Insert test method>. Proceed with installation only after substrates pass testing.

3.2 EPOXY-RESIN TERRAZZO INSTALLATION

A. Comply with NTMA's written recommendations for terrazzo and accessory installation.

B. Place according to manufacturer's written instructions and NTMA's "Terrazzo Specifications and Design Guide."

C. Installation Tolerance: Limit variation in terrazzo surface from level to [1/4 inch in 10 feet (6.4 mm in 3 m)] <Insert dimensions>; noncumulative.

D. Primer: Apply to terrazzo substrates according to manufacturer's written instructions.

Revise "Strip Materials" Paragraph below to suit Project. Indicate location and spacing of strip materials on Drawings or insert below.

E. Strip Materials:

1. Divider and Control-Joint Strips:

a. Locate divider strips [in locations indicated] <Insert requirements>.

b. Install control-joint strips [back to back directly above concrete-slab control joints] [in locations indicated] <Insert requirements>.

c. Install control-joint strips with [1/4-inch (6.4-mm)] <Insert dimension> gap between strips, and install sealant in gap.

d. Install strips in adhesive setting bed without voids below strips, or mechanically anchor strips as required to attach strips to substrate, as recommended by strip manufacturer.

Retain "Accessory Strips" Subparagraph below for accessory strips.

2. Accessory Strips: Install [as required to provide a complete installation] [in locations indicated] <Insert requirements>.

Retain "Abrasive Strips" Subparagraph below for abrasive strips.

3. Abrasive Strips: Install with surface of abrasive strip positioned [1/16 inch (1.6 mm)] <Insert dimension> higher than terrazzo surface.

F. Repair: Cut out and replace terrazzo areas that evidence lack of bond with substrate. Cut out terrazzo areas in panels defined by strips and replace to match adjacent terrazzo, or repair panels according to NTMA's written recommendations, as approved by Architect.

3.3 CLEANING AND PROTECTION

A. Cleaning:

1. Remove grinding dust from installation and adjacent areas.

2. Wash surfaces with cleaner according to NTMA's written recommendations and manufacturer's written instructions; rinse surfaces with water and allow them to dry thoroughly.

B. Sealing:

1. Seal surfaces according to NTMA's written recommendations.

2. Apply sealer according to sealer manufacturer's written instructions.

C. Protection: Provide final protection and maintain conditions, in a manner acceptable to Installer, that ensure that terrazzo is without damage or deterioration at time of Substantial Completion.

END OF SECTION 096623

	RESINOUS MATRIX TERRAZZO FLOORING
	096623 - 1



