Copyright 2011 AIA
MasterSpec Professional
02/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 099113 - EXTERIOR PAINTING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes surface preparation and the application of paint systems on [exterior substrates.] [the following exterior substrates:]

1. Concrete.

2. Clay masonry.

3. Concrete masonry units (CMU).

4. Steel.

5. Galvanized metal.

6. Aluminum (not anodized or otherwise coated).

7. Stainless-steel flashing.

8. Wood.

9. Plastic trim fabrications.

10. Exterior portland cement plaster (stucco).

11. Exterior gypsum board.

1.2 DEFINITIONS

Definitions of gloss levels below are from "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").

Retain terms that remain after this Section has been edited for a project.

A. Gloss Level 1: Not more than 5 units at 60 degrees and 10 units at 85 degrees, according to ASTM D 523.

B. Gloss Level 3: 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, according to ASTM D 523.

C. Gloss Level 4: 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, according to ASTM D 523.

D. Gloss Level 5: 35 to 70 units at 60 degrees, according to ASTM D 523.

E. Gloss Level 6: 70 to 85 units at 60 degrees, according to ASTM D 523.

F. Gloss Level 7: More than 85 units at 60 degrees, according to ASTM D 523.

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product. Include preparation requirements and application instructions.

B. Samples: For each type of paint system and each color and gloss of topcoat.

C. Product List: For each product indicated. Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

1.4 MAINTENANCE MATERIAL SUBMITTALS

A. Furnish extra materials[, from the same product run,] that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Retain "Paint" Subparagraph below for projects that require only limited quantities of extra materials. If necessary, replace percentage with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

1. Paint: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert number> of each material and color applied.

1.5 QUALITY ASSURANCE

A. Mockups: Apply mockups of each paint system indicated and each color and finish selected to verify preliminary selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

1. Architect will select one surface to represent surfaces and conditions for application of each paint system specified in Part 3.

a. Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

b. Other Items: Architect will designate items or areas required.

2. Final approval of color selections will be based on mockups.

a. If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations in SECTION 099100 "Painting" for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 MANUFACTURERS

Retain "Products" Paragraph below and insert lists of manufacturers and products in other Part 2 articles to require specific products or a comparable product from other manufacturers.

See lists of products currently approved by MPI in its "MPI Approved Products List," www.paintinfo.com. See "Writing Guide" Article in the Evaluations in Section 099100 "Painting" for further discussion.

A. Products: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include, but are not limited to products] listed in other Part 2 articles for the paint category indicated.

2.2 PAINT, GENERAL

A. MPI Standards: Provide products that comply with MPI standards indicated and that are listed in its "MPI Approved Products List."

B. Material Compatibility:

Systems could fail if paints used for individual coats are incompatible. MPI's paint systems match primers and topcoats and take compatibility into consideration.

1. Provide materials for use within each paint system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

2. For each coat in a paint system, provide products recommended in writing by manufacturers of topcoat for use in paint system and on substrate indicated.

C. VOC Content: Provide materials that comply with VOC limits of authorities having jurisdiction.

D. Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

1. [10] [20] [30] <Insert number> percent of surface area will be painted with deep tones.

Manufacturers' names and product designations can be inserted in subsequent articles. Paints in these articles are specified by reference to MPI paint categories and optional MPI numbers. Note that each paint category below is unique within this Section and is identical to that used in the Exterior Painting Schedule at the end of Part 3.

If retaining subsequent articles, first revise the Exterior Painting Schedule; then retain, delete, and insert appropriate products in subsequent articles to correspond with paint systems specified in the Exterior Painting Schedule.

2.3 BLOCK FILLERS

A. Block Filler, Latex, Interior/Exterior:[ MPI #4.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.4 PRIMERS/SEALERS

A. Primer, Alkali Resistant, Water Based:[ MPI #3.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

B. Primer, Bonding, Water Based:[ MPI #17.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

C. Primer, Bonding, Solvent Based:[ MPI #69.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

D. Wood-Knot Sealer: Sealer recommended in writing by topcoat manufacturer for exterior use in paint system indicated.

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.5 METAL PRIMERS

A. Primer, Alkyd, Anti-Corrosive for Metal:[ MPI #79.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

B. Primer, Alkyd, Quick Dry, for Metal:[ MPI #76.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

C. Primer, Galvanized, Water Based:[ MPI #134.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

D. Primer, Galvanized: As recommended in writing by topcoat manufacturer.

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

E. Primer, Quick Dry, for Aluminum:[ MPI #95.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.6 WOOD PRIMERS

A. Primer, Latex for Exterior Wood:[ MPI #6.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

B. Primer, Alkyd for Exterior Wood:[ MPI #5.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

C. Primer, Oil for Exterior Wood:[ MPI #7.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.7 WATER-BASED PAINTS

A. Latex, Exterior Flat (Gloss Level 1):[ MPI #10.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

B. Latex, Exterior Semi-Gloss (Gloss Level 5):[ MPI #11.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

C. Latex, Exterior, Gloss (Gloss Level 6:[ MPI #119.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

D. Light Industrial Coating, Exterior, Water Based (Gloss Level 3):[ MPI #161.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

E. Light Industrial Coating, Exterior, Water Based, Semi-Gloss (Gloss Level 5):[ MPI #163.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

F. Light Industrial Coating, Exterior, Water Based, Gloss (Gloss Level 6):[ MPI #164.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.8 SOLVENT-BASED PAINTS

A. Alkyd, Exterior Flat (Gloss Level 1):[ MPI #8.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

B. Alkyd, Exterior, Semi-Gloss (Gloss Level 5):[ MPI #94.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

C. Alkyd, Exterior Gloss (Gloss Level 6):[ MPI #9.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

D. Alkyd, Quick Dry, Semi-Gloss (Gloss Level 5):[ MPI #81.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

E. Alkyd, Quick Dry, Gloss (Gloss Level 7):[ MPI #96.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.9 TEXTURED AND HIGH-BUILD COATINGS

A. Primer for Textured Coating, Latex, Flat: As recommended in writing by topcoat manufacturer.

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

B. Intermediate Coat for Textured Coating, Latex, Flat: As recommended in writing by topcoat manufacturer.

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

C. Textured Coating, Latex, Flat:[ MPI #42.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

D. Primer for Latex, Exterior, High Build: As recommended in writing by topcoat manufacturer.

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

E. Intermediate Coat for Latex, Exterior, High Build: As recommended in writing by topcoat manufacturer.

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

F. Latex, Exterior, High Build:[ MPI #40.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.10 ALUMINUM PAINT

A. Aluminum Paint:[ MPI #1.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

2.11 FLOOR COATINGS

A. Sealer, Water Based, for Concrete Floors:[ MPI #99.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

B. Sealer, Solvent Based, for Concrete Floors:[ MPI #104.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

C. Floor Paint, Latex, Low Gloss (Maximum Gloss Level 3):[ MPI #60.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

D. Floor Enamel, Alkyd, Gloss (Gloss Level 6):[ MPI #27.]

1. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

B. Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in five subparagraphs below are based on "MPI Manual."

1. Concrete: 12 percent.

2. Masonry (Clay and CMU): 12 percent.

3. Wood: 15 percent.

4. Portland Cement Plaster: 12 percent.

5. Gypsum Board: 12 percent.

C. Verify suitability of substrates, including surface conditions and compatibility with existing finishes and primers.

D. Proceed with coating application only after unsatisfactory conditions have been corrected.

1. Application of coating indicates acceptance of surfaces and conditions.

3.2 PREPARATION

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and paint systems specified in the Exterior Painting Schedule.

A. Comply with manufacturer's written instructions and recommendations in "MPI Manual" applicable to substrates and paint systems indicated.

B. Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

1. Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems indicated.

3.3 APPLICATION

A. Apply paints according to manufacturer's written instructions and recommendations in "MPI Manual."

B. Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

3.4 CLEANING AND PROTECTION

A. Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

B. At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

3.5 EXTERIOR PAINTING SCHEDULE

Paint systems in this article are based on "MPI Manual." For renovation projects, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

A. Concrete Substrates, Nontraffic Surfaces:

1. Latex System:

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 3.1A; second corresponds to MPI EXT 3.1K.

a. Prime Coat: Latex, exterior, matching topcoat.

b. Prime Coat: Primer, alkali resistant, water based[, MPI #3].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

d. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

e. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

f. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

g. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Latex Aggregate/Latex System" Subparagraph below corresponds to MPI EXT 3.1B.

2. Latex Aggregate/Latex System:

a. Prime Coat: Textured coating, latex, flat[, MPI #42].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"High-Build Latex System" Subparagraph below corresponds to MPI EXT 3.1L.

3. High-Build Latex System: Dry film thickness not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Custom Grade system.

a. Prime Coat: As recommended in writing by topcoat manufacturer.

b. Intermediate Coat: As recommended in writing by topcoat manufacturer.

c. Topcoat: Latex, exterior, high build[, MPI #40].

"Latex Aggregate System" Subparagraph below corresponds to MPI EXT 3.1N.

4. Latex Aggregate System:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Custom Grade system.

a. Prime Coat: As recommended in writing by topcoat manufacturer.

b. Intermediate Coat: As recommended in writing by topcoat manufacturer.

c. Topcoat: Textured coating, latex, flat[, MPI #42].

B. Concrete Substrates, Traffic Surfaces:

"Latex Floor Paint System" Subparagraph below corresponds to MPI EXT 3.2A.

1. Latex Floor Paint System:

a. Prime Coat: Floor paint, latex, low gloss (maximum Gloss Level 3)[, MPI #60].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Floor paint, latex, low gloss (maximum Gloss Level 3)[, MPI #60].

c. Topcoat: Floor paint, latex, low gloss (maximum Gloss Level 3)[, MPI #60].

"Alkyd Floor Enamel System" Subparagraph below corresponds to MPI EXT 3.2D.

2. Alkyd Floor Enamel System:

a. Prime Coat: Floor enamel, alkyd, gloss (Gloss Level 6)[, MPI #27].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Floor enamel, alkyd, gloss (Gloss Level 6)[, MPI #27].

c. Topcoat: Floor enamel, alkyd, gloss (Gloss Level 6)[, MPI #27].

d. Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

"Water-Based Clear Sealer System" Subparagraph below corresponds to MPI EXT 3.2H.

3. Water-Based Clear Sealer System:

a. Prime Coat: Sealer, water based, for concrete floors[, MPI #99].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Sealer, water based, for concrete floors[, MPI #99].

c. Topcoat: Sealer, water based, for concrete floors[, MPI #99].

"Solvent-Based Clear Sealer System" Subparagraph below corresponds to MPI EXT 3.2G.

4. Solvent-Based Clear Sealer System:

a. Prime Coat: Sealer, solvent based, for concrete floors[, MPI #104].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Sealer, solvent based, for concrete floors[, MPI #104].

c. Topcoat: Sealer, solvent based, for concrete floors[, MPI #104].

C. Clay-Masonry Substrates:

"Latex System" Subparagraph below corresponds to MPI EXT 4.1A.

1. Latex System:

a. Prime Coat: Latex, exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"High-Build Latex System" Subparagraph below corresponds to MPI EXT 4.1H.

2. High-Build Latex System: Dry film thickness not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Custom Grade system.

a. Prime Coat: As recommended in writing by topcoat manufacturer.

b. Intermediate Coat: As recommended in writing by topcoat manufacturer.

c. Topcoat: Latex, exterior, high build[, MPI #40].

"Latex Aggregate System" Subparagraph below corresponds to MPI EXT 4.1B.

3. Latex Aggregate System:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Custom Grade system.

a. Prime Coat: As recommended in writing by topcoat manufacturer.

b. Intermediate Coat: As recommended in writing by topcoat manufacturer.

c. Topcoat: Textured coating, latex, flat[, MPI #42].

D. CMU Substrates:

"Latex System" Subparagraph below corresponds to MPI EXT 4.2A.

1. Latex System:

a. Prime Coat: Block filler, latex, interior/exterior[, MPI #4].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Latex over Alkali-Resistant Primer System" Subparagraph below corresponds to MPI EXT 4.2L.

2. Latex over Alkali-Resistant Primer System:

a. Prime Coat: Primer, alkali resistant, water based[, MPI #3].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"High-Build Latex System" Subparagraph below corresponds to MPI EXT 4.2K.

3. High-Build Latex System: Dry film thickness not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Custom Grade system.

a. Prime Coat: As recommended in writing by topcoat manufacturer.

b. Intermediate Coat: As recommended in writing by topcoat manufacturer.

c. Topcoat: Latex, exterior, high build[, MPI #40].

"Latex Aggregate System" Subparagraph below corresponds to MPI EXT 4.2B.

4. Latex Aggregate System:

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Custom Grade system.

a. Prime Coat: As recommended in writing by topcoat manufacturer.

b. Intermediate Coat: As recommended in writing by topcoat manufacturer.

c. Topcoat: Textured coating, latex, flat[, MPI #42].

E. Steel Substrates:

"Water-Based Light Industrial Coating System" Subparagraph below corresponds to MPI EXT 5.1C.

1. Water-Based Light Industrial Coating System:

Retain one of two "Prime Coat" subparagraphs below. If retaining second, specify primer complying with MPI #79 in Section where substrate is specified.

a. Prime Coat: Primer, alkyd, anti-corrosive for metal[, MPI #79].

b. Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

d. Topcoat: Light industrial coating, exterior, water based (Gloss Level 3)[, MPI #161].

e. Topcoat: Light industrial coating, exterior, water based, semi-gloss (Gloss Level 5)[, MPI #163].

f. Topcoat: Light industrial coating, exterior, water based, gloss (Gloss Level 6)[, MPI #164].

"Alkyd System" Subparagraph below corresponds to MPI EXT 5.1D.

2. Alkyd System:

Retain one of two "Prime Coat" subparagraphs below. If retaining second, specify primer complying with MPI #79 in Section where substrate is specified.

a. Prime Coat: Primer, alkyd, anticorrosive for metal[, MPI #79].

b. Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Exterior alkyd enamel matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

d. Topcoat: Alkyd, exterior, flat (Gloss Level 1)[, MPI #8].

e. Topcoat: Alkyd, exterior, semi-gloss (Gloss Level 5)[, MPI #94].

f. Topcoat: Alkyd, exterior, gloss (Gloss Level 6)[, MPI #9].

"Quick-Drying Enamel System" Subparagraph below corresponds to MPI EXT 5.1A.

3. Quick-Drying Enamel System:

a. Prime Coat: Primer, alkyd, quick dry, for metal[, MPI #76].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Alkyd, quick dry, matching topcoat.

Retain one of two "Topcoat" subparagraphs below.

c. Topcoat: Alkyd, quick dry, semi-gloss (Gloss Level 5)[, MPI #81].

d. Topcoat: Alkyd, quick dry, gloss (Gloss Level 7)[, MPI #96].

"Aluminum Paint System" Subparagraph below corresponds to MPI EXT 5.1K.

4. Aluminum Paint System:

Retain one of two "Prime Coat" subparagraphs below. If retaining second, specify primer complying with MPI #79 in Section where substrate is specified.

a. Prime Coat: Primer, alkyd, anti-corrosive for metal[, MPI #79].

b. Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Aluminum paint[, MPI #1].

d. Topcoat: Aluminum paint[, MPI #1].

Galvanized-metal substrates should not be chromate passivated if primer is field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

F. Galvanized-Metal Substrates:

1. Latex System:

Retain one of two "Prime Coat" subparagraphs below. "MPI Manual" recommends first (corresponds to MPI EXT 5.3H) for low-contact/traffic areas.

a. Prime Coat: Primer, galvanized, water based[, MPI #134].

b. Prime Coat: Primer, galvanized metal[, as recommended in writing by topcoat manufacturer for exterior use on galvanized-metal substrates with topcoat indicated].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

d. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

e. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

f. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

g. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

2. Water-Based Light Industrial Coating System:

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 5.3J.

a. Prime Coat: Primer, galvanized, water based[, MPI #134].

b. Prime Coat: Primer, galvanized metal[, as recommended in writing by topcoat manufacturer for exterior use on galvanized-metal substrates with topcoat indicated].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

d. Topcoat: Light industrial coating, exterior, water based (Gloss Level 3)[, MPI #161].

e. Topcoat: Light industrial coating, exterior, water based, semi-gloss (Gloss Level 5)[, MPI #163].

f. Topcoat: Light industrial coating, exterior, water based, gloss (Gloss Level 6)[, MPI #164].

3. Alkyd System:

a. Prime Coat: Primer, galvanized metal[, as recommended in writing by topcoat manufacturer for exterior use on galvanized-metal substrates with topcoat indicated].

Retain "Intermediate Coat" Paragraph if required.

b. Intermediate Coat: Exterior alkyd enamel matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

c. Topcoat: Alkyd, exterior, flat (Gloss Level 5)[, MPI #8].

d. Topcoat: Alkyd, exterior, semi-gloss (Gloss Level 5)[, MPI #94].

e. Topcoat: Alkyd, exterior, gloss (Gloss Level 5)[, MPI #9].

G. Aluminum Substrates:

"Latex System" Subparagraph below corresponds to MPI EXT 5.4H.

1. Latex System:

a. Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Water-Based Light Industrial Coating System" Subparagraph below corresponds to MPI EXT 5.4G.

2. Water-Based Light Industrial Coating System:

a. Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

c. Topcoat: Light industrial coating, exterior, water based (Gloss Level 3)[, MPI #161].

d. Topcoat: Light industrial coating, exterior, water based, semi-gloss (Gloss Level 5)[, MPI #163].

e. Topcoat: Light industrial coating, exterior, water based, gloss (Gloss Level 6)[, MPI #164].

"Alkyd System" Subparagraph below corresponds to MPI EXT 5.4F.

3. Alkyd System:

a. Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Exterior alkyd enamel matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

c. Topcoat: Alkyd, exterior, flat (Gloss Level 5)[, MPI #8].

d. Topcoat: Alkyd, exterior, semi-gloss (Gloss Level 5)[, MPI #94].

e. Topcoat: Alkyd, exterior, gloss (Gloss Level 5)[, MPI #9].

H. Stainless-Steel Substrates:

"Latex System" Subparagraph below corresponds to MPI EXT 5.6F.

1. Latex System:

a. Prime Coat: Primer, bonding, solvent based[, MPI #69].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Water-Based Light Industrial Coating System" Subparagraph below corresponds to MPI EXT 5.6G.

2. Water-Based Light Industrial Coating System:

a. Prime Coat: Primer, quick dry, for aluminum[, MPI #95].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

c. Topcoat: Light industrial coating, exterior, water based (Gloss Level 3)[, MPI #161].

d. Topcoat: Light industrial coating, exterior, water based, semi-gloss (Gloss Level 5)[, MPI #163].

e. Topcoat: Light industrial coating, exterior, water based, gloss (Gloss Level 6)[, MPI #164].

I. Wood Substrates: Including [wood trim] [architectural woodwork] [doors] [windows] [wood siding] [wood fences] [wood-based panel products] [glued-laminated construction] [exposed joists] [exposed beams] [wood shingles and shakes (excluding roofs)] <Insert description>.

"Latex System" Subparagraph below corresponds to MPI EXT 6.1L, MPI EXT 6.2M, MPI EXT 6.3L, MPI EXT 6.4K, and MPI EXT 6.6E.

1. Latex System:

a. Prime Coat: Primer, latex for exterior wood[, MPI #6].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Latex over Alkyd Primer System" Subparagraph below corresponds to MPI EXT 6.1A, MPI EXT 6.2A, MPI EXT 6.3A, MPI EXT 6.4G, and MPI EXT 6.6A.

2. Latex over Alkyd Primer System:

Retain one of two "Prime Coat" subparagraphs below; retain second for wood-based panel products.

a. Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

b. Prime Coat: Primer, oil for exterior wood[, MPI #7].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

d. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

e. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

f. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

g. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Alkyd System" Subparagraph below corresponds to MPI EXT 6.1B, MPI EXT 6.2C, MPI EXT 6.3B, MPI EXT 6.4B, and MPI EXT 6.6B.

3. Alkyd System:

Retain one of two "Prime Coat" subparagraphs below.

a. Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

b. Prime Coat: Primer, oil for exterior wood[, MPI #7].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Exterior alkyd enamel matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

d. Topcoat: Alkyd, exterior, flat (Gloss Level 5)[, MPI #8].

e. Topcoat: Alkyd, exterior, semi-gloss (Gloss Level 5)[, MPI #94].

f. Topcoat: Alkyd, exterior, gloss (Gloss Level 5)[, MPI #9].

J. Wood Substrates, Traffic Surfaces: Including [lumber decking] [stairs] <Insert description>.

"Latex System" Subparagraph below corresponds to MPI EXT 6.5E.

1. Latex System:

a. Prime Coat: Primer, latex for exterior wood[, MPI #6].

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Custom Grade system.

b. Intermediate Coat: Interior/exterior latex floor and porch (low gloss).

c. Topcoat: Interior/exterior latex floor and porch (low gloss).

1) With additive to increase skid resistance of painted surface.

"Latex over Alkyd Primer System" Subparagraph below corresponds to MPI EXT 6.5A.

2. Latex over Alkyd Primer System:

a. Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

For a Premium Grade system, "MPI Manual" requires intermediate coat; "MPI Manual" does not include a Custom Grade system.

b. Intermediate Coat: Interior/exterior latex floor and porch (low gloss).

c. Topcoat: Interior/exterior latex floor and porch (low gloss).

1) With additive to increase skid resistance of painted surface.

"Alkyd Floor Enamel System" Subparagraph below corresponds to MPI EXT 6.5B.

3. Alkyd Floor Enamel System:

a. Prime Coat: Floor enamel, alkyd, gloss (Gloss Level 6)[, MPI #27].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Floor enamel, alkyd, gloss (Gloss Level 6)[, MPI #27].

c. Topcoat: Floor enamel, alkyd, gloss (Gloss Level 6)[, MPI #27].

d. Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

K. Plastic Trim Fabrication Substrates:

"Latex System" Subparagraph below corresponds to MPI EXT 6.8A.

1. Latex System:

Retain one of two "Prime Coat" subparagraphs below.

a. Prime Coat: Primer, bonding, water based[, MPI #17].

b. Prime Coat: Primer, bonding, solvent based[, MPI #69].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

d. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

e. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

f. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

g. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Alkyd System" Subparagraph below corresponds to MPI EXT 6.8B.

2. Alkyd System:

Retain one of two "Prime Coat" subparagraphs below.

a. Prime Coat: Primer, bonding, water based[, MPI #17].

b. Prime Coat: Primer, bonding, solvent based[, MPI #69].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

c. Intermediate Coat: Exterior alkyd enamel matching topcoat.

Retain one of three "Topcoat" subparagraphs below.

d. Topcoat: Alkyd, exterior, flat (Gloss Level 5)[, MPI #8].

e. Topcoat: Alkyd, exterior, semi-gloss (Gloss Level 5)[, MPI #94].

f. Topcoat: Alkyd, exterior, gloss (Gloss Level 5)[, MPI #9].

L. Portland Cement Plaster Substrates:

"Latex System" Subparagraph below corresponds to MPI EXT 9.1A.

1. Latex System:

a. Prime Coat: Latex, exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"Latex over Alkali-Resistant Primer System" Subparagraph below corresponds to MPI EXT 9.1J.

2. Latex over Alkali-Resistant Primer System:

a. Prime Coat: Primer, alkali resistant, water based[, MPI #3].

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

"High-Build Latex System" Subparagraph below corresponds to MPI EXT 9.1H.

3. High-Build Latex System: Dry film thickness not less than 10 mils (0.25 mm).

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written recommendations for primers and number of coats for a Premium Grade system and does not include a Custom Grade system.

a. Prime Coat: As recommended in writing by topcoat manufacturer.

b. Intermediate Coat: As recommended in writing by topcoat manufacturer.

c. Topcoat: Latex, exterior, high build[, MPI #40].

M. Exterior Gypsum Board Substrates:

"Latex System" Subparagraph below corresponds to MPI EXT 9.2A.

1. Latex System:

a. Prime Coat: Latex, exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete intermediate coat for a Custom Grade system.

b. Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below.

c. Topcoat: Latex, exterior flat (Gloss Level 1)[, MPI #10].

d. Topcoat: Latex, exterior, low sheen (Gloss Level 3-4)[, MPI #15].

e. Topcoat: Latex, exterior semi-gloss (Gloss Level 5)[, MPI #11].

f. Topcoat: Latex, exterior gloss (Gloss Level 6)[, MPI #119].

END OF SECTION 099113

	EXTERIOR PAINTING
	099113 - 1



