Copyright 2010 AIA
MasterSpec Professional
02/10

Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 123661 - SIMULATED STONE COUNTERTOPS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

Revise list below to suit Project.

1. Cultured marble countertops [and backsplashes].

2. Solid-surface-material countertops [and backsplashes].

3. Quartz agglomerate countertops [and backsplashes].

1.2 ACTION SUBMITTALS

A. Product Data: For countertop materials[ and sinks].

B. LEED Submittals:

First option in "Certificates for (Credit MR 6) (Credit MR 7)" Subparagraph below applies to LEED-CS; second applies to LEED-NC, LEED-CI, and LEED for Schools.

1. Certificates for [Credit MR 6] [Credit MR 7]: Chain-of-custody certificates indicating that wood products comply with forest certification requirements. Include documentation that manufacturer is certified for chain of custody by an FSC-accredited certification body. Include statement indicating cost for each certified wood product.

"Product Data for Credit IEQ 4.4" Subparagraph below applies to LEED-NC, LEED-CI, and LEED-CS.

2. Product Data for Credit IEQ 4.4: For adhesives and composite wood products, documentation indicating that product contains no urea formaldehyde.

"Laboratory Test Reports for Credit IEQ 4" Subparagraph below applies to LEED for Schools.

3. Laboratory Test Reports for Credit IEQ 4: For [adhesives] [sealants] [and] [composite wood and agrifiber products], documentation indicating that products comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings: For countertops. Show materials, finishes, edge and backsplash profiles, methods of joining, and cutouts for plumbing fixtures.

D. Samples: For each type of material exposed to view.

PART 2 -  PRODUCTS

2.1 CULTURED MARBLE COUNTERTOPS

Delete "Configuration" Paragraph below if countertop is detailed on Drawings.

A. Configuration: Provide countertops with the following front and backsplash style:

Retain one front and one backsplash style in first two subparagraphs below or revise to suit Project.

1. Front: [No drip (raised marine edge with rolled front)] [Straight, slightly eased at top] [1/2-inch (12.7-mm) bullnose] [Radius edge with apron, 2 inches (50 mm) high with 3/8-inch (9.5-mm) radius].

2. Backsplash: [Coved, with 3/8-inch (9.5-mm) radius cove and top] [Straight, with 3/8-inch (9.5-mm) radius cove and slightly eased at top] [Straight, slightly eased at cove and top].

3. Endsplash: [Matching backsplash] [None].

B. Fabrication: Fabricate tops in one piece with integral sink bowls and backsplashes.

2.2 SOLID-SURFACE-MATERIAL COUNTERTOPS

Delete "Configuration" Paragraph below if countertop is detailed on Drawings.

A. Configuration: Provide countertops with the following front and backsplash style:

Retain one front and one backsplash style in first two subparagraphs below or revise to suit Project.

1. Front: [Straight, slightly eased at top] [Beveled] [3/4-inch (19-mm) bullnose] [Radius edge with apron, 2 inches (50 mm) high with 3/8-inch (9.5-mm) radius] [1-1/2-inch (38-mm) laminated bullnose] [1-inch (25-mm) laminated bullnose] [Wood-trimmed edge as indicated].

2. Backsplash: [Straight, slightly eased at corner] [Beveled] [Radius edge with 3/8-inch (9.5-mm) radius].

3. Endsplash: [Matching backsplash] [None].

Retain one of two "Countertops" paragraphs below and revise to suit Project. Availability of 3/4-inch- (19-mm-) thick, solid surface material is limited.

B. Countertops: [1/2-inch- (12.7-mm-)] [3/4-inch- (19-mm-)] thick, solid surface material[ with wood-trimmed edges] [ with front edge built up with same material].

C. Countertops: 1/4-inch- (6.4-mm-) thick, solid surface material laminated to 3/4-inch- (19-mm-) thick particleboard with [wood-trimmed exposed edges] [exposed edges built up with 3/4-inch- (19-mm-) thick, solid surface material] [exposed edges faced with 1/4-inch- (6.4-mm-) thick, solid surface material].

D. Backsplashes: [1/2-inch- (12.7-mm-)] [3/4-inch- (19-mm-)] thick, solid surface material[ with wood-trimmed edges].

2.3 QUARTZ AGGLOMERATE COUNTERTOPS

Delete "Configuration" Paragraph below if countertop is detailed on Drawings.

A. Configuration: Provide countertops with the following front and backsplash style:

Retain one front and one backsplash style in first two subparagraphs below or revise to suit Project.

1. Front: [Straight, slightly eased at top] [Beveled] [3/4-inch (19-mm) bullnose] [Radius edge with apron, 2 inches (50 mm) high with 3/8-inch (9.5-mm) radius] [1-1/2-inch (38-mm) laminated bullnose] [1-inch (25-mm) laminated bullnose] [Wood-trimmed edge as indicated].

2. Backsplash: [Straight, slightly eased at corner] [Beveled] [Radius edge with 3/8-inch (9.5-mm) radius].

3. Endsplash: [Matching backsplash] [None].

B. Countertops: [1/2-inch- (12.7-mm-)] [3/4-inch- (19-mm-)] thick, quartz agglomerate[ with wood-trimmed edges] [ with front edge built up with same material].

C. Backsplashes: [1/2-inch- (12.7-mm-)] [3/4-inch- (19-mm-)] thick, quartz agglomerate[ with wood-trimmed edges].

2.4 COUNTERTOP MATERIALS

Retain "Certified Wood Materials" Paragraph below if required for LEED. Before retaining, verify availability of FSC-certified wood-based products.

A. Certified Wood Materials: Fabricate countertops with wood and wood-based products produced from wood obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

Retain "Composite Wood and Agrifiber Products" Paragraph below if required for LEED for Schools Credit IEQ 4.

B. Composite Wood and Agrifiber Products: Provide products that comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers," including 2004 Addenda.

Retain "Particleboard" Paragraph or "Plywood" Paragraph below if 1/4-inch- (6.4-mm-) thick, solid surface material is specified or if subtops are required.

Retain one of two grades in "Particleboard" Paragraph below. Retain option prohibiting urea formaldehyde if required for LEED-NC, LEED-CI, or LEED-CS Credit IEQ 4.4.

C. Particleboard: ANSI A208.1, [Grade M-2] [Grade M-2-Exterior Glue] [, made with binder containing no urea formaldehyde].

D. Plywood: Exterior softwood plywood complying with DOC PS 1, Grade C-C Plugged, touch sanded.

Retain "Adhesives" Paragraph below if required for LEED for Schools Credit IEQ 4.

E. Adhesives: Adhesives shall comply with the testing and product requirements of the California Department of Health Services' "Standard Practice for the Testing of Volatile Organic Emissions from Various Sources Using Small-Scale Environmental Chambers."

F. Cultured Marble: Gel-coated solid fabrication of filled plastic resin complying with ANSI Z124.3, Type 4, with precoated finish, and not less than 1/2 inch (12.7 mm) thick.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers. See Section 016000 "Product Requirements."

1. Manufacturers: Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Cultured marble manufacturers tend to be local or regional rather than national; consequently, the list below should be revised to remove those manufacturers that do not serve the project's area and to insert other local manufacturers.

a. Bathroom World Manufacturing Company.

b. Cameo Marble.

c. Cherry Marble Group.

d. Comar Products, Inc.

e. Craig Baker Marble Co., Inc.

f. Cultured Marble Products.

g. Custom Marble Products.

h. Custom Marble Products, Inc.

i. Imperial Marble Corp.

j. Marbleon, Inc.

k. MarCraft, Inc.

l. Princess Marble.

m. Roma Marble, Inc.

n. Rynone Manufacturing Corp.

o. Tiffany Marble.

p. <Insert manufacturer>.

2. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

G. Solid Surface Material: Homogeneous solid sheets of filled plastic resin complying with ANSI SS1.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers. See Section 016000 "Product Requirements."

1. Manufacturers: Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. Avonite Surfaces.

b. E. I. du Pont de Nemours and Company.

c. Formica Corporation.

d. LG Chemical, Ltd.

e. Meganite Inc.

f. Samsung Chemical USA, Inc.

g. Swan Corporation (The).

h. Transolid, Inc.

i. Wilsonart International.

j. <Insert manufacturer>.

Delete option in first subparagraph below if 1/4-inch- (6.4-mm-) thick material is not used.

2. Type: Provide Standard Type[ or Veneer Type made from material complying with requirements for Standard Type, as indicated] unless Special Purpose Type is indicated.

3. Integral Sink Bowls: Comply with ISSFA-2 and ANSI Z124.3, Type 5 or Type 6, without a precoated finish.

4. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

H. Quartz Agglomerate: Solid sheets consisting of quartz aggregates bound together with a matrix of filled plastic resin and complying with the "Physical Characteristics of Materials" Article of ANSI SS1.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers. See Section 016000 "Product Requirements."

1. Manufacturers: Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. Cambria.

b. Cosentino USA.

c. E. I. du Pont de Nemours and Company.

d. LG Chemical, Ltd.

e. Meganite Inc.

f. Samsung Chemical USA, Inc.

g. Technistone USA, Inc.

h. Transolid, Inc.

i. <Insert manufacturer>.

2. Colors and Patterns: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Retain paragraph below for countertops with decorative wood edge. Wood species are examples only; other species may be available. Show detail on Drawings.

I. Solid Wood Edges and Trim: Clear [red oak] [white oak] [hard maple] [cherry] <Insert species> lumber, free of defects, selected for compatible grain and color, and kiln dried to 7 percent moisture content.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Fasten countertops by screwing through corner blocks of base units into underside of countertop. Align adjacent surfaces and, using adhesive in color to match countertop, form seams to comply with manufacturer's written instructions. Carefully dress joints smooth, remove surface scratches, and clean entire surface.

END OF SECTION 123661

	SIMULATED STONE COUNTERTOPS
	123661 - 1



