Copyright 2010 AIA
MasterSpec Professional
08/10

Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 321223 - IMPRINTED ASPHALT
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes embossing patterns in [new] [and] [existing] asphalt pavement.

1.2 PREINSTALLATION MEETINGS

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. Samples: For each exposed product and for each color and texture specified.

1.4 QUALITY ASSURANCE

A. Installer Qualifications: Imprinted-asphalt manufacturer's authorized Installer who is trained and approved for installation of imprinted asphalt required for this Project.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 MANUFACTURERS

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Retain "Basis-of-Design Product" Paragraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's name and model number are indicated on Drawings.

B. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

1. Deco Asphalt.

2. Integrated Paving Concepts Inc.

3. Pattern Paving Products.

4. <Insert manufacturer's name>.

2.2 MATERIALS

This article is based on products by Integrated Paving Concepts and Pattern Paving Products; revise to suit Project.

A. Templates: Imprinted-asphalt manufacturer's standard flexible templates for imprinting pattern into hot asphalt paving.

1. Pattern: [Running bond brick] [Cobblestone] [Custom pattern indicated on Drawings] <Insert pattern>.

Retain "Coating System" Paragraph below only for coated imprinted asphalt.

B. Coating System: Imprinted-asphalt manufacturer's standard system formulated for exterior application on asphalt paving surfaces.

1. Colorant: UV-stable pigment blend, added to each coating layer.

2. Color: [White] [Yellow] <Insert color>.

Retain "Precut Marking Material" Paragraph below only for inlaid, reflectorized, heat-bonded, pavement-marking pattern.

C. Precut Marking Material: Imprinted-asphalt manufacturer's standard, reflectorized, thermoplastic, 90-mil (2.3-mm) minimum thickness, formulated for exterior application in imprinted, asphalt paving surfaces, and matching the imprinted pattern of templates.

PART 3 -  EXECUTION

3.1 IMPRINTING ASPHALT

This article is based on products by Integrated Paving Concepts and Pattern Paving Products; revise to suit Project.

A. General: Imprint asphalt according to manufacturer's written instructions, using manufacturer's recommended equipment.

B. Verify that utilities, traffic loop detectors, and other items requiring a cut and installation beneath the asphalt surface have been completed and that asphalt surface has been repaired flush with adjacent asphalt prior to beginning installation of imprinted asphalt.

Retain "Freshly Laid Asphalt" Paragraph below if imprinting can immediately follow asphalt installation.

C. Freshly Laid Asphalt: Immediately after asphalt has been laid and compacted but still plastic, begin the surface-imprinting process.

1. Monitor asphalt surface temperature to comply with manufacturer's written recommendations to ensure required temperature to perform surface imprinting.

2. Reheat asphalt if surface temperature drops below that required.

Retain "Reheating Asphalt" Paragraph below for imprinting existing asphalt pavement and for reheating new asphalt pavement.

D. Reheating Asphalt: Soften asphalt pavement surface by heating to a depth of at least 1/2 inch (13 mm) without burning asphalt.

1. Heat to a temperature of 300 to 325 deg F (149 to 163 deg C) immediately before applying templates.

2. Regularly monitor the pavement temperature to prevent overheating.

3. Direct flame heaters are not permitted.

4. If pavement is overheated and begins to emit black smoke, remove damaged pavement by milling down 1 inch (25 mm) and replace removed pavement with new, compacted surface course prior to resuming imprinting work.

In "Imprinting the Surface" Paragraph below, retain first option for coated imprinted asphalt. Retain second option for inlaid, reflectorized, heat-bonded, pavement-marking pattern.

E. Imprinting the Surface: Apply and imprint templates to a minimum depth [of 1/4 inch (6 mm)] [as required to embed precut marking material flush or barely beneath pavement surface].

Retain "Applying Coating" Paragraph below only for coated imprinted asphalt. Retain first option for dry climate zone. Retain second option for other locations.

F. Applying Coating: After imprinted surface has cooled, apply [two layers of base coating followed by two layers] [four layers] of top coating. Do not allow traffic until coating has completely dried and cured.

Retain "Applying Precut Marking Material" Paragraph below only for inlaid, reflectorized, heat-bonded, pavement-marking pattern.

G. Applying Precut Marking Material: Position precut marking material aligned with imprinted pattern and slowly heat to a temperature no higher than 325 deg F (163 deg C) until marking material begins to liquefy and flow. Do not allow traffic until installed marking material has cooled to ambient temperature.

END OF SECTION 321223

	IMPRINTED ASPHALT
	321223 - 1



