Copyright 2011 AIA
MasterSpec Professional
11/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 321373 - CONCRETE PAVING JOINT SEALANTS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Cold-applied joint sealants.

2. Hot-applied joint sealants.

3. Joint-sealant backer materials.

4. Primers.

1.2 PREINSTALLATION MEETINGS

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. Samples: For each kind and color of joint sealant required.

C. Paving-Joint-Sealant Schedule: Include the following information:

1. Joint-sealant application, joint location, and designation.

2. Joint-sealant manufacturer and product name.

3. Joint-sealant formulation.

4. Joint-sealant color.

1.4 INFORMATIONAL SUBMITTALS

A. Product certificates.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 MATERIALS, GENERAL

A. Compatibility: Provide joint sealants, backing materials, and other related materials that are compatible with one another and with joint substrates under conditions of service and application, as demonstrated by joint-sealant manufacturer, based on testing and field experience.

2.2 COLD-APPLIED JOINT SEALANTS

A. Single-Component, Nonsag, Silicone Joint Sealant: ASTM D 5893/D 5893M, Type NS.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Crafco Inc., an ERGON company; RoadSaver Silicone.

b. Dow Corning Corporation; 888.

c. Pecora Corporation; 301 NS.

d. <Insert manufacturer's name; product name or designation>.

B. Single-Component, Self-Leveling, Silicone Joint Sealant: ASTM D 5893/D 5893M, Type SL.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Crafco Inc., an ERGON company; RoadSaver Silicone SL.

b. Dow Corning Corporation; 890-SL.

c. Pecora Corporation; 300 SL.

d. <Insert manufacturer's name; product name or designation>.

C. Multicomponent, Nonsag, Urethane, Elastomeric Joint Sealant: ASTM C 920, Type M, Grade NS, Class 25, for Use T.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Meadows, W.R.,Inc; Pourthane NS.

b. <Insert manufacturer's name; product name or designation>.

D. Single Component, Pourable, Urethane, Elastomeric Joint Sealant: ASTM C 920, Type S, Grade P, Class 25, for Use T.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Meadows, W.R.,Inc; Pourthane SL.

b. <Insert manufacturer's name; product name or designation>.

E. Multicomponent, Pourable, Urethane, Elastomeric Joint Sealant: ASTM C 920, Type M, Grade P, Class 25, for Use T.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Pecora Corporation; [Dynatred] [Dynatrol II-SG] [Urexpan NR-200].

b. <Insert manufacturer's name; product name or designation>.

2.3 HOT-APPLIED JOINT SEALANTS

Classifications of sealants in this article are based on ASTM D 6690. Type I is for moderate climates and tested down to zero deg F (minus 18 deg C) with 50 percent extension. Type II and Type III are for most climates and tested down to minus 20 deg F (minus 29 deg C) with 50 percent extension. Type IV is for very cold climates and tested down to minus 20 deg F (minus 29 deg C) with 200 percent extension.

A. Hot-Applied, Single-Component Joint Sealant: ASTM D 6690, Type I.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Crafco Inc; [Asphalt Rubber Plus] [Asphalt Rubber Plus Type 2] [RoadSaver 203] [RoadSaver 211] [RoadSaver 515].

b. Meadows, W.R.,Inc; [Sealtight 1190] [Sealtight 164].

c. Right Pointe; JTS Asphalt Rubber Modified 043.

d. <Insert manufacturer's name; product name or designation>.

B. Hot-Applied, Single-Component Joint Sealant: ASTM D 6690, Type I or Type II.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Crafco Inc; [RoadSaver 201] [RoadSaver 220] [RoadSaver 221] [RoadSaver 534].

b. Right Pointe; [JTS 3405 Parking Lot Sealant 007] [JTS 3405 Rubber 009].

c. <Insert manufacturer's name; product name or designation>.

C. Hot-Applied, Single-Component Joint Sealant: ASTM D 6690, Type I, II, or III.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Crafco Inc; RoadSaver 222.

b. Meadows, W.R.,Inc; Sealtight 3405.

c. Right Pointe; [JTS 3405 Regular 003] [JTS 3405 Rubber 009].

d. <Insert manufacturer's name; product name or designation>.

In "Hot-Applied, Single-Component Joint Sealant" Paragraph below, Type IV sealants may not be suitable for paving areas with high levels of foot traffic.

D. Hot-Applied, Single-Component Joint Sealant: ASTM D 6690, Type IV.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Crafco Inc; RoadSaver 231.

b. Meadows, W.R.,Inc; Sealtight 3405M.

c. <Insert manufacturer's name; product name or designation>.

2.4 JOINT-SEALANT BACKER MATERIALS

Retain "Round Backer Rods for Cold- and Hot-Applied Joint Sealants" or "Round Backer Rods for Cold-Applied Joint Sealants" Paragraph below for use in joints such as contraction joints cut partially through paving material.

A. Round Backer Rods for Cold- and Hot-Applied Joint Sealants: ASTM D 5249, Type 1, of diameter and density required to control sealant depth and prevent bottom-side adhesion of sealant.

B. Round Backer Rods for Cold-Applied Joint Sealants: ASTM D 5249, Type 3, of diameter and density required to control joint-sealant depth and prevent bottom-side adhesion of sealant.

Retain "Backer Strips for Cold- and Hot-Applied Joint Sealants" Paragraph below for use in joints extending through the full depth of the paving.

C. Backer Strips for Cold- and Hot-Applied Joint Sealants: ASTM D 5249; Type 2; of thickness and width required to control joint-sealant depth, prevent bottom-side adhesion of sealant, and fill remainder of joint opening under sealant.

2.5 PRIMERS

Generally retain this article unless it is known that priming of substrates is not required with joint sealants specified. Purpose of primers is to improve adhesion of joint sealant to substrate.

A. Primers: Product recommended by joint-sealant manufacturer where required for adhesion of sealant to joint substrates indicated.

PART 3 -  EXECUTION

3.1 INSTALLATION OF JOINT SEALANTS

A. Comply with joint-sealant manufacturer's written installation instructions for products and applications indicated unless more stringent requirements apply.

B. Cleaning of Joints: Clean out joints immediately to comply with joint-sealant manufacturer's written instructions.

C. Joint Priming: Prime joint substrates where indicated or where recommended in writing by joint-sealant manufacturer.

D. Joint-Sealant Installation Standard: Comply with recommendations in ASTM C 1193 for use of joint sealants as applicable to materials, applications, and conditions.

E. Install joint-sealant backings to support joint sealants during application and at position required to produce cross-sectional shapes and depths of installed sealants relative to joint widths that allow optimum sealant movement capability.

1. Do not leave gaps between ends of joint-sealant backings.

2. Do not stretch, twist, puncture, or tear joint-sealant backings.

3. Remove absorbent joint-sealant backings that have become wet before sealant application and replace them with dry materials.

F. Install joint sealants immediately following backing installation, using proven techniques that comply with the following:

1. Place joint sealants so they fully contact joint substrates.

2. Completely fill recesses in each joint configuration.

3. Produce uniform, cross-sectional shapes and depths relative to joint widths that allow optimum sealant movement capability.

G. Tooling of Nonsag Joint Sealants: Immediately after joint-sealant application and before skinning or curing begins, tool sealants according to the following requirements to form smooth, uniform beads of configuration indicated; to eliminate air pockets; and to ensure contact and adhesion of sealant with sides of joint:

1. Remove excess joint sealant from surfaces adjacent to joints.

2. Use tooling agents that are approved in writing by joint-sealant manufacturer and that do not discolor sealants or adjacent surfaces.

H. Provide joint configuration to comply with joint-sealant manufacturer's written instructions unless otherwise indicated.

I. Clean off excess joint sealant as the Work progresses, by methods and with cleaning materials approved in writing by joint-sealant manufacturers.

END OF SECTION 321373
	CONCRETE PAVING JOINT SEALANTS
	321373 - 1



