Copyright 2010 AIA
MasterSpec Professional
08/10

Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 321713 - PARKING BUMPERS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes wheel stops.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

C. Samples: For each exposed product and for each color and texture specified.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PARKING BUMPERS

Retain "Concrete Wheel Stops" or "Resilient Wheel Stops" Paragraph below if wheel stops are required.

A. Concrete Wheel Stops: Precast, steel-reinforced, air-entrained concrete, [4000-psi (27.6-MPa)] <Insert value> minimum compressive strength, [4-1/2 inches (115 mm) high by 9 inches (225 mm) wide by 72 inches (1800 mm) long] <Insert dimensions>. Provide chamfered corners, transverse drainage slots on underside, and a minimum of two factory-formed or -drilled vertical holes through wheel stop for anchoring to substrate.

1. Mounting Hardware: Galvanized-steel [spike or dowel, 1/2-inch (13-mm) diameter, 10-inch (254-mm) minimum length] [lag screw, shield, and washers; 1/2-inch (13-mm) diameter, 8-inch (203-mm) minimum length] [hardware as standard with wheel-stop manufacturer].

B. Resilient Wheel Stops: Solid, integrally colored, 96 percent postconsumer or commingled postconsumer and preconsumer recycled rubber or plastic; UV stabilized; [4 inches (100 mm) high by 6 inches (150 mm) wide by 72 inches (1800 mm) long] <Insert dimensions>. Provide chamfered corners and a minimum of two factory-formed or -drilled vertical holes through wheel stop for anchoring to substrate.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed. Retain option and delete insert note if manufacturer's name and model number are indicated on Drawings.

2. Basis-of-Design Product: Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

a. Checkers Industrial Safety Products, Inc.

b. GNR Technologies.

c. Plastic Safety Systems, Inc.

d. Scientific Developments, Inc.

e. Technoflex.

f. Traffic Logix.

g. <Insert manufacturer's name>.

3. Color: [Black] [Yellow] [Gray] [Green] [Blue] <Insert color>.

Retain "Embedded Markings" Subparagraph below if required.

4. Embedded Markings: Molded-in, [blue] [white] [yellow] reflective markings, permanently inset in exposed surface.

5. Mounting Hardware: Galvanized-steel [spike or dowel, 1/2-inch (13-mm) diameter, 10-inch (254-mm) minimum length] [lag screw, shield, and washers; 1/2-inch (13-mm) diameter, 8-inch (203-mm) minimum length] [hardware as standard with wheel-stop manufacturer].

6. Adhesive: As recommended by wheel-stop manufacturer for adhesion to pavement.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. General: Install wheel stops according to manufacturer's written instructions unless otherwise indicated.

Retain first paragraph below where permanently installed resilient stops are required or if mechanical attachment is considered insufficient.

B. Install wheel stops in bed of adhesive before anchoring.

C. Securely anchor wheel stops to pavement with hardware in each preformed vertical hole in wheel stop as recommended in writing by manufacturer.

END OF SECTION 321713

	PARKING BUMPERS
	321713 - 1



