Copyright 2003 AIA
MASTERSPEC Full Length
11/03 (R 05/06)

Copyright 2003 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 09681 - CARPET TILE
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes modular, [fusion-bonded] [tufted] <Insert carpet tile construction> carpet tile.

B. Related Sections include the following:

List below only products that the reader might expect to find in this Section but are specified elsewhere.

1. Division 1 Section "Selective Demolition" for removing existing floor coverings.

2. Division 9 Section "[Resilient Floor Tile] [Resilient Wall Base and Accessories]" for resilient wall base and accessories installed with carpet tile.

3. Division 9 Section "Carpet."

1.3 SUBMITTALS

A. Product Data:  For each type of product indicated.  Include manufacturer's written data on physical characteristics, durability, and fade resistance.  Include installation recommendations for each type of substrate.

B. Shop Drawings:  Show the following:

Retain, delete, or revise subparagraphs below to suit Project.

1. Columns, doorways, enclosing walls or partitions, built-in cabinets, and locations where cutouts are required in carpet tiles.

2. Existing flooring materials to be removed.

3. Existing flooring materials to remain.

4. Carpet tile type, color, and dye lot.

5. Type of subfloor.

6. Type of installation.

7. Pattern of installation.

8. Pattern type, location, and direction.

9. Pile direction.

10. Type, color, and location of insets and borders.

11. Type, color, and location of edge, transition, and other accessory strips.

12. Transition details to other flooring materials.

C. Samples:  For each of the following products and for each color and texture required.  Label each Sample with manufacturer's name, material description, color, pattern, and designation indicated on Drawings and in schedules.

Delete subparagraphs below if not applicable.

1. Carpet Tile:  Full-size Sample.

2. Exposed Edge, Transition, and other Accessory Stripping:  12-inch- (300-mm-) long Samples.

D. LEED Submittal:

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.3; coordinate with requirements selected in Part 2 for carpet tile and adhesives.

1. Product Data for Credit EQ 4.3:

a. For carpet tile, documentation indicating compliance with testing and product requirements of Carpet and Rug Institute's "Green Label Plus" program.

b. For installation adhesive, including printed statement of VOC content.

E. Product Schedule:  For carpet tile.  Use same designations indicated on Drawings.

Coordinate first paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

F. Qualification Data:  For Installer.

G. Product Test Reports:  Based on evaluation of comprehensive tests performed by a qualified testing agency.

H. Maintenance Data:  For carpet tiles to include in maintenance manuals.  Include the following:

1. Methods for maintaining carpet tile, including cleaning and stain-removal products and procedures and manufacturer's recommended maintenance schedule.

2. Precautions for cleaning materials and methods that could be detrimental to carpet tile.

I. Warranty:  Special warranty specified in this Section.

1.4 QUALITY ASSURANCE

Delete paragraph below if Installer certification is not required; other Installer qualifications are included in Division 1 Section "Quality Requirements."

A. Installer Qualifications:  An experienced installer who is certified by the Floor Covering Installation Board or who can demonstrate compliance with its certification program requirements.

Delete paragraph below if no fire-resistance-rated units are required.

B. Fire-Test-Response Characteristics:  Provide products with the critical radiant flux classification indicated in Part 2, as determined by testing identical products per ASTM E 648 by an independent testing and inspecting agency acceptable to authorities having jurisdiction.

Delete paragraph and subparagraph below if not required.  If retaining, indicate location, size, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

C. Mockups:  Before installing carpet tile, build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

Retain subparagraph below if mockups are erected as part of building rather than separately and the intention is to make an exception to the default requirement in Division 1 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

1. Approved mockups may become part of the completed Work if undamaged at time of Substantial Completion.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 1.

D. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination."

Retain paragraph above if requirements in Division 1 are adequate for Project.  Retain paragraph below if additional requirements are necessary; include information about conference.  Identify specific participants not mentioned in Division 1.

E. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination." Review methods and procedures related to carpet tile installation including, but not limited to, the following:

Delete subparagraphs below if not required.  If retaining, revise to include product-specific requirements.  Insert additional requirements to suit Project.  Retain first subparagraph for occupied buildings if delivery must be controlled and coordinated, e.g., for tenant spaces in occupied office buildings with multiple tenants.

1. Review delivery, storage, and handling procedures.

2. Review ambient conditions and ventilation procedures.

1.5 DELIVERY, STORAGE, AND HANDLING

A. Comply with CRI 104, Section 5, "Storage and Handling."

1.6 PROJECT CONDITIONS

A. Comply with CRI 104, Section 7.2, "Site Conditions; Temperature and Humidity" and Section 7.12, "Ventilation."

B. Environmental Limitations:  Do not install carpet tiles until wet work in spaces is complete and dry, and ambient temperature and humidity conditions are maintained at the levels indicated for Project when occupied for its intended use.

Delete first paragraph below if products are not adhesively applied to concrete substrates.  Revise to suit Project.

C. Do not install carpet tiles over concrete slabs until slabs have cured and are sufficiently dry to bond with adhesive and concrete slabs have pH range recommended by carpet tile manufacturer.

D. Where demountable partitions or other items are indicated for installation on top of carpet tiles, install carpet tiles before installing these items.

1.7 WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this Article are not less than remedies available to Owner under prevailing local laws.  Coordinate with Division 1 Section "Product Requirements."

Revise paragraph and subparagraphs below if manufacturers have separate warranties for various characteristics.

A. Special Warranty for Carpet Tiles:  Manufacturer's standard form in which manufacturer agrees to repair or replace components of carpet tile installation that fail in materials or workmanship within specified warranty period.

1. Warranty does not include deterioration or failure of carpet tile due to unusual traffic, failure of substrate, vandalism, or abuse.

2. Failures include, but are not limited to, more than 10 percent loss of face fiber, edge raveling, snags, runs, [loss of tuft bind strength,] [dimensional stability,] [excess static discharge,] <Insert failure characteristic> and delamination.

Verify available warranties and insert number in subparagraph below.

3. Warranty Period:  [10] <Insert number> years from date of Substantial Completion.

If Installer warranty is available and required to suit Project, add here.

1.8 EXTRA MATERIALS

Extra materials may not be allowed for publicly funded projects.

A. Furnish extra materials described below, before installation begins, that match products installed and that are packaged with protective covering for storage and identified with labels describing contents.

Revise subparagraph below to suit Project.  Replace percentage with a specific number of units.

1. Carpet Tile:  Full-size units equal to [5] <Insert number> percent of amount installed for each type indicated, but not less than 10 sq. yd. (8.3 sq. m).

PART 2 -  PRODUCTS

Insert designation in article title below to coordinate Specifications with Drawings.  Replace insert note with the designation used on Drawings or in schedules to indicate locations where a specific type of carpet tile is required.  Copy Article below and re-edit it for each product required.  If a project includes only one type of carpet tile, consider deleting the designation in article title.

2.1 CARPET TILE <Insert designation>

Retain one of two paragraphs and list of manufacturers and products below.  See Division 1 Section "Product Requirements."

A. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

B. Products:  Subject to compliance with requirements, provide one of the following:

For competitive bidding, copy subparagraph and associated subparagraphs below for each additional product.

1. <Insert manufacturer's name; product name or designation.>

a. Color:  [Match Architect's samples] [As selected by Architect from manufacturer's full range] <Insert color>.

Generally delete color above and pattern below if they are described by product designation.

b. Pattern:  [Match Architect's samples] <Insert pattern>.

For competitive bidding from several sources, delete subparagraph below.

c. Source:  <Insert carpet tile supplier's name and contact information.>

Delete remainder of this Article if products are limited to those listed above.

C. Fiber Content:  [100 percent nylon 6, 6] [100 percent nylon 6] [100 percent polypropylene] [100 percent wool] [80 percent wool; 20 percent nylon 6, 6] [80 percent wool; 20 percent nylon 6] <Insert fiber and content by percentage.>

Retain first paragraph below and insert proprietary fiber type such as Antron, Ultron, or Zeftron if required.

D. Fiber Type:  <Insert proprietary fiber type.>

E. Pile Characteristic:  [Level-loop] [Cut] [Cut-and-loop] <Insert construction> pile.

Revise paragraphs and subparagraphs remaining in this Article to suit Project; add additional requirements if any.  There are many criteria for specifying carpet tile construction and many test methods for specifying carpet tile performance, but there is little consistency among manufacturers in test methods used or in readily providing comprehensive technical information for carpet tile.  See Evaluations for guidelines.

F. Yarn Twist:  <Insert twist in TPI (TPCM).>

G. Yarn Count:  <Insert yarn count.>

H. Density:  <Insert oz./cu. yd. (g/cu. cm).>

Test method in first paragraph below is applicable only to finished level-loop and cut-pile constructions with tuft heights less than 0.25 inch (6.3 mm).

I. Pile Thickness:  <Insert inches (mm)> for finished carpet tile[ per ASTM D 6859].

J. Stitches:  <Insert stitches per inch (mm).>

K. Gage:  <Insert gage in ends per inch (mm).>

Do not include weight of backings in first paragraph below.

L. Surface Pile Weight:  <Insert oz./sq. yd. (g/sq. m).>

M. Total Weight:  <Insert oz./sq. yd. (g/sq. m)> for finished carpet tile.

Revise paragraph below to suit Project; for example, if antimicrobial treatment is integral to backing formulation, if backing density and thickness are optional characteristics to be selected, or if performance characteristics and test method results for backings are available.

N. Primary Backing/Backcoating:  [Manufacturer's standard composite materials] [PVC] [Fiberglass-reinforced PVC] [Fiberglass-reinforced amorphous resin] [Reinforced polyurethane composite cushion] [Reinforced polyurethane composite] [Reinforced thermoplastic copolymer] <Insert specific primary backing materials; consult manufacturers>.

Delete paragraph below if not required.

O. Secondary Backing:  [Manufacturer's standard material] <Insert specific secondary backing material>.

Retain one or both paragraphs above or first paragraph below to describe backing system.

P. Backing System:  <Insert proprietary name.>

Q. Size:  [18 by 18 inches (457 by 457 mm)] [24 by 24 inches (610 by 610 mm)] [18 by 36 inches (457 by 914 mm)] [36 by 36 inches (914 by 914 mm)] <Insert dimension>.

Delete paragraph below if soil resistance is integral to carpet tile fiber or if soil resistance is not needed for Project; consult manufacturer.

R. Applied Soil-Resistance Treatment:  [Manufacturer's standard material] <Insert treatment>.

Delete first paragraph below if antimicrobial treatment is not needed for Project; consult manufacturer.

S. Antimicrobial Treatment:  [Manufacturer's standard material] <Insert treatment>.

T. Performance Characteristics:  As follows:

Delete first subparagraph below if not required.  Verify requirements of authorities having jurisdiction.

1. Critical Radiant Flux Classification:  Not less than [0.45 W/sq. cm] [0.22 W/sq. cm].

2. Dry Breaking Strength:  Not less than 100 lbf (445 N) per ASTM D 2646.

First and second options in subparagraph below are HUD-recommended minimums for cut pile and loop pile, respectively, per its Use of Materials Bulletin No. 44d.  Third option is minimum average recommended by CRI for school carpet with backing other than unitary backing.  DuPont recommends 5 lbf (22 N) for cut pile and 10 lbf (45 N) for loop pile.  More than 5 lbf (22 N) for cut pile and 10 lbf (45 N) for loop pile may be required for high-frequency traffic locations.

3. Tuft Bind:  Not less than [3 lbf (13 N)] [5 lbf (22 N)] [6.2 lbf (28 N)] [8 lbf (36 N)] [10 lbf (45 N)] <Insert tuft bind> per ASTM D 1335.

Delete first subparagraph below if no secondary backing.  First option is recommended by CRI for carpet with primary and secondary backing installed in schools.  Second option is required by GSA per its "Technical Requirements Booklet for Carpet, Carpet Tiles and Carpet Cushion Fsc Group 72, Part I, Section A."

4. Delamination:  Not less than [3.5 lbf/in. (15 N/mm)] [4 lbf/in. (18 N/mm)] <Insert force> per ASTM D 3936.

5. Dimensional Tolerance:  Within 1/32 inch (0.8 mm) of specified size dimensions, as determined by physical measurement.

6. Dimensional Stability:  0.2 percent or less per ISO 2551 (Aachen Test).

Retain subparagraph below for wool or wool blends only.

7. Resistance to Insects:  Comply with AATCC 24.

Delete first subparagraph below if not required.

8. Noise Reduction Coefficient (NRC):  <Insert NRC> per ASTM C 423.

9. Colorfastness to Crocking:  Not less than 4, wet and dry, per AATCC 165.

First option in subparagraph below is minimum recommended by CRI for carpet for general use, second option is for carpet installed in schools.

10. Colorfastness to Light:  Not less than 4 after [40] [60] <Insert number> AFU (AATCC fading units) per AATCC 16, Option E.

Retain subparagraph below if retaining antimicrobial treatment.

11. Antimicrobial Activity:  Not less than 2-mm halo of inhibition for gram-positive bacteria; not less than 1-mm halo of inhibition for gram-negative bacteria; no fungal growth; per AATCC 174.

First option in subparagraph below is typical for commercial carpet tile for general use; second option may be available for greater static control.

12. Electrostatic Propensity:  Less than [3.5] [2] <Insert number> kV per AATCC 134.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.3.

13. Environmental Requirements:  Provide carpet tile that complies with testing and product requirements of Carpet and Rug Institute's "Green Label Plus" program.

Insert other performance characteristics to suit Project, such as smoke density, texture retention, additional colorfastness characteristics, and quantification of soil-resistance treatment.

2.2 INSTALLATION ACCESSORIES

Revise paragraph below to suit Project.

A. Trowelable Leveling and Patching Compounds:  Latex-modified, hydraulic-cement-based formulation provided or recommended by carpet tile manufacturer.

Revise paragraph below to suit product(s) and Project.

B. Adhesives:  Water-resistant, mildew-resistant, nonstaining, pressure-sensitive type to suit products and subfloor conditions indicated, that complies with flammability requirements for installed carpet tile and is recommended by carpet tile manufacturer for releasable installation.

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.3.

1. VOC Limits:  Provide adhesives with VOC content not more than 50 g/L when calculated according to 40 CFR 59, Subpart D (EPA method 24).

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for maximum moisture content, alkalinity range, installation tolerances, and other conditions affecting carpet tile performance.  Examine carpet tile for type, color, pattern, and potential defects.

Retain paragraph and subparagraphs below if products are adhesively attached to concrete subfloors.

B. Concrete Subfloors:  Verify that concrete slabs comply with ASTM F 710 and the following:

Revise first subparagraph below to suit Project.

1. Slab substrates are dry and free of curing compounds, sealers, hardeners, and other materials that may interfere with adhesive bond.  Determine adhesion and dryness characteristics by performing bond and moisture tests recommended by carpet tile manufacturer.

2. Subfloor finishes comply with requirements specified in Division 3 Section "Cast-in-Place Concrete" for slabs receiving carpet tile.

3. Subfloors are free of cracks, ridges, depressions, scale, and foreign deposits.

Delete paragraph and subparagraphs below if no wood subfloors.

C. For wood subfloors, verify the following:

1. Underlayment over subfloor complies with requirements specified in Division 6 Section "Rough Carpentry."

2. Underlayment surface is free of irregularities and substances that may interfere with adhesive bond or show through surface.

Delete paragraph and subparagraph below if no metal subfloors.

D. For metal subfloors, verify the following:

1. Underlayment surface is free of irregularities and substances that may interfere with adhesive bond or show through surface.

Delete paragraph and subparagraph below if no painted subfloors.

E. For painted subfloors, verify the following:

1. Perform bond test recommended in writing by adhesive manufacturer.

Delete first paragraph and subparagraphs below if no raised access flooring systems.  See Evaluations.  Consider tightening installation tolerances for access flooring in Division 10 Section "Access Flooring."

F. For raised access flooring systems, verify the following:

1. Access floor complies with requirements specified in Division 10 Section "Access Flooring."

2. Access floor substrate is compatible with carpet tile and adhesive if any.

3. Underlayment surface is flat, smooth, evenly planed, tightly jointed, and free of irregularities, gaps greater than [1/8 inch (3 mm)] <Insert dimension>, protrusions more than 1/32 inch (0.8 mm), and substances that may interfere with adhesive bond or show through surface.

G. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. General:  Comply with CRI 104, Section 6.2, "Site Conditions; Floor Preparation," and with carpet tile manufacturer's written installation instructions for preparing substrates indicated to receive carpet tile installation.

Revise paragraph below to suit product and Project.  Dimensions below are recommended by CRI.

B. Use trowelable leveling and patching compounds, according to manufacturer's written instructions, to fill cracks, holes, depressions, and protrusions in substrates.  Fill or level cracks, holes and depressions 1/8 inch (3 mm) wide or wider and protrusions more than 1/32 inch (0.8 mm), unless more stringent requirements are required by manufacturer's written instructions.

Retain paragraph below if products are adhesively attached to concrete substrates.

C. Remove coatings, including curing compounds, and other substances that are incompatible with adhesives and that contain soap, wax, oil, or silicone, without using solvents.  Use mechanical methods recommended in writing by carpet tile manufacturer.

Delete first paragraph below if no metal substrates.

D. Clean metal substrates of grease, oil, soil and rust, and prime if directed by adhesive manufacturer.  Rough sand painted metal surfaces and remove loose paint.  Sand aluminum surfaces, to remove metal oxides, immediately before applying adhesive.

E. Broom and vacuum clean substrates to be covered immediately before installing carpet tile.

3.3 INSTALLATION

A. General:  Comply with CRI 104, Section 14, "Carpet Modules," and with carpet tile manufacturer's written installation instructions.

Revise first paragraph below if mill-applied peel-and-stick adhesives or standard adhesives are used.  Full-spread glue-down installation is appropriate for wheel traffic.  Partial glue-down installation is appropriate for carpet tiles of moderate dimensional stability, weight, and mass.  Free-lay installation is appropriate for dimensionally stable carpet tiles with heavy backings.  Revise second option if spot-glued installation is recommended by manufacturer and suits product and Project.

B. Installation Method:  [As recommended in writing by carpet tile manufacturer] [Glue down; install every tile with full-spread, releasable, pressure-sensitive adhesive] [Partial glue down; install periodic tiles with releasable, pressure-sensitive adhesive] [Free lay; install carpet tiles without adhesive].

C. Maintain dye lot integrity.  Do not mix dye lots in same area.

D. Cut and fit carpet tile to butt tightly to vertical surfaces, permanent fixtures, and built-in furniture including cabinets, pipes, outlets, edgings, thresholds, and nosings.  Bind or seal cut edges as recommended by carpet tile manufacturer.

E. Extend carpet tile into toe spaces, door reveals, closets, open-bottomed obstructions, removable flanges, alcoves, and similar openings.

F. Maintain reference markers, holes, and openings that are in place or marked for future cutting by repeating on finish flooring as marked on subfloor.  Use nonpermanent, nonstaining marking device.

G. Install pattern parallel to walls and borders.

Delete paragraph below if no raised access flooring systems.  Adhesive in seams may impede panel removal and replacement.

H. Stagger joints of carpet tiles so carpet tile grid is offset from access flooring panel grid.  Do not fill seams of access flooring panels with carpet adhesive; keep seams free of adhesive.

3.4 CLEANING AND PROTECTION

A. Perform the following operations immediately after installing carpet tile:

1. Remove excess adhesive, seam sealer, and other surface blemishes using cleaner recommended by carpet tile manufacturer.

2. Remove yarns that protrude from carpet tile surface.

3. Vacuum carpet tile using commercial machine with face-beater element.

B. Protect installed carpet tile to comply with CRI 104, Section 16, "Protection of Indoor Installations."

C. Protect carpet tile against damage from construction operations and placement of equipment and fixtures during the remainder of construction period.  Use protection methods indicated or recommended in writing by carpet tile manufacturer.

END OF SECTION 09681END OF SECTION 09681

CARPET TILE
09681 - 1

