Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications


Copyright 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 09651 - RESILIENT FLOOR TILE 
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Vinyl composition floor tile.

1.2 SUBMITTALS

First four paragraphs below are defined in Division 01 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For each type of product indicated.

B. SPiRiT Submittals:

Retain subparagraph below if low-emitting materials are required for LEED Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives.

1. Product Data for Credit IEQ 5.C4:  For adhesives, including printed statement of VOC content and chemical components.

First paragraph below assumes manufacturer's standard-size Samples are acceptable.  Revise to suit Project.

C. Samples:  Full-size units of each color and pattern of floor tile required.

Remaining paragraph is defined in Division 01 Section "Submittal Procedures" as an "Informational Submittal."

D. Maintenance data.

1.3 QUALITY ASSURANCE

Delete entire Article if fire-test-response testing is not required by authorities having jurisdiction.  In most building codes, floor tile is exempt from fire-test-response requirements.  See "Fire-Test-Response Characteristics" Article in the Evaluations in Division 09 Section "Resilient Flooring" for additional information.

A. Fire-Test-Response Characteristics:  As determined by testing identical products according to ASTM E 648 or NFPA 253 by a qualified testing agency.

1. Critical Radiant Flux Classification:  Class I, not less than 0.45 W/sq. cm.

1.4 PROJECT CONDITIONS

A. Maintain ambient temperatures within range recommended by manufacturer in spaces to receive floor tile.

B. Until Substantial Completion, maintain ambient temperatures within range recommended by manufacturer.

C. Close spaces to traffic during floor tile installation.

D. Close spaces to traffic for 48 hours after floor tile installation.

E. Install floor tile after other finishing operations, including painting, have been completed.

1.5 EXTRA MATERIALS

A. Deliver to Owner.  Furnish extra materials matching products installed as described below, packaged with protective covering for storage, identified with labels clearly describing contents.

1. Not less than (1) box for each 20 boxes or fraction thereof, of each class, wearing surface, color, pattern, size of resilient floor tile installed.  If fewer than 20 boxes are used, furnish one (1) box minimum.

PART 2 -  PRODUCTS

2.1 VINYL COMPOSITION FLOOR TILE

Copy this article and re-edit for each product.

Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

See Editing Instruction No. 1 in the Evaluations in Division 09 Section "Resilient Flooring" for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

A. Tile Standard:  ASTM F 1066, Class 2, through-pattern tile.

B. Wearing Surface:  Smooth.

A limited number of products are available in 3/32- and 3/16-inch (2.4- and 4.8-mm) thicknesses; if applicable, insert in first paragraph below.

C. Thickness:  0.125 inch (3.2 mm).

D. Size:  12 by 12 inches (305 by 305 mm).

E. Colors and Patterns:  As selected by Architect from full range of industry colors.

2.2 INSTALLATION MATERIALS

A. Trowelable Leveling and Patching Compounds:  Latex-modified, portland cement based or blended hydraulic-cement-based formulation provided or approved by manufacturer for applications indicated.

B. Adhesives:  Water-resistant type recommended by manufacturer to suit floor tile and substrate conditions indicated.

Retain subparagraph below if low-emitting materials are required for LEED Credit EQ 4.1.  VOC limits are those in South Coast Air Quality Management District Rule #1168.

1. Use adhesives that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

Rule #1168 establishes no VOC limitation for solid vinyl floor tiles; revise if extending VOC limits to this floor tile type.

a. Vinyl Composition Floor Tile Adhesives:  Not more than 50 g/L.

PART 3 -  EXECUTION

3.1 PREPARATION

Extensive surface preparation is required over substrates from which existing products have been removed.  Requirements vary among manufacturers.  Insert requirements to suit Project.

A. Prepare substrates according to manufacturer's written instructions to ensure adhesion of resilient products.

B. Concrete Substrates:  Prepare according to ASTM F 710.

1. Verify that substrates are dry and free of curing compounds, sealers, and hardeners.

2. Remove substrate coatings and other substances that are incompatible with adhesives and that contain soap, wax, oil, or silicone, using mechanical methods recommended by manufacturer.  Do not use solvents.

3. Alkalinity and Adhesion Testing:  Perform tests recommended by manufacturer.  Proceed with installation only after substrates pass testing.

4. Moisture Testing:  Perform tests recommended by floor covering manufacturer.  Proceed with installation only after substrates pass testing.

C. Fill cracks, holes, and depressions in substrates with trowelable leveling and patching compound and remove bumps and ridges to produce a uniform and smooth substrate.

D. Do not install floor tiles until they are same temperature as space where they are to be installed.

1. Move resilient products and installation materials into spaces where they will be installed at least 48 hours in advance of installation.

E. Sweep and vacuum clean substrates to be covered by resilient products immediately before installation.

F. Apply concrete slab primer, if recommended by flooring manufacturer, prior to applying adhesive.  Apply according to manufacturer’s directions.

3.2 FLOOR TILE INSTALLATION

A. Comply with manufacturer's written instructions for installing floor tile.

B. Lay out floor tiles from center marks established with principal walls, discounting minor offsets, so tiles at opposite edges of room are of equal width.  Adjust as necessary to avoid using cut widths that equal less than one-half tile at perimeter.

C. Match floor tiles for color and pattern by selecting tiles from cartons in the same sequence as manufactured and packaged, if so numbered.  Discard broken, cracked, chipped, or deformed tiles.

If built-in items are required to be set on top of tile, indicate on Drawings and revise first paragraph below.

D. Scribe, cut, and fit floor tiles to butt neatly and tightly to vertical surfaces and permanent fixtures including built-in furniture, cabinets, pipes, outlets, and door frames.

E. Extend floor tiles into toe spaces, door reveals, closets, and similar openings.  Extend floor tiles to center of door openings.

F. Maintain reference markers, holes, and openings that are in place or marked for future cutting by repeating on floor tiles as marked on substrates.  Use chalk or other nonpermanent, nonstaining marking device.

Revise paragraph below if other-than-full-spread adhesive method is recommended by manufacturer for substrate and tile products selected.

G. Adhere floor tiles to flooring substrates using a full spread of adhesive applied to substrate to produce a completed installation without open cracks, voids, raising and puckering at joints, telegraphing of adhesive spreader marks, and other surface imperfections.

3.3 CLEANING AND PROTECTION
A. Perform following operations immediately after completing installation:

1. Remove visible all surface blemishes using cleaner recommended by manufacturers.

2. Sweep or vacuum floor thoroughly.

3. Do not wash floor until after time period recommended by resilient floor tile manufacturer.

4. Damp‑mop tile to remove black marks and soil.

B. Protect flooring against mars, marks, indentations, other damage from construction operations, placement of equipment, fixtures during remainder of construction period. Use protection      methods indicated, recommended by manufacturer.

1. Apply protective floor polish to tile surfaces that are free from soil, visible   adhesive, surface blemishes.

a. Use commercially available, metal, cross‑linked acrylic product acceptable to manufacturer.

b. Coordinate selection of floor polish with Owner's maintenance service.

2. Cover with undyed, untreated building paper until inspection for Substantial Completion.

3. Do not move heavy, sharp objects directly over floors. Place plywood or hardboard         panels over floors, under objects while they are being moved. Slide or roll objects over panels without moving panels.

C. Clean floors not more than four (4) days prior to dates scheduled for inspections intended to establish date of Substantial Completion in each area of Project. Clean floors using method recommended by manufacturer.

1.
Strip protective floor polish that was applied after completing installation prior to cleaning.  Clean floor coverings by method recommended by manufacturer.

2.
Polishing of floors as directed by LARNG.

END OF SECTION 09651


RESILIENT FLOOR TILE 

09651 - 1

