Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications


Copyright 2004 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 12485 - FOOT GRILLES
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. This Section includes recessed foot grilles and frames.

1.2 SUBMITTALS

A. Product Data:  For each type of foot grille and frame.

B. Shop Drawings:  Show the following:

Edit three subparagraphs below to suit Project.

1. Items penetrating foot grilles and frames.

2. Divisions between grille sections.

3. Perimeter floor moldings.

C. Samples:  For each type of product involving color selection.

1. Foot Grille:  12-inch- (300-mm-) square assembled sections.

2. Frame Members:  12-inch- (300-mm-) long Sample of each type and color.

D. Maintenance data.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

1. Basis-of-Design Product:  Subject to compliance with requirements, provide C/S Group – “Gridline G6” or a comparable product. 

2.2 MATERIALS

A. Stainless-Steel Sheet, Strip, Plate, and Flat Bars:  ASTM A 666, Type 304.

B. Stainless-Steel Angles:  ASTM A 276 or ASTM A 479/A 479M, corrosion resistant, Type 304.

2.3 FOOT GRILLES

A. Stainless-Steel Foot Grille:

1. Surface Treads:  Wires to be 0.086-by-0.177-inch (2.18-by-2.97-mm) electronically welded and spaced 0.118-inch- (2.99-mm) apart.

2. Support Rods:  Spaced 1 inch (25 mm) o.c., welded to each wire.

3. Load Capacity:  Unit must withstand 500 lb. wheel loads (load applied to a solid 5” x 2” wide polyurethane wheel, 1000 passes without damage).

Delete subparagraph above or first subparagraph below.

4. Pit Grating:  1-1/8 inches (28.5 mm) deep.

5. Stainless-Steel Finish:  Satin finish.

6. Grille Size: 
a. Width:   Extend a minimum of 8” pass entrance opening on both sides.

b. Depth:  A minimum of 48 inches (122 cm).
2.4 FRAMES

A. Provide manufacturer's standard frames of size and style for grille type.

2.5 FABRICATION

A. Shop fabricate foot grilles to greatest extent possible in sizes as indicated.

B. Fabricate frame members in single lengths or, where frame dimensions exceed maximum available lengths, provide minimum number of pieces possible.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Install recessed foot grilles and frames to comply with manufacturer's written instructions at locations indicated and with top of foot grilles and frames in relationship to one another and to adjoining finished flooring as recommended by manufacturer.  Set foot-grille tops at height for most effective cleaning action.

3.2 PROTECTION

A. After completing frame installations, provide temporary filler of plywood or fiberboard in foot-grille recesses and cover frames with plywood protective flooring.  Maintain protection until construction traffic has ended and Project is near Substantial Completion.

END OF SECTION 12485

FOOT GRILLES

12485 - 1

