Louisiana Army National Guard

Preliminary Review Documents

141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications


SECTION 02528 - CONCRETE WALKS AND CURBS & GUTTERS

PART 1 - GENERAL

1.1

DESCRIPTION

A.
Work included:

1.
This work consists of furnishing and constructing concrete curbs and gutters in accordance with these specifications and in conformance with lines, grades, dimensions and typical sections shown on the plans. 

1.2

REFERENCED SPECIFICATIONS

A.
Those parts of the referenced specifications, which as applicable hereto shall be considered as if written herein in full. 

1. LaDOTD:  “Louisiana Standard Specifications for Roads & Bridges”, 2000 Edition, and the Supplemental Specifications approved by LaDOTD.

2. A.S.T.M.

3. A.C.I.

4.   A.A.S.H.T.O. 

B.
Concrete shall conform to requirements of SECTION 02516 – “PORTLAND CEMENT CONCRETE PAVEMENT”. 


C.
Except as included herein or noted on the plan, all work shall conform to the requirements of the referenced specifications listed above. 

1.3
QUALITY ASSURANCE 

A.
Use adequate numbers of skilled workmen who are thoroughly trained and experienced in the necessary crafts and who are completely familiar with the specified requirements and the methods needed for the proper performance of the work of this section.  

1.
During all of the time that this work is in progress, the Contractor must have present at the site of the work, a foreman or superintendent who is not operating equipment. 

B. Use only equipment, which is specifically manufactured for and properly sized for the work to be performed. 

C. Testing and Inspection Service: The Owner shall employ and pay for a qualified independent testing laboratory to perform sampling, testing, and inspection services.

PART 2 - MATERIALS

2.1
Concrete for curbs and gutters shall display a minimum 28-day compressive strength of 4,000 PSI.

2.2
Concrete for sidewalks shall display a minimum 28-day compressive strength of 3,000 PSI.

2.3
All materials and work unless otherwise noted on the plans will comply with all of the requirements of L.D.O.T.D. Section 707 Curbs & Gutters and specified related sections.

PART 3 - EXECUTION


3.1
QUALITY ASSURANCE All work, unless otherwise noted on the plans, shall comply with all requirements of LaDOTD Manual Section 707 Curbs & Gutters and specified related sections.  

A. Provide a ¾ inch wide expansion joint with three, ¾ inch smooth steel dowel bars every thirty (30) ft.  The dowel bars shall be 36 inches in length.  Provide a preformed expansion material throughout the joint. 

END OF SECTION 02528

CONCRETE WALKS AND CURBS & GUTTERS


02528-2

