Copyright 2005 AIA
MASTERSPEC Full Length
08/05

Copyright 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 02741 - ASPHALT PAVING
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

A. Section Includes:

1. Cold milling of existing hot-mix asphalt pavement.

2. Hot-mix asphalt patching.

3. Hot-mix asphalt paving.

4. Hot-mix asphalt paving overlay.

5. Asphalt surface treatments.

6. Pavement-marking paint.

7. Traffic-calming devices.

8. Imprinted asphalt.

B. Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

1. Division 2 Sections for other paving installed as part of crosswalks in asphalt pavement areas.

2. Division 2 Section "Building Demolition" for demolition, removal, and recycling of existing asphalt pavements, and for geotextiles that are not embedded within courses of asphalt paving.

3. Division 2 Section "Earthwork" for aggregate subbase and base courses and for aggregate pavement shoulders.

4. Division 2 Section "Pavement Joint Sealants" for joint sealants and fillers at paving terminations.

5. Division 2 Section "Unit Pavers" for bituminous setting bed for pavers.

1.3 UNIT PRICES

Retain products and work included in this Section that are covered by unit prices.  Do not include amounts.  Insert descriptions of items in Part 2 or 3 to provide information affecting the cost of the Work that is not included under the unit price.

A. Work of this Section is affected by [Insert name of unit price].

1.4 DEFINITION

Retain definition remaining after this Section has been edited.

A. Hot-Mix Asphalt Paving Terminology:  Refer to ASTM D 8 for definitions of terms.

1.5 SUBMITTALS

First four paragraphs below are defined in Division 1 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For each type of product indicated.  Include technical data and tested physical and performance properties.

Retain one of two subparagraphs below.  Retain first if specifying state or local DOT standard paving mixes.  Retain second if specifying nonstandard mixes or DOT mixes without requiring certification.

1. Job-Mix Designs:  Certification, by authorities having jurisdiction, of approval of each job mix proposed for the Work.

2. Job-Mix Designs:  For each job mix proposed for the Work.

Retain first paragraph below if Shop Drawings are required.

B. Shop Drawings:  Indicate pavement markings, lane separations, and defined parking spaces.  Indicate, with international symbol of accessibility, spaces allocated for people with disabilities.

C. Samples:  For each paving fabric, 12 by 12 inches (300 by 300 mm) minimum.

D. Samples for Verification:  For the following products, in manufacturer's standard sizes unless otherwise indicated:

Retain required product samples in subparagraphs below.

1. Each paving fabric, 12 by 12 inches (300 by 300 mm) minimum.

2. Each type and color of preformed traffic-calming device.

3. Each pattern and color of imprinted asphalt[ and precut marking material].

Remaining paragraphs are defined in Division 1 Section "Submittal Procedures" as "Informational Submittals."

Coordinate first paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

E. Qualification Data:  For qualified [manufacturer] [and] [Installer].

Retain first paragraph below for material or product certificates from manufacturers.

F. Material Certificates:  For each paving material, from manufacturer.

Retain paragraph below for material test reports that are Contractor's responsibility.

G. Material Test Reports:  For each paving material.

1.6 QUALITY ASSURANCE

Retain first paragraph below if required.

A. Manufacturer Qualifications:  [A paving-mix manufacturer registered with and approved by authorities having jurisdiction or the DOT of state in which Project is located] <Insert requirement>.

Retain first paragraph below if imprinted asphalt is required.

B. Installer Qualifications:  Imprinted-asphalt manufacturer's authorized installer who is trained and approved for installation of imprinted asphalt required for this Project.

Retain first paragraph below if Contractor or manufacturer selects testing agency.  Qualification requirements are in addition to those specified in Division 1 Section "Quality Requirements," which also includes the definition for "NRTL" (nationally recognized testing laboratory).

C. Testing Agency Qualifications:  Qualified according to ASTM D 3666 for testing indicated.

Retain first paragraph below if asphalt paving work is located on public property and must comply with requirements of state or local DOT.  Also retain if referencing these requirements regardless of property ownership.

D. Regulatory Requirements:  Comply with materials, workmanship, and other applicable requirements of <Insert applicable standards> of <Insert name of state or local DOT> for asphalt paving work.

1. Measurement and payment provisions and safety program submittals included in standard specifications do not apply to this Section.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

E. Preinstallation Conference:  Conduct conference at [Project site] <Insert location>.

Retain subparagraphs below if additional requirements are necessary; include information about conference.  If retaining, revise to include product-specific requirements.  Insert additional requirements to suit Project.

1. Review methods and procedures related to hot-mix asphalt paving including, but not limited to, the following:

a. Review proposed sources of paving materials, including capabilities and location of plant that will manufacture hot-mix asphalt.

b. Review condition of subgrade and preparatory work.

c. Review requirements for protecting paving work, including restriction of traffic during installation period and for remainder of construction period.

d. Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

1.7 DELIVERY, STORAGE, AND HANDLING

Retain this article if pavement-marking materials are required.

A. Deliver pavement-marking materials to Project site in original packages with seals unbroken and bearing manufacturer's labels containing brand name and type of material, date of manufacture, and directions for storage.

B. Store pavement-marking materials in a clean, dry, protected location within temperature range required by manufacturer.  Protect stored materials from direct sunlight.

1.8 PROJECT CONDITIONS

A. Environmental Limitations:  Do not apply asphalt materials if subgrade is wet or excessively damp, if rain is imminent or expected before time required for adequate cure, or if the following conditions are not met:

1. Prime Coat:  Minimum surface temperature of 60 deg F (15.6 deg C).

2. Tack Coat:  Minimum surface temperature of 60 deg F (15.6 deg C).

3. Slurry Coat:  Comply with weather limitations in ASTM D 3910.

Revise temperature in first subparagraph below to suit Project.  Thicker asphalt base courses may be placed if surface temperature exceeds freezing.

4. Asphalt Base Course:  Minimum surface temperature of 40 deg F (4.4 deg C) and rising at time of placement.

5. Asphalt Surface Course:  Minimum surface temperature of 60 deg F (15.6 deg C) at time of placement.

B. Pavement-Marking Paint:  Proceed with pavement marking only on clean, dry surfaces and at a minimum ambient or surface temperature of [40 deg F (4.4 deg C) for oil-based materials] [55 deg F (12.8 deg C) for water-based materials], and not exceeding 95 deg F (35 deg C).

Retain paragraph below for coated imprinted asphalt.

C. Imprinted Asphalt Paving:  Proceed with coating imprinted pavement only when air temperature is at least 50 deg F (10 deg C) and rising and will not drop below 50 deg F (10 deg C) within 8 hours of coating application.  Proceed only if no precipitation is expected within two hours after applying the final layer of coating.

PART 2 -  PRODUCTS

2.1 AGGREGATES

A. General:  Use materials and gradations that have performed satisfactorily in previous installations.

Uncured or improperly cured slag aggregates have caused serious problems.  Delete slag aggregates in remaining paragraphs if not recommended for local use.

B. Coarse Aggregate:  ASTM D 692, sound; angular crushed stone, crushed gravel, or cured, crushed blast-furnace slag.

C. Fine Aggregate:  [ASTM D 1073] [or] [AASHTO M 29], sharp-edged natural sand or sand prepared from stone, gravel, cured blast-furnace slag, or combinations thereof.

In subparagraph below, reduce percentage of natural sand to 10 percent if slow, heavily loaded traffic is anticipated.

1. For hot-mix asphalt, limit natural sand to a maximum of 20 percent by weight of the total aggregate mass.

Retain paragraph below if common in local paving mixtures.

D. Mineral Filler:  [ASTM D 242] [or] [AASHTO M 17], rock or slag dust, hydraulic cement, or other inert material.

2.2 ASPHALT MATERIALS

Use of performance-graded asphalt binders developed by Superpave has generally replaced asphalt cement.  Asphalt binders graded by performance may contain polymer modifiers.  AASHTO M 320 and AASHTO MP 1a have no equivalent ASTM product standards.  Provisional Standard AASHTO MP 1a differs from AASHTO M 320 by incorporating new testing procedures for low temperatures; each standard identifies the same 37 performance grades.  Options in first paragraph below are examples only.  In first option, "PG" is "performance grade," "64" is the probable highest pavement temperature in deg C, and "-22" is the probable lowest temperature in minus deg C.  Consult AI or state or local DOT for asphalt-binder recommendations.

A. Asphalt Binder:  AASHTO M 320 or AASHTO MP 1a, [PG 64-22] [PG 58-28] [PG 70-22] <Insert performance grade>.

Retain first paragraph below with option for viscosity- or penetration-graded asphalt cement if these materials are available and required.  Viscosity testing measures properties more accurately than penetration testing.  Insert viscosity or penetration grades below if required.

B. Asphalt Cement:  [ASTM D 3381 for viscosity-graded material] [ASTM D 946 for penetration-graded material].

Retain one of first two paragraphs below if surface-applied prime coats are required.  Benefits of a prime coat, including temporary protection of the granular base from moisture, binding surface fine aggregate, and promoting bond of the paving course to the granular course, have been disputed in the asphalt industry.  In first paragraph, "MC-30" and "MC-70" are used on close-textured surfaces; "MC-250" is used on open-textured bases.  Where use of cutback asphalt is restricted by air pollution regulations or water quality-control restrictions, retain second paragraph.

C. Prime Coat:  ASTM D 2027, medium-curing cutback asphalt, [MC-30 or MC-70] [MC-250].

Refer to state or local DOT for details of asphalt emulsion prime coat; there are no ASTM or AASHTO product standards.

D. Prime Coat:  Asphalt emulsion prime coat complying with <Insert name of state or local> DOT requirements.

Retain first paragraph below if required.  Tack coat is usually diluted in equal amounts of water and emulsified asphalt.  It is usually applied to vertical surfaces of curbs, gutters, cold pavement joints, and structures in the pavement that will be in contact with hot-mix asphalt.  Tack coat is also applied to existing pavement surfaces to bond new hot-mix asphalt paving overlays.

E. Tack Coat:  [ASTM D 977] [or] [AASHTO M 140] emulsified asphalt, or [ASTM D 2397] [or] [AASHTO M 208] cationic emulsified asphalt, slow setting, diluted in water, of suitable grade and consistency for application.

Retain first paragraph below if required.  Fog seals are more diluted than tack coats, up to 5 parts water to 1 part emulsified asphalt.  Fog seals are surface treatments applied to rejuvenate existing hot-mix asphalt pavement surfaces.

F. Fog Seal:  [ASTM D 977] [or] [AASHTO M 140] emulsified asphalt, or [ASTM D 2397] [or] [AASHTO M 208] cationic emulsified asphalt, slow setting, factory diluted in water, of suitable grade and consistency for application.

Retain first paragraph below for mixing with emulsified asphalts.

G. Water:  Potable.

Retain paragraph below if filling voids and stabilizing existing portland cement concrete pavements with asphalt during repairs.  Revise to another method such as cementitious grouting if not using asphalt.

H. Undersealing Asphalt:  ASTM D 3141, pumping consistency.

2.3 AUXILIARY MATERIALS

Retain first paragraph below for weed control if required.  Some herbicides may be mixed with cutback-asphalt prime coats.

A. Herbicide:  Commercial chemical for weed control, registered by the EPA.  Provide in granular, liquid, or wettable powder form.

Retain first paragraph below for sand blotter over unabsorbed prime coat.

B. Sand:  [ASTM D 1073] [or] [AASHTO M 29], Grade Nos. 2 or 3.

Paving geotextile is placed over existing hot-mix asphalt pavement to minimize reflective cracking in new overlay.  It also reduces moisture infiltration into the old pavement structure.

C. Paving Geotextile:  AASHTO M 288, nonwoven polypropylene; resistant to chemical attack, rot, and mildew; and specifically designed for paving applications.

Retain first paragraph below if existing pavement requires filling of cracks and joints wider than 1/4 inch (6 mm) before placing paving geotextile or a surface treatment.  Retain option for type based on Project conditions.  Type I is for moderate climates and tested down to zero deg F (minus 18 deg C) with 50 percent extension.  Type II (formerly, ASTM D 3405) and Type III (formerly, FS SS-S-1401C) are for most climates and tested down to minus 20 deg F (minus 29 deg C) with 50 percent extension.  Type IV is for very cold climates and tested down to minus 20 deg F (minus 29 deg C) with 200 percent extension.

D. Joint Sealant:  [ASTM D 6690] [or] [AASHTO M 324], [Type I] [Type II or III] [Type IV], hot-applied, single-component, polymer-modified bituminous sealant.

Retain one of first four paragraphs below if pavement marking is required.  Verify availability with marking-paint manufacturers.

In first paragraph below, drying time of Type N is 15 to 30 minutes.  Type F dries faster, in 3 to 6 minutes if heated to about 125 deg F (51.5 deg C).  Type S dries slowest and should be used only where traffic cones can be in place for one hour or more.  Alkyd-resin-type pavement paints exceed 150-g/L VOC limits imposed by the EPA for "traffic-marking coatings," but may meet 450-g/L VOC limits imposed by the EPA for "zone-marking coatings."  See Evaluations.

E. Pavement-Marking Paint:  Alkyd-resin type, lead and chromate free, ready mixed, complying with AASHTO M 248, [Type N] [Type F] [Type S]; colors complying with FS TT-P-1952.

Select from colors in subparagraph below.  If more than one color is required, indicate locations of each on Drawings or by inserts.

1. Color:  [White] [Yellow] [Blue] [As indicated] <Insert color>.

F. Pavement-Marking Paint:  MPI #32 Alkyd Traffic Marking Paint.

Select from colors in subparagraph below.  If more than one color is required, indicate locations of each on Drawings or by inserts.

1. Color:  [White] [Yellow] [Blue] [As indicated] <Insert color>.

In first paragraph below, revise type to Type I if anticipated weather conditions are sufficiently benign.  See Evaluations.  Some formulations of waterborne emulsions are very quick drying, others less so; see manufacturer's literature.

G. Pavement-Marking Paint:  Latex, waterborne emulsion, lead and chromate free, ready mixed, complying with FS TT-P-1952, Type II, with drying time of less than [three] [45] minutes.

Select from colors in subparagraph below.  If more than one color is required, indicate locations of each on Drawings or by inserts.

1. Color:  [White] [Yellow] [Blue] [As indicated] <Insert color>.

H. Pavement-Marking Paint:  MPI #97 Latex Traffic Marking Paint.

Select from colors in subparagraph below.  If more than one color is required, indicate locations of each on Drawings or by inserts.

1. Color:  [White] [Yellow] [Blue] [As indicated] <Insert color>.

Retain first paragraph below with pavement-marking paints above if reflectorized pavement markings are required.

I. Glass Beads:  AASHTO M 247, Type 1.

Insert product requirements here for permanent-marking tapes or thermoplastic paints if required.  See Evaluations.

Retain one of first two paragraphs below if wheel stops are required.  Revise concrete strength or dimensions of wheel stops in first paragraph to suit Project.

J. Wheel Stops:  Precast, air-entrained concrete, 2500-psi (17.2-MPa) minimum compressive strength, [4-1/2 inches (115 mm) high by 9 inches (225 mm) wide by 72 inches (1800 mm) long] <Insert dimensions>.  Provide chamfered corners, drainage slots on underside, and holes for anchoring to substrate.

1. Dowels:  Galvanized steel, 3/4-inch (19-mm) diameter, 10-inch (254-mm) minimum length.

Revise materials or dimensions of wheel stops, dowels, and adhesive in paragraph below to suit Project.  Many manufacturers produce recycled rubber and plastic wheel stops.

K. Wheel Stops:  Solid, integrally colored, 96 percent recycled HDPE or commingled postconsumer and postindustrial recycled plastic; UV stabilized; [4 inches (100 mm) high by 6 inches (150 mm) wide by 72 inches (1800 mm) long] <Insert dimensions>.  Provide chamfered corners, drainage slots on underside, and holes for anchoring to substrate.

1. Dowels:  Galvanized steel, 3/4-inch (19-mm) diameter, 10-inch (254-mm) minimum length.

Retain subparagraph below where permanently installed HDPE or plastic stops are required or if mechanical attachment is considered insufficient.

2. Adhesive:  As recommended by wheel-stop manufacturer for application to asphalt pavement.

2.4 PREFORMED TRAFFIC-CALMING DEVICES

Retain this article if preformed traffic-calming devices are required.  Copy paragraph below and re-edit for each product.  Insert number to complete drawing designation.  Use these designations on Drawings to identify each product.

Revise materials or dimensions of devices, hardware, and adhesive below to suit Project.  If known, a specific manufacturer's product can be inserted.

A. Speed [Bumps] [Humps] [Cushions] <Insert drawing designation>:  Solid, integrally colored, 100 percent postconsumer or commingled postconsumer and postindustrial recycled [rubber] [plastic]; UV stabilized.  Provide holes for anchoring to substrate.

Retain one of first two subparagraphs below.  Retain first for speed bumps and second for speed humps and speed cushions.

1. Size:  Modular bumps [2 inches (51 mm) high by 10 inches (254 mm) wide by 72 inches (1800 mm) long] <Insert dimensions>, with overall length as dimensioned on Drawings.

2. Size:  Modular assemblies [3 inches (76 mm) high by 12 feet (3.7 m) in overall width] [4 inches (102 mm) high by 14 feet (4.3 m) in overall width] <Insert dimensions>, with overall length as dimensioned on Drawings.

In first subparagraph below, second hardware option is limited to asphalt where drilling holes is permitted.

3. Mounting Hardware:  Galvanized-steel [spike, 1/2-inch (13-mm) diameter, 10-inch (254-mm) minimum length] [lag screw, shield, and washers; 1/2-inch (13-mm) diameter, 8-inch (203-mm) minimum length] [hardware as standard with device manufacturer].

Retain subparagraph below where permanently installed devices are required or if traffic load is very heavy and mechanical attachment is insufficient.

4. Adhesive:  [As recommended by device manufacturer] <Insert requirement>.

2.5 IMPRINTED ASPHALT MATERIALS

Retain this article if imprinted asphalt paving is required.  Article is based on products by Integrated Paving Concepts.  If required, revise materials below to suit Project.

A. Templates:  Imprinted-asphalt manufacturer's standard flexible templates for imprinting pattern into hot asphalt paving.

1. Pattern:  [Running bond brick] [Cobblestone] [Custom pattern indicated on Drawings] <Insert pattern>.

Retain first paragraph below only for coated imprinted asphalt.

B. Coating System:  Imprinted-asphalt manufacturer's standard system formulated for exterior application on asphalt paving surfaces.

Retain first subparagraph below only for dry climate zone, such as Southwest USA, if recommended by manufacturer.

1. Base Coating:  Portland cement and epoxy-modified acrylic polymer blended with sand and aggregate, formulated for exterior application on asphalt paving surfaces.

2. Top Coating:  Epoxy-modified acrylic polymer blended with sand and aggregate, formulated for exterior application on asphalt paving surfaces.

3. Colorant:  UV-stable pigment blend, added to each coating layer.

4. Color:  [White] [Yellow] <Insert color>.

Retain paragraph below only for inlaid, reflectorized, heat-bonded, pavement-marking pattern.

C. Precut Marking Material:  Imprinted-asphalt manufacturer's standard, reflectorized, thermoplastic, 90-mil (2.3-mm) minimum thickness, formulated for exterior application on asphalt paving surfaces, and matching the imprinted pattern of templates.

2.6 MIXES

Retain first paragraph below if specifying state or local DOT standard paving mixes.  DOT standard paving mixes will usually be required for public roads.  Same paving mixes may also be used for private work.  If specifying a Superpave asphalt mix, revise paragraph by inserting details of aggregate gradations and paving mix.

A. Hot-Mix Asphalt:  Dense, hot-laid, hot-mix asphalt plant mixes approved by authorities having jurisdiction[; designed according to procedures in AI MS-2, "Mix Design Methods for Asphalt Concrete and Other Hot-Mix Types";] and complying with the following requirements:

1. Provide mixes with a history of satisfactory performance in geographical area where Project is located.

Revise subparagraphs below to identify state or local DOT specifications for each course.  Insert binder course in list if required.

2. Base Course:  <Insert mix designation>.

3. Surface Course:  <Insert mix designation>.

Retain first paragraph below for asphalt mixes that are based on ASTM D 3515 requirements.  Retain option for approval of these mixes by state or local DOT if that is the practice of authorities having jurisdiction.  Asphalt mixes may be further qualified by inserting minimum Hveem or Marshall test criteria and voids-in-mineral-aggregate (VMA) percentages.

B. Hot-Mix Asphalt:  Dense, hot-laid, hot-mix asphalt plant mixes[ approved by authorities having jurisdiction and] designed according to procedures in AI MS-2, "Mix Design Methods for Asphalt Concrete and Other Hot-Mix Types."

1. Provide mixes with a history of satisfactory performance in geographical area where Project is located.

2. Provide mixes complying with composition, grading, and tolerance requirements in ASTM D 3515 for the following nominal, maximum aggregate sizes:

Revise aggregate sizes in subparagraphs below for each course as required for Project.

a. Base Course:  [1 inch (25 mm)] <Insert size>.

b. Surface Course:  [1/2 inch (13 mm)] <Insert size>.

In paragraph below, retain appropriate type from options listed.  Slurry is a mixture of emulsified asphalt, fine aggregate, and mineral fillers.  Type 1 offers maximum crack penetration and is used for surface sealing of lightly trafficked areas such as parking lots.  Type 2, the most widely used gradation, is suited to moderate traffic, fills surface voids, corrects surface erosion, and builds a minimum wearing surface.  Type 3 builds a new wearing surface, may build up a crown, and improves skid resistance.

C. Emulsified-Asphalt Slurry:  ASTM D 3910, [Type 1] [Type 2] [Type 3].

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Verify that subgrade is dry and in suitable condition to begin paving.

Retain first paragraph below for full-depth asphalt pavement.

B. Proof-roll subgrade below pavements with heavy pneumatic-tired equipment to identify soft pockets and areas of excess yielding.  Do not proof-roll wet or saturated subgrades.

1. Completely proof-roll subgrade in one direction[, repeating proof-rolling in direction perpendicular to first direction].  Limit vehicle speed to 3 mph (5 km/h).

Revise minimum weight or type of vehicle in first subparagraph below if required.

2. Proof roll with a loaded 10-wheel, tandem-axle dump truck weighing not less than 15 tons (13.6 tonnes).

3. Excavate soft spots, unsatisfactory soils, and areas of excessive pumping or rutting, as determined by Architect, and replace with compacted backfill or fill as directed.

C. Proceed with paving only after unsatisfactory conditions have been corrected.

Retain paragraph below if imprinted asphalt paving is required.

D. Verify that utilities, traffic loop detectors, and other items requiring a cut and installation beneath the asphalt surface have been completed and that asphalt surface has been repaired flush with adjacent asphalt prior to beginning installation of imprinted asphalt.

3.2 COLD MILLING

Retain this article if removing a course or layer from an existing hot-mix asphalt pavement.

A. Clean existing pavement surface of loose and deleterious material immediately before cold milling.  Remove existing asphalt pavement by cold milling to grades and cross sections indicated.

1. Mill to a depth of [1-1/2 inches (38 mm)] [2 inches (50 mm)] [3 inches (75 mm)] <Insert depth>.

2. Mill to a uniform finished surface free of excessive gouges, grooves, and ridges.

3. Control rate of milling to prevent tearing of existing asphalt course.

4. Repair or replace curbs, manholes, and other construction damaged during cold milling.

5. Excavate and trim unbound-aggregate base course, if encountered, and keep material separate from milled hot-mix asphalt.

Retain first subparagraph below if applicable.

6. Transport milled hot-mix asphalt to asphalt recycling facility.

7. Keep milled pavement surface free of loose material and dust.

3.3 PATCHING

Retain this article if patching existing pavement.  Retain first paragraph below if existing pavement is hot-mix asphalt.

A. Hot-Mix Asphalt Pavement:  Saw cut perimeter of patch and excavate existing pavement section to sound base.  Excavate rectangular or trapezoidal patches, extending 12 inches (300 mm) into adjacent sound pavement, unless otherwise indicated.  Cut excavation faces vertically.  Remove excavated material.  Recompact existing unbound-aggregate base course to form new subgrade.

Retain first paragraph below if existing pavement is portland cement concrete.

B. Portland Cement Concrete Pavement:  Break cracked slabs and roll as required to reseat concrete pieces firmly.

1. Pump hot undersealing asphalt under rocking slab until slab is stabilized or, if necessary, crack slab into pieces and roll to reseat pieces firmly.

2. Remove disintegrated or badly cracked pavement.  Excavate rectangular or trapezoidal patches, extending into adjacent sound pavement, unless otherwise indicated.  Cut excavation faces vertically.  Recompact existing unbound-aggregate base course to form new subgrade.

Retain first paragraph below for coating vertical surfaces abutting hot-mix asphalt patches.

C. Tack Coat:  Apply uniformly to vertical surfaces abutting or projecting into new, hot-mix asphalt paving at a rate of 0.05 to 0.15 gal./sq. yd. (0.2 to 0.7 L/sq. m).

1. Allow tack coat to cure undisturbed before applying hot-mix asphalt paving.

2. Avoid smearing or staining adjoining surfaces, appurtenances, and surroundings.  Remove spillages and clean affected surfaces.

Retain one of two paragraphs below.  Retain first paragraph if a single asphalt course, preferred by AI, is proposed.  Retain second if separate asphalt courses are required.

D. Patching:  Fill excavated pavements with hot-mix asphalt base mix for full thickness of patch and, while still hot, compact flush with adjacent surface.

E. Patching:  Partially fill excavated pavements with hot-mix asphalt base mix and, while still hot, compact.  Cover asphalt base course with compacted, hot-mix surface layer finished flush with adjacent surfaces.

3.4 REPAIRS

Retain first paragraph below if surface irregularities of existing pavement to be repaved exceed ability of hot-mix paver to correct.  Leveling courses are usually applied over existing pavements before placing hot-mix asphalt overlays or other surface treatments.  Revise leveling-course mix to a base-course mix if appropriate.

A. Leveling Course:  Install and compact leveling course consisting of hot-mix asphalt surface course to level sags and fill depressions deeper than 1 inch (25 mm) in existing pavements.

1. Install leveling wedges in compacted lifts not exceeding 3 inches (75 mm) thick.

B. Crack and Joint Filling:  Remove existing joint filler material from cracks or joints to a depth of [1/4 inch (6 mm)] <Insert depth>.

1. Clean cracks and joints in existing hot-mix asphalt pavement.

2. Use emulsified-asphalt slurry to seal cracks and joints less than 1/4 inch (6 mm) wide.  Fill flush with surface of existing pavement and remove excess.

3. Use hot-applied joint sealant to seal cracks and joints more than 1/4 inch (6 mm) wide.  Fill flush with surface of existing pavement and remove excess.

3.5 SURFACE PREPARATION

A. General:  Immediately before placing asphalt materials, remove loose and deleterious material from substrate surfaces.  Ensure that prepared subgrade is ready to receive paving.

Retain first paragraph below if weed control is required.

B. Herbicide Treatment:  Apply herbicide according to manufacturer's recommended rates and written application instructions.  Apply to dry, prepared subgrade or surface of compacted-aggregate base before applying paving materials.

Retain subparagraph below unless full-depth asphalt pavement is proposed.

1. Mix herbicide with prime coat if formulated by manufacturer for that purpose.

Retain first paragraph below if priming unbound-aggregate base courses.

C. Prime Coat:  Apply uniformly over surface of compacted unbound-aggregate base course at a rate of 0.15 to 0.50 gal./sq. yd. (0.7 to 2.3 L/sq. m).  Apply enough material to penetrate and seal but not flood surface.  Allow prime coat to cure.

1. If prime coat is not entirely absorbed within 24 hours after application, spread sand over surface to blot excess asphalt.  Use enough sand to prevent pickup under traffic.  Remove loose sand by sweeping before pavement is placed and after volatiles have evaporated.

2. Protect primed substrate from damage until ready to receive paving.

Retain paragraph below if tack coating an existing hot-mix asphalt pavement before placing a paving overlay.

D. Tack Coat:  Apply uniformly to surfaces of existing pavement at a rate of 0.05 to 0.15 gal./sq. yd. (0.2 to 0.7 L/sq. m).

1. Allow tack coat to cure undisturbed before applying hot-mix asphalt paving.

2. Avoid smearing or staining adjoining surfaces, appurtenances, and surroundings.  Remove spillages and clean affected surfaces.

3.6 PAVING GEOTEXTILE INSTALLATION

Retain this article if using paving geotextile over existing hot-mix asphalt pavement.  Retain embedment material from three options in first paragraph below.

A. Apply [tack coat] [asphalt binder] [asphalt cement] uniformly to existing pavement surfaces at a rate of 0.20 to 0.30 gal./sq. yd. (0.8 to 1.2 L/sq. m).

B. Place paving geotextile promptly according to manufacturer's written instructions.  Broom or roll geotextile smooth and free of wrinkles and folds.  Overlap longitudinal joints 4 inches (100 mm) and transverse joints 6 inches (150 mm).

1. Protect paving geotextile from traffic and other damage and place hot-mix asphalt paving overlay the same day.

3.7 HOT-MIX ASPHALT PLACING

In addition to new work, this article applies to hot-mix asphalt paving overlay on existing asphalt or concrete pavements.

A. Machine place hot-mix asphalt on prepared surface, spread uniformly, and strike off.  Place asphalt mix by hand to areas inaccessible to equipment in a manner that prevents segregation of mix.  Place each course to required grade, cross section, and thickness when compacted.

Revise first two subparagraphs below to suit Project.  AI recommends that the minimum compacted thickness of hot-mix asphalt paving lift exceed three times the maximum nominal aggregate size.

1. Place hot-mix asphalt base course in number of lifts and thicknesses indicated.

2. Place hot-mix asphalt surface course in single lift.

Revise first subparagraph below to higher temperature if thin lifts in cool weather are likely.  See National Asphalt Pavement Association recommendations.

3. Spread mix at minimum temperature of 250 deg F (121 deg C).

4. Begin applying mix along centerline of crown for crowned sections and on high side of one-way slopes unless otherwise indicated.

5. Regulate paver machine speed to obtain smooth, continuous surface free of pulls and tears in asphalt-paving mat.

B. Place paving in consecutive strips not less than 10 feet (3 m) wide unless infill edge strips of a lesser width are required.

1. After first strip has been placed and rolled, place succeeding strips and extend rolling to overlap previous strips.  Complete a section of asphalt base course before placing asphalt surface course.

C. Promptly correct surface irregularities in paving course behind paver.  Use suitable hand tools to remove excess material forming high spots.  Fill depressions with hot-mix asphalt to prevent segregation of mix; use suitable hand tools to smooth surface.

3.8 JOINTS

A. Construct joints to ensure a continuous bond between adjoining paving sections.  Construct joints free of depressions, with same texture and smoothness as other sections of hot-mix asphalt course.

1. Clean contact surfaces and apply tack coat to joints.

2. Offset longitudinal joints, in successive courses, a minimum of 6 inches (150 mm).

3. Offset transverse joints, in successive courses, a minimum of 24 inches (600 mm).

4. Construct transverse joints at each point where paver ends a day's work and resumes work at a subsequent time.  Construct these joints [using either "bulkhead" or "papered" method according to AI MS-22, for both "Ending a Lane" and "Resumption of Paving Operations."] [as shown on Drawings.] <Insert joint requirement.>

5. Compact joints as soon as hot-mix asphalt will bear roller weight without excessive displacement.

6. Compact asphalt at joints to a density within 2 percent of specified course density.

3.9 COMPACTION

A. General:  Begin compaction as soon as placed hot-mix paving will bear roller weight without excessive displacement.  Compact hot-mix paving with hot, hand tampers or with vibratory-plate compactors in areas inaccessible to rollers.

1. Complete compaction before mix temperature cools to 185 deg F (85 deg C).

B. Breakdown Rolling:  Complete breakdown or initial rolling immediately after rolling joints and outside edge.  Examine surface immediately after breakdown rolling for indicated crown, grade, and smoothness.  Correct laydown and rolling operations to comply with requirements.

C. Intermediate Rolling:  Begin intermediate rolling immediately after breakdown rolling while hot-mix asphalt is still hot enough to achieve specified density.  Continue rolling until hot-mix asphalt course has been uniformly compacted to the following density:

Revise average density and range of acceptable densities in applicable subparagraph below if required.  First subparagraph refers to Marshall test method.  Revise to Superpave Gyratory Compactor method to verify field compaction if using Superpave method of mix design.  Second subparagraph refers to Rice test method preferred by AI.

1. Average Density:  96 percent of reference laboratory density according to [ASTM D 6927] [or] [AASHTO T 245], but not less than 94 percent nor greater than 100 percent.

2. Average Density:  92 percent of reference maximum theoretical density according to ASTM D 2041, but not less than 90 percent nor greater than 96 percent.

D. Finish Rolling:  Finish roll paved surfaces to remove roller marks while hot-mix asphalt is still warm.

E. Edge Shaping:  While surface is being compacted and finished, trim edges of pavement to proper alignment.  Bevel edges while asphalt is still hot; compact thoroughly.

F. Repairs:  Remove paved areas that are defective or contaminated with foreign materials and replace with fresh, hot-mix asphalt.  Compact by rolling to specified density and surface smoothness.

G. Protection:  After final rolling, do not permit vehicular traffic on pavement until it has cooled and hardened.

H. Erect barricades to protect paving from traffic until mixture has cooled enough not to become marked.

3.10 ASPHALT CURBS

Retain this article if hot-mix asphalt curbs are required.

A. Construct hot-mix asphalt curbs over compacted pavement surfaces.  Apply a light tack coat unless pavement surface is still tacky and free from dust.  Spread mix at minimum temperature of 250 deg F (121 deg C).

Revise subparagraph below to insert designations of state or local DOT if mixes are different.

1. Asphalt Mix:  Same as pavement surface-course mix.

B. Place hot-mix asphalt to curb cross section indicated or, if not indicated, to local standard shapes, by machine or by hand in wood or metal forms.  Tamp hand-placed materials and screed to smooth finish.  Remove forms after hot-mix asphalt has cooled.

3.11 ASPHALT TRAFFIC-CALMING DEVICES

Retain this article only for site-formed, asphalt traffic-calming devices.  Retain tolerance or revise to suit Project.

A. Construct hot-mix asphalt speed [bumps] [humps] [cushions] [and] [tables] over compacted pavement surfaces.  Apply a tack coat unless pavement surface is still tacky and free from dust.  Spread mix at minimum temperature of 250 deg F (121 deg C).

1. Tack Coat Application:  Apply uniformly to surfaces of existing pavement at a rate of 0.05 to 0.15 gal./sq. yd. (0.2 to 0.7 L/sq. m).

Revise first subparagraph below to insert designations of state or local DOT if mixes are different.

2. Asphalt Mix:  Same as pavement surface-course mix.

Retain subparagraph below for existing pavement, where height of traffic-calming device and speed of traffic warrant it or where this is local practice.  Consult state or local DOT for advice.

3. Before installation, mill pavement that will be in contact with bottom of traffic-calming device.  Mill to a depth of 1 inch (25 mm) from top of pavement to a clean, rough profile.

B. Place hot-mix asphalt to cross section indicated, by machine or by hand in wood or metal forms.  Tamp hand-placed materials and screed to smooth finish.  Remove forms after hot-mix asphalt has cooled.

3.12 INSTALLATION TOLERANCES

A. Pavement Thickness:  Compact each course to produce the thickness indicated within the following tolerances:

Retain thickness tolerances in subparagraphs below or revise to suit Project.

1. Base Course:  Plus or minus 1/2 inch (13 mm).

2. Surface Course:  Plus 1/4 inch (6 mm), no minus.

B. Pavement Surface Smoothness:  Compact each course to produce a surface smoothness within the following tolerances as determined by using a 10-foot (3-m) straightedge applied transversely or longitudinally to paved areas:

1. Base Course:  [1/4 inch (6 mm)] <Insert size>.

Revise subparagraph above or first subparagraph below to suit Project.

2. Surface Course:  [1/8 inch (3 mm)] <Insert size>.

Retain subparagraph below if crowned pavement surfaces are required.

3. Crowned Surfaces:  Test with crowned template centered and at right angle to crown.  Maximum allowable variance from template is 1/4 inch (6 mm).

Retain paragraph below only for site-formed, asphalt traffic-calming devices.  Retain tolerance or revise to suit Project.

C. Traffic-Calming Devices:  Compact and form asphalt to produce the contour indicated and within a tolerance of plus or minus 1/8 inch (3 mm) of height indicated above pavement surface.

3.13 SURFACE TREATMENTS

Retain this article if surface treatments, which are usually applied to older asphalt pavements, are required.  See Evaluations.

A. Fog Seals:  Apply fog seal at a rate of 0.10 to 0.15 gal./sq. yd. (0.45 to 0.7 L/sq. m) to existing asphalt pavement and allow to cure.  With fine sand, lightly dust areas receiving excess fog seal.

B. Slurry Seals:  Apply slurry coat in a uniform thickness according to ASTM D 3910 and allow to cure.

Rolling is needed where slurry thickness exceeds 1/4 inch (6 mm) or for surfaces subject to turning, braking, or accelerating forces.

1. Roll slurry seal to remove ridges and provide a uniform, smooth surface.

3.14 PAVEMENT MARKING

Retain this article if pavement marking is required.

A. Do not apply pavement-marking paint until layout, colors, and placement have been verified with Architect.

Marking-paint manufacturers caution that paint will bleed or tear surface of new asphalt unless asphalt is aged before painting.  This aging period may vary from 30 to 90 days.  If pavement marking must proceed immediately, consider revising to a phased application of a thin first coat followed by a thicker second coat once asphalt has aged.  Verify that two-coat application is recommended by pavement-marking manufacturer.

B. Allow paving to age for [30] [90] <Insert number> days before starting pavement marking.

C. Sweep and clean surface to eliminate loose material and dust.

Retain paragraph below if retaining waterborne emulsion pavement-marking paint.

D. Apply paint with mechanical equipment to produce pavement markings, of dimensions indicated, with uniform, straight edges.  Apply at manufacturer's recommended rates to provide a minimum wet film thickness of 15 mils (0.4 mm).

Retain subparagraph below if glass beads are required for reflectivity.

1. Broadcast glass beads uniformly into wet pavement markings at a rate of 6 lb/gal. (0.72 kg/L).

3.15 WHEEL STOPS

Retain this article if wheel stops are required.

Retain first paragraph below where permanently installed HDPE or plastic stops are required or if mechanical attachment is considered insufficient.

A. Install wheel stops in bed of adhesive as recommended by manufacturer.

B. Securely attach wheel stops to pavement with not less than two galvanized-steel dowels embedded at one-quarter to one-third points.  Securely install dowels into pavement and bond to wheel stop.  Recess head of dowel beneath top of wheel stop.

3.16 PREFORMED TRAFFIC-CALMING DEVICES

Retain this article if preformed traffic-calming devices are required.

Retain first paragraph below where permanently installed devices are required or if traffic load is very heavy and mechanical attachment is insufficient.

A. Install preformed speed [bumps] [humps] [cushions] in bed of adhesive as recommended by manufacturer for heavy traffic.

B. Securely attach preformed speed [bumps] [humps] [cushions] to pavement with hardware spaced as recommended by manufacturer for heavy traffic.  Recess head of hardware beneath top surface.

3.17 IMPRINTING ASPHALT

Retain this article if imprinted asphalt paving is required.  This article is based on products by Integrated Paving Concepts.  If required, revise procedures in paragraphs below to suit Project.

A. General:  Imprint asphalt according to manufacturer's written instructions, using manufacturer's recommended equipment.

Retain first paragraph below if imprinting can immediately follow asphalt installation.  This sequence, which allows little inspection and correction time after asphalt is installed, is not common because imprinted asphalt is usually retrofit.  Coordination between asphalt crews and imprinting crews is essential to maintain adequate surface temperature for imprinting in cool weather and during available daylight.

B. Freshly Laid Asphalt:  Immediately after asphalt has been laid and compacted but still plastic, begin the surface imprinting process.

1. Monitor asphalt surface temperature in compliance with manufacturer's written recommendations to ensure required temperature to perform surface imprinting.

2. Reheat asphalt if surface temperature drops below that required.

Retain first paragraph below for imprinting existing asphalt pavement and for reheating new asphalt pavement.

C. Reheating Asphalt:  Soften asphalt pavement surface by heating to a depth of at least 1/2 inch (13 mm) without burning asphalt.

1. Heat to a temperature of 300 to 325 deg F (149 to 163 deg C) immediately before applying templates.

2. Regularly monitor the pavement temperature to prevent overheating.

3. Direct flame heaters are not permitted.

4. If pavement is overheated and begins to emit black smoke, remove damaged pavement by milling down 1 inch (25 mm) and replace removed pavement with new, compacted surface course prior to resuming imprinting work.

In first paragraph below, retain first option for coated imprinted asphalt.  Retain second option for inlaid, reflectorized, heat-bonded, pavement-marking pattern.

D. Surface Imprinting:  Apply and imprint templates to a minimum depth [of 1/4 inch (6 mm)] [as required to embed precut marking material flush or barely beneath pavement surface].

Retain first paragraph below only for coated imprinted asphalt.  Retain first option for dry climate zone.  Retain second option for other locations.

E. Coating Application:  After imprinted surface has cooled, apply [two layers of base coating followed by two layers of top coating] [four layers of top coating].  Do not allow traffic until coating has completely dried and cured.

Retain paragraph below only for inlaid, reflectorized, heat-bonded, pavement-marking pattern.

F. Precut Marking Material Application:  Position precut marking material aligned with imprinted pattern and slowly heat to a temperature no higher than 325 deg F (163 deg C) until marking material begins to liquefy and flow.  Do not allow traffic until installed marking material has cooled to ambient temperature.

3.18 FIELD QUALITY CONTROL

A. Testing Agency:  [Owner will engage] [Engage] a qualified testing agency to perform tests and inspections.

B. Thickness:  In-place compacted thickness of hot-mix asphalt courses will be determined according to ASTM D 3549.

C. Surface Smoothness:  Finished surface of each hot-mix asphalt course will be tested for compliance with smoothness tolerances.

Retain first paragraph below only for site-formed, asphalt traffic-calming devices.

D. Traffic-Calming Devices:  Finished height of asphalt speed [bumps] [humps] [cushions] [and] [tables] above pavement will be measured for compliance with tolerances.

Revise methods of verifying field compaction if using Superpave mix-design system.  Consult state or local DOT for methods that have been successfully used.

E. In-Place Density:  Testing agency will take samples of uncompacted paving mixtures and compacted pavement according to [ASTM D 979] [or] [AASHTO T 168].

1. Reference maximum theoretical density will be determined by averaging results from four samples of hot-mix asphalt-paving mixture delivered daily to site, prepared according to ASTM D 2041, and compacted according to job-mix specifications.

2. In-place density of compacted pavement will be determined by testing core samples according to ASTM D 1188 or ASTM D 2726.

a. One core sample will be taken for every 1000 sq. yd. (836 sq. m) or less of installed pavement, with no fewer than 3 cores taken.

b. Field density of in-place compacted pavement may also be determined by nuclear method according to ASTM D 2950 and correlated with ASTM D 1188 or ASTM D 2726.

F. Replace and compact hot-mix asphalt where core tests were taken.

G. Remove and replace or install additional hot-mix asphalt where test results or measurements indicate that it does not comply with specified requirements.

3.19 DISPOSAL

Retain this article if repairs, patching, or cold milling of existing pavement is required.

A. Except for material indicated to be recycled, remove excavated materials from Project site and legally dispose of them in an EPA-approved landfill.

1. Do not allow milled materials to accumulate on-site.

END OF SECTION 02741

ASPHALT PAVING
02741 - 1

