Copyright 2000 AIA
MASTERSPEC
5/00

Copyright 2000, The American Institute of Architects (AIA)

SECTION 07551 - APP-MODIFIED BITUMINOUS MEMBRANE ROOFING
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project.

1. APP-modified bituminous membrane roofing.

2. Hybrid built-up and APP-modified bituminous membrane roofing.

3. Protected, APP-modified bituminous membrane roofing.

4. Vapor retarder.

5. Roof insulation.

Delete first paragraph below if no acoustical roof deck is required.

B. This Section includes the installation of acoustical roof deck rib insulation strips furnished under Division 5 Section "Steel Deck."

C. Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

1. Division 5 Section "Steel Deck" for furnishing acoustical deck rib insulation.

2. Division 6 Section "[Rough Carpentry] [Miscellaneous Carpentry]" for wood nailers, cants, curbs, and blocking[ and for wood-based, structural-use roof deck panels].

3. Division 7 Section "Building Insulation" for insulation beneath the roof deck.

4. Division 7 Section "Sheet Metal Flashing and Trim" for metal roof penetration flashings, flashings, and counterflashings.

5. Division 7 Section "Roof Expansion Assemblies."

6. Division 15 Section "Plumbing Specialties" for roof drains.

Unit prices may be required in bid documents.  Examples include temporary roofing and removal and replacement of wet roof insulation that may be discovered during reroofing.

D. Unit Prices:  Refer to Division 1 Section "Unit Prices" for description of Work in this Section affected by unit prices.

If alternates or allowances apply to work of this Section, insert brief paragraphs here to alert Contractor and reference appropriate Division 1 Section for specific details.

1.3 DEFINITIONS

A. Roofing Terminology:  Refer to ASTM D 1079 and glossary of NRCA's "The NRCA Roofing and Waterproofing Manual" for definition of terms related to roofing work in this Section.

Retain paragraph below if using traditional roofing asphalt, complying with ASTM D 312, for adhering roofing components other than APP-modified asphalt roofing sheets; delete if only SEBS-modified roofing asphalt complying with ASTM D 6152 is required.

B. Hot Roofing Asphalt:  Roofing asphalt heated to its equiviscous temperature, the temperature at which its viscosity is 125 centipoise for mop-applied roofing asphalt and 75 centipoise for mechanical spreader-applied roofing asphalt, within a range of plus or minus 25 deg F (14 deg C), measured at the mop cart or mechanical spreader immediately before application.

Retain two definitions below if design uplift pressure subparagraphs based on SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems" are retained in "Performance Requirements" Article.  Roofing system must resist, at a minimum, design uplift pressure.  Design uplift pressure, multiplied by a safety factor, produces the factored design uplift pressure.

C. Design Uplift Pressure:  The uplift pressure, calculated according to procedures in SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems," before multiplication by a safety factor.

D. Factored Design Uplift Pressure:  The uplift pressure, calculated according to procedures in SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems," after multiplication by a safety factor.

1.4 PERFORMANCE REQUIREMENTS

A. General:  Provide installed roofing membrane and base flashings that remain watertight; do not permit the passage of water; and resist specified uplift pressures, thermally induced movement, and exposure to weather without failure.

B. Material Compatibility:  Provide roofing materials that are compatible with one another under conditions of service and application required, as demonstrated by roofing manufacturer based on testing and field experience.

Retain paragraph and subparagraphs below if roofing system is to be designed to withstand uplift pressure established by ASCE 7.  Revise design uplift pressures in subparagraphs if local building code requirements are more stringent than ASCE 7.  Retain with "FMG Listing" Paragraph and subparagraphs below if both ASCE 7 and FMG criteria may apply.  Delineate dimensions of corners, perimeter, and field of roof on Drawings.

C. Roofing System Design:  Provide a roofing system that is identical to systems that have been successfully tested by a qualified testing and inspecting agency to resist uplift pressure calculated according to ASCE 7.

1. Corner Uplift Pressure:  <Insert number> lbf/sq. ft. (kN/sq. m).

2. Perimeter Uplift Pressure:  <Insert number> lbf/sq. ft. (kN/sq. m).

3. Field-of-Roof Uplift Pressure:  <Insert number> lbf/sq. ft. (kN/sq. m).

Retain paragraph and subparagraphs below if Project is FMG insured or if FMG requirements will set a minimum quality standard.  Coordinate requirements of FMG classification with other requirements in this Section.

D. FMG Listing:  Provide roofing membrane, base flashings, and component materials that comply with requirements in FMG 4450 and FMG 4470 as part of a roofing system and that are listed in FMG's "Approval Guide" for Class 1 or noncombustible construction, as applicable.  Identify materials with FMG markings.

Select one option in first subparagraph below based on windstorm classification of Project.  FMG Loss Prevention Data Sheet 1-28 multiplies the actual field-of-roof uplift pressure by a factor of 2 to obtain the factored pressure, the number that establishes the minimum FMG approval rating.  Verify availability of roofing systems that meet these classifications.  Other options for classifications increase in increments of 15, e.g., Class 1A-135, 1A-150, 1A-165, and higher.  "Class 1A" signifies meeting ASTM E 108, Class A fire performance for FMG-approved Class 1 roof covers.  For areas having three or more hailstorms annually, FMG recommends roofing systems rated SH (severe hail) instead of MH (moderate hail).

1. Fire/Windstorm Classification:  Class 1A-[60] [75] [90] [105] [120] <Insert number>.

2. Hail Resistance:  [MH] [SH].

Retain paragraph and subparagraphs below if roofing system is to be designed to withstand wind loads established from SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems."  SPRI derives design uplift pressure using ASCE 7's wind load procedure and increases this pressure by a safety factor.

E. Roofing System Design:  Provide a roofing system that is identical to systems that have been successfully tested by a qualified testing and inspecting agency to resist the factored design uplift pressures calculated according to SPRI's "Wind Load Design Guide for Fully Adhered and Mechanically Fastened Roofing Systems."

SPRI requires the calculated design uplift pressure for each roof area to be multiplied by a safety factor to arrive at uplift resistance required of the roofing system.  Delineate dimensions of corners, perimeter, and field of roof on Drawings.

1. Corner Design Uplift Pressure:  <Insert number> lbf/sq. ft. (kN/sq. m).

2. Perimeter Design Uplift Pressure:  <Insert number> lbf/sq. ft. (kN/sq. m).

3. Field-of-Roof Design Uplift Pressure:  <Insert number> lbf/sq. ft. (kN/sq. m).

4. Safety Factor:  <Insert number.>

1.5 SUBMITTALS

A. Product Data:  For each type of product indicated.

B. Shop Drawings:  For roofing system.  Include plans, elevations, sections, details, and attachments to other Work.

Adjust list below to suit Project.

1. Base flashings, cants, and membrane terminations.

2. Tapered insulation, including slopes.

3. Crickets, saddles, and tapered edge strips, including slopes.

4. Insulation fastening patterns.

C. Samples for Verification:  For the following products:

Adjust list below to suit Project.

1. 12-by-12-inch (300-by-300-mm) square of [base sheet] [base-ply sheet] [smooth-surfaced roofing membrane sheet] [flashing backer sheet].

2. 12-by-12-inch (300-by-300-mm) square of [smooth-surfaced roofing membrane cap sheet] [mineral-granule-surfaced roofing membrane cap sheet] [flashing sheet], of color specified.

3. 12-by-12-inch (300-by-300-mm) square of vapor retarder.

4. 12-by-12-inch (300-by-300-mm) square of roof insulation.

Aggregate ballast in subparagraph below is a ballast option for protected membrane roofing.

5. 10 lb (4.5 kg) of aggregate ballast in color and gradation indicated.

Retain first option in first subparagraph below if roof pavers are limited to walkways.  Retain second option if lightweight or heavyweight roof pavers are ballast for protected membrane roofing.

6. Full-size [walkway roof paver] [roof-paver ballast] in each color and texture required.

7. 12-by-12-inch (300-by-300-mm) square of walkway pad or walkway cap sheet.

8. Six insulation fasteners of each type, length, and finish.

Retain paragraph below if Installer certification is required in "Quality Assurance" Article or a special warranty is required.

D. Installer Certificates:  Signed by roofing system manufacturer certifying that Installer is approved, authorized, or licensed by manufacturer to install roofing system.

Retain paragraph and subparagraph below if "Performance Requirements" Article and either "Roofing System Design" or "FMG Listing" Paragraph are retained.

E. Manufacturer Certificates:  Signed by roofing manufacturer certifying that roofing system complies with requirements specified in "Performance Requirements" Article.

1. Submit evidence of meeting performance requirements.

Coordinate first paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

F. Qualification Data:  For Installer and manufacturer.

G. Product Test Reports:  Based on evaluation of comprehensive tests performed by manufacturer and witnessed by a qualified testing agency, for components of roofing system.

Insert specific model code organization in first paragraph below or revise if report must be from another source.

H. Research/Evaluation Reports:  For components of roofing system.

I. Maintenance Data:  For roofing system to include in maintenance manuals.

Retain paragraph below if desired.  Submittal of sample warranty provides Architect or Owner an opportunity to further verify that warranty coverage meets requirements.

J. Warranties:  Special warranties specified in this Section.

Retain below if manufacturer's final roof inspection report is required.

K. Inspection Report:  Copy of roofing system manufacturer's inspection report of completed roofing installation.

1.6 QUALITY ASSURANCE

FMG is launching a certified roofing installer program.  Add certification requirements to first paragraph below if Project is FMG insured and a certified roofing installer is required.

A. Installer Qualifications:  A qualified firm that is approved, authorized, or licensed by roofing system manufacturer to install manufacturer's product and that is eligible to receive manufacturer's warranty.

B. Manufacturer Qualifications:  A qualified manufacturer that has [UL listing] [FMG approval] for roofing system identical to that used for this Project.

Retain paragraph below if Contractor selects testing agency.

C. Testing Agency Qualifications:  An independent testing agency with the experience and capability to conduct the testing indicated, as documented according to ASTM E 548.

Retain first paragraph below if required to meet provisions of special manufacturer's warranty.  Consult manufacturer's literature for requirements because they vary.

D. Source Limitations:  Obtain components for roofing system [from] [or] [approved by] roofing system manufacturer.

E. Fire-Test-Response Characteristics:  Provide roofing materials with the fire-test-response characteristics indicated as determined by testing identical products per test method below by UL, FMG, or another testing and inspecting agency acceptable to authorities having jurisdiction.  Materials shall be identified with appropriate markings of applicable testing and inspecting agency.

Retain one of three options in subparagraph below based on fire classification of roof assembly and roof covering.  Delete subparagraph if exterior fire-test exposure is included in FMG class designation in "Performance Requirements" Article above.

1. Exterior Fire-Test Exposure:  Class  [A] [B] [C]; ASTM E 108, for application and roof slopes indicated.

Delete subparagraph below if fire-resistance rating of roof assembly is not applicable.  Indicate rating, testing agency, and testing agency's design designation on Drawings.

2. Fire-Resistance Ratings:  ASTM E 119, for fire-resistance-rated roof assemblies of which roofing system is a part.

Consider retaining paragraph below if roofing installation is large and complicated.  A preliminary roofing conference would precede a preinstallation conference and focus on roof deck construction and planning activities of roofing Installer.

F. Preliminary Roofing Conference:  Before starting roof deck construction, conduct conference at Project site.  Comply with requirements for preinstallation conferences in Division 1 Section "Project Management and Coordination."  Review methods and procedures related to roof deck construction and roofing system including, but not limited to, the following:

Delete subparagraphs below not required.  If retaining, revise to include Project-specific requirements.  Insert additional requirements to suit Project.

1. Meet with Owner, Architect, Owner's insurer if applicable, testing and inspecting agency representative, roofing Installer, roofing system manufacturer's representative, deck Installer, and installers whose work interfaces with or affects roofing including installers of roof accessories and roof-mounted equipment.

2. Review methods and procedures related to roofing installation, including manufacturer's written instructions.

3. Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

4. Examine deck substrate conditions and finishes for compliance with requirements, including flatness and fastening.

5. Review structural loading limitations of roof deck during and after roofing.

6. Review base flashings, special roofing details, roof drainage, roof penetrations, equipment curbs, and condition of other construction that will affect roofing system.

7. Review governing regulations and requirements for insurance and certificates if applicable.

8. Review temporary protection requirements for roofing system during and after installation.

9. Review roof observation and repair procedures after roofing installation.

Preinstallation conference below is recommended with or without preliminary roofing conference above.

G. Preinstallation Conference:  Conduct conference at Project site.  Comply with requirements in Division 1 Section "Project Management and Coordination."  Review methods and procedures related to roofing system including, but not limited to, the following:

Delete subparagraphs below not required.  If retaining, revise to include Project-specific requirements.  Insert additional requirements to suit Project.

1. Meet with Owner, Architect, Owner's insurer if applicable, testing and inspecting agency representative, roofing Installer, roofing system manufacturer's representative, deck Installer, and installers whose work interfaces with or affects roofing including installers of roof accessories and roof-mounted equipment.

2. Review methods and procedures related to roofing installation, including manufacturer's written instructions.

3. Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

4. Examine deck substrate conditions and finishes for compliance with requirements, including flatness and fastening.

5. Review structural loading limitations of roof deck during and after roofing.

6. Review base flashings, special roofing details, roof drainage, roof penetrations, equipment curbs, and condition of other construction that will affect roofing system.

7. Review governing regulations and requirements for insurance and certificates if applicable.

8. Review temporary protection requirements for roofing system during and after installation.

9. Review roof observation and repair procedures after roofing installation.

1.7 DELIVERY, STORAGE, AND HANDLING

A. Deliver roofing materials to Project site in original containers with seals unbroken and labeled with manufacturer's name, product brand name and type, date of manufacture, and directions for storage.

B. Store liquid materials in their original undamaged containers in a clean, dry, protected location and within the temperature range required by roofing system manufacturer.  Protect stored liquid material from direct sunlight.

1. Discard and legally dispose of liquid material that cannot be applied within its stated shelf life.

C. Protect roof insulation materials from physical damage and from deterioration by sunlight, moisture, soiling, and other sources.  Store in a dry location.  Comply with insulation manufacturer's written instructions for handling, storing, and protecting during installation.

D. Handle and store roofing materials and place equipment in a manner to avoid permanent deflection of deck.

1.8 PROJECT CONDITIONS

A. Weather Limitations:  Proceed with installation only when existing and forecasted weather conditions permit roofing system to be installed according to manufacturer's written instructions and warranty requirements.

1.9 WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this Article are not less than remedies available to Owner under prevailing local laws.  Coordinate with Division 1 Section "Product Requirements."

Retain paragraph below if manufacturer's labor-and-materials warranty, covering roofing system, is required.  Verify coverage offered by manufacturers because roof insulation, fasteners, and other roofing components may be excluded unless part of a roofing membrane manufacturer's roofing system warranty.  If adding special provisions, retitle paragraph "Special Roofing Manufacturer's Warranty."  Verify warranty availability and coordinate choice of manufacturers in Part 2 accordingly.

A. Special Warranty:  Manufacturer's standard form, without monetary limitation, in which manufacturer agrees to repair or replace components of roofing system that fail in materials or workmanship within specified warranty period.  Failure includes roof leaks.

Retain options in subparagraph below based on those used on Project.  Verify availability of manufacturer's total-system warranty and components included.

1. Special warranty includes roofing membrane, base flashings, [roofing membrane accessories] [roof insulation] [fasteners] [cover boards] [substrate board] [vapor retarder] [roof pavers] [walkway products] and other components of roofing system.

Revise warranty to period required and verify availability; 10- and 15-year periods predominate.  Standard manufacturers' warranties begin on completion of roofing system.  AIA Document A201 establishes that the period begins with Substantial Completion.

2. Warranty Period:  [10] [15] [20] years from date of Substantial Completion.

Usually delete below if retaining manufacturer's warranty above.  Manufacturer's labor-and-materials warranty typically binds Installer for the first two or three years.  If retaining special Project warranty below, use or modify sample roofing Installer's warranty form at end of this Section.  Alternately, insert copy of local roofing contractor association's warranty form or use another form as advised by Owner's counsel.  Revise below to reflect scope of special Project warranty.

B. Special Project Warranty:  Submit roofing Installer's warranty, on warranty form at end of this Section, signed by Installer, covering Work of this Section, including all components of roofing system such as roofing membrane, base flashing, roof insulation, fasteners, cover boards, substrate boards, vapor retarders, roof pavers, and walkway products, for the following warranty period:

1. Warranty Period:  [Two] <Insert number> years from date of Substantial Completion.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations in Division 7 Section "Modified Bituminous Membrane Roofing" for cautions about naming manufacturers and products.

A. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Retain above for nonproprietary or below for semiproprietary specification.  Refer to Division 1 Section "Product Requirements."

B. Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

1. APP-Modified Bituminous Membrane Roofing:

a. American Lubricants Co., Inc.

b. Bitec Inc.

c. CertainTeed Corporation.

d. Dibiten USA.

e. Ecology Roof Systems.

f. Firestone Building Products Company.

g. GAF Materials Corporation.

h. Garland Co., Inc. (The).

i. Hickman, W. P. Systems Inc.

j. Honeywell Commercial Roofing Systems.

k. ICA, Inc.

l. IKO Industries.

m. Johns Manville International, Inc.

n. Koppers Industries, Inc.

o. Malarkey Roofing Company.

p. Performance Roof Systems, Inc.

q. Polyglass USA, Inc.

r. Texas Refinery Corporation.

s. U.S. Intec, Inc.

t. <Insert manufacturer's name.>

Edit remainder of this Article with other Part 2 articles in which manufacturers and products, or manufacturers only, are named.  See Division 1 Section "Product Requirements" for an explanation of the terms "Available Products," "Products," "Available Manufacturers," and "Manufacturers" and the effect these terms have on "Comparable Product" and "Product Substitution" requirements.

C. In other Part 2 articles where titles below introduce lists, the following requirements apply for product selection:

1. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the products specified.

2. Products:  Subject to compliance with requirements, provide one of the products specified.

3. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the manufacturers specified.

4. Manufacturers:  Subject to compliance with requirements, provide products by the manufacturers specified.

2.2 APP-MODIFIED ASPHALT-SHEET MATERIALS

Retain paragraph below if using smooth-surfaced modified asphalt sheet as first ply, or base ply, of two-ply modified bituminous roofing membrane.  Two-ply composite modified bituminous roofing membranes are offered by several manufacturers.  Select option from ASTM product standards below.

A. Roofing Membrane Sheet:  [ASTM D 6222, Grade S, Type I or II, polyester-reinforced] [ASTM D 6223, Grade S, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; smooth surfaced; suitable for application method specified.

Retain paragraph below for smooth-surfaced roofing membrane cap sheet to be coated with roof coating.  Select option from ASTM product standards below.

B. Roofing Membrane Cap Sheet:  [ASTM D 6222, Grade S, Type I or II, polyester-reinforced] [ASTM D 6223, Grade S, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; smooth surfaced; suitable for application method specified.

Retain paragraph below for granule-surfaced roofing membrane cap sheet.  Select option from ASTM product standards below.

C. Roofing Membrane Cap Sheet:  [ASTM D 6222, Grade G, Type I or II, polyester-reinforced] [ASTM D 6223, Grade G, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; granular surfaced; suitable for application method specified, and as follows:

Select from options in subparagraphs below for granule material and color.

1. Granule Material:  Mineral [ceramic coated] [slate].

2. Granule Color:  [White] [Gray] [Tan] <Insert color>.

2.3 BASE-SHEET MATERIALS

Sheathing paper may be required as a slip sheet over wood-plank roof decks, usually under the base sheet.  Delete paragraph below if no wood-plank decks or if not required by manufacturer's specifications.

A. Sheathing Paper:  Red-rosin type, minimum 3 lb/100 sq. ft. (0.16 kg/sq. m).

Select one or two coated base sheets from first four paragraphs below if required by manufacturer's specifications.  Coated base sheets separate roofing membrane from deck, support and cushion roofing membrane from rough or irregular deck, and provide a strong first layer to the roofing membrane.  On nailable roof decks, base sheets may also provide a base layer to adhere rigid insulation.

Retain paragraph below for coated glass-fiber base sheet and select one of two options.  Type II is stronger and heavier than Type I.  Both may be classified by UL as "Class G-2" coated base sheets.

B. Base Sheet:  ASTM D 4601, Type  [I] [II], nonperforated, asphalt-impregnated and -coated, glass-fiber sheet, dusted with fine mineral surfacing on both sides.

Retain paragraph below for SBS-modified, asphalt-coated, glass-fiber base sheet.  Retain ASTM D 4601, Type II option if required.  Some roofing manufacturers offer this coated base sheet as a second adhered base sheet.

C. Base Sheet:  [ASTM D 4601, Type II, ]SBS-modified asphalt-impregnated and -coated sheet, with glass-fiber-reinforcing mat, dusted with fine mineral surfacing on both sides.

SBS-modified bituminous base sheets are available in different weights from different manufacturers.  Many products comfortably exceed minimum weight set by ASTM D 4601, Type II, which is 15.5 lb/100 sq. ft. (0.75 kg/sq. m).  Verify functional requirements with roofing system manufacturers because there are no other product standards.

1. Weight:  [25 lb/100 sq. ft. (1.2 kg/sq. m)] [40 lb/100 sq. ft. (1.95 kg/sq. m)] [50 lb/100 sq. ft. (2.4 kg/sq. m)] [60 lb/100 sq. ft. (2.9 kg/sq. m)] [75 lb/100 sq. ft. (3.7 kg/sq. m)], minimum.

Retain paragraph below for coated glass-fiber venting base sheet.  Venting base sheets may be used over insulating concrete decks or over existing roofing before reroofing.  Review other options with roofing system manufacturer and revise description to suit Project.

D. Base Sheet:  ASTM D 4897, Type II, venting, nonperforated, heavyweight, asphalt-impregnated and -coated, glass-fiber base sheet with coarse granular surfacing or embossed venting channels on bottom surface.

Retain paragraph below for coated organic base sheet.

E. Base Sheet:  ASTM D 2626, asphalt-saturated and -coated organic felt, dusted with fine mineral surfacing on both sides.

Retain below if using glass-fiber felt as second base sheet set in hot roofing asphalt.  Also retain if using glass-fiber-felt base sheet in lieu of coated base sheet over roof insulation or cover board.

F. Base Sheet:  ASTM D 2178, Type  [IV] [VI], asphalt-impregnated, glass-fiber felt.

2.4 BASE-PLY SHEET MATERIALS

Retain this Article if combining built-up roofing ply sheets with a modified bituminous membrane to produce a hybrid roofing system.  The term "glass-fiber base-ply sheet" is used in this Section to distinguish this part of roofing system from a conventional base sheet and from the base ply of a two-ply, APP-modified bituminous roofing membranes.

A. Glass-Fiber Base-Ply Sheet:  ASTM D 2178, Type  [IV] [VI], asphalt-impregnated, glass-fiber felt.

2.5 BASE FLASHING SHEET MATERIALS

Select backer sheet from first three paragraphs below if required behind exposed flashing sheet.  Coordinate selection with warranty duration.

Retain one of two paragraphs below if coated backer sheet to be mechanically fastened is required over wood sheathed parapet.  Although coated glass-fiber backer sheet is typical, coated organic backer sheet in second paragraph is also offered by some manufacturers.

A. Backer Sheet:  ASTM D 4601, Type  [I] [II], asphalt-impregnated and -coated, glass-fiber sheet, dusted with fine mineral surfacing on both sides.

B. Backer Sheet:  ASTM D 2626 asphalt-saturated and -coated organic felt, dusted with fine mineral surfacing on both sides.

Select backer sheet, if required, from paragraph below for first ply of a two-ply flashing membrane.  Select option from ASTM product standards below.

C. Backer Sheet:  [ASTM D 6222, Grade S, Type I or II, polyester-reinforced] [ASTM D 6223, Grade S, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; smooth surfaced; suitable for application method specified.

Select paragraph below for smooth-surfaced flashing sheet.  Select option from ASTM product standards below.

D. Flashing Sheet:  [ASTM D 6222, Grade S, Type I or II, polyester-reinforced] [ASTM D 6223, Grade S, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; smooth surfaced; suitable for application method specified.

Retain paragraph below for granule-surfaced flashing sheet.  Select option from ASTM product standards below.

E. Flashing Sheet:  [ASTM D 6222, Grade G, Type I or II, polyester-reinforced] [ASTM D 6223, Grade G, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; granular surfaced; suitable for application method specified, and as follows:

Select color from options in subparagraph below.

1. Granule Color:  [White] [Gray] [Tan] <Insert color>.

Retain below if glass-fiber fabric is required at upper flashing terminations.

F. Glass-Fiber Fabric:  Woven glass-fiber cloth, treated with asphalt, complying with ASTM D 1668, Type I.

2.6 AUXILIARY ROOFING MEMBRANE MATERIALS

A. General:  Auxiliary materials recommended by roofing system manufacturer for intended use and compatible with roofing membrane.

Retain paragraph below if priming concrete roof deck.

B. Asphalt Primer:  ASTM D 41.

Retain one of three options in paragraph below for traditional roofing asphalt used with base sheets or glass-fiber base-ply sheets.  Roofing asphalt is not used to adhere APP-modified bituminous roofing membranes or base flashings.  See roofing manufacturer's written instructions for requirements.  Although "steep" asphalt, Type III, is used, "extra steep" asphalt, Type IV, predominates.

C. Roofing Asphalt:  ASTM D 312, Type  [III] [IV] [III or IV as recommended by roofing system manufacturer for application] <Insert type>.

Retain paragraph below for SEBS-modified roofing asphalt, offered by some roofing system manufacturers for use with base sheets or glass-fiber base-ply sheets.

D. Roofing Asphalt:  ASTM D 6152, SEBS modified.

Retain paragraph below if adhering roofing membrane or base flashing in cold-applied adhesives.

E. Cold-Applied Adhesive:  Roofing system manufacturer's standard asphalt-based, one- or two-part, asbestos-free, cold-applied adhesive specially formulated for compatibility and use with [roofing membrane] [and] [base flashings].

Retain paragraph below if asphalt roofing cement is used to adhere flashings or integral metal sheet flashings.  Revise material if unacceptable to roofing system manufacturer.

F. Asphalt Roofing Cement:  ASTM D 4586, asbestos free, of consistency required by roofing system manufacturer for application.

Retain first paragraph below if sealant is needed for moving joints in sheet metal accessories or for certain locations where asphalt roofing cement may be inadequate or undesirable.

G. Mastic Sealant:  Polyisobutylene, plain or modified bitumen, nonhardening, nonmigrating, nonskinning, and nondrying.

H. Fasteners:  Factory-coated steel fasteners and metal or plastic plates meeting corrosion-resistance provisions in FMG 4470, designed for fastening roofing membrane components to substrate, tested by manufacturer for required pullout strength, and acceptable to roofing system manufacturer.

I. Metal Flashing Sheet:  Metal flashing sheet is specified in Division 7 Section "Sheet Metal Flashing and Trim."

Retain paragraph below if field-applied granules are required for incidental repairs.  Select option for type of mineral granule.

J. Roofing Granules:  [Ceramic-coated] [Slate] roofing granules, No. 11 screen size with 100 percent passing No. 8 (2.36-mm) sieve and 98 percent of mass retained on No. 40 (0.425-mm) sieve, color to match roofing membrane.

Retain first paragraph below if separator sheet is required over roofing membrane on protected membrane roofing.

K. Separator Sheet:  Polyethylene sheet, 4 mils (0.1 mm) thick, minimum.

L. Miscellaneous Accessories:  Provide miscellaneous accessories recommended by roofing system manufacturer.

2.7 SUBSTRATE BOARDS

Select one of three substrate boards below if required or delete this Article.  Substrate boards may serve as model-building-code-required thermal barriers separating foam insulation from steel or wood deck.  They may also be used over steel deck as part of a fire-resistance-rated roofing system or to provide a smooth substrate for a vapor retarder or temporary roofing.

A. Substrate Board:  ASTM C 36, Type X gypsum wall board, 5/8 inch (16 mm) thick.

B. Substrate Board:  ASTM C 1177/C 1177M, glass-mat, water-resistant gypsum substrate, [1/4 inch (6 mm)] [1/2 inch (13 mm)] [Type X, 5/8 inch (16 mm)] thick.

1. Product:  Subject to compliance with requirements, provide "Dens-Deck" by Georgia-Pacific Corporation.

C. Substrate Board:  ASTM C 728, perlite board, [3/4 inch (19 mm)] [1 inch (25 mm)] thick, seal coated.

Retain below with substrate board selected from paragraphs above.

D. Fasteners:  Factory-coated steel fasteners and metal or plastic plates meeting corrosion-resistance provisions in FMG 4470, designed for fastening substrate panel to roof deck.

2.8 VAPOR RETARDER

Delete this Article if vapor retarders are not required.  Review compatibility of vapor retarder with other roofing system materials.  A substrate board or layer of insulation will be needed because vapor retarders cannot be placed directly over a steel deck.  Retitle Article "Air Retarder" or "Vapor/Air Retarder" depending on function of retarder.

A. Polyethylene-Sheet Vapor Retarder:  ASTM D 4397, 6 mils (0.15 mm) thick, minimum, with maximum permeance rating of 0.13 perm (7.5 ng/Pa x s x sq. m).

Retain one of two subparagraphs below with paragraph above.

1. Tape:  Pressure-sensitive tape of type recommended by vapor-retarder manufacturer for sealing joints and penetrations in vapor retarder.

2. Adhesive:  Manufacturer's standard lap adhesive, FMG approved for vapor-retarder application.

B. Laminated-Sheet Vapor Retarder:  Kraft paper, 2 layers, laminated with asphalt and edge reinforced with woven fiberglass yarn with maximum permeance rating of 0.50 perm (29 ng/Pa x s x sq. m)[ and manufacturer's standard adhesive].

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Fortifiber Corporation; Pyro-Kure 600.

b. GAF Materials Corporation; Permate Vapor Retarder.

c. <Insert manufacturer's name; product.>

Retain one of first two paragraphs and associated subparagraphs below for self-adhering vapor retarder.  Retain first if rubberized asphalt adhesive is required and second if butyl rubber adhesive is required.  Butyl rubber adhesive might be used in hot desert or high-altitude climates.

C. Self-Adhering Sheet Vapor Retarder:  40-mil- (1.0-mm-) thick, polyethylene film laminated to layer of rubberized asphalt adhesive; maximum permeance rating of 0.1 perm (6 ng/Pa x s x sq. m); cold-applied, with slip-resisting surface and release paper backing.  Provide primer when recommended by vapor-retarder manufacturer.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Carlisle Coatings & Waterproofing, Div. of Carlisle Companies Inc.; Dri-Start "A."

b. Grace, W. R. & Co.--Conn.; Grace Ice and Water Shield.

c. <Insert manufacturer's name; product.>

D. Self-Adhering Sheet Vapor Retarder:  30- to 40-mil- (0.76- to 1.0-mm-) thick, polyethylene film laminated to layer of butyl rubber adhesive; maximum permeance rating of 0.1 perm (6 ng/Pa x s x sq. m); cold-applied, with slip-resisting surface and release paper backing.  Provide primer when recommended by vapor-retarder manufacturer.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article if multiple products are specified.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Carlisle Coatings & Waterproofing, Div. of Carlisle Companies Inc.; Dri-Start "HR."

b. Grace, W. R. & Co.--Conn.; Vycor Ultra.

c. <Insert manufacturer's name; product.>

E. Glass-Fiber Felts:  ASTM D 2178, Type IV, asphalt-impregnated, glass-fiber felt.

2.9 ROOF INSULATION

Delete from this Article insulation materials not required.  If retaining more than one insulation material, show location of each on Drawings or indicate where each layer is used in roofing system.  If allowing Contractor to select from more than one insulation material, limit options to insulations that will meet Project requirements and limitations.  Coordinate insulation selection and thicknesses indicated on Drawings with adjoining construction as well as HVAC design and energy program.

Roofing system manufacturers may require use of their own insulations or limit approvals to some insulation manufacturers.  Correlate lists of insulation manufacturers in subparagraphs below with insulation manufacturers approved by roofing system manufacturers, or delete lists altogether for total-system warranties.

A. General:  Provide preformed roof insulation boards that comply with requirements and referenced standards, selected from manufacturer's standard sizes and of thicknesses indicated.

B. Extruded-Polystyrene Board Insulation:  ASTM C 578, Type  [IV, 1.6-lb/cu. ft. (26-kg/cu. m)] [X, 1.3-lb/cu. ft. (21-kg/cu. m)] minimum density, square edged.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. DiversiFoam Products.

b. Dow Chemical Company.

c. Owens Corning.

d. Tenneco Building Products.

e. <Insert manufacturer's name.>

Retain paragraph and subparagraphs below for extruded-polystyrene board insulation installed above the membrane of a protected membrane roofing system.  First option below corresponds to DiversiFoam's "Certifoam 40 Drainage Board," Dow's "Styrofoam Roofmate," Owens Corning's "Foamular 404," and Tenneco's "Amofoam-DC."  Second option corresponds to DiversiFoam's "Certifoam Plaza Deck," Dow's "Styrofoam Plazamate," and Owens Corning's "Foamular 604."  Usually retain Type VI; limit Type VII to roofs with heavy pedestrian traffic.

C. Extruded-Polystyrene Board Insulation:  ASTM C 578, [Type VI, 1.8 lb/cu. ft. (29 kg/cu. m)] [Type VII, 2.2 lb/cu. ft. (35 kg/cu. m)] with 2 or 4 edges rabbeted.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. DiversiFoam Products.

b. Dow Chemical Company.

c. Owens Corning.

d. Tenneco Building Products.

e. <Insert manufacturer's name.>

Retain paragraph and subparagraph below for mortar-faced, extruded-polystyrene board insulation installed above the membrane of a protected membrane roofing system.  First option below describes "Lightguard" and second, "Heavyguard" from T. Clear Corporation.

D. Mortar-Faced, Extruded-Polystyrene Board Insulation:  ASTM C 578, Type VI, 1.8-lb/cu. ft. (29-kg/cu. m) minimum density, with tongue-and-groove edges on long dimension, and latex-modified cement mortar topping, [3/8 inch (9 mm) thick, 4 lb/sq. ft. (19.5 kg/sq. m)] [15/16 inch (23 mm) thick, 11 lb/sq. ft. (53.7 kg/sq. m)].

1. Product:  Subject to compliance with requirements, provide "[Lightguard] [Heavyguard]" by T. Clear Corporation.

Retain paragraph and subparagraphs below for unfaced molded-polystyrene board insulation.  Select density of insulation from options in paragraph.  Higher-density insulation offers improved compressive resistance, better ability to span steel deck flutes, and more rigid substrate.  However, costs increase as density increases.

E. Molded-Polystyrene Board Insulation:  ASTM C 578 Type  [II, 1.35-lb/cu. ft. (22-kg/cu. m)] [VIII, 1.15-lb/cu. ft. (18-kg/cu. m)]   [IX, 1.8-lb/cu. ft. (29-kg/cu. m)] minimum density.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Manufacturers with a third-party certification program satisfying model building code mandatory requirements for foam plastics[ and that produce FMG-approved molded polystyrene].

b. <Insert manufacturer's name.>

Retain paragraph and subparagraphs below for composite molded-polystyrene board insulation.

F. Composite Molded-Polystyrene Board Insulation:  ASTM C 578 Type  [II, 1.35-lb/cu. ft. (22-kg/cu. m)] [VIII, 1.15-lb/cu. ft. (18-kg/cu. m)]   [IX, 1.8-lb/cu. ft. (29-kg/cu. m)] minimum density, with factory-applied facings, as follows:

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Manufacturers with a third-party certification program satisfying model building code mandatory requirements for foam plastics[ and that produce FMG-approved molded polystyrene].

b. <Insert manufacturer's name.>

Select one of two "Facer" subparagraphs below, or revise to another board facer if required.  An example of the first product is "Perform 2" by AFM Corp., and of the second, "R-Control SpecLam" by AFM Corp.  If a field-installed cover board is required, see "Insulation Accessories" Article for options.

2. Facer:  ASTM C 208, Type II, Grade 1, cellulosic-fiber insulation board, asphalt coated, 1/2 inch (13 mm) thick.

3. Facer:  DOC PS 2, Exposure 1, oriented strand board, 7/16 inch (11 mm) thick.

Retain paragraph and subparagraphs below for polyisocyanurate board insulation with aluminum foil facers or felt or glass-fiber mat facers.

G. Polyisocyanurate Board Insulation:  ASTM C 1289, Type  [I, Class 1 aluminum foil] [II, felt or glass-fiber mat] facer on both major surfaces.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Apache Products Company.

b. Atlas Roofing Corporation.

c. Celotex Corporation.

d. Firestone Building Products Company.

e. GAF Materials Corporation.

f. Honeywell Commercial Roofing Systems.

g. Hunter Panels, LLC.

h. Johns Manville International, Inc.

i. Koppers Industries.

j. Performance Roof Systems, Inc.

k. RMAX.

l. <Insert manufacturer's name.>

Retain paragraph and subparagraphs below for composite polyisocyanurate board insulation faced with insulation board on one side and felt or glass-fiber mat facer on the other.  Revise to include other facer types not yet recognized in ASTM C 1289 if applicable.

H. Composite Polyisocyanurate Board Insulation:  ASTM C 1289, faced with insulation board on one major surface, as indicated below by type, and felt or glass-fiber mat facer on the other.

Coordinate first subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Apache Products Company.

b. Atlas Roofing Corporation.

c. Celotex Corporation.

d. Firestone Building Products Company.

e. GAF Materials Corporation.

f. Honeywell Commercial Roofing Systems.

g. Hunter Panels, LLC.

h. Johns Manville International, Inc.

i. Koppers Industries.

j. RMAX.

k. <Insert manufacturer's name.>

2. Type III (perlite-insulation-board facer), [1/2 inch (13 mm)] [3/4 inch (19 mm)] thick.

3. Type IV (cellulosic-fiber-insulation-board facer), Grade 1, 1/2 inch (13 mm) thick.

Retain paragraph and subparagraphs below for perlite board insulation.

I. Perlite Board Insulation:  ASTM C 728; composed of expanded perlite, cellulosic fibers, binders, and waterproofing agents with top surface seal-coated.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Celotex Corporation.

b. GAF Materials Corporation.

c. Honeywell Commercial Roofing Systems.

d. Johns Manville International, Inc.

e. Koppers Industries.

f. <Insert manufacturer's name.>

Retain paragraph and subparagraphs below for cellulosic-fiber board insulation.

J. Cellulosic-Fiber Board Insulation:  ASTM C 208, Type II, Grade 1, fibrous-felted wood fiber or other cellulosic-fiber and water-resistant binders, asphalt impregnated, chemically treated for deterioration.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Celotex Corporation.

b. Firestone Building Products Company.

c. GAF Materials Corporation.

d. Georgia-Pacific Corporation.

e. Homasote Company (The).

f. Honeywell Commercial Roofing Systems.

g. Huebert Fiberboard Co.

h. Koppers Industries.

i. Masonite Corp.

j. Temple - Inland Inc.

k. <Insert manufacturer's name.>

K. Glass-Fiber-Board Insulation:  ASTM C 726, combining glass fibers with thermosetting resin binders, faced on one side with asphalt-coated fiberglass scrim and kraft paper.

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Honeywell Commercial Roofing Systems.

b. Johns Manville International, Inc.

c. <Insert manufacturer's name.>

Cellular-glass board insulation dimensions are 24 by 48 inches (600 by 1219 mm).

L. Cellular-Glass Board Insulation:  ASTM C 552, Type IV, faced on both sides with manufacturer's standard kraft-paper sheets.

1. Product:  Subject to compliance with requirements, provide "Foamglas" by Pittsburgh Corning Corporation.

Retain paragraph below if tapered insulation is required.  Most of the commonly used insulations are available in tapered form; verify with manufacturers.  With some exceptions, codes require roof slopes to be no less than 1/4 inch per 12 inches (1:48).  Insulation is manufactured with tapers ranging from 1/8 inch per 12 inches (1:96) to 1/2 inch per 12 inches (1:24).

M. Tapered Insulation:  Provide factory-tapered insulation boards fabricated to slope of [1/4 inch per 12 inches (1:48)] <Insert slope>, unless otherwise indicated.

Retain below with or without tapered insulation above; delete if not required.

N. Provide preformed saddles, crickets, tapered edge strips, and other insulation shapes where indicated for sloping to drain.  Fabricate to slopes indicated.

2.10 INSULATION ACCESSORIES

A. General:  Roof insulation accessories recommended by insulation manufacturer for intended use and compatible with membrane roofing.

Retain paragraph below if insulation requires mechanical fastening.

B. Fasteners:  Factory-coated steel fasteners and metal or plastic plates meeting corrosion-resistance provisions in FMG 4470, designed for fastening roof insulation to substrate, and acceptable to roofing system manufacturer.

Retain paragraph below if adhering insulation in cold fluid-applied adhesive.

C. Cold Fluid-Applied Adhesive:  Manufacturer's standard cold fluid-applied adhesive formulated to adhere roof insulation to substrate.

Retain one of two insulation cant strips below; delete both if using wood cants specified in Division 6 Section "Rough Carpentry" or "Miscellaneous Carpentry."

D. Insulation Cant Strips:  ASTM C 728, perlite insulation board.

E. Insulation Cant Strips:  ASTM C 208, Type II, Grade 1, cellulosic-fiber insulation board.

Retain paragraph below if wood nailer strips are required.  Wood nailer strips are used to prevent insulation slippage and to backnail roofing membrane on sloping roof decks.  Revise to add material requirements for wood nailer strips here if preferred.

F. Wood Nailer Strips:  Comply with requirements in Division 6 Section "[Rough Carpentry] [Miscellaneous Carpentry]."

Retain one of three paragraphs below.  Use at roof perimeter if no parapet or vertical wall exists.

G. Tapered Edge Strips:  ASTM C 728, perlite insulation board.

H. Tapered Edge Strips:  ASTM C 208, Type II, Grade 1, cellulosic-fiber insulation board.

I. Tapered Edge Strips:  ASTM C 726, glass-fiber insulation board.

Select one of four cover boards below if required.  Cover or overlay boards are usually needed over noncomposite foam insulation or over existing roofing before installing new roofing.  Revise to add proprietary faced cover boards if required.

J. Cover Board:  ASTM C 208, Type II, Grade 1, cellulosic-fiber insulation board, 1/2 inch (13 mm) thick.

K. Cover Board:  ASTM C 728, perlite insulation board, 3/4 inch (19 mm) thick, with top surface seal-coated.

L. Cover Board:  ASTM C 1177/C 1177M, glass-mat, water-resistant gypsum substrate, [1/4 inch (6 mm)] [1/2 inch (13 mm)] thick.

1. Product:  Subject to compliance with requirements, provided "Dens-Deck" by Georgia-Pacific Corporation.

M. Cover Board:  ASTM C 726, glass-fiber rigid insulation, faced on one side with asphalt-coated fiberglass scrim and kraft paper, 3/4 inch (19 mm) thick.

N. Substrate Joint Tape:  6- or 8-inch- (150- or 200-mm-) wide, coated, glass-fiber joint tape.

Protection mats below, sometimes called "filter fabrics" or "fabric mats," limit aggregate ballast movement and control insulation flotation in protected membrane roofing systems.

O. Protection Mat:  Woven or nonwoven polypropylene, polyolefin, or polyester fabric mat, water permeable and resistant to ultraviolet degradation, type and weight as recommended by roofing system manufacturer for application.

Retain below if T. Clear's proprietary metal securement system is required for mortar-faced board insulation.  If preferred, specify gravel stop or counterflashing in Division 7 Section "Sheet Metal Flashing and Trim" or "Manufactured Roof Specialties," as applicable.

P. Metal Securement System:  Perimeter securement flashing and strapping fabricated from stainless steel, a minimum of 0.031 inch (0.8 mm) thick.  Provide fasteners as recommended by mortar-faced insulation manufacturer.

2.11 COATING MATERIALS

Retain this Article if roof coatings are required over smooth-surfaced, APP-modified bituminous roofing membrane or base flashing.  Coatings protect against ultraviolet exposure and degradation and may be required to achieve fire rating.  Recoating may be required at five- to seven-year intervals depending on severity of exposure.

Asphalt-emulsion coatings in first two paragraphs below may be finish coatings or may be a base coat for an aluminum-pigmented finish coating.  ASTM D 1227 applies to asphalt emulsions for use as protective coatings over roofing with minimum roof slope of 1/2 inch per 12 inches (1:24).  Revise description to SBS- or SEBS-modified asphalt emulsions if required.

A. Roof Coating:  ASTM D 1227, Type II Class  [1, mineral-colloid-emulsified, fibered] [2, chemically emulsified, filled or fibered] asphalt emulsion, asbestos free.

B. Roof Coating:  ASTM D 1227, Type III, Class  [1, mineral-colloid-emulsified] [2, chemically emulsified] asphalt emulsion, nonfibered.

Select one of two options in paragraph below to add reflective surface coating to roofing membrane.

C. Roof Coating:  ASTM D 2824, Type  [I, nonfibered] [III, fibered, asbestos-free] aluminum-pigmented asphaltic coating.

Retain paragraph below for acrylic emulsion roof coating.

D. Roof Coating:  ASTM D 6083, acrylic elastomer emulsion coating, formulated for use on bituminous roof surfaces.

Select color from options below.

1. Color:  [White] [Gray] [Buff] <Insert color>.

2.12 WALKWAYS

Retain paragraph below for roof walkway pads.  First option includes composition walkway pads produced by some roofing system manufacturers and independently manufactured products such as Celotex's "Carey-Tred" and W. R. Meadows' "Whitewalk."  Second option includes reconstituted products such as Humane's "Roof-Gard Pads."  Verify requirements with roofing system manufacturers and revise description if required.

A. Walkway Pads:  [Mineral-granule-surfaced, reinforced asphaltic composition] [Polymer-modified, reconstituted solid-rubber, surface-textured], slip-resisting pads, manufactured as a traffic pad for foot traffic and acceptable to roofing system manufacturer, [3/8 inch (10 mm)] [1/2 inch (13 mm)] [3/4 inch (19 mm)] thick, minimum.

1. Pad Size:  <Insert size.>

Select backer strip if required under cap sheet strips, from paragraph below, for first ply of two-ply walkway strip.  Select option from ASTM product standards below.

B. Walkway Backer Strips:  [ASTM D 6222, Grade S, Type I or II, polyester-reinforced] [ASTM D 6223, Grade S, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; smooth surfaced; suitable for application method specified.

Retain paragraph below for roofing membrane cap sheet strips used as walkways.  Select option from ASTM product standards below.

C. Walkway Cap Sheet Strips:  [ASTM D 6222, Grade G, Type I or II, polyester-reinforced] [ASTM D 6223, Grade G, Type I or II, composite polyester- and glass-fiber-reinforced], APP-modified asphalt sheet; granular surfaced; suitable for application method specified, and as follows:

Select from options in subparagraphs below for granule material and color.

1. Granule Material:  Mineral [ceramic coated] [slate].

2. Granule Color:  [White] [Gray] [Tan] <Insert color>.

2.13 PROTECTED MEMBRANE ROOFING AGGREGATE BALLAST

Retain this Article for aggregate-ballasted, protected membrane roofing.

A. Aggregate Ballast:  Provide aggregate ballast that will withstand weather exposure without significant deterioration and will not contribute to membrane degradation, of the following type and size:

Select aggregate type from options in subparagraph below.  If smooth-faced aggregate is preferred, verify availability and cost.  Add requirements for color if necessary.

1. Aggregate Type:  [Smooth, washed, riverbed gravel or other acceptable smooth-faced stone] [or] [crushed gravel or crushed stone].

Retain one or more "Size" subparagraphs below to suit Project.

2. Size:  ASTM D 448, Size 4, ranging from 3/4 to 1-1/2 inches (19 to 38 mm).

3. Size:  ASTM D 448, Size 2, ranging from 1-1/2 to 2-1/2 inches (38 to 63 mm).

Ballast size below is based on recommendations in FMG Loss Prevention Data Sheet 1-29.

4. Size:  ASTM D 448, Size 3, ranging from 1 to 2 inches (25 to 50 mm).

2.14 PROTECTED MEMBRANE ROOFING PAVER BALLAST

Retain this Article if roof-paver ballast is required for protected membrane roofing.  Pavers may be used alone or with aggregate ballast for functional or decorative reasons.

Retain interlocking, lightweight roof pavers in paragraph and subparagraphs below if required.

A. Lightweight Roof Pavers:  Interlocking, lightweight concrete units, specially factory cast for use as roof ballast; grooved back, with four-way drainage capability; beveled, doweled, or otherwise profiled; and as follows:

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Hanover Architectural Products.

b. Rapid Building Systems.

c. Roofblok, Ltd.

d. Westile Roofing Products.

e. <Insert manufacturer's name.>

Coordinate size selection below with minimum paver coverage required, especially at corners, perimeter, penetrations, and above large wall openings.  Paver sizes vary with manufacturer and include 8 by 16, 12 by 12, 12 by 16-1/2, and 12 by 18 inches (200 by 400, 300 by 300, 300 by 420, and 300 by 450 mm).

2. Size:  <Insert actual size(s) of pavers.>

Insert weight of roof paver in subparagraph below.  Dow requires interlocking, lightweight roof pavers weighing at least 11 lb/sq. ft. (53.7 kg/sq. m) to be placed over its insulation and over entire roof.  Verify availability with manufacturers selected.

3. Weight:  <Insert weight or acceptable weight range.>

Select compressive strength from options in subparagraph below.

4. Compressive Strength:  [2500 psi (17 MPa)] [5000 psi (34 MPa)] <Insert strength>, minimum.

Retain one option in subparagraph below.  If retaining first, indicate colors and textures in a separate schedule.

5. Colors and Textures:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Retain heavyweight roof pavers in paragraph and subparagraphs below if required.  Heavyweight roof pavers may be used as ballast as well as walkways for protected membrane roofing.

B. Heavyweight Roof Pavers:  Heavyweight, hydraulically pressed, concrete units, [square edged] [with top edges beveled 3/16 inch (5 mm)], factory cast for use as roof pavers; absorption not greater than 5 percent, ASTM C 140; no breakage and maximum 1 percent mass loss when tested for freeze-thaw resistance, ASTM C 67; and as follows:

Coordinate subparagraph and associated subparagraphs below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Hanover Architectural Products.

b. Rapid Building Systems.

c. Roofblok, Ltd.

d. Sunny Brook Pressed Concrete Co.

e. Wausau Tile, Inc.; Terra-Paving Div.

f. Westile Roofing Products.

g. <Insert manufacturer's name.>

Coordinate size selection below with minimum paver coverage required, especially at corners, perimeter, penetrations, and above large wall openings.  Consider handling of pavers as weight increases.  Other sizes include 12 by 12 and 18 by 18 inches (300 by 300 and 450 by 450 mm).

2. Size:  [24 by 24 inches (600 by 600 mm)] <Insert size>.  Manufacture pavers to dimensional tolerances of plus or minus 1/16 inch (1.6 mm) in length, height, and thickness.

Select weight of roof paver from options in subparagraph below.  ANSI/SPRI RP-4, System 1, all locations, and System 2, field of roof, allow roof pavers weighing 18 lb/sq. ft. (90 kg/sq. m) or more.  System 3 requires roof pavers weighing 22 lb/sq. ft. (110 kg/sq. m) or more.  Verify availability with manufacturers selected.

3. Weight:  [18 lb/sq. ft. (90 kg/sq. m)] [22 lb/sq. ft. (110 kg/sq. m)] <Insert weight>.

Select compressive strength from options in subparagraph below.

4. Compressive Strength:  [7500 psi (52 MPa)] [6500 psi (45 MPa)] <Insert strength>, minimum.

Retain one option in subparagraph below.  If retaining first, indicate colors and textures in a separate schedule.

5. Colors and Textures:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Delete paver supports, which are used to elevate pavers and facilitate drainage, in subparagraphs below if not required.  Retain first subparagraph if paver supports are integrally cast.  Retain second subparagraph if separate pedestal supports, which are used to space, level, and stabilize pavers, are required.  Pedestals may be of fixed height or adjustable for leveling pavers over a sloped substrate.  Besides roof-paver producers, pedestal manufacturers include Envirospec and Tremco.

6. Paver Supports:  Integral corner pedestals.

7. Paver Supports:  Paver manufacturer's standard SBR rubber, high-density polyethylene, or polyurethane paver support assembly, including [fixed-height] [adjustable or stackable] pedestals, shims, and spacer tabs for joint spacing of [1/8 inch (3 mm)] [3/16 inch (5 mm)] [1/8 to 3/16 inch (3 to 5 mm)].

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates, areas, and conditions, with Installer present, for compliance with the following requirements and other conditions affecting performance of roofing system:

1. Verify that roof openings and penetrations are in place and set and braced and that roof drains are securely clamped in place.

Wood cants, blocking, curbs, and nailers are required at edges of roof penetrations, area dividers, and terminations.  Wood nailers are not required on lightweight insulating concrete decks or on noninsulated, nailable decks.

2. Verify that wood cants, blocking, curbs, and nailers are securely anchored to roof deck at penetrations and terminations and that nailers match thicknesses of insulation.

Retain subparagraph below for steel roof deck.

3. Verify that surface plane flatness and fastening of steel roof deck complies with requirements in Division 5 Section "Steel Deck."

Retain or revise first two subparagraphs and associated subparagraph below for concrete roof decks.

4. Verify that concrete curing compounds that will impair adhesion of roofing components to roof deck have been removed.

5. Verify that concrete substrate is visibly dry and free of moisture.  Test for capillary moisture by plastic sheet method according to ASTM D 4263.

Delete subparagraph below if no hot roofing asphalt is required.

a. Test for moisture by pouring 1 pint (0.5 L) of hot roofing asphalt on deck at start of each day's work and at start of each roof area or plane.  Do not proceed with roofing work if test sample foams or can be easily and cleanly stripped after cooling.

Delete first subparagraph below if no wood or plywood decks.

6. Verify that deck is securely fastened with no projecting fasteners and with no adjacent units in excess of 1/16 inch (1.6 mm) out of plane relative to adjoining deck.

7. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. Clean substrate of dust, debris, moisture, and other substances detrimental to roofing installation according to roofing system manufacturer's written instructions.  Remove sharp projections.

B. Prevent materials from entering and clogging roof drains and conductors and from spilling or migrating onto surfaces of other construction.  Remove roof-drain plugs when no work is taking place or when rain is forecast.

Retain paragraph below if priming concrete deck before installing overlying roofing system components in hot roofing asphalt.

C. Prime surface of concrete deck with asphalt primer at a rate of 3/4 gal./100 sq. ft. (0.3 L/sq. m) and allow primer to dry.

Retain below if acoustical roof deck rib insulation, shaped to fit into topside ribs of acoustical roof deck, is installed in this Section.

D. Install acoustical roof deck rib insulation strips, specified in Division 5 Section "Steel Deck," according to acoustical roof deck manufacturer's written instructions.

3.3 SUBSTRATE BOARD INSTALLATION

Delete this Article if not required.

A. Install substrate board with long joints in continuous straight lines, perpendicular to roof slopes with end joints staggered between rows.  Tightly butt substrate boards together.

Retain one of two subparagraphs below if mechanical fastening is required.

1. Fasten substrate board to top flanges of steel deck according to recommendations in FMG's "Approval Guide" for specified Windstorm Resistance Classification.

2. Fasten substrate board to top flanges of steel deck to resist uplift pressure at corners, perimeter, and field of roof according to roofing system manufacturer's written instructions.

3.4 VAPOR-RETARDER INSTALLATION

Delete this Article if not required.  Retain selected vapor-retarder material from paragraphs below.  Retitle Article "Air Barrier" if that is primary function and revise installation requirements if necessary.  Vapor retarder must be fully supported by substrate.  Steel deck requires substrate board.

A. Loosely lay polyethylene-sheet vapor retarder in a single layer over area to receive vapor retarder, side and end lapping each sheet a minimum of 2 inches (50 mm) and 6 inches (150 mm), respectively.

Select one of two options in subparagraph below.

1. Seal side and end laps with [tape] [adhesive].

B. Install laminated-sheet vapor retarder in a single layer over area to receive vapor retarder, side and end lapping each sheet a minimum of 2 inches (50 mm) and 6 inches (150 mm), respectively.  Bond vapor retarder to deck as follows:

Select one of two subparagraphs below.

1. Apply adhesive at rate recommended by vapor-retarder manufacturer.  Seal laps with adhesive.

2. Apply ribbons of hot roofing asphalt at spacing, temperature, and rate recommended by vapor-retarder manufacturer.  Seal laps with hot roofing asphalt.

C. Self-Adhering Sheet Vapor Retarder:  Prime substrate if required by manufacturer.  Install self-adhering sheet vapor retarder over area to receive vapor retarder, side and end lapping each sheet a minimum of 3-1/2 inches (90 mm) and 6 inches (150 mm), respectively.  Seal laps by rolling.

D. Install 2 glass-fiber felt plies lapping each sheet 19 inches (483 mm) over preceding sheet.  Embed each sheet in a solid mopping of hot roofing asphalt.  Glaze-coat completed surface with hot roofing asphalt.  Apply hot roofing asphalt at a rate of 20 lb/100 sq. ft. (1 kg/sq. m), plus or minus 25 percent.

Always retain below.  To function effectively, vapor retarders or air barriers must prevent air movement into roofing system.

E. Completely seal vapor retarder at terminations, obstructions, and penetrations to prevent air movement into roofing system.

3.5 INSULATION INSTALLATION

A. Comply with roofing system manufacturer's written instructions for installing roof insulation.

Retain paragraph below if mechanically fastening base sheet to substrate before adhering first layer of insulation.

B. Install one lapped base sheet course and mechanically fasten to substrate according to roofing system manufacturer's written instructions.

Roofing system manufacturers require nailer strips for insulation-covered roof decks with slopes greater than 1 inch per 12 inches (1:12).  Verify roofing system manufacturer's backnailing requirements for reducing nailer-strip spacing as roof slope increases.  Absent manufacturer's written instructions, NRCA recommends spacing nailers approximately 16 feet (4.88 m) apart for slopes up to 3 inches per 12 inches (3:12) and 48 inches (1220 mm) apart for greater slopes.  Delete nailer strips on lightweight insulating concrete decks or other noninsulated nailable decks.

C. Nailer Strips:  Mechanically fasten 4-inch nominal- (89-mm actual-) width wood nailer strips of same thickness as insulation perpendicular to sloped roof deck at the following spacing:

1. [16 feet (4.88 m)] <Insert spacing> apart for roof slopes greater than 1 inch per 12 inches (1:12) but less than 3 inches per 12 inches (3:12).

2. [48 inches (1220 mm)] <Insert spacing> apart for roof slopes greater 3 inches per 12 inches (3:12).

Insulation cant strips may be mechanically fastened or set in hot asphalt depending on substrate and roofing system manufacturer's written instructions.

D. Insulation Cant Strips:  Install and secure preformed 45-degree insulation cant strips at junctures of roofing membrane system with vertical surfaces or angle changes greater than 45 degrees.

Retain first paragraph below if tapered insulation is required.

E. Install tapered insulation under area of roofing to conform to slopes indicated.

F. Install insulation with long joints of insulation in a continuous straight line with end joints staggered between rows, abutting edges and ends between boards.  Fill gaps exceeding 1/4 inch (6 mm) with insulation.

1. Cut and fit insulation within 1/4 inch (6 mm) of nailers, projections, and penetrations.

Revise thickness in first paragraph below to suit Project.  NRCA recommendations for maximum thickness of a single layer vary with insulation material; 1-1/2 inches (38 mm) for perlite and glass fiber, 2 inches (50 mm) for polyisocyanurate and molded and extruded polystyrene, and 3 inches (75 mm) for cellular glass.

G. Install one or more layers of insulation under area of roofing to achieve required thickness.  Where overall insulation thickness is [1-1/2 inches (38 mm)] [2 inches (50 mm)] or greater, install 2 or more layers with joints of each succeeding layer staggered from joints of previous layer a minimum of 6 inches (150 mm) in each direction.

H. Trim surface of insulation where necessary at roof drains so completed surface is flush and does not restrict flow of water.

I. Install tapered edge strips at perimeter edges of roof that do not terminate at vertical surfaces.

Retain paragraph below if adhering each layer of insulation.

J. Adhered Insulation:  Install each layer of insulation and adhere to substrate as follows:

Retain applicable subparagraph below.

1. Set each layer of insulation in a solid mopping of hot roofing asphalt.

2. Set each layer of insulation in a cold fluid-applied adhesive.

Retain paragraph below if mechanically fastening insulation layers.

K. Mechanically Fastened Insulation:  Install each layer of insulation and secure to deck using mechanical fasteners specifically designed and sized for fastening specified board-type roof insulation to deck type.

Retain first subparagraph below when Project is FMG insured or FMG requirements are proposed as a performance standard.  Retain second subparagraph if number of fasteners will be based on ASCE 7's uplift pressure.  Coordinate with Part 1 "Performance Requirements" Article.  Fastener numbers will increase at corners and perimeter over number required for field of roof.

1. Fasten insulation according to requirements in FMG's "Approval Guide" for specified Windstorm Resistance Classification.

2. Fasten insulation to resist uplift pressure at corners, perimeter, and field of roof.

Retain paragraph and subparagraphs below if mechanically fastening the first layer of insulation and adhering the remaining layers.  This is the most common application method.

L. Mechanically Fastened and Adhered Insulation:  Install each layer of insulation and secure first layer of insulation to deck using mechanical fasteners specifically designed and sized for fastening specified board-type roof insulation to deck type.

Retain first subparagraph below when Project is FMG insured or FMG requirements are proposed as a performance standard.  Retain second subparagraph if fastening is calculated from ASCE 7's uplift pressure.  Coordinate with Part 1 "Performance Requirements" Article.  Fastener numbers will increase at corners and perimeter over number required for field of roof.

1. Fasten first layer of insulation according to requirements in FMG's "Approval Guide" for specified Windstorm Resistance Classification.

2. Fasten first layer of insulation to resist uplift pressure at corners, perimeter, and field of roof.

Select one of two subparagraphs below.

3. Install subsequent layers of insulation in a solid mopping of hot roofing asphalt.

4. Install subsequent layers of insulation in a cold fluid-applied adhesive.

Retain below if cover boards will be field installed over roof insulation and immediately below roofing membrane.  Joint taping protects molded- or extruded-polystyrene insulation against damage from hot roofing asphalt and minimizes offsets at joints between adjacent cover boards.

M. Install cover boards over insulation with long joints in continuous straight lines with end joints staggered between rows.  Stagger joints from joints in insulation below a minimum of 6 inches (150 mm) in each direction.  Loosely butt cover boards together and fasten to roof deck.  Tape joints if required by roofing system manufacturer.

1. Fasten according to requirements in FMG's "Approval Guide" for specified Windstorm Resistance Classification.

2. Fasten to resist uplift pressure at corners, perimeter, and field of roof.

3. Apply hot roofing asphalt to underside and immediately bond cover board to substrate.

3.6 ROOFING MEMBRANE INSTALLATION, GENERAL

Always retain paragraph below.

A. Install roofing membrane system according to roofing system manufacturer's written instructions and applicable recommendations of ARMA/NRCA's "Quality Control Guidelines for the Application of Polymer Modified Bitumen Roofing."

Retain subparagraph below if referencing NRCA's specification-plate classification system.  Retain one selection from first group of options denoting number of APP-modified asphalt sheets.  Retain one selection from second group of options denoting deck types:  "N" for nailable, "I" for insulated, and "C" for concrete or non-nailable deck.  Retain one selection from third group of options denoting adhering method:  "T" for torched and "L" for cold-applied adhesive.  Retain one selection from fourth group of options, if applicable, denoting number of glass-fiber base-ply sheets with or without base sheet.  Retain one selection from fifth group of options denoting surfacing type:  "S" for smooth surfaced, "M" for mineral-granule-surfaced cap sheet, and "P" for protected membrane roofing.  See Editing Instruction No. 2 in the Evaluations in Division 7 Section "Modified Bituminous Membrane Roofing" for more information.

B. Install roofing system MBA[1] [2]-[N] [I] [C]-[T] [L]-G[0 with base sheet] [1] [1 with base sheet] [2] [2 with base sheet]-[S] [M] [P], according to specification-plate classifications in NRCA's "The NRCA Roofing and Waterproofing Manual" and requirements in this Section.

Delete paragraph below if not applicable.

C. Start installation of roofing membrane in presence of roofing system manufacturer's technical personnel.

Retain paragraph and subparagraph below if roof slope exceeds minimum permitted by roofing system manufacturer.  Revise minimum roof slope to suit application.

D. Where roof slope exceeds [1/2 inch per 12 inches (1:24)] [3/4 inch per 12 inches (1:18)] <Insert slope>, install roofing membrane sheets parallel with slope.

Retain first option in subparagraph below for backnailing to nailer strips for insulated and non-nailable decks.  Retain second option for backnailing directly to nailable substrate.

1. Backnail roofing membrane sheets to [nailer strips] [substrate] according to roofing system manufacturer's written instructions.

E. Cooperate with testing and inspecting agencies engaged or required to perform services for installing roofing system.

F. Coordinate installing roofing system so insulation and other components of the roofing membrane system not permanently exposed are not subjected to precipitation or left uncovered at the end of the workday or when rain is forecast.

1. Provide tie-offs at end of each day's work to cover exposed roofing membrane sheets and insulation with a course of coated felt set in roofing cement or hot roofing asphalt with joints and edges sealed.

2. Complete terminations and base flashings and provide temporary seals to prevent water from entering completed sections of roofing system.

3. Remove and discard temporary seals before beginning work on adjoining roofing.

Retain one of first two paragraphs below if using hot roofing asphalt for base sheets, base-ply sheets, and base flashing backer sheets.  APP-modified asphalt roofing sheets are not adhered in hot roofing asphalt.  Retain first for traditional roofing asphalt complying with ASTM D 312; retain second for SEBS-modified roofing asphalt.  Heating and application requirements may differ among roofing system manufacturers.

G. Asphalt Heating:  Do not raise roofing asphalt temperature above equiviscous temperature range more than one hour before time of application.  Do not exceed roofing asphalt manufacturer's recommended temperature limits during roofing asphalt heating.  Do not heat roofing asphalt within 25 deg F (14 deg C) of flash point.  Discard roofing asphalt maintained at a temperature exceeding finished blowing temperature for more than 4 hours.

H. Asphalt Heating:  Heat and apply SEBS-modified roofing asphalt according to roofing system manufacturer's written instructions.

I. Substrate-Joint Penetrations:  Prevent roofing asphalt from penetrating substrate joints, entering building, or damaging roofing system components or adjacent building construction.

3.7 BASE-SHEET INSTALLATION

Retain this Article if base sheet is required.  Retain paragraph below if sheathing paper is required over wood decks by roofing system manufacturer.  Base sheet placed under roof insulation is specified in "Insulation Installation" Article.

A. Loosely lay one course of sheathing paper, lapping edges and ends a minimum of 2 inches (50 mm) and 6 inches (150 mm), respectively.

Retain paragraph and subparagraphs below if base sheet is required as first ply of roofing membrane.

B. Install lapped base sheet course, extending sheet over and terminating beyond cants.  Attach base sheet as follows:

Select appropriate installation method from subparagraphs below.  Usually retain first for nailable substrate and second, third, or fourth for non-nailable or insulated substrates.  Mechanically fasten or spot- or strip-mop vented base sheets because they vent laterally.

1. Mechanically fasten to substrate.

2. Spot- or strip-mop to substrate with hot roofing asphalt.

3. Adhere to substrate in a solid mopping of hot roofing asphalt.

4. Adhere to substrate in a uniform coating of cold-applied adhesive.

Retain paragraph and subparagraphs below if second base sheet is required.

C. Install a second lapped base sheet course, extending sheet over and terminating beyond cants.  Attach base sheet as follows:

Select appropriate installation method from subparagraphs below.  Usually retain first for nailable substrate and second or third for non-nailable or insulated substrates.

1. Mechanically fasten to substrate.

2. Adhere to substrate in a solid mopping of hot roofing asphalt.

3. Adhere to substrate in a uniform coating of cold-applied adhesive.

3.8 BASE-PLY SHEET INSTALLATION

Retain this Article if installing a hybrid roofing system.  Glass-fiber base-ply sheets may be applied directly to non-nailable deck, base sheet, or insulation.  Shingled glass-fiber base-ply sheets form the built-up roofing portion of a hybrid roofing system.  Select number of base-ply sheets from options in paragraph below.

A. Install [two] [three] glass-fiber base-ply sheets according to roofing system manufacturer's written instructions starting at low point of roofing system.  Align glass-fiber base-ply sheets without stretching.  Shingle side laps of glass-fiber base-ply sheets uniformly to ensure required number of glass-fiber base-ply sheets covers substrate at any point.  Shingle in direction to shed water.  Extend glass-fiber base-ply sheets over and terminate beyond cants.

1. Embed each glass-fiber base-ply sheet in a continuous mopping of hot roofing asphalt, to form a uniform membrane without glass-fiber base-ply sheets touching.

3.9 APP-MODIFIED BITUMINOUS MEMBRANE INSTALLATION

Retain first option in paragraph below if modified bituminous portion of roofing membrane is built up with two APP-modified bituminous roofing plies.  Retain cap sheet option alone if a single APP-modified bituminous membrane ply is required.

A. Install modified bituminous roofing membrane [sheet] [and] [cap sheet] according to roofing manufacturer's written instructions, starting at low point of roofing system.  Extend roofing membrane sheets over and terminate beyond cants, installing as follows:

Select one of two subparagraphs below.

1. Adhere to substrate in cold-applied adhesive.

2. Torch apply to substrate.

Subparagraph below may be required depending on type of membrane reinforcement and type of bonding adhesive, or, in colder weather, to minimize creases and fishmouths and to permit sheet to lay flat.  Verify need with manufacturer.  Delete if not applicable.

3. Unroll roofing membrane sheets and allow them to relax for minimum time period required by manufacturer.

B. Laps:  Accurately align roofing membrane sheets, without stretching, and maintain uniform side and end laps.  Stagger end laps.  Completely bond and seal laps, leaving no voids.

1. Repair tears and voids in laps and lapped seams not completely sealed.

Retain subparagraph below for torched or heat-welded laps of granule-finished roofing membrane cap sheet if required.  Granule application to beads is considered temporary.

2. Apply roofing granules to cover exuded bead at laps while bead is hot.

C. Install roofing membrane sheets so side and end laps shed water.

3.10 FLASHING AND STRIPPING INSTALLATION

A. Install base flashing over cant strips and other sloping and vertical surfaces, at roof edges, and at penetrations through roof, and secure to substrates according to roofing system manufacturer's written instructions and as follows:

Smooth surfaces of masonry and concrete walls and parapets usually require priming before applying hot asphalt or cold adhesive.

1. Prime substrates with asphalt primer if required by roofing system manufacturer.

Retain one of three subparagraphs below if a single backer sheet is required behind flashing sheet.  Retain first for backer sheets mechanically fastened to wood-surfaced walls or parapets and second or third for adhered backer sheets.

2. Backer Sheet Application:  Mechanically fasten backer sheet to walls or parapets.[ Adhere backer sheet over roofing membrane at cants in cold-applied adhesive.]

3. Backer Sheet Application:  Install backer sheet and adhere to substrate in a solid mopping of hot roofing asphalt.

4. Backer Sheet Application:  Install backer sheet and adhere to substrate in cold-applied adhesive at rate required by roofing system manufacturer.

Retain one of three subparagraphs below or revise to suit Project.  Usually APP-modified flashing sheets may be applied by any method below.

5. Flashing Sheet Application:  Adhere flashing sheet to substrate in cold-applied adhesive at rate required by roofing system manufacturer.

6. Flashing Sheet Application:  Adhere flashing sheet to substrate in asphalt roofing cement; apply cement at rate required by roofing system manufacturer.

7. Flashing Sheet Application:  Torch apply flashing sheet to substrate.

Revise dimensions in first paragraph below if required.  Verify minimum and maximum height limits with manufacturers if necessary.  NRCA recommends a minimum base-flashing height of 8 inches (200 mm).

B. Extend base flashing up walls or parapets a minimum of 8 inches (200 mm) above roofing membrane and 4 inches (100 mm) onto field of roofing membrane.

C. Mechanically fasten top of base flashing securely at terminations and perimeter of roofing.

Delete subparagraph below if temporarily sealing upper termination of flashings awaiting counterflashing.  Retain option if specifying termination seal.

1. Seal top termination of base flashing[ with a strip of glass-fiber fabric set in asphalt roofing cement].

Revise paragraph below to describe a particular stripping arrangement if required.  Manufacturers offer many variations of stripping-in metal flanges and horizontal legs of metal edgings.  Some roofing manufacturers show metal items set on either base sheet or strip of modified bituminous membrane where water flow is toward, rather than away from, metal item.  Cap or finish sheet extends over metal, minimizing water flow against an exposed lap seam.

D. Install roofing membrane cap-sheet stripping where metal flanges and edgings are set on membrane roofing according to roofing system manufacturer's written instructions.

Delete below if no interior roof drains.  NRCA recommends flashing size below while some roofing manufacturers permit 27-inch- (685-mm-) square units.

E. Roof Drains:  Set [30-by-30-inch (760-by-760-mm)] <Insert size> metal flashing in bed of roofing-manufacturer-approved asphaltic adhesive on completed roofing membrane.  Cover metal flashing with roofing membrane cap-sheet stripping and extend a minimum of [4 inches (100 mm)] [6 inches (150 mm)] beyond edge of metal flashing onto field of roofing membrane.  Clamp roofing membrane, metal flashing, and stripping into roof-drain clamping ring.

1. Install stripping according to roofing system manufacturer's written instructions.

3.11 COATING INSTALLATION

Retain this Article if roof coatings are required.

A. Apply coatings to [roofing membrane] [and] [base flashings] according to manufacturer's written instructions, by spray, roller, or other suitable application method.

3.12 WALKWAY INSTALLATION

Retain this Article if walkways set directly on roofing membrane are required.

Retain paragraph below if required.

A. Walkway Pads:  Install walkway pads in cold-applied adhesive, using units of size indicated or, if not indicated, of manufacturer's standard size according to walkway pad manufacturer's written instructions.

Retain paragraph and subparagraph below if required.  Select option in paragraph if two walkway strip plies are required.

B. Walkway Strips:  Install walkway [backer and ]cap sheet strips over roofing membrane.

Retain applicable option below.

1. Install walkway strips [in cold-applied adhesive] [by torch application].

3.13 PROTECTED MEMBRANE ROOFING INSULATION AND BALLAST INSTALLATION

Retain this Article for protected membrane roofing installations.  NRCA recommends that roof slope be not less than 1/4 inch per 12 inches (1:48) for drainage.

Retain paragraph below if required.

A. Loosely lay separator sheet over cooled roofing membrane, with minimum 2-inch (50-mm) side laps and 4-inch (150-mm) end laps.

Retain paragraph and subparagraphs below for extruded-polystyrene insulation loosely laid over membrane.

B. Insulation:  Loosely lay board insulation units over roofing membrane, with long joints of insulation in a continuous straight line and with end joints staggered between rows.  Abut edges and ends between units.  Install to achieve required insulation thickness over roofing membrane.  Cut and fit to within 3/4 inch (19 mm) of projections and penetrations.

Delete subparagraph below if not required or revise to suit Project.  Revise if one or more insulation layers are topped with final layer of mortar-faced board insulation.

1. Where overall insulation thickness is 2 inches (50 mm) or more, install required thickness in 2 or more layers with joints of each succeeding layer staggered over joints of previous layer a minimum of 6 inches (150 mm) in each direction.

Retain subparagraph below for aggregate ballast.  Protection mat is usually omitted under roof-paver ballast.

2. Install protection mat over insulation, overlapping edges and ends at least 12 inches (300 mm).  Do not lap ends of fabric sheets within 72 inches (1800 mm) of roof perimeter.  Extend fabric 2 to 3 inches (50 to 75 mm) above ballast at perimeter and penetrations.  Apply additional protection mat layer around penetrations to prevent aggregate from getting between penetrations and insulation.  Do not cover drains or restrict water flow to drains.

Retain paragraph and subparagraphs below if using aggregate ballast over protection mat and insulation.

C. Aggregate Ballast:  Apply aggregate ballast uniformly over protection mat at roofing system manufacturer's recommended rate, but not less than the following, spreading with care to minimize possibility of damage to roofing membrane.  Leave roof insulation ballasted at the end of the workday.

Two subparagraphs below are based on ANSI/SPRI RP-4.  First corresponds to System 1, second to System 2.  Delineate dimensions of corners, perimeter, and field of roof on Drawings.  Revise to Dow's recommendations in Dow Technote 508 if required.

1. Ballast Weight:  Size 4 aggregate, 10 lb/sq. ft. (50 kg/sq. m).

2. Ballast Weight:  Size 2 aggregate, 13 lb/sq. ft. (65 kg/sq. m), at corners and perimeter; Size 4 aggregate, 10 lb/sq. ft. (50 kg/sq. m), elsewhere.

Delete both subparagraphs above and retain subparagraph below if FMG recommendations apply.  Insert weight of aggregate for each part of roof, based on recommendations in FMG Loss Prevention Data Sheet 1-29.  Delineate dimensions of corners, perimeter, and field of roof on Drawings, based on FMG requirements.

3. Ballast Weight:  Size 3 aggregate, <Insert weight>, at corners; <Insert weight>, at perimeter; and <Insert weight>, elsewhere.

Retain one of two paragraphs below if roof-paver ballast is required.  Retain first for lightweight roof pavers.  Retain second if combining roof-paver and aggregate ballast based on ANSI/SPRI RP-4, System 3.  Revise to Dow's recommendations in Dow Technote 508 or recommendations of another insulation manufacturer if required.

D. Roof-Paver Ballast:  Install lightweight roof-paver ballast according to manufacturer's written instructions.

E. Roof-Paver and Aggregate Ballast:  Install heavyweight roof pavers according to manufacturer's written instructions, on roof corners and perimeter as defined by ANSI/SPRI RP-4.  Install Size 2 aggregate ballast elsewhere on roofing at a minimum rate of 13 lb/sq. ft. (65 kg/sq. m).

Retain subparagraph below if using separate pedestal assemblies beneath heavyweight roof pavers.

1. Install roof pavers on pedestals according to pedestal manufacturer's written instructions.

F. Roof-Paver Walkways:  Install heavyweight roof pavers according to manufacturer's written instructions.

Retain paragraph and applicable subparagraph below if using mortar-faced extruded insulation over roofing membrane.  Minimum ballast loads below are based on ANSI/SPRI RP-4, System 1 and 2 requirements for protected membrane roofing using mortar-faced extruded insulation.  Revise applicable subparagraph to include T. Clear's ballast requirements if more stringent.  Revise minimum ballast loads or mechanical securement to reflect special or custom roof design if ANSI/SPRI RP-4, System 3 is required.

G. Mortar-Faced Extruded Insulation:  Install mortar-faced extruded insulation loosely laid, according to manufacturer's written instructions, with tongue-and-groove joints nested.  Stagger end joints of adjoining rows and abut insulation.

Retain subparagraph below if ANSI/SPRI RP-4, System 1 design is required.  Heavyweight roof pavers of not less than 22 lb/sq. ft. (110 kg/sq. m) are required.

1. Install heavyweight roof pavers over mortar-faced extruded insulation to a width not less than 24 inches (600 mm) on roof perimeter as defined by ANSI/SPRI RP-4.

Retain subparagraph below if ANSI/SPRI RP-4, System 2 design is required.  Heavyweight roof pavers of not less than 22 lb/sq. ft. (110 kg/sq. m) are required.

2. Install heavyweight roof pavers over mortar-faced extruded insulation on roof corners and perimeter as defined by ANSI/SPRI RP-4.

Retain below and delete both subparagraphs above if perimeter mechanical securement is required.  Revise description of perimeter edge conditions below if requirements differ, depending on whether a parapet wall or a gravel stop is detailed on Drawings.  Coordinate inclusion of gravel stop or counterflashing for parapet with Division 7 Section "Sheet Metal Flashing and Trim" or "Manufactured Roof Specialties," as applicable.

3. Mechanically fasten strapping and perimeter edge securement system over mortar-faced extruded insulation according to manufacturer's written instructions.

3.14 FIELD QUALITY CONTROL

Retain this Article if field inspecting and testing are required.  Revise to suit local practices and requirements of authorities having jurisdiction if applicable.  Quality-control inspections by roofing Contractor are already mandated in "General Installation Requirements" Article in ARMA/NRCA's "Quality Control Guidelines for the Application of Polymer Modified Bitumen Roofing."

A. Testing Agency:  Owner will engage a qualified independent testing and inspecting agency to perform roof tests and inspections and to prepare test reports.

Paragraph and subparagraphs below are based on Appendix 2 of ARMA/NRCA's "Quality Control Guidelines for the Application of Polymer Modified Bitumen Roofing."  ARMA/NRCA recommends continuous visual examination of roofing installation.  Test cuts are intended to evaluate problems observed during quality-assurance inspections.

B. Test Cuts:  Test specimens will be removed to evaluate problems observed during quality-assurance inspections of roofing membrane as follows:

1. Approximate quantities of components within roofing membrane will be determined according to ASTM D 3617.

2. Test specimens will be examined for interply voids according to ASTM D 3617 and to comply with criteria established in Appendix 3 of ARMA/NRCA's "Quality Control Guidelines for the Application of Polymer Modified Bitumen Roofing."

A roof inspection is required by manufacturer before warranty issue.  Revise scope of inspection and source of report to a qualified roofing consultant or an independent testing and inspecting agency if preferred.

C. Final Roof Inspection:  Arrange for roofing system manufacturer's technical personnel to inspect roofing installation on completion and submit report to Architect.

Retain subparagraph below if Architect or Owner wants to be present during manufacturer's final inspection.

1. Notify Architect or Owner 48 hours in advance of date and time of inspection.

D. Repair or remove and replace components of roofing system where test results or inspections indicate that they do not comply with specified requirements.

E. Additional testing and inspecting, at Contractor's expense, will be performed to determine compliance of replaced or additional work with specified requirements.

3.15 PROTECTING AND CLEANING

A. Protect roofing system from damage and wear during remainder of construction period.  When remaining construction will not affect or endanger roofing, inspect roofing for deterioration and damage, describing its nature and extent in a written report, with copies to Architect and Owner.

B. Correct deficiencies in or remove roofing system that does not comply with requirements, repair substrates, and repair or reinstall roofing system to a condition free of damage and deterioration at time of Substantial Completion and according to warranty requirements.

Retain below if coating membrane or if using fluid-applied bonding materials.

C. Clean overspray and spillage from adjacent construction using cleaning agents and procedures recommended by manufacturer of affected construction.

3.16 ROOFING INSTALLER'S WARRANTY

Delete this Article, retain this warranty, or include another roofing Installer's warranty form if required.  Coordinate with Part 1 "Warranty" Article.  Another sample layout of this warranty is included in the Evaluations in Division 7 Section "Modified Bituminous Membrane Roofing."

A. WHEREAS <Insert name> of <Insert address>, herein called the "Roofing Installer," has performed roofing and associated work ("work") on the following project:

1. Owner:  <Insert name of Owner.>

2. Address:  <Insert address.>

3. Building Name/Type:  <Insert information.>

4. Address:  <Insert address.>

5. Area of Work:  <Insert information.>

6. Acceptance Date:  <Insert date.>

7. Warranty Period:  <Insert time.>

8. Expiration Date:  <Insert date.>

B. AND WHEREAS Roofing Installer has contracted (either directly with Owner or indirectly as a subcontractor) to warrant said work against leaks and faulty or defective materials and workmanship for designated Warranty Period,

C. NOW THEREFORE Roofing Installer hereby warrants, subject to terms and conditions herein set forth, that during Warranty Period he will, at his own cost and expense, make or cause to be made such repairs to or replacements of said work as are necessary to correct faulty and defective work and as are necessary to maintain said work in a watertight condition.

D. This Warranty is made subject to the following terms and conditions:

1. Specifically excluded from this Warranty are damages to work and other parts of the building, and to building contents, caused by:

a. lightning;

Insert required wind speed below.

b. peak gust wind speed exceeding <Insert wind speed> mph (m/sec);

c. fire;

d. failure of roofing system substrate, including cracking, settlement, excessive deflection, deterioration, and decomposition;

e. faulty construction of parapet walls, copings, chimneys, skylights, vents, equipment supports, and other edge conditions and penetrations of the work;

f. vapor condensation on bottom of roofing; and

g. activity on roofing by others, including construction contractors, maintenance personnel, other persons, and animals, whether authorized or unauthorized by Owner.

2. When work has been damaged by any of foregoing causes, Warranty shall be null and void until such damage has been repaired by Roofing Installer and until cost and expense thereof have been paid by Owner or by another responsible party so designated.

3. Roofing Installer is responsible for damage to work covered by this Warranty but is not liable for consequential damages to building or building contents resulting from leaks or faults or defects of work.

4. During Warranty Period, if Owner allows alteration of work by anyone other than Roofing Installer, including cutting, patching, and maintenance in connection with penetrations, attachment of other work, and positioning of anything on roof, this Warranty shall become null and void on date of said alterations, but only to the extent said alterations affect work covered by this Warranty.  If Owner engages Roofing Installer to perform said alterations, Warranty shall not become null and void unless Roofing Installer, before starting said work, shall have notified Owner in writing, showing reasonable cause for claim, that said alterations would likely damage or deteriorate work, thereby reasonably justifying a limitation or termination of this Warranty.

5. During Warranty Period, if original use of roof is changed and it becomes used for, but was not originally specified for, a promenade, work deck, spray-cooled surface, flooded basin, or other use or service more severe than originally specified, this Warranty shall become null and void on date of said change, but only to the extent said change affects work covered by this Warranty.

6. Owner shall promptly notify Roofing Installer of observed, known, or suspected leaks, defects, or deterioration and shall afford reasonable opportunity for Roofing Installer to inspect work and to examine evidence of such leaks, defects, or deterioration.

7. This Warranty is recognized to be the only warranty of Roofing Installer on said work and shall not operate to restrict or cut off Owner from other remedies and resources lawfully available to Owner in cases of roofing failure.  Specifically, this Warranty shall not operate to relieve Roofing Installer of responsibility for performance of original work according to requirements of the Contract Documents, regardless of whether Contract was a contract directly with Owner or a subcontract with Owner's General Contractor.

E. IN WITNESS THEREOF, this instrument has been duly executed this <Insert day>  day of <Insert month>, <Insert year>.

1. Authorized Signature:  <Insert signature.>

2. Name:  <Insert name.>

3. Title:  <Insert title.>

END OF SECTION 07551

APP-MODIFIED BITUMINOUS MEMBRANE ROOFING
07551 - 1

