Copyright 2004 AIA
MASTERSPEC Full Length
11/04 (R 05/06)

Copyright 2004 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 09401 - PORTLAND CEMENT TERRAZZO FLOORING
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

A. Section Includes:

1. Poured-in-place portland cement terrazzo flooring[ and base].

2. Poured-in-place rustic terrazzo flooring.

3. Precast terrazzo units.

B. Related Sections:

Retain subparagraph below for requirements that Contractor might expect to find in this Section but are specified in other Sections.

1. Division 7 Section "Joint Sealants" for sealants installed with terrazzo.

Allowances are sometimes used for special terrazzo patterns.  If allowances apply to Work of this Section, insert brief paragraph here to alert Contractor and reference appropriate Division 1 Section for specific details.

1.3 SUBMITTALS

First five paragraphs below are defined in Division 1 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For each type of product indicated.

B. LEED Submittals:

Retain first subparagraph below if recycled content is required for LEED-NC or LEED-CI Credits MR 4.1 and MR 4.2; coordinate with requirements selected in Part 2 for granular materials.

1. Product Data for Credit MR 4.1[ and Credit MR 4.2]: For [marble chips,] [aggregates,] documentation indicating percentages by weight of postconsumer and preconsumer recycled content.

a. Include statement that indicates cost for each product having recycled content.

Retain subparagraph below if low-emitting materials used on the interior of the building are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives.

2. Product Data for Credit EQ 4.1:  For adhesives, including printed statement of VOC content.

C. Shop Drawings:  Include terrazzo installation requirements.  Include plans, elevations, sections, component details, and attachments to other work.  Show layout of the following:

1. Divider strips.

2. Control-joint strips.

3. Accessory strips.

4. Abrasive strips.

Retain first subparagraph below for structural portland cement terrazzo or for any type of rustic terrazzo.

5. Expansion-joint strips.

6. Stair treads, risers, and landings.

7. Precast terrazzo jointing and edge configurations.

8. Terrazzo patterns.

9. <Insert requirements>.

D. Samples for Initial Selection:  NTMA color plates showing the full range of colors and patterns available for each terrazzo type indicated.

Delete "Samples for Initial Selection" Paragraph above if colors, patterns, and other characteristics are preselected and specified or scheduled.  Retain first paragraph below with or without above.

E. Samples for Verification:  For each type, material, color, and pattern of terrazzo and accessory required showing the full range of color, texture, and pattern variations expected.  Label each terrazzo sample to identify matrix color and [marble-chip] [aggregate] types, sizes, and proportions.  Prepare samples of same thickness and from same material to be used for the Work in size indicated below:

1. Terrazzo:  [6-inch- (150-mm-)] <Insert size> square Samples.

2. Precast Terrazzo:  [6-inch- (150-mm-)] <Insert size> square Samples.

3. Accessories:  [6-inch- (150-mm-)] <Insert size> long Samples of each exposed strip item required.

Remaining paragraphs are defined in Division 1 Section "Submittal Procedures" as "Informational Submittals."

Coordinate first paragraph below with qualification requirements in Division 1 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

F. Qualification Data:  For qualified Installer.

Retain first paragraph below for material or product certificates from manufacturers.

G. Material Certificates:  For each type of terrazzo material or product, from manufacturer.

NTMA publishes recommendations for minimum maintenance-program requirements.

H. Maintenance Data:  For terrazzo to include in maintenance manuals.

1.4 QUALITY ASSURANCE

If applicable for Project location and if contractor membership is desired, retain first paragraph below.  See "Installer Considerations" Article in the Evaluations in Division 9 Section "Terrazzo Flooring." Consult NTMA for list of contractor members.

A. Installer Qualifications:  An installer who is a contractor member of NTMA.

B. Source Limitations for [Marble Chips] [Aggregates]:  Obtain each color, grade, type, and variety of granular materials from one source with resources to provide materials of consistent quality in appearance and physical properties.

C. NTMA Standards:  Comply with NTMA's "Terrazzo Specifications and Design Guide" and with written recommendations for terrazzo type indicated unless more stringent requirements are specified.

D. Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

1. Build mockups for terrazzo including accessories.

a. Size:  Minimum 100 sq. ft. (9 sq. m) of typical poured-in-place flooring[ and base] condition for each color and pattern [in locations indicated] [in locations directed by Architect] <Insert location requirements>.

Insert mockup requirements for precast terrazzo units if any.

Retain subparagraph below if mockups are installed as part of building rather than erected separately and the intention is to make an exception to the default requirement in Division 1 Section "Quality Requirements" for demolishing and removing mockups when directed unless otherwise indicated.

2. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Retain paragraph below if Work of this Section is extensive or complex enough to justify a preinstallation conference.

E. Preinstallation Conference:  Conduct conference at [Project site] <Insert location>.

Retain subparagraph below if additional requirements are necessary; include information about conference.

1. Review methods and procedures related to terrazzo including, but not limited to, the following:

a. Inspect and discuss condition of substrate and other preparatory work performed by other trades.

b. Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

c. Review special terrazzo designs and patterns.

Delete first subparagraph below if only rustic terrazzo is required; rustic terrazzo is not ground.

d. Review dust-control procedures.

Retain first subparagraph below for rustic terrazzo or for installations that begin before completing building enclosure.

e. Review weather and forecasted weather conditions and procedures for coping with unfavorable conditions.

f. <Insert agenda items>.

If needed, insert list of conference participants not mentioned in Division 1 Section "Project Management and Coordination."

1.5 DELIVERY, STORAGE, AND HANDLING

A. Deliver materials to Project site in supplier's original wrappings and containers, labeled with source's or manufacturer's name, material or product brand name, and lot number if any.

B. Store materials in their original, undamaged packages and containers, inside a well-ventilated area protected from weather, moisture, soiling, extreme temperatures, and humidity.

1.6 PROJECT CONDITIONS

Retain first paragraph below for portland cement terrazzo, which is generally used at interior locations.

A. Environmental Limitations:  Maintain temperature above 50 deg F (10 deg C) for 48 hours before and during terrazzo installation.

Retain first paragraph below for rustic terrazzo, which is generally used at exterior locations.

B. Weather Limitations:  Proceed with rustic terrazzo installation only when forecasted weather conditions permit work to be performed according to NTMA's written recommendations and temperatures remain above 45 deg F (7.2 deg C).

Retain first paragraph below for precast terrazzo.

C. Field Measurements:  Verify actual dimensions of construction contiguous with precast terrazzo by field measurements before fabrication.

Retain paragraph below for portland cement terrazzo.  Dust control is not required for rustic terrazzo because grinding operations do not apply.

D. Control and collect dust produced by grinding operations.  Protect adjacent construction from detrimental effects of grinding operations.

Retain subparagraph below if required.

1. Provide dustproof partitions and temporary enclosures to limit dust migration and to isolate areas from noise.

PART 2 -  PRODUCTS

2.1 PORTLAND CEMENT TERRAZZO

Portland cement terrazzo is generally used for building interiors.  See "Portland Cement Terrazzo" Article in the Evaluations in Division 9 Section "Terrazzo Flooring" for a discussion of portland cement terrazzo types.

A. Portland Cement Terrazzo Type:  [Sand cushion] [Structural] [Bonded] [Monolithic] [Installed over metal deck].

B. Materials:

1. Portland Cement:  ASTM C 150, Type 1.

Retaining second or third option in first subparagraph below limits NTMA plate selections.  Coordinate with mix specified or retain default requirement.  White cement is uniform in color.  Gray cement may not be uniform in color and may produce matrix shade variations.

a. Color for Exposed Matrix:  [As required by mix indicated] [White] [Gray] <Insert requirements>.

2. Water:  Potable.

Retain first subparagraph below for sand-cushion or bonded portland cement terrazzo.

3. Sand:  ASTM C 33.

Marble chips are the most commonly employed granular material.  Aggregate sizing may not be based on NTMA gradation standards for marble chips.  Consult NTMA and manufacturers for recommendations and incorporate requirements.

4. [Marble Chips] [Aggregates]:  Complying with NTMA gradation standards for mix indicated and containing no deleterious or foreign matter.

Retain option in first subparagraph below for large-size marble chips Nos. 5 through 8.  Large-size marble chips are used with Venetian terrazzo.  See "Terrazzo Matrices" Article in the Evaluations in Division 9 Section "Terrazzo Flooring" for a discussion of granular materials.

a. Abrasion and Impact Resistance:  Less than 40 percent loss per ASTM C 131[ and ASTM C 535].

b. 24-Hour Absorption Rate:  Less than 0.75 percent.

c. Dust Content:  Less than 1.0 percent by weight.

Retain first subparagraph below if recycled content of granular materials is required for LEED-NC or LEED-CI Credits MR 4.1 and MR 4.2.  An alternative method of meeting Credit MR 4.1 and MR 4.2 requirements is to retain requirement in Division 1 Section "LEED Requirements" that gives Contractor option and responsibility for determining how Credit MR 4.1 and MR 4.2 requirements will be met.

d. Recycled Content:  Provide products with average recycled content such that postconsumer recycled content plus one-half of preconsumer recycled content is not less than <Insert value> percent.

If desired for decorative effect, insert requirements for aggregates other than marble chips, such as granite, quartz, pea gravel, mother-of-pearl, or other suitable granules.  Consult NTMA for recommendations.

5. Matrix Pigments:  Pure mineral or synthetic pigments, alkali resistant, durable under exposure to sunlight, and compatible with terrazzo matrix.

Retain first subparagraph below for monolithic portland cement terrazzo.

6. Bonding Agent:  Neat portland cement or epoxy or acrylic bonding agents formulated for use with topping indicated.

Retain two subparagraphs below for sand-cushion portland cement terrazzo.

7. Underbed Reinforcement:  Galvanized welded-wire reinforcement, 2 by 2 inches (51 by 51 mm) by 0.062-inch- (1.57-mm-) diameter wire, complying with ASTM A 185 and ASTM A 82, except for minimum wire size.

8. Isolation Membrane:  Polyethylene sheeting, ASTM D 2103, Type 13300, 4 mils (0.1 mm) thick; or unperforated asphalt felt, ASTM D 226, Type I (No. 15).

C. Mixes:

Retain first subparagraph below for structural portland cement terrazzo or portland cement terrazzo installed over metal deck.  These terrazzo applications require a structural-concrete underbed.

1. Underbed:  Structural-concrete underbed as specified in Division 3 Section "[Cast-in-Place Concrete] <Insert Section title>."

Retain first subparagraph below for sand-cushion or bonded portland cement terrazzo.

2. Underbed:  Comply with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated for component proportions and mixing.

See "Terrazzo Matrices" Article in the Evaluations in Division 9 Section "Terrazzo Flooring" for a discussion of NTMA plate number designations and custom design mixes.

Retain first subparagraph below for NTMA-formulated design mixes.

3. Portland Cement Terrazzo:  Comply with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated for matrix and marble-chip proportions and mixing.

a. Formulated Mix Color and Pattern:  [As selected by Architect from NTMA standard-terrazzo plates] [As selected by Architect from NTMA Venetian-terrazzo plates] <Insert NTMA color plate designation>.

Retain subparagraph below for custom design mixes.

4. Portland Cement Terrazzo:  Comply with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated for matrix and [marble-chip] [aggregate] proportions and mixing.

a. Custom Mix Color and Pattern:  [Match Architect's sample] [Match existing] <Insert custom design mix attributes>.

2.2 RUSTIC TERRAZZO

Rustic terrazzo, commonly used for exterior locations, is a variation of portland cement terrazzo.  See "Rustic Terrazzo" Article in the Evaluations in Division 9 Section "Terrazzo Flooring" for a discussion of rustic terrazzo types.

A. Rustic Terrazzo Type:  [Structural] [Bonded] [Monolithic] [Unbonded].

B. Materials:

1. Portland Cement:  ASTM C 150, Type 1.

a. Color for Exposed Matrix:  [As required by mix indicated] <Insert requirements>.

2. Water:  Potable.

Retain first subparagraph below for underbed of structural, bonded, or unbonded rustic terrazzo.

3. Sand:  ASTM C 33.

4. [Marble Chips] [Aggregates]:  As required for mix indicated, sizes complying with NTMA gradation standards, 0.25 percent maximum 24-hour absorption rate, and containing no deleterious or foreign matter.

Retain first subparagraph below if recycled content of granular materials is required for LEED-NC or LEED-CI Credits MR 4.1 and MR 4.2.  An alternative method of meeting Credit MR 4.1 and MR 4.2 requirements is to retain requirement in Division 1 Section "LEED Requirements" that gives Contractor option and responsibility for determining how Credit MR 4.1 and MR 4.2 requirements will be met.

a. Recycled Content:  Provide products with average recycled content such that postconsumer recycled content plus one-half of preconsumer recycled content is not less than <Insert value> percent.

5. Matrix Pigments:  Pure mineral or synthetic pigments, alkali resistant, durable under exposure to sunlight and weather, and compatible with matrix binder.

Retain first subparagraph below for underbed of structural, bonded, or unbonded rustic terrazzo.

6. Air-Entraining Agent:  Complying with NTMA's written recommendations and recommended by supplier for intended use.

Retain first subparagraph below for bonded rustic terrazzo.

7. Underbed Bonding Agent:  Neat portland cement.

Retain first subparagraph below for monolithic rustic terrazzo.

8. Topping Bonding Agent:  Neat portland cement, or epoxy or acrylic bonding agents formulated for use with topping indicated.

Retain subparagraph below for unbonded rustic terrazzo.

9. Isolation Membrane:  Polyethylene sheeting, ASTM D 2103, Type 13300, 4 mils (0.1 mm) thick.

C. Mixes:

Retain first subparagraph below for structural or unbonded rustic terrazzo.  These terrazzo applications require a structural-concrete underbed.

1. Underbed:  Structural-concrete underbed as specified in Division 3 Section "[Cast-in-Place Concrete] <Insert Section title>."

Retain first subparagraph below for bonded rustic terrazzo.

2. Underbed:  Comply with NTMA's "Terrazzo Specifications and Design Guide" for component proportions and mixing.

a. Exterior Applications:  Provide air-entraining agent.

See "Terrazzo Matrices" Article in the Evaluations in Division 9 Section "Terrazzo Flooring" for a discussion of NTMA plate number designations and custom design mixes.

Retain first subparagraph below for NTMA-formulated design mixes.

3. Rustic Terrazzo:  Comply with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated for matrix and marble-chip proportions and mixing.

a. Formulated Mix Color and Pattern:  [As selected by Architect from NTMA rustic-terrazzo plates] <Insert NTMA color plate designation>.

Retain subparagraph below for custom design mixes.

4. Rustic Terrazzo:  Comply with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated for matrix and [marble-chip] [aggregate] proportions and mixing.

a. Custom Mix Color and Pattern:  [Match Architect's sample] [Match existing] <Insert custom design mix attributes>.

2.3 STRIP MATERIALS

Refer to "Strip Materials" Article in the Evaluations in Division 9 Section "Terrazzo Flooring" for discussion of strip material types, finishes, and placement.  Heavy-top divider strips and heavy-top angle divider strips have a more visible top-section width than standard divider strips.

A. Standard Divider Strips:  One-piece, flat-type strips for grouting into sawed joints prepared in concrete slab or underbed.

1. Material:  [As indicated] [White-zinc alloy] [Brass] <Insert requirements>.

2. Depth:  [As indicated] [3/4 inch (19 mm)] [1-1/4 inches (32 mm)] [2 inches (51 mm)] <Insert dimension>.

3. Width:  [As indicated] [0.05 inch (1.27 mm)] [1/8 inch (3.2 mm)] [1/4 inch (6.4 mm)] <Insert dimension>.

B. Heavy-Top Divider Strips:  One-piece, flat-type strips for grouting into sawed joints prepared in concrete slab or underbed.

1. Base-Section Material:  [As indicated] [White-zinc alloy] [Galvanized steel] <Insert requirements>.

2. Top-Section Material:  [As indicated] [White-zinc alloy] [Brass] [Plastic, in color selected from manufacturer's full range] <Insert requirements>.

3. Depth:  [As indicated] [3/4 inch (19 mm)] [1-1/4 inches (32 mm)] [2 inches (51 mm)] <Insert dimension>.

4. Top-Section Width:  [As indicated] [1/8 inch (3.2 mm)] [1/4 inch (6.4 mm)] [1/2 inch (12.7 mm)] <Insert dimension>.

C. Heavy-Top Angle Divider Strips:  One-piece, L-type angle strips with anchoring device and in depth required for topping thickness indicated.

1. Material:  [As indicated] [White-zinc alloy] [Brass] [Plastic, in color selected from manufacturer's full range] <Insert requirements>.

2. Top-Section Width:  [As indicated] [1/8 inch (3.2 mm)] [1/4 inch (6.4 mm)] [3/8 inch (9.5 mm)] [1/2 inch (12.7 mm)] <Insert dimension>.

D. Control-Joint Strips:  Separate, double L-type angles, positioned back to back, that match material, thickness, and color of divider strips and in depth required for topping thickness indicated.

Retain first paragraph below for structural portland cement terrazzo or for any type of rustic terrazzo.

E. Expansion-Joint Strips:  [Brass] [Plastic strips in color selected from manufacturer's full range], with removable zip-strip top for installing sealant; [in width indicated] [minimum 1/2 inch (12.7 mm) wide] <Insert width>.

F. Accessory Strips:  Match divider strip width, material, and color unless otherwise indicated.  Use the following types of accessory strips as required to provide a complete installation:

Revise list below to suit Project.

1. Base-bead strips for exposed top edge of terrazzo base.

2. Edge-bead strips for exposed edges of terrazzo.

3. Nosings for terrazzo stair treads and landings.

4. <Insert requirements>.

Retain paragraph below for terrazzo stair treads and landings.

G. Abrasive Strips:  Silicon carbide or aluminum oxide, or combination of both, in epoxy-resin binder and set in channel.

1. Width:  [1/2 inch (12.7 mm)] <Insert dimension>.

2. Depth:  As required by terrazzo thickness.

3. Length:  [4 inches (100 mm) less than stair width] [As indicated] <Insert dimension>.

4. Color:  [As selected by Architect from manufacturer's full range] <Insert requirements>.

2.4 MISCELLANEOUS ACCESSORIES

A. Strip Adhesive:  Adhesive recommended by manufacturer for this use.

Retain subparagraph below if low-emitting materials are required for LEED Credit EQ 4.1.  VOC limit is that for multipurpose construction adhesives.

1. Use adhesives that have a VOC content of 70 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

B. Anchoring Devices:

Revise list below to suit Project.

1. Strips:  Provide mechanical anchoring devices for strip materials as required for secure attachment to substrate.

2. Precast Terrazzo:  Provide mechanical anchoring devices as recommended by fabricator for proper anchorage and support of units for conditions of installation and support.

Retain first paragraph below if expansion-joint strips are used.

C. Isolation and Expansion-Joint Material:  Closed-cell polyethylene foam, nonabsorbent to liquid water and gas, and nonoutgassing in unruptured state; butyl rubber; rubber; or cork; [in width indicated] [minimum 1/2 inch (12.7 mm) wide] <Insert width>.

Retain first paragraph below for portland cement terrazzo.

D. Portland Cement Terrazzo Cleaner:  Chemically neutral cleaner with pH factor between 7 and 10 that is biodegradable, phosphate free, and recommended by cleaner manufacturer for use on terrazzo type indicated.

Retain first paragraph below for rustic terrazzo.

E. Rustic Terrazzo Cleaner:  Solution of muriatic acid and water for use on terrazzo type indicated.

F. Sealer:  Slip- and stain-resistant, penetrating-type sealer that is chemically neutral with pH factor between 7 and 10; does not affect color or physical properties of terrazzo; is recommended by sealer manufacturer; and complies with NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated.

Retain subparagraph below for rustic terrazzo.

1. Rustic Terrazzo:  Use solvent acrylic-type sealer.

2.5 PRECAST TERRAZZO

A. Precast Terrazzo Units:

See Editing Instruction No. 1 in the Evaluations in Division 9 Section "Terrazzo Flooring" for cautions about naming manufacturers.  Retain one of two subparagraphs and list of manufacturers below.  See Division 1 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

a. Precast Terrazzo Enterprises, Inc.

b. Romoco Precast Terrazzo Products.

c. Wausau Tile, Inc.; Terra Paving Products Division.

d. <Insert manufacturer's name>.

B. Precast Terrazzo Base Units:  Minimum 3/4-inch- (19-mm-) thick, reinforced portland cement terrazzo units cast in maximum lengths possible, but not less than 36 inches (900 mm).

1. Type:  [As indicated] [Coved with minimum 3/4-inch (19-mm) radius] [Straight] [Splayed] <Insert requirements>.

Retain first option in first subparagraph below if top edge is concealed.

2. Top Edge:  [Straight, unfinished] [Beveled with polished top surface] [Radius edge with polished top surface] <Insert requirements>.

Retain first subparagraph below for coved-toe bases.  Insert metal-divider requirements if desired.

3. Metal Toe Strip:  [Zinc] [Brass].

4. Outside Corner Units:  With finished returned edges at outside corner.

5. Color, Pattern, and Finish:  [As selected by Architect from manufacturer's full range] [Match Architect's sample] [Match adjacent poured-in-place terrazzo flooring] <Insert requirements>.

Retain first paragraph below for precast terrazzo stair treads, thresholds, sills, benches, planters, and custom units.  Detail profile, anchorage, and other requirements on Drawings or insert below.

C. Precast Terrazzo Units[ for] [Stair Treads] [Thresholds] [Sills] [Benches] [and] [Planters] <Insert requirements>:  Comply with NTMA's written recommendations for fabricating precast terrazzo units in sizes and profiles indicated.  Reinforce units as required by unit sizes, profiles, and thicknesses and as recommended by manufacturer.

Verify requirements of authorities having jurisdiction for treads.

1. Stair Treads:  [Three-line] [Two-line] [One-line] [Abrasive nosing strip and two-line] <Insert requirements> abrasive inserts at nosings.

2. Color, Pattern, and Finish:  [As selected by Architect from manufacturer's full range] [Match Architect's sample] [Match adjacent poured-in-place terrazzo flooring] <Insert requirements>.

Insert requirements for other types of precast terrazzo units to suit Project.

Retain paragraph below for custom precast terrazzo components.

D. Precast Terrazzo Finishing:

1. Finish exposed-to-view edges or reveals to match face finish.

2. Ease exposed edges to 1/8-inch (3-mm) radius.

3. <Insert requirements>.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates and areas, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance.

B. Proceed with installation only after unsatisfactory conditions, including levelness tolerances, have been corrected.

3.2 PREPARATION

A. Clean substrates to produce clean, dry, and neutral substrate for terrazzo application.

1. Remove substances, including oil, grease, and curing compounds, that might impair bond of terrazzo system.

Retain subparagraph below for smooth concrete substrates or insert requirements for other substrates such as wood or quarry tile; consult manufacturers for recommendations.

2. Roughen concrete substrates before installing terrazzo system according to NTMA's written recommendations.

Retain paragraph below for portland cement terrazzo.  Dust control is not required for rustic terrazzo because grinding operations do not apply.

B. Protect other work from dust generated by grinding operations.  Control dust to prevent air pollution and comply with environmental protection regulations.

Retain subparagraph below if required.

1. Erect and maintain temporary enclosures and other suitable methods to limit dust migration and to ensure adequate ambient temperatures and ventilation conditions during installation.

3.3 INSTALLATION, GENERAL

A. Comply with NTMA's written recommendations for terrazzo and accessory installation.

Coordinate concrete-slab flatness and levelness tolerances with NTMA recommendations, especially for monolithic portland cement terrazzo and for monolithic rustic terrazzo.  See Division 3 Section "Cast-in-Place Concrete" for floor and slab tolerances.

B. Installation Tolerance:  Limit variation in terrazzo surface from level to [1/4 inch in 10 feet (6 mm in 3 m)] <Insert dimensions>; noncumulative.

Retain and revise first paragraph below for structural portland cement terrazzo or for any type of rustic terrazzo.

C. [Structural Portland Cement] [Structural Rustic] [Bonded Rustic] [Monolithic Rustic] [Unbonded Rustic] Terrazzo:  Install isolation and expansion material where [terrazzo and underbed abut] [terrazzo abuts] adjacent construction and directly above substrate expansion joints.

Retain and revise first paragraph below for structural portland cement terrazzo or portland cement terrazzo installed over metal deck, or for structural or unbonded rustic terrazzo.

D. Underbed:  Install structural-concrete underbed according to requirements specified in "Division 3 Section "[Cast-in-Place Concrete] <Insert Section title>."

Retain first paragraph below for sand-cushion or bonded portland cement terrazzo or for bonded rustic terrazzo.

E. Underbed:

1. Comply with NTMA's "Terrazzo Specifications and Design Guide" for underbed installation.

Retain first three subparagraphs below for sand-cushion portland cement terrazzo only.

2. Cover entire surface to receive terrazzo with dusting of sand.

3. Install isolation membrane over sand, overlapping ends and edges a minimum of 3 inches (75 mm).

4. Install welded wire reinforcement, overlapping at edges and ends at least two squares.[  Stop mesh a minimum of 1 inch (25 mm) short of expansion joints.]

5. Place underbed and screed to elevation indicated below finished floor elevation.

Revise first paragraph below to suit Project.  Indicate location and spacing of strip materials on Drawings or insert below.

F. Strip Materials:

1. Divider and Control-Joint Strips:

a. Locate divider strips [over each edge of steel beams and girders] [centered over steel beams and joists] [directly over control joints, breaks, and saw cuts in concrete slabs] [in locations indicated] <Insert requirements>.

b. Install control-joint strips [back to back and directly above concrete-slab control joints] [in locations indicated] <Insert requirements>.

c. Install control-joint strips with [1/4-inch (6.4-mm)] <Insert dimension> gap between strips, and install sealant in gap.

d. Install strips in adhesive setting bed without voids below strips, or mechanically anchor strips as required to attach strips to substrate, as recommended by strip manufacturer.

Retain first subparagraph below for structural portland cement terrazzo or for any type of rustic terrazzo.

2. Expansion-Joint Strips:  Form expansion joints using divider strips and install directly above concrete-slab expansion joints.

Retain first subparagraph below for accessory strips.

3. Accessory Strips:  Install accessory strips as required to provide a complete installation.

Retain subparagraph below for abrasive strips.  First option is based on NTMA recommendations for precast terrazzo stair treads; second, on Romoco's product literature.

4. Abrasive Strips:  Install with surface of abrasive strip positioned [1/16 inch (1.6 mm)] [1/32 inch (0.8 mm)] <Insert dimension> higher than terrazzo surface.

G. Repair:  Cut out and replace terrazzo areas that evidence lack of bond with substrate or underbed, including areas that emit a "hollow" sound if tapped.  Cut out terrazzo areas in panels defined by strips and replace to match adjacent terrazzo, or repair panels according to NTMA's written recommendations, as approved by Architect.

3.4 PORTLAND CEMENT TERRAZZO INSTALLATION

A. Pour in place, cure, and finish portland cement terrazzo according to NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated.

B. Terrazzo Topping Thickness:  [As indicated] <Insert thickness>.

C. Finishing:

1. Seed additional [marble chips] [aggregates] in matrix to uniformly distribute granular material on surface.

2. Delay fine grinding until heavy trade work is complete and construction traffic through area is restricted.

3. Fine Grinding:  Grind with stones 120 grit or finer until all grout is removed from surface.  Repeat rough grinding, grout coat, and fine grinding if large voids exist after initial fine grinding.  Produce surface with a minimum of 70 percent aggregate exposure.

4. <Insert requirements>.

3.5 RUSTIC TERRAZZO INSTALLATION

A. Pour in place, cure, and finish rustic terrazzo according to NTMA's "Terrazzo Specifications and Design Guide" for terrazzo type indicated.

B. Terrazzo Topping Thickness:  [As indicated] <Insert thickness>.

C. Finishing:

1. Seed additional [marble chips] [aggregates] in matrix to uniformly distribute granular material on surface.

2. <Insert requirements>.

3.6 PRECAST TERRAZZO INSTALLATION

A. Install precast terrazzo units using method recommended by NTMA and manufacturer unless otherwise indicated.

B. Installation Tolerance:  Set units with alignment level and true to dimensions, varying [1/8 inch (3.2 mm)] <Insert dimension> maximum in length, height, or width; noncumulative.

C. Do not install units that are chipped, cracked, discolored, or improperly finished.

D. Seal joints between units with [cement grout matching precast terrazzo matrix] [joint sealant] <Insert requirements>.

3.7 CLEANING AND PROTECTION

Retain first paragraph below for portland cement terrazzo and precast terrazzo.

A. Portland Cement Terrazzo[ and] [ Precast Terrazzo] Cleaning:

1. Remove grinding dust from installation and adjacent areas.

2. Wash surfaces with cleaner immediately after[ grouting precast terrazzo units and] final cleaning of terrazzo flooring.

3. Wash surfaces with cleaner according to NTMA's written recommendations and manufacturer's written instructions; rinse surfaces with water and allow to dry thoroughly.

Retain first paragraph below for rustic terrazzo only.

B. Rustic Terrazzo Cleaning:  Clean surfaces with 1:10 solution of muriatic acid in water.  Legally contain and dispose of runoff from cleaning operations.  Rinse surfaces with water and allow to dry thoroughly.

Retain first paragraph below for portland cement terrazzo, rustic terrazzo, and precast terrazzo.

C. Sealing:

1. Seal surfaces according to NTMA's written recommendations.

2. Apply sealer according to sealer manufacturer's written instructions.

D. Protection:  Provide final protection and maintain conditions, in a manner acceptable to Installer, that ensure that terrazzo is without damage or deterioration at time of Substantial Completion.

END OF SECTION 09401END OF SECTION 09401

PORTLAND CEMENT TERRAZZO FLOORING
09401 - 1

