Copyright 2004 AIA
MASTERSPEC
08/04
PRODUCT MASTERSPEC LICENSED BY ARCOM TO NATIONAL GYPSUM COMPANY

Copyright 2004 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

This PRODUCT MASTERSPEC section is licensed by ARCOM (November, 2004) for distribution by National Gypsum Company. Changes made to MASTERSPEC by National Gypsum Company are indicated using underline/strikeout text.  Review and accept changes according to project requirements and specifier's practice. The underline and strikeout portions of the text in this Section are not provided by, endorsed by, or representative of the opinions of ARCOM or The American Institute of Architects.  For more information contact National Gypsum Company, 2001 Rexford Road, Charlotte, NC 28211. Phone 1-800-NATIONAL. Fax 704-365-7276.

SECTION 09265 - GYPSUM BOARD SHAFT-WALL ASSEMBLIES
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes gypsum board shaft-wall assemblies for the following:

Adjust list below to suit Project.

1. Shaft-wall enclosures.

2. Chase enclosures.

Delete first subparagraph below when gypsum board shaft-wall assemblies are not used at stair enclosures.

3. Stair enclosures.

4. Horizontal enclosures.

B. Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

1. Division 1 Section "LEED Requirements" for additional LEED requirements.

2. Division 7 Section "Fire-Resistive Joint Systems" for head-of-wall assemblies that incorporate gypsum board shaft-wall assemblies.

1.3 SUBMITTALS

A. Product Data:  For each gypsum board shaft-wall assembly indicated.

Retain paragraph and subparagraphs below for LEED.  Submittals are not required to be submitted to the U.S. Green Building Council as part of LEED certification process but are necessary to verify compliance with indicated LEED credits.

B. LEED Submittals:

Retain subparagraph below if low-emitting materials are required for LEED Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives.

1. Credit EQ 4.1:  Product Data for adhesives, including printed statement of VOC content.

Retain subparagraph and associated subparagraph below if recycled content is required for LEED Credits MR 4.1 and MR 4.2; coordinate with requirements selected in Part 2 for sound attenuation insulation.

2. Credit MR 4.1[ and Credit MR 4.2]:  Product Data indicating percentages by weight of postconsumer and preconsumer recycled content for sound attenuation insulation.

a. Include statement indicating costs for each product having recycled content.

1.4 QUALITY ASSURANCE

Assemblies are fire-response tested as proprietary systems; therefore, stud type, which is described by its profile, used in one shaft-wall manufacturer's assemblies cannot be substituted for a different type required for another manufacturer's assemblies.

Indicate fire-resistance ratings of specific assemblies on Drawings.

A. Fire-Resistance Ratings:  Provide materials and construction identical to those of assemblies with fire-resistance ratings determined according to ASTM E 119 by a testing and inspecting agency.

Retain paragraph below if shaft wall is part of STC-rated assemblies.  Indicate design designations of specific assemblies on Drawings.

B. STC-Rated Assemblies:  Provide materials and construction identical to those of assemblies tested according to ASTM E 90 and classified according to ASTM E 413 by a testing and inspecting agency.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 1.

C. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination."  Review methods and procedures for installing gypsum board shaft-wall assemblies including, but not limited to, the following:

Delete subparagraphs below if not required.  If retaining, revise to include Project-specific requirements.  Insert additional requirements to suit Project.

1. Fasteners proposed for anchoring nonstructural steel framing to building structure.

2. Sprayed fire-resistive materials applied to structural steel framing.

3. Elevator equipment, including hoistway doors, elevator call buttons, and elevator floor indicators.

4. Wiring devices in shaft-wall assemblies.

5. Doors and other items penetrating shaft-wall assemblies.

6. Items supported by shaft-wall-assembly framing.

7. Mechanical work enclosed within shaft-wall assemblies.

1.5 DELIVERY, STORAGE, AND HANDLING

A. Deliver materials in original packages, containers, and bundles bearing brand name and identification of manufacturer or supplier.

B. Store materials inside under cover and keep them dry and protected against damage from weather, direct sunlight, surface contamination, corrosion, construction traffic, and other causes.

C. Stack panels flat on leveled supports off floor or slab to prevent sagging.

1.6 PROJECT CONDITIONS

A. Environmental Limitations:  Comply with ASTM C 840 requirements or with gypsum board manufacturer's written recommendations, whichever are more stringent.

Delete first paragraph below if infeasible for fast-track construction.

B. Do not install interior products until installation areas are enclosed and conditioned.

C. Do not install panels that are wet, moisture damaged, or mold damaged.

1. Indications that panels are wet or moisture damaged include, but are not limited to, discoloration, sagging, and irregular shape.

2. Indications that panels are mold damaged include, but are not limited to, fuzzy or splotchy surface contamination and discoloration.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  
A. 
B. 
C. Basis-of-Design Product:  Subject to compliance with requirements, provide gypsum board shaftwall assemblies by National Gypsum Company or a comparable product by one of the following:

1. American Gypsum Company.

2. BPB America Inc.

3. G-P Gypsum.

4. Lafarge North America Inc.

5. 
6. PABCO Gypsum.

7. Temple-Inland Forest Products Corporation.

8. USG Corporation.

9. <Insert manufacturer's name.>

2.2 GYPSUM BOARD SHAFT-WALL ASSEMBLIES, GENERAL

A. Provide materials and components complying with requirements of fire-resistance-rated assemblies indicated.

1. Provide panels in maximum lengths available to eliminate or minimize end-to-end butt joints.

2. Provide auxiliary materials complying with gypsum board shaft-wall assembly manufacturer's written recommendations.

2.3 PANEL PRODUCTS

A. Gypsum Liner Panels:  Comply with ASTM C 442/C 442M and ASTM C 1396.

Examples of standard liner panels include American Gypsum's "American Gypsum Shaft Liner," BPB's "ProRoc Shaftliner," G-P Gypsum's "Tough Rock Fireguard Shaftliner," Lafarge's "Firecheck Shaftliner Type X," National Gypsum's "Fire-Shield Shaftliner," PABCO's "Pabcore Gypsum Liner Board," Temple-Inland's "Fire-Rated Silent Guard Gypsum Shaftliner System," and USG's "Sheetrock Brand Gypsum Liner Panel."

1. Type X:  Manufacturer's proprietary liner panels with moisture-resistant paper faces.

a. Basis-of-Design Product:  National Gypsum Company; Gold Bond Brand 1 inch Fire-Shield Shaftliner.

b. Core:  1 inch (25.4 mm) thick.

c. Long Edges:  Double bevel.

Examples of moisture- and mold-resistant liner panels include G-P Gypsum's "Dens-Glass Ultra Shaftliner" panels, which have coated glass-mat facings, and National Gypsum's "Fire-Shield Shaftliner XP" panels, which have paper facings.

2. Mold- and Mildew-Resistant Type X:  Manufacturer's proprietary liner panels with moisture- and mold-resistant core and surfaces.

a. Basis-of-Design Product:  National Gypsum Company; Gold Bond Brand 1 inch Fire-Shield Shaftliner XP.

b. Core:  1 inch (25.4 mm) thick.

c. Long Edges:  Double bevel.

Retain paragraph below if exposed surfaces of shaft walls will receive gypsum veneer plaster finish.

B. Gypsum Base for Gypsum Veneer Plaster:  As specified in Division 9 Section "Gypsum Veneer Plastering."

1. Basis-of-Design Product:  National Gypsum Company; [Gold Bond Brand Kal-Kore Fire-Shield Plaster Base] [Gold Bond Brand Kal-Kore Fire-Shield C Plaster Base] [Hi-Abuse Brand Kal-Kore Fire-Shield Plaster Base].

Retain paragraph below if exposed surfaces of shaft walls or backing panels of multilayer applications are gypsum board.

C. Gypsum Board:  As specified in Division 9 Section "Gypsum Board."

1. Basis-of-Design Product:  National Gypsum Company; [Gold Bond Brand Fire-Shield Wallboard] [Gold Bond Brand Fire-Shield C Wallboard].

Consider using water-resistant backing board if finish panels may be installed before building is fully enclosed.

D. Water-Resistant Gypsum Backing Board:  As specified in Division 9 Section "Gypsum Board."

1. Basis-of-Design Product:  National Gypsum Company; [Gold Bond Brand Fire-Shield MR Board] [Gold Bond Brand Fire-Shield C MR Board].

E. Mold- and Mildew-Resistant Gypsum Wallboard:  As specified in Division 9 Section "Gypsum Board."

1. Basis-of-Design Product:  National Gypsum Company; [Gold Bond Brand XP Fire-Shield Wallboard] [Gold Bond Brand XP Fire-Shield C Wallboard].

Retain paragraph below if exposed surfaces of shaft walls will receive ceramic tile finish.

F. Cementitious Backer Units:  As specified in Division 9 Section "Ceramic Tile."

1. Basis-of-Design Product:  National Gypsum Company;  PermaBase Brand Cement Board.

G. Bendable Cementitious Backer Units:  As specified in Division 9 Section "Ceramic Tile."

1. Basis-of-Design Product:  National Gypsum Company;  PermaBase Flex Brand Cement Board.

2.4 NON-LOAD-BEARING STEEL FRAMING

A. Framing Members:  Comply with ASTM C 754 for conditions indicated.

Steel framing complies with ASTM C 645 for material thickness; stud type and size do not apply.

B. Steel Sheet Components:  Comply with ASTM C 645 requirements for metal, unless otherwise indicated.

See "Corrosion Protection of Steel Framing" Article in the Evaluations for discussion of corrosion-resistant coatings on components.

1. Protective Coating:  [ASTM A 653/A 653M, G40 (Z120)] [ASTM A 653/A 653M, G60 (Z180)] [Coating with equivalent corrosion resistance of ASTM A 653/A 653M, G40 (Z120)], hot-dip galvanized, unless otherwise indicated.

2.5 AUXILIARY MATERIALS

A. General:  Provide auxiliary materials that comply with referenced product standards and manufacturer's written recommendations.

B. Trim Accessories:  Cornerbead, edge trim, and control joints of material and shapes specified in Division 9 Section "[Gypsum Veneer Plastering] [Gypsum Board]" that comply with gypsum board shaft-wall assembly manufacturer's written recommendations for application indicated.

Retain two paragraphs below if exposed surfaces of shaft walls will receive gypsum veneer plaster finish.

C. Gypsum Base Joint-Reinforcing Materials:  As specified in Division 9 Section "Gypsum Veneer Plastering."

D. Gypsum Veneer Plaster:  ASTM C 587 and as specified in Division 9 Section "Gypsum Veneer Plastering."

Retain paragraph below if exposed surfaces of shaft walls or backing panels of multilayer applications are gypsum board.

E. Gypsum Board Joint-Treatment Materials:  As specified in Division 9 Section "Gypsum Board."

Delete first paragraph and subparagraph below if no multilayer applications.

F. Laminating Adhesive:  Adhesive or joint compound recommended by manufacturer for directly adhering gypsum face-layer panels[ and gypsum-base face-layer panels] to backing-layer panels in multilayer construction.

Retain subparagraph below if low-emitting materials are required for LEED Credit EQ 4.1.  VOC limit is that for gypsum board and panel adhesives in South Coast Air Quality Management District Rule #1168.

1. Use adhesives that have a VOC content of 50 g/L or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

G. Steel Drill Screws:  ASTM C 1002, unless otherwise indicated.

Delete subparagraph below if no cementitious backer units.

1. For fastening cementitious backer units, use screws of type and size recommended by panel manufacturer.

H. Track Fasteners:  Power-driven fasteners of size and material required to withstand loading conditions imposed on shaft-wall assemblies without exceeding allowable design stress of track, fasteners, or structural substrates in which anchors are embedded.

Retain subparagraph below if expansion anchors are acceptable.  Verify safety factor with Project's structural engineer.  Revise to suit Project or insert specific load requirements and names of acceptable products.

1. Expansion Anchors:  Fabricated from corrosion-resistant materials, with capability to sustain, without failure, a load equal to 5 times design load, as determined by testing per ASTM E 488 conducted by a qualified testing agency.

Retain subparagraph below if power-actuated fasteners are acceptable.  Verify safety factor with Project's structural engineer.

2. Power-Actuated Anchors:  Fastener system of type suitable for application indicated, fabricated from corrosion-resistant materials, with capability to sustain, without failure, a load equal to 10 times design load, as determined by testing per ASTM E 1190 conducted by a qualified testing agency.

I. Sound Attenuation Blankets:  ASTM C 665, Type I (blankets without membrane facing), produced by combining thermosetting resins with mineral fibers manufactured from glass, slag wool, or rock wool.

1. Fire-Resistance-Rated Assemblies:  Comply with mineral-fiber requirements of assembly.

J. Acoustical Sealant:  As specified in Division 7 Section "Joint Sealants."

2.6 GYPSUM BOARD SHAFT-WALL ASSEMBLIES <Insert drawing designation; e.g., SW-1>

Copy and re-edit this Article for each gypsum board shaft-wall assembly required, and indicate locations of each on Drawings.  Delete requirements shown on Drawings.

Retain paragraph below, along with paragraph of same title in "Manufacturers" Article, for basis-of-design specification.  Verify that design designations are indicated on Drawings.

A. Basis-of-Design Product:  National Gypsum Company assembly indicated on Drawings by design designation of a qualified testing agency.

Edit first two paragraphs below to suit Project.

B. Fire-Resistance Rating:  [As indicated] [1 hour] [2 hours] [3 hours] [4 hours] <Insert rating>.

C. STC Rating:  [As indicated] [51, minimum] <Insert rating>.

D. Studs:  Manufacturer's standard profile for repetitive members, corner and end members, and fire-resistance-rated assembly indicated.

1. Depth:  [As indicated] [2-1/2 inches (64 mm)] [4 inches (102 mm)] [6 inches (152 mm)].

Edit subparagraph below for base-metal thickness.  Note that thicknesses offered by various manufacturers differ.  See the Evaluations for discussion of steel sheet thicknesses.

2. Minimum Base-Metal Thickness:  [As indicated] [0.0179 inch (0.45 mm)] [0.0220 inch (0.55 mm)] [0.0329 inch (0.84 mm)] <Insert value>.

E. Runner Tracks:  Manufacturer's standard J-profile track with long-leg length as standard with manufacturer, but at least [2 inches (51 mm)] <Insert dimension> long and in depth matching studs.

1. Minimum Base-Metal Thickness:  [As indicated] [Matching steel studs] [0.0179 inch (0.45 mm)] [0.0220 inch (0.55 mm)] [0.0329 inch (0.84 mm)] <Insert value>.

Paragraph below specifies firestop tracks for isolating partition framing from structure above in specific fire-resistance-rated assemblies.  If retaining, revise to coordinate with rated assemblies selected and indicate design designations of assemblies on Drawings.

F. Firestop Tracks:  Top runner manufactured to allow partition heads to expand and contract with movement of structure while maintaining continuity of fire-resistance-rated assembly indicated; in thickness not less than indicated for studs and in width to accommodate depth of studs.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  Retain one of two subparagraphs and list of manufacturers and products below.  See Division 1 Section "Product Requirements."

1. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

2. Products:  Subject to compliance with requirements, provide one of the following:

a. Dietrich Metal Framing; The System by Metal-Lite, Inc.

b. Fire Trak Corp.; Fire Trak[ attached to studs with Fire Trak Slip Clip].

c. <Insert manufacturer's name; product name or designation.>

Retain and edit first paragraph below for framing elevator hoistway entrances.  Note that thicknesses offered by various manufacturers differ.  See the Evaluations for discussion of steel sheet thicknesses.

G. Jamb Struts:  Manufacturer's standard J-profile strut with long-leg length of 3 inches (76 mm), in depth matching studs, and not less than [0.0329 inch (0.84 mm)] <Insert thickness> thick.

H. Room-Side Finish:  [As indicated] [Gypsum board] [Gypsum veneer plaster] [Cementitious backer units].

Generally delete paragraph above and below and show room- and shaft-side finishes on Drawings.

I. Shaft-Side Finish:  [As indicated] [As indicated by fire-resistance-rated assembly design designation].

Delete paragraph below if not applicable.

J. Insulation:  Sound attenuation blankets.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates to which gypsum board shaft-wall assemblies attach or abut, with Installer present, including hollow-metal frames, elevator hoistway door frames, cast-in anchors, and structural framing.  Examine for compliance with requirements for installation tolerances and other conditions affecting performance.

B. Examine panels before installation.  Reject panels that are wet, moisture damaged, or mold damaged.

C. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

Delete this Article if no sprayed fire-resistive materials.

A. Sprayed Fire-Resistive Materials:  Coordinate with gypsum board shaft-wall assemblies so both elements of Work remain complete and undamaged.  Patch or replace sprayed fire-resistive materials removed or damaged during installation of shaft-wall assemblies to comply with requirements specified in Division 7 Section "Sprayed Fire-Resistive Materials."

Detail requirements for attaching gypsum board assemblies to construction protected by sprayed fire-resistive materials on Drawings.

1. Before sprayed fire-resistive materials are applied, attach offset anchor plates or ceiling runner tracks to surfaces indicated to receive sprayed fire-resistive materials.  Where offset anchor plates are required, provide continuous plates fastened to building structure not more than 24 inches (610 mm) o.c.

B. After sprayed fire-resistive materials are applied, remove only to extent necessary for installation of gypsum board shaft-wall assemblies and without reducing the fire-resistive material thickness below that which is required to obtain fire-resistance rating indicated.  Protect remaining fire-resistive materials from damage.

3.3 INSTALLATION

A. General:  Install gypsum board shaft-wall assemblies to comply with requirements of fire-resistance-rated assemblies indicated, manufacturer's written installation instructions, and the following:

1. ASTM C 754 for installing steel framing except comply with framing spacing indicated.

2. Division 9 Section "[Gypsum Veneer Plastering] [Gypsum Board]" for applying and finishing panels.

Retain subparagraph below if exposed surfaces of shaft walls will receive ceramic tile finish.

3. Division 9 Section "Ceramic Tile" for cementitious backer units.

Retain first paragraph below for architectural or building expansion joints with gypsum board shaft-wall assemblies.  Include details on Drawings showing expansion-joint construction and locations.

B. Do not bridge architectural or building expansion joints with shaft-wall assemblies; frame both sides of expansion joints with furring and other support.

C. Install supplementary framing in gypsum board shaft-wall assemblies around openings and as required for blocking, bracing, and support of gravity and pullout loads of fixtures, equipment, services, heavy trim, furnishings, and similar items that cannot be supported directly by shaft-wall assembly framing.

Fully detail elevator hoistway openings in shaft-wall assemblies.  Manufacturers' written recommendations for framing elevator hoistway entrance door openings differ.  If retaining subparagraph below, revise to suit Project and assemblies selected.  Insert requirements for other openings to suit Project.

1. At elevator hoistway entrance door frames, provide jamb struts on each side of door frame.

Fully detail support for items attached to shaft-wall assemblies; subparagraph below is an example only.  If retaining, indicate size of reinforcing plate on Drawings.  Insert requirements for other items to suit Project.

2. Where handrails directly attach to gypsum board shaft-wall assemblies, provide galvanized steel reinforcing strip with [0.0312-inch (0.79-mm)] <Insert thickness> minimum thickness of base (uncoated) metal, accurately positioned and secured behind at least 1 [gypsum base for veneer plaster] [gypsum board] [cementitious backer unit] face-layer panel.

Delete paragraph below if no stair enclosures or if not applicable.

D. Integrate stair hanger rods with gypsum board shaft-wall assemblies by locating cavity of assemblies where required to enclose rods.

Fully detail items penetrating shaft-wall assemblies on Drawings.

E. At penetrations in shaft wall, maintain fire-resistance rating of shaft-wall assembly by installing supplementary steel framing around perimeter of penetration and fire protection behind boxes containing wiring devices, elevator call buttons, elevator floor indicators, and similar items.

See "Crack Control" Article in the Evaluations for discussion of assemblies subjected to differential structural movements.

F. Isolate perimeter of gypsum panels from building structure to prevent cracking of panels, while maintaining continuity of fire-rated construction.

If retaining paragraph below, indicate locations and details of firestop tracks on Drawings.

G. Firestop Tracks:  Where indicated, install to maintain continuity of fire-resistance-rated assembly indicated.

Generally retain first option in paragraph below and show joints on Drawings to comply with ASTM C 840 requirements for spacing control joints.

H. Control Joints:  Install control joints [at locations indicated on Drawings] [according to ASTM C 840 and in specific locations approved by Architect], while maintaining fire-resistance rating of gypsum board shaft-wall assemblies.

Revise first paragraph below to suit Project and details shown on Drawings.  Delete if sound or air leakage is not a concern.

I. Seal gypsum board shaft walls with acoustical sealant at perimeter of each assembly where it abuts other work and at joints and penetrations within each assembly.  Install acoustical sealant to withstand dislocation by air-pressure differential between shaft and external spaces; maintain an airtight and smoke-tight seal; and comply with ASTM C 919 requirements or with manufacturer's written instructions, whichever are more stringent.

J. In elevator shafts where gypsum board shaft-wall assemblies cannot be positioned within 4 inches (102 mm) of the shaft face of structural beams, floor edges, and similar projections into shaft, install 1/2- or 5/8-inch- (13- or 16-mm-) thick, gypsum board cants covering tops of projections.  No recesses allowed (at steel beams especially).

1. Slope cant panels at least 75 degrees from horizontal.  Set base edge of panels in adhesive and secure top edges to shaft walls at 24 inches (610 mm) o.c. with screws fastened to shaft-wall framing.

2. Where steel framing is required to support gypsum board cants, install framing at 24 inches (610 mm) o.c. and extend studs from the projection to shaft-wall framing.

Paragraph below is based on recommendation in ASTM C 840 for metal framing.

K. Installation Tolerance:  Install each framing member so fastening surfaces vary not more than 1/8 inch (3mm) from the plane formed by faces of adjacent framing.

3.4 PROTECTION

A. Protect installed products from damage from weather, condensation, direct sunlight, construction, and other causes during remainder of the construction period.

B. Remove and replace panels that are wet, moisture damaged, or mold damaged.

1. Indications that panels are wet or moisture damaged include, but are not limited to, discoloration, sagging, and irregular shape.

2. Indications that panels are mold damaged include, but are not limited to, fuzzy or splotchy surface contamination and discoloration.

END OF SECTION 09265

GYPSUM BOARD SHAFT-WALL ASSEMBLIES
09265 - 1

