Louisiana Army National Guard

Preliminary Review Documents
141st Readiness Center (RC)

Jackson Barracks, New Orleans, Louisiana

Technical Specifications


SECTION 05310 - STEEL DECK

PART 1  - GENERAL

1.1
SECTION INCLUDES

    A.
All steel decking as shown on the drawings.

    B.

Standing Seam Metal Roofing, if required by the drawings, is specified in Division 7.

1.2


QUALITY ASSURANCE 

    A.

Standard Specifications:  Except as modified or supplemented herein, the decking shall be designed in accordance with the latest edition of AISI "Specifications for the Design of Cold-Formed Steel Structural Members and all applicable requirements contained in "Design Manual for Composite Decks, Form Decks and Roof Decks" of the Steel Deck Institute, Inc.

B.

Testing – Contractor’s  independent testing laboratory shall witness all welded connections.

1.3

SUBMITTALS  

A.

Manufacturer's Data:  For information only, submit 2 copies of manufacturer's specifications and installation instructions for each type of decking and accessories.  Include manufacturer's certifications as may be required to show compliance with these specifications.

B.

Shop Drawings:   Submit detailed drawings showing layout and types of deck panels, anchorage details, and conditions requiring closure panels, supplementary framing, cut openings, special jointing or other accessories.

PART 2 - PRODUCTS

2.1

MATERIALS 

A.

Deck, Dimensions and Properties:  Dimensions and properties of the various types of deck are shown on the drawings. Deck configurations shall be similar to that of the decks called for on the drawings.  Allowable stresses shall be equal to that of the deck specified on the drawings.

B.

Deck Coating:  Galvanized, ASTM A525, G90.

C.

Miscellaneous Steel Shapes:   ASTM A36.

D.

Sheet Metal Accessories:  ASTM A 526, commercial quality, galvanized.

PART 3  - EXECUTION  

3.1

INSTALLATION

A.

Deck sheets shall be erected and welded to supports in accordance with the manufacturer's specifications and erection layouts and as required to resist the uplift loads, if any, noted on the drawings.

B.

Side joints must be fastened together in accordance with manufacturer's specifications.  Cutting openings through the deck less than 16 square feet in area, and all skew cutting shall be performed in the field.  Deck shall be continuous over three (3) or more spans.

C.

Except where other permanent type edge closures are shown on the drawings, provide sheet metal edge closures around the perimeter of all steel deck areas, including openings, where concrete is to be applied to the deck.  Deck closures shall be of proper gage and configuration to retain the wet concrete.

3.2

TOUCH-UP

 A.

All damaged coating, including welds, shall be touched up with an approved coating before placing fill.
END OF SECTION 05310
STEEL DECK
05310 - 2

