Copyright 2002 and 2005 AIA
MASTERSPEC Full Length
08/02 (R 05/05)

Copyright 2002 and 2005 (R 08/03) by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 042000 - UNIT MASONRY
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes unit masonry assemblies consisting of the following:

Adjust list below to suit Project.

1. Concrete masonry units (CMUs).

2. Decorative concrete masonry units.

3. Pre-faced concrete masonry units.

4. Concrete brick.

5. Face brick.

6. Building (common) brick.

7. Hollow brick.

8. Glazed brick.

9. Structural-clay facing tile.

10. Firebox brick.

11. Clay flue lining units.

12. Stone trim units.

13. Mortar and grout.

14. Reinforcing steel.

15. Masonry joint reinforcement.

16. Ties and anchors.

17. Embedded flashing.

18. Miscellaneous masonry accessories.

19. Masonry-cell insulation.

20. Cavity-wall insulation.

B. Related Sections include the following:

List below only products, construction, and equipment that the reader might expect to find in this Section but are specified elsewhere.

1. Division 04 Section "Glass Unit Masonry" for glass block.

2. Division 07 Section "Bituminous Dampproofing" for dampproofing applied to cavity face of backup wythes of cavity walls.

3. Division 07 Section "Water Repellents" for water repellents applied to unit masonry assemblies.

Coordinate first subparagraph below with referenced Section.  Metal through-wall flashing is included in Division 07 Section "Sheet Metal Flashing and Trim" and in this Section.

4. Division 07 Section "Sheet Metal Flashing and Trim" for[ exposed] sheet metal flashing.

5. Division 07 Section "Penetration Firestopping" for firestopping at openings in masonry walls.

6. Division 07 Section "Fire-Resistive Joint Systems" for fire-resistive joint systems at heads of masonry walls.

7. Division 07 Section "Joint Sealants" for sealing control and expansion joints in unit masonry.

8. Division 08 Section "Louvers and Vents" for wall vents (brick vents).

9. Division 09 Section "Brick Flooring" for interior brick flooring.

10. Division 09 Section "Chemical-Resistant Brick Flooring" for chemical-resistant, interior brick flooring.

11. Division 09 Section "Stone Facing" for stone window stools.

12. Division 32 Section "Unit Paving" for exterior unit masonry paving.

13. Division 32 Section "Segmental Retaining Walls" for dry-laid, concrete unit retaining walls.

C. Products furnished, but not installed, under this Section include the following:

Two subparagraphs below are examples only.  Revise to suit Project.

Usually delete subparagraph below and specify in concrete Section.

1. Dovetail slots for masonry anchors, installed under Division 03 Section "Cast-in-Place Concrete."

Delete subparagraph below if installation of anchor sections is included in this Section.

2. Anchor sections of adjustable masonry anchors for connecting to structural frame, installed under Division 05 Section "Structural Steel Framing."

D. Products installed, but not furnished, under this Section include the following:

Three subparagraphs below are examples only.  Revise to suit Project.

1. Cast-stone trim, furnished under Division 04 Section "Cast Stone Masonry."

2. Steel [lintels] [and] [shelf angles] for unit masonry, furnished under Division 05 Section "Metal Fabrications."

3. Manufactured reglets in masonry joints for metal flashing, furnished under Division 07 Section "Sheet Metal Flashing and Trim."

Retain paragraph and subparagraphs below if allowances are specified for brick selection or for masonry testing.

E. Allowances:  The following are included under the allowances indicated as specified in Division 01 Section "Allowances":

Revise subparagraph below if allowances are required for other types of masonry units.  Include separate allowances for special shapes if required.

1. Face brick under the Face Brick Allowances.

Retain subparagraph below if testing is paid for by Contractor under an allowance.

2. [Preconstruction] [source quality-control] [and] [field quality-control] testing under Testing and Inspecting Allowance.

1.3 DEFINITIONS

Retain terms that remain after this Section has been edited.

A. Reinforced Masonry:  Masonry containing reinforcing steel in grouted cells.

1.4 PERFORMANCE REQUIREMENTS

Retain this Article if required for masonry designed by analytical methods.  See Editing Instruction No. 2 in the Evaluations.  Revise first paragraph below and insert required compressive strength of masonry if not indicated on Drawings.

A. Provide[ structural] unit masonry that develops indicated net-area compressive strengths (f'm) at 28 days.

B. Determine net-area compressive strength (f'm) of masonry from average net-area compressive strengths of masonry units and mortar types (unit-strength method) according to [Tables 1 and 2 in ACI 530.1/ASCE 6/TMS 602] [Table 21-D in the Uniform Building Code].

Retain paragraph above or below.  See Editing Instruction No. 2 in the Evaluations.

C. Determine net-area compressive strength (f'm) of masonry by testing masonry prisms according to [ASTM C 1314] [UBC Standard 21-17].

1.5 SUBMITTALS

A. Product Data:  For each type of product indicated.

B. Shop Drawings:  For the following:

Delete subparagraph below if considered unnecessary.

1. Masonry Units:  Show sizes, profiles, coursing, and locations of special shapes.

Delete subparagraph below if stone trim is not used.

2. Stone Trim Units:  Show sizes, profiles, and locations of each stone trim unit required.

Delete subparagraph below if reinforcing bars are not used.

3. Reinforcing Steel:  Detail bending and placement of unit masonry reinforcing bars.  Comply with ACI 315, "Details and Detailing of Concrete Reinforcement."[  Show elevations of reinforced walls.]

Delete subparagraph below if flashing material selected is not specially fabricated for corners, end dams, etc.

4. Fabricated Flashing:  Detail corner units, end-dam units, and other special applications.

C. Samples for Initial Selection:  For the following:

1. Decorative concrete masonry units, in the form of small-scale units.

2. Face brick, in the form of straps of five or more bricks.

3. Colored mortar.

4. Weep holes/vents.

Delete paragraph and subparagraphs above if colors and textures are preselected and specified or scheduled.  Retain paragraph and subparagraphs below with or without above.

D. Samples for Verification:  For each type and color of the following:

Revise or expand 10 subparagraphs below to suit Project.

1. [Exposed] [Decorative] concrete masonry units.

2. Pre-faced concrete masonry units.

3. [Face] [Hollow] brick[, in the form of straps of five or more bricks].

4. Special brick shapes.

5. Glazed brick.

6. Glazed structural-clay tile.

Delete subparagraph below if colored mortar is not used.

7. [Pigmented] [and] [colored-aggregate] mortar.  Make Samples using same sand and mortar ingredients to be used on Project.[  Label Samples to indicate types and amounts of pigments used.]

Delete first subparagraph below if stone trim is not used.

8. Stone trim.

9. Weep holes/vents.

10. Accessories embedded in masonry.

Retain paragraph and subparagraph below for critical work where record of mockup materials is desired.

E. List of Materials Used in Constructing Mockups:  List generic product names together with manufacturers, manufacturers' product names, model numbers, lot numbers, batch numbers, source of supply, and other information as required to identify materials used.  Include mix proportions for mortar and grout and source of aggregates.

1. Submittal is for information only.  Neither receipt of list nor approval of mockup constitutes approval of deviations from the Contract Documents unless such deviations are specifically brought to the attention of Architect and approved in writing.

Retain paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

F. Qualification Data:  For testing agency.

Usually retain paragraph and appropriate subparagraphs below.  See Editing Instruction No. 3 in the Evaluations for information on material certificates.

G. Material Certificates:  Include statements of material properties indicating compliance with requirements including compliance with standards and type designations within standards.  Provide for each type and size of the following:

1. Masonry units.

Retain first subparagraph below if required by authorities having jurisdiction or if the added assurance of quality that test reports provide is desired.

a. Include material test reports substantiating compliance with requirements.

b. For bricks, include size-variation data verifying that actual range of sizes falls within specified tolerances.

c. For exposed brick, include material test report for efflorescence according to ASTM C 67.

d. For surface-coated brick, include material test report for durability of surface appearance after 50-cycles of freezing and thawing per ASTM C 67[ or a list of addresses of buildings in Project's area where proposed brick has been used successfully and with a history of durability].

Retain first subparagraph below only if retaining unit-strength method in "Performance Requirements" Article or if requirements for average net-area compressive strength of units are retained in Part 2.

e. For masonry units used in structural masonry, include data and calculations establishing average net-area compressive strength of units.

2. Cementitious materials.  Include brand, type, and name of manufacturer.

3. Preblended, dry mortar mixes.  Include description of type and proportions of ingredients.

Retain first subparagraph below if one-half the allowable stresses are used for design of masonry under the 1997 Uniform Building Code and unit-strength method is used.

4. Grout mixes.  Include description of type and proportions of ingredients.

5. Reinforcing bars.

6. Joint reinforcement.

7. Anchors, ties, and metal accessories.

Requirements in paragraph and subparagraphs below are from the 2002 MSJC Specification.

H. Mix Designs:  For each type of mortar[ and grout].  Include description of type and proportions of ingredients.

1. Include test reports, per [ASTM C 780] [UBC Standard 21-16], for mortar mixes required to comply with property specification.

2. Include test reports, per [ASTM C 1019] [UBC Standard 21-18], for grout mixes required to comply with compressive strength requirement.

Retain paragraph below only if retaining unit-strength method in "Performance Requirements" Article.

I. Statement of Compressive Strength of Masonry:  For each combination of masonry unit type and mortar type, provide statement of average net-area compressive strength of masonry units, mortar type, and resulting net-area compressive strength of masonry determined according to [Tables 1 and 2 in ACI 530.1/ASCE 6/TMS 602] [Table 21-D in the Uniform Building Code].

Delete paragraph below if not required.

J. Cold-Weather Procedures:  Detailed description of methods, materials, and equipment to be used to comply with cold-weather requirements.

1.6 QUALITY ASSURANCE

Retain first paragraph below if Contractor or manufacturer selects testing agency.

A. Testing Agency Qualifications:  An independent agency qualified according to ASTM C 1093 for testing indicated, as documented according to ASTM E 548.

B. Source Limitations for Masonry Units:  Obtain exposed masonry units of a uniform texture and color, or a uniform blend within the ranges accepted for these characteristics, through one source from a single manufacturer for each product required.

C. Source Limitations for Mortar Materials:  Obtain mortar ingredients of a uniform quality, including color for exposed masonry, from a single manufacturer for each cementitious component and from one source or producer for each aggregate.

See Editing Instruction No. 3 in the Evaluations for information on preconstruction testing.

D. Preconstruction Testing Service:  Owner will engage a qualified independent testing agency to perform preconstruction testing indicated below.  Payment for these services will be made [by Owner] [from the Testing and Inspecting Allowance, as authorized by Change Orders].  Retesting of materials that fail to meet specified requirements shall be done at Contractor's expense.

Usually delete four subparagraphs below if retaining prism test.

1. Clay Masonry Unit Test:  For each type of unit required, per ASTM C 67.

2. Concrete Masonry Unit Test:  For each type of unit required, per ASTM C 140.

Delete subparagraph below if mortar is specified to comply with proportion specification.

3. Mortar Test (Property Specification):  For each mix required, per [ASTM C 780] [UBC Standard 21-16].

Delete subparagraph below if grout is specified by proportions stated in ASTM C 476 or UBC Standard 21-19 rather than by compressive strength.

4. Grout Test (Compressive Strength):  For each mix required, per [ASTM C 1019] [UBC Standard 21-18].

Usually select from test methods in four subparagraphs above.  Retain subparagraph below only if prism test is specified, in "Performance Requirements" Article, for determining compressive strength of masonry.

5. Prism Test:  For each type of construction required, per [ASTM C 1314] [UBC Standard 21-17].

Delete first paragraph below if fire-rated masonry is not used.

E. Fire-Resistance Ratings:  Where indicated, provide materials and construction identical to those of assemblies with fire-resistance ratings determined per ASTM E 119 by a testing and inspecting agency, by equivalent concrete masonry thickness, or by other means, as acceptable to authorities having jurisdiction.

F. Sample Panels:  Build sample panels to verify selections made under sample submittals and to demonstrate aesthetic effects.  Comply with requirements in Division 01 Section "Quality Requirements" for mockups.

1. Build sample panels for [each type of exposed unit masonry construction] [typical exterior wall] [typical interior wall] [typical exterior and interior walls] in sizes approximately [48 inches (1200 mm)] [60 inches (1500 mm)] <Insert size> long by [48 inches (1200 mm)] <Insert size> high[ by full thickness].

Delete first subparagraph below if not applicable.

2. Where masonry is to match existing, erect panels adjacent and parallel to existing surface.

3. Clean[ one-half of] exposed faces of panels with masonry cleaner indicated.

4. Protect approved sample panels from the elements with weather-resistant membrane.

5. Approval of sample panels is for color, texture, and blending of masonry units; relationship of mortar and sealant colors to masonry unit colors; tooling of joints; aesthetic qualities of workmanship; and other material and construction qualities specifically approved by Architect in writing.

a. Approval of sample panels does not constitute approval of deviations from the Contract Documents contained in sample panels unless such deviations are specifically approved by Architect in writing.

Usually retain sample panel requirements above and delete mockup requirements below.  Revise wording if only one mockup is required.

G. Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects[ and set quality standards for materials and execution].

Retain subparagraph below for large-scale mockup or include in Division 01 Section "Quality Requirements."  Indicate on Drawings' portion of wall represented by mockup or draw mockup as separate element.

1. Build mockup of typical wall area as shown on Drawings.

Retain subparagraph and associated subparagraphs below for limited mockups.

2. Build mockups for [each type of exposed unit masonry construction] [typical exterior wall] [typical interior wall] [typical exterior and interior walls] in sizes approximately [48 inches (1200 mm)] [60 inches (1500 mm)] [72 inches (1800 mm)] [96 inches (2400 mm)] <Insert size> long by [48 inches (1200 mm)] [60 inches (1500 mm)] [72 inches (1800 mm)] <Insert size> high by full thickness, including face and backup wythes and accessories.

a. Include a sealant-filled joint at least 16 inches (400 mm) long in [each] [exterior wall] [each exterior wall] mockup.

Delete any of four subparagraphs below that do not apply or are not required.

b. Include lower corner of window opening[ framed with stone trim] at upper corner of exterior wall mockup.  Make opening approximately 12 inches (300 mm) wide by 16 inches (400 mm) high.

Retain first subparagraph below to show materials and methods used for through-wall flashing if required.

c. Include through-wall flashing installed for a 24-inch (600-mm) length in corner of exterior wall mockup approximately 16 inches (400 mm) down from top of mockup, with a 12-inch (300-mm) length of flashing left exposed to view (omit masonry above half of flashing).

d. Include [metal] [wood] studs, sheathing, veneer anchors, flashing, and weep holes in exterior masonry-veneer wall mockup.

e. Include [glazed structural-clay tile] [pre-faced concrete masonry units] on one face of interior unit masonry wall mockup.

Delete first subparagraph below if not applicable.

3. Where masonry is to match existing, erect mockups adjacent and parallel to existing surface.

4. Clean[ one-half of] exposed faces of mockups with masonry cleaner as indicated.

5. Protect accepted mockups from the elements with weather-resistant membrane.

6. Approval of mockups is for color, texture, and blending of masonry units; relationship of mortar and sealant colors to masonry unit colors; tooling of joints; and aesthetic qualities of workmanship.

Delete subparagraphs below if mockups are only for establishing appearance factors.

a. Approval of mockups is also for other material and construction qualities specifically approved by Architect in writing.

b. Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless such deviations are specifically approved by Architect in writing.

Retain subparagraph below if mockups are erected as part of building rather than separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

7. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 01.

H. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 01 Section "Project Management and Coordination."

1.7 DELIVERY, STORAGE, AND HANDLING

A. Store masonry units on elevated platforms in a dry location.  If units are not stored in an enclosed location, cover tops and sides of stacks with waterproof sheeting, securely tied.  If units become wet, do not install until they are dry.

Delete two paragraphs below if a preblended, dry mortar mix is required.

B. Store cementitious materials on elevated platforms, under cover, and in a dry location.  Do not use cementitious materials that have become damp.

C. Store aggregates where grading and other required characteristics can be maintained and contamination avoided.

Generally retain first paragraph below because there is nothing in this Section that would prohibit Contractor from using a preblended, dry mortar mix.

D. Deliver preblended, dry mortar mix in moisture-resistant containers designed for lifting and emptying into dispensing silo.  Store preblended, dry mortar mix in delivery containers on elevated platforms, under cover, and in a dry location or in a metal dispensing silo with weatherproof cover.

E. Store masonry accessories, including metal items, to prevent corrosion and accumulation of dirt and oil.

1.8 PROJECT CONDITIONS

A. Protection of Masonry:  During construction, cover tops of walls, projections, and sills with waterproof sheeting at end of each day's work.  Cover partially completed masonry when construction is not in progress.

Increase extent of cover in first subparagraph below as needed to suit local climatic conditions.

1. Extend cover a minimum of 24 inches (600 mm) down both sides and hold cover securely in place.

2. Where 1 wythe of multiwythe masonry walls is completed in advance of other wythes, secure cover a minimum of 24 inches (600 mm) down face next to unconstructed wythe and hold cover in place.

B. Do not apply uniform floor or roof loads for at least 12 hours and concentrated loads for at least 3 days after building masonry walls or columns.

C. Stain Prevention:  Prevent grout, mortar, and soil from staining the face of masonry to be left exposed or painted.  Immediately remove grout, mortar, and soil that come in contact with such masonry.

1. Protect base of walls from rain-splashed mud and from mortar splatter by spreading coverings on ground and over wall surface.

2. Protect sills, ledges, and projections from mortar droppings.

3. Protect surfaces of window and door frames, as well as similar products with painted and integral finishes, from mortar droppings.

4. Turn scaffold boards near the wall on edge at the end of each day to prevent rain from splashing mortar and dirt onto completed masonry.

D. Cold-Weather Requirements:  Do not use frozen materials or materials mixed or coated with ice or frost.  Do not build on frozen substrates.  Remove and replace unit masonry damaged by frost or by freezing conditions.  Comply with cold-weather construction requirements contained in [ACI 530.1/ASCE 6/TMS 602] [Section 2104.3 in the Uniform Building Code].

1. Cold-Weather Cleaning:  Use liquid cleaning methods only when air temperature is 40 deg F (4 deg C) and above and will remain so until masonry has dried, but not less than 7 days after completing cleaning.

E. Hot-Weather Requirements:  Comply with hot-weather construction requirements contained in ACI 530.1/ASCE 6/TMS 602.

PART 2 -  PRODUCTS

2.1 MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

Edit this Article with other Part 2 articles in which manufacturers and products, or manufacturers only, are named.  See Division 01 Section "Product Requirements" for an explanation of the terms "Available Products," "Products," "Available Manufacturers," and "Manufacturers" and the effect these terms have on "Comparable Product" and "Product Substitution" requirements.

A. In other Part 2 articles where titles below introduce lists, the following requirements apply to product selection:

1. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, products specified.

2. Products:  Subject to compliance with requirements, provide one of the products specified.

3. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, manufacturers specified.

4. Manufacturers:  Subject to compliance with requirements, provide products by one of the manufacturers specified.

2.2 MASONRY UNITS, GENERAL

A. Defective Units:  Referenced masonry unit standards may allow a certain percentage of units to exceed tolerances and to contain chips, cracks, or other defects exceeding limits stated in the standard.  Do not uses units where such defects, including dimensions that vary from specified dimensions by more than stated tolerances, will be exposed in the completed Work or will impair the quality of completed masonry.

2.3 CONCRETE MASONRY UNITS (CMUs)

A. Shapes:  Provide shapes indicated and as follows:

On Drawings, show details of special conditions and special shapes needed.  Revise first subparagraph below to suit Project.

1. Provide special shapes for lintels, corners, jambs, sashes, movement joints, headers, bonding, and other special conditions.

2. Provide [square-edged] [bullnose] units for outside corners, unless otherwise indicated.

Retain first paragraph and subparagraphs below for increased water resistance of units if required.  If retaining, also retain water-repellent mortar admixture.

B. Integral Water Repellent:  Provide units made with integral water repellent [for exposed units] [and] [where indicated].

1. Integral Water Repellent:  Liquid polymeric, integral water-repellent admixture that does not reduce flexural bond strength.  Units made with integral water repellent, when tested as a wall assembly made with mortar containing integral water-repellent manufacturer's mortar additive according to ASTM E 514, with test period extended to 24 hours, show no visible water or leaks on the back of test specimen.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Addiment Incorporated; Block Plus W-10.

2) Grace Construction Products, a unit of W. R. Grace & Co. - Conn.; Dry-Block.

3) Master Builders, Inc.; Rheopel.

4) <Insert manufacturer's name; product name or designation.>

C. Concrete Masonry Units:  [ASTM C 90] [UBC Standard 21-4].

See Editing Instruction No. 2 in the Evaluations before selecting unit compressive strength in subparagraph below.  Usually delete below if retaining Part 1 "Performance Requirements" Article.  Minimum average net-area compressive strength per ASTM C 90 is 1900 psi (13.1 MPa).

1. Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of [1900 psi (13.1 MPa)] [2150 psi (14.8 MPa)] [2800 psi (19.3 MPa)] [3050 psi (21.0 MPa)] <Insert value>.

See Editing Instruction No. 4 in the Evaluations before selecting weight classification in subparagraph below.  Select one of three weights or delete subparagraph for Contractor's option.  Select last option for default requirement if more than one weight is used.

2. Weight Classification:  [Lightweight] [Medium weight] [Normal weight][, unless otherwise indicated].

If selecting UBC Standard 21-4 in paragraph above and Type I moisture-controlled units are required, insert a subparagraph here stating that requirement after verifying local availability of Type I units.  ASTM C 90 no longer includes requirements for moisture-controlled units.

3. Size (Width):  Manufactured to dimensions 3/8 inch less than nominal dimensions.

Retain subparagraph above if IP dimensions are used; retain below if SI (metric) dimensions are used.

4. Size (Width):  Manufactured to the following dimensions:

First of each pair of options in six subparagraphs below is a metric size, second is equivalent metric dimension for IP size.  If retaining first options, verify availability.

a. 100 mm nominal; [90] [92] mm actual.

b. 150 mm nominal; [140] [143] mm actual.

c. 200 mm nominal; [190] [194] mm actual.

d. 250 mm nominal; [240] [244] mm actual.

e. 300 mm nominal; [290] [295] mm actual.

f. 400 mm nominal; [390] [396] mm actual.

Delete subparagraph below if color and texture of faces are not critical.  ASTM C 90 requires at least four units for sample, representing the range of color and texture permitted.

5. Exposed Faces:  Provide color and texture matching the range represented by Architect's sample.

Retain subparagraph below if direct application of plaster is used.

6. Faces to Receive Plaster:  Where units are indicated to receive a direct application of plaster, provide textured-face units made with gap-graded aggregates.

Insert ASTM C 129 or UBC Standard 21-5 for non-load-bearing concrete masonry units if desired; they are not usually an inventory item and may have to be ordered in large quantities.  Indicate load-bearing and non-load-bearing units on Drawings if both are specified.

D. Decorative Concrete Masonry Units:  [ASTM C 90] [UBC Standard 21-4].

See Editing Instruction No. 2 in the Evaluations before selecting unit compressive strength in subparagraph below.  Usually delete below if retaining Part 1 "Performance Requirements" Article.  Minimum average net-area compressive strength per ASTM C 90 is 1900 psi (13.1 MPa).

1. Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of [1900 psi (13.1 MPa)] [2150 psi (14.8 MPa)] [2800 psi (19.3 MPa)] [3050 psi (21.0 MPa)] <Insert value>.

See Editing Instruction No. 4 in the Evaluations before selecting weight classification in subparagraph below.  Select one of three weights.  Weight classification affects appearance and water absorption.

2. Weight Classification:  [Lightweight] [Medium weight] [Normal weight].

If selecting UBC Standard 21-4 in paragraph above and Type I moisture-controlled units are required, insert a subparagraph here stating that requirement after verifying local availability of Type I units.  ASTM C 90 no longer includes requirements for moisture-controlled units.

3. Size (Width):  Manufactured to dimensions specified in "Concrete Masonry Units" Paragraph above.

4. Pattern and Texture:

Select from five subparagraphs below and revise to suit Project.  Retain option if appearance is critical.

a. Standard pattern, ground finish.[  Match Architect's samples.]

b. Standard pattern, split-face finish.[  Match Architect's samples.]

c. Standard pattern, split-ribbed finish.[  Match Architect's samples.]

d. Scored vertically so units laid in running bond appear as square units laid in stacked bond, standard finish.[  Match Architect's samples.]

e. Triple scored vertically so units laid in running bond appear as vertical units laid in stacked bond (soldier courses), standard finish.[  Match Architect's samples.]

Select one of three options in subparagraph below.  If selecting first, indicate colors in a separate schedule.

5. Colors:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Retain subparagraph below if special aggregate is required to match sample.

6. Special Aggregate:  Provide units made with aggregate matching aggregate in Architect's sample.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

Revise paragraph below if medium- or normal-weight units are required.

E. Pre-faced Concrete Masonry Units:  Lightweight [hollow] [solid] concrete units complying with [ASTM C 90] [UBC Standard 21-4], with manufacturer's standard smooth resinous facing complying with ASTM C 744.

See Editing Instruction No. 2 in the Evaluations before selecting unit compressive strength in subparagraph below.  Usually delete below if retaining Part 1 "Performance Requirements" Article.  Minimum average net-area compressive strength per ASTM C 90 is 1900 psi (13.1 MPa).

1. Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of [1900 psi (13.1 MPa)] [2150 psi (14.8 MPa)] [2800 psi (19.3 MPa)] [3050 psi (21.0 MPa)] <Insert value>.

If selecting UBC Standard 21-4 in paragraph above and Type I moisture-controlled units are required, insert a subparagraph here stating that requirement after verifying local availability of Type I units.  ASTM C 90 no longer includes requirements for moisture-controlled units.

2. Size:  Manufactured to dimensions specified in "Concrete Masonry Units" Paragraph above, but with pre-faced surfaces having 1/16-inch- (1.5-mm-) wide returns of facing to create 1/4-inch- (6.5-mm-) wide mortar joints with modular coursing.

Select one of three options in subparagraph below.  If selecting first, indicate colors and patterns in a separate schedule.

3. Colors and Patterns:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

4. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

Insert other forms of block, e.g., sound absorbing, preinsulated, etc., where required.

F. Concrete Building Brick:  [ASTM C 55] [UBC Standard 21-3].

See Editing Instruction No. 2 in the Evaluations before selecting unit compressive strength in subparagraph below.  Usually delete below if retaining Part 1 "Performance Requirements" Article.  Minimum average net-area compressive strength per ASTM C 55 is 2500 psi (17.3 MPa) for Grade S and 3500 psi (24.1 MPa) for Grade N.

1. Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of [2500 psi (17.3 MPa)] [3500 psi (24.1 MPa)] <Insert value>.

See Editing Instruction No. 4 in the Evaluations before selecting weight classification in subparagraph below.  Select one of three weights or delete subparagraph for Contractor's option.

2. Weight Classification:  [Lightweight] [Medium weight] [Normal weight].

If selecting UBC Standard 21-3 in paragraph above and Type I moisture-controlled units are required, insert a subparagraph here stating that requirement after verifying local availability of Type I units.  ASTM C 90 no longer includes requirements for moisture-controlled units.

Select one size from options in two subparagraphs below, or delete both subparagraphs for Contractor's option if concrete brick is required only to adjust dimensions in concrete masonry unit construction.

3. Size (Actual Dimensions):  3-5/8 inches (92 mm) wide by [2-1/4 inches (57 mm)] [2-3/4 inches (70 mm)] [3-5/8 inches (92 mm)] high by 7-5/8 inches (194 mm) long.

Retain subparagraph above for IP sizes with equivalent SI (metric) dimensions or subparagraph below for products manufactured to metric sizes.  If retaining below, verify availability of sizes.

4. Size (Actual Dimensions):  90 mm wide by [57] [70] [90] mm high by 190 mm long.

2.4 [CONCRETE] [AND] [MASONRY] LINTELS

Delete paragraph below if not allowed.

A. General:  Provide either concrete or masonry lintels, at Contractor's option, complying with requirements below.

Three paragraphs below require that reinforcement be indicated on Drawings.

B. Concrete Lintels:  Precast units made from concrete matching concrete masonry units in color, texture, and compressive strength and with reinforcing bars indicated or required to support loads indicated.  Cure precast lintels by same method used for concrete masonry units.

Retain paragraph above or first paragraph below, depending on appearance desired.

C. Concrete Lintels:  Precast or formed-in-place concrete lintels complying with requirements in Division 03 Section "Cast-in-Place Concrete."

D. Masonry Lintels:  Prefabricated or built-in-place masonry lintels made from bond beam concrete masonry units with reinforcing bars placed as indicated and filled with coarse grout.  Cure precast lintels before handling and installing.  Temporarily support built-in-place lintels until cured.

2.5 BRICK

A. General:  Provide shapes indicated and as follows:

1. For ends of sills and caps and for similar applications that would otherwise expose unfinished brick surfaces, provide units without cores or frogs and with exposed surfaces finished.

On Drawings, show details of special conditions and special shapes required.  Revise three subparagraphs below to suit Project.

2. Provide special shapes for applications where stretcher units cannot accommodate special conditions, including those at corners, movement joints, bond beams, sashes, and lintels.

3. Provide special shapes for applications requiring brick of size, form, color, and texture on exposed surfaces that cannot be produced by sawing.

4. Provide special shapes for applications where shapes produced by sawing would result in sawed surfaces being exposed to view.

Select one of two grades in paragraph below, usually the first, and one of three types to match brick selected.  See Editing Instructions No. 5 and No. 6 in the Evaluations.

B. Face Brick:  [ASTM C 216] [UBC Standard 21-1], Grade [SW] [MW or SW], Type [FBX] [FBS] [FBA].

See Editing Instruction No. 2 in the Evaluations before selecting unit compressive strength in subparagraph below.  Usually delete below if retaining Part 1 "Performance Requirements" Article.  Below is based on net area, as in Table 1 in the 2002 MSJC Specification, rather than gross area reported by ASTM C 67.  Minimum average gross-area compressive strength per ASTM C 216 is 3000 psi (20.7 MPa) for Grade SW and 2500 psi (17.2 MPa) for Grade MW.

1. Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of [3000 psi (20.7 MPa)] [4400 psi (30.3 MPa)] [5500 psi (37.9 MPa)] [6400 psi (44.1 MPa)] [8000 psi (55.2 MPa)] [8400 psi (57.9 MPa)] <Insert value>.

Consider retaining first subparagraph below; it eliminates the need to wet brick before laying.  Before retaining, verify that brick selected complies with requirements.  See Evaluations.

2. Initial Rate of Absorption:  Less than 30 g/30 sq. in. (30 g/194 sq. cm) per minute when tested per ASTM C 67.

3. Efflorescence:  Provide brick that has been tested according to ASTM C 67 and is rated "not effloresced."

Delete subparagraph below if surface-coated brick is not used.

4. Surface Coating:  Brick with colors or textures produced by application of coatings shall withstand 50 cycles of freezing and thawing per ASTM C 67 with no observable difference in the applied finish when viewed from 10 feet (3 m)[ or shall have a history of successful use in Project's area].

Sizes in remaining subparagraphs are examples only.  Verify availability of sizes with local suppliers and revise to suit Project.

Select from 3 subparagraphs below for 3 courses in 8 inches (203 mm).

5. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-1/4 inches (57 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-1/4 inches (57 mm) high by 7-5/8 inches (194 mm) long].

6. Size (Actual Dimensions):  [3-1/2 inches (89 mm)] [or] [3-5/8 inches (92 mm)] wide by 2-1/4 inches (57 mm) high by 8 inches (203 mm) long.

7. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-1/4 inches (57 mm) high by 11-1/2 inches (292 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-1/4 inches (57 mm) high by 11-5/8 inches (295 mm) long].

Select from two subparagraphs below for nominal bed depth of 3 inches (75 mm) and 5 courses in 16 inches (406 mm).

8. Size (Actual Dimensions):  [2-3/4 inches (70 mm) wide by 2-3/4 inches (70 mm) high by 8 inches (203 mm) long] [or] [3 inches (76 mm) wide by 2-3/4 inches (70 mm) high by 8 inches (203 mm) long].

9. Size (Actual Dimensions):  [2-3/4 inches (70 mm) wide by 2-5/8 inches (67 mm) high by 9-5/8 inches (244 mm) long] [or] [3 inches (76 mm) wide by 2-3/4 inches (70 mm) high by 9-5/8 inches (244 mm) long].

Select from four subparagraphs below for nominal bed depth of 4 inches (100 mm) and 5 courses in 16 inches (406 mm).

10. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-3/4 inches (70 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-13/16 inches (71 mm) high by 7-5/8 inches (194 mm) long].

11. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-3/4 inches (70 mm) high by 8 inches (203 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-13/16 inches (71 mm) high by 8 inches (203 mm) long].

12. Size (Actual Dimensions):  3-5/8 inches (92 mm) wide by 2-5/8 inches (67 mm) high by 9-5/8 inches (244 mm) long.

13. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-3/4 inches (70 mm) high by 11-1/2 inches (292 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-13/16 inches (71 mm) high by 11-5/8 inches (295 mm) long].

Select subparagraph below for nominal bed depth of 3 inches (75 mm) and course height of 4 inches (102 mm).

14. Size (Actual Dimensions):  3 inches (76 mm) wide by 3-5/8 inches (92 mm) high by 11-5/8 inches (295 mm) long.

Select from two subparagraphs below for nominal bed depth of 4 inches (100 mm) and course height of 4 inches (102 mm).

15. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 3-1/2 inches (89 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 3-5/8 inches (92 mm) high by 7-5/8 inches (194 mm) long].

16. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 3-1/2 inches (89 mm) high by 11-1/2 inches (292 mm) long] [or] [3-5/8 inches (92 mm) wide by 3-5/8 inches (92 mm) high by 11-5/8 inches (295 mm) long].

Select subparagraph below for square brick, 8 inches (203 mm) in nominal size.

17. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 7-1/2 inches (190 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 7-5/8 inches (194 mm) high by 7-5/8 inches (194 mm) long].

Select from 13 subparagraphs above for IP sizes with equivalent SI (metric) dimensions or first subparagraph below for products manufactured to metric sizes.

18. Size (Actual Dimensions):  90 mm wide by [57] [70] [90] [190] mm high by [190] [290] mm long.

19. Application:  Use where brick is exposed, unless otherwise indicated.

20. [Where shown to "match existing,"  ]provide face brick matching color range, texture, and size of existing adjacent brickwork.

a. <Insert information on existing brick if known.>

Delete subparagraph below if brick is specified by product name.  First three options are examples of descriptive requirements for appearance where proprietary specifications and allowances cannot be used.  Select last option if allowance is used.

21. Color and Texture:  [Medium brown, wire-cut] [Full-range red, sand molded] [Buff, velour] [Match Architect's samples] [As selected by Architect].

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

22. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation for acceptable face brick.>

Select one of three grades in paragraph below, usually the first unless brick is not exposed to weather.  See Editing Instruction No. 5 in the Evaluations.

C. Building (Common) Brick:  [ASTM C 62] [UBC Standard 21-1], Grade [SW] [MW or SW] [NW, MW, or SW].

See Editing Instruction No. 2 in the Evaluations before selecting unit compressive strength in subparagraph below.  Usually delete below if retaining Part 1 "Performance Requirements" Article.  Below is based on net area, as in Table 1 in the 2002 MSJC Specification, rather than gross area reported by ASTM C 67.  Minimum average gross-area compressive strength per ASTM C 62 is 3000 psi (20.7 MPa) for Grade SW, 2500 psi (17.2 MPa) for Grade MW, and 1500 psi (10.3 MPa) for Grade NW.

1. Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of [3000 psi (20.7 MPa)] [4400 psi (30.3 MPa)] [5500 psi (37.9 MPa)] [6400 psi (44.1 MPa)] [8000 psi (55.2 MPa)] [8400 psi (57.9 MPa)] <Insert value>.

Retain one of three subparagraphs below or delete all three for Contractor's option if size is unimportant.

2. Size:  Match size of face brick.

3. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-1/4 inches (57 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-1/4 inches (57 mm) high by 7-5/8 inches (194 mm) long].

Retain subparagraph above for IP sizes with equivalent SI (metric) dimensions or subparagraph below for products manufactured to metric sizes.  Revise either to suit Project.

4. Size (Actual Dimensions):  90 mm wide by 57 mm high by 190 mm long.

Revise subparagraph below if building brick is used in exposed locations.

5. Application:  Use where brick is indicated for concealed locations.[  Face brick complying with requirements for grade, compressive strength, and size indicated for building brick may be substituted for building brick.]

Hollow brick is not simply face brick with the usual cores (holes); it is brick that has voids (cores and cells) exceeding 25 percent of gross cross-sectional area.  See Evaluations.  If retaining paragraph below, select one grade, class, and type.  See Editing Instructions No. 5 and No. 6 in the Evaluations.

D. Hollow Brick:  [ASTM C 652] [UBC Standard 21-1], Grade [SW] [MW or SW], Class [H40V (void areas between 25 and 40 percent of gross cross-sectional area)] [H60V (void areas between 40 and 60 percent of gross cross-sectional area)], Type [HBX] [HBS] [HBA] [HBB].

See Editing Instruction No. 2 in the Evaluations before selecting unit compressive strength in first subparagraph below.  Usually delete below if retaining Part 1 "Performance Requirements" Article.  Below is based on net area, as in Table 1 in the 2002 MSJC Specification, rather than gross area reported by ASTM C 67.  Minimum average gross-area compressive strength per ASTM C 652 is 3000 psi (20.7 MPa) for Grade SW and 2500 psi (17.2 MPa) for Grade MW.

1. Unit Compressive Strength:  Provide units with minimum average net-area compressive strength of [3000 psi (20.7 MPa)] [4400 psi (30.3 MPa)] [5500 psi (37.9 MPa)] [6400 psi (44.1 MPa)] [8000 psi (55.2 MPa)] [8400 psi (57.9 MPa)] <Insert value>.

2. Efflorescence:  Provide brick that has been tested according to ASTM C 67 and is rated "not effloresced."

Delete subparagraph below if surface-coated brick is not used.

3. Surface Coating:  Brick with colors or textures produced by application of coatings shall withstand 50 cycles of freezing and thawing per ASTM C 67 with no observable difference in the applied finish when viewed from 10 feet (3 m)[ or shall have a history of successful use in Project's area].

Sizes in five subparagraphs below are examples only.  Verify availability of sizes with local suppliers and revise to suit Project.

4. Size (Actual Dimensions):  [5-1/2 inches (140 mm) wide by 3-1/2 inches (89 mm) high by 11-1/2 inches (292 mm) long] [or] [5-5/8 inches (143 mm) wide by 3-5/8 inches (92 mm) high by 11-5/8 inches (295 mm) long].

5. Size (Actual Dimensions):  [7-1/2 inches (190 mm) wide by 3-1/2 inches (89 mm) high by 11-1/2 inches (292 mm) long] [or] [7-5/8 inches (194 mm) wide by 3-5/8 inches (92 mm) high by 11-5/8 inches (295 mm) long].

6. Size (Actual Dimensions):  [5-1/2 inches (140 mm) wide by 3-1/2 inches (89 mm) high by 15-1/2 inches (394 mm) long] [or] [5-5/8 inches (143 mm) wide by 3-5/8 inches (92 mm) high by 15-5/8 inches (397 mm) long].

7. Size (Actual Dimensions):  [7-1/2 inches (190 mm) wide by 3-1/2 inches (89 mm) high by 15-1/2 inches (394 mm) long] [or] [7-5/8 inches (194 mm) wide by 3-5/8 inches (92 mm) high by 15-5/8 inches (397 mm) long].

8. Size (Actual Dimensions):  4-5/8 inches (117 mm) wide by 2-3/4 inches (70 mm) high by 9-5/8 inches (244 mm) long.

Select from five subparagraphs above for IP sizes with equivalent SI (metric) dimensions or first subparagraph below for products manufactured to metric sizes.

9. Size (Actual Dimensions):  [140] [190] mm wide by 90 mm high by 290 mm long.

10. Application:  Use where brick is exposed, unless otherwise indicated.

11. [Where shown to "match existing,"  ]provide hollow brick matching color range, texture, and size of existing adjacent brickwork.

a. <Insert information on existing brick if known.>

Delete subparagraph below if brick is specified by product name.  First three options are examples of descriptive requirements for appearance where proprietary specifications and allowances cannot be used.  Select last option if allowance is used.

12. Color and Texture:  [Medium brown, wire-cut] [Full-range red, smooth texture] [Buff, velour] [Match Architect's samples] [As selected by Architect].

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

13. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation for acceptable hollow brick.>

Retain one of three paragraphs below for solid brick (at least 75 percent solid).  First paragraph is for brick that is fired before glazing and then fired again; second is for single-fired glazed brick; third allows the use of either.  See Editing Instructions No. 5 and No. 6 in the Evaluations for information on grades and types for face brick that is fired before glazing.

E. Glazed Face Brick:  [ASTM C 216] [UBC Standard 21-1], Grade [SW] [MW or SW], Type [FBX] [FBS] [FBA]; with glaze complying with ASTM C 126.

F. Glazed Face Brick:  ASTM C 1405, Class [Exterior] [Interior], Grade [S (Select)] [SS (Select Sized or Ground Edge)].

G. Glazed Face Brick:  Either ASTM C 1405, Class [Exterior] [Interior], Grade S (Select) or [ASTM C 216] [UBC Standard 21-1], Grade [SW] [MW or SW], Type FBX; with glaze complying with ASTM C 126.

Retain paragraph below for hollow brick (less than 75 percent solid).  Coordinate with manufacturers' list for sizes selected.  See Editing Instructions No. 5 and No. 6 in the Evaluations for information on grades and types.

H. Glazed Hollow Brick:  Hollow brick complying with [ASTM C 652] [UBC Standard 21-1], Grade [SW] [MW or SW], Class [H40V (void areas between 25 and 40 percent of gross cross-sectional area)] [H60V (void areas between 40 and 60 percent of gross cross-sectional area)], Type [HBX] [HBS] [HBA]; with glaze complying with ASTM C 126.

Copy requirement for unit compressive strength from "Face Brick" or "Hollow Brick" Paragraph above and insert here if required.

Sizes in remaining subparagraphs are examples only.  Verify availability of sizes with local suppliers and revise to suit Project.

Select from 2 subparagraphs below for 3 courses in 8 inches (203 mm).

1. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-1/4 inches (57 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-1/4 inches (57 mm) high by7-5/8 inches (194 mm) long].

2. Size (Actual Dimensions):  [3-1/2 inches (89 mm)] [or] [3-5/8 inches (92 mm)] wide by 2-1/4 inches (57 mm) high by 8 inches (203 mm) long.

Select from 3 subparagraphs below for 5 courses in 16 inches (406 mm).

3. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-3/4 inches (70 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-13/16 inches (71 mm) high by 7-5/8 inches (194 mm) long].

4. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-3/4 inches (70 mm) high by 8 inches (203 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-13/16 inches (71 mm) high by 8 inches (203 mm) long].

5. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 2-3/4 inches (70 mm) high by 11-1/2 inches (292 mm) long] [or] [3-5/8 inches (92 mm) wide by 2-13/16 inches (71 mm) high by 11-5/8 inches (295 mm) long].

Retain first subparagraph below for square brick, 8 inches (203 mm) nominal size.

6. Size (Actual Dimensions):  [3-1/2 inches (89 mm) wide by 7-1/2 inches (190 mm) high by 7-1/2 inches (190 mm) long] [or] [3-5/8 inches (92 mm) wide by 7-5/8 inches (194 mm) high by 7-5/8 inches (194 mm) long].

7. Size (Actual Dimensions):  5-5/8 inches (143 mm) wide by 3-5/8 inches (92 mm) high by 11-5/8 inches (295 mm) long.

8. Size (Actual Dimensions):  7-5/8 inches (194 mm) wide by 3-5/8 inches (92 mm) high by 11-5/8 inches (295 mm) long.

Select from eight subparagraphs above for IP sizes with equivalent SI (metric) dimensions or from two subparagraphs below for products manufactured to metric sizes.

9. Size (Actual Dimensions):  90 mm wide by [57] [70] [90] [190] mm high by [190] [290] mm long.

10. Size (Actual Dimensions):  [140] [190] mm wide by 90 mm high by 290 mm long.

Delete subparagraph below if no units have two opposite faces exposed.

11. Provide Type I (single-faced units) where only one finished face is exposed when units are installed, and Type II (double-faced units) where two opposite finished faces are exposed when units are installed.

Select one of three options in subparagraph below.  If selecting first, indicate colors in a separate schedule.

12. Colors:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

13. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

Insert calcium silicate (sand-lime) brick if required.  See Evaluations.

2.6 STRUCTURAL-CLAY FACING TILE

A. General:

1. Provide solid, multicored, or hollow units, with shape and direction of cores optional, unless otherwise indicated.

Retain subparagraph below for correctional and seismic applications; otherwise, delete below and retain subparagraph above.

2. Provide multicored units designed for use in reinforced, grouted masonry; either with vertical cores and with webs notched to receive horizontal reinforcement, or with horizontal cores and with holes in bed shells for placement of grout and to receive vertical reinforcement.

Delete first subparagraph below if no exterior applications.

3. Where indicated for exterior applications, provide units recommended by manufacturer for exterior use in Project's location.

4. Provide special shapes where required for corners, jambs, coved bases, sills, and other special conditions indicated, including applications that cannot be produced by sawing standard units.

Retain or revise requirements in first subparagraph below to suit shapes required; delete if special shapes are comprehensively indicated on Drawings.

a. Provide [bullnose] [square-edged] units for outside corners, unless otherwise indicated.

b. Provide coved internal corners.

Revise first subparagraph below if nonrecessed, coved base units are required and available from manufacturers listed.

c. Provide recessed, coved base units.

5. Where direct application of plaster is indicated or where bonded to backup masonry, provide units with rough, combed, or scored faces.

Select one grade if retaining paragraph below.  Grade S is for use with comparatively narrow joints and Grade SS is for use where variation of face dimension must be small, such as in stacked bond.  Grade SS applies primarily to 8W Series units.

B. Glazed Structural-Clay Facing Tile:  ASTM C 126, Grade [S (Select)] [SS (Select Sized or Ground Edged)].

Retain one of three subparagraphs below, or insert other sizes.  Verify availability and coordinate with manufacturers' list of sizes.

1. Sizes:  6T Series with actual face dimensions of 5-1/6 inches (131 mm) high by 11-3/4 inches (298 mm) long by widths indicated.

2. Sizes:  8W Series with actual face dimensions of 7-3/4 inches (197 mm) high by 15-3/4 inches (400 mm) long by widths indicated.

3. Sizes:  4W Series with actual face dimensions of 7-3/4 inches (197 mm) high by 7-3/4 inches (197 mm) long by 3-3/4 inches (95 mm) wide.

Delete first subparagraph below if no units have two opposite faces exposed.

4. Provide Type I (single-faced units) where only one finished face is exposed when units are installed, and Type II (double-faced units) where two opposite finished faces are exposed when units are installed.

5. Provide special units glazed on ends and tops, as well as faces for corners, jambs, sills, pilasters, columns, and other applications indicated, where glazed units are exposed on other surfaces and faces.

Select one of three options in subparagraph below.  If selecting first, indicate colors and patterns in a separate schedule.

6. Colors and Patterns:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

7. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

Select one type and class from paragraph below.  Verify availability of products for type, class, and other characteristics selected.  See Evaluations for explanation of type and class.

C. Unglazed Structural-Clay Facing Tile:  ASTM C 212, Type [FTX] [FTS], [Standard] [Special-Duty] class.

1. Number of Faces:  Single faced where only one finished face is exposed when units are installed.

Delete subparagraph above or below if not applicable.

2. Number of Faces:  Double faced where both finished faces are exposed when units are installed.

Retain subparagraph below and indicate size on Drawings, or insert specific size.

3. Size:  As indicated.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

4. [Available ]Products:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation.>

2.7 FIREPLACE AND CHIMNEY LINING UNITS

Retain first paragraph below for residential fireplaces if required.

A. Firebox Brick:  ASTM C 1261, size required to produce lining thickness indicated.

B. Clay Flue Lining Units:  ASTM C 315.

2.8 STONE TRIM UNITS

This Article is intended for stone lintels and similar units built into masonry.  For stone trim secured with stone anchors, use Division 04 Section "Exterior Stone Cladding" instead of requirements in this Section.  For thin stone trim set as adhered veneer, use Division 04 Section "Stone Masonry."

A. Granite:  ASTM C 615.

Retain subparagraph below for a generic specification, or delete and specify by naming one or more acceptable varieties.

1. Description:  [Fine] [Medium]-grained, [white] [pink] [gray] [black] stone.[  Uniform pattern, without veining].

First option in paragraph below generally applies to very porous limestone that should only be used in mild climates; second, to oolitic and some dolomitic limestone; third, to dolomitic limestone.

B. Limestone:  ASTM C 568, Classification [I Low] [II Medium] [III High]-Density.

Retain subparagraph below if Indiana limestone is required.  If retaining, select Classification II Medium-Density in paragraph above.

1. Variety and Sources:  Indiana oolitic limestone quarried in Lawrence, Monroe, or Owen Counties, Indiana.

Delete subparagraph below if Indiana limestone is not used.  Select and Standard grades are hard to get in large sizes; gray is more plentiful than buff.  Verify availability with producers.

a. Grade and Color:  [Select, buff] [Select, gray] [Standard, buff] [Standard, gray] [Rustic, buff] [Rustic, gray] [Variegated], according to grade and color classification established by ILI.

C. Marble:  ASTM C 503, Classification [I Calcite] [II Dolomite] [III Serpentine] [IV Travertine].

Retain subparagraph below for a generic specification, or delete and specify by naming one or more acceptable varieties.

1. Description:  Uniform, fine- to medium-grained, white stone with only slight veining.

D. Quartz-Based Stone:  ASTM C 616, Classification[I Sandstone] [II Quartzitic Sandstone] [III Quartzite].

Retain paragraph and list below for semiproprietary or proprietary specification.  Refer to Division 01 Section "Product Requirements."

E. Varieties and Sources:  Subject to compliance with requirements, provide[ one of] the following:

1. <Insert, in separate subparagraphs, names of varieties and producers, distributors, or importers.>

Some finishes in first paragraph below are not suitable for all stone varieties.  For additional finishes, see Division 04 Section "Stone Masonry."

F. Finish:  [Polished] [Honed] [Smooth] [Machine tooled, 4 bats per 1 inch (25 mm)] [Machine tooled, 6 bats per 1 inch (25 mm)] [Machine tooled, 8 bats per 1 inch (25 mm)] [Chat sawed] [Split face] [Rock face (pitched face)] <Insert finish>.

Delete subparagraph below if not required.

1. Finish for [Tops of Sills] [and] [Soffits of Lintels]:  [Sand rubbed] [Split face] <Insert finish>.

G. Provide stone units accurately shaped, with exposed faces dressed true, and with beds and joints at right angles to faces.

Retain applicable references in three subparagraphs below.  No references for quartz-based stone currently exist.

1. For granite, comply with recommendations in NBGQA's "Specifications for Architectural Granite."

2. For limestone, comply with recommendations in ILI's "Indiana Limestone Handbook."

3. For marble, comply with recommendations in MIA's "Dimensional Stone--Design Manual IV."

2.9 MORTAR AND GROUT MATERIALS

Coordinate requirements in this Article with those in "Mortar and Grout Mixes" Article.

Retain one or more of five paragraphs and associated subparagraphs below.  Delete masonry cement and mortar cement if not allowed by "Mortar and Grout Mixes" Article.  See Evaluations for discussion of masonry cement and mortar cement.

A. Portland Cement:  ASTM C 150, Type I or II, except Type III may be used for cold-weather construction.  Provide natural color or white cement as required to produce mortar color indicated.

B. Hydrated Lime:  [ASTM C 207] [UBC Standard 21-13], Type S.

Mix below allows better control of color than job-mixed, portland cement-lime mortar.

C. Portland Cement-Lime Mix:  Packaged blend of portland cement complying with ASTM C 150, Type I or Type III, and hydrated lime complying with ASTM C 207, Type S.

D. Masonry Cement:  [ASTM C 91] [UBC Standard 21-11].

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Capital Materials Corporation; Flamingo Color Masonry Cement.

b. Essroc, Italcementi Group; [Brixment] [or] [Velvet].

c. Holcim (US) Inc.; [Mortamix Masonry Cement] [Rainbow Mortamix Custom Buff Masonry Cement] [White Mortamix Masonry Cement].

d. Lafarge North America Inc.; [Magnolia Masonry Cement] [Lafarge Masonry Cement] [Florida Super Masonry] [Trinity Super White Masonry Type S] [Trinity White Masonry Type N].

e. Lehigh Cement Company; [Lehigh Masonry Cement] [Lehigh White Masonry Cement].

f. National Cement Company, Inc.; Coosa Masonry Cement.

g. <Insert manufacturer's name; product name or designation.>

E. Mortar Cement:  [ASTM C 1329] [UBC Standard 21-14].

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Lafarge North America Inc.; [Lafarge Mortar Cement] [or] [Magnolia Superbond Mortar Cement].

b. <Insert manufacturer's name; product name or designation.>

Retain first paragraph and subparagraphs below for colored cement or for pigments added at Project site.

F. Mortar Pigments:  Natural and synthetic iron oxides and chromium oxides, compounded for use in mortar mixes.  Use only pigments with a record of satisfactory performance in masonry mortar.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Bayer Corporation, Industrial Chemicals Div.; Bayferrox Iron Oxide Pigments.

b. Davis Colors; True Tone Mortar Colors.

c. Solomon Grind-Chem Services, Inc.; SGS Mortar Colors.

d. <Insert manufacturer's name; product name or designation.>

G. Colored Cement Product:  Packaged blend made from [portland cement and lime] [masonry cement] [or] [mortar cement] and mortar pigments, all complying with specified requirements, and containing no other ingredients.

1. Formulate blend as required to produce color indicated or, if not indicated, as selected from manufacturer's standard colors.

Retain applicable subparagraphs below to suit types of cement retained above.  Percentages below are for pigments containing only metallic oxides.  If pigments containing carbon black are used, carbon black must be limited to 2 percent of portland cement by weight or 1 percent of masonry or mortar cement.

2. Pigments shall not exceed 10 percent of portland cement by weight.

3. Pigments shall not exceed 5 percent of [masonry cement] [or] [mortar cement] by weight.

Coordinate subparagraph and lists below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

4. [Available ]Products:

a. Colored Portland Cement-Lime Mix:

1) Capital Materials Corporation; Riverton Portland Cement Lime Custom Color.

2) Holcim (US) Inc.; Rainbow Mortamix Custom Color Cement/Lime.

3) Lafarge North America Inc.; Eaglebond.

4) Lehigh Cement Company; Lehigh Custom Color Portland/Lime Cement.

5) <Insert manufacturer's name; product name or designation.>

b. Colored Masonry Cement:

1) Capital Materials Corporation; Flamingo Color Masonry Cement.

2) Essroc, Italcementi Group; Brixment-in-Color.

3) Holcim (US) Inc.; Rainbow Mortamix Custom Color Masonry Cement.

4) Lafarge North America Inc.; [Florida Custom Color Masonry] [or] [Magnolia Masonry Cement].

5) Lehigh Cement Company; Lehigh Custom Color Masonry Cement.

6) National Cement Company, Inc.; Coosa Masonry Cement.

7) <Insert manufacturer's name; product name or designation.>

c. Colored Mortar Cement:

1) Lafarge North America Inc.; Magnolia Superbond Mortar Cement.

2) <Insert manufacturer's name; product name or designation.>

H. Aggregate for Mortar:  ASTM C 144.

1. For mortar that is exposed to view, use washed aggregate consisting of natural sand or crushed stone.

Delete subparagraph below if not required.

2. For joints less than 1/4 inch (6.5 mm) thick, use aggregate graded with 100 percent passing the No. 16 (1.18-mm) sieve.

Retain subparagraph below for white mortar.

3. White-Mortar Aggregates:  Natural white sand or crushed white stone.

Retain subparagraph below for colored-aggregate mortar.

4. Colored-Mortar Aggregates:  Natural sand or crushed stone of color necessary to produce required mortar color.

I. Aggregate for Grout:  ASTM C 404.

J. Epoxy Pointing Mortar:  ASTM C 395, epoxy-resin-based material formulated for use as pointing mortar for structural-clay tile facing units (and approved for such use by manufacturer of units); in color indicated or, if not otherwise indicated, as selected by Architect from manufacturer's colors.

Retain paragraph below if firebox brick and clay flue linings are used.

K. Refractory Mortar Mix:  Ground fireclay or non-water-soluble, calcium aluminate, medium-duty refractory mortar that passes ASTM C 199 test; or an equivalent product acceptable to authorities having jurisdiction.

Paragraph below is an example requirement for a concrete admixture often used in cold weather as an antifreeze.  Appendix X1 in ASTM C 270 and BIA recommend not using admixtures.

L. Cold-Weather Admixture:  Nonchloride, noncorrosive, accelerating admixture complying with ASTM C 494/C 494M, Type C, and recommended by manufacturer for use in masonry mortar of composition indicated.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Addiment Incorporated; Mortar Kick.

b. Euclid Chemical Company (The); Accelguard 80.

c. Grace Construction Products, a unit of W. R. Grace & Co. - Conn.; Morset.

d. Sonneborn, Div. of ChemRex; Trimix-NCA.

e. <Insert manufacturer's name; product name or designation.>

Retain first paragraph and subparagraphs below if integral water repellent is used in concrete masonry units.

M. Water-Repellent Admixture:  Liquid water-repellent mortar admixture intended for use with concrete masonry units, containing integral water repellent by same manufacturer.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Addiment Incorporated; Mortar Tite.

b. Grace Construction Products, a unit of W. R. Grace & Co. - Conn.; Dry-Block Mortar Admixture.

c. Master Builders, Inc.; [Color Cure Mortar Admix] [or] [Rheomix Rheopel].

d. <Insert manufacturer's name; product name or designation.>

N. Water:  Potable.

2.10 REINFORCEMENT

Delete paragraph below if no reinforcing bars in grouted cells are required.  Revise if another grade of steel is required.  Revise to specify epoxy-coated, stainless-steel, or galvanized bars if required.

A. Uncoated Steel Reinforcing Bars:  ASTM A 615/A 615M or ASTM A 996/A 996M, Grade 60 (Grade 420).

Standards in first paragraph below include requirements for "mill-galvanized, carbon steel," "hot-dip galvanized, carbon steel," and "stainless steel"; it is not necessary to specify these materials separately.

B. Masonry Joint Reinforcement, General:  [ASTM A 951] [UBC Standard 21-10].

Mill-galvanized coating is not as thick as hot-dip galvanized coating.  According to standards referenced in paragraph above, mill-galvanized coating may be applied to wire before fabricating but hot-dip galvanized coating must be applied after fabricating.

1. Interior Walls:  [Mill-] [Hot-dip] galvanized, carbon steel.

2. Exterior Walls:  [Hot-dip galvanized, carbon] [Stainless] steel.

3. Wire Size for Side Rods:  [W1.7 or 0.148-inch (3.8-mm)] [W2.8 or 0.188-inch (4.8-mm)] diameter.

Select one wire size from options in subparagraph above and below.

4. Wire Size for Cross Rods:  [W1.7 or 0.148-inch (3.8-mm)] [W2.8 or 0.188-inch (4.8-mm)] diameter.

Retain first subparagraph below and select one wire size if adjustable (two-piece) type reinforcement is required.

5. Wire Size for Veneer Ties:  [W1.7 or 0.148-inch (3.8-mm)] [W2.8 or 0.188-inch (4.8-mm)] diameter.

6. Spacing of Cross Rods, Tabs, and Cross Ties:  Not more than 16 inches (407 mm) o.c.

7. Provide in lengths of not less than 10 feet (3 m)[, with prefabricated corner and tee units].

C. Masonry Joint Reinforcement for Single-Wythe Masonry:  Either ladder or truss type with single pair of side rods.

D. Masonry Joint Reinforcement for Multiwythe Masonry:

Select acceptable types from three subparagraphs below and coordinate with requirements in Part 3.  More than one type may be needed; Part 3 "Composite Masonry" and "Cavity Walls" articles specify types required for various applications.

1. Ladder type with 1 side rod at each face shell of hollow masonry units more than 4 inches (100 mm) in width, plus [1 side rod] [2 side rods] at each wythe of masonry 4 inches (100 mm) or less in width.

2. Tab type, either ladder or truss design, with 1 side rod at each face shell of backing wythe and with rectangular tabs sized to extend at least halfway through facing wythe but with at least 5/8-inch (16-mm) cover on outside face.

Retain option in subparagraph below in Seismic Design Categories E and F (UBC Seismic Zones 3 and 4) and in other locations if continuous horizontal wire is used to reinforce veneer wythe.

3. Adjustable (two-piece) type, either ladder or truss design, with one side rod at each face shell of backing wythe and with separate ties that extend into facing wythe.  Ties have two hooks that engage eyes or slots in reinforcement and resist movement perpendicular to wall.  Ties extend at least halfway through facing wythe but with at least 5/8-inch (16-mm) cover on outside face.[  Ties have hooks or clips to engage a continuous horizontal wire in the facing wythe.]

E. Masonry Joint Reinforcement for Veneers Anchored with Seismic Masonry-Veneer Anchors:  Single 0.188-inch- (4.8-mm-) diameter, [hot-dip galvanized, carbon] [stainless]-steel continuous wire.

2.11 TIES AND ANCHORS

A. Materials:  Provide ties and anchors specified in subsequent paragraphs that are made from materials that comply with eight subparagraphs below, unless otherwise indicated.

Select from eight subparagraphs below only those materials referenced in subsequent paragraphs.

First subparagraph below is allowed only for anchors and ties in interior walls where humidity is less than 75 percent.

1. Mill-Galvanized, Carbon-Steel Wire:  ASTM A 82; with ASTM A 641/A 641M, Class 1 coating.

2. Hot-Dip Galvanized, Carbon-Steel Wire:  ASTM A 82; with ASTM A 153/A 153M, Class B-2 coating.

Select Type 304 in subparagraph below unless higher corrosion resistance of Type 316 is required.

3. Stainless-Steel Wire:  ASTM A 580/A 580M, Type [304] [316].

First subparagraph below is allowed only for anchors and ties in interior walls where humidity is less than 75 percent.

4. Galvanized Steel Sheet:  ASTM A 653/A 653M, Commercial Steel, G60 (Z180) zinc coating.

5. Steel Sheet, Galvanized after Fabrication:  ASTM A 1008/A 1008M, Commercial Steel, hot-dip galvanized after fabrication to comply with ASTM A 153/A 153M.

Select Type 304 in subparagraph below unless higher corrosion resistance of Type 316 is required.

6. Stainless-Steel Sheet:  ASTM A 666, Type [304] [316].

Retain subparagraph below if required for rigid anchors.

7. Steel Plates, Shapes, and Bars:  ASTM A 36/A 36M.

Retain subparagraph below if required for anchors for stone trim.

8. Stainless Steel bars:  ASTM A 276 or ASTM a 666, Type 304.

If retaining last option in first paragraph below, note that the 2002 MSJC Code does not allow ties made from galvanized steel sheet for interior use in spaces where humidity exceeds 75 percent.

B. Corrugated Metal Ties:  Metal strips not less than 7/8 inch (22 mm) wide with corrugations having a wavelength of 0.3 to 0.5 inch (7.6 to 12.7 mm) and an amplitude of 0.06 to 0.10 inch (1.5 to 2.5 mm) made from [steel sheet, galvanized after fabrication] [stainless-steel sheet] not less than [0.043 inch (1.1 mm)] [0.053 inch (1.3 mm)] [0.067 inch (1.7 mm)] [0.097 inch (2.5 mm)] thick.[  Ties made from galvanized steel sheet may be used in interior walls, unless otherwise indicated.]

C. Wire Ties, General:  Unless otherwise indicated, size wire ties to extend at least halfway through veneer but with at least 5/8-inch (16-mm) cover on outside face.  Outer ends of wires are bent 90 degrees and extend 2 inches (50 mm) parallel to face of veneer.

D. Individual Wire Ties:  Rectangular units with closed ends and not less than 4 inches (100 mm) wide.

1. Z-shaped ties with ends bent 90 degrees to provide hooks not less than 2 inches (50 mm) long may be used for masonry constructed from solid units or hollow units laid with cells horizontal.

2. Where wythes [do not align] [are of different materials], use adjustable ties with pintle-and-eye connections having a maximum adjustment of 1-1/4 inches (32 mm).

If retaining last option in subparagraph below, note that the 2002 MSJC Code does not allow ties made from mill-galvanized wire for interior use in spaces where humidity exceeds 75 percent.

3. Wire:  Fabricate from [3/16-inch- (4.8-mm-)] [1/4-inch- (6.4-mm-)] diameter, [hot-dip galvanized steel] [stainless-steel] wire.[  Mill-galvanized wire ties may be used in interior walls, unless otherwise indicated.]

Retain first paragraph and subparagraphs below if applicable to Project.  Indicate details on Drawings.

E. Adjustable Anchors for Connecting to Structure:  Provide anchors that allow vertical or horizontal adjustment but resist tension and compression forces perpendicular to plane of wall.

If retaining last option in subparagraph below, note that the 2002 MSJC Code does not allow ties made from mill-galvanized wire for interior use in spaces where humidity exceeds 75 percent.

1. Anchor Section for Welding to Steel Frame:  Crimped 1/4-inch- (6.4-mm-) diameter, [hot-dip galvanized steel] [stainless-steel] wire.[  Mill-galvanized wire may be used at interior walls, unless otherwise indicated.]

Delete first option in subparagraph below if triangular wire ties are used for connecting to concrete.  If retaining last option, note that the 2002 MSJC Code does not allow ties made from mill-galvanized wire for interior use in spaces where humidity exceeds 75 percent.

2. Tie Section[ for Steel Frame]:  Triangular-shaped wire tie, sized to extend within 1 inch (25 mm) of masonry face, made from [0.188-inch- (4.8-mm-)] [0.25-inch- (6.4-mm-)] diameter, [hot-dip galvanized steel] [stainless-steel] wire.[  Mill-galvanized wire may be used at interior walls, unless otherwise indicated.]

If selecting either of last two options in subparagraph below, note that the 2002 MSJC Code does not allow ties made from galvanized steel sheet for interior use in spaces where humidity exceeds 75 percent.

3. Connector Section for Concrete:  Dovetail tabs for inserting into dovetail slots in concrete and attached to tie section; formed from [0.053-inch- (1.3-mm-) thick, steel sheet, galvanized after fabrication] [0.097-inch- (2.5-mm-) thick, steel sheet, galvanized after fabrication] [0.062-inch- (1.6-mm-) thick, stainless-steel sheet] [0.109-inch- (2.8-mm-) thick, stainless-steel sheet].  [0.064-inch- (1.6-mm-) thick, galvanized sheet may be used at interior walls, unless otherwise indicated.] [0.108-inch- (2.7-mm-) thick, galvanized sheet may be used at interior walls, unless otherwise indicated.]

Select subparagraph above or below if anchors are required for connecting to concrete.

4. Tie Section for Concrete:  Corrugated metal ties with dovetail tabs for inserting into dovetail slots in concrete and sized to extend to within 1 inch (25 mm) of masonry face.

F. Partition Top anchors:  0.097-inch- (2.5-mm-) thick metal plate with 3/8-inch- (10-mm-) diameter metal rod 6 inches (150 mm) long welded to plate and with closed-end plastic tube fitted over rod that allows rod to move in and out of tube.  Fabricate from [steel, hot-dip galvanized after fabrication] [stainless steel].

Rigid anchors can be used to connect T-intersections of CMU shear walls in lieu of masonry bonding or bond beams.  They are also often used at T-intersections of other CMU walls, although masonry bonding and T-shaped masonry joint reinforcement may be used.  Delete first paragraph and subparagraph below if not required.

G. Rigid Anchors:  Fabricate from steel bars [1-1/2 inches (38 mm) wide by 1/4 inch (6.4 mm) thick by 24 inches (600 mm) long, with ends turned up 2 inches (50 mm) or with cross pins, unless otherwise indicated] [bent to configuration indicated].

Select one of three options in subparagraph below. Rigid anchors may not be fully embedded in mortar or grout and, therefore, require a coating for corrosion protection. ACI 530.1/ASCE 6/TMS 602 requires hot-dip galvanized or epoxy coating.

1. Corrosion Protection:  [Hot-dip galvanized to comply with ASTM A 153/A 153M] [Epoxy coating 0.020 inch (0.51 mm) thick] [Rust-inhibitive paint].

H. Stone Anchors:  Fabricate dowels, cramps, and other stone anchors from stainless steel.

I. Adjustable Masonry-Veneer Anchors

1. General:  Provide anchors that allow vertical adjustment but resist tension and compression forces perpendicular to plane of wall, for attachment over sheathing to wood or metal studs, and as follows:

Subparagraph below is from BIA Technical Notes 28B.

a. Structural Performance Characteristics:  Capable of withstanding a 100-lbf (445-N) load in both tension and compression without deforming or developing play in excess of 0.05 inch (1.3 mm).

Usually retain first of two subparagraphs below and delete types of anchors considered unacceptable from the following associated subparagraphs.

2. Contractor's Option:  Unless otherwise indicated, provide any of the following types of anchors:

3. Screw-Attached, Masonry-Veneer Anchors:  Units consisting of a wire tie and a metal anchor section.

Four subparagraphs below are examples of proprietary anchor sections.  Insert others to suit Project.  First describes Dur-O-Wal's "D/A 213" and Wire-Bond's "RJ-711."

a. Anchor Section:  Rib-stiffened, sheet metal plate with screw holes top and bottom, 2-3/4 inches (70 mm) wide by 3 inches (75 mm) high; with projecting tabs having slotted holes for inserting vertical legs of wire tie specially formed to fit anchor section.

Subparagraph below describes Dur-O-Wal's "D/A 210," Heckmann Building Products' "315-D," Hohmann & Barnard's "DW-10HS" and "DW-10," and Wire-Bond's "1004, Type III."  Select longer lengths for Hohmann & Barnard's "DW-10" and shorter lengths for others.

b. Anchor Section:  Sheet metal plate, 1-1/4 inches (32 mm) wide by [6 inches (150 mm)] [9 inches (225 mm)] long, with screw holes top and bottom and with raised rib-stiffened strap, 5/8 inch (16 mm) wide by [3-5/8 inches (92 mm)] [5-1/2 inches (140 mm)] long, stamped into center to provide a slot between strap and plate for inserting wire tie.

Subparagraph below describes Hohmann & Barnard's "DW-10-X."

c. Anchor Section:  Gasketed sheet metal plate, 1-1/4 inches (32 mm) wide by 6 inches (150 mm) long, with screw holes top and bottom; top and bottom ends bent to form pronged legs of length to match thickness of insulation or sheathing; and raised rib-stiffened strap, 5/8 inch (16 mm) wide by 6 inches (150 mm) long, stamped into center to provide a slot between strap and plate for inserting wire tie.  Provide anchor manufacturer's standard, self-adhering, modified bituminous gaskets manufactured to fit behind anchor plate and extend beyond pronged legs.

Subparagraph below describes Heckmann's "Pos-I-Tie."

d. Anchor Section:  Zinc-alloy barrel section with flanged head with eye and corrosion-resistant, self-drilling screw.  Eye designed to receive wire tie and to serve as head for drilling fastener into framing.  Barrel length to suit sheathing thickness, allowing screw to seat directly against framing with flanged head covering hole in sheathing.

Retain first subparagraph below with any subparagraph above.

e. Fabricate sheet metal anchor sections and other sheet metal parts from [0.067-inch- (1.7-mm-) thick, steel sheet, galvanized after fabrication] [0.097-inch- (2.5-mm-) thick, steel sheet, galvanized after fabrication] [0.078-inch- (2.0-mm-) thick, stainless-steel sheet] [0.109-inch- (2.8-mm-) thick, stainless-steel sheet].

f. Wire Ties:  Triangular-, rectangular-, or T-shaped wire ties fabricated from [0.188-inch- (4.8-mm-)] [0.25-inch- (6.4-mm-)] diameter, [hot-dip galvanized steel] [stainless-steel] wire.

Coordinate first subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

g. [Available ]Products:

1) Dayton Superior Corporation, Dur-O-Wal Division; [D/A 213] [or] [D/A 210 with D/A 700-708].

2) Heckmann Building Products Inc.; [315-D with 316] [or] [Pos-I-Tie].

3) Hohmann & Barnard, Inc.; [DW-10] [DW-10HS] [or] [DW-10-X].

4) Wire-Bond; [1004, Type III] [or] [RJ-711].

5) <Insert manufacturer's name; product name or designation.>

4. Slip-in, Masonry-Veneer Anchors:  Units consisting of a wire tie section and an anchor section designed to interlock with metal studs and be slipped into place as sheathing is installed.

Subparagraph below describes Hohmann & Barnard's "AA308."

a. Wire-Type Anchor:  Bent wire anchor section with an eye to receive the wire tie.  Wire tie has a vertical leg that slips into the eye of anchor section and allows vertical adjustment.  Both sections are made from 3/16-inch (4.8-mm), hot-dip galvanized wire.

Subparagraph below describes BLOK-LOK's "STUD-LOK."

b. Strap-and-Wire Type Anchor:  Flat metal strap with notch to interlock with flange of metal stud and two holes for inserting vertical legs of wire tie specially formed to fit anchor section.  Strap is made from 0.067-inch- (1.7-mm-) thick, steel sheet, galvanized after fabrication; anchor wire tie is made from 3/16-inch (4.8-mm), hot-dip galvanized wire.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

c. [Available ]Products:

1) BLOK-LOK Limited; STUD-LOK.

2) Hohmann & Barnard, Inc.; AA308.

3) <Insert manufacturer's name; product name or designation.>

Anchors in subparagraph below may be used for other than seismic conditions.

5. Seismic Masonry-Veneer Anchors:  Units consisting of a metal anchor section and a connector section designed to engage a continuous wire embedded in the veneer mortar joint.

Two subparagraphs below describe Dur-O-Wal's "D/A 213S."

a. Anchor Section:  Rib-stiffened, sheet metal plate with screw holes top and bottom, 2-3/4 inches (70 mm) wide by 3 inches (75 mm) high; with projecting tabs having slotted holes for inserting vertical leg of connector section.

b. Connector Section:  Rib-stiffened, sheet metal bent plate with down-turned leg designed to fit in anchor section slot and with integral tabs designed to engage continuous wire.  Size connector to extend at least halfway through veneer but with at least 5/8-inch (16-mm) cover on outside face.

Two subparagraphs below describe Wire-Bond's "RJ-711 with Wire-Bond clip."

c. Anchor Section:  Rib-stiffened, sheet metal plate with screw holes top and bottom, 2-3/4 inches (70 mm) wide by 3 inches (75 mm) high; with projecting tabs having slotted holes for inserting vertical legs of wire tie specially formed to fit anchor section.  Size wire tie to extend at least 1-1/2 inches (38 mm) into veneer but with at least 5/8-inch (16-mm) cover on outside face.

d. Connector Section:  Sheet metal clip welded to wire tie with integral tabs designed to engage continuous wire.

First two subparagraphs below describe Hohmann & Barnard's "DW-10-X-Seismiclip."

e. Anchor Section:  Gasketed sheet metal plate, 1-1/4 inches (32 mm) wide by 6 inches (150 mm) long, with screw holes top and bottom; top and bottom ends bent to form pronged legs to bridge insulation or sheathing and contact studs; and raised rib-stiffened strap, 5/8 inch (16 mm) wide by 6 inches (150 mm) long, stamped into center to provide a slot between strap and plate for inserting wire tie.  Provide anchor manufacturer's standard, self-adhering, modified bituminous gaskets manufactured to fit behind anchor plate and extend beyond pronged legs.

f. Connector Section:  Triangular wire tie and rigid PVC extrusion with snap-in grooves for inserting continuous wire.  Size wire tie to extend at least halfway through veneer but with at least 5/8-inch (16-mm) cover on outside face.

g. Fabricate sheet metal anchor sections and other sheet metal parts from [0.067-inch- (1.7-mm-) thick, steel sheet, galvanized after fabrication] [0.097-inch- (2.5-mm-) thick, steel sheet, galvanized after fabrication] [0.078-inch- (2.0-mm-) thick, stainless-steel sheet] [0.109-inch- (2.8-mm-) thick, stainless-steel sheet].

h. Fabricate wire connector sections from [0.188-inch- (4.8-mm-)] [0.25-inch- (6.4-mm-)] diameter, [hot-dip galvanized, carbon] [stainless]-steel wire.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

i. [Available ]Products:

1) Dayton Superior Corporation, Dur-O-Wal Division; D/A 213S.

2) Hohmann & Barnard, Inc.; DW-10-X-Seismiclip.

3) Wire-Bond; RJ-711 with Wire-Bond clip.

4) <Insert manufacturer's name; product name or designation.>

Fasteners below are for steel studs from 0.033 to 0.112 inch (0.8 to 2.8 mm) thick.  "Climaseal" and "Stalgard" finishes by ITW Buildex and Elco Industries comply with coating description.

6. Polymer-Coated, Steel Drill Screws for Steel Studs:  ASTM C 954 except manufactured with hex washer head and neoprene washer, No. 10 (4.8-mm) diameter by length required to penetrate steel stud flange with not less than 3 exposed threads, and with organic polymer coating with salt-spray resistance to red rust of more than 800 hours per ASTM B 117.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

Although fasteners listed below are generally available only in large quantities if purchased directly from fastener manufacturer, they are available in smaller quantities from manufacturers of masonry anchors.

1) ITW Buildex; Teks Maxiseal with Climaseal finish.

2) Textron Inc., Textron Fastening Systems; Elco Dril-Flex with Stalgard finish.

3) <Insert manufacturer's name; product name or designation.>

See Evaluations and BIA Technical Notes 28B for use of stainless-steel screws.

7. Stainless-Steel Drill Screws for Steel Studs:  Proprietary fastener consisting of carbon-steel drill point and 300 Series stainless-steel shank, complying with ASTM C 954 except manufactured with hex washer head and neoprene washer, No. 10 (4.8-mm) diameter by length required to penetrate steel stud flange with not less than three exposed threads.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

Although fasteners listed below are generally available only in large quantities if purchased directly from fastener manufacturer, they are available in smaller quantities from manufacturers of masonry anchors.

1) Dayton Superior Corporation, Dur-O-Wal Division; Stainless Steel SX Fastener.

2) ITW Buildex; Scots long life Teks.

3) <Insert manufacturer's name; product name or designation.>

2.12 MISCELLANEOUS ANCHORS

A. Unit Type Inserts in Concrete:  Cast-iron or malleable-iron wedge-type inserts.

Usually delete paragraph above and below and specify (including installation) in the concrete section if required.

B. Dovetail Slots in Concrete:  Furnish dovetail slots with filler strips, of slot size indicated, fabricated from 0.034-inch (0.9-mm), galvanized steel sheet.

Revise paragraph below if ASTM A 325 (ASTM A 325M) bolts are required.

C. Anchor Bolts:  [Headed] [or] [L-shaped] steel bolts complying with ASTM A 307, Grade A (ASTM F 568M, Property Class 4.6); with ASTM A 563 (ASTM A 563M) hex nuts and, where indicated, flat washers; hot-dip galvanized to comply with ASTM A 153/A 153M, Class C; of dimensions indicated.

Usually delete paragraph and subparagraphs below and include in Sections specifying items anchored.  If retaining, select acceptable types and verify safety factors with Project's structural engineer.  Overhead, vibratory, and other critical loads generally require higher safety factors.

D. Postinstalled Anchors:  Provide [chemical] [or] [torque-controlled expansion] anchors, with capability to sustain, without failure, a load equal to six times the load imposed when installed in solid or grouted unit masonry and equal to four times the load imposed when installed in concrete, as determined by testing per ASTM E 488 conducted by a qualified independent testing agency.

1. Corrosion Protection:  Carbon-steel components zinc plated to comply with ASTM B 633, Class Fe/Zn 5 (5 microns) for Class SC 1 service condition (mild).

Subparagraph above and below are examples only.  Above protects against corrosion from an indoor atmosphere; revise to suit other service conditions after verifying availability of thicker coatings.

2. Corrosion Protection:  Stainless-steel components complying with ASTM F 593 and ASTM F 594, Alloy Group 1 or 2 (ASTM F 738M and ASTM F 836M, Alloy Group 1 or 4) for bolts and nuts; ASTM A 666 or ASTM A 276, Type 304 or 316, for anchors.

Insert other kinds of anchors as required.

2.13 EMBEDDED FLASHING MATERIALS

See Evaluations for discussion of flashing materials before editing this Article.

Coordinate paragraph and subparagraphs below with Division 07 Section "Sheet Metal Flashing and Trim."  Metal through-wall flashing is included in that Section.

A. Metal Flashing:  Provide metal flashing[, where flashing is exposed or partly exposed and where indicated,] complying with [SMACNA's "Architectural Sheet Metal Manual] [Division 07 Section "Sheet Metal Flashing and Trim]" and as follows:

Delete three subparagraphs below if referencing Division 07 Section "Sheet Metal Flashing and Trim."  Insert terne-coated stainless steel or lead-coated copper if required.

1. Stainless Steel:  ASTM A 240/A 240M, Type 304, 0.016 inch (0.4 mm) thick.

2. Copper:  ASTM B 370, Temper H00 or H01, cold-rolled copper sheet, 10-oz./sq. ft. (3-kg/sq. m) weight or 0.0135 inch (0.34 mm) thick for fully concealed flashing; 16-oz./sq. ft. (5-kg/sq. m) weight or 0.0216 inch (0.55 mm) thick elsewhere.

3. Fabricate continuous flashings in sections 96 inches (2400 mm) long minimum, but not exceeding 12 feet (3.6 m). Provide splice plates at joints of formed, smooth metal flashing.

Delete subparagraph below if referencing Division 07 Section "Sheet Metal Flashing and Trim" or if plain (flat) sheet metal flashing is acceptable.  Revise if dovetail pattern is required for interlocking bond.

4. Fabricate through-wall metal flashing embedded in masonry from [stainless steel] [copper], with ribs at 3-inch (75-mm) intervals along length of flashing to provide an integral mortar bond.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Cheney Flashing Company; [Cheney Flashing (Dovetail)] [or] [Cheney 3-Way Flashing (Sawtooth)].

2) Keystone Flashing Company, Inc.; Keystone 3-Way Interlocking Thruwall Flashing.

3) <Insert manufacturer's name; product name or designation.>

Delete subparagraph below if referencing Division 07 Section "Sheet Metal Flashing and Trim" or if not required.

5. Fabricate through-wall flashing with snaplock receiver on exterior face where indicated to receive counterflashing.

Usually retain one or both subparagraphs below if metal through-wall flashing is used.  See Evaluations.

6. Fabricate through-wall flashing with drip edge [where] [, unless otherwise] indicated.  Fabricate by extending flashing 1/2 inch (13 mm) out from wall, with outer edge bent down 30 degrees[ and hemmed].

7. Fabricate through-wall flashing with sealant stop [where] [, unless otherwise] indicated.  Fabricate by bending metal back on itself 3/4 inch (19 mm) at exterior face of wall and down into joint 3/8 inch (10 mm) to form a stop for retaining sealant backer rod.

Retain subparagraph below if either of two subparagraphs above are used with ribbed metal flashing.

8. Fabricate metal [drip edges] [and] [sealant stops] for ribbed metal flashing from plain metal flashing of same metal as ribbed flashing and extending at least 3 inches (75 mm) into wall with hemmed inner edge to receive ribbed flashing and form a hooked seam.  Form hem on upper surface of metal so that completed seam will shed water.

Retain one or both subparagraphs below for use with flexible flashing if required.  See Evaluations.

9. Metal Drip Edges:  Fabricate from stainless steel.  Extend at least 3 inches (75 mm) into wall and 1/2 inch (13 mm) out from wall, with outer edge bent down 30 degrees[ and hemmed].

10. Metal Flashing Terminations:  Fabricate from stainless steel.  Extend at least 3 inches (75 mm) into wall and out to exterior face of wall.  At exterior face of wall, bend metal back on itself for 3/4 inch (19 mm) and down into joint 3/8 inch (10 mm) to form a stop for retaining sealant backer rod.

Delete subparagraph below if metal strips are not used at expansion joints.

11. Metal Expansion-Joint Strips:  Fabricate from [stainless steel] [copper] to shapes indicated.

Delete first paragraph and subparagraphs below if only metal flashing is allowed.  If concealed metal flashing is required at certain locations, indicate those locations on Drawings or revise below.

B. Flexible Flashing:  For flashing not exposed to the exterior, use[ one of] the following, unless otherwise indicated:

Subparagraph below is an example only; revise if other laminated products are required.

1. Copper-Laminated Flashing:  [5-oz./sq. ft. (1.5-kg/sq. m)] [7-oz./sq. ft. (2-kg/sq. m)] copper sheet bonded with asphalt between 2 layers of glass-fiber cloth.  Use only where flashing is fully concealed in masonry.

Coordinate first subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Advanced Building Products Inc.; Copper Fabric Flashing.

2) AFCO Products Inc.; Copper Fabric.

3) Hohmann & Barnard, Inc.; H & B C-Fab Flashing.

4) Phoenix Building Products; Type FCC-Fabric Covered Copper.

5) Polytite Manufacturing Corp.; Copper Fabric Flashing.

6) Sandell Manufacturing Co., Inc.; Copper Fabric Flashing.

7) York Manufacturing, Inc.; York Copper Fabric Flashing.

8) <Insert manufacturer's name; product name or designation.>

2. Asphalt-Coated Copper Flashing:  [5-oz./sq. ft. (1.5-kg/sq. m)] [7-oz./sq. ft. (2-kg/sq. m)] copper sheet coated with flexible asphalt.  Use only where flashing is fully concealed in masonry.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Advanced Building Products Inc.; Cop-R-Cote.

2) AFCO Products Inc.; Cop-A-Cote.

3) Hohmann & Barnard, Inc.; H & B C-Coat Flashing.

4) Phoenix Building Products; Type ACC-Asphalt Bituminous Coated.

5) Polytite Manufacturing Corp.; Coated Copper Flashing.

6) Sandell Manufacturing Co., Inc.; Coated Copper Flashing.

7) York Manufacturing, Inc.; Copperseal.

8) <Insert manufacturer's name; product name or designation.>

Some rubberized-asphalt flashing products are 0.040 inch (1.0 mm) thick; some are 0.030 inch (0.8 mm) thick; others are 0.025 inch (0.6 mm) thick.  BIA recommends 0.030 inch (0.76 mm) as a minimum thickness.

3. Rubberized-Asphalt Flashing:  Composite flashing product consisting of a pliable, adhesive rubberized-asphalt compound, bonded to a high-density, cross-laminated polyethylene film to produce an overall thickness of not less than [0.030 inch (0.8 mm)] [0.040 inch (1.0 mm)].

Coordinate first subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Advanced Building Products Inc.; Peel-N-Seal.

2) Carlisle Coatings & Waterproofing; CCW-705-TWF Thru-Wall Flashing.

3) Dayton Superior Corporation, Dur-O-Wal Division; Dur-O-Barrier-44.

4) Grace Construction Products, a unit of W. R. Grace & Co. - Conn.; Perm-A-Barrier Wall Flashing.

5) Heckmann Building Products Inc.; No. 82 Rubberized-Asphalt Thru-Wall Flashing.

6) Hohmann & Barnard, Inc.; Textroflash.

7) Polyguard Products, Inc.; Polyguard 300.

8) Polytite Manufacturing Corp.; Poly-Barrier Self-Adhering Wall Flashing.

9) Williams Products, Inc.; Everlastic MF-40.

10) <Insert manufacturer's name; product name or designation.>

4. Elastomeric Thermoplastic Flashing:  Composite flashing product consisting of a polyester-reinforced ethylene interpolymer alloy as follows:

Retain one or more of first three subparagraphs below or show on Drawings where each is required.

a. Monolithic Sheet:  Elastomeric thermoplastic flashing, 0.040 inch (1.0 mm) thick.

b. Self-Adhesive Sheet:  Elastomeric thermoplastic flashing, 0.025 inch (0.6 mm) thick, with a 0.015-inch- (0.4-mm-) thick coating of rubberized-asphalt adhesive.

First subparagraph below is for applications where flashing extends to face of masonry.  This material may not be suitable for use at sealant joints because it will be difficult to remove the sealant for replacement without damaging the flashing.

c. Self-Adhesive Sheet with Drip Edge:  Elastomeric thermoplastic flashing, 0.025 inch (0.6 mm) thick, with a 0.015-inch- (0.4-mm-) thick coating of rubberized-asphalt adhesive.  Where flashing extends to face of masonry, rubberized-asphalt coating is held back approximately 1-1/2 inches (38 mm) from edge.

1) Color:  [Gray] [White] [Tan/buff] [Black].

d. Accessories:  Provide preformed corners, end dams, other special shapes, and seaming materials produced by flashing manufacturer.

Coordinate first subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

e. [Available ]Products:

1) Hyload, Inc.; Hyload Cloaked Flashing System.

2) <Insert manufacturer's name; product name or designation.>

5. EPDM Flashing:  Sheet flashing product made from ethylene-propylene-diene terpolymer, complying with ASTM D 4637, 0.040 inch (1.0 mm) thick.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Carlisle Coatings & Waterproofing; Pre-Kleened EPDM Thru-Wall Flashing.

2) Firestone Building Products; FlashGuard.

3) Heckmann Building Products Inc.; No. 81 EPDM Thru-Wall Flashing.

4) <Insert manufacturer's name; product name or designation.>

C. Single-Wythe CMU Flashing System:  System of CMU cell flashing pans and interlocking CMU web covers made from high-density polyethylene incorporating chemical stabilizers that prevent UV degradation.  Cell flashing pans have integral weep spouts that are designed to be built into mortar bed joints and weep collected moisture to the exterior of CMU walls and that extend into the cell to prevent clogging with mortar.

Coordinate subparagraph below with Part 2 "Manufacturers" Article.

1. Product:  Subject to compliance with requirements, provide "Blok-Flash" by Advanced Building Products Inc.

D. Solder and Sealants for Sheet Metal Flashings:[  As specified in Division 07 Section "Sheet Metal Flashing and Trim." ]

Select option in paragraph above or retain one or more of three subparagraphs below.

1. Solder for Stainless Steel:  ASTM B 32, Grade Sn60, with acid flux of type recommended by stainless-steel sheet manufacturer.

2. Solder for Copper:  ASTM B 32, Grade Sn50, 50 percent tin and 50 percent lead.

Revise subparagraph below if sealant of specific type, grade, class, and use is required.

3. Elastomeric Sealant:  ASTM C 920, chemically curing [urethane] [polysulfide] [silicone] sealant; of type, grade, class, and use classifications required to seal joints in sheet metal flashing and trim and remain watertight.

Delete paragraph and subparagraphs above if sheet metal flashing is not used.  Delete paragraph below if only sheet metal flashing is used.

E. Adhesives, Primers, and Seam Tapes for Flashings:  Flashing manufacturer's standard products or products recommended by flashing manufacturer for bonding flashing sheets to each other and to substrates.

2.14 MISCELLANEOUS MASONRY ACCESSORIES

Revise first two paragraphs below if a specific product is required.

A. Compressible Filler:  Premolded filler strips complying with ASTM D 1056, Grade 2A1; compressible up to 35 percent; of width and thickness indicated; formulated from [neoprene] [urethane] [or] [PVC].

B. Preformed Control-Joint Gaskets:  Made from [styrene-butadiene-rubber compound, complying with ASTM D 2000, Designation M2AA-805] [or] [PVC, complying with ASTM D 2287, Type PVC-65406] and designed to fit standard sash block and to maintain lateral stability in masonry wall; size and configuration as indicated.

C. Bond-Breaker Strips:  Asphalt-saturated, organic roofing felt complying with ASTM D 226, Type I (No. 15 asphalt felt).

D. Weep/Vent Products:  Use[ one of] the following, unless otherwise indicated:

Retain one or more of first six subparagraphs and associated subparagraphs below, or delete all if open-head joints are used for weep holes and vents.

1. Wicking Material:  Absorbent rope, made from [cotton] [or] [UV-resistant synthetic fiber], 1/4 to 3/8 inch (6 to 10 mm) in diameter, in length required to produce 2-inch (50-mm) exposure on exterior and 18 inches (450 mm) in cavity between wythes.  Use only for weeps.

2. Round Plastic Weep/Vent Tubing:  Medium-density polyethylene, 3/8-inch (9-mm) OD by 4 inches (100 mm) long.

3. Rectangular Plastic Weep/Vent Tubing:  Clear butyrate, 3/8 by 1-1/2 by 3-1/2 inches (9 by 38 by 89 mm) long.

4. Cellular Plastic Weep/Vent:  One-piece, flexible extrusion made from UV-resistant polypropylene copolymer, full height and width of head joint and depth 1/8 inch (3 mm) less than depth of outer wythe, in color selected from manufacturer's standard.

Coordinate first subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Advanced Building Products Inc.; Mortar Maze weep vent.

2) Dayton Superior Corporation, Dur-O-Wal Division; Cell Vents.

3) Heckmann Building Products Inc.; No. 85 Cell Vent.

4) Hohmann & Barnard, Inc.; Quadro-Vent.

5) Wire-Bond; Cell Vent.

6) <Insert manufacturer's name; product name or designation.>

5. Mesh Weep/Vent:  Free-draining mesh; made from polyethylene strands, full height and width of head joint and depth 1/8 inch (3 mm) less than depth of outer wythe; in color selected from manufacturer's standard.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Mortar Net USA, Ltd.; Mortar Net Weep Vents.

2) <Insert manufacturer's name; product name or designation.>

Mortar will corrode product below unless protected with paint.

6. Aluminum Weep Hole/Vent:  One-piece, L-shaped units made from sheet aluminum, designed to fit into a head joint and consisting of a vertical channel with louvers stamped in web and with a top flap to keep mortar out of the head joint; painted before installation to comply with Division 09 painting Sections in color approved by Architect to match that of mortar.

Coordinate first subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Hohmann & Barnard, Inc.; #343W - Wilko Weep Hole.

2) <Insert manufacturer's name; product name or designation.>

7. Vinyl Weep Hole/Vent:  One-piece, offset, T-shaped units made from flexible, injection-molded PVC, designed to fit into a head joint and consisting of a louvered vertical leg, flexible wings to seal against ends of masonry units, and a top flap to keep mortar out of the head joint; in color approved by Architect to match that of mortar.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

a. [Available ]Products:

1) Hohmann & Barnard, Inc.; #343 Louvered Weep Hole.

2) Williams Products, Inc.; Williams-Goodco Brick Vent.

3) Wire-Bond; Louvered Weepholes.

4) <Insert manufacturer's name; product name or designation.>

Products described in first paragraph and subparagraphs below can be used to keep weep holes clear and to keep cavity free draining.  See Evaluations.

E. Cavity Drainage Material:  Free-draining mesh, made from polymer strands that will not degrade within the wall cavity.

Usually retain subparagraph and two or more of four associated subparagraphs below to ensure competition in bidding.  If only one configuration is used, edit the subparagraph and combine it with the selected associated subparagraph.

1. Provide one of the following configurations:

Subparagraph below describes Mortar Net's "Mortar Net."

a. Strips, full-depth of cavity and 10 inches (250 mm) wide, with dovetail shaped notches 7 inches (175 mm) deep that prevent mesh from being clogged with mortar droppings.

First subparagraph below describes Advanced Building's "Mortar Break" and "Mortar Break II," respectively.  Usually select second option if cavity is 1-1/2 inches (38 mm) or larger.

b. Strips, not less than [3/4 inch (19 mm)] [1-1/2 inches (38 mm)] thick and 10 inches (250 mm) wide, with dimpled surface designed to catch mortar droppings and prevent weep holes from being clogged with mortar.

c. Sheets or strips full depth of cavity and installed to full height of cavity.

d. Sheets or strips not less than [3/4 inch (19 mm)] [1 inch (25 mm)] <Insert thickness> thick and installed to full height of cavity with additional strips 4 inches (100 mm) high at weep holes and thick enough to fill entire depth of cavity and prevent weep holes from being clogged with mortar.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

2. [Available ]Products:

Not all products listed below are available in all configurations described above.

a. Advanced Building Products Inc.; [Mortar Break] [Mortar Break II].

b. Archovations, Inc.; CavClear Masonry Mat.

c. Dayton Superior Corporation, Dur-O-Wal Division; Polytite MortarStop.

d. Mortar Net USA, Ltd.; Mortar Net.

e. <Insert manufacturer's name; product name or designation.>

F. Reinforcing Bar Positioners:  Wire units designed to fit into mortar bed joints spanning masonry unit cells with loops for holding reinforcing bars in center of cells.  Units are formed from 0.142-inch (3.6-mm) steel wire, hot-dip galvanized after fabrication.  Provide units with either two loops or four loops as needed for number of bars indicated.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Dayton Superior Corporation, Dur-O-Wal Division; D/A 810, D/A 812 or D/A 817.

b. Heckmann Building Products Inc.; No. 376 Rebar Positioner.

c. Hohmann & Barnard, Inc.; #RB or #RB-Twin Rebar Positioner.

d. Wire-Bond; O-Ring or Double O-Ring Rebar Positioner.

e. <Insert manufacturer's name; product name or designation.>

Insert other masonry accessories to suit Project.

2.15 MASONRY-CELL INSULATION

A. Loose-Granular Fill Insulation:  Perlite complying with ASTM C 549, Type II (surface treated for water repellency and limited moisture absorption) or Type IV (surface treated for water repellency and to limit dust generation).

B. Molded-Polystyrene Insulation Units:  Rigid, cellular thermal insulation formed by the expansion of polystyrene-resin beads or granules in a closed mold to comply with ASTM C 578, Type I.  Provide specially shaped units designed for installing in cores of masonry units.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Products:

a. Concrete Block Insulating Systems; Korfil.

b. Shelter Enterprises Inc.; Omni Core.

c. <Insert manufacturer's name; product name or designation.>

2.16 CAVITY-WALL INSULATION

A. Extruded-Polystyrene Board Insulation:  ASTM C 578, Type [IV] [X], closed-cell product extruded with an integral skin.

First paragraph below describes Dow's "Cavitymate Ultra."

B. Extruded-Polystyrene Board Insulation with Increased R-Value:  ASTM C 578, Type IV, but with an aged thermal resistance (R-value) for 1-inch (25-mm) thickness of 5.6 deg F x h x sq. ft./Btu at 75 deg F (1.0 K x sq. m/W at 24 deg C) at 5 years; closed-cell product with a carbon-black filler and extruded with an integral skin.

C. Molded-Polystyrene Board Insulation:  ASTM C 578, Type I.

D. Polyisocyanurate Board Insulation:  ASTM C 1289, Type I (aluminum-foil-faced), Class 2 (glass-fiber-reinforced).

Revise paragraph below to suit insulation selected, or delete if adhesive is not used.  See Evaluations.

E. Adhesive:  Type recommended by insulation board manufacturer for application indicated.

2.17 MASONRY CLEANERS

Verify acceptability of cleaner for cleaning masonry with pigmented mortar joints and for kinds of masonry units specified.

A. Proprietary Acidic Cleaner:  Manufacturer's standard-strength cleaner designed for removing mortar/grout stains, efflorescence, and other new construction stains from new masonry without discoloring or damaging masonry surfaces.  Use product expressly approved for intended use by cleaner manufacturer and manufacturer of masonry units being cleaned.

Coordinate subparagraph and list below with Part 2 "Manufacturers" Article.  Retain "Available" for nonproprietary and delete for semiproprietary specifications.

1. [Available ]Manufacturers:

a. Diedrich Technologies, Inc.

b. EaCo Chem, Inc.

c. ProSoCo, Inc.

d. <Insert manufacturer's name.>

2.18 MORTAR AND GROUT MIXES

A. General:  Do not use admixtures, including pigments, air-entraining agents, accelerators, retarders, water-repellent agents, antifreeze compounds, or other admixtures, unless otherwise indicated.

1. Do not use calcium chloride in mortar or grout.

2. Limit cementitious materials in mortar to portland cement[, mortar cement,] and lime.

Select subparagraph above or below, or delete both if masonry cement is acceptable.  Retain below if masonry cement is acceptable for unreinforced interior masonry.

3. Limit cementitious materials in mortar for exterior[ and reinforced] masonry to portland cement[, mortar cement,] and lime.

Delete subparagraph below if not retaining cold-weather admixture.

4. Add cold-weather admixture (if used) at same rate for all mortar that will be exposed to view, regardless of weather conditions, to ensure that mortar color is consistent.

Retain paragraph below if preblended mix is required.

B. Preblended, Dry Mortar Mix:  Furnish dry mortar ingredients in form of a preblended mix.  Measure quantities by weight to ensure accurate proportions, and thoroughly blend ingredients before delivering to Project site.

Retain and edit one of two paragraphs below.  See Evaluations.

C. Mortar for Unit Masonry:  Comply with [ASTM C 270] [BIA Technical Notes 8A] [UBC Standard 21-15], Proportion Specification.  Provide the following types of mortar for applications stated unless another type is indicated[ or needed to provide required compressive strength of masonry].

D. Mortar for Unit Masonry:  Comply with [ASTM C 270] [BIA Technical Notes 8A] [UBC Standard 21-15], Property Specification.  Provide the following types of mortar for applications stated unless another type is indicated[ or needed to provide required compressive strength of masonry].

For each masonry condition in five subparagraphs below applicable to Project, select one mortar type or revise to suit Project.  See Editing Instruction No. 7 in the Evaluations before making selections.

1. For masonry below grade or in contact with earth, use Type [M] [S].

Delete first subparagraph below if no masonry is grouted and reinforced with steel reinforcing bars.

2. For reinforced masonry, use Type [S] [N].

3. For mortar parge coats, use Type [S] [or] [N].

4. For exterior, above-grade, load-bearing and non-load-bearing walls and parapet walls; for interior load-bearing walls; for interior non-load-bearing partitions; and for other applications where another type is not indicated, use Type N.

Delete subparagraph below if not allowed.

5. For interior non-load-bearing partitions, Type O may be used instead of Type N.

Delete first paragraph and subparagraphs below if pigmented mortar is not required.

E. Pigmented Mortar:  Use colored cement product[ or select and proportion pigments with other ingredients to produce color required.  Do not add pigments to colored cement products].

Delete three subparagraphs below if not retaining option in paragraph above.  Percentages in first two subparagraphs are for pigments containing only metallic oxides.  If pigments containing carbon black are used, carbon black must be limited to 2 percent of portland cement by weight or 1 percent of masonry cement or mortar cement.

1. Pigments shall not exceed 10 percent of portland cement by weight.

2. Pigments shall not exceed 5 percent of [masonry cement] [or] [mortar cement] by weight.

Insert materials and proportions used for sample if known.

3. Mix to match Architect's sample.

F. Colored-Aggregate Mortar:  Produce required mortar color by using colored aggregates and natural color or white cement as necessary to produce required mortar color.

Insert materials and proportions used for sample if known.

1. Mix to match Architect's sample.

G. Grout for Unit Masonry:  Comply with [ASTM C 476] [UBC Standard 21-19].

1. Use grout of type indicated or, if not otherwise indicated, of type (fine or coarse) that will comply with [Table 1.15.1 in ACI 530.1/ASCE 6/TMS 602] [Table 21-C in the Uniform Building Code] for dimensions of grout spaces and pour height.

2. Provide grout with a slump of 8 to 11 inches (200 to 280 mm) as measured according to ASTM C 143/C 143M.

H. Epoxy Pointing Mortar:  Mix epoxy pointing mortar to comply with mortar manufacturer's written instructions.

2.19 SOURCE QUALITY CONTROL

See Editing Instruction No. 3 in the Evaluations before editing this Article.  Retain this Article only if unit-strength method is used, testing is required, and authorities having jurisdiction allow use of source quality-control testing instead of field quality-control testing for masonry units.

A. Owner will engage a qualified independent testing agency to perform source quality-control testing indicated below:

1. Payment for these services will be made [by Owner] [from Testing and Inspecting Allowance, as authorized by Change Orders].

2. Retesting of materials failing to comply with specified requirements shall be done at Contractor's expense.

B. Clay Masonry Unit Test:  For each type of unit furnished, per ASTM C 67.

C. Concrete Masonry Unit Test:  For each type of unit furnished, per ASTM C 140.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of work.

Delete first subparagraph below if not required.

1. For the record, prepare written report, endorsed by Installer, listing conditions detrimental to performance of work.

2. Verify that foundations are within tolerances specified.

Delete subparagraph below if not applicable.

3. Verify that reinforcing dowels are properly placed.

B. Before installation, examine rough-in and built-in construction for piping systems to verify actual locations of piping connections.

C. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 INSTALLATION, GENERAL

A. Thickness:  Build cavity and composite walls and other masonry construction to full thickness shown.  Build single-wythe walls to actual widths of masonry units, using units of widths indicated.

B. Build chases and recesses to accommodate items specified in this and other Sections.

C. Leave openings for equipment to be installed before completing masonry.  After installing equipment, complete masonry to match the construction immediately adjacent to opening.

D. Use full-size units without cutting if possible.  If cutting is required to provide a continuous pattern or to fit adjoining construction, cut units with motor-driven saws; provide clean, sharp, unchipped edges.  Allow units to dry before laying unless wetting of units is specified.  Install cut units with cut surfaces and, where possible, cut edges concealed.

E. Select and arrange units for exposed unit masonry to produce a uniform blend of colors and textures.

Subparagraph below is "means and methods" but helps ensure uniformity of blend.

1. Mix units from several pallets or cubes as they are placed.

Delete paragraph below if not applicable.

F. Matching Existing Masonry:  Match coursing, bonding, color, and texture of existing masonry.

Retain paragraph below for high-suction brick.  A simple test to determine if wetting is required consists of drawing a circle the size of a quarter on a brick and placing 20 drops of water in the circle; if water is absorbed within 1-1/2 minutes, the brick requires wetting.

G. Wetting of Brick:  Wet brick before laying if initial rate of absorption exceeds 30 g/30 sq. in. (30 g/194 sq. cm) per minute when tested per ASTM C 67.  Allow units to absorb water so they are damp but not wet at time of laying.

See Evaluations for discussion of tolerances.

H. Comply with construction tolerances in ACI 530.1/ASCE 6/TMS 602 and with the following:

1. For conspicuous vertical lines, such as external corners, door jambs, reveals, and expansion and control joints, do not vary from plumb by more than 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2 inch (12 mm) maximum.

2. For vertical alignment of exposed head joints, do not vary from plumb by more than 1/4 inch in 10 feet (6 mm in 3 m), or 1/2 inch (12 mm) maximum.

3. For conspicuous horizontal lines, such as lintels, sills, parapets, and reveals, do not vary from level by more than 1/8 inch in 10 feet (3 mm in 3 m), 1/4 inch in 20 feet (6 mm in 6 m), or 1/2 inch (12 mm) maximum.

If Type FBS Rough or Type FBA brick is used, revise tolerances in four subparagraphs below to allow for variation in brick size, or delete subparagraphs.  Consider restricting tolerances if Type FBX brick is used.

4. For exposed bed joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm), with a maximum thickness limited to 1/2 inch (12 mm).  Do not vary from bed-joint thickness of adjacent courses by more than 1/8 inch (3 mm).

5. For exposed head joints, do not vary from thickness indicated by more than plus or minus 1/8 inch (3 mm).  Do not vary from adjacent bed-joint and head-joint thicknesses by more than 1/8 inch (3 mm).

6. For faces of adjacent exposed masonry units, do not vary from flush alignment by more than 1/16 inch (1.5 mm) except due to warpage of masonry units within tolerances specified for warpage of units.

7. For exposed bed joints and head joints of stacked bond, do not vary from a straight line by more than 1/16 inch (1.5 mm) from one masonry unit to the next.

3.3 LAYING MASONRY WALLS

A. Lay out walls in advance for accurate spacing of surface bond patterns with uniform joint thicknesses and for accurate location of openings, movement-type joints, returns, and offsets.  Avoid using less-than-half-size units, particularly at corners, jambs, and, where possible, at other locations.

Pattern is usually running bond.  If other bond patterns are required, they must be specified in first paragraph below or indicated on Drawings.

B. Bond Pattern for Exposed Masonry:  Unless otherwise indicated, lay exposed masonry in [running bond] [stack bond] [one-third running bond] [Flemish bond] [English bond] [bond pattern indicated on Drawings]; do not use units with less than nominal 4-inch (100-mm) horizontal face dimensions at corners or jambs.

C. Lay concealed masonry with all units in a wythe in running bond or bonded by lapping not less than [2 inches (50 mm)] [4-inches (100-mm)].  Bond and interlock each course of each wythe at corners.  Do not use units with less than nominal 4-inch (100-mm) horizontal face dimensions at corners or jambs.

D. Stopping and Resuming Work:  Stop work by racking back units in each course from those in course below; do not tooth.  When resuming work, clean masonry surfaces that are to receive mortar, remove loose masonry units and mortar, and wet brick if required before laying fresh masonry.

E. Built-in Work:  As construction progresses, build in items specified in this and other Sections.  Fill in solidly with masonry around built-in items.

Revise paragraph below if flexible perimeter joint or thermal break is required.

F. Fill space between steel frames and masonry solidly with mortar, unless otherwise indicated.

Delete paragraph above and first paragraph below if not applicable.

G. Where built-in items are to be embedded in cores of hollow masonry units, place a layer of metal lath, wire mesh, or plastic mesh in the joint below and rod mortar or grout into core.

H. Fill cores in hollow concrete masonry units with grout 24 inches (600 mm) under bearing plates, beams, lintels, posts, and similar items, unless otherwise indicated.

I. Build non-load-bearing interior partitions full height of story to underside of solid floor or roof structure above, unless otherwise indicated.

Retain one or more of first three subparagraphs below or revise to suit Project.  Coordinate with firestopping requirements.  Retain first subparagraph if live-load deflection of structure above will produce stress in masonry.  Indicate on Drawings or add descriptive requirements to this Section for building walls around steel joists and similar construction if required.  Indicate joint-filler thickness on Drawings as well as details of connection required if structure acts as lateral support for partitions.

1. Install compressible filler in joint between top of partition and underside of structure above.

Spacing in first subparagraph below is an example only.

2. Fasten partition top anchors to structure above and build into top of partition.  Grout cells of CMUs solidly around plastic tubes of anchors and push tubes down into grout to provide 1/2-inch (13-mm) clearance between end of anchor rod and end of tube.  Space anchors [48 inches (1200 mm)] <Insert spacing> o.c., unless otherwise indicated.

3. Wedge non-load-bearing partitions against structure above with small pieces of tile, slate, or metal.  Fill joint with mortar after dead-load deflection of structure above approaches final position.

4. At fire-rated partitions, treat joint between top of partition and underside of structure above to comply with Division 07 Section "Fire-Resistive Joint Systems."

3.4 MORTAR BEDDING AND JOINTING

Delete first paragraph and subparagraphs below if no hollow concrete masonry units are required.  Mortar bedding of cross webs should be added if required.

A. Lay hollow [brick] [and] [concrete masonry units] as follows:

1. With face shells fully bedded in mortar and with head joints of depth equal to bed joints.

2. With webs fully bedded in mortar in all courses of piers, columns, and pilasters.

3. With webs fully bedded in mortar in grouted masonry, including starting course on footings.

4. With entire units, including areas under cells, fully bedded in mortar at starting course on footings where cells are not grouted.

B. Lay solid masonry units with completely filled bed and head joints; butter ends with sufficient mortar to fill head joints and shove into place.  Do not deeply furrow bed joints or slush head joints.

Delete first paragraph and subparagraphs below if structural-clay tile is not used.

C. Lay structural-clay tile as follows:

1. Lay vertical-cell units with full head joints, unless otherwise indicated.  Provide bed joints with full mortar coverage on face shells and webs.

2. Lay horizontal-cell units with full bed joints, unless otherwise indicated.  Keep drainage channels, if any, free of mortar.  Form head joints with sufficient mortar so excess will be squeezed out as units are placed in position.  Butter both sides of units to be placed, or butter one side of unit already in place and one side of unit to be placed.

3. Maintain joint thicknesses indicated except for minor variations required to maintain bond alignment.  If not indicated, lay walls with 1/4- to 3/8-inch- (6- to 10-mm-) thick joints.

4. Where epoxy-mortar pointed joints are indicated, rake out setting mortar to a uniform depth of 1/4 inch (6 mm) and point with epoxy mortar to comply with epoxy-mortar manufacturer's written instructions.

D. Set firebox brick in full bed of refractory mortar with full head joints.  Form joints by buttering both surfaces of adjoining brick and sliding it into place.  Make joints just wide enough to accommodate variations in size of brick, approximately 1/8 inch (3 mm).  Tool joints smooth on surfaces exposed to fire or smoke.

Delete paragraph above and below if no fireplaces.

E. Install clay flue liners to comply with ASTM C 1283.  Install flue liners ahead of surrounding masonry.  Set clay flue liners in full bed of refractory mortar 1/16 to 1/8 inch (1.6 to 3 mm) thick.  Strike joints flush on inside of flue to provide smooth surface.  Maintain expansion space between flue liner and surrounding masonry except where surrounding masonry is required to provide lateral support for flue liners.

Delete paragraph and subparagraphs below if no stone or cast-stone trim.

F. Set [stone] [cast-stone] trim units in full bed of mortar with full vertical joints.  Fill dowel, anchor, and similar holes.

1. Clean soiled surfaces with fiber brush and soap powder and rinse thoroughly with clear water.

2. Allow cleaned surfaces to dry before setting.

Retain subparagraph above for relatively impervious stones such as granite; retain subparagraph below for absorptive stones such as limestone and sandstone and for cast stone.

3. Wet joint surfaces thoroughly before applying mortar.

If another joint profile is used, revise first paragraph below or show on Drawings.

G. Tool exposed joints slightly concave when thumbprint hard, using a jointer larger than joint thickness, unless otherwise indicated.

Delete subparagraph below if no glazed masonry units.

1. For glazed masonry units, use a nonmetallic jointer 3/4 inch (19 mm) or more in width.

H. Cut joints flush for masonry walls to receive plaster or other direct-applied finishes (other than paint), unless otherwise indicated.

3.5 COMPOSITE MASONRY

A. Bond wythes of composite masonry together using one of the following methods:

Retain one or more bonding methods in three subparagraphs and associated subparagraphs below; edit methods retained to suit Project and office practice.

Revise spacings in subparagraph below to suit coursing, to comply with requirements of authorities having jurisdiction, or to comply with structural requirements imposed by wind or seismic forces.  Spacings are for wire ties 0.188 inch (4.8 mm) in diameter, wire ties 0.148 inch (3.8 mm) in diameter, and adjustable 2-piece ties, respectively.

1. Individual Metal Ties:  Provide ties as shown installed in horizontal joints, but not less than one metal tie for [4.5 sq. ft. (0.42 sq. m)] [2.67 sq. ft. (0.25 sq. m)] [1.77 sq. ft. (0.16 sq. m)] of wall area spaced not to exceed [36 inches (914 mm)] [24 inches (610 mm)] [16 inches (406 mm)] o.c. horizontally and 16 inches (406 mm) o.c. vertically.  Stagger ties in alternate courses.  Provide additional ties within 12 inches (305 mm) of openings and space not more than 36 inches (915 mm) apart around perimeter of openings.  At intersecting and abutting walls, provide ties at no more than 24 inches (610 mm) o.c. vertically.

Delete first subparagraph below if not required.

a. Where bed joints of wythes do not align, use adjustable (two-piece) type ties.

2. Masonry Joint Reinforcement:  Installed in horizontal mortar joints.

Delete one or both subparagraphs below if not required.

a. Where bed joints of both wythes align, use [ladder-type reinforcement extending across both wythes] [tab-type reinforcement].

b. Where bed joints of wythes do not align, use adjustable (two-piece) type reinforcement[ with continuous horizontal wire in facing wythe attached to ties].

First option in subparagraph below provides headers equal to 4 percent of wall area for standard modular-size brick; second option provides 4 percent coverage for thicker brick.

3. Header Bonding:  Provide masonry unit headers extending not less than 3 inches (76 mm) into each wythe.  Space headers not over [8 inches (203 mm)] [12 inches (305 mm)] clear horizontally and 16 inches (406 mm) clear vertically.

Delete paragraph and subparagraphs above and retain first paragraph below if bonding system is indicated on Drawings.

B. Bond wythes of composite masonry together using bonding system indicated on Drawings.

C. Collar Joints:  Solidly fill collar joints by parging face of first wythe that is laid and shoving units of other wythe into place.

Delete first paragraph below if no clay tile masonry.  Retain all options if full collar joints are required for all walls and partitions, or edit for limited requirements.  Solid collar joints are required if sum of all wythes is needed to comply with height-to-thickness ratio requirements.

D. Collar Joints in Clay Tile Masonry:  After each course is laid, fill the vertical, longitudinal joint between wythes solidly with mortar at [exterior walls, except cavity walls] [, and] [interior walls and partitions].

E. Corners:  Provide interlocking masonry unit bond in each wythe and course at corners, unless otherwise indicated.

Delete subparagraph below if masonry joint reinforcement is not used.

1. Provide continuity with masonry joint reinforcement at corners by using prefabricated L-shaped units as well as masonry bonding.

F. Intersecting and Abutting Walls:  Unless vertical expansion or control joints are shown at juncture, bond walls together as follows:

Select one of three subparagraphs below and revise to suit Project.  If more than one type of bonding is required, revise subparagraphs and show locations of each on Drawings.

1. Provide individual metal ties not more than [8 inches (203 mm)] [16 inches (406 mm)] o.c.

2. Provide continuity with masonry joint reinforcement by using prefabricated T-shaped units.

3. Provide rigid metal anchors not more than [24 inches (610 mm)] [48 inches (1220 mm)] o.c.  If used with hollow masonry units, embed ends in mortar-filled cores.

3.6 CAVITY WALLS

Delete this Article if cavity walls are not used.

A. Bond wythes of cavity walls together using one of the following methods:

Retain one or more bonding methods in four subparagraphs and associated subparagraphs below; edit methods retained to suit Project and office practice.

Revise spacings in subparagraph below to suit coursing, to comply with requirements of authorities having jurisdiction, or to comply with structural requirements imposed by wind or seismic forces.  Spacings are for wire ties 0.188 inch (4.8 mm) in diameter, wire ties 0.148 inch (3.8 mm) in diameter, and adjustable 2-piece ties, respectively.

1. Individual Metal Ties:  Provide ties as shown installed in horizontal joints, but not less than one metal tie for [4.5 sq. ft. (0.42 sq. m)] [2.67 sq. ft. (0.25 sq. m)] [1.77 sq. ft. (0.16 sq. m)] of wall area spaced not to exceed [36 inches (914 mm)] [24 inches (610 mm)] [16 inches (406 mm)] o.c. horizontally and 16 inches (406 mm) o.c. vertically.  Stagger ties in alternate courses.  Provide additional ties within 12 inches (305 mm) of openings and space not more than 36 inches (915 mm) apart around perimeter of openings.  At intersecting and abutting walls, provide ties at no more than 24 inches (610 mm) o.c. vertically.

Delete one or both of first two subparagraphs below if not required.

a. Where bed joints of wythes do not align, use adjustable (two-piece) type ties.

b. Where one wythe is of clay masonry and the other of concrete masonry, use adjustable (two-piece) type ties to allow for differential movement regardless of whether bed joints align.

2. Masonry Joint Reinforcement:  Installed in horizontal mortar joints.

Delete any of three subparagraphs below if not required.

a. Where bed joints of both wythes align, use [ladder-type reinforcement extending across both wythes] [tab-type reinforcement].

b. Where bed joints of wythes do not align, use adjustable (two-piece) type reinforcement[ with continuous horizontal wire in facing wythe attached to ties].

c. Where one wythe is of clay masonry and the other of concrete masonry, use adjustable (two-piece) type reinforcement[ with continuous horizontal wire in facing wythe attached to ties] to allow for differential movement regardless of whether bed joints align.

First option in first subparagraph below provides headers equal to 4 percent of wall area for standard modular-size brick; second option provides 4 percent coverage for thicker brick.

3. Header Bonding:  Provide masonry unit headers extending not less than 3 inches (76 mm) into each wythe.  Space headers not over [8 inches (203 mm)] [12 inches (305 mm)] clear horizontally and 16 inches (406 mm) clear vertically.

4. Masonry Veneer Anchors:  Comply with requirements for anchoring masonry veneers.

Delete paragraph and subparagraphs above and retain paragraph below if bonding system is indicated on Drawings.

B. Bond wythes of cavity walls together using bonding system indicated on Drawings.

Attempting to remove mortar fins from cavity or to trowel them flat against brick usually results in increased mortar droppings at base of cavity.

C. Keep cavities clean of mortar droppings and other materials during construction.  Bevel beds away from cavity, to minimize mortar protrusions into cavity.  Do not attempt to trowel or remove mortar fins protruding into cavity.

D. Parge cavity face of backup wythe in a single coat approximately 3/8 inch (10 mm) thick.  Trowel face of parge coat smooth.

Delete paragraph above or below, or both.  For higher quality, a parge coat can be combined with bituminous dampproofing applied over the parging.  Either coating can provide an air barrier that will prevent wind pressure from driving water through inner wythe.  Note that cracks may allow water leakage through coating and that it may be easier to coat inside face of inner wythe to provide air barrier.  See Evaluations.

E. Coat cavity face of backup wythe to comply with Division 07 Section "Bituminous Dampproofing."

Delete paragraph and subparagraph below if cavities are not insulated; revise if adhesive is not used.

F. Installing Cavity-Wall Insulation:  Place small dabs of adhesive, spaced approximately 12 inches (300 mm) o.c. both ways, on inside face of insulation boards, or attach with plastic fasteners designed for this purpose.  Fit courses of insulation between wall ties and other confining obstructions in cavity, with edges butted tightly both ways.  Press units firmly against inside wythe of masonry or other construction as shown.

1. Fill cracks and open gaps in insulation with crack sealer compatible with insulation and masonry.

3.7 MASONRY-CELL INSULATION

Delete paragraph below if granular insulation is not used.

A. Pour granular insulation into cavities to fill void spaces.  Maintain inspection ports to show presence of insulation at extremities of each pour area.  Close the ports after filling has been confirmed.  Limit the fall of insulation to 1 story in height, but not more than 20 feet (6 m).

Delete paragraph below if molded-polystyrene insulation units are not used.

B. Install molded-polystyrene insulation units into masonry unit cells before laying units.

3.8 MASONRY JOINT REINFORCEMENT

A. General:  Install entire length of longitudinal side rods in mortar with a minimum cover of 5/8 inch (16 mm) on exterior side of walls, 1/2 inch (13 mm) elsewhere.  Lap reinforcement a minimum of 6 inches (150 mm).

Revise subparagraph below if different spacing is required; delete if shown on Drawings.

1. Space reinforcement not more than 16 inches (406 mm) o.c.

Delete one or both subparagraphs below if not required.

2. Space reinforcement not more than 8 inches (203 mm) o.c. in foundation walls and parapet walls.

3. Provide reinforcement not more than 8 inches (203 mm) above and below wall openings and extending 12 inches (305 mm) beyond openings.

Delete subparagraph below if not required.

a. Reinforcement above is in addition to continuous reinforcement.

B. Interrupt joint reinforcement at control and expansion joints, unless otherwise indicated.

First paragraph below can be deleted if rigid anchors are used to bond walls at intersections.

C. Provide continuity at wall intersections by using prefabricated T-shaped units.

D. Provide continuity at corners by using prefabricated L-shaped units.

Retain paragraph above or option in paragraph below.

E. Cut and bend reinforcing units as directed by manufacturer for continuity at[ corners,] returns, offsets, column fireproofing, pipe enclosures, and other special conditions.

3.9 ANCHORING MASONRY TO STRUCTURAL MEMBERS

A. Anchor masonry to structural members where masonry abuts or faces structural members to comply with the following:

1. Provide an open space not less than [1/2 inch (13 mm)] [1 inch (25 mm)] in width between masonry and structural member, unless otherwise indicated.  Keep open space free of mortar and other rigid materials.

2. Anchor masonry to structural members with anchors embedded in masonry joints and attached to structure.

3. Space anchors as indicated, but not more than 24 inches (610 mm) o.c. vertically and 36 inches (915 mm) o.c. horizontally.

3.10 ANCHORING MASONRY VENEERS

A. Anchor masonry veneers to [wall framing] [concrete and masonry backup] with[ seismic] masonry-veneer anchors to comply with the following requirements:

1. Fasten [screw-attached] [and] [seismic] anchors [through sheathing to wall framing] [and] [to concrete and masonry backup] with metal fasteners of type indicated.  Use two fasteners unless anchor design only uses one fastener.

2. Insert slip-in anchors in metal studs as sheathing is installed.  Provide one anchor at each stud in each horizontal joint between sheathing boards.

BIA Technical Notes 28B recommends 2 inches (50 mm) of air space.  Wider air spaces require closer tie spacing.

3. Embed [tie sections] [connector sections and continuous wire] in masonry joints.  Provide not less than 2 inches (50 mm) of air space between back of masonry veneer and face of sheathing.

4. Locate anchor sections to allow maximum vertical differential movement of ties up and down.

5. Space anchors as indicated, but not more than 18 inches (458 mm) o.c. vertically and 24 inches (610 mm) o.c. horizontally, with not less than 1 anchor for each 2 sq. ft. (0.2 sq. m) of wall area.  Install additional anchors within 12 inches (305 mm) of openings and at intervals, not exceeding 8 inches (203 mm), around perimeter.

Retain subparagraph above or below to suit Project.  Revise veneer anchor spacing to suit coursing, to comply with requirements of authorities having jurisdiction, or to comply with structural requirements imposed by wind or seismic forces.  Above is BIA recommendation for metal-stud construction.  Below is based on the 2002 MSJC Code.  Closer spacing is for adjustable 2-piece anchors, wire anchors 0.148 inch (3.8 mm) in diameter, and corrugated sheet metal anchors; wider spacing is for all other anchors.

6. Space anchors as indicated, but not more than 16 inches (406 mm) o.c. vertically and [32 inches (813 mm)] [24 inches (610 mm)] o.c. horizontally with not less than 1 anchor for each [3.5 sq. ft. (0.33 sq. m)] [2.67 sq. ft. (0.25 sq. m)] of wall area.  Install additional anchors within 12 inches (305 mm) of openings and at intervals, not exceeding 36 inches (914 mm), around perimeter.

3.11 CONTROL AND EXPANSION JOINTS

A. General:  Install control and expansion joint materials in unit masonry as masonry progresses.  Do not allow materials to span control and expansion joints without provision to allow for in-plane wall or partition movement.

Show locations of joints on Drawings.

B. Form control joints in concrete masonry [as follows] [using one of the following methods]:

Retain one or more of four subparagraphs below.

1. Fit bond-breaker strips into hollow contour in ends of concrete masonry units on one side of control joint.  Fill resultant core with grout and rake out joints in exposed faces for application of sealant.

2. Install preformed control-joint gaskets designed to fit standard sash block.

3. Install interlocking units designed for control joints.  Install bond-breaker strips at joint.  Keep head joints free and clear of mortar or rake out joint for application of sealant.

4. Install temporary foam-plastic filler in head joints and remove filler when unit masonry is complete for application of sealant.

C. Form expansion joints in brick made from clay or shale as follows:

Retain one or more of first three subparagraphs below.

1. Build flanges of metal expansion strips into masonry.  Lap each joint 4 inches (100 mm) in direction of water flow.  Seal joints below grade and at junctures with horizontal expansion joints if any.

2. Build flanges of factory-fabricated, expansion-joint units into masonry.

3. Build in compressible joint fillers where indicated.

4. Form open joint full depth of brick wythe and of width indicated, but not less than [3/8 inch (10 mm)] [1/2 inch (13 mm)] <Insert minimum width> for installation of sealant and backer rod specified in Division 07 Section "Joint Sealants."

D. Provide horizontal, pressure-relieving joints by either leaving an air space or inserting a compressible filler of width required for installing sealant and backer rod specified in Division 07 Section "Joint Sealants," but not less than [3/8 inch (10 mm)] <Insert minimum width>.

Revise subparagraph below to suit Project.  Show locations of joints on Drawings.  See BIA and NCMA references.

1. Locate horizontal, pressure-relieving joints beneath shelf angles supporting masonry.

3.12 LINTELS

Delete this Article if steel and masonry lintels are not required.  Delete types of lintels not required.  Coordinate with Division 05 Section "Metal Fabrications."

A. Install steel lintels where indicated.

B. Provide [concrete] [or] [masonry] lintels where shown and where openings of more than 12 inches (305 mm) for brick-size units and 24 inches (610 mm) for block-size units are shown without structural steel or other supporting lintels.

Delete paragraph below if bearing is shown on Drawings.

C. Provide minimum bearing of 8 inches (200 mm) at each jamb, unless otherwise indicated.

3.13 FLASHING, WEEP HOLES, CAVITY DRAINAGE, AND VENTS

Retain option in first paragraph below if wall is designed on rain-screen principle with vents acting to equalize air-pressure differential between cavity and exterior.  Indicate spacing of vents and blocking on Drawings.  See Evaluations.

A. General:  Install embedded flashing and weep holes in masonry at shelf angles, lintels, ledges, other obstructions to downward flow of water in wall, and where indicated.[  Install vents at shelf angles, ledges, and other obstructions to upward flow of air in cavities, and where indicated.]

B. Install flashing as follows, unless otherwise indicated:

1. Prepare masonry surfaces so they are smooth and free from projections that could puncture flashing.  Where flashing is within mortar joint, place through-wall flashing on sloping bed of mortar and cover with mortar.  Before covering with mortar, seal penetrations in flashing with adhesive, sealant, or tape as recommended by flashing manufacturer.

Retain any of nine subparagraphs below and revise to suit wall configurations used.  Arrangement of flashing can be communicated better by detailing on Drawings rather than by relying on any of the nine subparagraphs.

2. At multiwythe masonry walls, including cavity walls, extend flashing through outer wythe, turned up a minimum of [4 inches (100 mm)] [8 inches (200 mm)], and through inner wythe to within 1/2 inch (13 mm) of the interior face of wall in exposed masonry.  Where interior face of wall is to receive furring or framing, carry flashing completely through inner wythe and turn flashing up approximately 2 inches (50 mm) on interior face.

Retain subparagraph above or below if multiwythe masonry walls are used.  NCMA recommends against extending flashing through inner wythe.  Delete last option below if metal is not used.

3. At multiwythe masonry walls, including cavity walls, extend flashing through outer wythe, turned up a minimum of [4 inches (100 mm)] [8 inches (200 mm)], and 1-1/2 inches (38 mm) into the inner wythe.[  Form 1/4-inch (6-mm) hook in edge of flashing embedded in inner wythe.]

Delete first subparagraph below if no masonry veneer over sheathing and studs.

4. At masonry-veneer walls, extend flashing through veneer, across air space behind veneer, and up face of sheathing at least 8 inches (200 mm); with upper edge tucked under building paper or building wrap, lapping at least 4 inches (100 mm).

5. At lintels and shelf angles, extend flashing a minimum of 6 inches (150 mm) into masonry at each end.  At heads and sills, extend flashing 6 inches (150 mm) at ends and turn up not less than 2 inches (50 mm) to form end dams.

Delete two subparagraphs below if ribbed sheet metal flashing is not used.

6. Interlock end joints of ribbed sheet metal flashing by overlapping ribs not less than 1-1/2 inches (38 mm) or as recommended by flashing manufacturer, and seal lap with elastomeric sealant complying with requirements in Division 07 Section "Joint Sealants" for application indicated.

7. Install metal [drip edges] [and] [sealant stops] with ribbed sheet metal flashing by interlocking hemmed edges to form hooked seam.  Seal seam with elastomeric sealant complying with requirements in Division 07 Section "Joint Sealants" for application indicated.

Retain one of three subparagraphs below if flexible flashing materials are used.  See Evaluations.

8. Install metal drip edges beneath flexible flashing at exterior face of wall.  Stop flexible flashing 1/2 inch (13 mm) back from outside face of wall and adhere flexible flashing to top of metal drip edge.

9. Install metal flashing termination beneath flexible flashing at exterior face of wall.  Stop flexible flashing 1/2 inch (13 mm) back from outside face of wall and adhere flexible flashing to top of metal flashing termination.

10. Cut flexible flashing off flush with face of wall after masonry wall construction is completed.

C. Install single-wythe CMU flashing system in bed joints of CMU walls where indicated to comply with manufacturer's written instructions.  Install CMU cell pans with upturned edges located below face shells and webs of CMUs above and with weep spouts aligned with face of wall.  Install CMU web covers so that they cover upturned edges of CMU cell pans at CMU webs and extend from face shell to face shell.

Delete first paragraph below if built-in reglets and nailers are not used.

D. Install reglets and nailers for flashing and other related construction where they are shown to be built into masonry.

E. Install weep holes in head joints in exterior wythes of first course of masonry immediately above embedded flashing and as follows:

1. Use [specified weep/vent products] [or] [open head joints] to form weep holes.

2. Use wicking material to form weep holes above flashing under brick sills.  Turn wicking down at lip of sill to be as inconspicuous as possible.

3. Space weep holes 24 inches (600 mm) o.c., unless otherwise indicated.

Retain subparagraph above if weep holes other than plastic tubing or wicking are used.  Retain subparagraph below if plastic tubing or wicking is used.

4. Space weep holes formed from [plastic tubing] [or] [wicking material] 16 inches (400 mm) o.c.

Delete subparagraph below if loose-fill insulation is not used or if weep holes do not require screening.

5. Cover cavity side of weep holes with plastic insect screening at cavities insulated with loose-fill insulation.

Delete subparagraph below if wicking is not used.

6. Trim wicking material flush with outside face of wall after mortar has set.

F. Place pea gravel in cavities as soon as practical to a height equal to height of first course above top of flashing, but not less than 2 inches (50 mm), to maintain drainage.

Delete subparagraph below if pea gravel is not used full height in cavities.

1. Fill cavities full height by placing pea gravel in cavities as masonry is laid so that at any point masonry does not extend more than 24 inches (600 mm) above top of pea gravel.

Delete paragraph and subparagraph above and paragraph below if cavity walls are not used.  Retain applicable products in Part 2 if retaining below.

G. Place cavity drainage material in cavities to comply with configuration requirements for cavity drainage material in Part 2 "Miscellaneous Masonry Accessories" Article.

Retain paragraph and subparagraph below if wall is designed on rain-screen principle with vents acting to equalize air-pressure differential between cavity and exterior.  Indicate spacing of vents and blocking on Drawings.  See Evaluations.

H. Install vents in head joints in exterior wythes at spacing indicated.  Use [specified weep/vent products] [or] [open head joints] to form vents.

1. Close cavities off vertically and horizontally with blocking in manner indicated.  Install through-wall flashing and weep holes above horizontal blocking.

3.14 REINFORCED UNIT MASONRY INSTALLATION

Usually retain first paragraph and subparagraphs below only if reinforced masonry beams, slabs, soffits, and similarly formed elements are required.

A. Temporary Formwork and Shores:  Construct formwork and shores as needed to support reinforced masonry elements during construction.

1. Construct formwork to provide shape, line, and dimensions of completed masonry as indicated.  Make forms sufficiently tight to prevent leakage of mortar and grout.  Brace, tie, and support forms to maintain position and shape during construction and curing of reinforced masonry.

2. Do not remove forms and shores until reinforced masonry members have hardened sufficiently to carry their own weight and other temporary loads that may be placed on them during construction.

B. Placing Reinforcement:  Comply with requirements in [ACI 530.1/ASCE 6/TMS 602] [Section 2104.5 in the Uniform Building Code].

C. Grouting:  Do not place grout until entire height of masonry to be grouted has attained enough strength to resist grout pressure.

1. Comply with requirements in [ACI 530.1/ASCE 6/TMS 602] [Section 2104.6 in the Uniform Building Code] for cleanouts and for grout placement, including minimum grout space and maximum pour height.

Retain subparagraph below unless high-lift grouting is allowed.  See Evaluations.  ACI 530.1/ASCE 6/TMS 602 limits grout lifts to 60 inches (1520 mm) unless an accepted grout demonstration panel is used to establish alternative grout placement methods.

2. Limit height of vertical grout pours to not more than [60 inches (1520 mm)] <Insert height>.

3.15 FIELD QUALITY CONTROL

See Editing Instruction No. 3 in the Evaluations before editing this Article.

A. Inspectors:  Owner will engage qualified independent inspectors to perform inspections and prepare reports.  Allow inspectors access to scaffolding and work areas, as needed to perform inspections.

Consider inserting a subparagraph listing inspections that will be performed.  Delete subparagraph below if not required.

1. Place grout only after inspectors have verified compliance of grout spaces and grades, sizes, and locations of reinforcement.

B. Testing Agency:  Owner will engage a qualified independent testing and inspecting agency to perform field tests and inspections indicated below and prepare test reports:

1. Payment for these services will be made [by Owner] [from Testing and Inspecting Allowance, as authorized by Change Orders].

2. Retesting of materials failing to comply with specified requirements shall be done at Contractor's expense.

Testing frequency in first paragraph below is from the 2002 MSJC Code and the 1997 Uniform Building Code.

C. Testing Frequency:  One set of tests for each 5000 sq. ft. (465 sq. m) of wall area or portion thereof.

D. Clay Masonry Unit Test:  For each type of unit provided, per ASTM C 67.

Retain paragraph above and first paragraph below if unit-strength method is used unless authorities having jurisdiction allow units to be tested as source quality control.  Delete both if retaining prism-test method.

E. Concrete Masonry Unit Test:  For each type of unit provided, per ASTM C 140.

If retaining paragraph below, select either or both tests listed; insert others if required.  Testing for mortar air content is especially desirable for reinforced masonry.  Testing for compressive strength is desirable if the property specification for mortar is used.

F. Mortar Test (Property Specification):  For each mix provided, per [ASTM C 780] [UBC Standard 21-16].  Test mortar for [mortar air content] [and] [compressive strength].

Paragraph above and below may be deleted if retaining prism test.  Paragraph above may also be deleted if mortar is specified to comply with proportion specification; paragraph below may also be deleted if grout is specified by proportions stated in ASTM C 476 or UBC Standard 21-19 rather than by compressive strength.

G. Grout Test (Compressive Strength):  For each mix provided, per [ASTM C 1019] [UBC Standard 21-18].

Usually retain appropriate test methods above.  Retain paragraph below only if prism test is specified in Part 1 "Performance Requirements" Article for determining compressive strength of masonry.  Delete last option below if seven-day tests are not required.

H. Prism Test:  For each type of construction provided, per [ASTM C 1314] [UBC Standard 21-17] at [7 days and at ]28 days.

3.16 PARGING

A. Parge exterior faces of below-grade masonry walls, where indicated, in 2 uniform coats to a total thickness of 3/4 inch (19 mm).  Dampen wall before applying first coat and scarify first coat to ensure full bond to subsequent coat.

B. Use a steel-trowel finish to produce a smooth, flat, dense surface with a maximum surface variation of 1/8 inch per foot (3 mm per 300 mm).  Form a wash at top of parging and a cove at bottom.

C. Damp-cure parging for at least 24 hours and protect parging until cured.

3.17 REPAIRING, POINTING, AND CLEANING

A. Remove and replace masonry units that are loose, chipped, broken, stained, or otherwise damaged or that do not match adjoining units.  Install new units to match adjoining units; install in fresh mortar, pointed to eliminate evidence of replacement.

B. Pointing:  During the tooling of joints, enlarge voids and holes, except weep holes, and completely fill with mortar.  Point up joints, including corners, openings, and adjacent construction, to provide a neat, uniform appearance.  Prepare joints for sealant application, where indicated.

C. In-Progress Cleaning:  Clean unit masonry as work progresses by dry brushing to remove mortar fins and smears before tooling joints.

D. Final Cleaning:  After mortar is thoroughly set and cured, clean exposed masonry as follows:

1. Remove large mortar particles by hand with wooden paddles and nonmetallic scrape hoes or chisels.

2. Test cleaning methods on sample wall panel; leave one-half of panel uncleaned for comparison purposes.  Obtain Architect's approval of sample cleaning before proceeding with cleaning of masonry.

3. Protect adjacent stone and nonmasonry surfaces from contact with cleaner by covering them with liquid strippable masking agent or polyethylene film and waterproof masking tape.

Delete subparagraph above and first subparagraph below if cleaners are not specified in Part 2 or if cleaners are not allowed.

4. Wet wall surfaces with water before applying cleaners; remove cleaners promptly by rinsing surfaces thoroughly with clear water.

5. Clean brick by bucket-and-brush hand-cleaning method described in BIA Technical Notes 20.

Retain subparagraph above or first subparagraph below.  Coordinate with products retained in Part 2.  If high-pressure water cleaning or other methods are acceptable, delete or revise below and insert applicable requirements.

6. Clean masonry with a proprietary acidic cleaner applied according to manufacturer's written instructions.

7. Clean concrete masonry by cleaning method indicated in NCMA TEK 8-2A applicable to type of stain on exposed surfaces.

Delete subparagraph below if no stone trim.

8. Clean stone trim to comply with stone supplier's written instructions.

Delete subparagraph below if no limestone trim.

9. Clean limestone units to comply with recommendations in ILI's "Indiana Limestone Handbook."

3.18 MASONRY WASTE DISPOSAL

A. Salvageable Materials:  Unless otherwise indicated, excess masonry materials are Contractor's property.  At completion of unit masonry work, remove from Project site.

Retain first paragraph and subparagraphs below if clean masonry waste can be used as fill in footing trenches, etc.  This diverts some material from waste stream, conserving landfill space and energy required to haul waste away.

B. Waste Disposal as Fill Material:  Dispose of clean masonry waste, including excess or soil-contaminated sand, waste mortar, and broken masonry units, by crushing and mixing with fill material as fill is placed.

1. Crush masonry waste to less than 4 inches (100 mm) in each dimension.

2. Mix masonry waste with at least two parts of specified fill material for each part of masonry waste.  Fill material is specified in Division 31 Section "Earth Moving."

Generally retain subparagraph below.  If required, increase limit if acid-soil plants are used for foundation plantings.

3. Do not dispose of masonry waste as fill within 18 inches (450 mm) of finished grade.

C. Excess Masonry Waste:  Remove excess clean masonry waste that cannot be used as fill, as described above, and other masonry waste, and legally dispose of off Owner's property.

END OF SECTION 042000

	UNIT MASONRY
	042000 - 1



