Copyright 2006 AIA
MASTERSPEC Full Length
02/06

Copyright 2006 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 061063 - EXTERIOR ROUGH CARPENTRY
Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. Section Includes:

1. Elevated decks including [wood decking] [plastic decking] [stairs] [railings] [and] [support framing].

2. Wood benches.

B. Related Sections:

Retain Sections in subparagraphs below that contain requirements Contractor might expect to find in this Section but are specified in other Sections.

1. Division 06 Section "Sheathing" for flexible flashing installed behind ledgers.

2. Division 06 Section "Exterior Finish Carpentry."

Retain subparagraph below if using sheet metal flashing on tops of deck framing and ledgers.

3. Division 07 Section "Sheet Metal Flashing and Trim" for sheet metal flashing used with exterior rough carpentry.

1.3 DEFINITIONS

Retain definition(s) remaining after this Section has been edited.

A. Boards:  Lumber of less than 2 inches nominal (38 mm actual) in thickness and 2 inches nominal (38 mm actual) or greater width.

B. Dimension Lumber:  Lumber of 2 inches nominal (38 mm actual) or greater but less than 5 inches nominal (114 mm actual) in least dimension.

C. Timber:  Lumber of 5 inches nominal (114 mm actual) or greater in least dimension.

Retain paragraph and list below if lumber grading agencies are referenced with products.

D. Lumber grading agencies, and the abbreviations used to reference them, include the following:

Coordinate list below with product lists; delete those not required.  See Evaluations.

1. NeLMA:  Northeastern Lumber Manufacturers' Association.

2. NLGA:  National Lumber Grades Authority.

3. RIS:  Redwood Inspection Service.

4. SPIB:  The Southern Pine Inspection Bureau.

5. WCLIB:  West Coast Lumber Inspection Bureau.

6. WWPA:  Western Wood Products Association.

1.4 SUBMITTALS

First three paragraphs below are defined in Division 01 Section "Submittal Procedures" as "Action Submittals."

A. Product Data:  For [preservative-treated wood products] [plastic decking] [and] [metal framing anchors].

1. For preservative-treated wood products, include chemical treatment manufacturer's written instructions for handling, storing, installing, and finishing treated material.

2. For [plastic decking] [and] [metal framing anchors], include installation instructions.

B. LEED Submittal:

Retain subparagraph below and "Forest Certification" Paragraph in "Quality Assurance" Article if wood products are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.

1. Certificates for Credit MR 7:  Chain-of-custody certificates certifying that wood products comply with forest certification requirements.  Include evidence that manufacturer is certified for chain of custody by an FSC-accredited certification body.

C. Samples:  For plastic decking, not less than 24 inches (600 mm) long, showing the range of variation to be expected in appearance, including surface texture.

Remaining paragraphs are defined in Division 01 Section "Submittal Procedures" as "Informational Submittals."

D. Material Certificates:

Delete first subparagraph below if species and grade are indicated for each use.

1. For lumber specified to comply with minimum allowable unit stresses.  Indicate species and grade selected for each use and design values approved by ALSC's Board of Review.

2. For preservative-treated wood products.  Indicate type of preservative used and net amount of preservative retained.[  For products receiving a waterborne treatment, include statement that moisture content of treated materials was reduced to levels specified before shipment to Project site.]

E. Certificates of Inspection:  Issued by lumber grading agency for exposed wood products not marked with grade stamp.

F. Evaluation Reports:  For the following, from <Insert applicable model code organization>:

Revise list below to retain only those products retained in Part 2.

1. Preservative-treated wood products.

2. Plastic decking.

3. Expansion anchors.

4. Metal framing anchors.

5. Decking fasteners.

1.5 QUALITY ASSURANCE

Retain this article if wood products are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.

A. Forest Certification:  Provide wood products obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

1.6 DELIVERY, STORAGE, AND HANDLING

A. Store materials under cover and protected from weather and contact with damp or wet surfaces.  Stack lumber flat with spacers between each bundle to provide air circulation.  Provide for air circulation around stacks and under coverings.

B. Handle and store plastic lumber to comply with manufacturer's written instructions.

PART 2 -  PRODUCTS

2.1 LUMBER, GENERAL

A. Lumber:  Comply with DOC PS 20 and with applicable rules of grading agencies indicated.  If no grading agency is indicated, provide lumber that complies with the applicable rules of any rules-writing agency certified by ALSC's Board of Review.  Provide lumber graded by an agency certified by ALSC's Board of Review to inspect and grade lumber under the rules indicated.

1. Factory mark each item with grade stamp of grading agency.

Retain first option in first subparagraph below if authorities having jurisdiction require grade stamps on all materials.

2. For items that are exposed to view in the completed Work, [mark grade stamp on end or back of each piece] [or] [omit grade stamp and provide certificates of grade compliance issued by grading agency].

In DOC PS 20, dressed sizes of green lumber are larger than dry lumber.

3. Where nominal sizes are indicated, provide actual sizes required by DOC PS 20 for moisture content specified.  Where actual sizes are indicated, they are minimum dressed sizes for dry wood products.

4. Provide dressed lumber, S4S, unless otherwise indicated.

2.2 DIMENSION LUMBER

Retain one of five options in first paragraph below or delete paragraph if green lumber is acceptable in all thicknesses.  Verify availability of lumber with 15 percent maximum moisture content before retaining.  Lumber more than 2-inch nominal (38-mm actual) thickness is often shipped green.

A. Maximum Moisture Content:  [15 percent] [19 percent] [15 percent for 2-inch nominal (38-mm actual) thickness or less; 19 percent for more than 2-inch nominal (38-mm actual) thickness] [15 percent for 2-inch nominal (38-mm actual) thickness or less; no limit for more than 2-inch nominal (38-mm actual) thickness] [19 percent for 2-inch nominal (38-mm actual) thickness or less; no limit for more than 2-inch nominal (38-mm actual) thickness].

First paragraph below can provide high-quality appearance, but will add cost and can require extra effort to enforce.  Delete if species and grades retained in paragraphs below are suitable without revision.  Revise title if applicable only to certain items, such as railings and benches.

B. Exposed Lumber:  Provide material hand selected for freedom from characteristics, on exposed surfaces and edges, that would impair finish appearance, including decay, honeycomb, knot holes, shake, splits, torn grain, and wane.

If retaining first paragraph below, retain one of five options for grade; verify with structural requirements.  Generally retain "No. 2" or "Construction or No. 2" option for best economy if grades meet structural requirements.

C. Deck[ and Stair] Framing:  [Select Structural] [No. 1] [No. 2] [Construction or No. 2] [Construction, Stud, or No. 3] grade and[ any of] the following species:

Revise list below; usually retain all species that meet requirements except those not available in Project's location.  Species groups are listed in order of decreasing strength (extreme fiber in bending).

1. Hem-fir (North); NLGA.

2. Southern pine; SPIB.

3. Douglas fir-larch; WCLIB or WWPA.

Species group in first subparagraph below includes "Southern pine" above; delete subparagraph above if retaining first subparagraph below.

4. Mixed southern pine; SPIB.

5. Spruce-pine-fir; NLGA.

6. Douglas fir-south; WWPA.

7. Hem-fir; WCLIB or WWPA.

8. Douglas fir-larch (North); NLGA.

9. Spruce-pine-fir (South); NeLMA, WCLIB, or WWPA.

First paragraph below is an example of a performance requirement that can be used instead of last paragraph above.  If retaining, select options or revise values and insert other properties to suit structural requirements of Project.

D. Deck[ and Stair] Framing:  Any species and grade with a modulus of elasticity of at least [1,500,000 psi (10 350 MPa)] [1,300,000 psi (8970 MPa)] [1,100,000 psi (7590 MPa)] [1,000,000 psi (6900 MPa)] [900,000 psi (6210 MPa)] and an extreme fiber stress in bending of at least [1000 psi (6.9 MPa)] [850 psi (5.86 MPa)] [700 psi (4.83 MPa)] [600 psi (4.14 MPa)] [500 psi (3.45 MPa)] for 2-inch nominal (38-mm actual) thickness and 12-inch nominal (286-mm actual) width for single-member use.

Retain first paragraph below if rectangular or square posts less than 5 inches nominal (114 mm actual) in least dimension are required; otherwise, delete and specify posts as timber or as round wood poles.

E. Dimension Lumber Posts:  [No. 2] [Construction or No. 2] [Construction, Stud, or No. 3] grade and[ any of] the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Spruce-pine-fir or spruce-pine-fir (South); NeLMA, NLGA, WCLIB, or WWPA.

Species group in first subparagraph below includes hem-fir (North) and spruce-pine-fir.

5. Northern species; NLGA.

Species group in first subparagraph below includes spruce-pine-fir (South).

6. Eastern softwoods; NeLMA.

Species group in subparagraph below includes hem-fir and spruce-pine-fir (South).

7. Western woods; WCLIB or WWPA.

Retain one or more of six paragraphs below for indicated items if they are 2 inches nominal (38 mm actual) or greater in least dimension; otherwise, specify as boards.

F. Dimension Lumber Decking[ and Stair Treads]:  [No. 2] [Construction or No. 2] grade and[ any of] the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Redwood; RIS.

G. Dimension Lumber Decking[ and Stair Treads]:  [Deck Heart or Construction Heart] [Deck Common or Construction Common] redwood; RIS.

H. Dimension Lumber Railing Members:  [Select Structural] [No. 1] [No. 2] [Construction or No. 2] grade and[ any of] the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Redwood; RIS.

5. Spruce-pine-fir or spruce-pine-fir (South); NeLMA, NLGA, WCLIB, or WWPA.

I. Dimension Lumber Railing Members:  [Heart Clear] [Heart B or Select Heart] redwood; RIS.

J. Dimension Lumber for Benches:  [Select Structural] [No. 1] grade and[ any of] the following species:

1. Hem-fir or hem-fir (North); NLGA, WCLIB, or WWPA.

2. Douglas fir-larch, Douglas fir-larch (North), or Douglas fir-south; NLGA, WCLIB, or WWPA.

3. Mixed southern pine; SPIB.

4. Redwood; RIS.

5. Spruce-pine-fir or spruce-pine-fir (South); NeLMA, NLGA, WCLIB, or WWPA.

K. Dimension Lumber for Benches:  [Heart Clear] [Heart B or Select Heart] redwood; RIS.

2.3 BOARDS

A. Maximum Moisture Content:  [15] [19] percent.

First paragraph below can provide high-quality appearance but may add cost.  Delete if species and grades retained in paragraphs below are suitable without revision.

B. Provide boards hand selected for freedom from characteristics, on exposed surfaces and edges, that would impair finish appearance, including decay, honeycomb, knot holes, shake, splits, torn grain, and wane.

C. Board Decking[ and Stair Treads]:  1-1/4-inch- (32-mm-) thick radius-edged decking of[ any of] the following species and grades:

1. Douglas fir-larch or Douglas fir-south, [Patio 1] [Patio 2], WWPA.

2. Douglas fir-larch, [Select Dex] [Commercial Dex], WCLIB.

3. Douglas fir-larch (North), [Select Patio] [Commercial Patio], NLGA.

4. Hem-fir, [Patio 1] [Patio 2], WWPA.

5. Hem-fir, [Select Dex] [Commercial Dex], WCLIB.

6. Hem-fir (North), [Select Patio] [Commercial Patio], NLGA.

7. Redwood, [Heart Clear] [Heart B or Select Heart]; RIS.

8. Southern pine, [Premium] [Standard], SPIB.

9. Western red cedar, [Patio 1] [Patio 2], WWPA.

10. Western red cedar, [Select Dex] [Commercial Dex], WCLIB.

11. Western red cedar (North), [Select Patio] [Commercial Patio], NLGA.

Revise thickness in first paragraph below to 1 inch (25 mm) if required.

D. Stair Treads:  1-1/4-inch- (32-mm-) thick stepping with half-round or rounded-edge nosing and[ any of] the following species and grades:

1. Douglas fir, C & Btr VG (Vertical Grain) stepping; NLGA, WCLIB, or WWPA.

2. Hem-fir, C & Btr VG (Vertical Grain) stepping; NLGA, WCLIB, or WWPA.

3. Redwood, [Heart Clear] [Heart B or Select Heart]; RIS.

4. Southern pine, [Edge Grain B & B stepping] [Near Rift B & B stepping] [B & B stepping]; SPIB.

E. Railing Boards:[  Any of the following species and grades:]

1. Douglas fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

2. Hem-fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

3. Redwood, [Heart Clear] [Heart B or Select Heart]; RIS.

4. Southern pine, B & B finish; SPIB.

F. Boards for Benches:[  Any of the following species and grades:]

1. Douglas fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

2. Hem-fir, C & Btr finish or C Select; NLGA, WCLIB, or WWPA.

3. Redwood, [Heart Clear] [Heart B or Select Heart]; RIS.

4. Southern pine, [Edge Grain B & B finish] [Near Rift B & B finish] [B & B finish]; SPIB.

G. Board Decking [Stair Treads] [and] [Boards for Benches]:  Radius-edged S4S boards, with one face free of planer skip, machine burn, and torn or chipped grain.

1. Species:  [Ipe] [Teak].

Imported lumber is not usually graded according to any of the U.S. grading rules.  Before revising subparagraph below, verify availability of lumber complying with requirements.

2. Grade Characteristics:

Retain one of first two subparagraphs below for general grade description.

a. Clear[ one face; small pin knots and worm holes allowed on back face].

b. Sound; small pin knots, worm holes, and fixed knots allowed.

Retain one or more of five subparagraphs below, and possibly add other requirements as needed to supplement general grade description in subparagraph retained above.

c. All heart[ one face].

d. Straight grained and parallel cut.

e. Free of heart centers.

f. No decay, incipient decay, honeycomb, knot holes, shakes, splits, or wane.

g. No discoloration.

2.4 TIMBER

A. Maximum Moisture Content:  [19 percent] [No limit].

B. Dressing:  Provide [dressed timber (S4S)] [or] [timber that is rough sawn (Rgh)] unless otherwise indicated.

C. Timber Posts:  Balsam fir, Douglas fir-larch, Douglas fir-larch (North), eastern hemlock tamarack (North), hem-fir, southern pine, western hemlock, or western hemlock (North); [No. 1] [No. 2], NeLMA, NLGA, SPIB, WCLIB, or WWPA.

D. Timber Posts:  Alaska cedar; [No. 1] [No. 2], WCLIB.

E. Timber Posts:  Southern pine; [No. 1] [No. 2], SPIB.

2.5 ROUND WOOD POLES

Standard in first paragraph below is a specification for round timber construction poles that is based on specification for wood piles.

A. Round Wood Poles:  Clean-peeled wood poles complying with ASTM D 3200; with at least 80 percent of inner bark removed and with knots and limbs cut flush with the surface.

B. Species:  <Insert species required>.

2.6 PRESERVATIVE TREATMENT

A. Pressure treat boards and dimension lumber with waterborne preservative according to AWPA C2.

B. Pressure treat timber with waterborne preservative according to AWPA C15 requirements for "sawn building poles and posts as structural members."

Delete subparagraph below if chromium and arsenic are not allowed.  Timber treated with preservatives other than CCA may not be readily available.

1. Treatment with CCA shall include post-treatment fixation process.

C. Pressure treat poles with waterborne preservative to comply with AWPA C4.

Delete subparagraph below if chromium and arsenic are not allowed.  Poles treated with preservatives other than CCA may not be readily available.

1. Treatment with CCA shall include post-treatment fixation process.

See Evaluations for information about treatment chemicals.

D. Preservative Chemicals:  Acceptable to authorities having jurisdiction.

1. Do not use chemicals containing arsenic or chromium [except for timber posts] [except for poles].

Usually retain one of first two paragraphs below.

E. Use process that includes water-repellent treatment.

F. Use process that does not include water repellents or other substances that might interfere with application of indicated finishes.

Revise options in first paragraph below to eliminate items for which treated kiln-dried wood is not required.

G. After treatment, redry [boards] [dimension lumber] [timber] [and] [poles] to 19 percent maximum moisture content.

H. Mark treated wood with treatment quality mark of an inspection agency approved by ALSC's Board of Review.

Retain first option in subparagraph below if authorities having jurisdiction require quality mark on all materials.

1. For items indicated to receive a stained or natural finish, [mark each piece on surface that will not be exposed] [or] [omit marking and provide certificates of treatment compliance issued by inspection agency].

Retain first option in paragraph below and delete subparagraphs if total treatment is required; otherwise, retain second option and applicable subparagraphs.

I. Application:  [Treat all exterior rough carpentry unless otherwise indicated.] [Treat items indicated on Drawings and the following:]

1. Framing members[ less than 18 inches (460 mm) above grade].

2. Sills and ledgers.

3. Members in contact with masonry or concrete.

4. Posts.

5. Round wood poles.

6. Decking.

7. Stair treads.

2.7 PLASTIC DECKING

A. Plastic Lumber, General:  Products acceptable to authorities having jurisdiction and for which current model code evaluation reports exist that show compliance with building code in effect for Project for indicated occupancy and type of construction.

1. Allowable loads and spans, as documented in evaluation reports or in information referenced in evaluation reports, shall not be less than design loads and spans indicated.

Most plastic decking is a composite product consisting of solid shapes made from recycled polyethylene and cellulose fiber (wood or agricultural waste fiber).

B. Composite Plastic Lumber:  [Solid] [or] [hollow] shapes made from a mixture of cellulose fiber and [polyethylene] [or] [polypropylene].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

a. Advanced Environmental Recycling Technologies, Inc.

b. Brite Manufacturing Inc.

c. Carney Timber Company, Inc.

d. Certainteed Corporation.

e. Correct Building Products, LLC.

f. Elk Composite Building Products, Inc.

g. Epoch Composite Products, Inc.

h. Fiber Composites, LLC.

i. Green Tree Composites, LLC.

j. Kadant Composites, Inc.

k. Louisiana-Pacific Corporation.

l. Master Mark Plastics.

m. Midwest Manufacturing Extrusion.

n. TimberTech.

o. Trex Company, Inc.

p. Universal Forest Products, Inc.

q. <Insert manufacturer's name>.

First subparagraph below lists some commonly available sizes; verify availability of sizes with manufacturers selected.  Most manufacturers advertise nominal sizes rather than actual sizes.

3. Decking Size:  [7/8 by 5-1/2 inches (22 by 140 mm) actual] [1-1/4 by 6 nominal, 1 by 5-1/2 inches (25 by 140 mm) actual] [1-1/2 by 6 nominal, 1-1/4 by 5-1/2 inches (32 by 140 mm) actual] [1-1/4 by 6 inches (32 by 152 mm) actual] [1-3/8 by 3-1/2 inches (35 by 89 mm) actual] [1-3/8 by 5-1/2 inches (35 by 140 mm) actual] [2 by 6 nominal, 1-1/2 by 5-1/2 inches (38 by 140 mm) actual] <Insert size>.

Verify availability of configuration in first subparagraph below with manufacturers selected.

4. Configuration:  Provide product with grooved edges designed for fastening with concealed splines.

5. Surface Texture:  [Woodgrain] [Smooth] [Manufacturer's standard] <Insert finish>.

6. Color:  [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color>.

All-plastic decking contains no cellulose fiber (wood or agricultural waste fiber), which can support mold and mildew.  Most all-plastic decking consists of hollow shapes made from PVC with no recycled content.

C. All-Plastic Lumber:  [Solid] [or] [hollow] shapes made from [high-density polyethylene (HDPE)] [PVC] [polystyrene] [or] [cellular PVC] with no cellulose fiber.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two subparagraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

1. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

2. Basis-of-Design Product:  Subject to compliance with requirements, provide [product indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable product by one of the following:

a. Cascades Re-Plast; Division of Plastiques Cascades, Inc.

b. Certainteed Corporation.

c. CPI Plastics Group Ltd.

d. Genova Products, Inc.

e. Kroy Building Products, Inc.

f. L.B. Plastics, Inc.

g. Outdoor Technologies, Inc.

h. Renew Plastics; a division of N.E.W. Plastics Corp.

i. Royal Crown Limited.

j. Thermal Industries, Inc.

k. U.S. Plastic Lumber Ltd.

l. Veka Inc.

m. Westech Fence.

n. <Insert manufacturer's name>.

First subparagraph below lists some commonly available sizes; verify availability of sizes with manufacturers selected.  Most manufacturers advertise nominal sizes rather than actual sizes.

3. Decking Size:  [1 by 6 inches (25 by 152 mm) actual] [1-1/4 by 6 nominal, 1 by 5-1/2 inches (25 by 140 mm) actual] [1-1/2 by 6 nominal, 1-1/4 by 5-1/2 inches (32 by 140 mm) actual] [2 by 4 nominal, 1-1/2 by 3-1/2 inches (38 by 89 mm) actual] [2 by 6 nominal, 1-1/2 by 5-1/2 inches (38 by 140 mm) actual] [1-5/8 by 5-3/4 inches (41 by 146 mm) actual] <Insert size>.

Verify availability of configurations in first subparagraph below with manufacturers selected.

4. Configuration:  Provide product with [grooved edges designed for fastening with concealed splines] [or] [tongue-and-groove edges designed for concealed fastening].

5. Surface Texture:  [Woodgrain] [Smooth] [Manufacturer's standard] <Insert finish>.

6. Color:  [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color>.

2.8 FASTENERS

A. General:  Provide fasteners of size and type indicated that comply with requirements specified in this article for material and manufacture.  Provide nails or screws, in sufficient length, to penetrate not less than 1-1/2 inches (38 mm) into wood substrate.

1. Use [stainless steel] [fasteners with hot-dip zinc coating complying with ASTM A 153/A 153M or ASTM F 2329] unless otherwise indicated.

2. For pressure-preservative-treated wood, use stainless-steel fasteners.

3. For [plastic] [wood] decking, use stainless-steel fasteners[ where fasteners are exposed to view].

California Redwood Association recommends stainless-steel fasteners or hot-dip galvanized-steel fasteners.

4. For redwood, use [brass/bronze] [stainless-steel] [hot-dip galvanized-steel] fasteners.

B. Nails:  ASTM F 1667.

Standard in first paragraph below covers power-driven staples, nails, P-nails, and allied fasteners.

C. Power-Driven Fasteners:  NES NER-272.

D. Wood Screws:  ASME B18.6.1.

E. Lag Screws:  ASME B18.2.1 (ASME B18.2.3.8M).

F. Carbon-Steel Bolts:  ASTM A 307 (ASTM F 568M) with ASTM A 563 (ASTM A 563M) hex nuts and, where indicated, flat washers all hot-dip zinc coated.

G. Stainless-Steel Bolts:  ASTM F 593, Alloy Group 1 or 2 (ASTM F 738M, Grade A1 or A4); with ASTM F 594, Alloy Group 1 or 2 (ASTM F 836M, Grade A1 or A4) hex nuts and, where indicated, flat washers.

H. Postinstalled Anchors:  Stainless-steel, [chemical] [or] [torque-controlled expansion] anchors with capability to sustain, without failure, a load equal to six times the load imposed when installed in unit masonry assemblies and equal to four times the load imposed when installed in concrete as determined by testing per ASTM E 488 conducted by a qualified independent testing and inspecting agency.

1. Stainless-steel bolts and nuts complying with ASTM F 593 and ASTM F 594, Alloy Group 1 or 2 (ASTM F 738M and ASTM F 836M, Grade A1 or A4).

2.9 METAL FRAMING ANCHORS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers.  Retain one of first two paragraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

A. Manufacturers:  Subject to compliance with requirements, [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

B. Basis-of-Design Products:  Subject to compliance with requirements, provide [products indicated on Drawings] <Insert manufacturer's name; product name or designation> or comparable products by one of the following:

1. Cleveland Steel Specialty Co.

2. Harlen Metal Products, Inc.

3. KC Metals Products, Inc.

4. Simpson Strong-Tie Co., Inc.

5. Southeastern Metals Manufacturing Co., Inc.

6. USP Structural Connectors.

7. <Insert manufacturer's name>.

If retaining first option in first paragraph below, indicate design loads for metal framing anchors on Drawings.

C. Allowable Design Loads:  Provide products with allowable design loads, as published by manufacturer, that meet or exceed those [indicated on Drawings] [of basis-of-design products] [of products of manufacturers listed].  Manufacturer's published values shall be determined from empirical data or by rational engineering analysis and demonstrated by comprehensive testing performed by a qualified independent testing agency.

Retain one of first two paragraphs below.  For pressure-preservative-treated wood, G185 (Z550) galvanizing or stainless steel should be used in exterior applications.  Type 304 is usually standard for stainless steel; Type 316 gives better corrosion resistance in coastal environments.

D. Galvanized-Steel Sheet:  Hot-dip, zinc-coated steel sheet complying with ASTM A 653/A 653M, [G60 (Z180)] [G90 (Z270)] [G185 (Z550)] coating designation.

E. Stainless-Steel Sheet:  ASTM A 666, [Type 304] [Type 316].

Four paragraphs below are examples only.  Revise to suit Project or delete all if using "Basis-of-Design Products" Paragraph and if they are not needed to provide salient characteristics for products.

F. Joist Hangers:  U-shaped, with 2-inch- (50-mm-) long seat and 1-1/4-inch- (32-mm-) wide nailing flanges at least 85 percent of joist depth.

1. Thickness:  [0.050 inch (1.3 mm)] [0.062 inch (1.6 mm)].

G. Top Flange Hangers:  U-shaped joist hangers, full depth of joist, formed from metal strap with tabs bent to extend over and be fastened to supporting member.

1. Strap Width:  [1-1/2 inches (38 mm)] [2 inches (50 mm)].

2. Thickness:  [0.050 inch (1.3 mm)] [0.062 inch (1.6 mm)].

H. Post Bases:  Adjustable-socket type for bolting in place with standoff plate to raise post 1 inch (25 mm) above base and with 2-inch- (50-mm-) minimum side cover, socket 0.062 inch (1.6 mm) thick, and standoff and adjustment plates 0.108 inch (2.8 mm) thick.

I. Joist Ties:  Flat straps, with holes for fasteners, for tying joists together over supports.

1. Width:  [3/4 inch (19 mm)] [1-1/4 inches (32 mm)].

2. Thickness:  [0.050 inch (1.3 mm)] [0.062 inch (1.6 mm)].

3. Length:  [16 inches (400 mm)] [24 inches (600 mm)] [As indicated].

2.10 CONCEALED DECKING FASTENERS

A. Deck Splines:  Plastic splines designed to fit in grooves routed into the sides of decking material and be fastened to deck framing with screws.  Splines provide uniform spacing of decking material.[  Splines are made from UV-resistant polypropylene.]

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Blue Heron Enterprises, LLC.; Eb-Ty Hidden Deck-Fastener.

b. KK Mfg. Co., Inc.; Lumber Loc Hidden Deck Fasteners.

c. <Insert manufacturer's name; product name or designation>.

B. Deck Clips:  Black oxide coated stainless-steel clips designed to be fastened to deck framing with screws, and to secure decking material with teeth that also provide uniform spacing of decking material.

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Tiger Claw Inc.; Tiger Claw Hidden Deck Fasteners.

b. <Insert manufacturer's name; product name or designation>.

C. Deck Tracks:  Formed metal strips designed to be fastened to deck framing and to secure decking material from underside with screws.  Made from [epoxy powder-coated, hot-dip galvanized steel] [stainless steel].

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  See Division 01 Section "Product Requirements."

1. Products:  Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Grabber Deckmaster, a division of John Wagner Associates, Inc.; Deckmaster.

b. Ty-Lan Enterprises Inc.; Shadoe Track.

c. <Insert manufacturer's name; product name or designation>.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates and conditions, with Installer present, for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

B. Proceed with installation only after unsatisfactory conditions have been corrected.

3.2 PREPARATION

A. Clean substrates of projections and substances detrimental to application.

B. Prime lumber to be painted, including both faces and edges.  Cut to required lengths and prime ends.  Comply with requirements in Division 09 Section "Exterior Painting."

3.3 INSTALLATION, GENERAL

A. Set exterior rough carpentry to required levels and lines, with members plumb, true to line, cut, and fitted.  Fit exterior rough carpentry to other construction; scribe and cope as needed for accurate fit.

B. Framing Standard:  Comply with AF&PA's "Details for Conventional Wood Frame Construction" unless otherwise indicated.

C. Install wood decking[ and stair treads] with crown up (bark side down).

D. Install plastic lumber to comply with manufacturer's written instructions.

E. Secure decking to framing with concealed decking fasteners.

F. Install metal framing anchors to comply with manufacturer's written instructions.

G. Do not splice structural members between supports unless otherwise indicated.

H. Provide blocking and framing as indicated and as required to support facing materials, fixtures, specialty items, and trim.

I. Sort and select lumber so that natural characteristics will not interfere with installation or with fastening other materials to lumber.  Do not use materials with defects that interfere with function of member or pieces that are too small to use with minimum number of joints or optimum joint arrangement.

J. Comply with AWPA M4 for applying field treatment to cut surfaces of preservative-treated lumber.

1. Use inorganic boron (SBX) for items that are continuously protected from liquid water.

2. Use copper naphthenate for items not continuously protected from liquid water.

K. Securely attach exterior rough carpentry work to substrate by anchoring and fastening as indicated, complying with the following:

If retaining first subparagraph below, verify that this is acceptable to authorities having jurisdiction.  Fasteners covered by NES NER-272 are manufactured by member companies of the International Staple, Nail and Tool Association.

1. NES NER-272 for power-driven fasteners.

Retain one of five subparagraphs below, with or without subparagraph above, as required to comply with requirements of Project and local codes.

2. Table 2304.9.1, "Fastening Schedule," in ICC's International Building Code.

3. Table 23-II-B-1, "Nailing Schedule," in ICBO's Uniform Building Code.

4. Table 2305.2, "Fastening Schedule," in BOCA's BOCA National Building Code.

5. Table 2306.1, "Fastening Schedule," in SBCCI's Standard Building Code.

6. Table R602.3(1), "Fastener Schedule for Structural Members" and Table R602.3(2), "Alternate Attachments," in ICC's International Residential Code for One- and Two-Family Dwellings.

Revise first paragraph below to include other kinds of nails if required.

L. Use common wire nails unless otherwise indicated.  Select fasteners of size that will not fully penetrate members where opposite side will be exposed to view.  Make tight connections between members.  Install fasteners without splitting wood; do not countersink nail heads unless otherwise indicated.

Delete paragraph below if no exposed framing.

M. For exposed work, arrange fasteners in straight rows parallel with edges of members, with fasteners evenly spaced, and with adjacent rows staggered.

Indicate locations of other fasteners, such as wood screws, bolts, and lag screws, on Drawings.

3.4 ELEVATED DECK JOIST FRAMING INSTALLATION

A. General:  Install joists with crown edge up and support ends of each member with not less than 1-1/2 inches (38 mm) of bearing on wood or metal, or 3 inches (76 mm) on masonry.  Attach floor joists where framed into wood supporting members by using wood ledgers as indicated or, if not indicated, by using metal joist hangers.  Do not notch joists.

B. Frame openings with headers and trimmers supported by metal joist hangers; double headers and trimmers where span of header exceeds 48 inches (1200 mm).

C. Lap members framing from opposite sides of beams or girders not less than 4 inches (102 mm) or securely tie opposing members together.  Provide solid blocking of 2-inch nominal (38-mm actual) thickness by depth of joist over supports.

Revise paragraph below to suit building code requirements.

D. Provide solid blocking of 2-inch nominal (38-mm actual) thickness by depth of joist at intervals of 96 inches (2438 mm) o.c., between joists.

3.5 STAIR INSTALLATION

A. Provide stair framing members of size, space, and configuration indicated or, if not indicated, to comply with the following requirements:

Subparagraphs below are examples only.  Revise to suit Project and design loads required by building code.  Treads and risers are finish carpentry.

1. Stringer Size:  2 by 12 inches nominal (38 by 286 mm actual), minimum.

2. Notching:  Notch stringers to receive treads, risers, and supports; leave at least 3-1/2 inches (89 mm) of effective depth.

3. Stringer Spacing:  At least three stringers for each 36-inch (914-mm) clear width of stair.

First paragraph below is an example only, based on NFPA 101 requirements.  Revise if more stringent tolerances are required.

B. Provide stair framing with no more than 3/16-inch (4.7-mm) variation between adjacent treads and risers and no more than 3/8-inch (9.5-mm) variation between largest and smallest treads and risers within each flight.

C. Treads and Risers:  Secure by gluing and [nailing] [screwing] to carriages.  Countersink fastener heads, fill flush, and sand filler.  Extend treads over carriages[ and finish with bullnose edge].

3.6 RAILING INSTALLATION

Descriptive requirements in this article cover basic railing installation only; supplement with complete details.

A. Balusters:  Fit to railings, glue, and [nail] [screw] in place.  Countersink fastener heads, fill flush, and sand filler.

B. Newel Posts:  Secure to stringers and risers with [through bolts] [lag screws] [countersunk-head wood screws and glue].

C. Railings:  Secure wall rails with metal brackets.  Fasten freestanding railings to newel posts and to trim at walls with countersunk-head wood screws or rail bolts and glue.

END OF SECTION 061063

	EXTERIOR ROUGH CARPENTRY
	061063 - 1



