Copyright 2003 and 2005 AIA
MASTERSPEC Full Length
05/03 (R 05/06)

Copyright 2003 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 064023 - INTERIOR ARCHITECTURAL WOODWORK
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project and to distinguish interior architectural woodwork from items made from wood but specified as finish carpentry, stock cabinets, etc., in other Sections.  AWI's definition of standing and running trim includes "rails used on corridor walls of hospitals or nursing homes, etc., and guard rails at glass openings."

1. Interior standing and running trim.

2. Interior frames and jambs.

3. Stairwork[ and rails].

4. Flush wood paneling[ and wainscots].

5. Interior ornamental work.

6. Wood cabinets.

7. Plastic-laminate cabinets.

8. Wood countertops.

9. Plastic-laminate countertops.

10. Solid-surfacing-material countertops.

11. Laminated-plastic laboratory tops.

12. Closet and utility shelving.

13. Shop finishing of interior woodwork.

B. Related Sections include the following:

List below only products, construction, and equipment that the reader might expect to find in this Section but are specified elsewhere.

1. Division 06 Section "Rough Carpentry" for wood furring, blocking, shims, and hanging strips required for installing woodwork and concealed within other construction before woodwork installation.

Retain subparagraph below if a woodwork section is used to specify only cabinets and countertops and if Section below is used to specify wood trim, etc.  For high-quality wood trim, delete below and include trim in this Section.

2. Division 06 Section "Finish Carpentry" for interior carpentry exposed to view that is not specified in this Section.

Supplemental Section in first subparagraph below offers more choices for paneling types than this Section.

3. Division 06 Section "Wood Paneling."

4. Division 09 Section "Stone Facing" for stone countertops.

1.3 DEFINITIONS

A. Interior architectural woodwork includes wood furring, blocking, shims, and hanging strips for installing woodwork items unless concealed within other construction before woodwork installation.

Delete paragraph below if no stairs or if carriages are included in rough carpentry.

B. Rough carriages for stairs are a part of interior architectural woodwork.  Platform framing, headers, partition framing, and other rough framing associated with stairwork are specified in Division 06 Section "Rough Carpentry."

1.4 SUBMITTALS

A. Product Data:  For each type of product indicated[, including] [cabinet hardware and accessories] [handrail brackets] [and] [finishing materials and processes].

Retain paragraph above or first paragraph below and edit to suit Project; delete both if not applicable.

B. Product Data:  For [panel products] [high-pressure decorative laminate] [adhesive for bonding plastic laminate] [solid-surfacing material] [fire-retardant-treated materials] [cabinet hardware and accessories] [handrail brackets] [and] [finishing materials and processes].

Retain subparagraph below with either paragraph above; delete if fire-retardant-treated wood is not required.

1. Include data for fire-retardant treatment from chemical treatment manufacturer and certification by treating plant that treated materials comply with requirements.

C. Shop Drawings:  Show location of each item, dimensioned plans and elevations, large-scale details, attachment devices, and other components.

Retain first subparagraph below only for ornate, complex, or very high quality work.

1. Show details full size.

2. Show locations and sizes of furring, blocking, and hanging strips, including concealed blocking and reinforcement specified in other Sections.

3. Show locations and sizes of cutouts and holes for [plumbing fixtures] [faucets] [soap dispensers] [and other items] installed in architectural woodwork.

Retain subparagraph below only for blueprint-matched work.

4. Show veneer leaves with dimensions, grain direction, exposed face, and identification numbers indicating the flitch and sequence within the flitch for each leaf.

Retain subparagraph below only if retaining other requirements for WI's quality certification program.

5. Apply WI-certified compliance label to first page of Shop Drawings.

D. Samples for Initial Selection:

Revise list below to suit Project.

1. Shop-applied transparent finishes.

2. Shop-applied opaque finishes.

3. Plastic laminates.

4. PVC edge material.

5. Thermoset decorative panels.

6. Solid-surfacing materials.

Delete paragraph and subparagraphs above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph and subparagraphs below with or without above.

E. Samples for Verification:

Delete items in subparagraphs below that are not actually needed for control of grain character, color, and finish or expand to include other items.  Sizes listed first comply with those in AWI standard; revise if other sizes are required.

1. Lumber with or for transparent finish, not less than [50 sq. in. (300 sq. cm)] [5 inches (125 mm) wide by 24 inches (600 mm) long], for each species and cut, finished on 1 side and 1 edge.

2. Veneer leaves representative of and selected from flitches to be used for transparent-finished woodwork.

3. Veneer-faced panel products with or for transparent finish, [8 by 10 inches (200 by 250 mm)] [12 by 24 inches (300 by 600 mm)], for each species and cut.  Include at least one face-veneer seam and finish as specified.

4. Lumber and panel products with shop-applied opaque finish, 50 sq. in. (300 sq. cm) for lumber and 8 by 10 inches (200 by 250 mm) for panels, for each finish system and color, with[ 1/2 of] exposed surface finished.

5. Plastic laminates, 8 by 10 inches (200 by 250 mm), for each type, color, pattern, and surface finish[, with 1 sample applied to core material] [and specified edge material applied to 1 edge].

6. Thermoset decorative-panels, 8 by 10 inches (200 by 250 mm), for each type, color, pattern, and surface finish[, with edge banding on 1 edge].

7. Solid-surfacing materials, 6 inches (150 mm) square.

8. Corner pieces as follows:

a. Cabinet-front frame joints between stiles and rails, as well as exposed end pieces, 18 inches (450 mm) high by 18 inches (450 mm) wide by 6 inches (150 mm) deep.

b. Miter joints for standing trim.

Delete subparagraph below if Product Data are acceptable.

9. Exposed cabinet hardware and accessories, one unit for each type[ and finish].

F. LEED Submittals:

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1; coordinate with requirements selected in Part 2 for adhesives.

1. Product Data for Credit EQ 4.1:  For installation adhesives, including printed statement of VOC content.

Retain subparagraph and associated subparagraphs below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4.

2. Product Data for Credit EQ 4.4:

a. For each composite-wood product used, documentation indicating that the bonding agent contains no urea formaldehyde.

b. For each adhesive used, documentation indicating that the adhesive contains no urea formaldehyde.

Retain subparagraph and associated subparagraph below if recycled content is required for LEED-NC or LEED-CI Credits MR 4.1 and MR 4.2.

3. Product Data for Credit(s) MR 4.1[ and MR 4.2]:  For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content

a. Include statement indicating costs for each product having recycled content.

Retain subparagraph and associated subparagraph below and "Forest Certification" Paragraph in "Quality Assurance" Article if wood products are required to be certified for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.

4. Certificates for Credit MR 7:  Chain-of-custody certificates certifying that products specified to be made from certified wood comply with forest certification requirements.  Include evidence that mill is certified for chain of custody by an FSC-accredited certification body.

a. Include statement indicating costs for each certified wood product.

G. Product Certificates:  For each type of product, signed by product manufacturer.

If retaining paragraph below, also retain paragraphs in "Quality Assurance" Article that require compliance with selected quality standard and certification program.

H. Woodwork Quality Standard Compliance Certificates:  [AWI Quality Certification Program certificates] [WI-certified compliance certificates].

Coordinate paragraph below with qualification requirements in Division 01 Section "Quality Requirements" and as supplemented in "Quality Assurance" Article.

I. Qualification Data:  For [Installer] [fabricator].

1.5 QUALITY ASSURANCE

Consider retaining one of two options in paragraph below if AWI quality certification or WI compliance certification is required.  AWI's quality certification is only available if fabricator is a certified participant.  WI will inspect work and provide certification for work that passes inspection if fabricator is not a licensed shop.

A. Fabricator Qualifications:  Shop that employs skilled workers who custom-fabricate products similar to those required for this Project and whose products have a record of successful in-service performance.[  Shop is a certified participant in AWI's Quality Certification Program.][  Shop is a licensee of WI's Certified Compliance Program.]

Delete first paragraph below if not required or available.  If AWI Quality Certification Program labels or certificates are required for installation, installer must be a certified participant.

B. Installer Qualifications:  [Fabricator of products] [Certified participant in AWI's Quality Certification Program] [Licensee of WI's Certified Compliance Program].

C. Source Limitations:  Engage a qualified woodworking firm to assume undivided responsibility for production of interior architectural woodwork with sequence-matched wood veneers [and wood doors with face veneers that are sequence matched with woodwork] [and transparent-finished wood doors that are required to be of same species as woodwork].

D. Quality Standard:  Unless otherwise indicated, comply with AWI's "Architectural Woodwork Quality Standards" for grades of interior architectural woodwork indicated for construction, finishes, installation, and other requirements.

1. Provide AWI Quality Certification Program [labels] [and] [certificates] indicating that woodwork[, including installation,] complies with requirements of grades specified.

Retain paragraph above or below.  Verify applicability of selected standard for Project's geographic location.  Review selected standard and coordinate its requirements with selected options.  Certification programs of both organizations are available to member and nonmember firms.  AWI's quality certification is only available if fabricator is a certified participant.  WI will inspect work and provide certification for work that passes inspection if fabricator is not a licensed shop.  Contact either organization for a list of certified woodworkers in Project's location.

E. Quality Standard:  Unless otherwise indicated, comply with WI's "Manual of Millwork" for grades of interior architectural woodwork indicated for construction, finishes, installation, and other requirements.

1. Provide WI-certified compliance [labels] [and] [certificates] indicating that woodwork[, including installation,] complies with requirements of grades specified.

Generally delete subparagraph below unless Drawings and Specifications are more restrictive than quality standard.  Retain with either "Quality Standard" Paragraph above.

2. The Contract Documents contain selections chosen from options in the quality standard and additional requirements beyond those of the quality standard.  Comply with such selections and requirements in addition to the quality standard.

Delete paragraph below if no fire-retardant-treated materials or products are required.

F. Fire-Test-Response Characteristics:  Where fire-retardant materials or products are indicated, provide materials and products with specified fire-test-response characteristics as determined by testing identical products per test method indicated by UL, ITS, or another testing and inspecting agency acceptable to authorities having jurisdiction.  Identify with appropriate markings of applicable testing and inspecting agency in the form of separable paper label or, where required by authorities having jurisdiction, imprint on surfaces of materials that will be concealed from view after installation.

Paragraph below may be retained to specify interior architectural woodwork made from certified wood for LEED-NC or LEED-CI Credit MR 7, which requires that a minimum of 50 percent of wood-based materials be certified.  An alternative method of complying with Credit MR 7 requirement is to retain requirement in Division 01 Section "Sustainable Design Requirements" that gives Contractor the option and responsibility for determining how Credit MR 7 requirement will be met.

G. Forest Certification:  Provide interior architectural woodwork produced from wood obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

Delete paragraph and subparagraph below if not required.  If retaining, indicate location, size, and other details of mockups on Drawings or by inserts.  Revise wording if only one mockup is required.

H. Mockups:  Build mockups to verify selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

Retain subparagraph below if mockups are erected as part of building rather than separately and the intention is to make an exception to the default requirement in Division 01 Section "Quality Requirements" for demolishing and removing mockups when directed, unless otherwise indicated.

1. Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preinstallation conference.  If retaining, coordinate with Division 01.

I. Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 01 Section "Project Management and Coordination."

1.6 DELIVERY, STORAGE, AND HANDLING

A. Do not deliver woodwork until painting and similar operations that could damage woodwork have been completed in installation areas.  If woodwork must be stored in other than installation areas, store only in areas where environmental conditions comply with requirements specified in "Project Conditions" Article.

1.7 PROJECT CONDITIONS

A. Environmental Limitations:  Do not deliver or install woodwork until building is enclosed, wet work is complete, and HVAC system is operating and maintaining temperature and relative humidity at occupancy levels during the remainder of the construction period.

Generally retain paragraph above; retain first paragraph below if humidity will be controlled during occupancy.  If retaining below, select one of three relative humidity ranges or insert another based on local climatological data.  Three ranges given are for painted or finished woodwork.  First applies to Ontario, Quebec, and most of U.S.  Second applies to damp coastal areas of southern U.S. and the Maritime Provinces.  Third applies to dry southwestern U.S. and to Alberta, Manitoba, and Saskatchewan.  For unfinished woodwork, narrower ranges will be required to maintain optimum moisture content.  See map and discussion about relative humidity and moisture content at end of Section 1700 in AWI's quality standards.

B. Environmental Limitations:  Do not deliver or install woodwork until building is enclosed, wet work is complete, and HVAC system is operating and maintaining temperature between 60 and 90 deg F (16 and 32 deg C) and relative humidity between [25 and 55] [43 and 70] [17 and 50] <Insert humidity range> percent during the remainder of the construction period.

C. Field Measurements:  Where woodwork is indicated to fit to other construction, verify dimensions of other construction by field measurements before fabrication, and indicate measurements on Shop Drawings.  Coordinate fabrication schedule with construction progress to avoid delaying the Work.

1. Locate concealed framing, blocking, and reinforcements that support woodwork by field measurements before being enclosed, and indicate measurements on Shop Drawings.

Delete subparagraph below if not allowed.

2. Established Dimensions:  Where field measurements cannot be made without delaying the Work, establish dimensions and proceed with fabricating woodwork without field measurements.  Provide allowance for trimming at site, and coordinate construction to ensure that actual dimensions correspond to established dimensions.

1.8 COORDINATION

A. Coordinate sizes and locations of framing, blocking, furring, reinforcements, and other related units of Work specified in other Sections to ensure that interior architectural woodwork can be supported and installed as indicated.

Retain paragraph below if cabinet locks or other hardware applied to woodwork, such as hinges and locks applied to wood jambs, is specified in a hardware section.  Include a similar paragraph for other specific items requiring coordination, such as light fixtures installed in woodwork.

B. Hardware Coordination:  Distribute copies of approved hardware schedule specified in Division 08 Section "Door Hardware (Scheduled by Describing Products)" to fabricator of architectural woodwork; coordinate Shop Drawings and fabrication with hardware requirements.

PART 2 -  PRODUCTS

2.1 WOODWORK FABRICATORS

Retain this Article if a list of preapproved woodworkers is used as a quality-control procedure.  See Evaluations.

A. Available Fabricators:  Subject to compliance with requirements, fabricators offering interior architectural woodwork that may be incorporated into the Work include, but are not limited to, the following:

Retain paragraph above if additional firms will be considered; retain paragraph below if not.  If retaining above, include procedure for approving other firms in the Instructions to Bidders.

B. Fabricators:  Subject to compliance with requirements, provide interior architectural woodwork by one of the following:

Insert list of preapproved firms.  Refer to AWI's or WI's member list for names of woodworking firms that could potentially be included.

2.2 MATERIALS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.

A. General:  Provide materials that comply with requirements of [AWI's] [WI's] quality standard for each type of woodwork and quality grade specified, unless otherwise indicated.

B. Wood Species and Cut for Transparent Finish:  [Red oak, plain sawn or sliced] [White oak, rift sawn or cut] [White ash, plain sawn or sliced] [Hickory, plain sawn or sliced] <Insert species and cut>.

If all transparent-finished woodwork is same species and cut, retain paragraph above and delete separate requirements for species and cut in other articles; otherwise, delete above.  Similarly, if all opaque-finished woodwork is same species, retain paragraph below and delete separate requirements for species in other articles; otherwise, delete below.  For opaque-finished woodwork, closed-grain hardwood is a better choice than softwoods, except for Economy grade.

C. Wood Species for Opaque Finish:  [Any closed-grain hardwood] [Eastern white pine, sugar pine, or western white pine] <Insert species>.

Retain paragraph and subparagraphs below if AWI standard is used or if requirements for wood products selected exceed those in WI standard.  Delete standards for products not used.

D. Wood Products:  Comply with the following:

Retain first subparagraph below if recycled content is required for LEED-NC or LEED-CI Credits MR 4.1 and MR 4.2.  Recycled content of medium-density fiberboard and particleboard varies greatly; consult manufacturers before inserting requirement.

1. Recycled Content of Medium-Density Fiberboard and Particleboard:  Provide products with an average recycled content so postconsumer recycled content plus one-half of preconsumer recycled content is not less than <Insert number> percent.

2. Hardboard:  AHA A135.4.

If retaining subparagraph below and low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4, retain option prohibiting urea formaldehyde.  See Evaluations.  SierraPine's "Medex," "Medex NC," and "Medite II" and Weyerhaeuser's "Premier Plus" fiberboard are made without urea formaldehyde.

3. Medium-Density Fiberboard:  ANSI A208.2, Grade MD[, made with binder containing no urea formaldehyde].

Retain second option in subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4.  Retaining second option will eliminate formaldehyde from resins used to bind particles together but will decrease competition and may increase costs.  See Evaluations.  Particleboard with exterior glue is made by Rodman Industries.

4. Particleboard:  ANSI A208.1, Grade [M-2] [M-2-Exterior Glue].

Retain first subparagraph below instead of subparagraph above if straw-based particleboard is required for LEED-NC or LEED-CI Credit MR 6.  Particleboard below also complies with low-emitting materials requirement for LEED-NC or LEED-CI Credit EQ 4.4.  See Evaluations.

5. Particleboard:  Straw-based particleboard complying with requirements in ANSI A208.1, Grade M-2, except for density.

6. Softwood Plywood:  DOC PS 1[, Medium Density Overlay].

Note that the term "plywood" in subparagraph below refers to a wood-based panel with veneers applied to both faces; core may be made up of veneers (either hardwood or softwood), particleboard, medium-density fiberboard, hardboard, or glued-up lumber.  If retaining below and low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4, retain option prohibiting urea formaldehyde.  See Evaluations.

7. Veneer-Faced Panel Products (Hardwood Plywood):  HPVA HP-1[, made with adhesive containing no urea formaldehyde].

First paragraph below describes "Permalam," frequently called "melamine." If retaining, also retain "Medium-Density Fiberboard" Subparagraph and applicable "Particleboard" subparagraphs in "Wood Products" Paragraph above.

E. Thermoset Decorative Panels:  Particleboard or medium-density fiberboard finished with thermally fused, melamine-impregnated decorative paper complying with LMA SAT-1.

1. Provide PVC or polyester edge banding complying with LMA EDG-1 on components with exposed or semiexposed edges.

F. High-Pressure Decorative Laminate:  NEMA LD 3, grades as indicated or, if not indicated, as required by woodwork quality standard.

1. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering high-pressure decorative laminates that may be incorporated into the Work include, but are not limited to, the following:

Retain subparagraph above for nonproprietary or subparagraph below for semiproprietary specification.  Refer to Division 01 Section "Product Requirements." Retain list of manufacturers with either subparagraph.

2. Manufacturer:  Subject to compliance with requirements, provide high-pressure decorative laminates by one of the following:

a. Abet Laminati, Inc.

b. Arborite; Division of ITW Canada, Inc.

c. Formica Corporation.

d. Lamin-Art, Inc.

e. Nevamar Company, LLC; Decorative Products Div.

f. Panolam Industries International Incorporated.

g. Westinghouse Electric Corp.; Specialty Products Div.

h. Wilsonart International; Div. of Premark International, Inc.

i. <Insert manufacturer's name.>

Retain first paragraph and subparagraphs below for laboratory tops where high degree of chemical resistance is required.

G. Chemical-Resistant, High-Pressure Decorative Laminate:  NEMA LD 3, Grade HGP, and as follows:

1. Laminate has the following ratings when tested with indicated reagents according to NEMA LD 3, Test Procedure 3.9.5:

a. Nitric Acid (30 Percent):  Moderate effect.

b. Sulfuric Acid (77 Percent):  Moderate effect.

c. Hydrochloric Acid (37 Percent):  Moderate effect.

d. Phosphoric Acid (75 Percent):  No effect.

e. Acetic Acid (98 Percent):  No effect.

f. Formaldehyde:  No effect.

g. Ethyl Acetate:  No effect.

h. Ethyl Ether:  No effect.

i. Phenol (85 Percent):  Moderate effect.

j. Benzene:  No effect.

k. Xylene:  No effect.

l. Butyl Alcohol:  No effect.

m. Furfural:  No effect.

n. Methyl Ethyl Ketone:  No effect.

o. Sodium Hydroxide (25 Percent):  No effect.

p. Sodium Sulfide (15 Percent):  No effect.

q. Ammonium Hydroxide (28 Percent):  No effect.

r. Zinc Chloride:  No effect.

s. Gentian Violet:  No effect.

t. Methyl Red:  No effect.

2. Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, the following:

Retain subparagraph above for nonproprietary or subparagraph below for semiproprietary specification.  Refer to Division 01 Section "Product Requirements." Retain list of products with either subparagraph.

3. Products:  Subject to compliance with requirements, provide one of the following:

Products listed below do not have identical chemical resistance.  Verify acceptability before retaining.

a. Formica Corporation; Lab Grade 840 Black.

b. Panolam Industries International Incorporated; Pionite Chemguard.

c. Wilsonart International, Div. of Premark International, Inc.; Chemsurf.

d. <Insert manufacturer's name; product name or designation.>

H. Solid-Surfacing Material:  Homogeneous solid sheets of filled plastic resin complying with ISSFA-2.

1. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

Retain subparagraph above for nonproprietary or subparagraph below for semiproprietary specification.  Refer to Division 01 Section "Product Requirements." Retain list of manufacturers with either subparagraph.

2. Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

Companies listed below make a range of products that are not all equal in appearance or in performance characteristics.  Some products offered may not comply with ISSFA-2 requirements for Standard type; some may not comply with ISSFA-2 at all.  Verify acceptability of products before retaining manufacturers.

a. ABA Industries.

b. Avonite, Inc.

c. E. I. du Pont de Nemours and Company.

d. Formica Corporation.

e. LG Chemical, Ltd.

f. Meganite Inc.; a division of the Pyrochem Group.

g. Nevamar Company, LLC; Decorative Products Div.

h. Samsung; Cheil Industries Inc.

i. Swan Corporation (The).

j. Transolid, Inc.

k. Wilsonart International; Div. of Premark International, Inc.

l. <Insert manufacturer's name.>

Delete option in first subparagraph below if 1/4-inch- (6.4-mm-) thick material is not used.  Special Purpose type is not subject to all the requirements for Standard type.  Special Purpose type must comply with requirements for fungal and bacterial resistance, consistency of color, stain resistance, visual defects, light resistance, boiling water resistance, and high-temperature resistance.  Standard type must comply with these same requirements and with requirements for radiant heat resistance, linear thermal expansion, flexural strength, flexural modulus, Barcol hardness, flatness, and impact resistance.

3. Type:  Standard type[ or Veneer type made from material complying with requirements for Standard type, as indicated], unless Special Purpose type is indicated.

4. Colors and Patterns:  [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range].

I. Float Glass for Cabinet Doors:  ASTM C 1036, Type I, Class [1 (clear)] [2 or 3 (tinted)], Quality-Q3, [3.0 mm] [4.0 mm] [5.0 mm] [6.0 mm] thick.

Delete subparagraph below if option for clear glass is selected in paragraph above.

1. Tint Color:  [Blue-green] [Bronze] [Green] [Gray] <Insert color>.

Delete paragraph above or first paragraph below.  Retain option for seamed exposed edges below if unframed glass doors are used.

J. Tempered Float Glass for Cabinet Doors:  ASTM C 1048, Kind FT, Condition A, Type I, Class [1 (clear)] [2 or 3 (tinted)], Quality-Q3[, with exposed edges seamed before tempering], 6 mm thick, unless otherwise indicated.

Delete subparagraph below if option for clear glass is selected in paragraph above.

1. Tint Color:  [Blue-green] [Bronze] [Green] [Gray] <Insert color>.

K. Mirror Glass for Cabinet Doors:  ASTM C 1503, Mirror [Select] [Glazing], Quality-Q3, [3.0 mm] [4.0 mm] [5.0 mm] [6.0 mm] thick.

L. Decorative Glass for Cabinet Doors:  Provide decorative glass complying with Division 08 Section "Decorative Glass Glazing."

M. Tempered Float Glass for Cabinet Shelves:  ASTM C 1048, Kind FT, Condition A, Type I, Class [1 (clear)] [2 or 3 (tinted)], Quality-Q3; with exposed edges seamed before tempering, 6 mm thick.

Delete subparagraph below if option for clear glass is selected in paragraph above.

1. Tint Color:  [Blue-green] [Bronze] [Green] [Gray] <Insert color>.

2.3 FIRE-RETARDANT-TREATED MATERIALS

Delete this Article if not applicable.  If fire-retardant materials are required, verify requirements and acceptability of various materials with authorities having jurisdiction,

A. General:  Where fire-retardant-treated materials are indicated, use materials complying with requirements in this Article, that are acceptable to authorities having jurisdiction, and with fire-test-response characteristics specified.

1. Do not use treated materials that do not comply with requirements of referenced woodworking standard or that are warped, discolored, or otherwise defective.

2. Use fire-retardant-treatment formulations that do not bleed through or otherwise adversely affect finishes.  Do not use colorants to distinguish treated materials from untreated materials.

3. Identify fire-retardant-treated materials with appropriate classification marking of UL, U.S. Testing, Timber Products Inspection, or another testing and inspecting agency acceptable to authorities having jurisdiction.

B. Fire-Retardant-Treated Lumber and Plywood by Pressure Process:  Comply with performance requirements of AWPA C20 (lumber) and AWPA C27 (plywood).  Use the following treatment type:

1. Exterior Type:  Organic-resin-based formulation thermally set in wood by kiln drying.

Type in subparagraph above is suitable for both exterior and interior applications.  Type in first subparagraph below is only for interior applications.  See Evaluations.

2. Interior Type A:  Low-hygroscopic formulation.

3. Mill lumber after treatment within limits set for wood removal that do not affect listed fire-test-response characteristics, using a woodworking plant certified by testing and inspecting agency.

Delete subparagraph above or first subparagraph below.  Before retaining above, verify that wood species and treatment process specified are approved for milling after treatment.

4. Mill lumber before treatment and implement special procedures during treatment and drying processes that prevent lumber from warping and developing discolorations from drying sticks or other causes, marring, and other defects affecting appearance of treated woodwork.

5. Kiln-dry materials before and after treatment to levels required for untreated materials.

Retain paragraph and subparagraphs below, if required, with either AWI or WI standard.  Note that this particleboard contains urea formaldehyde.  It complies with requirements for Class I (Class A) finish but not requirements of model codes for use where noncombustible materials are required.

C. Fire-Retardant Particleboard:  Panels complying with the following requirements, made from softwood particles and fire-retardant chemicals mixed together at time of panel manufacture to achieve flame-spread index of 25 or less and smoke-developed index of 25 or less per ASTM E 84.

1. For panels 3/4 inch (19 mm) thick and less, comply with ANSI A208.1 for Grade M-2 except for the following minimum properties:  modulus of rupture, 1600 psi (11 MPa); modulus of elasticity, 300,000 psi (2070 MPa); internal bond, 80 psi (550 kPa); and screw-holding capacity on face and edge, 250 and 225 lbf (1100 and 1000 N), respectively.

2. For panels 13/16 to 1-1/4 inches (20 to 32 mm) thick, comply with ANSI A208.1 for Grade M-1 except for the following minimum properties:  modulus of rupture, 1300 psi (9 MPa); modulus of elasticity, 250,000 psi (1720 MPa); linear expansion, 0.50 percent; and screw-holding capacity on face and edge, 250 and 175 lbf (1100 and 780 N), respectively.

3. Product:  Subject to compliance with requirements, provide "Duraflake FR" by Weyerhaeuser.

Fiberboard in paragraph below complies with requirements for Class I (Class A) finish but not requirements of model codes for use where noncombustible materials are required.

D. Fire-Retardant Fiberboard:  Medium-density fiberboard panels complying with ANSI A208.2, made from softwood fibers, synthetic resins, and fire-retardant chemicals mixed together at time of panel manufacture to achieve flame-spread index of 25 or less and smoke-developed index of 200 or less per ASTM E 84.

1. Product:  Subject to compliance with requirements, provide "Medite FR" by SierraPine Ltd.; Medite Div.

2.4 CABINET HARDWARE AND ACCESSORIES

Where close matching of cabinet hardware and door hardware is required, it may be preferable to specify cabinet hardware in Division 08.

A. General:  Provide cabinet hardware and accessory materials associated with architectural cabinets, except for items specified in Division 08 Section "Door Hardware (Scheduled by Describing Products)."

Paragraphs and subparagraphs below describing hardware items are examples only; edit to suit Project.  Delete if schedule is included on Drawings.

B. Butt Hinges:  2-3/4-inch (70-mm), 5-knuckle steel hinges made from 0.095-inch- (2.4-mm-) thick metal, and as follows:

1. Semiconcealed Hinges for Flush Doors:  BHMA A156.9, B01361.

2. Semiconcealed Hinges for Overlay Doors:  BHMA A156.9, B01521.

Hinges in first paragraph below are not as strong as heavy-duty butt hinges above.

C. Frameless Concealed Hinges (European Type):  BHMA A156.9, B01602, [100] [135] [170] degrees of opening[, self-closing].

D. Back-Mounted Pulls:  BHMA A156.9, B02011.

E. Wire Pulls:  Back mounted, solid [metal] [plastic], [4 inches (100 mm) long, 5/16 inch (8 mm) in diameter] [5 inches (127 mm) long, 2-1/2 inches (63.5 mm) deep, and 5/16 inch (8 mm) in diameter].

F. Catches:  [Magnetic catches, BHMA A156.9, B03141] [Push-in magnetic catches, BHMA A156.9, B03131] [Roller catches, BHMA A156.9, B03071] [Ball friction catches, BHMA A156.9, B03013].

First option in paragraph below specifies standards and clip-type rests for mounting at ends of shelves; second specifies standards and knife-type brackets for mounting at rear of shelves.

G. Adjustable Shelf Standards and Supports:  [BHMA A156.9, B04071; with shelf rests, B04081] [BHMA A156.9, B04102; with shelf brackets, B04112].

Shelf rests in first paragraph below are installed in holes drilled in cabinet sides and partitions.

H. Shelf Rests:  BHMA A156.9, B04013; [metal] [plastic] [metal, two-pin type with shelf hold-down clip].

I. Drawer Slides:  BHMA A156.9, B05091.

1. Standard Duty (Grade 1, Grade 2, and Grade 3): Side mounted[ and extending under bottom edge of drawer]; [full-extension] [partial-extension] type; [zinc-plated steel] [epoxy-coated steel] with polymer rollers.

2. Heavy Duty (Grade 1HD-100 and Grade 1HD-200):  Side mounted; [full-extension] [full-overtravel-extension] type; zinc-plated steel ball-bearing slides.

Grades in five subparagraphs below correspond to the following initial load test requirements:  Grade 2: 30 lbf (13.3 kg); Grade 1: 50 lbf (22.2 kg); Grade 1HD-100: 100 lbf (44.5 kg); Grade 1HD-200: 200 lbf (90 kg).

3. Box Drawer Slides:  [Grade 1] [Grade 1HD-100]; for drawers not more than 6 inches (150 mm) high and 24 inches (600 mm) wide.

4. File Drawer Slides:  [Grade 1HD-100] [Grade 1HD-200]; for drawers more than 6 inches (150 mm) high or 24 inches (600 mm) wide.

5. Pencil Drawer Slides:  [Grade 2] [Grade 1]; for drawers not more than 3 inches (75 mm) high and 24 inches (600 mm) wide.

6. Keyboard Slides:  [Grade 1] [Grade 1HD-100]; for computer keyboard shelves.

7. Trash Bin Slides:  [Grade 1HD-100] [Grade 1HD-200]; for trash bins not more than 20 inches (500 mm) high and 16 inches (400 mm) wide.

J. [Plastic] [Aluminum] Slides for Sliding Glass Doors:  BHMA A156.9, B07063.

K. Door Locks:  BHMA A156.11, E07121.

Locks specified in paragraph above and below are deadbolt locks, surface mounted on inside of door or drawer with only the cylinder exposed on outside; revise either paragraph if another type of lock is required.

L. Drawer Locks:  BHMA A156.11, E07041.

Sizes in first paragraph below are two of the many offered.  Other colors, materials, and styles are also available.  1-1/4-inch (32-mm) grommet is "OG series"; 2-inch (51-mm) grommet is "SG series."

M. Grommets for Cable Passage through Countertops:  [1-1/4-inch (32-mm)] [2-inch (51-mm)] <Insert size> OD, [brown] [black] <Insert color>, molded-plastic grommets and matching plastic caps with slot for wire passage.

1. Product:  Subject to compliance with requirements, provide "[OG] [SG] series" by Doug Mockett & Company, Inc.

N. Paper Slots:  [12 inches (305 mm)] [17 inches (432 mm)] long by 1-3/4 inches (45 mm) wide by 1 inch (25 mm) deep; [brown] [black] <Insert color>, molded-plastic, paper-slot liner with 1/4-inch (6.4-mm) lip.

In subparagraph below, "Model CP-2" is 12-inch (305-mm) slot; "Model CP-1" is 17-inch (432-mm) slot.

1. Product:  Subject to compliance with requirements, provide "Model [CP-2] [CP-1]" by Doug Mockett & Company, Inc.

O. Exposed Hardware Finishes:  For exposed hardware, provide finish that complies with BHMA A156.18 for BHMA finish number indicated.

Subparagraphs below are examples only.  Revise to suit Project.  If more than one finish is required, indicate location of each here or on Drawings.  See Evaluations.

1. Dark, Oxidized, Satin Bronze, Oil Rubbed:  BHMA 613 for bronze base; BHMA 640 for steel base; match Architect's sample.

2. Bright Brass, Clear Coated:  BHMA 605 for brass base; BHMA 632 for steel base.

3. Satin Brass, Blackened, Bright Relieved, Clear Coated:  BHMA 610 for brass base; BHMA 636 for steel base.

4. Satin Chromium Plated:  BHMA 626 for brass or bronze base; BHMA 652 for steel base.

5. Bright Chromium Plated:  BHMA 625 for brass or bronze base; BHMA 651 for steel base.

6. Satin Stainless Steel:  BHMA 630.

P. For concealed hardware, provide manufacturer's standard finish that complies with product class requirements in BHMA A156.9.

2.5 MISCELLANEOUS MATERIALS

A. Furring, Blocking, Shims, and Hanging Strips:  Softwood or hardwood lumber, kiln dried to less than 15 percent moisture content.

Delete paragraph above or first paragraph below, or both, if specified in a carpentry section.

B. Furring, Blocking, Shims, and Hanging Strips:  Fire-retardant-treated softwood lumber, kiln dried to less than 15 percent moisture content.

C. Rough Carriages for Stairs:  [Select Structural] [No. 1] [No. 2] grade and[ any of] the following species, kiln dried to 15 percent maximum moisture content:

If retaining paragraph above, retain one or more of eight subparagraphs below.  Species groups listed do not have equal properties.

1. Douglas fir-larch.

2. Douglas fir-south.

3. Douglas fir-larch (north).

4. Hem-fir.

5. Hem-fir (north).

6. Southern pine.

7. Spruce-pine-fir (south).

8. Spruce-pine-fir.

Retain paragraph above or first paragraph and subparagraphs below if rough carriages for stairs are required.  Laminated veneer lumber is less prone to warping and shrinking than dimension lumber and is more readily available in larger depths and longer lengths.

D. Rough Carriages for Stairs:  Laminated veneer lumber, made with an exterior-type adhesive complying with ASTM D 2559, and with the following allowable design values as determined according to ASTM D 5456:

Verify properties of available products before selecting options in two subparagraphs below.

1. Extreme Fiber Stress in Bending, Edgewise:  [2850 psi (19.7 MPa)] [2600 psi (17.9 MPa)] [2500 psi (17.2 MPa)] <Insert value> for 12-inch nominal- (286-mm actual-) depth members.

2. Modulus of Elasticity, Edgewise:  [2,000,000 psi (13 800 MPa)] [1,800,000 psi (12 400 MPa)] <Insert value>.

E. Anchors:  Select material, type, size, and finish required for each substrate for secure anchorage.  Provide nonferrous-metal or hot-dip galvanized anchors and inserts on inside face of exterior walls and elsewhere as required for corrosion resistance.  Provide toothed-steel or lead expansion sleeves for drilled-in-place anchors.

F. Handrail Brackets:  [Cast] [Extruded] [Stamped] from [malleable iron] [aluminum] [bronze] [stainless steel] with wall flange drilled [for exposed anchor] [and tapped for concealed hanger bolt] and with support arm for screwing to underside of rail.  Sized to provide 1-1/2-inch (38-mm) clearance between handrail and wall.

Retain paragraph above or below, or both, if rail brackets are required.

G. Handrail/Bumper Rail Brackets:  Pairs of extruded-aluminum channels; one for fastening to back of rail and one for fastening to face of wall.  They are then assembled in overlapping fashion and fastened together top and bottom with self-tapping screws.  Sized to provide 1-1/2-inch (38-mm) clearance between handrail and wall.

Retain paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.4.  See Evaluations.

H. Adhesives, General:  Do not use adhesives that contain urea formaldehyde.

Retain paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.1.

I. VOC Limits for Installation Adhesives and Glues:  Use installation adhesives that comply with the following limits for VOC content when calculated according to 40 CFR 59, Subpart D (EPA Method 24):

Edit list below by deleting applications not used.  VOC limits listed are from South Coast Air Quality Management District Rule #1168.

1. Wood Glues:  30 g/L.

2. Contact Adhesive:  250 g/L.

Retain one of five options in paragraph below or delete all and leave as woodworker's option.  See AWI standard and Editing Instruction No. 2 in the Evaluations.  First and second options are suitable for general use and for postforming.  Use only unpigmented product with through-color laminate.  Water-based varieties must be used where VOC limits apply.  Third option is white or yellow wood glue and is good for use with through-color laminates; it is not for postforming and has poor water, chemical, and heat resistance.  Fourth option has good water and chemical resistance and resistance to temperature fluctuations; it is also suitable for postforming and for through-color laminates.  Retain fifth option if required for fire resistance; it is the only adhesive with flame-spread index less than 25.  Resorcinol also has good water and chemical resistance; it is not for postforming or for through-color laminates.

J. Adhesive for Bonding Plastic Laminate:  [Unpigmented contact cement] [Contact cement] [PVA] [Urea formaldehyde] [Resorcinol].

Retain subparagraph below unless good chemical, fire, or temperature resistance is required.

1. Adhesive for Bonding Edges:  Hot-melt adhesive[ or adhesive specified above for faces].

2.6 FABRICATION, GENERAL

If all woodwork is same grade, retain first paragraph below and delete separate grades in other articles; otherwise, delete paragraph or retain as default and indicate exceptions in other articles.

A. Interior Woodwork Grade:  Unless otherwise indicated, provide [Premium] [Custom] [Economy]-grade interior woodwork complying with referenced quality standard.

B. Wood Moisture Content:  Comply with requirements of referenced quality standard for wood moisture content in relation to ambient relative humidity during fabrication and in installation areas.

C. Sand fire-retardant-treated wood lightly to remove raised grain on exposed surfaces before fabrication.

D. Fabricate woodwork to dimensions, profiles, and details indicated.  Ease edges to radius indicated for the following:

1. Corners of Cabinets and Edges of Solid-Wood (Lumber) Members 3/4 Inch (19 mm) Thick or Less:  1/16 inch (1.5 mm).

2. Edges of Rails and Similar Members More Than 3/4 Inch (19 mm) Thick:  1/8 inch (3 mm).

For highest-quality work, delete subparagraphs above and retain subparagraph below; otherwise, delete below.

3. Corners of Cabinets and Edges of Solid-Wood (Lumber) Members and Rails:  1/16 inch (1.5 mm).

If applicable, insert subparagraph to describe conditions where eased edges are not required.

E. Complete fabrication, including assembly[, finishing,] and hardware application, to maximum extent possible before shipment to Project site.  Disassemble components only as necessary for shipment and installation.  Where necessary for fitting at site, provide ample allowance for scribing, trimming, and fitting.

Retain subparagraph below if Architect will examine work in woodwork shop before it is shipped to Project site.

1. Notify Architect seven days in advance of the dates and times woodwork fabrication will be complete.

Retain subparagraph below for high-quality and large or complex work.

2. Trial fit assemblies at fabrication shop that cannot be shipped completely assembled.  Install dowels, screws, bolted connectors, and other fastening devices that can be removed after trial fitting.  Verify that various parts fit as intended and check measurements of assemblies against field measurements indicated on Shop Drawings before disassembling for shipment.

F. Shop-cut openings to maximum extent possible to receive hardware, appliances, plumbing fixtures, electrical work, and similar items.  Locate openings accurately and use templates or roughing-in diagrams to produce accurately sized and shaped openings.  Sand edges of cutouts to remove splinters and burrs.

1. Seal edges of openings in countertops with a coat of varnish.

G. Install glass to comply with applicable requirements in Division 08 Section "Glazing" and in GANA's "Glazing Manual." For glass in wood frames, secure glass with removable stops.

2.7 INTERIOR STANDING AND RUNNING TRIM FOR TRANSPARENT FINISH

Retain one of three grades in first paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

B. Wood Species and Cut:  [Red oak, plain sawn] [Match species and cut indicated for other types of transparent-finished architectural woodwork located in same area of building, unless otherwise indicated] <Insert species and cut>.

Retain subparagraph below with second option in paragraph above if split finishes are required.

1. Provide split species on trim that faces areas with different wood species, matching each face of woodwork to species and cut of finish wood surfaces in areas finished.

Delete paragraph below if trim is not wide enough to allow gluing for width or if gluing for width is not objectionable.

C. For trim items wider than available lumber, use veneered construction.  Do not glue for width.

Delete paragraph below if rails are not wide enough or thick enough to allow gluing for width or thickness or if gluing for width or thickness is not objectionable.  AWI's definition of standing and running trim includes "rails used on corridor walls of hospitals or nursing homes, etc., and guard rails at glass openings."

D. For rails wider or thicker than available lumber, use veneered construction.  Do not glue for width or thickness.

See Editing Instruction No. 2 in the Evaluations.

E. Backout or groove backs of flat trim members and kerf backs of other wide, flat members, except for members with ends exposed in finished work.

Retain paragraph below or revise if not applicable to all casings.  Plant assembly of casings applies only to Premium and Custom grades and is not required by AWI standards unless so specified.

F. Assemble casings in plant except where limitations of access to place of installation require field assembly.

Retain paragraph below only if required for monumental work.

G. Assemble moldings in plant to maximum extent possible.  Miter corners in plant and prepare for field assembly with bolted fittings designed to pull connections together.

2.8 INTERIOR STANDING AND RUNNING TRIM FOR OPAQUE FINISH

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

For opaque-finished woodwork, closed-grain hardwood is generally a better choice than softwoods, except for Economy grade.

B. Wood Species:  [Any closed-grain hardwood] [Eastern white pine, sugar pine, or western white pine] <Insert species>.

See Editing Instruction No. 2 in the Evaluations.

C. Backout or groove backs of flat trim members and kerf backs of other wide, flat members, except for members with ends exposed in finished work.

Retain paragraph below or revise if not applicable to all casings.  Plant assembly of casings applies only to Premium and Custom grades and is not required by AWI standards unless so specified.

D. Assemble casings in plant except where limitations of access to place of installation require field assembly.

Retain paragraph below only if required for monumental work.

E. Assemble moldings in plant to maximum extent possible.  Miter corners in plant and prepare for field assembly with bolted fittings designed to pull connections together.

2.9 INTERIOR FRAMES AND JAMBS FOR TRANSPARENT FINISH

This Article generally applies to shop-assembled frames.  Job-built work is standing trim.

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

Options in paragraph below are examples only.  Retain second option if frames and jambs must match other wood surfaces such as standing and running trim, cabinets, or paneling.

B. Wood Species and Cut:  [Red oak, plain sawn] [Match species and cut indicated for other types of transparent-finished architectural woodwork located in same area of building, unless otherwise indicated] <Insert species and cut>.

Delete paragraph below if frames or jambs are not wide enough to allow gluing for width or if gluing for width is not objectionable.

C. For frames or jambs wider than available lumber, use veneered construction.  Do not glue for width.

Delete paragraph and subparagraph below if fire-rated frames are not required.

D. Fire-Rated Interior Frames and Jambs:  Products fabricated from fire-retardant particleboard or fire-retardant medium-density fiberboard with veneered, exposed surfaces and listed and labeled by a testing and inspecting agency acceptable to authorities having jurisdiction, for fire ratings indicated, based on testing according to NFPA 252.

1. Fire Rating:  20 minutes.

2.10 INTERIOR FRAMES AND JAMBS FOR OPAQUE FINISH

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

For opaque-finished woodwork, closed-grain hardwood is generally a better choice than softwoods, except for Economy grade.

B. Wood Species:  [Any closed-grain hardwood] [Eastern white pine, sugar pine, or western white pine] <Insert species>.

Insert requirements for fire-rated frames if needed; copy from "Interior Frames and Jambs for Transparent Finish" Article and revise to suit Project.

2.11 STAIRWORK[ AND RAILS]

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

B. Grade:

C. Wood Species and Cut for Transparent Finish:  [Red oak, quarter sawn] [Hard maple, plain sawn] [Quarter-sawn, red-oak treads; plain-sawn, hard-maple handrails] <Insert species and cut>.

Retain one of three options in first paragraph below.  For opaque-finished woodwork, especially for items that are subject to impact, closed-grain hardwood is a better choice than softwoods, except for Economy grade.

D. Wood Species for Opaque Finish:  [Any closed-grain hardwood] [Eastern white pine, sugar pine, or western white pine] [Any closed-grain hardwood, except that eastern white pine, sugar pine, or western white pine may be used for risers, stringers, and moldings] <Insert species>.

E. Finishes for Stair Parts:  As follows:

Retain one finish for each item in subparagraphs below.

1. Treads:  [Transparent] [Opaque].

2. Risers:  [Transparent] [Opaque].

3. Stringers:  [Transparent] [Opaque].

4. Balusters:  [Transparent] [Opaque].

5. Handrails:  [Transparent] [Opaque].

6. Scotia, Cove, and Other Moldings:  [Transparent] [Opaque].

Paragraph and subparagraphs below are based on assumption that stairs are assembled, at least in sections, in the woodwork shop.  "Fabrication, General" Article requires that Contractor "complete fabrication, including assembly(, finishing,) and hardware application, to maximum extent possible before shipment to Project site," based on the assumption that this will result in better work.  Part 3 "Installation" Article includes a requirement that Contractor "complete fabrication at Project site to comply with requirements for fabrication in Part 2, to extent that it was not completed in the shop" so that if Contractor is not required to perform fabrication specified below, requirements will still apply.  WI requires that stairwork "be furnished knocked down" for all grades.  AWI is silent on the matter.  Copy and move paragraph and appropriate subparagraphs to Part 3 if field assembly is required.

F. Cut carriages to accurately fit treads and risers.  Glue treads to risers, and glue and nail treads and risers to carriages.

Delete first subparagraph below if no wall or face stringers or if housed stringers are not required.  AWI requires that wall stringers be housed with treads and risers wedged and glued for Premium grade only, but requires that face stringers be housed with treads and risers wedged and glued for both Premium and Custom grades.  WI requires that housed stringers be machined to receive treads, risers, and wedges for both Premium and Custom grades, but does not require that wall or face stringers be housed in any grade.

1. House [wall] [and] [face] stringers and glue and wedge treads and risers.

2. Fabricate stairs with treads and risers no more than 1/8 inch (3 mm) from indicated position and no more than 1/16 inch (1.5 mm) out of position for adjacent treads and risers.

2.12 FLUSH WOOD PANELING[ AND WAINSCOTS]

Other forms of paneling included in standards are laminate-clad flush paneling and stile and rail paneling; insert or specify those in a separate section.

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.  Premium grade is required for blueprint-matched paneling.

A. Grade:  [Premium] [Custom] [Economy].

Options in paragraph below are examples only.  Retain one or insert others.

B. Wood Species and Cut:  [White oak, rift cut] [White ash, plain sliced] [Red gum, plain sliced] [Brown ash, plain sliced] [Hickory, plain sliced] [As indicated] <Insert species and cut>.

Usually retain subparagraph below, particularly for rare woods that may not be available in lumber.  Also retain if cores must be fire-retardant treated.

1. Lumber Trim and Edges:  At fabricator's option, trim and edges indicated as solid wood (except moldings) may be either lumber or veneered construction compatible with grain and color of veneered panels.

Retain one of three options in paragraph below.

C. Matching of Adjacent Veneer Leaves:  [Book] [Slip] [Random] match.

Retain one of three options in first paragraph below.

D. Veneer Matching within Panel Face:  [Running] [Balance] [Center-balance] match.

E. Panel-Matching Method:  No matching between panels is required.  Select and arrange panels for similarity of grain pattern and color between adjacent panels.

Retain paragraph above for Economy grade; retain paragraph below for Custom or Premium grade.

F. Panel-Matching Method:  Match panels within each separate area by the following method:

Retain one of four subparagraphs below, which are listed in order of increasing cost.  To retain control over joint location, retain "as indicated" and show panel joints on Drawings.  Last two subparagraphs apply to Premium grade.

1. Premanufactured sets used full width[ as indicted].

2. Premanufactured sets selectively reduced in width[ as indicated].

3. Sequence-matched, uniform-size sets[ as indicated].

4. Blueprint-matched panels and components.

If retaining blueprint matching, retain one of two subparagraphs below and coordinate with Division 01 Sections referenced.  These requirements may also be used with sequence-matched sets.

5. Refer to Division 01 Section "Summary" for requirements concerning flitches reserved by Architect.

6. Refer to Division 01 Section "Allowances" for allowances covering the purchase of wood face veneers for panels and components.

Retain one of five options in paragraph below if panels are arranged two or more panels high.  See Evaluations.  If vertical matching is required because of high ceiling height, verify availability of flitches with sufficient length before retaining first option.

G. Vertical Panel-Matching Method:  [Continuous match; veneer leaves of upper panels are continuations of veneer leaves of lower panels] [Vertical book match; veneer leaves are individually book matched from lower panels to upper panels] [Vertical slip match; veneer leaves are individually slip matched from lower panels to upper panels] [Panel vertical book match; panels are book matched from lower panels to upper panels] [Panel vertical slip match; panels are slip matched from lower panels to upper panels].

Delete paragraph below if not applicable.

H. Fire-Retardant-Treated Paneling:  Provide panels consisting of wood veneer and fire-retardant particleboard or fire-retardant medium-density fiberboard.  Panels shall have flame-spread index of [75] [25] or less and smoke-developed index of 450 or less per ASTM E 84.

2.13 INTERIOR ORNAMENTAL WORK FOR TRANSPARENT FINISH

AWI uses the term "interior ornamental work" to refer to miscellaneous items of woodwork not included in other categories in its standard.  WI includes these items with the term "millwork" in the category "Interior - Trim, Jambs & Millwork."

A. Interior ornamental work for transparent finish includes the following:

Edit list below to suit Project.

1. Balustrades.

2. Columns.

3. Grilles.

4. Mantels.

5. Pediment heads.

6. Pilasters.

7. <Insert description.>

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

B. Grade:  [Premium] [Custom] [Economy].

Options in paragraph below are examples only.  Retain second option if ornamental work must match other wood surfaces such as cabinets or paneling.

C. Wood Species and Cut:  [Red oak, plain sawn or cut] [Match species and cut indicated for other types of transparent-finished architectural woodwork located in same area of building, unless otherwise indicated] <Insert species and cut>.

2.14 INTERIOR ORNAMENTAL WORK FOR OPAQUE FINISH

AWI uses the term "interior ornamental work" to refer to miscellaneous items of woodwork not included in other categories in its standard.  WI includes these items with the term "millwork" in the category "Interior - Trim, Jambs & Millwork."

A. Interior ornamental work for opaque finish includes the following:

Edit list below to suit Project.

1. Balustrades.

2. Columns.

3. Grilles.

4. Mantels.

5. Pediment heads.

6. Pilasters.

7. <Insert description.>

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

B. Grade:  [Premium] [Custom] [Economy].

For opaque-finished woodwork, closed-grain hardwood is generally a better choice than softwoods, except for Economy grade.

C. Wood Species:  [Any closed-grain hardwood] [Eastern white pine, sugar pine, or western white pine] <Insert species>.

2.15 WOOD CABINETS FOR TRANSPARENT FINISH

Retain one of four grades in first paragraph below; delete paragraph if one grade is specified for all interior woodwork.  Laboratory grade only applies to WI.  If retaining Laboratory grade, special finishes must be inserted into "Shop Finishing" Article.  See Evaluations and WI's manual.

A. Grade:  [Premium] [Custom] [Economy] [Laboratory].

B. AWI Type of Cabinet Construction:  [Flush overlay] [Reveal overlay] [Reveal overlay on face frame] [Flush inset] [Flush inset with face frame] [As indicated].

Retain one of six options in paragraph above if AWI standard is referenced.  If WI standard is referenced, delete paragraph above and select one requirement for WI construction style, construction type, and door and drawer front style from three paragraphs below.  See WI's manual when making selections.

C. WI Construction Style:  Style [A, Frameless] [B, Face Frame].

D. WI Construction Type:  Type [I, multiple self-supporting units rigidly joined together] [II, single-length sections to fit access openings].

E. WI Door and Drawer Front Style:  [Flush overlay] [Reveal overlay] [Lipped] [Flush].

Delete paragraph below if reveal overlay construction is not used.  Dimension given is an example only.

F. Reveal Dimension:  [1/2 inch (13 mm)] [As indicated] <Insert dimension>.

Options in paragraph below are examples only.  Retain one or insert others where required by design or construction of cabinets indicated.

G. Wood Species and Cut for Exposed Surfaces:  [Red oak, plain sawn or sliced] [White ash, plain sawn or sliced] [White birch, plain sawn or sliced] [As indicated] <Insert species and cut>.

Retain one of three options in subparagraph below for Premium-grade cabinets, or delete all if selecting lower-quality grade or if grain matching is not required.

1. Grain Direction:  [Vertically for drawer fronts, doors, and fixed panels] [Horizontally for drawer fronts, doors, and fixed panels] [As indicated].

Retain one of three options in subparagraph below for Premium- or Custom-grade cabinets.

2. Matching of Veneer Leaves:  [Book] [Slip] [Random] match.

Retain subparagraph below in addition to one option in subparagraph above only for large pieces or decorative, four-way matching.  See Evaluations.

3. Vertical Matching of Veneer Leaves:  End match.

Retain one of three options in subparagraph below for Premium-grade cabinets.

4. Veneer Matching within Panel Face:  [Running] [Balance] [Center-balance] match.

Retain subparagraph below for blueprint matching when only cabinets are to be matched.

5. Veneer Matching within Room:  Provide cabinet veneers in each room or other space from a single flitch with doors, drawer fronts, and other surfaces matched in a sequenced set with continuous match where veneers are interrupted perpendicular to the grain.

Delete five subparagraphs above and retain subparagraph below if blueprint-matched paneling is specified for same area as cabinets.

6. Comply with veneer and other matching requirements indicated for blueprint-matched paneling.

Delete paragraph and subparagraphs below for woodworker's option from choices in standard.  See Editing Instruction No. 2 in the Evaluations.

H. Semiexposed Surfaces:  Provide surface materials indicated below:

Retain one option in each of three subparagraphs below or revise to suit Project.

1. Surfaces Other Than Drawer Bodies:  [Same species and cut indicated for exposed surfaces] [Thermoset decorative panels] [Compatible species to that indicated for exposed surfaces, stained to match].

2. Drawer Sides and Backs:  [Solid-hardwood lumber, same species indicated for exposed surfaces] [Solid-hardwood lumber, stained to match species indicated for exposed surfaces] [Solid-hardwood lumber] [Thermoset decorative panels].

3. Drawer Bottoms:  [Hardwood plywood] [Thermoset decorative panels].

Delete paragraph below if not desired.  Dust panels are not required by standards.

I. Provide dust panels of 1/4-inch (6.4-mm) plywood or tempered hardboard above compartments and drawers, unless located directly under tops.

2.16 WOOD CABINETS FOR OPAQUE FINISH

Retain one of four grades in first paragraph below; delete paragraph if one grade is specified for all interior woodwork.  Laboratory grade only applies to WI.  If retaining Laboratory grade, special finishes must be inserted into "Shop Finishing" Article.  See Evaluations and WI's manual.

A. Grade:  [Premium] [Custom] [Economy] [Laboratory].

B. AWI Type of Cabinet Construction:  [Flush overlay] [Reveal overlay] [Reveal overlay on face frame] [Flush inset] [Flush inset with face frame] [As indicated].

Retain one of six options in paragraph above if AWI standard is referenced.  If WI standard is referenced, delete paragraph above and select one requirement for WI construction style, construction type, and door and drawer front style from three paragraphs below.  See WI's manual when making selections.

C. WI Construction Style:  Style [A, Frameless] [B, Face Frame].

D. WI Construction Type:  Type [I, multiple self-supporting units rigidly joined together] [II, single-length sections to fit access openings].

E. WI Door and Drawer Front Style:  [Flush overlay] [Reveal overlay] [Lipped] [Flush].

Delete first paragraph below if reveal overlay construction is not used.  Dimension given is an example only.

F. Reveal Dimension:  [1/2 inch (13 mm)] [As indicated] <Insert dimension>.

G. Species for Exposed Lumber Surfaces:  Any closed-grain hardwood.

Paragraph above and below are examples if specifier wants to limit selection rather than allow woodworker to select from products permitted by referenced woodworking standard.  Revise or delete both.  See Editing Instruction No. 2 in the Evaluations.

H. Panel Product for Exposed Surfaces:  Medium-density [fiberboard] [overlay].

Delete paragraph and subparagraphs below for woodworker's option from choices in standard.  See Editing Instruction No. 2 in the Evaluations.

I. Semiexposed Surfaces:  Provide surface materials indicated below:

Retain one option from each of three subparagraphs below or revise to suit Project.

1. Surfaces Other Than Drawer Bodies:  [Match materials indicated for exposed surfaces] [Thermoset decorative panels].

2. Drawer Sides and Backs:  [Solid-hardwood lumber] [Thermoset decorative panels].

3. Drawer Bottoms:  [Hardwood plywood] [Thermoset decorative panels].

Delete paragraph below if not desired.  Dust panels are not required by standards.

J. Provide dust panels of 1/4-inch (6.4-mm) plywood or tempered hardboard above compartments and drawers, unless located directly under tops.

2.17 PLASTIC-LAMINATE CABINETS

Retain one of four grades in first paragraph below; delete paragraph if one grade is specified for all interior woodwork.  Laboratory grade only applies to WI.  If retaining Laboratory grade, special finishes must be inserted into "Shop Finishing" Article.  See Evaluations and WI's manual.

A. Grade:  [Premium] [Custom] [Economy] [Laboratory].

B. AWI Type of Cabinet Construction:  [Flush overlay] [Reveal overlay] [Reveal overlay on face frame] [Flush inset] [Flush inset with face frame] [As indicated].

Retain one of six options in paragraph above if AWI standard is referenced.  If WI standard is referenced, delete paragraph above and select one requirement for WI construction style, construction type, and door and drawer front style from three paragraphs below.  See WI's manual when making selections.

C. WI Construction Style:  Style [A, Frameless] [B, Face Frame].

D. WI Construction Type:  Type [I, multiple self-supporting units rigidly joined together] [II, single-length sections to fit access openings].

E. WI Door and Drawer Front Style:  [Flush overlay] [Reveal overlay] [Lipped] [Flush].

Delete first paragraph below if reveal overlay construction is not used.  Dimension given is an example only.

F. Reveal Dimension:  [1/2 inch (13 mm)] [As indicated] <Insert dimension>.

G. Laminate Cladding for Exposed Surfaces:  High-pressure decorative laminate complying with the following requirements:

Retain grade designations from options in subparagraphs below.  Grade HGS is 1.2 mm thick, Grades HGL and HGP are 1.0 mm thick, and Grade VGS is 0.7 mm thick.  AWI and WI standards require minimum thickness of 0.028 inch (0.7 mm) regardless of surface type.

1. Horizontal Surfaces Other Than Tops:  Grade [HGS] [HGL].

2. Postformed Surfaces:  Grade [HGP].

3. Vertical Surfaces:  Grade [HGS] [VGS].

Retain one edge construction from subparagraph below.  Coordinate with standards and grade selection.

4. Edges:  [Grade HGS] [Grade VGS] [PVC tape, 0.018-inch (0.460-mm) minimum thickness, matching laminate in color, pattern, and finish] [PVC T-mold matching laminate in color, pattern, and finish] [PVC edge banding,0.12 inch (3 mm) thick, matching laminate in color, pattern, and finish].

Delete paragraph and subparagraphs below for woodworker's option from choices in standard.  See Editing Instruction No. 2 in the Evaluations.

H. Materials for Semiexposed Surfaces:

1. Surfaces Other Than Drawer Bodies:  [High-pressure decorative laminate, Grade VGS] [High-pressure decorative laminate, Grade CLS] [Thermoset decorative panels].

Retain one edge construction from subparagraph below if retaining high-pressure decorative laminate in subparagraph above.

a. Edges of Plastic-Laminate Shelves:  [PVC tape, 0.018-inch (0.460-mm) minimum thickness, matching laminate in color, pattern, and finish] [PVC T-mold matching laminate in color, pattern, and finish] [PVC edge banding,0.12 inch (3 mm) thick, matching laminate in color, pattern, and finish].

Retain first subparagraph below if required to provide balanced construction.

b. For semiexposed backs of panels with exposed plastic-laminate surfaces, provide surface of high-pressure decorative laminate, Grade [VGS] [CLS].

2. Drawer Sides and Backs:  [Solid-hardwood lumber] [Thermoset decorative panels].

3. Drawer Bottoms:  [Hardwood plywood] [Thermoset decorative panels].

Retain first paragraph below if required to provide balanced construction.

I. Concealed Backs of Panels with Exposed Plastic Laminate Surfaces:  High-pressure decorative laminate, Grade BKL.

J. Colors, Patterns, and Finishes:  Provide materials and products that result in colors and textures of exposed laminate surfaces complying with the following requirements:

Retain one of three subparagraphs and associated subparagraphs below.  If retaining first, indicate colors, patterns, and finishes in a separate schedule.

1. As indicated by laminate manufacturer's designations.

2. Match Architect's sample.

3. As selected by Architect from laminate manufacturer's full range in the following categories:

a. Solid colors, [gloss] [matte] finish.

b. Solid colors with core same color as surface, [gloss] [matte] finish.

c. Wood grains, [gloss] [matte] finish.

d. Patterns, [gloss] [matte] finish.

Delete paragraph below if not desired.  Dust panels are not required by standards.

K. Provide dust panels of 1/4-inch (6.4-mm) plywood or tempered hardboard above compartments and drawers, unless located directly under tops.

2.18 WOOD COUNTERTOPS

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

Retain one type of top and related requirements in three paragraphs below, or retain more than one and indicate locations of each on Drawings or in schedules.

B. Type of Top:  Solid wood for transparent finish, edge glued, with crown direction reversed in adjacent boards, to produce widths indicated.  Select boards for similarity of color and grain and arrange boards for optimum match between adjacent boards.  Species and cut as follows:

Options in subparagraph below are examples only.  Retain one or insert others.

1. Wood Species and Cut:  [Red oak, plain sawn] [Hickory, plain sawn] [African mahogany, plain sawn] [As indicated] <Insert species and cut>.

First paragraph below is for a butcher-block effect; paragraph above is for a more uniform effect.

C. Type of Top:  Solid laminated for transparent finish.  Narrow strips of lumber glued together with crown direction reversed in adjacent strips.  Arrange strips for random mix of color and grain.  Species and cut as follows:

Options in subparagraph below are examples only.  Retain one or insert others.

1. Wood Species:  [Red oak] [Hard maple] [Teak] [As indicated] <Insert species>.

Options in subparagraph below are examples only.

2. Strip Thickness:  [3/4 inch (19 mm)] [1-1/2 inches (38 mm)] [As indicated].

D. Type of Top:  Panel product for transparent finish (wood veneer laminated over core) as follows:

Options in subparagraph below are examples only.  Retain one or insert others.

1. Wood Species and Cut:  [Red oak, rift cut] [Hickory, plain sliced] [Walnut, plain sliced] [As indicated] <Insert species and cut>.

Retain one of three options in subparagraph below.

2. Matching of Adjacent Veneer Leaves:  [Book] [Slip] [Random] match.

Retain subparagraph below only if tops are longer than veneer leaves or if required for special effect.  Show on Drawings.

3. Matching of Adjacent Veneer Leaves:  End match.

Retain one of three options in subparagraph below.

4. Veneer Matching within Panel Face:  [Running] [Balance] [Center-balance] match.

Retain one of three options in subparagraph below.

5. Edge Treatment:  [Solid wood matching face for species and cut] [Wood veneer matching face for species and cut] [As indicated].

Retain one of seven options in subparagraph below or delete all and leave as woodworker's option from choices in standard.  See Editing Instruction No. 2 in the Evaluations.

6. Core Material:  [Particleboard or medium-density fiberboard] [Particleboard] [Medium-density fiberboard] [Particleboard made with exterior glue] [Medium-density fiberboard made with exterior glue] [Exterior-grade plywood] [Fire-retardant particleboard].

2.19 PLASTIC-LAMINATE COUNTERTOPS

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

Retain first option in first paragraph below for flat countertops; retain second for postformed countertops.

B. High-Pressure Decorative Laminate Grade:  [HGS] [HGP].

C. Colors, Patterns, and Finishes:  Provide materials and products that result in colors and textures of exposed laminate surfaces complying with the following requirements:

Retain one of three subparagraphs and associated subparagraphs below.  If retaining first, indicate colors, patterns, and finishes in a separate schedule.

1. As indicated by manufacturer's designations.

2. Match Architect's sample.

3. As selected by Architect from manufacturer's full range in the following categories:

a. Solid colors, [gloss] [matte] finish.

b. Solid colors with core same color as surface, [gloss] [matte] finish.

c. Wood grains, [gloss] [matte] finish.

d. Patterns, [gloss] [matte] finish.

Delete paragraph below if no wood-grain laminates.

D. Grain Direction:  Parallel to cabinet fronts.

Retain one of three edge treatments in paragraph below or revise to suit Project.  If retaining lumber edge, indicate profile on Drawings.

E. Edge Treatment:  [Same as laminate cladding on horizontal surfaces] [Lumber edge for transparent finish matching wood species and cut on cabinet surfaces] [As indicated].

Retain one of seven options in first paragraph below or delete all and leave as woodworker's option from choices in standard.  See Editing Instruction No. 2 in the Evaluations.

F. Core Material:  [Particleboard or medium-density fiberboard] [Particleboard] [Medium-density fiberboard] [Particleboard made with exterior glue] [Medium-density fiberboard made with exterior glue] [Exterior-grade plywood] [Fire-retardant particleboard].

G. Core Material at Sinks:  [Particleboard made with exterior glue] [Medium-density fiberboard made with exterior glue] [or] [exterior-grade plywood].

H. Backer Sheet:  Provide plastic-laminate backer sheet, Grade BKL, on underside of countertop substrate.

Retain paragraph above for highest-quality work; retain paragraph below for high-quality work.  AWI requires backer sheet for Premium grade and paper backer for Custom grade when unsupported area of 3/4-inch (19-mm) top exceeds 6 sq. ft. (0.6 sq. m).

I. Paper Backing:  Provide paper backing on underside of countertop substrate.

2.20 SOLID-SURFACING-MATERIAL COUNTERTOPS

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom] [Economy].

Retain one of two options in first paragraph below.

B. Solid-Surfacing-Material Thickness:  [1/2 inch (13 mm)] [3/4 inch (19 mm)].

C. Colors, Patterns, and Finishes:  Provide materials and products that result in colors of solid-surfacing material complying with the following requirements:

Retain one of three options in subparagraph below.  If retaining first, indicate colors, patterns, and finishes in a separate schedule.

1. [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range].

D. Fabricate tops in one piece, unless otherwise indicated.  Comply with solid-surfacing-material manufacturer's written recommendations for adhesives, sealers, fabrication, and finishing.

Delete first subparagraph below if tops do not have applied edges.

1. Fabricate tops with shop-applied edges of materials and configuration indicated.

2. Fabricate tops with [shop-applied backsplashes] [loose backsplashes for field application].

Delete two paragraphs below if no sinks.

E. Install integral sink bowls in countertops in shop.

F. Drill holes in countertops for plumbing fittings and soap dispensers in shop.

2.21 LAMINATED-PLASTIC LABORATORY TOPS

This Article applies only to WI-referenced woodwork.  Delete if not applicable or if AWI standards are referenced in Part 1 "Quality Assurance" Article.

Retain one of two grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.

A. Grade:  [Premium] [Custom].

Retain third option in first paragraph below only where a high degree of chemical resistance is required; otherwise, retain first for flat laboratory tops, second for postformed laboratory tops.

B. High-Pressure Decorative Laminate:  [Grade HGS] [Grade HGP] [Chemical-resistant, Grade HGP].

C. Colors and Patterns:  Provide materials and products that result in colors and patterns of exposed laminate surfaces complying with the following requirements:

Retain one of two subparagraphs below.  If retaining first, indicate colors and patterns in a separate schedule.

1. As indicated by manufacturer's designations.

2. As selected by Architect from manufacturer's full range of [solid colors] [colors and patterns].

Retain one of five options in paragraph below or delete all and leave as woodworker's option from choices in standard.  See Editing Instruction No. 2 in the Evaluations.

D. Core Material:  [Particleboard] [Particleboard made with exterior glue] [Fire-retardant particleboard] [Rotary-cut lauan or closed-grain hardwood plywood] [Exterior-grade rotary-cut lauan or closed-grain hardwood plywood].

Insert other types of laboratory tops, including composition stone, glass-reinforced polyester, and epoxy resin.  See WI standard.

2.22 CLOSET AND UTILITY SHELVING

This Article applies only to AWI-referenced woodwork.  Delete if not applicable or if WI standards are referenced in Part 1 "Quality Assurance" Article.  Copy and re-edit this Article if both transparent- and opaque-finished shelves are required.

Retain one of three grades in paragraph below; delete paragraph if one grade is specified for all interior woodwork.  Coordinate with shelf material.

A. Grade:  [Premium] [Custom] [Economy].

Retain one material in first paragraph below.  Not all options apply to all grades; coordinate with grade selected in paragraph above.

B. Shelf Material:  3/4-inch (19-mm) [solid lumber] [veneer-faced panel product with solid-lumber edge] [veneer-faced panel product with veneer edge banding] [thermoset decorative panel with solid-lumber edge] [thermoset decorative panel with PVC or polyester edge banding] [medium-density fiberboard with solid-lumber edge] [particleboard with solid-lumber edge] [medium-density fiberboard with radiused edge] [particleboard with radiused and filled edge].

C. Cleats:  3/4-inch (19-mm) [solid lumber] [thermoset decorative panel] [panel product].

Delete paragraph below if not applicable.  For opaque-finished woodwork, closed-grain hardwood is generally a better choice than softwoods, except for Economy grade.

D. Wood Species:  [Red oak] [Match species indicated for other types of transparent-finished architectural woodwork located in same area of building, unless otherwise indicated] [Match species indicated for door to closet where shelving is located] [Any closed-grain hardwood] [Eastern white pine, sugar pine, or western white pine] <Insert species>.

2.23 SHOP FINISHING

Delete this Article if shop finishing is not required.  See Evaluations.  Shop finishing can be used to help comply with LEED-NC or LEED-CI Credit EQ 4.2, which limits VOC content of paints and coatings used within building.

Retain paragraph below and delete other grade requirements, or delete below and specify grades under finish types.  Finish grade can be different from Construction grade.

A. Grade:  Provide finishes of same grades as items to be finished.

Retain one of three paragraphs below to indicate extent of shop finishing required.  Paragraph below requires all work to be shop finished.

B. General:  Finish architectural woodwork at fabrication shop as specified in this Section.  Defer only final touchup, cleaning, and polishing until after installation.

Retain paragraph below if both painted and transparent finishes are used and only transparent finish is shop applied.

C. General:  Shop finish transparent-finished interior architectural woodwork at fabrication shop as specified in this Section.  Refer to Division 09 painting Sections for finishing opaque-finished architectural woodwork.

Retain paragraph below if both shop-finished and field-finished architectural woodwork is required and Drawings indicate which items are required to be shop finished.

D. General:  Drawings indicate items that are required to be shop finished.  Finish such items at fabrication shop as specified in this Section.  Refer to Division 09 painting Sections for finishing architectural woodwork not indicated to be shop finished.

Retain first paragraph below if any field-finished woodwork is required to be shop primed.

E. Shop Priming:  Shop apply the prime coat including backpriming, if any, for[ transparent-finished] items specified to be field finished.  Refer to Division 09 painting Sections for material and application requirements.

F. Preparation for Finishing:  Comply with referenced quality standard for sanding, filling countersunk fasteners, sealing concealed surfaces, and similar preparations for finishing architectural woodwork, as applicable to each unit of work.

Generally retain subparagraph below.  WI does not require backpriming; AWI only requires it for certain items and grades.  Backpriming helps moderate alternating shrinking and swelling caused by fluctuations in moisture content resulting from variations in relative humidity.

1. Backpriming:  Apply one coat of sealer or primer, compatible with finish coats, to concealed surfaces of woodwork.  Apply two coats to back of paneling and to end-grain surfaces.  Concealed surfaces of plastic-laminate-clad woodwork do not require backpriming when surfaced with plastic laminate, backing paper, or thermoset decorative panels.

G. Transparent Finish:

Retain one of three grades in first subparagraph below unless retaining paragraph requiring finish to be same grade as woodwork item being finished.

1. Grade:  [Premium] [Custom] [Economy].

2. AWI Finish System:  Synthetic penetrating oil.

3. AWI Finish System:  Nitrocellulose lacquer.

4. AWI Finish System:  Catalyzed lacquer.

System in subparagraph below has best resistance to yellowing.

5. AWI Finish System:  Acrylic lacquer.

System in subparagraph below are durable, repairable, and good general-purpose fine finish.

6. AWI Finish System:  Conversion varnish.

System in subparagraph below is durable and has good chemical resistance.

7. AWI Finish System:  Catalyzed vinyl.

System in subparagraph below is very durable but not easily repaired.

8. AWI Finish System:  Catalyzed polyurethane.

System in subparagraph below has high gloss (wet look), requires special care in applying, and is not generally repairable.

9. AWI Finish System:  Two-component polyester.

Retain one of last eight subparagraphs above if AWI standard is referenced; retain one of first ten subparagraphs below if WI standard is referenced.  Lacquers can affect surface-burning characteristics.

10. WI Finish System 1a.:  Nitrocellulose lacquer.

System in first subparagraph below is water-white and has best resistance to yellowing.

11. WI Finish System 1b.:  Acrylic lacquer.

12. WI Finish System 1c.:  Varnish.

13. WI Finish System 1d.:  Polyurethane.

System in first subparagraph below is nonyellowing.

14. WI Finish System 2:  Water-reducible acrylic lacquer.

15. WI Finish System 3a.:  Catalyzed lacquer.

System in first subparagraph below has best chemical resistance but may be difficult to repair.

16. WI Finish System 3b.:  Catalyzed vinyl lacquer.

17. WI Finish System 4:  Conversion varnish.

System in first subparagraph below is very durable but has poor repairability.

18. WI Finish System 5:  Catalyzed polyurethane.

19. WI Finish System 6:  Penetrating oil.

Retain one of three options in subparagraph below.

20. Staining:  [None required] [Match approved sample for color] [Match Architect's sample].

Treatment in first subparagraph below helps prevent blotchiness with wiping stains; it is optional with AWI.

21. Wash Coat for Stained Finish:  Apply wash-coat sealer to woodwork made from closed-grain wood before staining and finishing.

22. Open Finish for Open-Grain Woods:  Do not apply filler to open-grain woods.

Retain subparagraph above or below if open-grain wood is used.

23. Filled Finish for Open-Grain Woods:  After staining (if any), apply paste wood filler to open-grain woods and wipe off excess.  Tint filler to match stained wood.

Retain subparagraph below for highest-quality work to prevent solvent in filler from smearing stain.

a. Apply wash-coat sealer after staining and before filling.

Retain one of four options in subparagraph below; coordinate with effect and finish system selected.  Numerical values for gloss ratings are those published in AWI standard.  Retain flat sheen with oil finish.  Refer to AWI quality standard for sheens available for each finish system.

24. Sheen:  [Flat, 15-30] [Satin, 31-45] [Semigloss, 46-60] [Gloss, 61-100] gloss units measured on 60-degree gloss meter per ASTM D 523.

H. Opaque Finish:

Retain one of three grades in first subparagraph below unless retaining paragraph requiring finish to be same grade as woodwork item being finished.

1. Grade:  [Premium] [Custom] [Economy].

2. AWI Finish System:  Nitrocellulose lacquer.

Systems in three subparagraphs below are good general-purpose finishes, somewhat durable, and easily repaired.

3. AWI Finish System:  Catalyzed lacquer.

4. AWI Finish System:  Acrylic lacquer.

5. AWI Finish System:  Conversion varnish.

System in subparagraph is durable and has good chemical resistance.

6. AWI Finish System:  Catalyzed vinyl.

System in subparagraph below is very durable but not easily repaired.

7. AWI Finish System:  Catalyzed polyurethane.

System in subparagraph below is high gloss, requires special care in applying, and is not generally repairable.

8. AWI Finish System:  Two-component polyester.

Retain one of last seven subparagraphs above if AWI standard is referenced or one of first nine subparagraphs below if WI standard is referenced.  Lacquers can affect surface-burning characteristics.

9. WI Finish System 1a.:  Nitrocellulose lacquer.

10. WI Finish System 1b.:  Acrylic lacquer.

11. WI Finish System 2:  Water-reducible acrylic lacquer.

12. WI Finish System 3a.:  Catalyzed lacquer.

System in first subparagraph below has best chemical resistance but may be difficult to repair.

13. WI Finish System 3b.:  Catalyzed vinyl lacquer.

14. WI Finish System 4:  Conversion varnish.

System in first subparagraph below is very durable but has poor repairability.

15. WI Finish System 5:  Catalyzed polyurethane.

16. WI Finish System 7a.:  Synthetic enamel.

17. WI Finish System 7b.:  Opaque pigmented lacquer.

Retain one of three options in subparagraph below.  If retaining first, indicate colors in a separate schedule.

18. Color:  [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range].

Retain one of four options in subparagraph below; coordinate with effect and finish system selected.  Numerical values for gloss ratings are those published in AWI standard.  Refer to AWI quality standard for sheens available for each finish system.

19. Sheen:  [Flat, 15-30] [Satin, 31-45] [Semigloss, 46-60] [Gloss, 61-100] gloss units measured on 60-degree gloss meter per ASTM D 523.

If referencing WI standards and retaining Laboratory grade for casework, insert special finishes required.

PART 3 -  EXECUTION

3.1 PREPARATION

A. Before installation, condition woodwork to average prevailing humidity conditions in installation areas.

B. Before installing architectural woodwork, examine shop-fabricated work for completion and complete work as required, including removal of packing and backpriming.

3.2 INSTALLATION

Revise first paragraph below if installation grade is different from fabrication grade.

A. Grade:  Install woodwork to comply with requirements for the same grade specified in Part 2 for fabrication of type of woodwork involved.

B. Assemble woodwork and complete fabrication at Project site to comply with requirements for fabrication in Part 2, to extent that it was not completed in the shop.

C. Install woodwork level, plumb, true, and straight.  Shim as required with concealed shims.  Install level and plumb (including tops) to a tolerance of 1/8 inch in 96 inches (3 mm in 2400 mm).

D. Scribe and cut woodwork to fit adjoining work, refinish cut surfaces, and repair damaged finish at cuts.

Delete first paragraph below if no fire-retardant-treated wood.

E. Fire-Retardant-Treated Wood:  Handle, store, and install fire-retardant-treated wood to comply with chemical treatment manufacturer's written instructions, including those for adhesives used to install woodwork.

F. Anchor woodwork to anchors or blocking built in or directly attached to substrates.  Secure with countersunk, concealed fasteners and blind nailing as required for complete installation.  Use fine finishing nails[ or finishing screws] for exposed fastening, countersunk and filled flush with woodwork and matching final finish if transparent finish is indicated.

Delete paragraph and subparagraphs below if not applicable or considered necessary.

G. Standing and Running Trim:  Install with minimum number of joints possible, using full-length pieces (from maximum length of lumber available) to greatest extent possible.  Do not use pieces less than [36 inches (900 mm)] [60 inches (1500 mm)] [96 inches (2400 mm)] long, except where shorter single-length pieces are necessary.[  Scarf running joints and stagger in adjacent and related members.]

1. Fill gaps, if any, between top of base and wall with plastic wood filler, sand smooth, and finish same as wood base if finished.

2. Install wall railings on indicated metal brackets securely fastened to wall framing.

3. Install standing and running trim with no more variation from a straight line than 1/8 inch in 96 inches (3 mm in 2400 mm).

Delete paragraph and subparagraph below if no paneling.

H. Paneling:  Anchor paneling to supporting substrate with [concealed panel-hanger clips] [splined connection strips].  Do not use face fastening, unless [covered by trim] [otherwise indicated].

1. Install flush paneling with no more than 1/16 inch in 96-inch (1.5 mm in 2400-mm) vertical cup or bow and 1/8 inch in 96-inch (3 mm in 2400-mm) horizontal variation from a true plane.

Delete first paragraph below if no stairwork.

I. Stairs:  Securely anchor carriages to supporting substrates.  Install stairs with treads and risers no more than 1/8 inch (3 mm) from indicated position.

J. Railings:

1. General:  Install rails with no more than 1/8 inch in 96-inch (3 mm in 2400-mm) variation from a straight line.

2. Stair Rails:  Glue and dowel or pin balusters to treads and railings, and railings to newel posts.

3. Wall Rails:  Support rails on indicated metal brackets securely fastened to wall framing.

Consider retaining subparagraph below for rails that are not adequately detailed on Drawings.  If retaining, insert a default bracket spacing based on Project conditions and design of rail.

a. Space rail brackets not more than <Insert dimension> o.c.

K. Cabinets:  Install without distortion so doors and drawers fit openings properly and are accurately aligned.  Adjust hardware to center doors and drawers in openings and to provide unencumbered operation.  Complete installation of hardware and accessory items as indicated.

1. Install cabinets with no more than 1/8 inch in 96-inch (3 mm in 2400-mm) sag, bow, or other variation from a straight line.

2. Maintain veneer sequence matching of cabinets with transparent finish.

Revise requirements in subparagraph below as necessary for seismic restraint of cabinets.  Delete if hanging cleats are used and are detailed on Drawings.

3. Fasten wall cabinets through back, near top and bottom, at ends and not more than 16 inches (400 mm) o.c. with [No. 10 wafer-head screws sized for 1-inch (25-mm) penetration into wood framing, blocking, or hanging strips] [No. 10 wafer-head sheet metal screws through metal backing or metal framing behind wall finish] [toggle bolts through metal backing or metal framing behind wall finish].

Delete paragraph and subparagraphs above if no cabinets; delete first paragraph and subparagraphs below if no tops that are not a part of base cabinets.

L. Countertops:  Anchor securely by screwing through corner blocks of base cabinets or other supports into underside of countertop.

Delete first subparagraph below if no solid-surfacing-material countertops.

1. Align adjacent solid-surfacing-material countertops and form seams to comply with manufacturer's written recommendations using adhesive in color to match countertop.  Carefully dress joints smooth, remove surface scratches, and clean entire surface.

2. Install countertops with no more than 1/8 inch in 96-inch (3 mm in 2400-mm) sag, bow, or other variation from a straight line.

Delete first subparagraph below if applied backsplashes are not used.

3. Secure backsplashes [to tops with concealed metal brackets at 16 inches (400 mm) o.c.] [and] [to walls with adhesive].

4. Calk space between backsplash and wall with sealant specified in Division 07 Section "Joint Sealants."

M. Touch up finishing work specified in this Section after installation of woodwork.  Fill nail holes with matching filler where exposed.

Retain paragraph above or below, or both; coordinate with selections made in Part 2 "Shop Finishing" Article.

N. Refer to Division 09 Sections for final finishing of installed architectural woodwork[ not indicated to be shop finished].

3.3 ADJUSTING AND CLEANING

A. Repair damaged and defective woodwork, where possible, to eliminate functional and visual defects; where not possible to repair, replace woodwork.  Adjust joinery for uniform appearance.

B. Clean, lubricate, and adjust hardware.

C. Clean woodwork on exposed and semiexposed surfaces.  Touch up shop-applied finishes to restore damaged or soiled areas.

END OF SECTION 064023

INTERIOR ARCHITECTURAL WOODWORK
064023 - 1

