Copyright 2002 and 2005 AIA
MASTERSPEC Full Length
02/02 (R 05/05)

Copyright 2002 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 312000 - EARTH MOVING
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

A. This Section includes the following:

Adjust list below to suit Project.

1. Preparing subgrades for [slabs-on-grade] [walks] [pavements] [lawns and grasses] [and] [exterior plants].

2. Excavating and backfilling for buildings and structures.

3. Drainage course for slabs-on-grade.

4. Subbase course for concrete [walks] [pavements].

5. Subbase[ and base] course for asphalt paving.

6. Subsurface drainage backfill for walls and trenches.

7. Excavating and backfilling for utility trenches.

8. Excavating and backfilling trenches for buried mechanical and electrical utilities and pits for buried utility structures.

B. Related Sections include the following:

List below only products and construction that the reader might expect to find in this Section but are specified elsewhere.

1. Division 01 Section "Allowances" for quantity allowance provisions related to unit-price rock excavation and authorized additional excavation.

2. Division 01 Section "Unit Prices" for unit-price rock excavation and authorized additional excavation provisions.

3. Division 01 Section "[Construction Progress Documentation] [Photographic Documentation]" for recording preexcavation and earthwork progress.

4. Division 01 Section "Temporary Facilities and Controls" for temporary controls, utilities, and support facilities.

5. Division 01 Section "Temporary Tree and Plant Protection" for protecting and trimming trees to remain.

6. Division 03 Section "Cast-in-Place Concrete" for granular course if placed over vapor retarder and beneath the slab-on-grade.

7. Divisions 21, 22, 23, 26, 27, and 28 Sections for installing underground mechanical and electrical utilities and buried mechanical and electrical structures.

8. Division 31 Section "Site Clearing" for temporary erosion and sedimentation control measures, site stripping, grubbing, stripping[ and stockpiling] topsoil, and removal of above- and below-grade improvements and utilities.

9. Division 31 Section "Dewatering" for lowering and disposing of ground water during construction.

10. Division 31 Section "Excavation Support and Protection" for shoring, bracing, and sheet piling of excavations.

11. Division 31 Section "Drilled Concrete Piers and Shafts" for excavation of shafts and disposal of surplus excavated material.

12. Division 32 Section "Turf and Grasses" for finish grading, including preparing and placing topsoil and planting soil for lawns.

13. Division 32 Section "Plants" for planting bed establishment and tree and shrub pit excavation and planting.

14. Division 33 Section "Subdrainage" for drainage of [foundations] [slabs-on-grade] [walls] [and] [landscaped areas].

1.3 UNIT PRICES

Retain this Article if unit prices are required for rock excavation or if authorized additional excavation is anticipated.

A. Unit prices for earthwork are included in Division 01 Section "Unit Prices."

B. Quantity allowances for earthwork are included in Division 01 Section "Allowances."

Retain paragraph and subparagraphs below for classified excavation.  Measurements are examples only; revise dimensions to suit Project conditions and office standards.  Consider separate unit prices for open rock excavation and trench rock excavation.

C. Rock Measurement:  Volume of rock actually removed, measured in original position, but not to exceed the following.  Unit prices for rock excavation include replacement with approved materials.

1. [24 inches (600 mm)] <Insert dimension> outside of concrete forms other than at footings.

2. [12 inches (300 mm)] <Insert dimension> outside of concrete forms at footings.

3. [6 inches (150 mm)] <Insert dimension> outside of minimum required dimensions of concrete cast against grade.

4. Outside dimensions of concrete walls indicated to be cast against rock without forms or exterior waterproofing treatments.

5. [6 inches (150 mm)] <Insert dimension> beneath bottom of concrete slabs-on-grade.

6. [6 inches (150 mm)] <Insert dimension> beneath pipe in trenches, and the greater of [24 inches (600 mm)] <Insert dimension> wider than pipe or [42 inches (1065 mm)] <Insert dimension> wide.

1.4 DEFINITIONS

Retain definitions that remain after this Section has been edited.  Revise to suit office or local earthwork practices.

A. Backfill:  Soil material or controlled low-strength material used to fill an excavation.

1. Initial Backfill:  Backfill placed beside and over pipe in a trench, including haunches to support sides of pipe.

2. Final Backfill:  Backfill placed over initial backfill to fill a trench.

B. Base Course:  Course placed between the subbase course and hot-mix asphalt paving.

C. Bedding Course:  Course placed over the excavated subgrade in a trench before laying pipe.

D. Borrow Soil:  Satisfactory soil imported from off-site for use as fill or backfill.

Revise heading in first paragraph below to read "Capillary Water Barrier" or a similar title if required.

E. Drainage Course:  Course supporting the slab-on-grade that also minimizes upward capillary flow of pore water.

F. Excavation:  Removal of material encountered above subgrade elevations and to lines and dimensions indicated.

1. Authorized Additional Excavation:  Excavation below subgrade elevations or beyond indicated lines and dimensions as directed by Architect.  Authorized additional excavation and replacement material will be paid for according to Contract provisions for [unit prices] [changes in the Work].

2. Bulk Excavation:  Excavation more than [10 feet (3 m)] <Insert dimension> in width and more than [30 feet (9 m)] <Insert dimension> in length.

3. Unauthorized Excavation:  Excavation below subgrade elevations or beyond indicated lines and dimensions without direction by Architect.  Unauthorized excavation, as well as remedial work directed by Architect, shall be without additional compensation.

G. Fill:  Soil materials used to raise existing grades.

Retain one of two "rock" definitions below for classified excavation.  See Evaluations for further discussion.

Retain paragraph and subparagraphs below if performance of Contractor's equipment is used to define "rock."

H. Rock:  Rock material in beds, ledges, unstratified masses, conglomerate deposits, and boulders of rock material that exceed [1 cu. yd. (0.76 cu. m)] <Insert volume> for bulk excavation or [3/4 cu. yd. (0.57 cu. m)] <Insert volume> for footing, trench, and pit excavation that cannot be removed by rock excavating equipment equivalent to the following in size and performance ratings, without systematic drilling, ram hammering, ripping, or blasting, when permitted:

Retain subparagraph below for confined excavation.  Revise size and performance ratings of equipment to suit Project; ratings are based on Caterpillar's "Model No. 320CL."

1. Excavation of Footings, Trenches, and Pits:  Late-model, track-mounted hydraulic excavator; equipped with a 42-inch- (1065-mm-) wide, maximum, short-tip-radius rock bucket; rated at not less than 138-hp (103-kW) flywheel power with bucket-curling force of not less than 28,090 lbf (125 kN) and stick-crowd force of not less than 18,650 lbf (83 kN); measured according to SAE J-1179.

Retain subparagraph below for mass or bulk excavation.  Revise size and performance ratings of equipment to suit Project; ratings are based on Caterpillar's "Model No. 973C."

2. Bulk Excavation:  Late-model, track-mounted loader; rated at not less than 210-hp (157-kW) flywheel power and developing a minimum of 48,510-lbf (216-kN) breakout force with a general-purpose bare bucket; measured according to SAE J-732.

Retain first paragraph below if standard penetration values are used to define "rock."  Revise number of blows or penetration resistance to suit office practice.  No correlation is intended between equipment- and geotechnical-based definitions of "rock" ; both are arbitrary values chosen to standardize criteria for defining "rock."

I. Rock:  Rock material in beds, ledges, unstratified masses, conglomerate deposits, and boulders of rock material [3/4 cu. yd. (0.57 cu. m)] <Insert volume> or more in volume that exceed a standard penetration resistance of [100 blows/2 inches (97 blows/50 mm)] <Insert number> when tested by an independent geotechnical testing agency, according to ASTM D 1586.

J. Structures:  Buildings, footings, foundations, retaining walls, slabs, tanks, curbs, mechanical and electrical appurtenances, or other man-made stationary features constructed above or below the ground surface.

K. Subbase Course:  Course placed between the subgrade and base course for hot-mix asphalt pavement, or course placed between the subgrade and a cement concrete pavement or a cement concrete or hot-mix asphalt walk.

L. Subgrade:  Surface or elevation remaining after completing excavation, or top surface of a fill or backfill immediately below subbase, drainage fill, or topsoil materials.

M. Utilities:  On-site underground pipes, conduits, ducts, and cables, as well as underground services within buildings.

1.5 SUBMITTALS

Retain only those Submittals required for Project.

A. Product Data:  For the following:

1. Each type of plastic warning tape.

2. Geotextile.

3. Controlled low-strength material, including design mixture.

4. Geofoam.

B. Samples:  12-by-12-inch (300-by-300-mm) Sample of [subdrainage] [separation] geotextile.

Delete test reports below if not required.

C. Material Test Reports:  From a qualified testing agency indicating and interpreting test results for compliance of the following with requirements indicated:

Omit classification and compaction curve of on-site soil if geotechnical report will suffice.

1. Classification according to ASTM D 2487 of each [on-site] [and] [borrow] soil material proposed for fill and backfill.

2. Laboratory compaction curve according to [ASTM D 698] [ASTM D 1557] for each [on-site] [and] [borrow] soil material proposed for fill and backfill.

Submittals in three paragraphs below are for record purposes only.

D. Blasting Plan:  For record purposes[; approved by authorities having jurisdiction].

Delete paragraph above and first paragraph below if blasting is not allowed.  Retain below only if seismic survey is required with blasting.

E. Seismic Survey Report:  For record purposes; from seismic survey agency.

F. Preexcavation Photographs or Videotape:  Show existing conditions of adjoining construction and site improvements, including finish surfaces, that might be misconstrued as damage caused by earthwork operations.  Submit before earthwork begins.

1.6 QUALITY ASSURANCE

Delete paragraph and subparagraphs below if explosives are not permitted.

A. Blasting:  Comply with applicable requirements in NFPA 495, "Explosive Materials Code," and prepare a blasting plan reporting the following:

1. Types of explosive and sizes of charge to be used in each area of rock removal, types of blasting mats, sequence of blasting operations, and procedures that will prevent damage to site improvements and structures on Project site and adjacent properties.

2. Seismographic monitoring during blasting operations.

Retain paragraph and subparagraphs below if rock is anticipated, blasting is permitted, and independent oversight is required.  Revise reporting requirements to suit Project.

B. Seismic Survey Agency:  An independent testing agency, acceptable to authorities having jurisdiction, experienced in seismic surveys and blasting procedures to perform the following services:

1. Report types of explosive and sizes of charge to be used in each area of rock removal, types of blasting mats, sequence of blasting operations, and procedures that will prevent damage to site improvements and structures on Project site and adjacent properties.

2. Seismographic monitoring during blasting operations.

Retain paragraph below if Contractor selects agency for rock-definition testing.

C. Geotechnical Testing Agency Qualifications:  An independent testing agency qualified according to ASTM E 329 to conduct soil materials and rock-definition testing, as documented according to ASTM D 3740 and ASTM E 548.

Delete paragraph below if Work of this Section is not extensive or complex enough to justify a preexcavation conference.  If retaining, coordinate with and insert agenda items below that are not listed in Division 01.

D. Preexcavation Conference:  Conduct conference at Project site to comply with requirements in Division 01 Section "Project Management and Coordination."

1.7 PROJECT CONDITIONS

Delete first paragraph and subparagraphs below if no existing utilities.  Coordinate with requirements specified in Division 01 Section "Temporary Facilities and Controls" for temporary utilities.

A. Existing Utilities:  Do not interrupt utilities serving facilities occupied by Owner or others unless permitted in writing by Architect and then only after arranging to provide temporary utility services according to requirements indicated.

Edit first subparagraph below to suit Project.

1. Notify Architect not less than two days in advance of proposed utility interruptions.

2. Do not proceed with utility interruptions without Architect's written permission.

3. Contact utility-locator service for area where Project is located before excavating.

B. Demolish and completely remove from site existing underground utilities indicated to be removed.  Coordinate with utility companies to shut off services if lines are active.

PART 2 -  PRODUCTS

2.1 SOIL MATERIALS

A. General:  Provide borrow soil materials when sufficient satisfactory soil materials are not available from excavations.

Revise two paragraphs and associated subparagraph below and identify soil materials according to geotechnical engineer's written recommendations.  Revise soil groups and size of stone to suit Project.  Add liquid limit and plasticity index if further qualifying satisfactory soil groups.  Most soils are classified according to ASTM D 2487.  Heavy civil or highway projects may use AASHTO M 145.

B. Satisfactory Soils:  [ASTM D 2487 Soil Classification Groups GW, GP, GM, SW, SP, and SM] [AASHTO M 145 Soil Classification Groups A-1, A-2-4, A-2-5, and A-3], or a combination of these groups; free of rock or gravel larger than [3 inches (75 mm)] <Insert dimension> in any dimension, debris, waste, frozen materials, vegetation, and other deleterious matter.

C. Unsatisfactory Soils:  Soil Classification Groups [GC, SC, CL, ML, OL, CH, MH, OH, and PT according to ASTM D 2487] [A-2-6, A-2-7, A-4, A-5, A-6, and A-7 according to AASHTO M 145], or a combination of these groups.

1. Unsatisfactory soils also include satisfactory soils not maintained within 2 percent of optimum moisture content at time of compaction.

Terms, descriptions, and gradations of granular soil materials in paragraphs below are examples only.  Revise to comply with local practices and to suit Project.  For example, granular materials may be referenced by state or local highway designations rather than by ASTM classifications.

D. Subbase Material:  Naturally or artificially graded mixture of natural or crushed gravel, crushed stone, and natural or crushed sand; ASTM D 2940; with at least 90 percent passing a 1-1/2-inch (37.5-mm) sieve and not more than 12 percent passing a No. 200 (0.075-mm) sieve.

E. Base Course:  Naturally or artificially graded mixture of natural or crushed gravel, crushed stone, and natural or crushed sand; ASTM D 2940; with at least 95 percent passing a 1-1/2-inch (37.5-mm) sieve and not more than 8 percent passing a No. 200 (0.075-mm) sieve.

F. Engineered Fill:  Naturally or artificially graded mixture of natural or crushed gravel, crushed stone, and natural or crushed sand; ASTM D 2940; with at least 90 percent passing a 1-1/2-inch (37.5-mm) sieve and not more than 12 percent passing a No. 200 (0.075-mm) sieve.

G. Bedding Course:  Naturally or artificially graded mixture of natural or crushed gravel, crushed stone, and natural or crushed sand; ASTM D 2940; except with 100 percent passing a 1-inch (25-mm) sieve and not more than 8 percent passing a No. 200 (0.075-mm) sieve.

H. Drainage Course:  Narrowly graded mixture of [washed ]crushed stone, or crushed or uncrushed gravel; ASTM D 448; coarse-aggregate grading Size 57; with 100 percent passing a 1-1/2-inch (37.5-mm) sieve and 0 to 5 percent passing a No. 8 (2.36-mm) sieve.

I. Filter Material:  Narrowly graded mixture of natural or crushed gravel, or crushed stone and natural sand; ASTM D 448; coarse-aggregate grading Size 67; with 100 percent passing a 1-inch (25-mm) sieve and 0 to 5 percent passing a No. 4 (4.75-mm) sieve.

J. Sand:  ASTM C 33; fine aggregate, natural, or manufactured sand.

K. Impervious Fill:  Clayey gravel and sand mixture capable of compacting to a dense state.

2.2 GEOTEXTILES

Retain paragraph below if nonwoven geotextile is used in subsurface drainage applications.  Performance requirements in AASHTO M 288 have been widely adopted by geotextile manufacturers and are repeated below.  The geotechnical report may also include geotextile recommendations.  See Evaluations for list of geotextile manufacturers.

A. Subsurface Drainage Geotextile:  Nonwoven needle-punched geotextile, manufactured for subsurface drainage applications, made from polyolefins or polyesters; with elongation greater than 50 percent; complying with AASHTO M 288 and the following, measured per test methods referenced:

Retain subparagraph below if AASHTO M 288 survivability classification is required.  Survivability rates a geotextile's ability to withstand installation stresses and is divided into 3 classes by AASHTO M 288.  Survivability measures grab, seam, tear, and puncture strength.  Class 2 is the default class recommended by AASHTO M 288 for subsurface drainage applications.  Revise to Class 1 if higher strength is required or Class 3 if lower strength is permitted.

1. Survivability:  Class 2; AASHTO M 288.

Retain subparagraph above or four subparagraphs below.  Strength values below correspond to AASHTO M 288 Survivability Class 2 for subsurface drainage applications.  Revise if other strength values are required.

2. Grab Tensile Strength:  157 lbf (700 N); ASTM D 4632.

3. Sewn Seam Strength:  142 lbf (630 N); ASTM D 4632.

4. Tear Strength:  56 lbf (250 N); ASTM D 4533.

5. Puncture Strength:  56 lbf (250 N); ASTM D 4833.

AASHTO M 288 bases selection of apparent opening size for subsurface drainage geotextiles on percentages of backfill soils passing a No. 200 (0.075-mm) sieve.  First option in subparagraph below corresponds to less than 15 percent; second, to 15 to 50 percent; and third, to greater than 50 percent for Class 2 geotextiles.

6. Apparent Opening Size:  [No. 40 (0.425-mm)] [No. 60 (0.250-mm)] [No. 70 (0.212-mm)] sieve, maximum; ASTM D 4751.

AASHTO M 288 bases selection of permittivity for subsurface drainage geotextiles on percentages of backfill soils passing a No. 200 (0.075-mm) sieve.  First option in subparagraph below corresponds to less than 15 percent; second, to 15 to 50 percent; and third, to greater than 50 percent for Class 2 geotextiles.

7. Permittivity:  [0.5] [0.2] [0.1] per second, minimum; ASTM D 4491.

Requirement in subparagraph below corresponds to default value in AASHTO M 288 for Class 2 subsurface drainage geotextiles.

8. UV Stability:  50 percent after 500 hours' exposure; ASTM D 4355.

Retain paragraph and subparagraphs below if a separation geotextile is required.  A typical use is to separate subgrade from granular soil materials such as subbase, base, or engineered fill.  The geotechnical report may also include geotextile recommendations.  See Evaluations for list of geotextile manufacturers.

B. Separation Geotextile:  Woven geotextile fabric, manufactured for separation applications, made from polyolefins or polyesters; with elongation less than 50 percent; complying with AASHTO M 288 and the following, measured per test methods referenced:

Survivability rates a geotextile's ability to withstand installation stresses and is divided into 3 classes by AASHTO M 288.  Survivability measures grab, seam, tear, and puncture strength.  Class 2 is the default class recommended by AASHTO M 288 for separation geotextile applications.

1. Survivability:  Class 2; AASHTO M 288.

Retain subparagraph above or four subparagraphs below.  Strength values below correspond to AASHTO M 288 Survivability Class 2 for separation geotextile applications.  Revise if other strength values are required.

2. Grab Tensile Strength:  247 lbf (1100 N); ASTM D 4632.

3. Sewn Seam Strength:  222 lbf (990 N); ASTM D 4632.

4. Tear Strength:  90 lbf (400 N); ASTM D 4533.

5. Puncture Strength:  90 lbf (400 N); ASTM D 4833.

Requirements in three subparagraphs below correspond to default values in AASHTO M 288 for Class 2 separation geotextiles.

6. Apparent Opening Size:  No. 60 (0.250-mm) sieve, maximum; ASTM D 4751.

7. Permittivity:  0.02 per second, minimum; ASTM D 4491.

8. UV Stability:  50 percent after 500 hours' exposure; ASTM D 4355.

2.3 CONTROLLED LOW-STRENGTH MATERIAL

A. Controlled Low-Strength Material:  Low-density, self-compacting, flowable concrete material as follows:

1. Portland Cement:  ASTM C 150, Type [I] [II] [or] [III].

2. Fly Ash:  ASTM C 618, Class C or F.

3. Normal-Weight Aggregate:  ASTM C 33, [3/4-inch (19-mm)] [3/8-inch (10-mm)] <Insert dimension> nominal maximum aggregate size.

Retain first subparagraph below if low-density, controlled low-strength material is required.

4. Foaming Agent:  ASTM C 869.

5. Water:  ASTM C 94/C 94M.

Delete subparagraph below for low-density, controlled low-strength material using foaming agent.

6. Air-Entraining Admixture:  ASTM C 260.

Retain one of two paragraphs and associated subparagraphs below.

B. Produce low-density, controlled low-strength material with the following physical properties:

Properties in subparagraphs below are based on a range of proportions published by various foam manufacturers.  Revise or add other physical properties for a particular application if required.

1. As-Cast Unit Weight:  [30 to 36 lb/cu. ft. (480 to 576 kg/cu. m)] [36 to 42 lb/cu. ft. (576 to 675 kg/cu. m)] <Insert unit weight range> at point of placement, when tested according to ASTM C 138/C 138M.

2. Compressive Strength:  [80 psi (550 kPa)] [140 psi (965 kPa)] <Insert strength>, when tested according to ASTM C 495.

Insert other physical properties, in addition to selecting strength in paragraph below, if required for a particular application.

C. Produce conventional-weight, controlled low-strength material with [80-psi (550-kPa)] [140-psi (965-kPa)] <Insert strength> compressive strength when tested according to ASTM C 495.

2.4 GEOFOAM

A. Extruded-Polystyrene Board Insulation:  ASTM C 578, Type [IV, 1.60 lb/cu. ft. (26 kg/cu. m)] [X, 1.30 lb/cu. ft. (21 kg/cu. m)] [VI, 1.80 lb/cu. ft. (29 kg/cu. m)].

B. Molded-Polystyrene Board Insulation:  ASTM C 578, Type [I, 0.90 lb/cu. ft. (15 kg/cu. m)] [VIII, 1.15 lb/cu. ft. (18 kg/cu. m)] [II, 1.35 lb/cu. ft. (22 kg/cu. m)].

Retain subparagraph below if requiring molded polystyrene to deter termites.

1. Manufacture molded polystyrene with an inorganic mineral registered with the EPA and suitable for application as a termite deterrent.

To limit displacement of geofoam blocks, connectors may be used.  Multibarbed galvanized steel sheet connectors in first option in paragraph below are trademarked by AFM Corporation; www.geofoam.com.  Steel reinforcing bars in second option may also be used.

C. Geofoam Connectors:  [Geofoam manufacturer's multibarbed galvanized steel sheet connectors] [Deformed steel reinforcing bars, 3/4 inch (19 mm) in diameter].

2.5 ACCESSORIES

Delete warning tapes in this Article if not required.  Use may be mandatory for underground hazardous utilities.

A. Warning Tape:  Acid- and alkali-resistant polyethylene film warning tape manufactured for marking and identifying underground utilities, 6 inches (150 mm) wide and 4 mils (0.1 mm) thick, continuously inscribed with a description of the utility; colored as follows:

Select paragraph above or below and revise description, if required, to suit Project.  Retain both and indicate on Drawings where each tape is required.

B. Detectable Warning Tape:  Acid- and alkali-resistant polyethylene film warning tape manufactured for marking and identifying underground utilities, a minimum of 6 inches (150 mm) wide and 4 mils (0.1 mm) thick, continuously inscribed with a description of the utility, with metallic core encased in a protective jacket for corrosion protection, detectable by metal detector when tape is buried up to 30 inches (750 mm) deep; colored as follows:

Revise colors below to comply with local practice or requirements of authorities having jurisdiction.

1. Red:  Electric.

2. Yellow:  Gas, oil, steam, and dangerous materials.

3. Orange:  Telephone and other communications.

4. Blue:  Water systems.

5. Green:  Sewer systems.

PART 3 -  EXECUTION

3.1 PREPARATION

A. Protect structures, utilities, sidewalks, pavements, and other facilities from damage caused by settlement, lateral movement, undermining, washout, and other hazards created by earthwork operations.

B. Preparation of subgrade for earthwork operations including removal of vegetation, topsoil, debris, obstructions, and deleterious materials from ground surface is specified in Division 31 Section "Site Clearing."

C. Protect and maintain erosion and sedimentation controls, which are specified in Division 31 Section "Site Clearing," during earthwork operations.

Delete paragraph below if not applicable.

D. Provide protective insulating materials to protect subgrades and foundation soils against freezing temperatures or frost.

3.2 DEWATERING

A. Prevent surface water and ground water from entering excavations, from ponding on prepared subgrades, and from flooding Project site and surrounding area.

B. Protect subgrades from softening, undermining, washout, and damage by rain or water accumulation.

1. Reroute surface water runoff away from excavated areas.  Do not allow water to accumulate in excavations.  Do not use excavated trenches as temporary drainage ditches.

2. Install a dewatering system[, specified in Division 31 Section "Dewatering," ] to keep subgrades dry and convey ground water away from excavations.  Maintain until dewatering is no longer required.

3.3 EXPLOSIVES

A. Explosives:  Do not use explosives.

Delete paragraph above if use of explosives will be permitted.  Delete paragraph and subparagraphs below if explosives will not be permitted.

B. Explosives:  Obtain written permission from authorities having jurisdiction before bringing explosives to Project site or using explosives on Project site.

1. Perform blasting without damaging adjacent structures, property, or site improvements.

2. Perform blasting without weakening the bearing capacity of rock subgrade and with the least-practicable disturbance to rock to remain.

3.4 EXCAVATION, GENERAL

Retain paragraph and subparagraphs below if excavation is unclassified and no changes in the Contract Sum or the Contract Time will be authorized for rock excavation.

A. Unclassified Excavation:  Excavate to subgrade elevations regardless of the character of surface and subsurface conditions encountered.  Unclassified excavated materials may include rock, soil materials, and obstructions.  No changes in the Contract Sum or the Contract Time will be authorized for rock excavation or removal of obstructions.

1. If excavated materials intended for fill and backfill include unsatisfactory soil materials and rock, replace with satisfactory soil materials.

2. Remove rock to lines and grades indicated to permit installation of permanent construction without exceeding the following dimensions:

Measurements in subparagraphs below are examples only; revise to suit Project conditions and office standards.

a. [24 inches (600 mm)] <Insert dimension> outside of concrete forms other than at footings.

b. [12 inches (300 mm)] <Insert dimension> outside of concrete forms at footings.

c. [6 inches (150 mm)] <Insert dimension> outside of minimum required dimensions of concrete cast against grade.

d. Outside dimensions of concrete walls indicated to be cast against rock without forms or exterior waterproofing treatments.

e. [6 inches (150 mm)] <Insert dimension> beneath bottom of concrete slabs on grade.

f. [6 inches (150 mm)] <Insert dimension> beneath pipe in trenches, and the greater of [24 inches (600 mm)] <Insert dimension> wider than pipe or [42 inches (1065 mm)] <Insert dimension> wide.

Delete paragraph and subparagraphs above and retain paragraph and subparagraphs below if excavation is classified and adjustments in the Contract Sum and, if applicable, the Contract Time will be authorized for rock excavation.  See Evaluations for further discussion.

B. Classified Excavation:  Excavate to subgrade elevations.  Material to be excavated will be classified as earth and rock.  Do not excavate rock until it has been classified and cross sectioned by Architect.  The Contract Sum will be adjusted for rock excavation according to unit prices included in the Contract Documents.  Changes in the Contract time may be authorized for rock excavation.

Revise description in first subparagraph below if removal of surface features and underground utility structures is specified in Division 02 Section "Structure Demolition" or Division 31 Section "Site Clearing."

1. Earth excavation includes excavating pavements and obstructions visible on surface; underground structures, utilities, and other items indicated to be removed; together with soil, boulders, and other materials not classified as rock or unauthorized excavation.

a. Intermittent drilling; blasting, if permitted; ram hammering; or ripping of material not classified as rock excavation is earth excavation.

2. Rock excavation includes removal and disposal of rock.  Remove rock to lines and subgrade elevations indicated to permit installation of permanent construction without exceeding the following dimensions:

Measurements in subparagraphs below are examples only; revise to suit Project conditions and office standards.

a. [24 inches (600 mm)] <Insert dimension> outside of concrete forms other than at footings.

b. [12 inches (300 mm)] <Insert dimension> outside of concrete forms at footings.

c. [6 inches (150 mm)] <Insert dimension> outside of minimum required dimensions of concrete cast against grade.

d. Outside dimensions of concrete walls indicated to be cast against rock without forms or exterior waterproofing treatments.

e. [6 inches (150 mm)] <Insert dimension> beneath bottom of concrete slabs on grade.

f. [6 inches (150 mm)] <Insert dimension> beneath pipe in trenches, and the greater of [24 inches (600 mm)] <Insert dimension> wider than pipe or [42 inches (1065 mm)] <Insert dimension> wide.

3.5 EXCAVATION FOR STRUCTURES

Revise tolerances in this Article to suit office practice if applicable.

A. Excavate to indicated elevations and dimensions within a tolerance of plus or minus 1 inch (25 mm).  If applicable, extend excavations a sufficient distance from structures for placing and removing concrete formwork, for installing services and other construction, and for inspections.

Revise subparagraph below if footings and foundations are placed on engineered fill.

1. Excavations for Footings and Foundations:  Do not disturb bottom of excavation.  Excavate by hand to final grade just before placing concrete reinforcement.  Trim bottoms to required lines and grades to leave solid base to receive other work.

Delete first subparagraph below if not required.

2. Pile Foundations:  Stop excavations 6 to 12 inches (150 to 300 mm) above bottom of pile cap before piles are placed.  After piles have been driven, remove loose and displaced material.  Excavate to final grade, leaving solid base to receive concrete pile caps.

3. Excavation for Underground Tanks, Basins, and Mechanical or Electrical Utility Structures:  Excavate to elevations and dimensions indicated within a tolerance of plus or minus 1 inch (25 mm).  Do not disturb bottom of excavations intended as bearing surfaces.

3.6 EXCAVATION FOR WALKS AND PAVEMENTS

A. Excavate surfaces under walks and pavements to indicated lines, cross sections, elevations, and subgrades.

3.7 EXCAVATION FOR UTILITY TRENCHES

Revise this Article to suit Project.  Coordinate with utility Sections in other Divisions.

A. Excavate trenches to indicated gradients, lines, depths, and elevations.

1. Beyond building perimeter, excavate trenches to allow installation of top of pipe below frost line.

B. Excavate trenches to uniform widths to provide the following clearance on each side of pipe or conduit.  Excavate trench walls vertically from trench bottom to 12 inches (300 mm) higher than top of pipe or conduit, unless otherwise indicated.

Retain, revise, or delete subparagraph below to suit Project.

1. Clearance:  [12 inches (300 mm) each side of pipe or conduit] [As indicated].

Select one of two "Trench Bottoms" paragraphs and associated subparagraphs below.  Revise to suit Project, requirements of authorities having jurisdiction, type of pipe or conduit, and manufacturer's installation requirements.

C. Trench Bottoms:  Excavate and shape trench bottoms to provide uniform bearing and support of pipes and conduit.  Shape subgrade to provide continuous support for bells, joints, and barrels of pipes and for joints, fittings, and bodies of conduits.  Remove projecting stones and sharp objects along trench subgrade.

1. For pipes and conduit less than 6 inches (150 mm) in nominal diameter and flat-bottomed, multiple-duct conduit units, hand-excavate trench bottoms and support pipe and conduit on an undisturbed subgrade.

2. For pipes and conduit 6 inches (150 mm) or larger in nominal diameter, shape bottom of trench to support bottom 90 degrees of pipe circumference.  Fill depressions with tamped sand backfill.

3. Excavate trenches 6 inches (150 mm) deeper than elevation required in rock or other unyielding bearing material to allow for bedding course.

Delete paragraph and subparagraphs above and retain paragraph and subparagraph below if a bedding course is required under pipe.

D. Trench Bottoms:  Excavate trenches 4 inches (100 mm) deeper than bottom of pipe elevation to allow for bedding course.  Hand excavate for bell of pipe.

1. Excavate trenches 6 inches (150 mm) deeper than elevation required in rock or other unyielding bearing material to allow for bedding course.

3.8 SUBGRADE INSPECTION

A. Notify Architect when excavations have reached required subgrade.

B. If Architect determines that unsatisfactory soil is present, continue excavation and replace with compacted backfill or fill material as directed.

Revise locations for proof-rolling in paragraph below if required.

C. Proof-roll subgrade [below the building slabs and pavements] <Insert locations> with heavy pneumatic-tired equipment to identify soft pockets and areas of excess yielding.  Do not proof-roll wet or saturated subgrades.

1. Completely proof-roll subgrade in one direction[, repeating proof-rolling in direction perpendicular to first direction].  Limit vehicle speed to 3 mph (5 km/h).

Revise minimum weight or type of vehicle in first subparagraph below if required.

2. Proof-roll with a loaded 10-wheel, tandem-axle dump truck weighing not less than 15 tons (13.6 tonnes).

3. Excavate soft spots, unsatisfactory soils, and areas of excessive pumping or rutting, as determined by Architect, and replace with compacted backfill or fill as directed.

D. Authorized additional excavation and replacement material will be paid for according to Contract provisions for [unit prices] [changes in the Work].

E. Reconstruct subgrades damaged by freezing temperatures, frost, rain, accumulated water, or construction activities, as directed by Architect, without additional compensation.

3.9 UNAUTHORIZED EXCAVATION

Revise this Article to suit Project.

A. Fill unauthorized excavation under foundations or wall footings by extending bottom elevation of concrete foundation or footing to excavation bottom, without altering top elevation.  Lean concrete fill, with 28-day compressive strength of 2500 psi (17.2 MPa), may be used when approved by Architect.

1. Fill unauthorized excavations under other construction or utility pipe as directed by Architect.

3.10 STORAGE OF SOIL MATERIALS

A. Stockpile borrow soil materials and excavated satisfactory soil materials without intermixing.  Place, grade, and shape stockpiles to drain surface water.  Cover to prevent windblown dust.

1. Stockpile soil materials away from edge of excavations.  Do not store within drip line of remaining trees.

3.11 BACKFILL

A. Place and compact backfill in excavations promptly, but not before completing the following:

Delete or revise subparagraphs below to suit Project.

1. Construction below finish grade including, where applicable, subdrainage, dampproofing, waterproofing, and perimeter insulation.

2. Surveying locations of underground utilities for Record Documents.

3. Testing and inspecting underground utilities.

4. Removing concrete formwork.

5. Removing trash and debris.

6. Removing temporary shoring and bracing, and sheeting.

7. Installing permanent or temporary horizontal bracing on horizontally supported walls.

B. Place backfill on subgrades free of mud, frost, snow, or ice.

3.12 UTILITY TRENCH BACKFILL

A. Place backfill on subgrades free of mud, frost, snow, or ice.

B. Place and compact bedding course on trench bottoms and where indicated.  Shape bedding course to provide continuous support for bells, joints, and barrels of pipes and for joints, fittings, and bodies of conduits.

Revise dimensions or extent of concrete backfill in first paragraph below to suit Project.

C. Backfill trenches excavated under footings and within 18 inches (450 mm) of bottom of footings with satisfactory soil; fill with concrete to elevation of bottom of footings.  Concrete is specified in Division 03 Section "[Cast-in-Place Concrete] [Miscellaneous Cast-in-Place Concrete]."

D. Provide 4-inch- (100-mm-) thick, concrete-base slab support for piping or conduit less than 30 inches (750 mm) below surface of roadways.  After installing and testing, completely encase piping or conduit in a minimum of 4 inches (100 mm) of concrete before backfilling or placing roadway subbase.

Delete paragraph and subparagraph below if specifying controlled low-strength material as initial backfill.  If retaining, revise maximum particle size to suit type of pipe or conduit.

E. Place and compact initial backfill of [subbase material] [satisfactory soil], free of particles larger than 1 inch (25 mm) in any dimension, to a height of 12 inches (300 mm) over the utility pipe or conduit.

1. Carefully compact initial backfill under pipe haunches and compact evenly up on both sides and along the full length of utility piping or conduit to avoid damage or displacement of piping or conduit.  Coordinate backfilling with utilities testing.

Retain first paragraph below if controlled low-strength material is permitted or required as initial backfill instead of a soil material in paragraph above.

F. Controlled Low-Strength Material:  Place initial backfill of controlled low-strength material to a height of 12 inches (300 mm) over the utility pipe or conduit.

G. Backfill voids with satisfactory soil while installing and removing shoring and bracing.

H. Place and compact final backfill of satisfactory soil to final subgrade elevation.

Retain paragraph below if controlled low-strength material is permitted or required as final backfill instead of satisfactory soil in paragraph above.

I. Controlled Low-Strength Material:  Place final backfill of controlled low-strength material to final subgrade elevation.

Revise tape depths in paragraph below to suit office practice if applicable.

J. Install warning tape directly above utilities, 12 inches (300 mm) below finished grade, except 6 inches (150 mm) below subgrade under pavements and slabs.

3.13 SOIL FILL

A. Plow, scarify, bench, or break up sloped surfaces steeper than 1 vertical to 4 horizontal so fill material will bond with existing material.

B. Place and compact fill material in layers to required elevations as follows:

Delete subparagraphs below not required.  Revise soil materials to suit Project.  Other soil materials, such as a drainage course or subbase or base courses, may still be required over fill.

1. Under grass and planted areas, use satisfactory soil material.

2. Under walks and pavements, use satisfactory soil material.

3. Under steps and ramps, use engineered fill.

4. Under building slabs, use engineered fill.

Retain subparagraph below if backfill or fill beneath footings and foundations is required.  Coordinate material selection with geotechnical engineer's written recommendations.

5. Under footings and foundations, use engineered fill.

C. Place soil fill on subgrades free of mud, frost, snow, or ice.

3.14 GEOFOAM FILL

Retain this Article if geofoam is required.

A. Place a leveling course of sand, [2 inches (50 mm)] <Insert dimension> thick, over subgrade.  Finish leveling course to a tolerance of 1/2 inch (13 mm) when tested with a 10-foot (3-m) straightedge.

1. Place leveling course on subgrades free of mud, frost, snow, or ice.

B. Install geofoam blocks in layers with abutting edges and ends and with the long dimension of each block at right angles to blocks in each subsequent layer.  Offset joints of blocks in successive layers.

C. Install geofoam connectors at each layer of geofoam to resist horizontal displacement according to geofoam manufacturer's written instructions.

Retain paragraph below if a geotextile cover is required for soil separation or to distribute uplift buoyancy.

D. Cover geofoam with [subdrainage] [separation] geotextile before placing overlying soil materials.

3.15 SOIL MOISTURE CONTROL

Revise percentage in paragraph and second subparagraph below according to geotechnical engineer's written recommendations.

A. Uniformly moisten or aerate subgrade and each subsequent fill or backfill soil layer before compaction to within 2 percent of optimum moisture content.

1. Do not place backfill or fill soil material on surfaces that are muddy, frozen, or contain frost or ice.

2. Remove and replace, or scarify and air dry otherwise satisfactory soil material that exceeds optimum moisture content by 2 percent and is too wet to compact to specified dry unit weight.

3.16 COMPACTION OF SOIL BACKFILLS AND FILLS

Revise depth of layers in first paragraph below to suit Project.

A. Place backfill and fill soil materials in layers not more than [8 inches (200 mm)] <Insert dimension>in loose depth for material compacted by heavy compaction equipment, and not more than 4 inches (100 mm) in loose depth for material compacted by hand-operated tampers.

B. Place backfill and fill soil materials evenly on all sides of structures to required elevations, and uniformly along the full length of each structure.

Select option in paragraph below based on ASTM test method required.  Replace the term "unit weight" with "density" if preferred.

C. Compact soil materials to not less than the following percentages of maximum dry unit weight according to [ASTM D 698] [ASTM D 1557]:

Retain applicable subparagraphs below.  Percentages of maximum dry unit weight are examples only; revise to suit Project.  Delete scarifying and recompacting existing subgrade when proof-rolling will suffice.

1. Under structures, building slabs, steps, and pavements, scarify and recompact top 12 inches (300 mm) of existing subgrade and each layer of backfill or fill soil material at [95] <Insert percentage> percent.

2. Under walkways, scarify and recompact top 6 inches (150 mm) below subgrade and compact each layer of backfill or fill soil material at [92] <Insert percentage> percent.

3. Under lawn or unpaved areas, scarify and recompact top 6 inches (150 mm) below subgrade and compact each layer of backfill or fill soil material at [85] <Insert percentage> percent.

4. For utility trenches, compact each layer of initial and final backfill soil material at [85] <Insert percentage> percent.

3.17 GRADING

A. General:  Uniformly grade areas to a smooth surface, free of irregular surface changes.  Comply with compaction requirements and grade to cross sections, lines, and elevations indicated.

1. Provide a smooth transition between adjacent existing grades and new grades.

2. Cut out soft spots, fill low spots, and trim high spots to comply with required surface tolerances.

B. Site Grading:  Slope grades to direct water away from buildings and to prevent ponding.  Finish subgrades to required elevations within the following tolerances:

Revise subparagraphs below to suit Project.

1. Lawn or Unpaved Areas:  Plus or minus [1 inch (25 mm)] <Insert tolerance>.

2. Walks:  Plus or minus [1 inch (25 mm)] <Insert tolerance>.

3. Pavements:  Plus or minus [1/2 inch (13 mm)] <Insert tolerance>.

C. Grading inside Building Lines:  Finish subgrade to a tolerance of 1/2 inch (13 mm) when tested with a 10-foot (3-m) straightedge.

3.18 SUBSURFACE DRAINAGE

Retain paragraphs below describing subdrainage conditions as required.  Revise particulars to coordinate with Drawings.

A. Subdrainage Pipe:  Specified in Division 33 Section "Subdrainage."

B. Subsurface Drain:  Place subsurface drainage geotextile around perimeter of subdrainage trench.  Place a 6-inch (150-mm) course of filter material on subsurface drainage geotextile to support subdrainage pipe.  Encase subdrainage pipe in a minimum of 12 inches (300 mm) of filter material, placed in compacted layers 6 inches (150 mm) thick, and wrap in subsurface drainage geotextile, overlapping sides and ends at least 6 inches (150 mm).

Retain one of two options in subparagraph below if compaction of filter material is required.  In first option, revise percentage if required.

1. Compact each filter material layer [to 85 percent of maximum dry unit weight according to ASTM D 698] [with a minimum of two passes of a plate-type vibratory compactor].

Retain "Subsurface Drain" Paragraph above if retaining "Drainage Backfill" Paragraph below.  Delete paragraph and subparagraphs below if not using free-draining granular backfill against walls.

C. Drainage Backfill:  Place and compact filter material over subsurface drain, in width indicated, to within 12 inches (300 mm) of final subgrade, in compacted layers 6 inches (150 mm) thick.  Overlay drainage backfill with 1 layer of subsurface drainage geotextile, overlapping sides and ends at least 6 inches (150 mm).

Retain one of two options in subparagraph below if compaction of filter material is required.  In first option, revise percentage if required.

1. Compact each filter material layer [to 85 percent of maximum dry unit weight according to ASTM D 698] [with a minimum of two passes of a plate-type vibratory compactor].

Revise subparagraph below according to geotechnical engineer's written recommendations or delete if no special impervious fill cap is required.

2. Place and compact impervious fill over drainage backfill in 6-inch- (150-mm-) thick compacted layers to final subgrade.

3.19 SUBBASE AND BASE COURSES

A. Place subbase[ and base] course on subgrades free of mud, frost, snow, or ice.

B. On prepared subgrade, place subbase[ and base] course under pavements and walks as follows:

Delete two subparagraphs below if not applicable.

1. Install separation geotextile on prepared subgrade according to manufacturer's written instructions, overlapping sides and ends.

2. Place base course material over subbase course under hot-mix asphalt pavement.

Retain option in four subparagraphs below if "and base" option is retained in paragraphs above.

3. Shape subbase[ and base] course to required crown elevations and cross-slope grades.

4. Place subbase[ and base] course 6 inches (150 mm) or less in compacted thickness in a single layer.

5. Place subbase[ and base] course that exceeds 6 inches (150 mm) in compacted thickness in layers of equal thickness, with no compacted layer more than 6 inches (150 mm) thick or less than 3 inches (75 mm) thick.

6. Compact subbase[ and base] course at optimum moisture content to required grades, lines, cross sections, and thickness to not less than [95] <Insert percentage> percent of maximum dry unit weight according to [ASTM D 698] [ASTM D 1557].

Revise paragraph below to suit Project or delete if not applicable.

C. Pavement Shoulders:  Place shoulders along edges of subbase and base course to prevent lateral movement.  Construct shoulders, at least 12 inches (300 mm) wide, of satisfactory soil materials and compact simultaneously with each subbase and base layer to not less than [95] <Insert percentage> percent of maximum dry unit weight according to [ASTM D 698] [ASTM D 1557].

3.20 DRAINAGE COURSE

A. Place drainage course on subgrades free of mud, frost, snow, or ice.

B. On prepared subgrade, place and compact drainage course under cast-in-place concrete slabs-on-grade as follows:

Retain applicable subparagraphs below.

1. Install subdrainage geotextile on prepared subgrade according to manufacturer's written instructions, overlapping sides and ends.

2. Place drainage course 6 inches (150 mm) or less in compacted thickness in a single layer.

3. Place drainage course that exceeds 6 inches (150 mm) in compacted thickness in layers of equal thickness, with no compacted layer more than 6 inches (150 mm) thick or less than 3 inches (75 mm) thick.

Revise percentage of compaction in subparagraph below and change compaction test from ASTM D 698 to ASTM D 4254 or ASTM D 1557 if required.  Replace the term "unit weight" with "density" if preferred.

4. Compact each layer of drainage course to required cross sections and thicknesses to not less than [95] <Insert percentage> percent of maximum dry unit weight according to ASTM D 698.

3.21 FIELD QUALITY CONTROL

A. Testing Agency:  Owner will engage a qualified independent geotechnical engineering testing agency to perform field quality-control testing.

Revise testing in paragraph below to suit Project or delete if not applicable.

B. Allow testing agency to inspect and test subgrades and each fill or backfill layer.  Proceed with subsequent earthwork only after test results for previously completed work comply with requirements.

Revise paragraph below to suit Project or delete if not applicable.  If retaining, add other field tests, such as California bearing ratio of subgrades, subbases, and bases for paving, if required.

C. Footing Subgrade:  At footing subgrades, at least one test of each soil stratum will be performed to verify design bearing capacities.  Subsequent verification and approval of other footing subgrades may be based on a visual comparison of subgrade with tested subgrade when approved by Architect.

Revise first paragraph below to suit Project.

D. Testing agency will test compaction of soils in place according to ASTM D 1556, ASTM D 2167, ASTM D 2922, and ASTM D 2937, as applicable.  Tests will be performed at the following locations and frequencies:

Frequencies of testing in subparagraphs below are examples only; revise to suit Project.

1. Paved and Building Slab Areas:  At subgrade and at each compacted fill and backfill layer, at least 1 test for every [2000 sq. ft. (186 sq. m)] <Insert area> or less of paved area or building slab, but in no case fewer than 3 tests.

2. Foundation Wall Backfill:  At each compacted backfill layer, at least 1 test for each [100 feet (30 m)] <Insert dimension> or less of wall length, but no fewer than 2 tests.

3. Trench Backfill:  At each compacted initial and final backfill layer, at least 1 test for each [150 feet (46 m)] <Insert dimension> or less of trench length, but no fewer than 2 tests.

E. When testing agency reports that subgrades, fills, or backfills have not achieved degree of compaction specified, scarify and moisten or aerate, or remove and replace soil to depth required; recompact and retest until specified compaction is obtained.

3.22 PROTECTION

A. Protecting Graded Areas:  Protect newly graded areas from traffic, freezing, and erosion.  Keep free of trash and debris.

B. Repair and reestablish grades to specified tolerances where completed or partially completed surfaces become eroded, rutted, settled, or where they lose compaction due to subsequent construction operations or weather conditions.

1. Scarify or remove and replace soil material to depth as directed by Architect; reshape and recompact.

C. Where settling occurs before Project correction period elapses, remove finished surfacing, backfill with additional soil material, compact, and reconstruct surfacing.

1. Restore appearance, quality, and condition of finished surfacing to match adjacent work, and eliminate evidence of restoration to greatest extent possible.

3.23 DISPOSAL OF SURPLUS AND WASTE MATERIALS

A. Disposal:  Remove surplus satisfactory soil and waste material, including unsatisfactory soil, trash, and debris, and legally dispose of it off Owner's property.

Retain paragraph above or paragraph and subparagraph below.

B. Disposal:  Transport surplus satisfactory soil to designated storage areas on Owner's property.  Stockpile or spread soil as directed by Architect.

1. Remove waste material, including unsatisfactory soil, trash, and debris, and legally dispose of it off Owner's property.

END OF SECTION 312000

	EARTH MOVING
	312000 - 1



