Copyright 2004 and 2005 AIA
MASTERSPEC Full Length
02/04 (R 05/06)

Copyright 2004 and 2005 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 099300 - STAINING AND TRANSPARENT FINISHING
This Section uses the term "Architect."  Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 RELATED DOCUMENTS

A. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

1.2 SUMMARY

If this Section specifies only stains or transparent finishes, revise Section Title to accurately reflect its content.

A. This Section includes surface preparation and the application of wood finishes on the following substrates:

Adjust lists below to suit Project.

1. Exterior Substrates:

a. Exposed glue-laminated beams and columns.

b. Exposed dimension lumber (rough carpentry).

c. Dressed lumber (finish carpentry).

d. Exposed wood panel products.

e. Wood decks and stairs.

f. Wood shingles and shakes (excluding roofs).

2. Interior Substrates:

a. Exposed glue-laminated beams and columns.

b. Exposed dimension lumber (rough carpentry).

c. Dressed lumber (finish carpentry).

d. Exposed wood panel products.

B. Related Sections include the following:

List below only products that the reader might expect to find in this Section but are specified elsewhere.

1. Division 09 wood flooring Sections for stains and transparent finishes applied to wood flooring.

2. Division 09 Section "Exterior Painting" for surface preparation and application of standard paint systems on exterior substrates.

3. Division 09 Section "Interior Painting" for surface preparation and application of standard paint systems on interior substrates.

4. Division 09 painting Sections for special-use coatings.

1.3 SUBMITTALS

A. Product Data:  For each type of product indicated.

B. LEED Submittal:

Retain subparagraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.2; coordinate with requirements selected in Part 2 for interior stains and transparent finishes.

1. Product Data for Credit EQ 4.2:  For interior primers, stains, and transparent finishes, including printed statement of VOC content.

C. Samples for Initial Selection:  For each type of product indicated.

Delete paragraph above if colors and other characteristics are preselected and specified or scheduled.  Retain first paragraph and subparagraphs below with or without above.

D. Samples for Verification:  For each type of finish system and in each color and gloss of finish indicated.

1. Submit Samples on representative samples of actual wood substrates, 8 inches (200 mm) square.

2. Label each Sample for location and application area.

E. Product List:  For each product indicated, include the following:

1. Cross-reference to finish system and locations of application areas.  Use same designations indicated on Drawings and in schedules.

See "Writing Guide" Article in the Evaluations for discussion of subparagraph below.

2. Printout of MPI's current "MPI Approved Products List" for each product category specified in Part 2, with the product proposed for use highlighted.

1.4 QUALITY ASSURANCE

A. MPI Standards:

1. Products:  Complying with MPI standards indicated and listed in its "MPI Approved Products List."

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise subparagraph below and finish systems specified in Part 3.

2. Preparation and Workmanship:  Comply with requirements in "MPI Architectural Painting Specification Manual" for products and finish systems indicated.

Delete paragraph and subparagraphs below if not required.

B. Mockups:  Apply benchmark samples of each finish system indicated and each color selected to verify preliminary selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

1. Architect will select one surface to represent surfaces and conditions for application of each type of finish system and substrate.

a. Vertical and Horizontal Surfaces:  Provide samples of at least 100 sq. ft. (9 sq. m).

b. Other Items:  Architect will designate items or areas required.

Delete subparagraph and associated subparagraph below if no stains.

2. Final approval of stain color selections will be based on benchmark samples.

a. If preliminary stain color selections are not approved, apply additional benchmark samples of additional stain colors selected by Architect at no added cost to Owner.

1.5 DELIVERY, STORAGE, AND HANDLING

A. Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

1. Maintain containers in clean condition, free of foreign materials and residue.

2. Remove rags and waste from storage areas daily.

If necessary, add special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site.

1.6 PROJECT CONDITIONS

A. Apply finishes only when temperature of surfaces to be finished and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

Delete paragraph below if no exterior finishes.

B. Do not apply exterior finishes in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

1.7 EXTRA MATERIALS

Extra materials may not be allowed for publicly funded projects.

A. Furnish extra materials described below that are from same production run (batch mix) as materials applied and that are packaged for storage and identified with labels describing contents.

Retain subparagraph below for projects that require only limited quantities of extra materials.  If necessary, replace percentage with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

1. Quantity:  Furnish an additional [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert number> of each material and color applied.

To efficiently edit the Part 2, first edit the Exterior Wood-Finish-System Schedule and the Interior Wood-Finish-System Schedule in Part 3; then retain, delete, and insert appropriate products in Part 2 to correspond with finish systems in the schedules.

PART 2 -  PRODUCTS

"Manufacturers" Article lists manufacturers with MPI-approved products for MPI paint and coating categories included in the Section Text.  The list was current when this Section was updated; see MPI's current "MPI Approved Products List" at www.paintinfo.com for updated lists of manufacturers.

If preferred, delete Article below and insert products names under each paint category specified in subsequent articles.  See lists of products currently approved by MPI in its "MPI Approved Products List," easily reached via the electronic version of the Supporting Documents (accessed via MASTERWORKS pull-down menu).  See "Writing Guide" Article in the Evaluations for further discussion.

2.1 MANUFACTURERS

See Editing Instruction No. 1 in the Evaluations for cautions about naming manufacturers and products.  Retain one of two paragraphs and list of manufacturers below.  See Division 01 Section "Product Requirements."

A. Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

B. Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

1. Benjamin Moore & Co.

2. Benjamin Moore & Co., Limited (Canada).

3. Bennette Paint Mfg. Co., Inc.

4. BLP Mobile Paint Manufacturing.

5. Cabot Incorporated, Samuel.

6. California Paints.

7. Cloverdale Paint.

8. Color Wheel Paints & Coatings.

9. Columbia Paint & Coatings.

10. Coronado Paint.

11. Diamond Vogel Paints.

12. Dunn-Edwards Corporation.

13. Durant Paints Inc.

14. Duron, Inc.

For this Section, Endura offers only moisture-cured clear polyurethane (gloss); delete Endura if not required.

15. Endura.

16. Farrell-Calhoun.

17. Flex Bon Paints.

18. Frazee Paint.

19. General Paint.

20. Griggs Paint.

21. Hallman Lindsay Quality Paints.

22. Hirshfield's, Inc.

23. ICI Devoe (Canada).

24. ICI Paints.

25. ICI Paints (Canada).

26. Insl-x.

27. Iowa Paint Manufacturing Company, Inc.

28. Kelly-Moore Paints.

For this Section, Kryton Canada Corporation offers only moisture-cured clear polyurethane (gloss); delete Kryton if not required.

29. Kryton Canada Corporation.

30. Kwal-Howells Paint.

31. M.A.B. Paints.

32. McCormick Paints.

33. Miller Paint.

34. Mills Paint.

35. Northern Paint.

36. PARA Paints.

37. Parker Paint Mfg. Co. Inc.

38. Porter Paints.

39. PPG Architectural Finishes, Inc.

40. Rodda Paint Co.

41. Sherwin-Williams Company (The)

42. Sico, Inc.

43. Sigma Coatings.

44. Spectra-Tone.

45. Tamms Industries, Inc.

46. Tower Paint.

47. Vista Paint.

48. <Insert manufacturer's name.>

2.2 MATERIALS, GENERAL

A. Material Compatibility:

Systems could fail if materials used for individual coats are incompatible.  MPI's finish systems take product compatibility into consideration.

1. Provide materials for use within each finish system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

2. For each coat in a finish system, provide products recommended in writing by manufacturers of topcoat for use in finish system and on substrate indicated.

Retain first paragraph below if low-emitting materials are required for LEED-NC or LEED-CI Credit EQ 4.2; coordinate with products selected.  If retaining, consider deleting "VOC Content" subparagraph from each product type paragraph retained in subsequent articles to avoid the appearance of conflicting requirements.  For names of products that comply, see products listed as complying with LEED requirements for VOCs on "MPI Approved Products List" (available at www.paintinfo.com).

B. VOC Content of Field-Applied Interior Primers, Stains, and Transparent Finishes:  Provide products that comply with the following limits for VOC content, exclusive of colorants added to a tint base, when calculated according to 40 CFR 59, Subpart D (EPA Method 24); these requirements do not apply to primers, stains, and transparent finishes that are applied in a fabrication or finishing shop:

First two subparagraphs below apply to LEED-NC.

1. Flat Primers:  VOC content of not more than 50 g/L.

2. Nonflat Primers:  VOC content of not more than 150 g/L.

First subparagraph below applies to LEED-CI.

3. Primers, Sealers, and Undercoaters:  VOC content of not more than 200 g/L.

Remaining subparagraphs apply to both LEED-NC and LEED-CI.

4. Clear Wood Finishes, Varnishes:  VOC not more than 350 g/L.

5. Clear Wood Finishes, Lacquers:  VOC not more than 550 g/L.

6. Floor Coatings:  VOC not more than 100 g/L.

7. Shellacs, Clear:  VOC not more than 730 g/L.

8. Stains:  VOC not more than 250 g/L.

Delete paragraph below if no stains.

C. Stain Colors:  [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

Products in subsequent articles are specified by reference to MPI categories.  Retaining requirements for VOC content or Environmental Performance Rating (EPR) further limits product selection; coordinate selections with products of manufacturers retained in "Manufacturers" Article.

2.3 WOOD FILLERS

A. Wood Filler Paste:  MPI #91.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2] [E3].

2.4 PRIMERS AND SEALERS

A. Exterior Alkyd Wood Primer:  MPI #5.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E2] [E3].

B. Exterior Latex Wood Primer:  MPI #6.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2] [E3].

C. Exterior Oil Wood Primer:  MPI #7.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of E2.

D. Wood Preservative:  MPI #37.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E3].

E. Alkyd Sanding Sealer:  MPI #102.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2] [E3].

F. Lacquer Sanding Sealer:  MPI #84.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2] [E3].

G. Shellac:  MPI #88.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E2] [E3].

2.5 STAINS

A. Exterior Semitransparent Stain (Solvent Based):  MPI #13.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2].

B. Exterior Solid-Color Stain (Solvent Based):  MPI #14.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2] [E3].

C. Exterior, Solid-Color Latex Stain:  MPI #16.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2] [E3].

D. Stain for Wood Decks:  MPI #33.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E3].

E. Interior Wood Stain (Semitransparent):  MPI #90.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.  Coordinate with topcoat products.

1. VOC Content:  E Range of [E1] [E2].

2.6 VARNISHES

A. Exterior Marine Spar Varnish (Gloss):  MPI #28, Gloss Level 7.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2].

B. Exterior Varnish (Gloss):  MPI #29, Gloss Level 6.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of E1.

C. Exterior Varnish (Semigloss):  MPI #30, Gloss Level 5.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of E1.

D. Interior Varnish (Flat):  MPI #73, Gloss Level 1, alkyd type.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

E. Interior Varnish (Semigloss):  MPI #74, Gloss Level 5, alkyd type.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

F. Interior Varnish (Gloss):  MPI #75, Gloss Level 6, alkyd type.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

2.7 POLYURETHANE FINISHES

A. Two-Component Aliphatic Polyurethane (Clear):  MPI #78.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

B. Interior, Oil-Modified, Clear Urethane (Satin):  MPI #57, Gloss Level 4.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2].

C. Interior, Oil-Modified, Clear Urethane (Gloss):  MPI #56, Gloss Level 6.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

D. Moisture-Cured Clear Polyurethane (Flat):  MPI #71, Gloss Level 1.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of E2.

E. Moisture-Cured Clear Polyurethane (Gloss):  MPI #31.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

2.8 WATERBORNE ACRYLIC FINISHES

A. Waterborne Clear Acrylic (Satin):  MPI #128, Gloss Level 4.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

2. Environmental Performance Rating:  [EPR 1] [EPR 2] [EPR 3].

B. Waterborne Clear Acrylic (Semigloss):  MPI #129, Gloss Level 5.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

2. Environmental Performance Rating:  [EPR 1] [EPR 2] [EPR 3].

C. Waterborne Clear Acrylic (Gloss):  MPI #130, Gloss Level 6.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

2. Environmental Performance Rating:  [EPR 1] [EPR 2] [EPR 3].

2.9 LACQUERS

A. Lacquer (Clear Flat):  MPI #87, Gloss Level 1.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

B. Lacquer (Clear Satin):  MPI #85, Gloss Level 4.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

C. Lacquer (Clear Gloss):  MPI #86, Gloss Level 6.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of [E1] [E2] [E3].

2.10 OIL FINISH

A. Danish Oil:  MPI #92.

If deleting "Manufacturers" Article, insert manufacturers' names and product designations here.

1. VOC Content:  E Range of E3.

PART 3 -  EXECUTION

3.1 EXAMINATION

A. Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of work.

Percentage in first subparagraph below is based on "MPI Architectural Painting Specification Manual."

1. Maximum Moisture Content of Wood Substrates:  15 percent when measured with an electronic moisture meter.

2. Verify compatibility with and suitability of substrates, including compatibility with existing finishes.

3. Begin finish application only after unsatisfactory conditions have been corrected and surfaces are dry.

4. Beginning application of finish system constitutes Contractor's acceptance of substrate and conditions.

3.2 PREPARATION

For renovation projects, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and finish systems specified in the Exterior Wood-Finish-System Schedule and the Interior Wood-Finish-System Schedule at the end of Part 3.

A. Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates indicated.

B. Remove plates, machined surfaces, and similar items already in place that are not to be finished.  If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and finishing.

1. After completing finishing operations, reinstall items that were removed; use workers skilled in the trades involved.  Remove surface-applied protection if any.

C. Clean and prepare surfaces to be finished according to manufacturer's written instructions for each particular substrate condition and as specified.

1. Remove surface dirt, oil, or grease by washing with a detergent solution; rinse thoroughly with clean water and allow to dry.  Remove grade stamps and pencil marks by sanding lightly.  Remove loose wood fibers by brushing.

2. Remove mildew by scrubbing with a commercial wash formulated for mildew removal and as recommended by stain manufacturer.

Avoid using steel nails under a stain because of rust.  Delete or revise subparagraph below if noncorrosive nails are specified in other Sections.

3. Countersink steel nails, if used, and fill with putty tinted to final color to eliminate rust leach stains.

Delete paragraph below if not required.

D. Apply wood filler paste to open-grain woods, as defined in "MPI Architectural Painting Specification Manual," to produce smooth, glasslike finish.

3.3 APPLICATION

A. Apply finishes according to manufacturer's written instructions.

1. Use applicators and techniques suited for finish and substrate indicated.

2. Finish surfaces behind movable equipment and furniture same as similar exposed surfaces.

B. Apply finishes to produce surface films without cloudiness, holidays, lap marks, brush marks, runs, ropiness, or other surface imperfections.

3.4 FIELD QUALITY CONTROL

Retain this Article for large projects or critical finishes where additional control is desired.  Delete if tests are not required.

A. Owner reserves the right to invoke the following procedure at any time and as often as Owner deems necessary during the period when finishes are being applied:

1. Owner will engage the services of a qualified testing agency to sample finish materials being used.  Samples of material delivered to Project site will be taken, identified, sealed, and certified in presence of Contractor.

2. Testing agency will perform tests for compliance with product requirements.

3. Owner may direct Contractor to stop applying finishes if test results show materials being used do not comply with product requirements.  Contractor shall remove noncomplying materials from Project site, pay for testing, and refinish surfaces finished with rejected materials.  Contractor will be required to remove rejected materials from previously finished surfaces if, on refinishing with complying materials, the two finishes are incompatible.

3.5 CLEANING AND PROTECTION

A. At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

B. After completing finish application, clean spattered surfaces.  Remove spattered materials by washing, scraping, or other methods.  Do not scratch or damage adjacent finished surfaces.

C. Protect work of other trades against damage from finish application.  Correct damage by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

D. At completion of construction activities of other trades, touch up and restore damaged or defaced finished wood surfaces.

To efficiently edit the Section Text, first edit the Exterior Wood-Finish-System Schedule and the Interior Wood-Finish-System Schedule below; then retain, delete, and insert appropriate products in Part 2 to correspond with finish systems specified in the schedules.

3.6 EXTERIOR WOOD-FINISH-SYSTEM SCHEDULE

Finish systems in this Article are based on "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").  For renovation projects, consult "MPI Maintenance Repainting Manual" and revise finish systems accordingly.

Coordinate substrates and finish systems retained in this Article with products retained in Part 2.

A. Exposed Glue-Laminated Beam and Column Substrates:

1. Solid-Color, Solvent-Based Stain System:  MPI EXT 6.1C.

"MPI Manual" requires two stain coats for a Premium Grade system; it does not include a Custom Grade system.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

b. Two Stain Coats:  Exterior solid-color stain (solvent based).

2. Varnish Over Semitransparent Stain System:  MPI EXT 6.1D.

a. Stain Coat:  Exterior semitransparent stain (solvent based).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Exterior [marine spar varnish (gloss)] [varnish (gloss)] [varnish (semigloss)].

3. Varnish System:  MPI EXT 6.1K.

"MPI Manual" requires four finish coats for a Premium Grade system and three finish coats for a Custom Grade system.

a. [Four] [Three] Finish Coats:  Exterior [marine spar varnish (gloss)] [varnish (gloss)] [varnish (semigloss)].

4. Clear, Two-Component Polyurethane Over Stain System:  MPI EXT 6.1E.

a. Stain Coat:  Exterior semitransparent stain (solvent based).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Two-component aliphatic polyurethane (clear).

5. Clear, Two-Component Polyurethane System:  MPI EXT 6.1H.

"MPI Manual" requires three finish coats for a Premium Grade system; it does not include a Custom Grade system.

a. Three Finish Coats:  Two-component aliphatic polyurethane (clear).

B. Exposed Rough Carpentry Substrates:

1. Solid-Color Latex Stain System:  MPI EXT 6.2B.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior, solid-color latex stain.

2. Solid-Color, Solvent-Based Stain System:  MPI EXT 6.2D.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior solid-color stain (solvent based).

3. Semitransparent Stain System:  MPI EXT 6.2L.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Exterior semitransparent stain (solvent based).

4. Varnish Over Semitransparent Stain System:  MPI EXT 6.2E.

a. Stain Coat:  Exterior semitransparent stain (solvent based).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Exterior [marine spar varnish (gloss)] [varnish (gloss)] [varnish (semigloss)].

5. Varnish System:  MPI EXT 6.2K.

"MPI Manual" requires four finish coats for a Premium Grade system and three finish coats for a Custom Grade system.

a. [Four] [Three] Finish Coats:  Exterior varnish [(marine spar, high gloss)] [(gloss)] [(semigloss)].

6. Clear, Two-Component Polyurethane System:  MPI EXT 6.2H.

"MPI Manual" requires three finish coats for a Premium Grade system; it does not include a Custom Grade system.

a. Three Finish Coats:  Two-component aliphatic polyurethane (clear).

C. Finish Carpentry Substrates:

1. Solid-Color Latex Stain System:  MPI EXT 6.3K.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior, solid-color latex stain.

2. Solid-Color, Solvent-Based Stain System:  MPI EXT 6.3C.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior solid-color stain (solvent based).

3. Semitransparent Stain System:  MPI EXT 6.3D.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Exterior semitransparent stain (solvent based).

4. Varnish Over Semitransparent Stain System:  MPI EXT 6.3E.

a. Stain Coat:  Exterior semitransparent stain (solvent based).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Exterior varnish [(marine spar, high gloss)] [(gloss)] [(semigloss)].

5. Varnish System:  MPI EXT 6.3F.

"MPI Manual" requires four finish coats for a Premium Grade system and three finish coats for a Custom Grade system.

a. [Four] [Three] Finish Coats:  Exterior varnish [(marine spar, high gloss)] [(gloss)] [(semigloss)].

6. Clear, Two-Component Polyurethane System:  MPI EXT 6.3G.

"MPI Manual" requires three finish coats for a Premium Grade system; it does not include a Custom Grade system.

a. Three Finish Coats:  Two-component aliphatic polyurethane (clear).

D. Exposed Wood Panel-Product Substrates:

1. Solid-Color Latex Stain System:  MPI EXT 6.4A.

a. Prime Coat:  Exterior [alkyd] [latex] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior, solid-color latex stain.

2. Solid-Color, Solvent-Based Stain System:  MPI EXT 6.4C.

"MPI Manual" requires prime coat for a Premium Grade system and omits prime coat for a Custom Grade system.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

b. Two Stain Coats:  Exterior solid-color stain (solvent based).

3. Semitransparent Stain System:  MPI EXT 6.4D.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Exterior semitransparent stain (solvent based).

4. Varnish Over Semitransparent Stain System:  MPI EXT 6.4J.

a. Stain Coat:  Exterior semitransparent stain (solvent based).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Exterior varnish [(marine spar, high gloss)] [(gloss)] [(semigloss)].

5. Varnish System:  MPI EXT 6.4H.

"MPI Manual" requires four finish coats for a Premium Grade system and three finish coats for a Custom Grade system.

a. [Four] [Three] Finish Coats:  Exterior varnish [(marine spar, high gloss)] [(gloss)] [(semigloss)].

E. Wood Deck and Stair Substrates:

1. MPI EXT 6.5D.

a. Preservative Coat:  Wood preservative.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Stain for wood decks.

2. MPI EXT 6.5F.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Stain for wood decks.

F. Wood Shingle and Shake Substrates (Excluding Roofs):

1. Solid-Color Latex Stain System:  MPI EXT 6.6D.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior, solid-color latex stain.

2. Solid-Color, Solvent-Based Stain System:  MPI EXT 6.6C.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior solid-color stain (solvent based).

3. Semitransparent Stain System:  MPI EXT 6.6F.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Exterior semitransparent stain (solvent based).

3.7 INTERIOR WOOD-FINISH-SYSTEM SCHEDULE

Finish systems in this Article are based on "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").  For renovation projects, consult "MPI Maintenance Repainting Manual" and revise finish systems accordingly.

Coordinate substrates and finish systems retained in this Article with products retained in Part 2.

A. Exposed Glue-Laminated Beam and Column Substrates:

1. Alkyd Varnish Over Stain System:  MPI INT 6.1K.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Interior varnish [(flat)] [(semigloss)] [(gloss)].

2. Alkyd Varnish Over Stain and Sealer System:  MPI INT 6.1P.

a. Stain Coat:  Interior wood stain (semitransparent).

b. Seal Coat:  Alkyd sanding sealer.

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

c. [Two Finish Coats] [One Finish Coat]:  Interior varnish [(flat)] [(semigloss)] [(gloss)].

3. Alkyd Varnish Over Sealer System:  MPI INT 6.1C.

a. Seal Coat:  Alkyd sanding sealer.

"MPI Manual" requires two finish coats for a Premium Grade system; it does not include a Custom Grade system.

b. Two Finish Coats:  Interior varnish [(flat)] [(semigloss)] [(gloss)].

4. Polyurethane Varnish Over Stain System:  MPI INT 6.1J.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

5. Polyurethane Varnish System:  MPI INT 6.1D.

a. One Factory-Applied Finish Coat:  Matching field-applied finish coats.

"MPI Manual" requires one factory-applied finish coat and two field-applied finish coats for a Premium Grade system; it does not include a Custom Grade system.

b. Two Field-Applied Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

6. Moisture-Cured Clear Polyurethane Over Stain System:  MPI INT 6.1S.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Moisture-cured clear polyurethane [(flat)] [(gloss)].

7. Waterborne Clear Acrylic Over Stain System:  MPI INT 6.1R.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Waterborne clear acrylic [(satin)] [(semigloss)] [(gloss)].

8. Waterborne Clear Acrylic System:  MPI INT 6.F.

"MPI Manual" requires three finish coats for a Premium Grade system; it does not include a Custom Grade system.

a. Three Finish Coats:  Waterborne clear acrylic [(satin)] [(semigloss)] [(gloss)].

9. Solid-Color Latex Stain System:  MPI INT 6.1T.

a. Prime Coat:  Exterior [alkyd] [oil] wood primer.

"MPI Manual" requires two stain coats for a Premium Grade system and one stain coat for a Custom Grade system.

b. [Two Stain Coats] [One Stain Coat]:  Exterior, solid-color latex stain.

10. Solid-Color, Solvent-Based Stain System:  MPI INT 6.1H.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Exterior solid-color stain (solvent based).

11. Semitransparent Stain System:  MPI INT 6.1G.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Exterior semitransparent stain (solvent based).

B. Exposed Rough Carpentry Substrates:

1. Alkyd Varnish Over Stain and Sealer System:  MPI INT 6.2K.

a. Stain Coat:  Interior wood stain (semitransparent).

b. Seal Coat:  Alkyd sanding sealer.

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

c. [Two Finish Coats] [One Finish Coat]:  Interior varnish [(flat)] [(semigloss)] [(gloss)].

2. Alkyd Varnish Over Sealer System:  MPI INT 6.2P.

a. Seal Coat:  Alkyd sanding sealer.

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

b. [Two Finish Coats] [One Finish Coat]:  Interior varnish [(flat)] [(semigloss)] [(gloss)].

3. Polyurethane Varnish Over Stain System:  MPI INT 6.2J.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

4. Polyurethane Varnish System:  MPI INT 6.2H.

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

a. [Three] [Two] Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

5. Moisture-Cured Clear Polyurethane Over Stain System:  MPI INT 6.2N.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Moisture-cured clear polyurethane [(flat)] [(gloss)].

6. Waterborne Clear Acrylic Over Stain System:  MPI INT 6.2M.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Waterborne clear acrylic [(satin)] [(semigloss)] [(gloss)].

C. Finish Carpentry Substrates:

1. Alkyd Varnish Over Stain and Sealer System:  MPI INT 6.3D.

a. Stain Coat:  Interior wood stain (semitransparent).

b. Seal Coat:  [Alkyd sanding sealer] [Shellac].

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

c. [Two Finish Coats] [One Finish Coat]:  Interior varnish [(semigloss)] [(gloss)].

2. Alkyd Varnish Over Sealer System:  MPI INT 6.3J.

a. Seal Coat:  [Alkyd sanding sealer] [Shellac].

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

b. [Two Finish Coats] [One Finish Coat]:  Interior varnish [(semigloss)] [(gloss)].

3. Polyurethane Varnish Over Stain System:  MPI INT 6.3E.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

4. Polyurethane Varnish System:  MPI INT 6.3K.

a. One Factory-Applied Finish Coat:  Matching field-applied finish coats.

"MPI Manual" requires one factory-applied finish coat and two field-applied finish coats for a Premium Grade system; it does not include a Custom Grade system.

b. Two Field-Applied Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

5. Moisture-Cured Clear Polyurethane Over Stain System:  MPI INT 6.3Y.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Moisture-cured clear polyurethane [(flat)] [(gloss)].

6. Moisture-Cured Clear Polyurethane System:  MPI INT 6.3X.

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

a. [Three] [Two] Finish Coats:  Moisture-cured clear polyurethane [(flat)] [(gloss)].

7. Clear, Two-Component Polyurethane System:  MPI INT 6.3Z.

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

a. [Three] [Two] Finish Coats:  Two-component aliphatic polyurethane (clear).

8. Waterborne Clear Acrylic Over Stain System:  MPI INT 6.3W.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Waterborne clear acrylic [(satin)] [(semigloss)] [(gloss)].

9. Waterborne Clear Acrylic System:  MPI INT 6.3Q.

"MPI Manual" requires three finish coats for a Premium Grade system; it does not include a Custom Grade system.

a. Three Finish Coats:  Waterborne clear acrylic [(satin)] [(semigloss)] [(gloss)].

10. Lacquer Over Stain and Sealer System:  MPI INT 6.3F.

a. Stain Coat:  Interior wood stain (semitransparent).

b. Seal Coat:  Lacquer sanding sealer.

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

c. [Two Finish Coats] [One Finish Coat]:  Lacquer (clear [flat] [satin] [gloss]).

11. Lacquer Over Sealer System:  MPI INT 6.3H.

a. Seal Coat:  Lacquer sanding sealer.

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

b. [Two Finish Coats] [One Finish Coat]:  Lacquer (clear [flat] [satin] [gloss]).

12. Semitransparent Stain System:  MPI INT 6.3C.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.  It is not recommended for use on doors.

a. Two Stain Coats:  Exterior semitransparent stain (solvent based).

13. Danish Oil System:  MPI INT 6.3M.

"MPI Manual" requires two finish coats for a Premium Grade system; it does not include a Custom Grade system.

a. Two Finish Coats:  Danish oil.

D. Exposed Wood Panel-Product Substrates:

1. Alkyd Varnish Over Sealer and Stain System:  MPI INT 6.4D.

a. Stain Coat:  Interior wood stain (semitransparent).

b. Seal Coat:  [Alkyd sanding sealer] [Shellac].

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

c. [Two Finish Coats] [One Finish Coat]:  Interior varnish [(flat)] [(semigloss)] [(gloss)].

2. Alkyd Varnish Over Sealer System:  MPI INT 6.4G.

a. Seal Coat:  [Alkyd sanding sealer] [Shellac].

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

b. [Two Finish Coats] [One Finish Coat]:  Interior varnish [(flat)] [(semigloss)] [(gloss)].

3. Polyurethane Varnish Over Stain System:  MPI INT 6.4E.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

4. Polyurethane Varnish System:  MPI INT 6.4.J.

a. One Factory-Applied Finish Coat:  Matching field-applied finish coats.

"MPI Manual" requires one factory-applied finish coat and two field-applied finish coats for a Premium Grade system; it does not include a Custom Grade system.

b. Two Field-Applied Finish Coats:  Interior, oil-modified, clear urethane [(satin)] [(gloss)].

5. Moisture-Cured Clear Polyurethane Over Stain System:  MPI INT 6.4V.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Moisture-cured clear polyurethane [(flat)] [(gloss)].

6. Waterborne Clear Acrylic Over Stain System:  MPI INT 6.4U.

a. Stain Coat:  Interior wood stain (semitransparent).

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Waterborne clear acrylic [(satin)] [(semigloss)] [(gloss)].

7. Lacquer Over Stain and Sealer System:  MPI INT 6.4F.

a. Stain Coat:  Interior wood stain (semitransparent).

b. Seal Coat:  Lacquer sanding sealer.

"MPI Manual" requires two finish coats for a Premium Grade system and one finish coat for a Custom Grade system.

c. [Two Finish Coats] [One Finish Coat]:  Lacquer (clear [flat] [satin] [gloss]).

8. Lacquer Over Sealer System:  MPI INT 6.4Y.

a. Seal Coat:  Lacquer sanding sealer.

"MPI Manual" requires three finish coats for a Premium Grade system and two finish coats for a Custom Grade system.

b. [Three] [Two] Finish Coats:  Lacquer (clear [flat] [satin] [gloss]).

9. Semitransparent Stain System:  MPI INT 6.4C.

"MPI Manual" requires two stain coats for a Custom Grade system; it does not include a Premium Grade system.

a. Two Stain Coats:  Exterior semitransparent stain (solvent based).

10. Danish Oil System:  MPI INT 6.4K.

"MPI Manual" requires two finish coats for a Premium Grade system; it does not include a Custom Grade system.

a. Two Finish Coats:  Danish oil.

END OF SECTION 099300

STAINING AND TRANSPARENT FINISHING
099300 - 1

