Copyright 2011 AIA
MasterSpec Professional
08/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 034100 - PRECAST STRUCTURAL CONCRETE
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes precast structural concrete.

1.2 PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Product Certificates for Credit MR 5" Subparagraph below applies to LEED-NC, LEED-CS, and LEED for Schools.

2. Product Certificates for Credit MR 5: For products and materials required to comply with requirements for regional materials, certificates indicating location of material manufacturer and point of extraction, harvest, or recovery for each raw material. Include statement indicating distance to Project, cost for each regional material, and fraction by weight that is considered regional.

Retain "Design Mixtures for Credit ID 1.1" Subparagraph below if fly ash, ground granulated blast-furnace slag, silica fume, or other materials are used as portland cement replacements for LEED-NC, LEED-CS, or LEED for Schools Credit ID 1.1. To achieve this credit, replacement materials must be substituted for at least 40 percent of the portland cement that would otherwise be used.

3. Design Mixtures for Credit ID 1.1: For each concrete mixture containing fly ash as a replacement for portland cement or other portland cement replacements and for equivalent concrete mixtures that do not contain portland cement replacements.

C. Design Mixtures: For each precast concrete mixture.

D. Shop Drawings:

1. Include member locations, plans, elevations, dimensions, shapes and sections, openings, support conditions, and types of reinforcement, including special reinforcement.

2. Detail fabrication and installation of precast structural concrete units, including connections at member ends and to adjoining construction.

Retain "Delegated-Design Submittal" Paragraph below if design services have been delegated to Contractor.

E. Delegated-Design Submittal: For precast structural concrete indicated to comply with performance requirements and design criteria, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

1.4 INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

A. Qualification Data: For [Installer] [fabricator] [testing agency].

Retain "Welding certificates" Paragraph below if retaining "Welding Qualifications" Paragraph in "Quality Assurance" Article.

B. Welding certificates.

Retain "Material certificates" Paragraph below to require submittal of material certificates from manufacturers.

C. Material certificates.

Retain "Material Test Reports" Paragraph below for material test reports that are Contractor's responsibility.

D. Material Test Reports: For aggregates.

E. Source quality-control reports.

Retain "Field quality-control reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting. Retain option if Contractor is responsible for special inspections.

F. Field quality-control[ and special inspection] reports.

1.5 QUALITY ASSURANCE

A. Fabricator Qualifications: A firm that assumes responsibility for engineering precast structural concrete units to comply with performance requirements. Responsibility includes preparation of Shop Drawings and comprehensive engineering analysis by a qualified professional engineer.

Usually retain first subparagraph below and retain a category to qualify a fabricator. A precast concrete plant certified to produce products in Category C2A, for example, is also certified to produce products in Categories C1, C1A, and C2 but not in Category C3, C3A, C4, or C4A. See Evaluations for discussion of PCI's Group C and Group CA categories.

1. Designated as a PCI-certified plant as follows:

a. Group C, [Category C1 - Precast Concrete Products (no prestressed reinforcement)] [Category C2 - Prestressed Hollowcore and Repetitively Produced Products] [Category C3 - Prestressed Straight Strand Structural Members] [Category C4 - Prestressed Deflected Strand Structural Members].

Retain subparagraph below if required for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5.

2. Fabricator is located within 500 miles (800 km) of Project site.

B. Quality-Control Standard: For manufacturing procedures, testing requirements, and quality-control recommendations for types of units required, comply with PCI MNL 116, "Manual for Quality Control for Plants and Production of Structural Precast Concrete Products."

Retain "Welding Qualifications" Paragraph below if shop or field welding is required. If retaining, also retain "Welding certificates" Paragraph in "Informational Submittals" Article.

C. Welding Qualifications: Qualify procedures and personnel according to the following:

1. AWS D1.1/D1.1M, "Structural Welding Code - Steel."

2. AWS D1.4/D1.4M, "Structural Welding Code - Reinforcing Steel."

1.6 COORDINATION

A. Furnish loose connection hardware and anchorage items to be embedded in or attached to other construction before starting that Work. Provide locations, setting diagrams, templates, instructions, and directions, as required, for installation.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Delegated Design" Paragraph below if Contractor is required to assume responsibility for design.

A. Delegated Design: Engage a qualified professional engineer, as defined in Section 014000 "Quality Requirements," to design precast structural concrete units.

B. Design Standards: Comply with ACI 318 (ACI 318M) and with design recommendations in PCI MNL 120, "PCI Design Handbook - Precast and Prestressed Concrete," applicable to types of precast structural concrete units indicated.

C. Structural Performance: Precast structural concrete units and connections shall withstand design loads indicated within limits and under conditions indicated.

Retain "Fire-Resistance Rating" Subparagraph below if required. Fire ratings depend on occupancy and building construction type and are generally a building code requirement.

1. Fire-Resistance Rating: Select material and minimum thicknesses to provide indicated fire rating.

2.2 REINFORCING MATERIALS

Retain one or more paragraphs in this article to suit steel reinforcement requirements. Distinguish locations of each type of reinforcement here or on Drawings. If retaining "Performance Requirements" Article, consider reviewing selections with fabricators.

Retain "Recycled Content of Steel Products" Paragraph below if recycled content is required for LEED Credit MR 4. USGBC allows a default value of 25 percent to be used for steel, without documentation; higher percentages can be claimed if they are supported by appropriate documentation.

A. Recycled Content of Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] [60] <Insert number> percent.

B. Reinforcing Bars: ASTM A 615/A 615M, Grade 60 (Grade 420), deformed.

Retain "Low-Alloy-Steel Reinforcing Bars" Paragraph below for reinforcement that is welded or if added ductility is sought.

C. Low-Alloy-Steel Reinforcing Bars: ASTM A 706/A 706M, deformed.

D. Steel Bar Mats: ASTM A 184/A 184M, fabricated from [ASTM A 615/A 615M, Grade 60 (Grade 420)] [ASTM A 706/A 706M], deformed bars, assembled with clips.

E. Plain-Steel Welded Wire Reinforcement: ASTM A 185/A 185M, fabricated from [as-drawn steel] [galvanized-steel] wire into flat sheets.

F. Deformed-Steel Welded Wire Reinforcement: ASTM A 497/A 497M or ASTM A 1064/A 1064M, flat sheet.

G. Supports: Suspend reinforcement from back of mold or use bolsters, chairs, spacers, and other devices for spacing, supporting, and fastening reinforcing bars and welded wire reinforcement in place according to PCI MNL 116.

2.3 PRESTRESSING TENDONS

Retain this article if precast concrete units are prestressed, either pretensioned or post-tensioned.

A. Strand: ASTM A 416/A 416M, Grade 270 (Grade 1860), uncoated, seven-wire, low-relaxation strand.

For aggressive climates, revise subparagraph below by adding an anchorage device encapsulation system consisting of caps and sleeves.

1. Coat unbonded post-tensioning strand with post-tensioning coating complying with ACI 423.7 and sheath with polypropylene tendon sheathing complying with ACI 423.7. Include anchorage devices and coupler assemblies.

2.4 CONCRETE MATERIALS

Retain materials in this article as required; revise to suit Project.

Retain "Regional Materials" Paragraph below if required for LEED-NC, LEED-CS, or LEED for Schools Credit MR 5.

A. Regional Materials: Precast structural concrete shall be manufactured from aggregates[ and cement] that have been extracted or recovered, as well as manufactured, within 500 miles (800 km) of Project site.

B. Portland Cement: ASTM C 150/C 150M, Type I or Type III, gray, unless otherwise indicated.

C. Supplementary Cementitious Materials:

Retain mineral or cementitious admixtures in first four subparagraphs below. Because fly ash and gray silica fume affect color uniformity, they are not recommended by PCI where appearance is important. White silica fume is available.

1. Fly Ash: ASTM C 618, Class C or F, with maximum loss on ignition of 3 percent.

2. Metakaolin: ASTM C 618, Class N.

3. Silica Fume: ASTM C 1240, with optional chemical and physical requirement.

4. Ground Granulated Blast-Furnace Slag: ASTM C 989, Grade 100 or 120.

Retain "Blended Hydraulic Cement" Subparagraph below if factory-blended hydraulic cement is permitted; verify availability of options before specifying. Fly ash, slag, or pozzolanic materials in the nonportland cement part of blended hydraulic cement may slow rate of concrete strengthening and affect color uniformity.

5. Blended Hydraulic Cement: ASTM C 595/C 595M, [Type IS, portland blast-furnace slag] [Type IP, portland-pozzolan] [Type I (PM), pozzolan-modified portland] [Type I (SM), slag-modified portland] cement.

ASTM C 33/C 33M limits deleterious substances in coarse aggregate depending on climate severity and in-service location of concrete. Class 5S is the most restrictive designation for architectural concrete exposed to severe weathering. PCI MNL 116 also establishes strict limits on deleterious substances for fine and coarse aggregates.

D. Normal-Weight Aggregates: Except as modified by PCI MNL 116, ASTM C 33/C 33M, with coarse aggregates complying with [Class 5S] [Class 5M] [Class 4S] [Class 4M]. Stockpile fine and coarse aggregates for each type of exposed finish from a single source (pit or quarry) for Project.

E. Water: Potable; free from deleterious material that may affect color stability, setting, or strength of concrete and complying with chemical limits of PCI MNL 116.

F. Air-Entraining Admixture: ASTM C 260, certified by manufacturer to be compatible with other required admixtures.

G. Chemical Admixtures: Certified by manufacturer to be compatible with other admixtures and to not contain calcium chloride, or more than 0.15 percent chloride ions or other salts by weight of admixture.

2.5 STEEL CONNECTION MATERIALS

Revise this article to suit Project. Add other materials as required.

A. Carbon-Steel Shapes and Plates: ASTM A 36/A 36M.

B. Carbon-Steel-Headed Studs: ASTM A 108, Grade 1010 through 1020, cold finished, AWS D1.1/D1.1M, Type A or B, with arc shields and with minimum mechanical properties of PCI MNL 116.

C. Carbon-Steel Plate: ASTM A 283/A 283M, Grade C.

D. Malleable-Iron Castings: ASTM A 47/A 47M, Grade 32510 or Grade 35028.

E. Carbon-Steel Castings: ASTM A 27/A 27M, Grade 60-30 (Grade 415-205).

F. High-Strength, Low-Alloy Structural Steel: ASTM A 572/A 572M.

G. Carbon-Steel Structural Tubing: ASTM A 500/A 500M, Grade B or Grade C.

H. Wrought Carbon-Steel Bars: ASTM A 675/A 675M, Grade 65 (Grade 450).

I. Deformed-Steel Wire or Bar Anchors: ASTM A 496/A 496M or ASTM A 706/A 706M.

ASTM A 307 defines the term "studs" to include stud stock and threaded rods.

J. Carbon-Steel Bolts and Studs: ASTM A 307, Grade A (ASTM F 568M, Property Class 4.6); carbon-steel, hex-head bolts and studs; carbon-steel nuts, ASTM A 563 (ASTM A 563M); and flat, unhardened steel washers, ASTM F 844.

High-strength bolts are used for friction-type connections between steel members and are not recommended by PCI between steel and concrete because concrete creep and crushing of concrete during bolt tightening reduce effectiveness.

K. High-Strength Bolts and Nuts: ASTM A 325 (ASTM A 325M) or ASTM A 490 (ASTM A 490M,) Type 1, heavy hex steel structural bolts; heavy hex carbon-steel nuts, ASTM A 563 (ASTM A 563M); and hardened carbon-steel washers, ASTM F 436 (ASTM F 436M).

1. Do not zinc coat ASTM A 490 (ASTM A 490M) bolts.

Retain "Zinc-Coated Finish" Paragraph below if galvanized finish is required. Revise locations of galvanized items if required. Field welding is generally not permitted on galvanized elements unless galvanizing is removed or acceptable welding procedures are submitted. Hot-dip galvanized finish provides greater corrosion resistance than electrodeposited zinc coating. Electrodeposition is usually limited to threaded fasteners.

L. Zinc-Coated Finish: For exterior steel items[, steel in exterior walls,] and items indicated for galvanizing, apply zinc coating by [hot-dip process according to ASTM A 123/A 123M or ASTM A 153/A 153M] [electrodeposition according to ASTM B 633, SC 3, Types 1 and 2].

1. Galvanizing Repair Paint: High-zinc-dust-content paint with dry film containing not less than 94 percent zinc dust by weight, and complying with DOD-P-21035B or SSPC-Paint 20.

Retain "Shop-Primed Finish" Paragraph below if required. Revise locations of priming if required. MPI 79 in first option below provides some corrosion protection, while SSPC-Paint 25, without topcoating, provides minimal corrosion protection.

M. Shop-Primed Finish: Prepare surfaces of nongalvanized-steel items, except those surfaces to be embedded in concrete, according to requirements in SSPC-SP 3, and shop apply [lead- and chromate-free, rust-inhibitive primer, complying with performance requirements in MPI 79] [SSPC-Paint 25] according to SSPC-PA 1.

2.6 BEARING PADS

Retain this article if applicable. Coordinate selection of bearing pad with fabricator.

A. Provide bearing pads for precast structural concrete units as recommended by precast fabricator for application.

2.7 GROUT MATERIALS

Add other proprietary grout systems to suit Project. Indicate locations of each type of grout in this article or on Drawings if retaining more than one type. Sand-cement grout in "Sand-Cement Grout" Paragraph below is commonly used in keyed joints between hollow-core floor and roof slabs and wall units.

A. Sand-Cement Grout: Portland cement, ASTM C 150/C 150M, Type I, and clean, natural sand, ASTM C 144 or ASTM C 404. Mix at ratio of 1 part cement to 2-1/2 to 3 parts sand, by volume, with minimum water required for placement and hydration. Water-soluble chloride ion content less than 0.06 percent by weight of cement when tested according to ASTM C 1218/C 1218M.

Retain "Nonmetallic, Nonshrink Grout" Paragraph below if required or if cement-grout shrinkage could cause structural deficiency. For critical installations, require manufacturer to provide field supervision.

B. Nonmetallic, Nonshrink Grout: Packaged, nonmetallic, noncorrosive, nonstaining grout containing selected silica sands, portland cement, shrinkage-compensating agents, plasticizing and water-reducing agents, complying with ASTM C 1107/C 1107M, Grade A for drypack and Grades B and C for flowable grout and of consistency suitable for application within a 30-minute working time. Water-soluble chloride ion content less than 0.06 percent by weight of cement when tested according to ASTM C 1218/C 1218M.

C. Epoxy-Resin Grout: Two-component, mineral-filled epoxy resin; ASTM C 881/C 881M, of type, grade, and class to suit requirements.

2.8 INSULATED FLAT-WALL PANEL ACCESSORIES

Retain this article if insulated flat-wall panels are required. Retain insulation material in "Molded-Polystyrene Board Insulation," "Extruded-Polystyrene Board Insulation," or "Polyisocyanurate Board Insulation" Paragraph below; if using more than one type, identify location of each on Drawings.

A. Molded-Polystyrene Board Insulation: ASTM C 578, [Type XI, 0.70 lb/cu. ft. (12 kg/cu. m)] [Type I, 0.90 lb/cu. ft. (15 kg/cu. m)] [Type VIII, 1.15 lb/cu. ft. (18 kg/cu. m)] [Type II, 1.35 lb/cu. ft. (22 kg/cu. m)] [Type IX, 1.80 lb/cu. ft. (29 kg/cu. m)]; [square] [ship-lap] edges; with thickness of <Insert dimension>.

B. Extruded-Polystyrene Board Insulation: ASTM C 578, [Type X, 1.30 lb/cu. ft. (21 kg/cu. m)] [Type IV, 1.55 lb/cu. ft. (26 kg/cu. m)] [Type VI, 1.80 lb/cu. ft. (29 kg/cu. m)] [Type VII, 2.20 lb/cu. ft. (35 kg/cu. m)] [Type V, 3.00 lb/cu. ft. (48 kg/cu. m)]; [square] [ship-lap] edges; with thickness of <Insert dimension>.

C. Polyisocyanurate Board Insulation: ASTM C 591, [Type I, 1.8 lb/cu. ft. (29 kg/cu. m)] [Type II, 2.5 lb/cu. ft. (40 kg/cu. m)] [Type III, 3.0 lb/cu. ft. (48 kg/cu. m)] unfaced, with thickness of <Insert dimension>.

Retain one or more options in "Wythe Connectors" Paragraph below.

D. Wythe Connectors: [Glass-fiber-reinforced vinylester connectors] [Polypropylene pin connectors] [Stainless-steel pin connectors] [Bent galvanized reinforcing bars] [Galvanized welded wire trusses] [Galvanized bent wire connectors] [Epoxy-coated carbon-fiber grid] [Fiberglass trusses] manufactured to connect wythes of precast concrete panels.

2.9 CONCRETE MIXTURES

A. Prepare design mixtures for each type of precast concrete required.

Retain first subparagraph below if required for LEED-NC, LEED-CS, or LEED for Schools Credit ID 1.1. This credit can be achieved by replacing at least 40 percent of the portland cement, which would otherwise be used in concrete, with other cementitious materials. 40 percent replacement value applies to the average of all concrete used for Project; requirement below can be reduced if requirement for other concrete on Project is increased sufficiently to make up for the reduction.

1. Use fly ash, pozzolan, ground granulated blast-furnace slag, and silica fume as needed to reduce the total amount of portland cement, which would otherwise be used, by not less than 40 percent.

Retain subparagraph below if fly ash, ground granulated blast-furnace slag, or metakaolin and silica fume are permitted. Percentages are PCI examples; revise to suit Project.

2. Limit use of fly ash to [20] [35] percent replacement of portland cement by weight and ground granulated blast-furnace slag to [20] [50] percent of portland cement by weight; metakaolin and silica fume to 10 percent of portland cement by weight.

B. Design mixtures may be prepared by a qualified independent testing agency or by qualified precast plant personnel at precast structural concrete fabricator's option.

C. Limit water-soluble chloride ions to maximum percentage by weight of cement permitted by ACI 318 (ACI 318M) or PCI MNL 116 when tested according to ASTM C 1218/C 1218M.

D. Normal-Weight Concrete Mixtures: Proportion [face and backup mixtures] [full-depth mixture] [face and backup mixtures or full-depth mixtures, at fabricator's option] by either laboratory trial batch or field test data methods according to ACI 211.1, with materials to be used on Project, to provide normal-weight concrete with the following properties:

Retain "Compressive Strength (28 Days)" Subparagraph below or revise to suit Project. Higher-strength mixtures may be available; verify availability with fabricators.

1. Compressive Strength (28 Days): 5000 psi (34.5 MPa).

Water-cementitious materials ratio of 0.40 to 0.45 is usual for precast structural concrete. Lower ratios may be possible with use of high-range water reducers. Revise ratio in "Maximum Water-Cementitious Materials Ratio" Subparagraph below to suit Project.

2. Maximum Water-Cementitious Materials Ratio: 0.45.

Water absorption indicates susceptibility to weather staining. PCI states that limits in "Water Absorption" Paragraph below are suitable for average exposures. Different parts of a single panel cannot be produced with different absorptions. Verify that fabricators can produce units with lower water absorption because special consolidation techniques to increase concrete density are required.

E. Water Absorption: Limit water absorption to 6 percent by weight or 14 percent by volume, tested according to ASTM C 642, except for boiling requirement.

F. Add air-entraining admixture at manufacturer's prescribed rate to result in concrete at point of placement having an air content complying with PCI MNL 116.

G. When included in design mixtures, add other admixtures to concrete mixtures according to manufacturer's written instructions.

H. Concrete Mix Adjustments: Concrete mix design adjustments may be proposed if characteristics of materials, Project conditions, weather, test results, or other circumstances warrant.

2.10 FABRICATION

A. Cast-in Anchors, Inserts, Plates, Angles, and Other Anchorage Hardware: Fabricate anchorage hardware with sufficient anchorage and embedment to comply with design requirements. Accurately position for attachment of loose hardware, and secure in place during precasting operations. Locate anchorage hardware where it does not affect position of main reinforcement or concrete placement.

1. Weld-headed studs and deformed bar anchors used for anchorage according to AWS D1.1/D1.1M and AWS C5.4, "Recommended Practices for Stud Welding."

Coordinate first paragraph below with Section 055000 "Metal Fabrications" for furnishing and installing loose hardware items.

B. Furnish loose hardware items including steel plates, clip angles, seat angles, anchors, dowels, cramps, hangers, and other hardware shapes for securing precast structural concrete units to supporting and adjacent construction.

C. Cast-in reglets, slots, holes, and other accessories in precast structural concrete units as indicated on the Contract Drawings.

Retain first paragraph below if applicable.

D. Cast-in openings larger than 10 inches (250 mm) in any dimension. Do not drill or cut openings or prestressing strand without Architect's approval.

E. Reinforcement: Comply with recommendations in PCI MNL 116 for fabricating, placing, and supporting reinforcement.

F. Reinforce precast structural concrete units to resist handling, transportation, and erection stresses and specified in-place loads.

Retain first paragraph below if precast, prestressed structural concrete units are required. Decision to prestress may be left to fabricator if objective is to aid handling and to control cracking of units during installation.

G. Prestress tendons for precast structural concrete units by either pretensioning or post-tensioning methods. Comply with PCI MNL 116.

H. Comply with requirements in PCI MNL 116 and in this Section for measuring, mixing, transporting, and placing concrete. After concrete batching, no additional water may be added.

I. Place concrete in a continuous operation to prevent cold joints or planes of weakness from forming in precast concrete units.

J. Thoroughly consolidate placed concrete by vibration without dislocating or damaging reinforcement and built-in items, and minimize pour lines, honeycombing, or entrapped air voids on surfaces. Use equipment and procedures complying with PCI MNL 116.

K. Comply with PCI MNL 116 procedures for hot- and cold-weather concrete placement.

L. Identify pickup points of precast structural concrete units and orientation in structure with permanent markings, complying with markings indicated on Shop Drawings. Imprint or permanently mark casting date on each precast structural concrete unit on a surface that does not show in finished structure.

M. Cure concrete, according to requirements in PCI MNL 116, by moisture retention without heat or by accelerated heat curing using live steam or radiant heat and moisture. Cure units until compressive strength is high enough to ensure that stripping does not have an effect on performance or appearance of final product.

N. Discard and replace precast structural concrete units that do not comply with requirements, including structural, manufacturing tolerance, and appearance, unless repairs meet requirements in PCI MNL 116 and meet Architect's approval.

2.11 CASTING INSULATED WALL PANELS

Retain this article if integrally insulated wall panels are required.

A. Cast, screed, and consolidate wythe supported by mold.

B. Place insulation boards abutting edges and ends of adjacent boards. Insert wythe connectors through insulation, and consolidate concrete around connectors according to connector manufacturer's written instructions.

C. Cast, screed, and consolidate top wythe to meet required finish.

2.12 FABRICATION TOLERANCES

A. Fabricate precast structural concrete units to shapes, lines, and dimensions indicated so each finished unit complies with PCI MNL 116 product dimension tolerances as well as position tolerances for cast-in items.

2.13 COMMERCIAL FINISHES

Retain type of commercial structural finish, grouped by PCI as a "C" designation, in one or more of "Commercial Grade," "Standard Grade," "Grade B Finish," and "Grade A Finish" paragraphs below. If more than one finish is required, create a finish schedule, add locations to finish descriptions, or indicate on Drawings. Finishes below are in ascending order of finish quality and cost. Insert other specific finish requirements to suit Project.

Retain "Commercial Grade" Paragraph below when product is not visible in completed structure or when function of structure does not require an enhanced surface. This finish is essentially an "as-cast" one.

A. Commercial Grade: Remove fins and protrusions larger than 1/8 inch (3 mm) and fill holes larger than 1/2 inch (13 mm). Rub or grind ragged edges. Faces must have true, well-defined surfaces. Air holes, water marks, and color variations are permitted. Limit form joint offsets to 3/16 inch (5 mm).

Retain "Standard Grade" Paragraph below where products are exposed to view but function of structure does not require a special finish. Surface is suitable for an applied textured coating, but not necessarily suitable for painting. This finish is typical for structural products.

B. Standard Grade: Normal plant-run finish produced in molds that impart a smooth finish to concrete. Surface holes smaller than 1/2 inch (13 mm) caused by air bubbles, normal color variations, form joint marks, and minor chips and spalls are permitted. Fill air holes greater than 1/4 inch (6 mm) in width that occur more than once per 2 sq. in. (1300 sq. mm). Major or unsightly imperfections, honeycombs, or structural defects are not permitted. Limit joint offsets to 1/8 inch (3 mm).

Retain "Grade B Finish" Paragraph below for visually exposed structural members such as columns or walls.

C. Grade B Finish: Fill air pockets and holes larger than 1/4 inch (6 mm) in diameter with sand-cement paste matching color of adjacent surfaces. Fill air holes greater than 1/8 inch (3 mm) in width that occur more than once per 2 sq. in. (1300 sq. mm). Grind smooth form offsets or fins larger than 1/8 inch (3 mm). Repair surface blemishes due to holes or dents in molds. Discoloration at form joints is permitted.

Retain "Grade A Finish" Paragraph below where surface is painted or coated with a textured or sanded coating; some surface blemishes are visible. Grade A finish is not applicable to extruded precast structural concrete products using zero-slump concrete in their process.

D. Grade A Finish: Repair surface blemishes and fill air holes with the exception of air holes 1/16 inch (1.6 mm) in width or smaller, and form marks where the surface deviation is less than 1/16 inch (1.6 mm). Float apply a neat cement-paste coating to exposed surfaces. Rub dried paste coat with burlap to remove loose particles. Discoloration at form joints is permitted. Grind smooth all form joints.

Retain one of first two paragraphs below. Screed or float finish in first paragraph is standard with PCI for unformed surfaces. Revise to describe extent to which float or trowel marks, variations of texture, or other surface blemishes are permitted. Require samples to establish acceptance criteria for any exposed finish. Revise finish below to light-broom or as-cast finish if float finish is unnecessary.

E. Screed or float finish unformed surfaces. Strike off and consolidate concrete with vibrating screeds to a uniform finish. Hand screed at projections. Normal color variations, minor indentations, minor chips, and spalls are permitted. Major imperfections, honeycombing, or defects are not permitted.

Retain first paragraph below if upgrading unformed surfaces to smooth, steel trowel finish.

F. Smooth, steel trowel finish unformed surfaces. Consolidate concrete, bring to proper level with straightedge, float, and trowel to a smooth, uniform finish.

Retain paragraph below if composite concrete topping is required.

G. Apply roughened surface finish according to ACI 318 (ACI 318M) to precast concrete units that receive concrete topping after installation.

2.14 SOURCE QUALITY CONTROL

Retain "Testing" Paragraph below if establishing a minimum standard of plant testing and inspecting. PCI MNL 116 mandates source testing requirements and a plant "Quality Systems Manual." PCI plant certification also ensures periodic auditing of plants complying with PCI MNL 116.

A. Testing: Test and inspect precast structural concrete according to PCI MNL 116 requirements and ASTM C 1610/C 1610M, ASTM C 1611/C 1611M, ASTM C 1621/C 1621M, and ASTM C 1712/C 1712M.

B. Defective Units: Discard and replace precast structural concrete units that do not comply with requirements, including strength, manufacturing tolerances, and color and texture range. Chipped, spalled, or cracked units may be repaired, subject to Architect's approval.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Install clips, hangers, bearing pads, and other accessories required for connecting precast structural concrete units to supporting members and backup materials.

B. Erect precast structural concrete level, plumb, and square within specified allowable tolerances. Provide temporary structural framing, shoring, and bracing as required to maintain position, stability, and alignment of units until permanent connections are complete.

1. Maintain horizontal and vertical joint alignment and uniform joint width as erection progresses.

2. Remove projecting lifting devices and use plastic patch caps or sand-cement grout to fill voids within recessed lifting devices flush with surface of adjacent precast surfaces when recess is exposed.

Retain subparagraph below if voids of hollow-core slabs are used for electrical raceways or mechanical ducts.

3. For hollow-core slab voids used as electrical raceways or mechanical ducts, align voids between units and tape butt joint at end of slabs.

C. Connect precast structural concrete units in position by bolting, welding, grouting, or as otherwise indicated on Shop Drawings. Remove temporary shims, wedges, and spacers as soon as practical after connecting and grouting are completed.

D. Field cutting of precast units is not permitted without approval of Architect.

"Fasteners" Paragraph below refers to fastening under the control of precast concrete erector. Coordinate with and repeat warning in other Sections if additional construction is fastened to precast, prestressed concrete units.

E. Fasteners: Do not use drilled or powder-actuated fasteners for attaching accessory items to precast, prestressed concrete units.

F. Welding: Comply with applicable requirements in AWS D1.1/D1.1M and AWS D1.4/D1.4M for welding, welding electrodes, appearance, quality of welds, and methods used in correcting welding work.

G. At bolted connections, use lock washers, tack welding, or other approved means to prevent loosening of nuts after final adjustment.

In "Grouting or Dry-Packing Connections and Joints" Paragraph below, revise locations and extent of grouting if required.

H. Grouting or Dry-Packing Connections and Joints: Grout connections and joints and open spaces at keyways, connections, and joints where required or indicated on Shop Drawings. Retain flowable grout in place until hard enough to support itself. Alternatively, pack spaces with stiff dry-pack grout material, tamping until voids are completely filled.

3.2 ERECTION TOLERANCES

A. Erect precast structural concrete units level, plumb, square, and in alignment without exceeding the noncumulative erection tolerances of PCI MNL 135.

B. Minimize variations between adjacent slab members by jacking, loading, or other method recommended by fabricator and approved by Architect.

3.3 FIELD QUALITY CONTROL

Retain first option in "Special Inspections" Paragraph below if Owner engages special inspector. Consider retaining second option if authorities having jurisdiction allow Contractor to engage special inspector. If retaining second option, retain "Field quality-control reports" Paragraph in "Informational Submittals" Article.

A. Special Inspections: [Owner will engage] [Engage] a qualified special inspector to perform the following special inspections:

1. Erection of precast structural concrete members.

2. <Insert special inspections>.

Retain "Testing Agency" Paragraph below, with or without "Special Inspections" Paragraph above, to identify who shall perform tests and inspections. If retaining second option in "Testing Agency" Paragraph, retain "Field quality-control reports" Paragraph in "Informational Submittals" Article.

B. Testing Agency: [Owner will engage] [Engage] a qualified testing agency to perform tests and inspections.

C. Visually inspect field welds and test according to ASTM E 165 or to ASTM E 709 and ASTM E 1444. High-strength bolted connections are subject to inspections.

D. Testing agency will report test results promptly and in writing to Contractor and Architect.

E. Repair or remove and replace work where tests and inspections indicate that it does not comply with specified requirements.

F. Additional testing and inspecting, at Contractor's expense, shall be performed to determine compliance of replaced or additional work with specified requirements.

G. Prepare test and inspection reports.

3.4 REPAIRS

Blemishes occurring after delivery are normally repaired after erecting units. Repairs of production chips, cracks, and spalls take place at manufacturer's plant.

A. Repair precast structural concrete units if permitted by Architect.

1. Repairs may be permitted if structural adequacy, serviceability, durability, and appearance of units have not been impaired.

Precast concrete manufacturer develops appropriate repair mixtures and techniques during production sample approval process.

B. Mix patching materials and repair units so cured patches blend with color, texture, and uniformity of adjacent exposed surfaces and show no apparent line of demarcation between original and repaired work, when viewed in typical daylight illumination from a distance of 20 feet (6 m).

Retain first paragraph below if using galvanized anchors, connections, and other items.

C. Prepare and repair damaged galvanized coatings with galvanizing repair paint according to ASTM A 780/A 780M.

Retain first paragraph below if items are prime painted.

D. Wire brush, clean, and paint damaged prime-painted components with same type of shop primer.

E. Remove and replace damaged precast structural concrete units that cannot be repaired or when repairs do not comply with requirements as determined by Architect.

3.5 CLEANING

A. Clean mortar, plaster, fireproofing, weld slag, and other deleterious material from concrete surfaces and adjacent materials immediately.

B. Clean exposed surfaces of precast concrete units after erection and completion of joint treatment to remove weld marks, other markings, dirt, and stains.

1. Perform cleaning procedures, if necessary, according to precast concrete fabricator's written recommendations. Protect other work from staining or damage due to cleaning operations.

2. Do not use cleaning materials or processes that could change the appearance of exposed concrete finishes or damage adjacent materials.

END OF SECTION 034100

	PRECAST STRUCTURAL CONCRETE
	034100 - 1



