Copyright 2010 AIA
MasterSpec Professional
05/10

Copyright 2010 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 054000 - COLD-FORMED METAL FRAMING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

1. Load-bearing wall framing.

2. Exterior non-load-bearing wall framing.

1.2 ACTION SUBMITTALS

A. Product Data: For each type of cold-formed steel framing product and accessory.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

C. Shop Drawings:

1. Include layout, spacings, sizes, thicknesses, and types of cold-formed steel framing; fabrication; and fastening and anchorage details, including mechanical fasteners.

2. Indicate reinforcing channels, opening framing, supplemental framing, strapping, bracing, bridging, splices, accessories, connection details, and attachment to adjoining work.

1.3 INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

A. Qualification Data: For testing agency.

B. Welding certificates.

C. Product test reports.

D. Research reports.

1.4 QUALITY ASSURANCE

A. Product Tests: Mill certificates or data from a qualified independent testing agency.

B. Welding Qualifications: Qualify procedures and personnel according to AWS D1.3/D1.3M, "Structural Welding Code - Sheet Steel."

Consider retaining paragraph below if Project is limited to one- and two-family residential construction, framing is fully detailed, and this AISI document is acceptable to authorities having jurisdiction.

C. Comply with AISI S230 "Standard for Cold-Formed Steel Framing - Prescriptive Method for One and Two Family Dwellings."

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 MANUFACTURERS

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

1. AllSteel & Gypsum Products, Inc.

2. California Expanded Metal Products Company.

3. ClarkWestern Building Systems, Inc.

4. Consolidated Fabricators Corp.; Building Products Division.

5. Craco Mfg., Inc.

6. Custom Stud Inc.

7. Design Shapes in Steel.

8. Dietrich Metal Framing; a Worthington Industries company.

9. Formetal Co. Inc. (The).

10. MarinoWARE.

11. MBA Building Supplies, Inc.

12. Nuconsteel; a Nucor Company.

13. Olmar Supply, Inc.

14. Quail Run Building Materials, Inc.

15. SCAFCO Corporation.

16. Southeastern Stud & Components, Inc.

17. State Building Products, Inc.

18. Steel Construction Systems.

19. Steel Network, Inc. (The).

20. Steel Structural Systems.

21. Steeler, Inc.

22. Super Stud Building Products, Inc.

23. Telling Industries, LLC.

24. United Metal Products, Inc.

25. United Steel Manufacturing.

26. <Insert manufacturer's name>.

2.2 PERFORMANCE REQUIREMENTS

A. AISI Specifications and Standards: Unless more stringent requirements are indicated, comply with AISI S100 and AISI S200.

Retain "Fire-Resistance Ratings" Paragraph below only if products specified are part of a fire-resistance-rated assembly. Indicate rating, testing agency, and testing agency's design designation on Drawings.

B. Fire-Resistance Ratings: Comply with ASTM E 119; testing by a qualified testing agency.

1. Indicate design designations from UL's "Fire Resistance Directory" or from the listings of another qualified testing agency.

2.3 COLD-FORMED STEEL FRAMING, GENERAL

Retain this article to supplement specific framing articles that follow.

Retain "Recycled Content of Steel Products" Paragraph below if required for LEED Credit MR 4. USGBC allows a default value of 25 percent to be used for steel, without documentation; higher percentages can be claimed if they are supported by appropriate documentation. The Steel Recycling Institute indicates that steel sheet typically has 23 percent postconsumer recycled content and 1.5 percent preconsumer recycled content.

A. Recycled Content of Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.

B. Steel Sheet: ASTM A 1003/A 1003M, Structural Grade, Type H, metallic coated, of grade and coating weight as follows:

Retain minimum grade requirements from options in "Grade" Subparagraph below. If more than one grade option is required, indicate location of each on Drawings.

1. Grade: [ST33H (ST230H)] [ST50H (ST340H)] [As required by structural performance] <Insert grade>.

Minimum coating requirement for Structural Grade, Type H steel is G60 (Z180) or equivalent. Retain first option in "Coating" Subparagraph below if ASTM A 1003/A 1003M's listing of minimum coating thicknesses is required. This minimum coating designation assumes normal exposure conditions and construction practices. When more severe exposure conditions are probable, for example, in coastal areas, consider specifying a heavier coating. BIA recommends G90 (Z275) coating for stud backup applications. Verify availability of heavier-coated steel. If more than one coating option is required, indicate location of each on Drawings.

2. Coating: [G60 (Z180), A60 (ZF180), AZ50 (AZ150), or GF30 (ZGF90)] [G90 (Z275) or equivalent] <Insert coating weight>.

Retain "Steel Sheet for (Vertical Deflection) (Drift) Clips" Paragraph below if applicable.

C. Steel Sheet for [Vertical Deflection] [Drift] Clips: ASTM A 653/A 653M, structural steel, zinc coated, of grade and coating as follows:

Retain grade requirements from options in "Grade" Subparagraph below.

1. Grade: [33 (230)] [50 (340), Class 1] [As required by structural performance].

2. Coating: [G60 (Z180)] [G90 (Z275)].

2.4 LOAD-BEARING WALL FRAMING

Retain this article if load-bearing steel studs are required. Distinguish location of axial load-bearing framing from exterior non-load-bearing wall framing here or on Drawings. Indicate stud and track web depth on Drawings or insert here.

A. Steel Studs: Manufacturer's standard C-shaped steel studs, of web depths indicated, punched, with stiffened flanges, and as follows:

Retain one steel thickness from "Minimum Base-Metal Thickness" Subparagraph below or revise to suit Project. Sequence corresponds to common thickness designators 33, 43, 54, 68, and 97 and obsolete 20-, 18-, 16-, 14-, and 12-gage designations. If retaining different thicknesses for different components, indicate locations here or in framing articles below.

1. Minimum Base-Metal Thickness: [0.0329 inch (0.84 mm)] [0.0428 inch (1.09 mm)] [0.0538 inch (1.37 mm)] [0.0677 inch (1.72 mm)] [0.0966 inch (2.45 mm)].

Flange widths vary with application. If sheathing or masonry ties are required, consider minimum flange width of 1-5/8 inches (41 mm). Sequence corresponds to common flange width designators 137, 162, 200, and 250.

2. Flange Width: [1-3/8 inches (35 mm)] [1-5/8 inches (41 mm)] [2 inches (51 mm)] [2-1/2 inches (63 mm)].

Indicate whether design is based on gross or effective section properties.

3. Section Properties: <Insert minimum allowable calculated section modulus, moment of inertia, and allowable moment>.

B. Steel Track: Manufacturer's standard U-shaped steel track, of web depths indicated, unpunched, with straight flanges, and matching minimum base-metal thickness of steel studs.

C. Steel Box or Back-to-Back Headers: Manufacturer's standard C-shapes used to form header beams, of web depths indicated, unpunched, with stiffened flanges, and as follows:

Retain one steel thickness from "Minimum Base-Metal Thickness" Subparagraph below or revise to suit Project. Sequence corresponds to common thickness designators 33, 43, 54, 68, and 97 and obsolete 20-, 18-, 16-, 14-, and 12-gage designations. If retaining different thicknesses for different locations, indicate locations here or in the framing articles below.

1. Minimum Base-Metal Thickness: [0.0329 inch (0.84 mm)] [0.0428 inch (1.09 mm)] [0.0538 inch (1.37 mm)] [0.0677 inch (1.72 mm)] [0.0966 inch (2.45 mm)].

Flange widths vary with application; coordinate with wall width.

2. Flange Width: [1-3/8 inches (35 mm)] [1-5/8 inches (41 mm)] [2 inches (51 mm)] [2-1/2 inches (63 mm)].

Indicate whether design is based on gross or effective section properties.

3. Section Properties: <Insert minimum allowable calculated section modulus, moment of inertia, and allowable moment>.

2.5 EXTERIOR NON-LOAD-BEARING WALL FRAMING

Retain this article if exterior non-load-bearing wall framing, sometimes called "curtain-wall" framing by manufacturers, is required. Indicate stud and track web depth on Drawings or insert here.

A. Steel Studs: Manufacturer's standard C-shaped steel studs, of web depths indicated, punched, with stiffened flanges, and as follows:

Retain one steel thickness from "Minimum Base-Metal Thickness" Subparagraph below or revise to suit Project. Sequence corresponds to common thickness designators 33, 43, 54, 68, and 97 and obsolete 20-, 18-, 16-, 14-, and 12-gage designations.

1. Minimum Base-Metal Thickness: [0.0329 inch (0.84 mm)] [0.0428 inch (1.09 mm)] [0.0538 inch (1.37 mm)] [0.0677 inch (1.72 mm)] [0.0966 inch (2.45 mm)].

Flange widths vary with application. If sheathing or masonry ties are required, consider minimum flange width of 1-5/8 inches (41 mm). Sequence corresponds to common flange width designators 137, 162, 200, and 250.

2. Flange Width: [1-3/8 inches (35 mm)] [1-5/8 inches (41 mm)] [2 inches (51 mm)] [2-1/2 inches (63 mm)].

Indicate whether design is based on gross or effective section properties.

3. Section Properties: <Insert minimum allowable calculated section modulus, moment of inertia, and allowable moment>.

B. Steel Track: Manufacturer's standard U-shaped steel track, of web depths indicated, unpunched, with unstiffened flanges, and matching minimum base-metal thickness of steel studs.

Retain "Vertical Deflection Clips," "Single Deflection Track," or "Double Deflection Tracks" Paragraph below for components to cope with vertical deflection of the primary structure.

Retain "Vertical Deflection Clips" Paragraph below if required; revise to add displacement if deflection of primary structure is not indicated.

C. Vertical Deflection Clips: Manufacturer's standard [bypass] [head] clips, capable of accommodating upward and downward vertical displacement of primary structure through positive mechanical attachment to stud web.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. AllSteel & Gypsum Products, Inc.

b. ClarkWestern Building Systems, Inc.

c. Dietrich Metal Framing; a Worthington Industries company.

d. MarinoWARE.

e. SCAFCO Corporation.

f. Steel Network, Inc. (The).

g. Steeler, Inc.

h. <Insert manufacturer's name>.

Retain "Single Deflection Track" Paragraph below if required. Revise description, as applicable, if limiting types of single-leg track.

D. Single Deflection Track: Manufacturer's single, deep-leg, U-shaped steel track; unpunched, with unstiffened flanges, of web depth to contain studs while allowing free vertical movement, with flanges designed to support horizontal loads and transfer them to the primary structure.

E. Double Deflection Tracks: Manufacturer's double, deep-leg, U-shaped steel tracks, consisting of nested inner and outer tracks; unpunched, with unstiffened flanges.

Retain "Drift Clips" Paragraph below if drift clips are required to accommodate horizontal and vertical deflection of the primary structure.

F. Drift Clips: Manufacturer's standard bypass or head clips, capable of isolating wall stud from upward and downward vertical displacement and lateral drift of primary structure through positive mechanical attachment to stud web and structure.

2.6 FRAMING ACCESSORIES

Revise minimum yield strength of accessories as required.

A. Fabricate steel-framing accessories from steel sheet, ASTM A 1003/A 1003M, Structural Grade, Type H, metallic coated, of same grade and coating weight used for framing members.

B. Provide accessories of manufacturer's standard thickness and configuration.

2.7 ANCHORS, CLIPS, AND FASTENERS

Delete "Steel Shapes and Clips" Paragraph below if rolled steel shapes and clips are not required or are specified in another Section.

A. Steel Shapes and Clips: ASTM A 36/A 36M, zinc coated by hot-dip process according to ASTM A 123/A 123M.

Retain grade of anchor bolt, head type, and type of protective coating from "Anchor Bolts" Paragraph below. Revise if using high-strength, low-alloy anchor bolts.

B. Anchor Bolts: ASTM F 1554, [Grade 36] [Grade 55], threaded carbon-steel [hex-headed bolts] [headless, hooked bolts] [headless bolts, with encased end threaded,] and carbon-steel nuts; and flat, hardened-steel washers; zinc coated by [hot-dip process according to ASTM A 153/A 153M, Class C] [mechanically deposition according to ASTM B 695, Class 50].

Retain "Expansion Anchors" Paragraph below if expansion anchors are acceptable. Verify safety factor with Project's structural engineer. Revise as required or insert specific load requirements and names of acceptable products.

C. Expansion Anchors: Fabricated from corrosion-resistant materials, with allowable load or strength design capacities calculated according to ICC-ES AC193 and ACI 318 greater than or equal to the design load, as determined by testing per ASTM E 488 conducted by a qualified testing agency.

Retain "Power-Actuated Anchors" Paragraph below if power-actuated fasteners are acceptable. Verify safety factor with Project's structural engineer.

D. Power-Actuated Anchors: Fastener system of type suitable for application indicated, fabricated from corrosion-resistant materials, with allowable load capacities calculated according to ICC-ES AC70, greater than or equal to the design load, as determined by testing per ASTM E 1190 conducted by a qualified testing agency.

E. Mechanical Fasteners: ASTM C 1513, corrosion-resistant-coated, self-drilling, self-tapping, steel drill screws.

1. Head Type: Low-profile head beneath sheathing, manufacturer's standard elsewhere.

2.8 MISCELLANEOUS MATERIALS

A. Galvanizing Repair Paint: [SSPC-Paint 20 or MIL-P-21035B] [ASTM A 780].

Retain appropriate grout from "Cement Grout" and "Nonmetallic, Nonshrink Grout" paragraphs below if concrete or masonry substrates require leveling before setting track or prefabricated assemblies.

B. Cement Grout: Portland cement, ASTM C 150, Type I; and clean, natural sand, ASTM C 404. Mix at ratio of 1 part cement to 2-1/2 parts sand, by volume, with minimum water required for placement and hydration.

C. Nonmetallic, Nonshrink Grout: Premixed, nonmetallic, noncorrosive, nonstaining grout containing selected silica sands, portland cement, shrinkage-compensating agents, and plasticizing and water-reducing agents, complying with ASTM C 1107/C 1107M, with fluid consistency and 30-minute working time.

D. Shims: Load bearing, high-density multimonomer plastic, and nonleaching; or of cold-formed steel of same grade and coating as framing members supported by shims.

E. Sealer Gaskets: Closed-cell neoprene foam, 1/4 inch (6.4 mm) thick, selected from manufacturer's standard widths to match width of bottom track or rim track members.

PART 3 -  EXECUTION

3.1 PREPARATION

Retain first paragraph below if bottom track of load-bearing walls requires a uniform-bearing surface on concrete or masonry construction.

A. Install load bearing shims or grout between the underside of load-bearing wall bottom track and the top of foundation wall or slab at locations with a gap larger than 1/4 inch (6 mm) to ensure a uniform bearing surface on supporting concrete or masonry construction.

Retain paragraph below if sealing the gap between framing and concrete or masonry construction.

B. Install sealer gaskets at the underside of wall bottom track or rim track and at the top of foundation wall or slab at stud or joist locations.

3.2 INSTALLATION, GENERAL

Retain this article with each specific framing classification in articles elsewhere below.

A. Cold-formed steel framing may be shop or field fabricated for installation, or it may be field assembled.

B. Install cold-formed steel framing according to AISI S200 and to manufacturer's written instructions unless more stringent requirements are indicated.

C. Install cold-formed steel framing and accessories plumb, square, and true to line, and with connections securely fastened.

D. Install framing members in one-piece lengths.

E. Install temporary bracing and supports to secure framing and support loads comparable in intensity to those for which structure was designed. Maintain braces and supports in place, undisturbed, until entire integrated supporting structure has been completed and permanent connections to framing are secured.

Include details on Drawings showing expansion-joint construction and locations.

F. Do not bridge building expansion joints with cold-formed steel framing. Independently frame both sides of joints.

Retain first paragraph below if insulation for exterior framing is required.

G. Install insulation, specified in Section 072100 "Thermal Insulation," in built-up exterior framing members, such as headers, sills, boxed joists, and multiple studs at openings, that are inaccessible on completion of framing work.

H. Fasten hole reinforcing plate over web penetrations that exceed size of manufacturer's approved or standard punched openings.

Revise "Erection Tolerances" Paragraph below to suit Project. Coordinate with limitations of subsequent finish materials.

I. Erection Tolerances: Install cold-formed steel framing level, plumb, and true to line to a maximum allowable tolerance variation of 1/8 inch in 10 feet (1:960) and as follows:

1. Space individual framing members no more than plus or minus 1/8 inch (3 mm) from plan location. Cumulative error shall not exceed minimum fastening requirements of sheathing or other finishing materials.

3.3 LOAD-BEARING WALL INSTALLATION

If this article is required, retain with "Installation, General" Article.

A. Install continuous top and bottom tracks sized to match studs. Align tracks accurately and securely anchor at corners and ends, and at spacings as follows:

Retain option in "Anchor Spacing" Subparagraph below to suit requirements and type of anchor.

1. Anchor Spacing: [24 inches (610 mm)] [32 inches (813 mm)] [To match stud spacing] [As shown on Shop Drawings].

B. Squarely seat studs against top and bottom tracks with gap not exceeding of 1/8 inch (3 mm) between the end of wall framing member and the web of track. Fasten both flanges of studs to top and bottom tracks. Space studs as follows:

1. Stud Spacing: [12 inches (305 mm)] [16 inches (406 mm)] [19.2 inches (488 mm)] [24 inches (610 mm)] [As indicated].

C. Set studs plumb, except as needed for diagonal bracing or required for nonplumb walls or warped surfaces and similar configurations.

D. Align studs vertically where floor framing interrupts wall-framing continuity. Where studs cannot be aligned, continuously reinforce track to transfer loads.

E. Align floor and roof framing over studs. Where framing cannot be aligned, continuously reinforce track to transfer loads.

F. Anchor studs abutting structural columns or walls, including masonry walls, to supporting structure as indicated.

G. Install headers over wall openings wider than stud spacing. Locate headers above openings as indicated. Fabricate headers of compound shapes indicated or required to transfer load to supporting studs, complete with clip-angle connectors, web stiffeners, or gusset plates.

1. Frame wall openings with not less than a double stud at each jamb of frame as indicated on Shop Drawings. Fasten jamb members together to uniformly distribute loads.

2. Install runner tracks and jack studs above and below wall openings. Anchor tracks to jamb studs with clip angles or by welding, and space jack studs same as full-height wall studs.

H. Install supplementary framing, blocking, and bracing in stud framing indicated to support fixtures, equipment, services, casework, heavy trim, furnishings, and similar work requiring attachment to framing.

1. If type of supplementary support is not indicated, comply with stud manufacturer's written recommendations and industry standards in each case, considering weight or load resulting from item supported.

Retain spacing of bridging from options in first paragraph below or revise to suit Project.

I. Install horizontal bridging in stud system, spaced vertically [48 inches (1220 mm)] [as indicated] [as indicated on Shop Drawings]. Fasten at each stud intersection.

Retain type of bridging required from three "Bridging" subparagraphs below or revise to suit Project. Insert locations if more than one type of bridging is required. Insert minimum size of flat steel strap, such as 1-1/2 by 0.0329 inch (38 by 0.84 mm), if default size is required.

1. Bridging: Cold-rolled steel channel, welded or mechanically fastened to webs of punched studs with a minimum of two screws into each flange of the clip angle for framing members up to 6 inches (150 mm) deep.

2. Bridging: Combination of flat, taut, steel sheet straps of width and thickness indicated and stud-track solid blocking of width and thickness to match studs. Fasten flat straps to stud flanges and secure solid blocking to stud webs or flanges.

3. Bridging: Proprietary bridging bars installed according to manufacturer's written instructions.

Retain first paragraph below only if required. Revise bracing type and reinforcement at terminations to suit Project. Description below usually applies to shear walls. Insert track reinforcing or gusset plate requirements to Drawings if applicable, particularly for shear walls. If sheathing provides bracing to one or both stud flanges, revise to suit Project.

J. Install steel sheet diagonal bracing straps to both stud flanges, terminate at and fasten to reinforced top and bottom tracks. Fasten clip-angle connectors to multiple studs at ends of bracing and anchor to structure.

K. Install miscellaneous framing and connections, including supplementary framing, web stiffeners, clip angles, continuous angles, anchors, and fasteners, to provide a complete and stable wall-framing system.

3.4 EXTERIOR NON-LOAD-BEARING WALL INSTALLATION

If this article is required, retain with "Installation, General" Article.

A. Install continuous tracks sized to match studs. Align tracks accurately and securely anchor to supporting structure as indicated.

Retain fastening of studs to top track only if required. Do not fasten studs to deflection track, such as in infill wall framing.

B. Fasten both flanges of studs to[ top and] bottom track unless otherwise indicated. Space studs as follows:

1. Stud Spacing: [12 inches (305 mm)] [16 inches (406 mm)] [19.2 inches (488 mm)] [24 inches (610 mm)] [As indicated].

C. Set studs plumb, except as needed for diagonal bracing or required for nonplumb walls or warped surfaces and similar requirements.

Indicate isolation details on Drawings or insert detailed description here.

D. Isolate non-load-bearing steel framing from building structure to prevent transfer of vertical loads while providing lateral support.

Retain one of first two subparagraphs below if using deflection track with infill wall framing. Delete both subparagraphs and retain third if deflection clips are required for bypassing or infill wall framing. Vertical deflection clips are used if wall is stick built or panelized. Single deflection track is used if stud wall is stick built; double deflection track is used with wall panels. Drift clips may be used in seismic areas.

1. Install single deep-leg deflection tracks and anchor to building structure.

2. Install double deep-leg deflection tracks and anchor outer track to building structure.

3. Connect vertical deflection clips to [bypassing] [infill] studs and anchor to building structure.

4. Connect drift clips to cold-formed metal framing and anchor to building structure.

E. Install horizontal bridging in wall studs, spaced vertically in rows indicated on Shop Drawings but not more than 48 inches (1220 mm) apart. Fasten at each stud intersection.

Retain "Top Bridging for Single Deflection Track" Subparagraph below if required.

1. Top Bridging for Single Deflection Track: Install row of horizontal bridging within [12 inches (305 mm)] [18 inches (450 mm)] of single deflection track. Install a combination of bridging and stud or stud-track solid blocking of width and thickness matching studs, secured to stud webs or flanges.

a. Install solid blocking at [96-inch (2440-mm) centers] [centers indicated] [centers indicated on Shop Drawings].

Retain type of bridging required from three "Bridging" subparagraphs below or revise to suit Project. Insert locations if more than one type of bridging is required. Insert minimum size of flat steel strap, such as 1-1/2 by 0.0329 inch (38 by 0.84 mm), if default size is required.

2. Bridging: Cold-rolled steel channel, welded or mechanically fastened to webs of punched studs.

3. Bridging: Combination of flat, taut, steel sheet straps of width and thickness indicated and stud-track solid blocking of width and thickness to match studs. Fasten flat straps to stud flanges and secure solid blocking to stud webs or flanges.

4. Bridging: Proprietary bridging bars installed according to manufacturer's written instructions.

F. Install miscellaneous framing and connections, including stud kickers, web stiffeners, clip angles, continuous angles, anchors, and fasteners, to provide a complete and stable wall-framing system.

3.5 FIELD QUALITY CONTROL

Retain this article if field testing and inspecting are required. Provisions below include shop and field testing and inspecting. Revise and insert a "Source Quality Control" Article to end of Part 2 if separate shop and field testing and inspecting are required. Revise "Testing" Paragraph below to include code-mandated special inspections or revise if Contractor engages testing agency.

A. Testing: Owner will engage a qualified independent testing and inspecting agency to perform field tests and inspections and prepare test reports.

B. Field and shop welds will be subject to testing and inspecting.

C. Testing agency will report test results promptly and in writing to Contractor and Architect.

D. Remove and replace work where test results indicate that it does not comply with specified requirements.

E. Additional testing and inspecting, at Contractor's expense, will be performed to determine compliance of replaced or additional work with specified requirements.

3.6 REPAIRS AND PROTECTION

Retain "Galvanizing Repairs" Paragraph below if applicable.

A. Galvanizing Repairs: Prepare and repair damaged galvanized coatings on fabricated and installed cold-formed steel framing with galvanized repair paint according to ASTM A 780 and manufacturer's written instructions.

B. Provide final protection and maintain conditions, in a manner acceptable to manufacturer and Installer, that ensure that cold-formed steel framing is without damage or deterioration at time of Substantial Completion.

END OF SECTION 054000

	COLD-FORMED METAL FRAMING
	054000 - 1



