Copyright 2012 AIA
MasterSpec Professional
02/12

Copyright 2012 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 055000 - METAL FABRICATIONS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section Includes:

Note that some items in list below are not described in detail in Part 2. These items are covered by material requirements and articles such as "Miscellaneous Framing and Supports," but they must be indicated in detail on Drawings. Also note that steel framing, supports, elevator machine beams, hoist beams, divider beams, and door frames that are attached to steel frame are specified in Section 051200 "Structural Steel Framing."

1. Miscellaneous steel framing and supports.

Retain first subparagraph below if prefabricated columns are not specified in Section 051200 "Structural Steel Framing."

2. Prefabricated building columns.

3. Shelf angles.

Retain first subparagraph below for elevator pit ladders and other metal ladders.

4. Metal ladders.

5. Ladder safety cages.

6. Metal floor plate[ and supports].

7. Elevator pit sump covers.

8. Structural-steel door frames.

9. Miscellaneous steel trim.

10. Metal bollards.

11. Wire rope parking garage guards.

12. [Pipe] [Downspout] guards.

Delete first subparagraph below if nosings and treads are specified with stairs and if cast-metal thresholds are specified with hardware.

13. Abrasive metal [nosings] [treads] [and] [thresholds].

Retain subparagraph below if bearing and leveling plates are not specified with items that they support.

14. Loose bearing and leveling plates.

B. Products furnished, but not installed, under this Section include the following:

1. Loose steel lintels.

2. Anchor bolts, steel pipe sleeves, slotted-channel inserts, and wedge-type inserts indicated to be cast into concrete or built into unit masonry.

Retain subparagraph below if weld plates and angles are not specified in same Section as work that is welded to them.

3. Steel weld plates and angles for casting into concrete for applications where they are not specified in other Sections.

1.2 ACTION SUBMITTALS

A. Product Data: For the following:

1. Prefabricated building columns.

2. Metal nosings and treads.

3. Paint products.

4. Grout.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Laboratory Test Reports for Credit IEQ 4.2" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit IEQ 4.2: For primers, documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's (formerly, the California Department of Health Services') "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Small-Scale Environmental Chambers."

C. Shop Drawings: Show fabrication and installation details.[ Include plans, elevations, sections, and details of metal fabrications and their connections. Show anchorage and accessory items.]

D. Samples for Verification: For each type and finish of extruded [nosing] [and] [tread].

Retain "Delegated-Design Submittal" Paragraph below if design services have been delegated to Contractor.

E. Delegated-Design Submittal: For ladders, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Delegated Design" Paragraph below if Contractor is required to assume responsibility for design.

A. Delegated Design: Engage a qualified professional engineer, as defined in Section 014000 "Quality Requirements," to design ladders.

Generally retain "Structural Performance of Aluminum Ladders" Paragraph below for aluminum ladders unless Project's structural engineer is required to design building components. Delete if sizes of ladder components are specified or indicated on Drawings.

B. Structural Performance of Aluminum Ladders: Aluminum ladders[, including landings,] shall withstand the effects of loads and stresses within limits and under conditions specified in ANSI A14.3.

"Thermal Movements" Paragraph below is for exterior metalwork; revise to suit Project conditions and metalwork exposure.

C. Thermal Movements: Allow for thermal movements from ambient and surface temperature changes acting on exterior metal fabrications by preventing buckling, opening of joints, overstressing of components, failure of connections, and other detrimental effects.

Differential values in "Temperature Change" Subparagraph below (for aluminum in particular) are suitable for most of the U.S.

1. Temperature Change: [120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces] <Insert temperature change>.

2.2 METALS

A. Metal Surfaces, General: Provide materials with smooth, flat surfaces unless otherwise indicated. For metal fabrications exposed to view in the completed Work, provide materials without seam marks, roller marks, rolled trade names, or blemishes.

Retain "Recycled Content of Steel Products" Paragraph below if required for LEED Credit MR 4. USGBC allows a default value of 25 percent to be used for steel without documentation; higher percentages can be claimed if they are supported by appropriate documentation. The Steel Recycling Institute indicates that hollow structural shapes and steel plates typically have 23 percent postconsumer recycled content and 1.5 percent preconsumer recycled content; rolled structural shapes typically have 57.5 percent postconsumer recycled content and 6.5 percent preconsumer recycled content.

B. Recycled Content of Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.

C. Steel Plates, Shapes, and Bars: ASTM A 36/A 36M.

Usually retain Type 304 in "Stainless-Steel Bars and Shapes" Paragraph below; Type 316L is for corrosive environments.

D. Stainless-Steel Bars and Shapes: ASTM A 276, [Type 304] [Type 316L].

"Rolled-Steel Floor Plate" Paragraph below specifies yield strength of 30 ksi (205 MPa); revise if higher strength is required.

E. Rolled-Steel Floor Plate: ASTM A 786/A 786M, rolled from plate complying with ASTM A 36/A 36M or ASTM A 283/A 283M, Grade C or D.

F. Rolled-Stainless-Steel Floor Plate: ASTM A 793.

G. Abrasive-Surface Floor Plate: Steel plate [with abrasive granules rolled into surface] [or] [with abrasive material metallically bonded to steel].

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

Products in list below have abrasive material metallically bonded to steel.

a. IKG Industries, a division of Harsco Corporation; Mebac.

b. SlipNOT Metal Safety Flooring; SlipNOT.

c. <Insert manufacturer's name; product name or designation>.

Round steel tubing and pipe are sized differently. Pipe is designated by the terms "nominal pipe size (NPS)" in inches or "diameter nominal (DN)" in millimeters, and by "weight" or "schedule number." The NPS is approximately equal to the ID for Schedule 40 or Standard Weight pipe; the DN is a rounded conversion of the NPS. For other weights, the size is neither OD nor ID because the OD is kept the same for all weights (to allow use of the same pipe fittings) and the ID is varied to provide the required wall thickness. Round tube is designated by OD and wall thickness. Although the size designations are different, only the round tube sizes that match pipe sizes are generally available.

H. Steel Tubing: ASTM A 500/A 500M, cold-formed steel tubing.

I. Steel Pipe: ASTM A 53/A 53M, Standard Weight (Schedule 40) unless otherwise indicated.

J. Zinc-Coated Steel Wire Rope: ASTM A 741.

1. Wire-Rope Fittings: Hot-dip galvanized-steel connectors with capability to sustain, without failure, a load equal to minimum breaking strength of wire rope with which they are used.

"Slotted Channel Framing" Paragraph below describes typical component of metal channel framing systems such as that manufactured by Unistrut.

K. Slotted Channel Framing: Cold-formed metal box channels (struts) complying with MFMA-4.

1. Size of Channels: [1-5/8 by 1-5/8 inches (41 by 41 mm)] [As indicated] <Insert size>.

Metal thicknesses in "Material" subparagraphs below are 12, 14, and 16 gage, respectively.

2. Material: Galvanized steel, ASTM A 653/A 653M, [commercial steel, Type B] [structural steel, Grade 33 (Grade 230)], with G90 (Z275) coating; [0.108-inch (2.8-mm)] [0.079-inch (2-mm)] [0.064-inch (1.6-mm)] nominal thickness.

3. Material: Cold-rolled steel, ASTM A 1008/A 1008M, [commercial steel, Type B] [structural steel, Grade 33 (Grade 230)]; [0.0966-inch (2.5-mm)] [0.0677-inch (1.7-mm)] [0.0528-inch (1.35-mm)] minimum thickness; [unfinished] [coated with rust-inhibitive, baked-on, acrylic enamel] [hot-dip galvanized after fabrication].

L. Cast Iron: Either gray iron, ASTM A 48/A 48M, or malleable iron, ASTM A 47/A 47M, unless otherwise indicated.

M. Aluminum Extrusions: ASTM B 221 (ASTM B 221M), Alloy 6063-T6.

N. Aluminum-Alloy Rolled Tread Plate: ASTM B 632/B 632M, Alloy 6061-T6.

O. Aluminum Castings: ASTM B 26/B 26M, Alloy 443.0-F.

P. Bronze Extrusions: ASTM B 455, Alloy UNS No. C38500 (extruded architectural bronze).

Q. Bronze Castings: ASTM B 584, Alloy UNS No. C83600 (leaded red brass) or No. C84400 (leaded semired brass).

R. Nickel Silver Castings: ASTM B 584, Alloy UNS No. C97600 (20 percent leaded nickel bronze).

2.3 FASTENERS

Usually retain Type 304 in "General" Paragraph below; retain Type 316 if required for corrosive environments.

A. General: Unless otherwise indicated, provide [Type 304] [Type 316] stainless-steel fasteners for exterior use and zinc-plated fasteners with coating complying with ASTM B 633 or ASTM F 1941 (ASTM F 1941M), Class Fe/Zn 5, at exterior walls. Select fasteners for type, grade, and class required.

1. Provide stainless-steel fasteners for fastening aluminum.

2. Provide stainless-steel fasteners for fastening stainless steel.

3. Provide stainless-steel fasteners for fastening nickel silver.

4. Provide bronze fasteners for fastening bronze.

B. Cast-in-Place Anchors in Concrete: Either threaded type or wedge type unless otherwise indicated; galvanized ferrous castings, either ASTM A 47/A 47M malleable iron or ASTM A 27/A 27M cast steel. Provide bolts, washers, and shims as needed, all hot-dip galvanized per ASTM F 2329.

C. Post-Installed Anchors: [Torque-controlled expansion anchors] [or] [chemical anchors].

Material in "Material for Interior Locations" Subparagraph below protects against corrosion in an indoor atmosphere.

1. Material for Interior Locations: Carbon-steel components zinc plated to comply with ASTM B 633 or ASTM F 1941 (ASTM F 1941M), Class Fe/Zn 5, unless otherwise indicated.

First option in "Material for Exterior Locations and Where Stainless Steel Is Indicated" Subparagraph below refers to Type 304 and similar alloys; second option refers to Type 316 and similar alloys.

2. Material for Exterior Locations and Where Stainless Steel Is Indicated: Alloy [Group 1 (A1)] [Group 2 (A4)] stainless-steel bolts, ASTM F 593 (ASTM F 738M), and nuts, ASTM F 594 (ASTM F 836M).

Retain "Slotted-Channel Inserts" Paragraph below if required for supporting elevator guide rails or other items on masonry or concrete walls.

D. Slotted-Channel Inserts: Cold-formed, hot-dip galvanized-steel box channels (struts) complying with MFMA-4, 1-5/8 by 7/8 inches (41 by 22 mm) by length indicated with anchor straps or studs not less than 3 inches (75 mm) long at not more than 8 inches (200 mm) o.c. Provide with temporary filler and tee-head bolts, complete with washers and nuts, all zinc-plated to comply with ASTM B 633, Class Fe/Zn 5, as needed for fastening to inserts.

2.4 MISCELLANEOUS MATERIALS

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools.

A. Low-Emitting Materials: Paints and coatings shall comply with the testing and product requirements of the California Department of Public Health's (formerly, the California Department of Health Services') "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain one or more of "Shop Primers," "Universal Shop Primer," and "Water-Based Primer" paragraphs below. Second paragraph specifies a typical primer for painted finishes that provides minimum protection to steel. Third paragraph specifies a typical primer for high-performance coating. If retaining both, indicate on Drawings or in a schedule where each is required.

B. Shop Primers: Provide primers that comply with [Section 099113 "Exterior Painting."] [Section 099123 Interior Painting."] [Section 099600 "High-Performance Coatings."] [Section 099113 "Exterior Painting," Section 099123 Interior Painting," and Section 099600 "High-Performance Coatings."]

C. Universal Shop Primer: Fast-curing, lead- and chromate-free, universal modified-alkyd primer complying with MPI#79 and compatible with topcoat.

1. Use primer containing pigments that make it easily distinguishable from zinc-rich primer.

D. Water-Based Primer: Emulsion type, anticorrosive primer for mildly corrosive environments that is resistant to flash rusting when applied to cleaned steel, complying with MPI#107 and compatible with topcoat.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

E. Epoxy Zinc-Rich Primer: Complying with MPI#20 and compatible with topcoat.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. <Insert, in separate subparagraphs, manufacturer's name; product name or designation>.

F. Galvanizing Repair Paint: High-zinc-dust-content paint complying with SSPC-Paint 20 and compatible with paints specified to be used over it.

G. Bituminous Paint: Cold-applied asphalt emulsion complying with ASTM D 1187/D 1187M.

H. Nonshrink, Nonmetallic Grout: Factory-packaged, nonstaining, noncorrosive, nongaseous grout complying with ASTM C 1107/C 1107M. Provide grout specifically recommended by manufacturer for interior and exterior applications.

Retain "Concrete" Paragraph below if required for concrete-filled bollards, footings for bollards, or wheel guards.

I. Concrete: Comply with requirements in Section 033000 "Cast-in-Place Concrete" for normal-weight, air-entrained, concrete with a minimum 28-day compressive strength of 3000 psi (20 MPa).

2.5 FABRICATION, GENERAL

A. Shop Assembly: Preassemble items in the shop to greatest extent possible. Use connections that maintain structural value of joined pieces.

B. Cut, drill, and punch metals cleanly and accurately. Remove burrs and ease edges. Remove sharp or rough areas on exposed surfaces.

C. Weld corners and seams continuously to comply with the following:

1. Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

2. Obtain fusion without undercut or overlap.

3. Remove welding flux immediately.

4. At exposed connections, finish exposed welds and surfaces smooth and blended.

D. Form exposed connections with hairline joints, flush and smooth, using concealed fasteners or welds where possible. Locate joints where least conspicuous.

E. Fabricate seams and other connections that are exposed to weather in a manner to exclude water. Provide weep holes where water may accumulate.

F. Where units are indicated to be cast into concrete or built into masonry, equip with integrally welded steel strap anchors not less than 8 inches (200 mm) from ends and corners of units and 24 inches (600 mm) o.c.

First 14 articles below specify fabrication requirements for typical metal fabrications; revise those retained to suit Project and insert others as required. Not all metal fabrications require separate fabrication articles but instead rely on the general requirements above and details indicated on Drawings.

2.6 MISCELLANEOUS FRAMING AND SUPPORTS

A. General: Provide steel framing and supports not specified in other Sections as needed to complete the Work.

B. Fabricate units from steel shapes, plates, and bars of welded construction unless otherwise indicated. Fabricate to sizes, shapes, and profiles indicated and as necessary to receive adjacent construction.

Revise first paragraph below if girders are spliced. Add ASTM A 325 (ASTM A 325M) bolts to "Fasteners" Article if required for splicing or for connecting to pipe columns.

C. Fabricate steel girders for wood frame construction from continuous steel shapes of sizes indicated.

Delete subparagraph below if nailers are not used or are fastened with powder-actuated fasteners.

1. Where wood nailers are attached to girders with bolts or lag screws, drill or punch holes at 24 inches (600 mm) o.c.

Revise paragraph below if tubing is used. Revise default weld size requirement, or delete and detail welds on Drawings to suit Project.

D. Fabricate steel pipe columns for supporting wood frame construction from steel pipe with steel baseplates and top plates as indicated. Drill or punch baseplates and top plates for anchor and connection bolts and weld to pipe with fillet welds all around. Make welds the same size as pipe wall thickness unless otherwise indicated.

2.7 PREFABRICATED BUILDING COLUMNS

Delete this article if prefabricated building columns are specified in Section 051200 "Structural Steel Framing."

Retain "Manufacturers" Paragraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

A. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

1. Black Rock Column, Inc.

2. Dean Lally L.P.

3. Dean, George H., Inc.

4. <Insert manufacturer's name>.

B. General: Provide prefabricated building columns consisting of load-bearing structural-steel members protected by concrete fireproofing encased in an outer non-load-bearing steel shell. Fabricate connections to comply with details shown or as needed to suit type of structure indicated.

C. Fire-Resistance Ratings: Provide prefabricated building columns listed and labeled by a testing and inspecting agency acceptable to authorities having jurisdiction for ratings indicated, based on testing according to ASTM E 119.

Insert UL design number here or indicate on Drawings if required.

1. Fire-Resistance Rating: [4 hours] [3 hours] [2 hours] [As indicated].

2.8 SHELF ANGLES

Retain this article for angles supported from concrete frame. Angles connected to structural-steel framing are specified in Section 051200 "Structural Steel Framing."

A. Fabricate shelf angles from steel angles of sizes indicated and for attachment to concrete framing. Provide horizontally slotted holes to receive 3/4-inch (19-mm) bolts, spaced not more than 6 inches (150 mm) from ends and 24 inches (600 mm) o.c., unless otherwise indicated.

B. For cavity walls, provide vertical channel brackets to support angles from backup masonry and concrete.

C. Galvanize shelf angles located in exterior walls.

D. Prime shelf angles located in exterior walls with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

Retain paragraph below if inserts are not specified in Section 033000 "Cast-in-Place Concrete."

E. Furnish wedge-type concrete inserts, complete with fasteners, to attach shelf angles to cast-in-place concrete.

2.9 METAL LADDERS

A. General:

ANSI A14.3 specifies minimum design requirements for ladders and safety cages.

1. Comply with ANSI A14.3[, except for elevator pit ladders].

2. For elevator pit ladders, comply with ASME A17.1/CSA B44.

B. Steel Ladders:

Delete first subparagraph below if spacing is indicated on Drawings or if minimum spacing in referenced standards is acceptable. ANSI A14.3 and ASME A17.1/CSA B44 minimum spacing is 16 inches (406 mm).

1. Space siderails [16 inches (406 mm)] [18 inches (457 mm)] apart unless otherwise indicated.

First option in "Siderails" Subparagraph below is ANSI A14.3 minimum dimension for normal atmospheric exposures; second is minimum for unusual atmospheric exposures.

2. Siderails: Continuous, [3/8-by-2-1/2-inch (9.5-by-64-mm)] [1/2-by-2-1/2-inch (12.7-by-64-mm)] steel flat bars, with eased edges.

First option in "Rungs" Subparagraph below is ANSI A14.3 minimum dimension for normal atmospheric exposures; second is minimum for unusually corrosive atmospheric exposures.

3. Rungs: [3/4-inch- (19-mm-) diameter] [3/4-inch- (19-mm-) square] [1-inch- (25-mm-) diameter] [1-inch- (25-mm-) square] steel bars.

4. Fit rungs in centerline of siderails; plug-weld and grind smooth on outer rail faces.

5. Provide nonslip surfaces on top of each rung.

6. Galvanize [exterior ]ladders, including brackets.

7. Prime [exterior ]ladders, including brackets and fasteners, with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

C. Aluminum Ladders:

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. ACL Industries, Inc.

b. Alco-Lite Industrial Products.

c. Halliday Products.

d. O'Keeffe's Inc.

e. Precision Ladders, LLC.

f. Royalite Manufacturing, Inc.

g. Thompson Fabricating, LLC.

h. <Insert manufacturer's name>.

Delete first subparagraph below if spacing is indicated on Drawings or if minimum spacing in referenced standards is acceptable. ANSI A14.3 and ASME A17.1/CSA B44 minimum spacing is 16 inches (406 mm).

2. Space siderails [16 inches (406 mm)] [18 inches (457 mm)] apart unless otherwise indicated.

3. Siderails: Continuous extruded-aluminum channels or tubes, not less than 2-1/2 inches (64 mm) deep, 3/4 inch (19 mm) wide, and 1/8 inch (3.2 mm) thick.

4. Rungs: Extruded-aluminum tubes, not less than 3/4 inch (19 mm) deep and not less than 1/8 inch (3.2 mm) thick, with ribbed tread surfaces.

2.10 LADDER SAFETY CAGES

ANSI A14.3 requires safety cages for ladders longer than 24 feet (7.3 m) unless a ladder safety system is provided. OSHA regulations require cages for ladders longer than 20 feet (6 m).

A. Fabricate ladder safety cages to comply with ANSI A14.3. Assemble by welding or with stainless-steel fasteners.

B. Provide primary hoops at tops and bottoms of cages and spaced not more than 20 feet (6 m) o.c. Provide secondary intermediate hoops spaced not more than 48 inches (1200 mm) o.c. between primary hoops.

C. Galvanize steel ladder safety cages, including brackets and fasteners.

D. Prime steel ladder safety cages, including brackets and fasteners, with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

2.11 METAL FLOOR PLATE

A. Fabricate from [rolled-steel floor] [rolled-stainless-steel floor] [rolled-aluminum-alloy tread] [abrasive-surface floor] plate of thickness indicated below:

1. Thickness: [1/8 inch (3.2 mm)] [3/16 inch (4.8 mm)] [1/4 inch (6.4 mm)] [5/16 inch (8 mm)] [3/8 inch (9.5 mm)] [As indicated].

B. Provide [steel] [stainless-steel] [aluminum] angle supports as indicated.

C. Provide flush [steel] [stainless-steel] [aluminum] bar drop handles for lifting removable sections, one at each end of each section.

2.12 ELEVATOR PIT SUMP COVERS

A. Fabricate from [1/8-inch (3.2-mm)] [3/16-inch (4.8-mm)] [rolled-steel floor] [abrasive-surface floor] plate with four 1-inch- (25-mm-) diameter holes for water drainage and for lifting.

2.13 STRUCTURAL-STEEL DOOR FRAMES

Retain this article for structural-steel door frames built into masonry or concrete walls and not attached to structural-steel building frame. Door frames connected to structural-steel framing are specified in Section 051200 "Structural Steel Framing."

A. Fabricate structural-steel door frames from steel shapes, plates, and bars of size and to dimensions indicated, fully welded together, with 5/8-by-1-1/2-inch (16-by-38-mm) steel channel stops. Plug-weld built-up members and continuously weld exposed joints. Reinforce frames and drill and tap as necessary to accept finish hardware.

1. Provide with integrally welded steel strap anchors for securing door frames into adjoining concrete or masonry.

B. Galvanize [exterior ]steel frames.

C. Prime [exterior ]steel frames with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

2.14 MISCELLANEOUS STEEL TRIM

A. Unless otherwise indicated, fabricate units from steel shapes, plates, and bars of profiles shown with continuously welded joints and smooth exposed edges. Miter corners and use concealed field splices where possible.

B. Provide cutouts, fittings, and anchorages as needed to coordinate assembly and installation with other work.

C. Galvanize [exterior ]miscellaneous steel trim.

D. Prime [exterior ]miscellaneous steel trim with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

2.15 METAL BOLLARDS

Usually retain Schedule 40 steel pipe in first paragraph below. Schedule 80 is suitable for security applications.

A. Fabricate metal bollards from [Schedule 40 steel pipe] [Schedule 80 steel pipe] [1/4-inch (6.4-mm) wall-thickness rectangular steel tubing] [steel shapes, as indicated].

Retain subparagraph below if required; delete if bollards are concrete filled.

1. Cap bollards with 1/4-inch- (6.4-mm-) thick steel plate.

Retain first paragraph below if required for mounting bollards on structural slab or on existing pavement.

B. Fabricate bollards with 3/8-inch- (9.5-mm-) thick steel baseplates for bolting to concrete slab. Drill baseplates at all four corners for 3/4-inch (19-mm) anchor bolts.

C. Fabricate sleeves for bollard anchorage from steel [pipe] [or] [tubing] with 1/4-inch- (6.4-mm-) thick steel plate welded to bottom of sleeve.

D. Prime bollards with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

2.16 WIRE ROPE PARKING GARAGE GUARDS

A. Wire Rope Parking Garage Guards: 3/4-inch- (19-mm-) diameter, zinc-coated steel wire ropes with wire rope fittings for securing to parking garage columns and walls and for tightening wire rope.

2.17 [PIPE] [DOWNSPOUT] GUARDS

First paragraph below is an example of pipe or downspout protection for building exteriors, parking garages, and other locations where subject to damage by vehicles.

A. Fabricate [pipe] [downspout] guards from 3/8-inch- (9.5-mm-) thick by 12-inch- (300-mm-) wide steel plate, bent to fit flat against the wall or column at both ends and to fit around pipe with 2-inch (50-mm) clearance between pipe and pipe guard. Drill each end for two 3/4-inch (19-mm) anchor bolts.

B. Galvanize [pipe] [downspout] guards.

C. Prime [pipe] [downspout] guards with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

2.18 ABRASIVE METAL [NOSINGS] [TREADS] [AND] [THRESHOLDS]

A. Cast-Metal Units: Cast [iron] [aluminum] [bronze (leaded red or semired brass)] [nickel silver (leaded nickel bronze)], with an integral-abrasive, as-cast finish consisting of aluminum oxide, silicon carbide, or a combination of both.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Safety Tread Co., Inc.

b. Balco, Inc.

c. Barry Pattern & Foundry Co., Inc.

d. Granite State Casting Co.

e. Safe-T-Metal Company, Inc.

f. Wooster Products Inc.

g. <Insert manufacturer's name>.

B. Extruded Units: [Aluminum] [Bronze], with abrasive filler consisting of aluminum oxide, silicon carbide, or a combination of both, in an epoxy-resin binder.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

1. Manufacturers: Subject to compliance with requirements, [provide products by the following] [provide products by one of the following] [available manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following]:

a. ACL Industries, Inc.

b. American Safety Tread Co., Inc.

c. Amstep Products.

d. Armstrong Products, Inc.

e. Balco, Inc.

f. Granite State Casting Co.

g. Wooster Products Inc.

h. <Insert manufacturer's name>.

Retain one of two subparagraphs below.

2. Provide ribbed units, with abrasive filler strips projecting 1/16 inch (1.5 mm) above aluminum extrusion.

3. Provide solid-abrasive-type units without ribs.

Retain one of first two paragraphs below.

C. Provide anchors for embedding units in concrete, either integral or applied to units, as standard with manufacturer.

D. Drill for mechanical anchors and countersink. Locate holes not more than 4 inches (100 mm) from ends and not more than 12 inches (300 mm) o.c.

E. Apply bituminous paint to concealed surfaces of cast-metal units.

F. Apply clear lacquer to concealed surfaces of extruded units.

2.19 LOOSE BEARING AND LEVELING PLATES

A. Provide loose bearing and leveling plates for steel items bearing on masonry or concrete construction. Drill plates to receive anchor bolts and for grouting.

2.20 LOOSE STEEL LINTELS

A. Fabricate loose steel lintels from steel angles and shapes of size indicated for openings and recesses in masonry walls and partitions at locations indicated.

B. Galvanize loose steel lintels located in exterior walls.

C. Prime loose steel lintels located in exterior walls with [zinc-rich primer.] [primer specified in Section 099600 "High-Performance Coatings."]

2.21 STEEL WELD PLATES AND ANGLES

A. Provide steel weld plates and angles not specified in other Sections, for items supported from concrete construction as needed to complete the Work. Provide each unit with no fewer than two integrally welded steel strap anchors for embedding in concrete.

2.22 FINISHES, GENERAL

A. Finish metal fabrications after assembly.

2.23 STEEL AND IRON FINISHES

A. Galvanizing: Hot-dip galvanize items as indicated to comply with ASTM A 153/A 153M for steel and iron hardware and with ASTM A 123/A 123M for other steel and iron products.

B. Shop prime iron and steel items[ not indicated to be galvanized] unless they are to be embedded in concrete, sprayed-on fireproofing, or masonry, or unless otherwise indicated.

Delete subparagraph below if specifying only one shop primer.

1. Shop prime with [universal shop primer] [primers specified in Section 099113 "Exterior Painting"] [primers specified in Section 099123 "Interior Painting"] unless [zinc-rich primer is] [primers specified in Section 099600 "High-Performance Coatings" are] indicated.

C. Preparation for Shop Priming: Prepare surfaces to comply with [SSPC-SP 6/NACE No. 3, "Commercial Blast Cleaning."] [SSPC-SP 3, "Power Tool Cleaning."] [requirements indicated below:]

Retain or revise any of four subparagraphs below to suit Project service conditions of installed work. Insert other exposures and preparation requirements where applicable. See SSPC's painting manual.

1. Exterior Items: SSPC-SP 6/NACE No. 3, "Commercial Blast Cleaning."

2. Items Indicated to Receive Zinc-Rich Primer: SSPC-SP 6/NACE No. 3, "Commercial Blast Cleaning."

3. Items Indicated to Receive Primers Specified in Section 099600 "High-Performance Coatings": SSPC-SP 6/NACE No. 3, "Commercial Blast Cleaning."

4. Other Items: SSPC-SP 3, "Power Tool Cleaning."

D. Shop Priming: Apply shop primer to comply with SSPC-PA 1, "Paint Application Specification No. 1: Shop, Field, and Maintenance Painting of Steel," for shop painting.

PART 3 -  EXECUTION

3.1 INSTALLATION, GENERAL

A. Cutting, Fitting, and Placement: Perform cutting, drilling, and fitting required for installing metal fabrications. Set metal fabrications accurately in location, alignment, and elevation; with edges and surfaces level, plumb, true, and free of rack; and measured from established lines and levels.

B. Fit exposed connections accurately together to form hairline joints. Weld connections that are not to be left as exposed joints but cannot be shop welded because of shipping size limitations. Do not weld, cut, or abrade surfaces of exterior units that have been hot-dip galvanized after fabrication and are for bolted or screwed field connections.

C. Field Welding: Comply with the following requirements:

1. Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

2. Obtain fusion without undercut or overlap.

3. Remove welding flux immediately.

4. At exposed connections, finish exposed welds and surfaces smooth and blended so no roughness shows after finishing and contour of welded surface matches that of adjacent surface.

D. Fastening to In-Place Construction: Provide anchorage devices and fasteners where metal fabrications are required to be fastened to in-place construction.

E. Provide temporary bracing or anchors in formwork for items that are to be built into concrete, masonry, or similar construction.

Retain articles below if applicable to Project. Insert others where needed to specify requirements applicable to a specific item not covered under general installation requirements above. Not all metal fabrications require separate installation articles but instead rely on the general requirements above and details indicated on Drawings.

3.2 INSTALLING METAL BOLLARDS

A. Fill metal-capped bollards solidly with concrete and allow concrete to cure seven days before installing.

Retain one or more of first three paragraphs below for anchoring bollards.

B. Anchor bollards to existing construction with [expansion anchors] [anchor bolts] [through bolts]. Provide four 3/4-inch (19-mm) bolts at each bollard unless otherwise indicated.

C. Anchor bollards in concrete [with pipe sleeves preset and anchored into concrete] [in formed or core-drilled holes]. Fill annular space around bollard solidly with nonshrink grout.

First paragraph below can be used for bollards located in landscaping or unit pavers.

D. Anchor bollards in place with concrete footings. Place concrete and vibrate or tamp for consolidation. Support and brace bollards in position until concrete has cured.

Retain paragraph below if bollards do not have metal caps.

E. Fill bollards solidly with concrete, mounding top surface to shed water.

3.3 INSTALLING BEARING AND LEVELING PLATES

A. Clean concrete and masonry bearing surfaces of bond-reducing materials, and roughen to improve bond to surfaces. Clean bottom surface of plates.

B. Set bearing and leveling plates on wedges, shims, or leveling nuts. After bearing members have been positioned and plumbed, tighten anchor bolts. Do not remove wedges or shims but, if protruding, cut off flush with edge of bearing plate before packing with nonshrink grout. Pack grout solidly between bearing surfaces and plates to ensure that no voids remain.

3.4 ADJUSTING AND CLEANING

Retain first "Touchup Painting" Paragraph below if touchup painting is included in this Section. Retain second paragraph if it is specified in Section 099113 "Exterior Painting" or Section 099123 "Interior Painting." Revise reference if Section 099600 "High Performance Coatings" is used.

A. Touchup Painting: Immediately after erection, clean field welds, bolted connections, and abraded areas. Paint uncoated and abraded areas with the same material as used for shop painting to comply with SSPC-PA 1 for touching up shop-painted surfaces.

B. Galvanized Surfaces: Clean field welds, bolted connections, and abraded areas and repair galvanizing to comply with ASTM A 780/A 780M.

END OF SECTION 055000

	METAL FABRICATIONS
	055000 - 1



