Copyright 2012 AIA
MasterSpec Professional
02/12

Copyright 2012 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 055119 - METAL GRATING STAIRS
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes industrial-type, straight-run stairs with steel-grating treads and railings attached to metal grating stairs.

1.2 ACTION SUBMITTALS

A. Product Data: For metal grating stairs.

B. LEED Submittals:

1. Product Data for Credit MR 4: For products having recycled content, documentation indicating percentages by weight of postconsumer and preconsumer recycled content. Include statement indicating cost for each product having recycled content.

"Laboratory Test Reports for Credit IEQ 4.2" Subparagraph below applies to LEED for Schools.

2. Laboratory Test Reports for Credit IEQ 4.2: For primers, documentation indicating that products comply with the testing and product requirements of the California Department of Public Health's (formerly, the California Department of Health Services') "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

C. Shop Drawings: Include plans, elevations, sections, details, and attachments.

Retain "Delegated-Design Submittal" Paragraph below if design services have been delegated to Contractor.

D. Delegated-Design Submittal: For stairs, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 PERFORMANCE REQUIREMENTS

Retain "Delegated Design" Paragraph below if Contractor is required to assume responsibility for design.

A. Delegated Design: Engage a qualified professional engineer, as defined in Section 014000 "Quality Requirements," to design stairs[ and railings].

B. Structural Performance of Stairs: Metal stairs shall withstand the effects of gravity loads and the following loads and stresses within limits and under conditions indicated:

First three subparagraphs below are based on the International Building Code (IBC); revise to suit Project and to comply with requirements of authorities having jurisdiction.

1. Uniform Load: 100 lbf/sq. ft. (4.79 kN/sq. m).

2. Concentrated Load: 300 lbf (1.33 kN) applied on an area of 4 sq. in. (2580 sq. mm).

3. Uniform and concentrated loads need not be assumed to act concurrently.

4. Stair Framing: Capable of withstanding stresses resulting from railing loads in addition to loads specified above.

Retain "Seismic Performance of Stairs" Paragraph below for projects requiring seismic design. Model building codes and ASCE/SEI 7 establish criteria for buildings subject to earthquake motions. Verify requirements of authorities having jurisdiction.

C. Seismic Performance of Stairs: Metal stairs shall withstand the effects of earthquake motions determined according to [ASCE/SEI 7] <Insert requirement>.

1. Component Importance Factor: 1.5.

2.2 METALS

A. Metal Surfaces, General: Provide materials with smooth, flat surfaces unless otherwise indicated. For components exposed to view in the completed Work, provide materials without seam marks, roller marks, rolled trade names, or blemishes.

Retain "Recycled Content of Steel Products" Paragraph below if required for LEED Credit MR 4. The USGBC allows a default value of 25 percent to be used for steel without documentation; higher percentages can be claimed if they are supported by appropriate documentation. The Steel Recycling Institute indicates that hollow structural shapes and steel plates typically have 23 percent postconsumer recycled content and 1.5 percent preconsumer recycled content; rolled structural shapes typically have 57.5 percent postconsumer recycled content and 6.5 percent preconsumer recycled content.

B. Recycled Content of Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than [25] <Insert number> percent.

Retain material types, qualities, and grades in remaining paragraphs below that are indicated in Specifications or on Drawings. Insert or delete items to suit Project.

C. Steel Plates, Shapes, and Bars: ASTM A 36/A 36M.

"Rolled-Steel Floor Plate" Paragraph below specifies minimum yield point of 30 ksi (205 MPa); revise if higher strength is required.

D. Rolled-Steel Floor Plate: ASTM A 786/A 786M, rolled from plate complying with ASTM A 36/A 36M or ASTM A 283/A 283M, Grade C or D.

E. Steel Bars for Grating Treads: ASTM A 36/A 36M or steel strip, ASTM A 1011/A 1011M or ASTM A 1018/A 1018M.

F. Wire Rod for Grating Crossbars: ASTM A 510 (ASTM A 510M).

G. Cast Iron: Either gray iron, ASTM A 48/A 48M, or malleable iron, ASTM A 47/A 47M, unless otherwise indicated.

H. Cast-Abrasive Nosings: Cast iron, with an integral abrasive, as-cast finish consisting of aluminum oxide, silicon carbide, or a combination of both.

2.3 FASTENERS

A. Provide zinc-plated fasteners with coating complying with ASTM B 633 or ASTM F 1941 (ASTM F 1941M), Class Fe/Zn 12 for exterior use, and Class Fe/Zn 5 where built into exterior walls. Select fasteners for type, grade, and class required.

2.4 MISCELLANEOUS MATERIALS

Retain "Low-Emitting Materials" Paragraph below if required for LEED for Schools.

A. Low-Emitting Materials: Paints and coatings shall comply with the testing and product requirements of the California Department of Public Health's (formerly, the California Department of Health Services') "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

Retain "Shop Primers" or "Universal Shop Primer" Paragraph below. Second paragraph specifies a typical primer for painted finishes that provides minimum protection to steel.

B. Shop Primers: Provide primers that comply with [Section 099113 "Exterior Painting" and Section 099123 "Interior Painting."] [Section 099600 "High-Performance Coatings."] [Section 099113 "Exterior Painting," Section 099123 "Interior Painting," and Section 099600 "High-Performance Coatings."]

C. Universal Shop Primer: Fast-curing, lead- and chromate-free, universal modified-alkyd primer complying with MPI#79 and compatible with topcoat.

D. Galvanizing Repair Paint: High-zinc-dust-content paint complying with SSPC-Paint 20 and compatible with paints specified to be used over it.

2.5 FABRICATION, GENERAL

A. Provide complete stair assemblies, including metal framing, hangers, clips, brackets, bearing plates, and other components necessary to support and anchor stairs and platforms on supporting structure.

1. Join components by welding unless otherwise indicated.

2. Use connections that maintain structural value of joined pieces.

B. Weld connections to comply with the following:

1. Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

2. Obtain fusion without undercut or overlap.

3. Remove welding flux immediately.

Delete first subparagraph below if appearance is not important or if economy is more important.

4. Weld exposed corners and seams continuously unless otherwise indicated.

5. At exposed connections, finish exposed welds to comply with NOMMA's "Voluntary Joint Finish Standards" for Type 4 welds: good quality, uniform undressed weld with minimal splatter.

C. Fabricate joints that are exposed to weather in a manner to exclude water. Provide weep holes where water may accumulate.

2.6 STEEL-FRAMED STAIRS

NAAMM standard in "NAAMM Stair Standard" Paragraph below includes only minimal requirements.

A. NAAMM Stair Standard: Comply with "Recommended Voluntary Minimum Standards for Fixed Metal Stairs" in NAAMM AMP 510, "Metal Stairs Manual," Industrial Class, unless more stringent requirements are indicated.

B. Stair Framing:

Steel plate stringers are less expensive than channels, except for longer spans, and allow railing posts to be welded to face of stringer. Allowing either plates or channels gives fabricator maximum flexibility.

1. Fabricate stringers of steel [plates] [or] [channels].

a. Provide closures for exposed ends of channel stringers.

2. Construct platforms of steel [plate] [or] [channel] headers and miscellaneous framing members as [needed to comply with performance requirements] [indicated].

3. Weld[ or bolt] stringers to headers; weld[ or bolt] framing members to stringers and headers.

Revise "Metal Bar-Grating Stairs" Paragraph below if other types of gratings are required. See Section 055300 "Metal Gratings" for additional grating types.

C. Metal Bar-Grating Stairs: Form treads and platforms to configurations shown from metal bar grating; fabricate to comply with NAAMM MBG 531, "Metal Bar Grating Manual."

Floor openings in areas required to be accessible to people with disabilities are limited to 1/2 inch (13 mm) in width by the ADA-ABA Accessibility Guidelines and ICC A117.1. This spacing is not close enough to support some high-heeled shoes.

1. Fabricate treads and platforms from [welded] [or] [pressure-locked] steel grating with openings in gratings no more than [5/16 inch (8 mm)] [1/2 inch (12 mm)] [3/4 inch (19 mm)] in least dimension.

2. Surface: [Plain] [Serrated].

3. Finish: [Shop primed] [Painted] [Galvanized].

4. Fabricate grating treads with [rolled-steel floor plate] [cast-abrasive] nosing and with steel angle or steel plate carrier at each end for stringer connections. Secure treads to stringers with bolts.

2.7 STAIR RAILINGS

A. Comply with applicable requirements in Section 055213 "Pipe and Tube Railings."

Delete or revise two subparagraphs below to suit railing type required. Coordinate with Section that specifies railings.

1. Rails may be bent at corners, rail returns, and wall returns, instead of using prefabricated fittings.

2. Connect posts to stair framing by direct welding unless otherwise indicated.

2.8 FINISHES

A. Finish metal stairs after assembly.

B. Galvanizing: Hot-dip galvanize items as indicated to comply with ASTM A 153/A 153M for steel and iron hardware and with ASTM A 123/A 123M for other steel and iron products.

C. Preparation for Shop Priming: Prepare uncoated ferrous-metal surfaces to comply with [SSPC-SP 6/NACE No. 3, "Commercial Blast Cleaning."] [SSPC-SP 3, "Power Tool Cleaning."]

D. Apply shop primer to uncoated surfaces of metal stair components, except those with galvanized finishes and those to be embedded in concrete or masonry unless otherwise indicated. Comply with SSPC-PA 1, "Paint Application Specification No. 1: Shop, Field, and Maintenance Painting of Steel," for shop painting.

PART 3 -  EXECUTION

3.1 INSTALLATION

A. Cutting, Fitting, and Placement: Perform cutting, drilling, and fitting required for installing metal stairs. Set units accurately in location, alignment, and elevation, measured from established lines and levels and free of rack.

B. Field Welding: Comply with requirements for welding in "Fabrication, General" Article.

3.2 ADJUSTING AND CLEANING

Retain "Touchup Painting" Paragraph below if touchup painting is included in this Section.

A. Touchup Painting: Immediately after erection, clean field welds, bolted connections, and abraded areas of shop paint, and paint exposed areas with same material as used for shop painting to comply with SSPC-PA 1 for touching up shop-painted surfaces.

B. Galvanized Surfaces: Clean field welds, bolted connections, and abraded areas and repair galvanizing to comply with ASTM A 780/A 780M.

END OF SECTION 055119

	METAL GRATING STAIRS
	055119 - 1



