Copyright 2011 AIA
MasterSpec Professional
11/11

Copyright 2011 by The American Institute of Architects (AIA)

Exclusively published and distributed by Architectural Computer Services, Inc. (ARCOM) for the AIA

SECTION 071326 - SELF-ADHERING SHEET WATERPROOFING
TIPS:
To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single‑File Formatting/Toggle/Editor's Notes.
To read detailed research, technical information about products and materials, and coordination checklists, click on Masterworks/Supporting Information.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

Verify that Section titles referenced in this Section are correct for this Project's Specifications; Section titles may have changed.

PART 1 -  GENERAL

1.1 SUMMARY

A. Section includes self-adhering modified bituminous sheet waterproofing.

1.2 PREINSTALLATION MEETINGS

A. Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

1.3 ACTION SUBMITTALS

A. Product Data: For each type of product.

Retain "Shop Drawings" Paragraph below if justified by extent or complexity of waterproofing.

B. Shop Drawings: Show locations and extent of waterproofing and details of substrate joints and cracks, sheet flashings, penetrations, inside and outside corners, tie-ins with adjoining waterproofing, and other termination conditions.

1.4 INFORMATIONAL SUBMITTALS

A. Sample warranties.

1.5 QUALITY ASSURANCE

Revise "Installer Qualifications" Paragraph below to suit warranty requirements; verify with manufacturers that installers meeting this requirement are available for Project location.

A. Installer Qualifications: An entity that employs installers and supervisors who are trained and approved by waterproofing manufacturer.

1.6 WARRANTY

Manufacturers of self-adhering sheet waterproofing rarely offer more than a materials-only warranty.

A. Manufacturer's Warranty: Manufacturer's standard materials-only warranty in which manufacturer agrees to furnish replacement waterproofing material for waterproofing that does not comply with requirements or that fails to remain watertight within specified warranty period.

Verify available warranties and warranty periods.

1. Warranty Period: [Three] [Five] <Insert number> years from date of Substantial Completion.

PART 2 -  PRODUCTS

See Editing Instruction No. 1 in the Evaluations for cautions about named manufacturers and products. For an explanation of options and Contractor's product selection procedures, see Section 016000 "Product Requirements."

2.1 MODIFIED BITUMINOUS SHEET WATERPROOFING

Retain option in "Modified Bituminous Sheet" Paragraph below if application with auxiliary products complying with VOC limits is required.

A. Modified Bituminous Sheet: Minimum 60-mil (1.5-mm) nominal thickness, self-adhering sheet consisting of 56 mils (1.4 mm) of rubberized asphalt laminated on one side to a 4-mil- (0.10-mm-) thick, polyethylene-film reinforcement, and with release liner on adhesive side[; formulated for application with primer or surface conditioner that complies with VOC limits of authorities having jurisdiction].

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

In first subparagraph below, American Hydrotech's "VM75" is 75-mil (1.9-mm) total thickness.

a. American Hydrotech, Inc; [VM75].

b. Carlisle Coatings & Waterproofing Inc; [CCW MiraDRI 860/861].

c. CETCO Building Materials Group, a subsidiary of AMCOL International Corp; [Envirosheet].

d. Grace Construction Products; W.R. Grace & Co. -- Conn; [Bituthene 3000/Low Temperature] [Bituthene 4000].

e. Henry Company; [Blueskin WP 100/200].

f. Meadows, W.R.,Inc; [SealTight Mel-Rol].

g. Nervastral, Inc; [BITU-MEM].

h. Polyguard Products, Inc; [Polyguard 650].

i. Protecto Wrap Company; [PW 100/60].

j. Soprema, Inc.

k. Tamko Building Products, Inc; [TW-60].

l. York Manufacturing, Inc; [HydroGard].

m. <Insert manufacturer's name; product name or designation>.

Verify that products retained in subparagraphs above comply with requirements in "Physical Properties" Subparagraph below; revise to suit Project.

2. Physical Properties:

a. Tensile Strength, Membrane: 250 psi (1.7 MPa) minimum; ASTM D 412, Die C, modified.

b. Ultimate Elongation: 300 percent minimum; ASTM D 412, Die C, modified.

c. Low-Temperature Flexibility: Pass at minus 20 deg F (minus 29 deg C); ASTM D 1970.

d. Crack Cycling: Unaffected after 100 cycles of 1/8-inch (3-mm) movement; ASTM C 836.

e. Puncture Resistance: 40 lbf (180 N) minimum; ASTM E 154.

f. Water Absorption: 0.2 percent weight-gain maximum after 48-hour immersion at 70 deg F (21 deg C); ASTM D 570.

g. Water Vapor Permeance: 0.05 perms (2.9 ng/Pa x s x sq. m) maximum; ASTM E 96/E 96M, Water Method.

Revise option in "Hydrostatic-Head Resistance" Subparagraph below if applicable. Named products exceed 200 feet (60 m) except for Nervastral and York, which report 150 feet (45 m).

h. Hydrostatic-Head Resistance: [200 feet (60 m)] <Insert value> minimum; ASTM D 5385.

Retain "Sheet Strips" Subparagraph below for concealed strip flashings. Modified bituminous waterproofing membrane cannot be used for exposed sheet flashings.

3. Sheet Strips: Self-adhering, rubberized-asphalt strips of same material and thickness as sheet waterproofing.

B. Modified Bituminous Sheet, Fabric Reinforced: Minimum 60-mil (1.5-mm) nominal thickness, self-adhering sheet consisting of rubberized-asphalt membrane with embedded fabric reinforcement, and with release liner on adhesive side.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Protecto Wrap Company; Jiffy Seal 140/60.

b. Royston; [104AHT Membrane] [Royal-Gard Plus Membrane 104ARHT].

c. <Insert manufacturer's name; product name or designation>.

Verify that products retained in subparagraphs above comply with requirements in "Physical Properties" Subparagraph below; revise to suit Project.

2. Physical Properties:

a. Pliability: No cracks when bent 180 degrees over a 1-inch (25-mm) mandrel at minus 25 deg F (minus 32 deg C); ASTM D 146.

b. Puncture Resistance: [40 lbf (180 N)] [100 lbf (445 N)] minimum; ASTM E 154.

c. Water Vapor Permeance: 0.05 perms (2.9 ng/Pa x s x sq. m) maximum; ASTM E 96/E 96M, Water Method.

Retain "Sheet Strips" Subparagraph below for concealed strip flashings. Modified bituminous waterproofing membrane cannot be used for exposed sheet flashings.

3. Sheet Strips: Self-adhering, reinforced, rubberized-asphalt strips of same material and thickness as sheet waterproofing.

2.2 AUXILIARY MATERIALS

A. General: Furnish auxiliary materials recommended by waterproofing manufacturer for intended use and compatible with sheet waterproofing.

1. Furnish liquid-type auxiliary materials that comply with VOC limits of authorities having jurisdiction.

B. Primer: Liquid [waterborne] [solvent-borne] primer recommended for substrate by sheet-waterproofing material manufacturer.

C. Surface Conditioner: Liquid, waterborne surface conditioner recommended for substrate by sheet-waterproofing material manufacturer.

D. Liquid Membrane: Elastomeric, two-component liquid, cold fluid applied, of trowel grade or low viscosity.

E. Substrate Patching Membrane: Low-viscosity, two-component, modified asphalt coating.

F. Metal Termination Bars: Aluminum bars, approximately 1 by 1/8 inch (25 by 3 mm) thick, predrilled at 9-inch (229-mm) centers.

Retain protection course type from four "Protection Course" paragraphs below if required. Delete paragraphs if molded-sheet drainage panels or insulation drainage panels replace protection course.

Asphaltic protection course in first "Protection Course" Paragraph below is manufactured by W. R. Meadows and several other waterproofing manufacturers.

G. Protection Course: ASTM D 6506, semirigid sheets of fiberglass or mineral-reinforced-asphaltic core, pressure laminated between two asphalt-saturated fibrous liners and as follows:

Retain one of two "Thickness" subparagraphs below.

1. Thickness: [1/8 inch (3 mm)] [1/4 inch (6 mm)], nominal.

2. Thickness: 1/8 inch (3 mm), nominal, for vertical applications; 1/4 inch (6 mm), nominal, elsewhere.

3. Adhesive: Rubber-based solvent type recommended by waterproofing manufacturer for protection course type.

Film-faced, fan-folded, extruded-polystyrene protection course in first "Protection Course" Paragraph below describes Dow Chemical Company's "Protection Board III" (first option) and Pactiv Building Products' "Green Guard PB4" and Owens Corning Insulating Systems' "Fanfold DWB" (second option).

H. Protection Course: Fan folded, with a core of extruded-polystyrene board insulation faced on [one side] [or] [both sides] with plastic film, nominal thickness 1/4 inch (6 mm), with compressive strength of not less than 8 psi (55 kPa) per ASTM D 1621, and maximum water absorption by volume of 0.6 percent per ASTM C 272.

Unfaced, extruded-polystyrene protection course in first "Protection Course" Paragraph below describes Owens Corning's "Foamular Half-Inch."

I. Protection Course: Extruded-polystyrene board insulation, unfaced, ASTM C 578, Type X, 1/2 inch (13 mm) thick.

J. Protection Course: Molded-polystyrene board insulation, ASTM C 578, Type I, 0.90-lb/cu. ft. (15-kg/cu. m) minimum density, 1-inch (25-mm) minimum thickness.

2.3 MOLDED-SHEET DRAINAGE PANELS

Retain this article if molded-sheet drainage panels are required. Retain "Molded-Sheet Drainage Panel" Paragraph below if specifying molded-sheet drainage panels in another Section; revise to suit Project.

A. Molded-Sheet Drainage Panel: Comply with Section 334600 "Subdrainage."

Retain one or both molded-sheet drainage-panel paragraphs below if specifying molded-sheet drainage panels in this Section; revise to suit Project. If not shown on Drawings, insert thickness requirement only after coordinating required thickness with required flow rate.

Retain "Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel" Paragraph below if required, usually for foundation walls. Option describes American Hydrotech's "Hydrodrain 400," Carlisle's "CCW MiraDRAIN 6200" and "CCW MiraDRAIN 6200XL," and W. R. Grace's "Hydroduct 220" and "Hydroduct 660."

B. Nonwoven-Geotextile-Faced, Molded-Sheet Drainage Panel: Composite subsurface drainage panel consisting of a studded, nonbiodegradable, molded-plastic-sheet drainage core; with a nonwoven, needle-punched geotextile facing with an apparent opening size not exceeding No. 70 (0.21-mm) sieve laminated to one side of the core[ and a polymeric film bonded to the other side]; and with a vertical flow rate of 9 to 15 gpm per ft. (112 to 188 L/min. per m).

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Hydrotech, Inc; [Hydrodrain 400] [Hydrodrain 420].

b. Carlisle Coatings & Waterproofing Inc; [CCW MiraDRAIN 6000] [CCW MiraDRAIN 6000XL] [CCW MiraDRAIN 6200] [CCW MiraDRAIN 6200XL].

c. Grace Construction Products; W.R. Grace & Co. -- Conn; [Hydroduct 220] [Hydroduct 660].

d. Protecto Wrap Company; [Protecto Drain 2000-V].

e. <Insert manufacturer's name; product name or designation>.

Retain "Woven-Geotextile-Faced, Molded-Sheet Drainage Panel" Paragraph below if required, usually for plaza decks. Option describes W. R. Grace's "Hydroduct 225."

C. Woven-Geotextile-Faced, Molded-Sheet Drainage Panel: Composite subsurface drainage panels consisting of a studded, nonbiodegradable, molded-plastic-sheet drainage core; with a woven-geotextile facing with an apparent opening size not exceeding No. 40 (0.425-mm) sieve laminated to one side of the core[ and a polymeric film bonded to the other side]; and with a horizontal flow rate not less than 2.8 gpm per ft. (35 L/min. per m).

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Hydrotech, Inc; Hydrodrain 700.

b. Carlisle Coatings & Waterproofing Inc; [CCW MiraDRAIN 9000] [CCW MiraDRAIN 9900].

c. Grace Construction Products; W.R. Grace & Co. -- Conn; Hydroduct 225.

d. Protecto Wrap Company; Protecto Drain 2000-H.

e. <Insert manufacturer's name; product name or designation>.

2.4 INSULATION DRAINAGE PANELS

If not shown on Drawings, insert thickness requirement for insulation drainage panels.

In "Unfaced Wall-Insulation Drainage Panels" Paragraph below, DiversiFoam's "CertiFoam 25 SL Drainage Board" and Dow's "Styrofoam Perimate" are Type IV. DiversiFoam's "CertiFoam 40 (with channel edges) Drainage Board" is Type VI.

A. Unfaced Wall-Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type IV, 25-psi (173-kPa)] [or] [Type VI, 40-psi (276-kPa)] minimum compressive strength; unfaced; fabricated with shiplap or channel edges and with one side having grooved drainage channels.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. DiversiFoam Products; [CertiFoam 25 SL] [CertiFoam 40 (with channel edges)].

b. Dow Chemical Company (The); [STYROFOAM Brand PERIMATE Insulation] [Styrofoam Perimate].

c. <Insert manufacturer's name; product name or designation>.

In "Geotextile-Faced, Wall-Insulation Drainage Panels" Paragraph below, Owens Corning's "Insul-Drain" and T. Clear's "Thermadry 750" are Type IV; T. Clear's "Thermadry 1250" is Type VI.

B. Geotextile-Faced, Wall-Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type IV, 25-psi (173-kPa)] [or] [Type VI, 40-psi (276-kPa)] minimum compressive strength; fabricated with tongue-and-groove edges and with one side having grooved drainage channels faced with nonwoven geotextile filter fabric.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. Owens Corning Insulating Systems LLC; Insul-Drain.

b. T. Clear Corporation, a subsidiary of Fin Pan Inc; [Thermadry 1250] [Thermadry 750].

c. <Insert manufacturer's name; product name or designation>.

In "Unfaced Plaza-Deck Insulation Drainage Panels" Paragraph below, Dow's "Styrofoam Ribbed Roofmate" and Owens Corning's "Foamular 404 RB" are Type VI; American Hydrotech's "Hydroguard" is also Type VI and has a cementitious surfacing for wear; DiversiFoam's "CertiFoam Plaza Deck" and Owens Corning's "Foamular 604 RB" are Type VII.

C. Unfaced Plaza-Deck Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type VI, 40-psi (276-kPa)] [or] [Type VII, 60-psi (414-kPa)] minimum compressive strength; unfaced; fabricated with shiplapped, channel, or tongue-and-groove edges and with one side having ribbed drainage channels.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. American Hydrotech, Inc; Hydroguard.

b. DiversiFoam Products; CertiFoam Plaza Deck.

c. Dow Chemical Company (The); STYROFOAM ROOFMATE Ribbed Insulation.

d. Owens Corning Insulating Systems LLC; [Foamular 404 RB] [Foamular 604 RB].

e. <Insert manufacturer's name; product name or designation>.

D. Geotextile-Faced, Plaza-Deck Insulation Drainage Panels: Extruded-polystyrene board insulation complying with ASTM C 578, [Type VI, 40-psi (276-kPa)] [or] [Type VII, 60-psi (414-kPa)] minimum compressive strength; fabricated with tongue-and-groove edges and with one side having grooved drainage channels faced with manufacturer's standard, nonwoven geotextile filter fabric.

Retain "Products" Subparagraph and list of manufacturers and products below to require specific products or a comparable product from other manufacturers.

1. Products: Subject to compliance with requirements, [provide the following] [provide one of the following] [available products that may be incorporated into the Work include, but are not limited to, the following]:

a. T. Clear Corporation, a subsidiary of Fin Pan Inc; [Thermadry 1250] [Thermadry 1750].

b. <Insert manufacturer's name; product name or designation>.

PART 3 -  EXECUTION

3.1 MODIFIED BITUMINOUS SHEET-WATERPROOFING APPLICATION

A. Prepare surfaces and install modified bituminous sheets according to waterproofing manufacturer's written instructions and recommendations in ASTM D 6135.

B. Apply primer to substrates at required rate and allow it to dry. Limit priming to areas that will be covered by sheet waterproofing in same day. Reprime areas exposed for more than 24 hours.

C. Apply and firmly adhere sheets over area to receive waterproofing. Accurately align sheets and maintain uniform 2-1/2-inch- (64-mm-) minimum lap widths and end laps. Overlap and seal seams, and stagger end laps to ensure watertight installation.

Retain subparagraph below for modified bituminous sheets; revise to suit Project. Verify that manufacturers produce low-temperature products. See Evaluations. An upper-limit temperature may be recommended by sheet manufacturer to reduce workmanship problems with more aggressive adhesion.

1. When ambient and substrate temperatures range between 25 and 40 deg F (minus 4 and plus 5 deg C), install self-adhering, modified bituminous sheets produced for low-temperature application. Do not use low-temperature sheets if ambient or substrate temperature is higher than 60 deg F (16 deg C).

Retain "Horizontal Application" Paragraph below for plaza-deck or near-horizontal conditions.

D. Horizontal Application: Apply sheets from low to high points of decks to ensure that laps shed water.

E. Apply continuous sheets over already-installed sheet strips, bridging substrate cracks, construction, and contraction joints.

F. Seal edges of sheet-waterproofing terminations with mastic.

Retain first paragraph below if terminating into other waterproofing.

G. Install sheet-waterproofing and auxiliary materials to tie into adjacent waterproofing.

H. Repair tears, voids, and lapped seams in waterproofing not complying with requirements. Slit and flatten fishmouths and blisters. Patch with sheet waterproofing extending 6 inches (150 mm) beyond repaired areas in all directions.

I. Immediately install protection course with butted joints over waterproofing membrane.

Retain applicable options in subparagraph below if drainage panels are used and are permitted by waterproofing manufacturer to replace protection course.

1. [Molded-sheet drainage panels] [Insulation drainage panels] may be used in place of a separate protection course to vertical applications when approved by waterproofing manufacturer and installed immediately.

3.2 MOLDED-SHEET DRAINAGE-PANEL INSTALLATION

A. Place and secure molded-sheet drainage panels, with geotextile facing away from wall or deck substrate, according to manufacturer's written instructions. Use adhesives or other methods that do not penetrate waterproofing. Lap edges and ends of geotextile to maintain continuity. Protect installed molded-sheet drainage panels during subsequent construction.

Retain subparagraph below if protection course is installed before installing molded-sheet drainage panels.

1. For vertical applications, install protection course before installing drainage panels.

3.3 INSULATION DRAINAGE-PANEL INSTALLATION

A. Install insulation drainage panels over waterproofed surfaces; cut and fit to within 3/4 inch (19 mm) of projections and penetrations.

B. Ensure that drainage channels are aligned and free of obstructions.

Retain first paragraph below if support is required during backfilling.

C. On vertical surfaces, set insulation drainage panels in adhesive or tape applied according to manufacturer's written instructions.

D. On horizontal surfaces, loosely lay insulation drainage panels according to manufacturer's written instructions. Stagger end joints and tightly abut insulation units.

3.4 PROTECTION, REPAIR, AND CLEANING

A. Do not permit foot or vehicular traffic on unprotected membrane.

B. Protect installed insulation drainage panels from damage due to UV light, harmful weather exposures, physical abuse, and other causes. Provide temporary coverings where insulation is subject to abuse and cannot be concealed and protected by permanent construction immediately after installation.

C. Correct deficiencies in or remove waterproofing that does not comply with requirements; repair substrates, reapply waterproofing, and repair sheet flashings.

D. Clean spillage and soiling from adjacent construction using cleaning agents and procedures recommended by manufacturer of affected construction.

END OF SECTION 071326

	SELF-ADHERING SHEET WATERPROOFING
	071326 - 1



